Supplementary data.

Experimental:

Low Temperature NMR studies on Cationic compounds.

General procedure:

The zirconocene complex (0.1 mmol) was dissolved in 0.25 ml of CD2Cl2 and transferred into a pre-cooled (-78 °C) NMR tube. The cation generating agent (0.21 mmol) such as B(C6F5)3 was dissolved in 0.28 ml of CD2Cl2 and transferred on top of the zirconocene solution in the NMR tube. The tube was sealed with a Suba Seal and shaken vigorously to ensure complete mixing. The colour changed to yellow and the sample was inserted into the pre-cooled (-60 °C) spectrometer. 1H, 13 C, HH-COSY and CH-COSY spectra were recorded at -60 °C. The sample was warmed up to ambient temperature in steps of 20K and at each step a 1H NMR spectrum was recorded.

Preparation of [Zr(-C5H4CMe2-p-C6H4Me)2]2+[MeB(C6F5)3]2- 5.

The compounds [Zr(-C5H4CMe2-p-C6H4Me)2Me2] (0.83 g, 1.6 mmol) and B(C6F5)3 (1.65 g, 3.2 mmol) were mixed together at -50 C and cold dichloromethane (8ml) was added. The colour changed immediately to dark red. Slow cooling of the reaction mixture to -80 C did not yield suitable crystals for X-ray analysis. A small portion of the reaction mixture was taken and the solvent was removed under reduced pressure to yield a yellow solid.  (Analysis(%): Found, C 52.35, H 3.0, Zr 5.8. C68H40F30B2Zr requires: C 53.0, H 2.6, Zr 5.9).

Preparation of [Zr(-C5H4CMe2Ph)2]2+[MeB(C6F5)3]2- 6.

The compounds [Zr(-C5H4CMe2Ph)2Me2] (0.183 g, 0.38 mmol) and B(C6F5)3 (0.384 g, 0.76 mmol) were dissolved separately in dichloromethane (2 ml) and the solutions were mixed together at -40 C to yield a clear, yellow solution. The reaction mixture was slowly cooled to -80 C giving yellow crystals which were not suitable for x-ray analysis. (Analysis (%), Found: C 52.2, H 2.95, Zr 5.4.  C66H36F30B2Zr requires: C 52.4, H 2.4, Zr 6.0).

Table 1: NMR data for 3, 4, 5 and 6¶

| Compound | 1H NMR (ppm) | assgnt | 13C NMR (ppm) | assgnt |  |
| --- | --- | --- | --- | --- | --- |
| [Zr(-C5H4CMe2Ph)2Me2] 3 | -0.24 (s, 6H)a 1.58 (s, 12H) 5.90 (“t”, 4H) 5.98 (“t”, 4H) 7.19-7.27 (m, 10H) | ZrMe CCH3 Cp’ Cp’ Ph | 29.90b 31.14 39.75 109.68 110.79 125.79 125.99 127.97 137.19 150.60 | CCH3 ZrMe CCH3 Cp’ Cp’ p-C-Ph m-C-Ph o-C-Ph i-C-Cp i-C-Ph |  |
| [Zr(-C5H4CMe2-p-C6H4Me)2Me2] 4 | -0.21 (s, 6H)a 1.56 (s, 12H) 2.31 (s, 6H) 5.91 (“t”, 4H) 5.98 (“t”, 4H) 7.10 (“s”, 8H) | ZrMe CCH3 PhMe Cp’ Cp’ Ph | 20.84b 29.91 31.06 39.38 109.57 110.14 125.85 128.64 135.23 137.36 147.74 | PhMe CCH3 ZrMe CCH3 Cp’ Cp’ m-C-Ph o-C-Ph i-C-PhMe i-C-Cp i-C-Ph |  |
| 5 | 0.40 (br, 6H)c 1.70 (br, 12H) 2.59 (s, 6H) 3.70 (s, 2H) 6.19 (s, 2H) 6.58 (s, 2H) 6.69 (d, 2H) 6.78 (s, 2H) 7.40 (d, 2H, JHH = 7.50 Hz) 8.05 (d, 2H, JHH = 5.00 Hz) 8.09 (d, 2H, JHH = 7.50 Hz) | CH3B CMe2 PhMe Cp4 Cp3 Cp2 Ph2 Cp1 Ph4 Ph1 Ph3 | 9.58d 20.39 23.69 27.96 38.48 108.20 112.21 112.66 118.71 126.20 128.43 131.33 133.25 142.44 142.59 145.10 | CH3B PhCH3 CC1H3 CC2H3 CMe2 Cp3 Cp2 Ph2 Cp1 PhMe Cp4 Ph4 i-C-Cp Ph1 i-C-Ph Ph3 |  |
| 6 | 0.42 (br, 6H)a 1.71 (s, 6H)c 1.73 (s, 6H)c 3.94 (s, 2H) 6.25 (s, 2H) 6.63 (s, 2H) 6.76 (s, 2H) 6.88 (s, 2H) 7.51 (s, 2H) 7.92 (s,2H) 8.24 (s, 2H) 8.33 (s, 2H) | CH3B CC2H3 CC1H3 Cp4 Cp3 Cp2 Ph2 Cp1 Ph4 p-H-Ph Ph1 Ph3 | 9.65b 23.90 27.69 38.91 108.97 113.37 113.97 119.11 127.61 129.84 130.33 134.10 143.03 144.39 144.58 |  | CH3B CC1H3 CC2H3 CMe2 Cp3 Ph2 Cp2 Cp1 Cp4 Ph4 p-C-Ph i-C-Cp Ph1 i-C-Ph Ph3 |

a CDCl3 300 MHz, 20 C; b CDCl3, 75.5 MHz, 20 C; c CD2Cl2 500 MHz; d CD2Cl2 125.7 MHz,  CpHn (n = 1 - 4) denotes hydrogens of the C5 ring, coupled to CpCn (connectivity determined by CH-correlation), PhHn follows analogue.

¶ The chemical shifts for the MeB(C6F5)3- anion are virtually the same in all compounds and are as followed: 19F NMR:  (ppm): -139.39 (d, 6F, o-F); -169.52 (t, 3F, p-F); -172.36 (t, 6F, o-F).