Copolymers of Vinyl Epoxides with Carbon Monoxide

Jong Tae Lee and Howard Alper*

Centre for Catalysis Research and Innovation, Department of Chemistry, University of

Ottawa, 10 Marie Curie, Ottawa, Ontario, Canada K1N 6N5

General Procedure for the Copolymerization of Vinyl Epoxides with Carbon Monoxide The copolymerization was carried out in a 45 ml autoclave. A mixture of [Pd(MeCN)4](BF4)2 (0.02 mmol), (R,R) - Me - DUPHOS (0.02 mmol), 1,4-naphthoquinone ( 0.25 mmol), formic acid (0.6 mmol) and vinyl epoxide (8 mmol) in 2 ml of nitromethane and 2 ml of chloroform was charged in the autoclave under N2. The autoclave was flushed 3 times with carbon monoxide and pressurized to 1,000 psi of carbon monoxide and then heated at 40 oC with magnetic stirring. After reaction, the  mixture was diluted with 5 ml of methylene chloride and filtered through a short Celite column to remove the catalyst. The solvent was reduced to about 2 ml under reduced pressure, and then the polymer was precipitated in ether. The solids were filtered,  extracted with methanol, and then dried under vacuum.

## Spectral Data of Copolymers [poly(1,4-ketone ) structure]

1 : 13C NMR (75 MHz, DMSO-d6, ppm) ; 211.8, 51.5, 46.5, 44.5, 43.5, 29.4,  27.3., IR(KBr, cm-1) ; 1706, 1260, 914, 835., Anal. Calcd: C, 66.65, H, 7.99. Found: C, 66.13, H, 7.89.

3 : 13C NMR (75 MHz, DMSO-d6, ppm) ; 211.9, 51.8, 46.2, 45.4, 43.8, 31.9, 30.4, 26.2, 25.7., IR (KBr, cm-1) ; 1702, 1261, 915, 834., Anal. Calcd: C,70.10, H,9.10. Found: C, 69.44, H, 9.08.

4 : 13C NMR (75 MHz, DMSO-d6, ppm) ; 211.8, 51.4, 45.9, 45.2, 43.7, 33.1, 31.8, 28.6, 28.4, 28.2, 25.4., IR (KBr, cm-1) ; 1706, 1260, 914, 833., Anal. Calcd: C,72.49, H,9.95. Found:

C,71.78, H,9.81.

5 : 13C NMR (75 MHz, DMSO-d6, ppm) ; 211.6, 52.1, 51.9, 50.9, 50.7, 36.1, 33.8, 30.5, 29.8, 26.2, 24.8, 24.2, 23.3., IR (KBr, cm-1) ; 1706, 1262, 908, 843., Anal. Calcd: C, 71.03, H, 7.94. Found: C, 71.83, H, 8.32.

6 : 13C NMR (75 MHz, DMSO-d6, ppm) ; 209.4, 71.4, 71.3, 50.3, 50.1, 46.3,  43.3., IR (KBr, cm-1) ; 1707, 1253, 907, 853., Anal. Calcd: C, 59.15, H, 7.09. Found: C, 58.83, H, 7.15.

Molar optical rotation [poly(spiroketal/1,4-ketone)structure] ; [D24 = + 3.4o (c=6.1mg/ml,

DMSO).