# Table 1. The Limiting Thresholds of Compounds Measured at 532 nm with Nanosecond Laser Pulses

| Compounds | Solvents | Structure types | Linear trans-mission (%) | (g (10-18cm2 | (e/(g (K() | Limiting thres-holds (J cm-2) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C60 | Toluene | - | 62 | 3.1 | 3.1 ( 0.3 | 1.6 | 5b |
| [Bu4N]3[WCu3Br4S4] | MeCN | cubane-shaped | 70 | 0.44 | - | 1.1 | 7a |
| [Bu4N]3[WAg3Br4S4] | MeCN | cubane-shaped | 70 | 1.4 | - | 0.6 | 7a |
| [Bu4N]3[MoAg3BrI3S4] | MeCN | cubane-shaped | 70 | 18 | - | 0.5 | 7a |
| Phthalocyanine derivatives | Toluene | - | 85 | 1.6 | 30 ( 6 | ( 0.1 | 6a,b |
| Mo2Ag4S8(PPh3)4 | MeCN | hexagonal-prismatic | 92 | - | - | ( 0.1 | 7c |
| [Et4N]2[MoS4Cu4(SCN)4(2-pic)4] (8) | DMF | Planar 'open' | 84 | 6.0 | 3.1 | 0.50 | This work |
| [Et4N]2[WS4Cu4(SCN)4(2-pic)4] (7) | DMF | planar 'open' | 86 | 0.4 | 4.6 | 0.30 | This work |
| MoS4Cu4Cl2(py)6 (6) | DMF | planar 'open' | 78 | 0.75 | 7.2 | 0.15 | This work |
| WS4Cu4Cl2(py)6 (5) | DMF | planar 'open' | 64 | 4.75 | 11.4 | 0.10 | This work |
| MoS4Cu4Br2(py)6 (4) | DMF | planar 'open' | 72 | 3.4 | 20 | 0.10 | This work |
| WS4Cu4Br2(py)6 (3) | DMF | planar 'open' | 72 | 1.06 | 26 | 0.08 | This work |
| MoS4Cu4I2(py)6 (2) | DMF | planar 'open' | 72 | 2.69 | 25 | 0.08 | This work |
| WS4Cu4I2(py)6 (1) | DMF | planar 'open' | 72 | 1.27 | 28 | 0.07 | This work |