Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

Table 1.  Crystal data and structure refinement for [Cu(INA)(OH)]H2O.

Identification code               candy2

Empirical formula                 C6 H7 Cu N O4

Formula weight                    220.67

Temperature                       293(2) K

Wavelength                        0.71070 A

Crystal system                    Monoclinic

Space group                       P2(1)/n

Unit cell dimensions              a = 3.53400(10) A   alpha = 90 deg.

b = 15.7680(5) A  beta = 96.8850(13) deg.

c = 13.0052(4) A   gamma = 90 deg.

Volume, Z                         719.48(4) A^3,  4

Density (calculated)              2.037 Mg/m^3

Absorption coefficient            3.004 mm^-1

F(000)                            444

Crystal size                      0.3 x 0.2 x 0.08 mm

Theta range for data collection   3.03 to 30.00 deg.

Limiting indices                  -4<=h<=4, -19<=k<=22, -18<=l<=18

Reflections collected             3585

Independent reflections           2078 [R(int) = 0.026]

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    2038 / 0 / 109

Goodness-of-fit on F^2            1.124

Final R indices [I>2sigma(I)]     R1 = 0.0364, wR2 = 0.0821

R indices (all data)              R1 = 0.0512, wR2 = 0.1216

Largest diff. peak and hole       0.970 and -0.687 e.A^-3

Table 2.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for [Cu(INA)(OH)]H2O.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

Cu(1)        2624(1)        780(1)       4949(1)        9(1)

O(1)         3131(5)       -284(1)       5705(1)        9(1)

N(1)         2571(6)       1796(1)       4035(2)       10(1)

C(2)         2548(7)       1654(2)       3011(2)       13(1)

C(3)         3414(7)       2281(2)       2332(2)       12(1)

C(4)         4350(7)       3086(2)       2712(2)       12(1)

C(5)         4260(8)       3238(2)       3763(2)       14(1)

C(6)         3355(7)       2580(2)       4397(2)       13(1)

C(10)        5602(7)       3774(2)       2010(2)       11(1)

O(11)        5370(6)       3579(1)       1060(1)       13(1)

O(12)        6811(7)       4450(1)       2416(2)       21(1)

O(1W)        9245(19)      5464(2)       4130(3)      107(2)

________________________________________________________________

Table 3.   Bond lengths [A] and angles [deg] for [Cu(INA)(OH)]H2O.

_____________________________________________________________

Cu(1)-O(1)                    1.942(2)

Cu(1)-O(1)#1                  1.973(2)

Cu(1)-N(1)                    1.994(2)

Cu(1)-O(11)#2                 2.004(2)

Cu(1)-O(1)#3                  2.249(2)

Cu(1)-Cu(1)#1                 2.9727(6)

O(1)-Cu(1)#1                  1.973(2)

O(1)-Cu(1)#3                  2.249(2)

N(1)-C(6)                     1.340(3)

N(1)-C(2)                     1.349(3)

C(2)-C(3)                     1.384(4)

C(3)-C(4)                     1.388(4)

C(4)-C(5)                     1.391(4)

C(4)-C(10)                    1.517(4)

C(5)-C(6)                     1.387(4)

C(10)-O(12)                   1.243(3)

C(10)-O(11)                   1.267(3)

O(11)-Cu(1)#4                 2.004(2)

O(1)-Cu(1)-O(1)#1            81.19(8)

O(1)-Cu(1)-N(1)             171.80(8)

O(1)#1-Cu(1)-N(1)            90.85(8)

O(1)-Cu(1)-O(11)#2           95.26(8)

O(1)#1-Cu(1)-O(11)#2        154.05(8)

N(1)-Cu(1)-O(11)#2           92.76(9)

O(1)-Cu(1)-O(1)#3            85.14(7)

O(1)#1-Cu(1)-O(1)#3         113.49(8)

N(1)-Cu(1)-O(1)#3            96.35(8)

O(11)#2-Cu(1)-O(1)#3         91.63(7)

O(1)-Cu(1)-Cu(1)#1           40.99(5)

O(1)#1-Cu(1)-Cu(1)#1         40.21(5)

N(1)-Cu(1)-Cu(1)#1          131.03(6)

O(11)#2-Cu(1)-Cu(1)#1       131.05(6)

O(1)#3-Cu(1)-Cu(1)#1        102.08(5)

Cu(1)-O(1)-Cu(1)#1           98.81(8)

Cu(1)-O(1)-Cu(1)#3           94.86(7)

Cu(1)#1-O(1)-Cu(1)#3        113.49(8)

C(6)-N(1)-C(2)              118.5(2)

C(6)-N(1)-Cu(1)             123.0(2)

C(2)-N(1)-Cu(1)             117.0(2)

N(1)-C(2)-C(3)              122.4(3)

C(2)-C(3)-C(4)              119.2(2)

C(3)-C(4)-C(5)              118.3(2)

C(3)-C(4)-C(10)             120.9(2)

C(5)-C(4)-C(10)             120.7(2)

C(6)-C(5)-C(4)              119.3(3)

N(1)-C(6)-C(5)              122.3(2)

O(12)-C(10)-O(11)           127.0(2)

O(12)-C(10)-C(4)            117.9(2)

O(11)-C(10)-C(4)            115.1(2)

C(10)-O(11)-Cu(1)#4         126.5(2)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y,-z+1    #2 x-1/2,-y+1/2,z+1/2

#3 -x,-y,-z+1    #4 x+1/2,-y+1/2,z-1/2

Table 4.   Anisotropic displacement parameters (A^2 x 10^3) for

[Cu(INA)(OH)]H2O.

The anisotropic displacement factor exponent takes the form:

-2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Cu(1)    12(1)       7(1)       8(1)       1(1)       5(1)       1(1)

O(1)     12(1)       7(1)       7(1)       1(1)       3(1)       2(1)

N(1)     11(1)       8(1)      11(1)       4(1)       4(1)       1(1)

C(2)     16(1)      11(1)      10(1)       0(1)       2(1)       0(1)

C(3)     16(1)      13(1)       9(1)       2(1)       3(1)      -1(1)

C(4)     11(1)      14(1)       9(1)       3(1)       3(1)       1(1)

C(5)     18(1)      12(1)      12(1)       1(1)       5(1)      -1(1)

C(6)     18(1)      11(1)      10(1)       1(1)       4(1)      -1(1)

C(10)    12(1)      11(1)      12(1)       3(1)       3(1)       0(1)

O(11)    21(1)      11(1)       9(1)       1(1)       6(1)      -3(1)

O(12)    35(1)      15(1)      12(1)       1(1)       5(1)     -10(1)

O(1W)   256(7)      36(2)      23(2)      -5(2)     -14(3)      -6(3)

_______________________________________________________________________

Table 5.   Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for [Cu(INA)(OH)]H2O.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(1)         3502(5)       -240(1)       6361(1)       10

H(2)         1928(7)       1115(2)       2753(2)       15

H(3)         3370(7)       2164(2)       1630(2)       15

H(5)         4800(8)       3776(2)       4037(2)       16

H(6)         3290(7)       2686(2)       5098(2)       15

H(1W)        9069(19)      5130(2)       4635(3)      129

H(2W)       11505(19)      5656(2)       4169(3)      129

H(3W)        7691(19)      5876(2)       4127(3)      129

H(4W)        8797(19)      5191(2)       3565(3)      129

________________________________________________________________

O1W hydrogens statistically disordered 50:50

Table 1.  Crystal data and structure refinement for [Cu(INA)2]2H2O.

Identification code               candy3

Empirical formula                 C12 H12 Cu N2 O6

Formula weight                    343.78

Temperature                       293(2) K

Wavelength                        0.71070 A

Crystal system                    Monoclinic

Space group                       Cc

Unit cell dimensions              a = 4.9410(2) A   alpha = 90 deg.

b = 25.0290(10) A beta = 97.834(2) deg.

c = 10.9600(4) A  gamma = 90 deg.

Volume, Z                         1342.75(9) A^3,  4

Density (calculated)              1.701 Mg/m^3

Absorption coefficient            1.656 mm^-1

F(000)                            700

Crystal size                      0.4 x 0.2 x 0.1 mm

Theta range for data collection   3.26 to 30.04 deg.

Limiting indices                  -6<=h<=6, -34<=k<=34, -15<=l<=15

Reflections collected             3592

Independent reflections           1880 [R(int) = 0.036]

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    1861 / 2 / 190

Goodness-of-fit on F^2            1.057

Final R indices [I>2sigma(I)]     R1 = 0.0449, wR2 = 0.0730

R indices (all data)              R1 = 0.0626, wR2 = 0.0889

Absolute structure parameter      0.09(2)

Largest diff. peak and hole       0.420 and -0.552 e.A^-3

Table 2.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for [Cu(INA)2]2H2O.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

Cu(1)        5026(1)       1132(1)       4430(1)       11(1)

N(1)         6586(11)      1741(2)       5497(5)       12(1)

C(10)        9409(13)      3167(3)       7465(6)       14(1)

O(1)         8214(9)       3293(2)       8375(4)       15(1)

O(2)        11402(7)       3415(1)       7145(4)       23(1)

C(12)        5527(14)      1890(3)       6519(6)       16(1)

C(13)        6364(13)      2353(3)       7163(7)       17(1)

C(14)        8350(13)      2672(3)       6759(6)       15(1)

C(15)        9471(11)      2519(2)       5714(4)       15(1)

C(16)        8522(10)      2056(2)       5110(4)       14(1)

N(2)         3468(9)        558(2)       3253(4)       13(1)

C(20)         -55(10)      -663(2)        744(5)       13(1)

O(3)        -2596(8)       -602(2)        369(4)       14(1)

O(4)         1449(7)      -1034(1)        483(3)       14(1)

C(22)        1148(11)       645(2)       2488(5)       18(1)

C(23)         -46(11)       264(2)       1680(5)       17(1)

C(24)        1179(10)      -232(2)       1613(4)       12(1)

C(25)        3587(10)      -323(2)       2394(5)       18(1)

C(26)        4648(11)        68(2)       3212(5)       17(1)

O(1W)       -3636(10)      1190(2)       -286(5)       50(1)

O(2W)         971(11)      1429(3)      -1350(6)       67(2)

________________________________________________________________

Table 3.   Bond lengths [A] and angles [deg] for [Cu(INA)2]2H2O.

_____________________________________________________________

Cu(1)-O(3)#1                  1.967(4)

Cu(1)-O(1)#2                  1.981(5)

Cu(1)-N(1)                    2.009(5)

Cu(1)-N(2)                    2.013(5)

Cu(1)-O(4)#3                  2.252(3)

N(1)-C(16)                    1.352(7)

N(1)-C(12)                    1.351(8)

C(10)-O(2)                    1.254(7)

C(10)-O(1)                    1.267(8)

C(10)-C(14)                   1.515(9)

O(1)-Cu(1)#4                  1.981(5)

C(12)-C(13)                   1.391(9)

C(13)-C(14)                   1.384(6)

C(14)-C(15)                   1.392(8)

C(15)-C(16)                   1.384(6)

N(2)-C(22)                    1.342(7)

N(2)-C(26)                    1.360(7)

C(20)-O(4)                    1.246(6)

C(20)-O(3)                    1.276(6)

C(20)-C(24)                   1.512(7)

O(3)-Cu(1)#5                  1.967(4)

O(4)-Cu(1)#6                  2.252(3)

C(22)-C(23)                   1.378(7)

C(23)-C(24)                   1.387(6)

C(24)-C(25)                   1.387(7)

C(25)-C(26)                   1.382(7)

O(3)#1-Cu(1)-O(1)#2         170.1(2)

O(3)#1-Cu(1)-N(1)            93.0(2)

O(1)#2-Cu(1)-N(1)            84.03(13)

O(3)#1-Cu(1)-N(2)            90.15(14)

O(1)#2-Cu(1)-N(2)            92.4(2)

N(1)-Cu(1)-N(2)             175.8(2)

O(3)#1-Cu(1)-O(4)#3          96.48(14)

O(1)#2-Cu(1)-O(4)#3          93.1(2)

N(1)-Cu(1)-O(4)#3            92.9(2)

N(2)-Cu(1)-O(4)#3            89.5(2)

C(16)-N(1)-C(12)            118.0(5)

C(16)-N(1)-Cu(1)            119.5(4)

C(12)-N(1)-Cu(1)            122.0(5)

O(2)-C(10)-O(1)             124.4(6)

O(2)-C(10)-C(14)            119.4(6)

O(1)-C(10)-C(14)            116.2(6)

C(10)-O(1)-Cu(1)#4          114.7(4)

N(1)-C(12)-C(13)            121.9(6)

C(14)-C(13)-C(12)           119.6(5)

C(13)-C(14)-C(15)           118.9(5)

C(13)-C(14)-C(10)           121.2(5)

C(15)-C(14)-C(10)           119.8(6)

C(16)-C(15)-C(14)           118.5(5)

N(1)-C(16)-C(15)            123.2(5)

C(22)-N(2)-C(26)            117.3(5)

C(22)-N(2)-Cu(1)            120.3(4)

C(26)-N(2)-Cu(1)            122.4(4)

O(4)-C(20)-O(3)             127.4(5)

O(4)-C(20)-C(24)            118.3(4)

O(3)-C(20)-C(24)            114.3(4)

C(20)-O(3)-Cu(1)#5          125.4(3)

C(20)-O(4)-Cu(1)#6          137.2(3)

N(2)-C(22)-C(23)            122.9(5)

C(22)-C(23)-C(24)           120.1(5)

C(23)-C(24)-C(25)           117.2(4)

C(23)-C(24)-C(20)           122.1(4)

C(25)-C(24)-C(20)           120.7(4)

C(26)-C(25)-C(24)           120.2(5)

N(2)-C(26)-C(25)            122.2(5)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x+1,-y,z+1/2    #2 x-1/2,-y+1/2,z-1/2

#3 x,-y,z+1/2    #4 x+1/2,-y+1/2,z+1/2    #5 x-1,-y,z-1/2

#6 x,-y,z-1/2

Table 4.   Anisotropic displacement parameters (A^2 x 10^3) for [Cu(INA)2]2H2O.

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Cu(1)    13(1)       8(1)      12(1)      -1(1)      -2(1)       0(1)

N(1)     13(3)       9(3)      11(3)      -2(2)      -4(2)       0(2)

C(10)    14(3)      10(3)      16(3)       5(2)      -5(3)      -1(2)

O(1)     21(3)      11(2)      12(2)       1(2)       1(2)      -1(2)

O(2)     24(2)      23(2)      25(2)     -10(2)       8(2)     -11(2)

C(12)    18(3)      16(3)      13(3)      -1(2)       3(3)      -1(2)

C(13)    14(3)      17(3)      22(3)       0(3)       4(3)      -1(2)

C(14)    13(3)      14(3)      14(3)      -3(2)      -7(3)       3(2)

C(15)    22(3)      13(2)      12(2)      -1(2)       4(2)       0(2)

C(16)    17(3)      13(2)      13(2)      -1(2)       3(2)       0(2)

N(2)     15(3)      13(2)      11(2)      -1(2)       1(2)      -3(2)

C(20)    18(3)      11(2)      10(2)      -1(2)       0(2)       2(2)

O(3)     13(2)      10(2)      18(2)      -1(2)      -5(2)      -1(2)

O(4)     16(2)      11(2)      16(2)      -5(1)       4(2)       1(1)

C(22)    16(3)      17(2)      20(3)      -1(2)      -5(2)       8(2)

C(23)    16(3)      14(2)      17(3)      -2(2)     -10(2)       0(2)

C(24)    15(3)      10(2)      11(2)      -1(2)      -2(2)       1(2)

C(25)    16(3)      13(2)      23(3)      -4(2)      -1(2)       4(2)

C(26)    18(3)      14(2)      16(3)       0(2)      -5(2)       3(2)

O(1W)    48(3)      59(3)      42(3)     -12(2)       0(2)      18(2)

O(2W)    42(3)      91(5)      69(4)       5(4)       9(3)      15(3)

_______________________________________________________________________

Table 5.   Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for [Cu(INA)2]2H2O.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(12A)       4200(14)      1676(3)       6799(6)       19

H(13A)       5594(13)      2448(3)       7860(7)       21

H(15A)      10826(11)      2723(2)       5428(4)       18

H(16A)       9252(10)      1957(2)       4405(4)       17

H(22A)        310(11)       977(2)       2504(5)       22

H(23A)      -1676(11)       339(2)       1179(5)       20

H(25A)       4490(10)      -648(2)       2368(5)       21

H(26A)       6222(11)        -6(2)       3754(5)       20

H(1W)       -5008(10)      1311(2)       -756(5)       75

H(2W)       -3590(10)      1340(2)        412(5)       75

H(3W)        -412(11)      1359(3)       -994(6)      100

H(4WA)        840(11)      1760(3)      -1518(6)      100

H(4WB)        676(11)      1267(3)      -2038(6)      100

________________________________________________________________

Table 1.  Crystal data and structure refinement for [Cu(INA)2(H2O)4].

Identification code               candy5

Empirical formula                 C12 H16 Cu N2 O8

Formula weight                    379.80

Temperature                       293(2) K

Wavelength                        0.71073 A

Crystal system                    Tricinic

Space group                       P-1

Unit cell dimensions              a = 6.357(2) A   alpha = 99.42(2) deg.

b = 6.926(2) A    beta = 105.36(2) deg.

c = 9.213(3) A   gamma = 108.14(2) deg.

Volume, Z                         358.0(2) A^3,  1

Density (calculated)              1.761 Mg/m^3

Absorption coefficient            1.572 mm^-1

F(000)                            195

Crystal size                      0.4 x 0.2 x 0.05 mm

Theta range for data collection   2.38 to 24.99 deg.

Limiting indices                  0<=h<=7, -7<=k<=7, -10<=l<=10

Reflections collected             1374

Independent reflections           1249 [R(int) = 0.0642]

Refinement method                 Full-matrix least-squares on F^2

Data / restraints / parameters    1237 / 0 / 106

Goodness-of-fit on F^2            1.093

Final R indices [I>2sigma(I)]     R1 = 0.0625, wR2 = 0.1465

R indices (all data)              R1 = 0.0976, wR2 = 0.2113

Largest diff. peak and hole       0.473 and -0.501 e.A^-3

Table 2.  Atomic coordinates ( x 10^4) and equivalent isotropic

displacement parameters (A^2 x 10^3) for [Cu(INA)2(H2O)4].

U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

Cu(1)        5000          5000          5000          29(1)

N(1)         2675(9)       3752(8)       2821(6)       26(1)

C(2)          333(12)      2983(11)      2516(8)       32(2)

C(3)        -1264(12)      2251(11)      1019(7)       30(2)

C(4)         -483(11)      2283(10)      -249(7)       26(1)

C(5)         1948(12)      3016(10)        69(7)       29(2)

C(6)         3443(12)      3724(11)      1590(7)       30(2)

C(10)       -2130(12)      1592(11)     -1914(8)       31(2)

O(11)       -4288(9)        601(9)      -2139(6)       43(1)

O(12)       -1282(9)       2013(9)      -2941(5)       42(1)

O(1W)        3466(7)       7049(7)       5408(5)       31(1)

O(2W)        2516(9)       2314(8)       5927(6)       46(1)

________________________________________________________________

Table 3.   Bond lengths [A] and angles [deg] for [Cu(INA)2(H2O)4].

_____________________________________________________________

Cu(1)-O(1W)#1                 1.997(5)

Cu(1)-O(1W)                   1.997(5)

Cu(1)-O(2W)                   2.468(6)

Cu(1)-O(2W)#1		  	2.468(6)

Cu(1)-N(1)#1                  2.006(5)

Cu(1)-N(1)                    2.006(5)

N(1)-C(2)                     1.347(8)

N(1)-C(6)                     1.349(8)

C(2)-C(3)                     1.378(9)

C(3)-C(4)                     1.385(9)

C(4)-C(5)                     1.398(10)

C(4)-C(10)                    1.508(8)

C(5)-C(6)                     1.373(9)

C(10)-O(12)                   1.239(9)

C(10)-O(11)                   1.270(9)

O(1W)#1-Cu(1)-O(1W)         179.998(2)

O(1W)#1-Cu(1)-N(1)#1         90.0(2)

O(1W)-Cu(1)-N(1)#1           90.0(2)

O(1W)#1-Cu(1)-N(1)           90.0(2)

O(1W)-Cu(1)-N(1)             90.0(2)

N(1)#1-Cu(1)-N(1)           180.0

C(2)-N(1)-C(6)              117.4(5)

C(2)-N(1)-Cu(1)             122.8(4)

C(6)-N(1)-Cu(1)             119.8(4)

N(1)-C(2)-C(3)              122.7(6)

C(2)-C(3)-C(4)              120.1(6)

C(3)-C(4)-C(5)              117.1(6)

C(3)-C(4)-C(10)             122.9(6)

C(5)-C(4)-C(10)             120.0(6)

C(6)-C(5)-C(4)              119.8(6)

N(1)-C(6)-C(5)              122.8(6)

O(12)-C(10)-O(11)           125.5(6)

O(12)-C(10)-C(4)            118.1(6)

O(11)-C(10)-C(4)            116.4(6)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y+1,-z+1

Table 4.   Anisotropic displacement parameters (A^2 x 10^3) for

[Cu(INA)2(H2O)4].

The anisotropic displacement factor exponent takes the form:

-2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Cu(1)    26(1)      38(1)      17(1)       0(1)      -2(1)      14(1)

N(1)     29(3)      30(3)      17(3)       1(2)       5(2)      12(2)

C(2)     26(4)      41(4)      23(3)      -1(3)       6(3)      12(3)

C(3)     24(3)      38(4)      23(3)       3(3)       3(3)      11(3)

C(4)     28(4)      21(3)      21(3)       3(3)       0(3)       8(3)

C(5)     33(4)      31(4)      20(3)       9(3)       7(3)       9(3)

C(6)     26(4)      34(4)      24(3)       6(3)       1(3)      13(3)

C(10)    31(4)      28(4)      25(3)       0(3)      -4(3)      11(3)

O(11)    31(3)      50(3)      32(3)       7(2)      -6(2)      10(3)

O(12)    35(3)      65(4)      23(3)      10(2)       3(2)      23(3)

O(1W)    25(2)      46(3)      19(2)       5(2)      -3(2)      18(2)

O(2W)    37(3)      54(4)      47(3)      16(3)       9(3)      21(3)

_______________________________________________________________________

Table 5.   Hydrogen coordinates ( x 10^4) and isotropic

displacement parameters (A^2 x 10^3) for [Cu(INA)2(H2O)4].

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H(2A)        -229(12)      2945(11)      3350(8)       38

H(3A)       -2867(12)      1735(11)       859(7)       36

H(5A)        2551(12)      3023(10)      -747(7)       35

H(6A)        5055(12)      4206(11)      1778(7)       36

H(1W)        3189(7)       7562(7)       4632(5)       38

H(2W)        4385(7)       8056(7)       6210(5)       38

H(3W)        2003(9)       2866(8)       6581(6)       55

H(4W)        3263(9)       1604(8)       6339(6)       55

________________________________________________________________