Table 1 Structural properties of the SBA-15 samples

| Samples SiO2/P123 ( r ) | Unit cell a as-syn. calcined (nm) | Pore size w a BJHads./BJHdes. (nm) | Wall thickness b (nm) | Pore volume a (cm3/g) | BET surface area a (m2/g) |
| --- | --- | --- | --- | --- | --- |
| 45 | 12.29 9.99 | 8.6 / 6.6 | 1.39 | 1.17 | 701 |
| 60 | 12.57 10.29 | 7.4 / 6.0 | 2.89 | 0.86 | 611 |
| 75 | 11.85 10.62 | 6.9 / 5.4 | 3.72 | 0.72 | 527 |

a We do not intend here to discuss the accuracy of the evaluation methods used. In any cases, they can be employed systematically to identify trends. However, the BJH is known to underestimate pore sizes by about 20-25% (ref. 8) b Calculated from a- wBJH adsorption