# Supplementary data

BETS as a source of molecular magnetic superconductors (BETS = bis(ethylenedithio)tetraselenafulvalene)

Hayao Kobayashi,a Akiko Kobayashi,b and Patrick Cassouxc

a Institute for Molecular Science, Okazaki 444-8585, Japan

b Research Centre for Spectrochemistry, Graduate School of Science, The University of Tokyo, Hongo, Bunkyo-ku, Tokyo 113-0033, Japan

c Equipe Précurseurs Moléculaires et Matériaux, LCC/CNRS, 205 Route de Narbonne, 31077 Toulouse Cedex 04, France

### List  of  BETS-based  compounds

| Anion | Stoichiometry | Morphology | Packing | Space gr. | RT | Behaviour | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | BETS |  |  |  |  | First synthesis | 0 |
|  | BETS |  |  |  |  | Prediction of usefulness | 1 |
|  | BETS |  |  | P21/c |  | Synth., isostructural to BEDT-TTF | 2 |
|  | BETS |  |  |  |  | Synth. | 5 |
|  | BETS |  |  | P21/n |  | Improved synth., structure | 40 |
| PF6- | (BETS)2PF6 |  |  or  | C2/c |  | M-I(28) | 2 |
|  | (BETS)2PF6(TCE)x | plate |  | C2/c |  | M (>4) | 2 |
| AsF6- | (BETS)2AsF6(TCE)x | plate |  | C2/c |  | M (>4) | 2 |
| SbF6- | (BETS)2SbF6 | plate |  | C2/c |  | M (>4) | 2, 6 |
|  | " | " | " | " | 0.5 | M (>15) | 8 |
| TaF6- | (BETS)2TaF6 | plate |  | C2/c | 10 | M (>4) | 2, 4, 6 |
|  | " | plate |  or  | C2/c |  | M-I(25) | 2 |
|  | " | plate |  | C2/c | 10 | M-I(70) | 4 |
|  | " | plate |  | C2/c |  | M-I(25) | 6 |
| ClO4- | (BETS)2ClO4 |  |  | P21/c |  | M (>4) | 2 |
|  | (BETS)2ClO4(TCE)x |  | (4x4) | P21/c |  | M (>4) | 6, 33 |
| BF4- | (BETS)2BF4 |  |  | P21/c |  | M (>4) | 2 |
|  | (BETS)2BF4(TCE)0,5 |  | (4x4) | P21/c |  | M (>4) | 2, 33 |

| Anion | Stoichiometry | Morphology | Packing | Space gr. | RT | Behaviour | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| HgBr42- | (BETS)4HgBr4 | plate |  | P21/c |  | M-I(70) | 2 |
|  | (BETS)4HgBrx | plate |  | P21/c |  | M (>4) | 2 |
|  | (BETS)4HgBr4(PhCl)0,25 | plate |  | I41/a |  | M (>4) | 2 |
|  | (BETS)4HgBr4(PhCl)0,25 | plate |  | I41/a | 10 | PM-I (100?) | 3 |
|  | (BETS)4HgBr4(PhCl)x |  |  | I41/a | 10 | M (>4) | 6 |
| Hg3I82- | (BETS)4Hg3I8 |  |  | P1 | 50 | M-I (200) | 25 |
|  | (BETS)4Hg3I8 (phase 1) |  |  |  | 200 | M (>4.6) | 35 |
|  | (BETS)4Hg3I8 (phase 2) |  |  | C2 | 100 | M-I (95) | 35 |
| KHg(SCN)4 | (BETS)2KHg(SCN)4 |  |  | P1 | 14 | M (>0.4) | 25 |
| NH4Hg(SCN)4 | (BETS)2 NH4Hg(SCN)4 |  |  | P1 | 3 | M (>0.4) | 25 |
| I3- | (BETS)2I3 |  |  | P1 |  | M-I(45) | 2, 6 |
|  | " |  | " |  |  | M-I(50), Optical reflectance | 13 |
|  | " |  | " |  |  | S-d-H, AMRO | 28 |
|  | " |  | " |  |  | NMR, ESR, magnetic studies | 60 |
| IBr2- | (BETS)2IBr2 |  |  | P1 |  | M-I(45) | 2 |
| AuI2- | (BETS)2AuI2 |  |  | P1 |  | M-I(45) | 2 |
| AuBr2- | (BETS)2BrI2 |  |  ? | P1 |  | M-I(37) | 2 |
| ICl2- | (BETS)2ICl2 |  |  | P1 |  | M-I(110) | 2 |
| Cu[N(CN)2]Br- | (BETS)2Cu[N(CN)2]Br | diamond plate |  | Pnma | 50 |  | 8 |
|  | " |  | " | " | 17//b | M (>4) | 11 |

| Anion | Stoichiometry | Morphology | Packing | Space gr. | RT | Behaviour | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| GaCl4- | (BETS)2GaCl4 | diamond plates |  | Pnma | 25 | M-I(270) | 5 |
|  | " | plates |  | Pnma | 70 | M-I(65) | 8, 63 |
|  | " |  | " |  | 50 | M (>4) | 10 |
|  | " |  | " |  |  | S-d-H, AMRO | 23, 27 |
|  | " |  | " |  |  | dH-vH | 47 |
| GaCl4- | (BETS)2GaCl4 |  |  | P1 |  | SC(8) | 9 |
|  | " |  | " |  |  | anisotropy of upper critical field | 53 |
|  | " |  | " |  |  | magnetic torque meas. | 62 |
| GaCl3Br- | (BETS)2GaCl3Br | needle |  | P1 | 50 | SC(7.5-10) up to 14 kbar | 14 |
| GaCl3Br- | (BETS)2GaCl3Br | " | " |  |  | SC(8) [suppression at 1 Tesla] | 16 |
| GaCl2,5Br1,5- | (BETS)2GaCl2,5Br1,5 | " | " |  |  | pressure meas. magnetic meas. | 34 |
| GaCl4-xBrx- | (BETS)2Ga4-xBrx | " | " |  |  | SC(7--8) | 20, 23 |
| GaCl4-xBrx- | (BETS)2GaCl4-xBrx | " | " |  |  | T/P/x phase diagram, SC | 49, 55 |
| GaCl4-xBrx- | (BETS)2GaCl4-xBrx | " | " |  |  | Calculations on the spin gap phase | 59 |
| GaBr4- | (BETS)2GaBr4 |  |  | Pnma | 50 | M (>4) | 10 |
|  | (BETS)2GaBr4 | needle | ' | P1 | 0.06 | PM-I (50), pressure meas. |  |
| GaCl3F- | (BETS)2GaCl3F | needle |  | P1 |  | SC(3.5) | 16, 20 |
| FeCl4- | (BETS)2FeCl4 | plate |  | Pnma | 50 | M (>4) | 10, 63, 65 |
|  | " | " | " |  | 100 | M (>2) | 15 |
|  | " | " | " |  |  | IR reflectance | 21 |
|  | " | " | " |  |  | S-d-H | 42 |
|  | " | " | " |  |  | magnetization | 64 |
| FeCl4- + GaCl4- | (BETS)2Fe0.75Ga0.25Cl4 | plate |  |  | 15-40 | M (>1,5) S-d-H, AMRO | 22, 30 |

| Anion | Stoichiometry | Morphology | Packing | Space gr. | RT | Behaviour | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| FeCl4- | (BETS)2FeCl4 | needle |  | P1 | 50 | M-I(8) | 10 |
|  | " | " | " |  |  | Magnetotransport: FRHCS | 11 |
|  | " | " | " |  | 20 | M-I(8.5), M (>4) at p> 3.5 kbar | 15 |
|  | " | " | " |  |  | Magnetic anisotropy | 29 |
|  | " | " | " |  |  | T/P/H phase diagram | 38 |
|  | " | " | " |  |  | magnetisation, antiferromagnetism, | 41, 65 |
|  | " | " | " |  |  | S-d-H,T/H phase diagram,calculations | 41 |
|  | " | " | " |  |  | RKKY Calculation on FRHCSs | 66 |
|  | " | " | " |  |  | torque anisotropy | 67 |
|  | " | " | " |  |  | 1st metal with AF ordering | 72 |
|  | " | " | " |  |  | Pressure induced SC transition | 73 |
| FeCl4- + GaCl4- | (BETS)2FexGa1-xCl4 | needle |  |  |  | unprecedented SC-I | 31, 57 |
|  | " | " | " |  |  | T/x phase diagram | 43 |
|  | " | " | " |  |  | SC with I magnetic ground state | 71 |
|  | " | " | " |  |  | magnetic properties | 74 |
| FeBr4- | (BETS)2FeBr4 | plate |  | Pnma | 50 | M (>4) | 10, 15 |
|  | " | " | " |  |  | Antiferromagnetic metal with SC | 69 |
| FeCl4-xBrx- | (BETS)2FeCl4-xBrx | needle |  | P1 |  | M-I(x-dependent T), FRHCS | 45 |

| Anion | Stoichiometry | Morphology | Packing | Space gr. | RT | Behaviour | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| InCl4- | (BETS)2InCl4 |  |  | Pnma | 50 | M (>4) | 10, 33 |
|  | (BETS)2InCl5(TEA)O.7 | plate |  | P21/a | 5 | M-I(55) | 26, 33 |
| InBr4- | (BETS)2InBr4 |  |  |  | 5 | I | 25 |
| InI4- | (BETS)2InI4 |  |  |  | 33 | M-I(205) | 25 |
| TlCl4- | (BETS)2TlCl4 |  |  | Pbnm | 3 | M-I(140) | 25 |
| TlBr4- | (BETS)2TlBr4 |  |  |  | 11 | M-I(65) | 25 |
| TlI4- | (BETS)2TlI4 |  |  | C2/c | 10 | I | 25 |
| (TlI4)(I3)- | (BETS)2(TlI4)(I3) |  |  | Pcab | 0.008 | I | 25 |
| TlHg(SeCN)4- | (BETS)2TlHg(SeCN)4 |  |  | P1 |  | M (>4), magnetores. and opt. meas. | 39, 56 |
| CF3SO3- | (BETS)2CF3SO3 |  |  | P21/a | 0.06 | M-I(80) | 8 |
| CoCl4- | (BETS)4CoCl4 | plate |  |  | 20 | M (>2) | 15, 16, 26 |
| MnCl4- | (BETS)2MnCl4 | plate |  |  | 40 | M-I(40) | 15 |
| MnBr4- | (BETS)2MnBr4 | plate |  |  | 50 | M-I(70) | 15 |
| NiCl4- | (BETS)2NiCl4 | plate |  |  | 50 | M-I(50) | 15, 26 |
| NiBr4- | (BETS)2NiBr4 | plate |  |  | 50 | weakly M (>4) | 15 |
| Ni(CN)4- | (BETS)2Ni(CN)4 | plate |  |  | 6 | high  (>4) | 15, 26 |
| Pd(CN)4- | (BETS)2Pd(CN)4 |  |  |  |  | M (>4) | 26 |
| Pt(CN)4- | (BETS)2Pt(CN)4 |  |  |  |  | M (>4) | 26 |

| Anion | Stoichiometry | Morphology | Packing | Space gr. | RT | Behaviour | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CuCl3- | (BETS)2CuCl4 | needle |  |  | 100 | M (>4) | 15 |
|  | (BETS)4Cu2Cl6 | needle |  |  | 100 | M (>4) | 16, 26 |
|  | " | " | " |  |  | S-d-H, AMRO | 16 |
|  | " | " | " | P21212 |  | magnetic meas; J = 163 K | 36 |
|  | (BETS)4Cu2Cl6 (phase II) |  |  | Pnab |  | S-d-H, AMRO | 30 |
|  | (BETS)4Cu4Cl8 (phase I) |  |  | Pbnb |  |  | 30 |
|  | (BETS)4Cu4Cl8 |  |  | Pccn | 0.01 | IR reflectivity | 68 |
|  | (BETS)xCuCl3 (phase III) |  |  |  |  |  | 30 |
| CuBr4- | (BETS)2CuBr4 | plate |  |  | 150 | M-I(55) | 15 |
| Bi2Cl82- | (BETS)2Bi2Cl8 | wide plate |  | P21/n | 0.1 | I | 37 |
| Bi3Cl123- | (BETS)6Bi3Cl12 | long plate |  | P1 | 20 | weakly M (>180) | 37 |
| C(CN)3- | (BETS)2C(CN)3 |  |  | A2/a | 50 | M (>4), S-d-H | 44, 56, 61 |
| C60x- | (BETS)2C60 | whisker |  | C2/c |  |  | 46 |
| Ag(CN)2- | (BETS)2Ag(CN)2 |  |  | P21212 | 100 | M (>4) | 48, 58 |
| Cu5I6- | (BETS)2Cu5I6 |  |  | P21 | 30 | M-I(30), M (>4 for P> 10 Kbar) | 51 |
| Cl2TCNQx- | (BETS)2(Cl2TCNQ) |  |  | P1 |  | SC(0.8 K/6 kbar) | 52 |
|  | " |  |  |  |  | M (>2) | 54 |
| Ag(CF3)4- | (BETS)2Ag(CF3)4(TCE) | blocks | L | Pnma |  | M (>2) | 70 |
| M = metal (>T = temperature); M-I(T) = metal-insulator; PM = pseudo-metal; RT = room temperature conductivity (in S/cm); FRHCS = Field Restored Highly Conducting State; S-d-H = Shubnikov de Haas oscillations; AMRO = Angle dependent magnetoresistance; dH-vH = de Haas-van Alphen oscillations; T/P/H = temperature/pressure/magnetic field |

References

0.	R. R. Schumaker, V. Y. Lee and E. M. Engler, IBM Research Report, 1983.

1.	R. Kato, RH. Kobayashi, A. Kobayashi, and Y. Sasaki, Chem. Lett., 1984, 1693-1696.

2.	R. Kato, H. Kobayashi, and A. Kobayashi, Synt. Met., 1991, 42, 2093-2096.

3.	T. Naito, A. Miyamoto, H. Kobayashi, R. Kato, A. Kobayashi, Chem. Lett., 1991, 1945-1948.

4.	R. Kato, A. Kobayashi, A. Miyamoto, H. Kobayashi, Chem. Lett., 1991, 1045-1048.

5.	L. K. Montgomery,  T. Burgin, C. Husting, L. Tilley, J. C. Huffman, K. D. Carlson, J. D. Dudek, G. A. Yaconi, U. Geiser and J. M. Williams, Mol. Cryst. Liq. Cryst., 1992, 211, 283-288.

6.	A. Kobayashi, R. Kato, T. Naito, and H. Kobayashi, Synt. Met., 1993, 56, 2078-2083.

7.	R. Kato, S. Aonuma, Y. Okano, H. Sawa, A. Kobayashi, and H. Kobayashi, Synt. Met., 1993, 56, 2084-2089.

8.	L.K. Montgomery, T. Burgin, J.C. Huffman, K.D. Carlson, J.D. Dudek, G.A. Yaconi, L.A. Megna, P.R. Mobley, W.W. Kwok, J.M. Williams, J.E. Shirber, D.L. Overmyer, J. Ren, C. Rovira, and M.-H. Whangbo, Synt. Met., 1993, 55-57, 2090-2095.

9.	H. Kobayashi, T. Udagawa, H. Tomita, K. Bun, T. Naito, and A. Kobayashi, Chem. Lett., 1993, 1559-1562.

10.	A. Kobayashi, T. Udagawa, H. Tomita, T. Naito, and H. Kobayashi, Chem. Lett., 1993, 2179-2182

11.	F. Goze, V.N. Laukhin, L. Brossard, A. Audouard, J.P. Ulmet, S. Askenazy, T. Naito, H. Kobayashi, A. Kobayashi, M. Tokumoto, and P. Cassoux, Europhys. Lett., 1994, 28, 6, 427-431.

12.	T. Burgin, T. Miebach, J. C. Huffman, L. K. Montgomery, J. A. Paradis, C. Rovira, M-H. Whangbo, S. N. Magonov, S. I. Khan, C. E. Strouse, D. L. Overmyer, J. E. Schriber, J. Mat. Chem., 1995, 5, 1659-1669.

13.	M. Inokuchi, H. Tajima, A. Kobayashi, T. Ohta, H. Kuroda, R. Kato, T. Naito, and H. Kobayashi, Bull. Chem. Soc. Jpn., 1995, 68, 547-553.

14.	H. Kobayashi, H. Tomita, T. Naito, H. Tanaka, A. Kobayashi, and T. Saito, J. Chem. Soc., Chem. Commun., 1995, 1225-1226.

15.	H. Kobayashi, H. Tomita, T. Naito, A. Kobayashi, F. Sakai, T. Watanabe, and P. Cassoux, J. Am. Chem. Soc., 1996, 118, 368-377.

16.	H. Kobayashi, T. Naito, A. Sato, K. Kawano, A. Kobayashi, H. Tanaka, T. Saito, M. Tokumoto, L. Brossard, and P. Cassoux, Mol. Cryst. Liq. Cryst., 1996, 284, 61-72.

17.	L. K. Montgomery, T. Burgin, T. Miechbach, D. Dunham, J. C. Huffman, J. E. Schirber, Mol. Cryst. Liq. Cryst., 1996, 284, 73-84.

18.	N. Kushch, C. Faulmann, P. Cassoux, L. Valade, I. Malfant, J.-P. Legros, C. Bowlas, A. Errami, A. Kobayashi, and H. Kobayashi, Mol. Cryst. Liq. Cryst., 1996, 284, 247-258.

19.	H. Kobayashi, A. Kobayashi, T. Naito, M. Tokumoto, L. Brossard, N. Kushch, and P. Cassoux, Mol. Cryst. Liq. Cryst., 1996, 285, 11-18.

20	H. Tanaka, A. Kobayashi, T. Saito, K. Kawano, T. Naito, and H. Kobayashi, Adv. Mat., 1996, 8, 10, 812-815.

21.	I. Olejniczak, A. Graja, N.D. Kushch, P. Cassoux, and H. Kobayashi, J. Phys. I France, 1996, 6, 1631-1641.

22.	N. D. Kushch, O.A. Dyachenko, V.V. Gritsenko, S.I. Pesotskii, R.B. Lubovskii, P. Cassoux, Ch. Faulmann, A.E. Kovalev, M.V. Kartsovnik, L. Brossard, H. Kobayashi, and A. Kobayashi, J. Phys. I France, 1996, 6, 1997-2009.

23	H. Tajima, A. Kobayashi, T. Naito, H. Kobayashi, Solid State Commun., 1996, 98, 755-759.

24.	H. Kobayashi, E. Arai, T. Naito, H. Tanaka, A. Kobayashi, and T. Saito, Synt. Met., 1997, 85, 1463-1464.

25.	L. K. Montgomery, B. W. Fravel, J.C. Huffman, C.C. Agosta, and S. A. Ivanov, Synt. Met., 1997, 85, 1521-1522.

26.	H. Kobayashi, E. Arai, T. Naito, H. Tanaka, A. Kobayashi, T. Saito, and P. Cassoux, Synt. Met., 1997, 85, 1595-1596.

27.	H. Tajima, A. Kobayashi, T. Naito,and H. Kobayashi, Synt. Met., 1997, 86, 1911-1912.

28.	N. Tajima, K. Matuo, M. Tamura, Y. Nishio, K. Kajita, T. Naito, and H. Kobayashi, Synt. Met., 1997, 86, 1981-1982.

29.	M. Tokumoto, T. Naito, H. Kobayashi, V. N. Laukhin, L. Brossard, and P. Cassoux, , Synt. Met., 1997, 86, 2161-2162.

30.	N. D. Kushch, O.A. Dyachenko, R.B. Lubovskii, S.I. Pesotskii, , M.V. Kartsovnik, , A.E. Kovalev P. Cassoux, H. Kobayashi, Adv. Mat. for Optics and Electronics, 1997, 7, 57-60.

31.	H. Kobayashi, A. Sato, E. Arai, H. Akutsu, A. Kobayashi, and P. Cassoux, J. Am. Chem. Soc., 1997, 119, 12392-12393.

32.	H. Akutsu, E. Arai, H. Kobayashi, H. Tanaka, A. Kobayashi, and P. Cassoux, J. Am. Chem. Soc., 1997, 119, 12681-12682.

33.	A. Kobayashi, H. Kobayashi, Mol. Cryst. Liq. Cryst., 1997, 296, 181-195.

34.	H. Kobayashi, H. Akutsu, E. Arai, H. Tanaka, A. Kobayashi, Phys. Rev. B. 1997, 56, 8526-8529.

35.	O. A. Bogdanova, V. V. Gritsenko, O.A. Dyachenko, E. I. Zhilyaeva, A. Kobayashi, H. Kobayashi, R. N. Lyubovskaya, R.B. Lyubovskii, and G. V. Shilov, Chem. Lett., 1997, 675-676.

36.	A. Kobayashi, A. Sato, E. Arai, . H. Kobayashi, C. Faulmann, N. Kushch, P. Cassoux, Solid State Commun., 1997, 103, 371-374.

37.	N. D. Kushch, O.A. Dyachenko, V. V. Gritsenko, P. Cassoux, C. Faulmann, A. Kobayashi, H. Kobayashi, J. Chem. Soc., Dalton Trans., 1998, 683-688.

38.	H. Akutsu, K. Kato, E. Arai, H. Kobayashi, A. Kobayashi, M. Tokumoto, L. Brossard and P. Cassoux, Solid State Communications, 1998, 105 (8), 485-489.

39.	N. D. Kushch, L. I. Buravov, S.I. Pesotskii, R.B. Lyubovskii, E. B. Yagubskii, M. C. Kaplunov, E. V. Golubev, B. Z. Narymbetov, S. S. Khasanov, L. V. Zorina, L. P. Rozenberg, R. P. Shibaeva, A. Kobayashi, H. Kobayashi, J. Mater. Chem., 1998, 8(4), 897-901.

40.	T. Courcet, I. Malfant, K. Pokhodnia, P. Cassoux, New. J. Chem., 1998, 6, 585-589.

41.	L. Brossard, R. Clerac, C. Coulon, M. Tokumoto, T. Ziman, D.K. Petrov, V.N. Laukhin, M.J. Naughton, A. Audouard, F. Goze, A. Kobayashi, H. Kobayashi, P. Cassoux, Eur. Phys. J. B, 1998, 1, 439-452.

42.	N. Harrison, C.H. Mielke, D.G. Rickel, L.K. Montgomery, C. Gerst, J.D. Thompson, PhysicalRev. B, 1998, 57, 8751-8754.

43.	A. Sato, E. Ojima, H. Akutsu, H. Kobayashi, A. Kobayashi, P. Cassoux, Chem. Lett ., 1998, 673-674.

44.	B.Z. Narymbetov, N.D. Kushch, L.V. Zorina, S.S. Khasanov, R.P. Shibaeva, T.G. Togonidze, A.E. Kovalev, M.V. Kartsovnik, L.I. Buravov, E.B. Yagubskii, E. Canadell, A. Kobayashi, H. Kobayashi, Eur. Phys. J. B, 1998, 5, 179-185.

45.	H. Akutsu, K. Kato, E. Ojima, H. Kobayashi, N. Tanaka, A. Kobayashi, PhysicalRev. B, 1998, 58, 9294-9302.

46.	M.M. Aslam, O. Ito, N. Sakurai, H. Moriyama, Fullerene Science and Technology, 1998, 6(6), 1007-1024.

47.	S.I. Pesotski, R.B. Lyubovskii, N.D. Kushch, M.V. Kartsovnik, W. Biberacher, K. Andres, H. Kobayashi, A. Kobayash, Journal of experimental and theoretical physics, 1999, 88, 114-117.

48.	S. Golhen, L. Ouahab, A. Lebeuze, M. Bouayed, P. Delhaes, Y. Kashimura, R. Kato, L. Binet, J.M. Fabre, J. Mater. Chem., 1999, 9, 387-393.

49.	H. Tanaka, A. Kobayashi, A. Sato, H. Akutsu, H. Kobayashi, J. Am. Chem. Soc., 1999, 121, 760-768.

50.	H. Tanaka, A. Kobayashi, H. Kobayashi, Chem . Lett ., 1999, 133-134.

51.	N.D. Kushch, O.A. Dyachenko, V.V. Gritsenko, L.I. Buravov, V.A. Tkacheva, E.B. Yagubskii, M.G. Kaplunov, E.V. Golubev, T.G. Togonidze, A. Kobayashi, H. Kobayashi, J. Mater. Chem., 1999, 9, 687-691.

52.	R. Kondo, T. Hasegawa, T. Mochida, S. Kagoshima, Y. Iwasa, Chem . Lett ., 1999, 333-334.

53.	M.A. Tanatar, T. Ishiguro, H. Tanaka, A. Kobayashi, H. Kobayashi, Journal of superconductivity, 1999, 12, 511-514.

54.	R. Kondo, S. Kagoshima, T. Hasegawa, T. Mochida, Y. Iwasa, Synth. Met., 1999, 102, 1628-1629.

55.	H. Kobayashi, H. Akutsu, H. Tanaka, A. Kobayashi, M. Tokumoto, L. Brossard, P. Cassoux, Synth. Met., 1999, 102, 1654-1657.

56.	L.V. Zorina, B.Z. Narymbetov, S.S. Khasanov, R.P. Shibaeva, N.D. Kushch, E.B. Yagubskii, A. Kobayashi, H. Kobayashi, Synth. Met., 1999, 102, 1735-1736.

57.	H. Kobayashi, H. Akutsu, E. Ojima, A. Sato, H. Tanaka, A. Kobayashi, P. Cassoux, Synth. Met., 1999, 103, 1837-1838.

58.	H. Mori, N. Sakurai, S. Tanaka, H. Moriyama, T. Mori, H. Kobayashi, A. Kobayashi, Synth. Met., 1999, 103, 1882.

59.	H. Seo, H. Fukuyama, Synth. Met., 1999, 103(1-3), 1951-1952.

60.	K. Kodama, T. Nakamura, T. Takahashi, E. Ojima, H. Kobayashi, Synth. Met., 1999, 103, 1963-1964.

61.	T.G. Togonidze, A.E. Kovalev, M.V. Kartsovnik, E. Canadell, N.D. Kushch, E.B. Yagubskii, Synth. Met., 1999, 103, 1969-1970.

62.	H. Uozaki, S. Kawamata, K. Okuda, K. Ueda, T. Sugimoto, N. Toyota, Synth. Met., 1999, 103, 1981-1982.

63.	H. Uozaki, S. Endo, H. Matsui, K. Ueda, T. Sugimoto, N. Toyota, Synth. Met., 1999, 103, 1983.

64.	H. Uozaki, K. Okamoto, S. Endo, H. Matsui, K. Ueda, T. Sugimoto, N. Toyota, Synth. Met., 1999, 103, 1984.

65.	D. Zhang, C. Probst, W. Biberacher, K. Andres, N. Kushch, H. Kobayashi, Synth. Met., 1999, 103, 2012-2013.

66.	T. Ziman, Synth. Met., 1999, 103, 2014-2015.

67	J.I. Oh, M.J. Naughton, T. Courcet, I. Malfant, P. Cassoux, M.Tokumoto ; M. Akutsu ; M. Kobayashi, A. Kobayashi, Synth. Met. 1999, 103, 1861-1864

68.	T. Courcet, I. Malfant, M. Gornitzka, P. Cassoux, H. Kobayashi, Synth. Met. 1999, 102, 1761-1762.

69.	E. Ojima, H. Fujiwara, K. Kato, H. Kobayashi, H. Tanaka, A. Kobayashi, M. Tokumoto, P. Cassoux-P, J. Am. Chem. Soc., 1999, 121, 5581-5582.

70.	J.A. Schlueter, U. Geiser, A.M. Kini, H.H. Wang, J.M. Williams, D. Naumann, T. Roy, B. Hoge, R. Eujen, Coord. Chem. Rev., 1999, 192, 781-810.

71.	H. Kobayashi, A. Sato, H. Tanaka, A. Kobayashi, P. Cassoux, Coord. Chem. Rev., 1999; 192, 921-932.

72.	A. Sato, E. Ojima, H. Kobayashi, Y. Hosokoshi, K. Inoue, A. Kobayashi, P. Cassoux, Adv. Mater., 1999, 11, 1192-1194.

73.	H. Tanaka, T. Adachi, E. Ojima, H. Fujiwara, K. Kato, H. Kobayashi, A. Kobayashi, P. Cassoux, J. Am. Chem. Soc., 1999, 121, 11243-11244.

74.	A. Sato, E. Ojima, H. Akutsu, Y. Nakazawa, H. Kobayashi, H. Tanaka, A. Kobayashi, P. Cassoux, Phys. Rev. B, 2000, 61, 111-114.