Table 1.  Crystal data and structure refinement for [Cu3(CN)3(pyr)].

Identification code 	[Cu3(CN)3(pyr)]

Empirical formula 	C7H4Cu3N5

# Formula weight 	348.77

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 15.8220(8) Å	 = 90.

b = 9.6848(5) Å	= 107.1420(10).

c = 20.4542(10) Å	 = 90.

Volume	2995.0(3) Å3

Z	12

Density (calculated)	2.320 Mg/m3

Absorption coefficient	6.299 mm-1

F(000)	2016

Crystal size	0.17 x 0.13 x 0.08 mm3

Theta range for data collection	2.08 to 28.27.

Index ranges	-21<=h<=19, -12<=k<=9, -24<=l<=26

Reflections collected	9981

Independent reflections	3627 [R(int) = 0.0413]

Completeness to theta = 28.27	97.7 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3627 / 0 / 205

Goodness-of-fit on F2	1.091

Final R indices [I>2sigma(I)]	R1 = 0.0562, wR2 = 0.1262

R indices (all data)	R1 = 0.0864, wR2 = 0.1348

Extinction coefficient	0.00035(4)

Largest diff. peak and hole	1.787 and -1.584 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu3(CN)3(pyr)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	1670(1)	7759(1)	834(1)	17(1)

Cu(2)	0	8034(1)	2500	21(1)

Cu(3)	-249(1)	7498(1)	49(1)	20(1)

Cu(4)	3086(1)	3024(1)	1715(1)	17(1)

Cu(5)	3578(1)	8024(1)	1602(1)	16(1)

N(10)	-1603(4)	7484(6)	27(3)	18(1)

N(11)	4937(5)	8021(6)	1626(3)	20(1)

N(12)	6721(4)	8010(6)	1696(3)	17(1)

N(1)	2287(5)	7564(7)	181(3)	19(1)

N(2)	1058(5)	7887(7)	1491(3)	17(1)

N(3)	638(5)	7947(6)	1869(4)	17(2)

N(4)	-33(5)	9415(7)	14(3)	24(2)

N(5)	-28(5)	5606(7)	16(4)	21(2)

N(6)	3327(5)	4922(7)	1728(4)	21(2)

N(7)	3383(5)	6120(7)	1695(4)	19(2)

N(8)	3338(4)	9927(6)	1596(3)	17(2)

N(9)	3291(5)	11142(6)	1631(3)	16(1)

C(1)	2287(5)	7564(7)	181(3)	19(1)

C(2)	1058(5)	7887(7)	1491(3)	17(1)

C(3)	638(5)	7947(6)	1869(4)	17(2)

C(4)	-33(5)	9415(7)	14(3)	24(2)

C(5)	-28(5)	5606(7)	16(4)	21(2)

C(6)	3327(5)	4922(7)	1728(4)	21(2)

C(7)	3383(5)	6120(7)	1695(4)	19(2)

C(8)	3338(4)	9927(6)	1596(3)	17(2)

C(9)	3291(5)	11142(6)	1631(3)	16(1)

C(10)	-2024(5)	8659(8)	111(4)	21(2)

C(11)	-2092(5)	6346(8)	-83(4)	23(2)

C(12)	5360(6)	6844(7)	1586(4)	22(2)

C(13)	5405(5)	9178(7)	1707(4)	21(2)

C(14)	6297(5)	9194(7)	1748(4)	19(2)

C(15)	6260(6)	6834(7)	1624(4)	19(2)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu3(CN)3(pyr)].

_____________________________________________________

Cu(1)-N(2) 	1.880(7)

Cu(1)-N(1) 	1.880(6)

Cu(1)-Cu(5) 	2.9749(15)

Cu(1)-Cu(3) 	2.9988(15)

Cu(2)-N(3) 	1.861(7)

Cu(2)-C(3)#1 	1.861(7)

Cu(2)-N(3)#1 	1.861(7)

Cu(2)-Cu(4)#2 	2.9810(10)

Cu(2)-Cu(4)#3 	2.9810(10)

Cu(3)-N(5) 	1.871(6)

Cu(3)-N(4) 	1.893(7)

Cu(3)-N(10) 	2.129(6)

Cu(4)-C(9)#4 	1.868(6)

Cu(4)-N(9)#4 	1.868(6)

Cu(4)-N(6) 	1.876(7)

Cu(4)-N(12)#5 	2.148(7)

Cu(4)-Cu(2)#6 	2.9810(10)

Cu(5)-N(8) 	1.881(6)

Cu(5)-N(7) 	1.889(7)

Cu(5)-N(11) 	2.136(7)

N(10)-C(11) 	1.327(10)

N(10)-C(10) 	1.356(10)

N(11)-C(13) 	1.327(9)

N(11)-C(12) 	1.337(9)

N(12)-C(15) 	1.337(9)

N(12)-C(14) 	1.349(9)

N(12)-Cu(4)#7 	2.148(7)

N(1)-C(1)#8 	1.146(13)

N(1)-N(1)#8 	1.146(13)

N(2)-N(3) 	1.159(8)

N(4)-C(4)#9 	1.142(14)

N(4)-N(4)#9 	1.142(14)

N(5)-C(5)#10 	1.179(13)

N(5)-N(5)#10 	1.179(13)

N(6)-N(7) 	1.167(9)

N(8)-N(9) 	1.182(8)

N(9)-Cu(4)#11 	1.868(6)

C(10)-C(11)#12 	1.383(11)

C(11)-C(10)#12 	1.383(11)

C(12)-C(15) 	1.402(10)

C(13)-C(14) 	1.388(10)

N(2)-Cu(1)-N(1)	178.0(3)

N(2)-Cu(1)-Cu(5)	105.8(2)

N(1)-Cu(1)-Cu(5)	74.1(2)

N(2)-Cu(1)-Cu(3)	74.6(2)

N(1)-Cu(1)-Cu(3)	105.5(2)

Cu(5)-Cu(1)-Cu(3)	179.55(4)

N(3)-Cu(2)-C(3)#1	174.8(4)

N(3)-Cu(2)-N(3)#1	174.8(4)

C(3)#1-Cu(2)-N(3)#1	0.0(5)

N(3)-Cu(2)-Cu(4)#2	72.6(2)

C(3)#1-Cu(2)-Cu(4)#2	107.4(2)

N(3)#1-Cu(2)-Cu(4)#2	107.4(2)

N(3)-Cu(2)-Cu(4)#3	107.4(2)

C(3)#1-Cu(2)-Cu(4)#3	72.6(2)

N(3)#1-Cu(2)-Cu(4)#3	72.6(2)

Cu(4)#2-Cu(2)-Cu(4)#3	179.62(6)

N(5)-Cu(3)-N(4)	157.1(3)

N(5)-Cu(3)-N(10)	101.0(3)

N(4)-Cu(3)-N(10)	101.4(3)

N(5)-Cu(3)-Cu(1)	86.0(2)

N(4)-Cu(3)-Cu(1)	76.8(2)

N(10)-Cu(3)-Cu(1)	149.95(17)

C(9)#4-Cu(4)-N(9)#4	0.0(4)

C(9)#4-Cu(4)-N(6)	156.5(3)

N(9)#4-Cu(4)-N(6)	156.5(3)

C(9)#4-Cu(4)-N(12)#5	101.2(3)

N(9)#4-Cu(4)-N(12)#5	101.2(3)

N(6)-Cu(4)-N(12)#5	101.9(3)

C(9)#4-Cu(4)-Cu(2)#6	82.9(2)

N(9)#4-Cu(4)-Cu(2)#6	82.9(2)

N(6)-Cu(4)-Cu(2)#6	79.6(2)

N(12)#5-Cu(4)-Cu(2)#6	150.00(17)

N(8)-Cu(5)-N(7)	156.7(3)

N(8)-Cu(5)-N(11)	101.6(3)

N(7)-Cu(5)-N(11)	100.9(3)

N(8)-Cu(5)-Cu(1)	84.8(2)

N(7)-Cu(5)-Cu(1)	78.3(2)

N(11)-Cu(5)-Cu(1)	150.43(18)

C(11)-N(10)-C(10)	115.8(7)

C(11)-N(10)-Cu(3)	122.7(5)

C(10)-N(10)-Cu(3)	121.4(5)

C(13)-N(11)-C(12)	117.1(7)

C(13)-N(11)-Cu(5)	121.5(5)

C(12)-N(11)-Cu(5)	121.3(5)

C(15)-N(12)-C(14)	117.6(7)

C(15)-N(12)-Cu(4)#7	121.4(5)

C(14)-N(12)-Cu(4)#7	121.0(5)

C(1)#8-N(1)-N(1)#8	0.0(8)

C(1)#8-N(1)-Cu(1)	175.5(9)

N(1)#8-N(1)-Cu(1)	175.5(9)

N(3)-N(2)-Cu(1)	176.2(6)

N(2)-N(3)-Cu(2)	177.9(6)

C(4)#9-N(4)-N(4)#9	0.00(8)

C(4)#9-N(4)-Cu(3)	175.0(9)

N(4)#9-N(4)-Cu(3)	175.0(9)

C(5)#10-N(5)-N(5)#10	0.0(7)

C(5)#10-N(5)-Cu(3)	173.7(9)

N(5)#10-N(5)-Cu(3)	173.7(9)

N(7)-N(6)-Cu(4)	172.7(6)

N(6)-N(7)-Cu(5)	173.7(6)

N(9)-N(8)-Cu(5)	172.2(6)

N(8)-N(9)-Cu(4)#11	172.8(6)

N(10)-C(10)-C(11)#12	121.4(7)

N(10)-C(11)-C(10)#12	122.8(7)

N(11)-C(12)-C(15)	121.4(7)

N(11)-C(13)-C(14)	122.5(7)

N(12)-C(14)-C(13)	120.5(7)

N(12)-C(15)-C(12)	120.8(7)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,y,-z+1/2    #2 -x+1/2,y+1/2,-z+1/2    #3 x-1/2,y+1/2,z

#4 x,y-1,z    #5 x-1/2,y-1/2,z    #6 x+1/2,y-1/2,z

#7 x+1/2,y+1/2,z    #8 -x+1/2,-y+3/2,-z    #9 -x,-y+2,-z

#10 -x,-y+1,-z    #11 x,y+1,z    #12 -x-1/2,-y+3/2,-z

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu3(CN)3(pyr)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	28(1) 	11(1)	22(1) 	1(1)	20(1) 	2(1)

Cu(2)	32(1) 	17(1)	24(1) 	0	22(1) 	0

Cu(3)	15(1) 	28(1)	18(1) 	-2(1)	6(1) 	-1(1)

Cu(4)	16(1) 	15(1)	20(1) 	2(1)	7(1) 	0(1)

Cu(5)	15(1) 	15(1)	19(1) 	1(1)	6(1) 	0(1)

N(10)	12(4) 	25(3)	20(3) 	5(2)	8(3) 	3(3)

N(11)	20(4) 	22(3)	20(4) 	2(2)	10(3) 	-1(3)

N(12)	14(4) 	18(3)	20(4) 	2(2)	8(3) 	2(2)

N(1)	15(4) 	32(4)	11(3) 	-7(3)	6(3) 	-1(3)

N(2)	15(4) 	27(4)	12(3) 	1(2)	7(3) 	2(3)

N(3)	24(4) 	10(3)	20(4) 	-2(2)	12(3) 	-2(2)

N(4)	12(5) 	44(4)	14(4) 	6(3)	2(3) 	2(3)

N(5)	16(5) 	27(3)	21(4) 	-4(3)	7(3) 	2(3)

N(6)	15(5) 	25(4)	24(4) 	7(3)	7(3) 	4(3)

N(7)	13(4) 	24(4)	22(4) 	0(3)	7(3) 	1(3)

N(8)	11(4) 	22(3)	18(4) 	1(3)	3(3) 	-1(3)

N(9)	12(4) 	17(3)	17(4) 	2(2)	4(3) 	-2(2)

C(1)	15(4) 	32(4)	11(3) 	-7(3)	6(3) 	-1(3)

C(2)	15(4) 	27(4)	12(3) 	1(2)	7(3) 	2(3)

C(3)	24(4) 	10(3)	20(4) 	-2(2)	12(3) 	-2(2)

C(4)	12(5) 	44(4)	14(4) 	6(3)	2(3) 	2(3)

C(5)	16(5) 	27(3)	21(4) 	-4(3)	7(3) 	2(3)

C(6)	15(5) 	25(4)	24(4) 	7(3)	7(3) 	4(3)

C(7)	13(4) 	24(4)	22(4) 	0(3)	7(3) 	1(3)

C(8)	11(4) 	22(3)	18(4) 	1(3)	3(3) 	-1(3)

C(9)	12(4) 	17(3)	17(4) 	2(2)	4(3) 	-2(2)

C(10)	14(4) 	34(4)	19(4) 	3(3)	8(3) 	-1(3)

C(11)	14(4) 	36(4)	19(4) 	0(3)	6(3) 	1(3)

C(12)	22(5) 	15(3)	31(5) 	8(3)	10(4) 	-1(3)

C(13)	23(5) 	24(4)	18(4) 	-9(3)	9(3) 	0(3)

C(14)	20(5) 	15(3)	23(4) 	-8(3)	8(3) 	-1(3)

C(15)	21(5) 	14(3)	25(4) 	8(3)	10(3) 	-1(3)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3) for [Cu3(CN)3(pyr)].

x 	y 	z 	U(eq)

H(10)	-1712	9486	190	26

H(11)	-1828	5516	-144	28

H(12)	5052	6014	1532	26

H(13)	5126	10010	1738	25

H(14)	6604	10026	1812	23

H(15)	6539	5999	1599	23

________________________________________________________________________