Table 1.  Crystal data and structure refinement for [Cu2(CN)2(2,5-dmp)].

Identification code 	[Cu2(CN)2(2,5-dmp)]

Empirical formula 	C8H8Cu2N4

Formula weight 	287.26

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 14.140(3) Å	= 90.

b = 8.8882(17) Å	= 97.584(4).

c = 7.2353(14) Å	 = 90.

Volume	901.4(3) Å3

Z	4

Density (calculated)	2.117 Mg/m3

Absorption coefficient	4.675 mm-1

F(000)	568

Crystal size	0.31 x 0.29 x 0.23 mm3

Theta range for data collection	2.71 to 28.27.

Index ranges	-18<=h<=18, -11<=k<=8, -7<=l<=9

Reflections collected	2866

Independent reflections	1077 [R(int) = 0.0192]

Completeness to theta = 28.27	96.5 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1077 / 0 / 81

Goodness-of-fit on F2	1.110

Final R indices [I>2sigma(I)]	R1 = 0.0236, wR2 = 0.0625

R indices (all data)	R1 = 0.0256, wR2 = 0.0635

Extinction coefficient	0.0009(4)

Largest diff. peak and hole	0.713 and -0.415 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(2,5-dmp)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	2900(1)	8462(1)	1263(1)	8(1)

N(3)	4174(1)	9322(2)	498(2)	7(1)

N(1)	2644(1)	5326(2)	2853(3)	6(1)

N(2)	2750(2)	6472(2)	2160(3)	13(1)

C(1)	2644(1)	5326(2)	2853(3)	6(1)

C(2)	2750(2)	6472(2)	2160(3)	13(1)

C(3)	5711(2)	9177(2)	-473(3)	8(1)

C(4)	4896(2)	8484(2)	7(3)	8(1)

C(5)	4795(2)	6809(3)	-68(3)	11(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(2,5-dmp)].

_____________________________________________________

Cu(1)-N(2) 	1.905(2)

Cu(1)-C(1)#1 	1.9678(19)

Cu(1)-N(1)#1 	1.9678(19)

Cu(1)-N(3) 	2.0975(18)

Cu(1)-C(2)#2 	2.526(2)

Cu(1)-Cu(1)#2 	2.6455(6)

N(3)-C(3)#3 	1.344(3)

N(3)-C(4) 	1.349(3)

N(1)-N(2) 	1.154(3)

N(1)-Cu(1)#4 	1.9678(19)

C(3)-N(3)#3 	1.344(3)

C(3)-C(4) 	1.391(3)

C(4)-C(5) 	1.496(3)

N(2)-Cu(1)-C(1)#1	127.24(8)

N(2)-Cu(1)-N(1)#1	127.24(8)

C(1)#1-Cu(1)-N(1)#1	0.00(13)

N(2)-Cu(1)-N(3)	124.48(8)

C(1)#1-Cu(1)-N(3)	99.48(7)

N(1)#1-Cu(1)-N(3)	99.48(7)

N(2)-Cu(1)-C(2)#2	108.23(7)

C(1)#1-Cu(1)-C(2)#2	101.07(7)

N(1)#1-Cu(1)-C(2)#2	101.07(7)

N(3)-Cu(1)-C(2)#2	86.94(7)

N(2)-Cu(1)-Cu(1)#2	65.07(7)

C(1)#1-Cu(1)-Cu(1)#2	128.25(5)

N(1)#1-Cu(1)-Cu(1)#2	128.25(5)

N(3)-Cu(1)-Cu(1)#2	110.90(5)

C(2)#2-Cu(1)-Cu(1)#2	43.16(5)

C(3)#3-N(3)-C(4)	116.56(19)

C(3)#3-N(3)-Cu(1)	118.39(15)

C(4)-N(3)-Cu(1)	125.04(14)

N(2)-N(1)-Cu(1)#4	164.34(17)

N(1)-N(2)-Cu(1)	173.77(19)

N(3)#3-C(3)-C(4)	123.3(2)

N(3)-C(4)-C(3)	120.13(18)

N(3)-C(4)-C(5)	119.19(19)

C(3)-C(4)-C(5)	120.7(2)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1/2,y+1/2,-z+1/2    #2 -x+1/2,-y+3/2,-z    #3 -x+1,-y+2,-z

#4 -x+1/2,y-1/2,-z+1/2

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(2,5-dmp)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	8(1) 	5(1)	10(1) 	0(1)	2(1) 	-1(1)

N(3)	7(1) 	7(1)	7(1) 	1(1)	0(1) 	-1(1)

N(1)	6(1) 	6(1)	7(1) 	1(1)	1(1) 	1(1)

N(2)	9(1) 	17(1)	14(1) 	-3(1)	2(1) 	0(1)

C(1)	6(1) 	6(1)	7(1) 	1(1)	1(1) 	1(1)

C(2)	9(1) 	17(1)	14(1) 	-3(1)	2(1) 	0(1)

C(3)	8(1) 	7(1)	10(1) 	0(1)	1(1) 	1(1)

C(4)	9(1) 	7(1)	8(1) 	-1(1)	0(1) 	-1(1)

C(5)	10(1) 	7(1)	17(1) 	-1(1)	4(1) 	0(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(2,5-dmp)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(2)	5370(20)	6380(30)	-140(50)	16(8)

H(1)	6160(20)	8610(30)	-700(40)	12(7)

H(3)	4320(30)	6440(40)	-1050(70)	48(13)

H(4)	4510(30)	6460(30)	1010(50)	25(9)

______________________________________________________________________________