Table 1.  Crystal data and structure refinement for [Cu2(CN)2(dpe)].

Identification code 	[Cu2(CN)2(dpe)]

Empirical formula 	C14H10Cu2N4

Formula weight 	361.34

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 6.861(3) Å	= 97.908(11).

b = 9.329(5) Å	= 99.529(11).

c = 11.793(6) Å	 = 109.624(13).

Volume	685.8(6) Å3

Z	2

Density (calculated)	1.750 Mg/m3

Absorption coefficient	3.093 mm-1

F(000)	360

Crystal size	0.19 x 0.04 x 0.02 mm3

Theta range for data collection	1.79 to 28.33.

Index ranges	-9<=h<=7, -12<=k<=10, -15<=l<=14

Reflections collected	4491

Independent reflections	3083 [R(int) = 0.0196]

Completeness to theta = 28.33	89.9 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3083 / 0 / 182

Goodness-of-fit on F2	1.027

Final R indices [I>2sigma(I)]	R1 = 0.0375, wR2 = 0.1027

R indices (all data)	R1 = 0.0419, wR2 = 0.1056

Extinction coefficient	0.010(2)

Largest diff. peak and hole	0.690 and -0.902 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(dpe)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	1554(1)	2741(1)	1010(1)	19(1)

Cu(2)	6126(1)	4200(1)	4945(1)	18(1)

N(5)	2208(4)	4532(3)	165(2)	18(1)

N(6)	5097(4)	12357(3)	-4225(2)	19(1)

N(1)	320(4)	657(3)	215(2)	25(1)

N(2)	2848(4)	3538(3)	2645(2)	16(1)

N(3)	3921(4)	3954(3)	3582(2)	23(1)

N(4)	9105(4)	4798(3)	4988(2)	21(1)

C(1)	320(4)	657(3)	215(2)	25(1)

C(2)	2848(4)	3538(3)	2645(2)	16(1)

C(3)	3921(4)	3954(3)	3582(2)	23(1)

C(4)	9105(4)	4798(3)	4988(2)	21(1)

C(5)	3584(4)	5954(3)	743(2)	19(1)

C(6)	4221(4)	7202(3)	198(2)	19(1)

C(7)	1411(4)	4351(3)	-996(2)	20(1)

C(8)	1931(4)	5545(3)	-1602(2)	20(1)

C(9)	3388(4)	7027(3)	-999(2)	18(1)

C(10)	4073(5)	8329(3)	-1588(3)	20(1)

C(11)	2891(4)	8522(3)	-2532(3)	19(1)

C(12)	3655(4)	9830(3)	-3119(2)	18(1)

C(13)	5788(4)	10482(3)	-3174(3)	21(1)

C(14)	6430(4)	11714(3)	-3728(3)	21(1)

C(15)	2279(4)	10478(3)	-3646(3)	23(1)

C(16)	3050(5)	11729(4)	-4171(3)	23(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(dpe)].

_____________________________________________________

Cu(1)-N(1) 	1.873(3)

Cu(1)-N(2) 	1.912(3)

Cu(1)-N(5) 	2.021(3)

Cu(2)-N(4) 	1.919(3)

Cu(2)-N(3) 	1.946(3)

Cu(2)-N(6)#1 	2.071(3)

Cu(2)-C(3)#2 	2.284(3)

Cu(2)-N(3)#2 	2.284(3)

Cu(2)-Cu(2)#2 	2.4883(11)

N(5)-C(5) 	1.346(4)

N(5)-C(7) 	1.353(4)

N(6)-C(16) 	1.344(4)

N(6)-C(14) 	1.352(4)

N(6)-Cu(2)#3 	2.071(3)

N(1)-C(1)#4 	1.159(6)

N(1)-N(1)#4 	1.159(6)

N(2)-N(3) 	1.155(4)

N(3)-Cu(2)#2 	2.284(3)

N(4)-C(4)#5 	1.152(5)

N(4)-N(4)#5 	1.152(5)

C(5)-C(6) 	1.385(4)

C(6)-C(9) 	1.397(4)

C(7)-C(8) 	1.383(4)

C(8)-C(9) 	1.408(4)

C(9)-C(10) 	1.461(4)

C(10)-C(11) 	1.335(4)

C(11)-C(12) 	1.471(4)

C(12)-C(15) 	1.391(4)

C(12)-C(13) 	1.400(4)

C(13)-C(14) 	1.379(4)

C(15)-C(16) 	1.384(4)

N(1)-Cu(1)-N(2)	127.78(12)

N(1)-Cu(1)-N(5)	122.75(12)

N(2)-Cu(1)-N(5)	108.55(10)

N(4)-Cu(2)-N(3)	125.68(12)

N(4)-Cu(2)-N(6)#1	111.06(10)

N(3)-Cu(2)-N(6)#1	109.30(11)

N(4)-Cu(2)-C(3)#2	102.19(11)

N(3)-Cu(2)-C(3)#2	108.43(10)

N(6)#1-Cu(2)-C(3)#2	95.60(10)

N(4)-Cu(2)-N(3)#2	102.19(11)

N(3)-Cu(2)-N(3)#2	108.43(10)

N(6)#1-Cu(2)-N(3)#2	95.60(10)

C(3)#2-Cu(2)-N(3)#2	0.00(15)

N(4)-Cu(2)-Cu(2)#2	130.53(9)

N(3)-Cu(2)-Cu(2)#2	60.55(9)

N(6)#1-Cu(2)-Cu(2)#2	110.36(7)

C(3)#2-Cu(2)-Cu(2)#2	47.88(7)

N(3)#2-Cu(2)-Cu(2)#2	47.88(7)

C(5)-N(5)-C(7)	117.3(2)

C(5)-N(5)-Cu(1)	120.03(19)

C(7)-N(5)-Cu(1)	122.60(19)

C(16)-N(6)-C(14)	116.8(2)

C(16)-N(6)-Cu(2)#3	121.16(19)

C(14)-N(6)-Cu(2)#3	122.02(19)

C(1)#4-N(1)-N(1)#4	0.0(4)

C(1)#4-N(1)-Cu(1)	174.4(4)

N(1)#4-N(1)-Cu(1)	174.4(4)

N(3)-N(2)-Cu(1)	168.0(2)

N(2)-N(3)-Cu(2)	161.6(2)

N(2)-N(3)-Cu(2)#2	126.8(2)

Cu(2)-N(3)-Cu(2)#2	71.57(10)

C(4)#5-N(4)-N(4)#5	0.0(4)

C(4)#5-N(4)-Cu(2)	177.9(4)

N(4)#5-N(4)-Cu(2)	177.9(4)

N(5)-C(5)-C(6)	123.0(3)

C(5)-C(6)-C(9)	120.0(3)

N(5)-C(7)-C(8)	123.4(3)

C(7)-C(8)-C(9)	119.3(3)

C(6)-C(9)-C(8)	117.0(3)

C(6)-C(9)-C(10)	120.5(3)

C(8)-C(9)-C(10)	122.4(3)

C(11)-C(10)-C(9)	124.7(3)

C(10)-C(11)-C(12)	123.1(3)

C(15)-C(12)-C(13)	116.8(3)

C(15)-C(12)-C(11)	121.2(3)

C(13)-C(12)-C(11)	121.9(3)

C(14)-C(13)-C(12)	119.8(3)

N(6)-C(14)-C(13)	123.3(3)

C(16)-C(15)-C(12)	120.0(3)

N(6)-C(16)-C(15)	123.3(3)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,y-1,z+1    #2 -x+1,-y+1,-z+1    #3 x,y+1,z-1

#4 -x,-y,-z    #5 -x+2,-y+1,-z+1

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(dpe)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	19(1) 	17(1)	18(1) 	2(1)	3(1) 	4(1)

Cu(2)	15(1) 	20(1)	19(1) 	5(1)	4(1) 	6(1)

N(5)	19(1) 	17(1)	18(1) 	3(1)	5(1) 	6(1)

N(6)	17(1) 	19(1)	20(1) 	5(1)	4(1) 	6(1)

N(1)	22(1) 	26(1)	23(1) 	1(1)	2(1) 	6(1)

N(2)	16(1) 	16(1)	16(1) 	2(1)	4(1) 	5(1)

N(3)	19(1) 	25(1)	25(1) 	5(1)	7(1) 	7(1)

N(4)	18(1) 	26(1)	18(1) 	3(1)	3(1) 	10(1)

C(1)	22(1) 	26(1)	23(1) 	1(1)	2(1) 	6(1)

C(2)	16(1) 	16(1)	16(1) 	2(1)	4(1) 	5(1)

C(3)	19(1) 	25(1)	25(1) 	5(1)	7(1) 	7(1)

C(4)	18(1) 	26(1)	18(1) 	3(1)	3(1) 	10(1)

C(5)	20(1) 	20(1)	15(1) 	1(1)	3(1) 	7(1)

C(6)	20(1) 	17(1)	20(1) 	2(1)	3(1) 	6(1)

C(7)	20(1) 	18(1)	19(1) 	-1(1)	1(1) 	5(1)

C(8)	20(1) 	22(1)	17(1) 	4(1)	3(1) 	8(1)

C(9)	17(1) 	19(1)	20(1) 	5(1)	5(1) 	8(1)

C(10)	21(1) 	18(1)	21(1) 	3(1)	7(1) 	7(1)

C(11)	16(1) 	18(1)	23(1) 	4(1)	7(1) 	5(1)

C(12)	19(1) 	18(1)	17(1) 	3(1)	5(1) 	6(1)

C(13)	17(1) 	25(1)	23(1) 	7(1)	5(1) 	11(1)

C(14)	15(1) 	25(1)	24(1) 	5(1)	6(1) 	7(1)

C(15)	13(1) 	27(2)	27(2) 	9(1)	3(1) 	5(1)

C(16)	18(1) 	26(1)	28(2) 	10(1)	5(1) 	10(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(dpe)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(5)	4131	6105	1545	22

H(6)	5203	8158	628	23

H(7)	465	3374	-1409	24

H(8)	1325	5370	-2398	24

H(10)	5428	9077	-1283	24

H(11)	1521	7796	-2833	23

H(13)	6769	10087	-2839	25

H(14)	7852	12124	-3761	25

H(15)	842	10071	-3646	27

H(16)	2105	12156	-4502	28

______________________________________________________________________________