Table 1.  Crystal data and structure refinement for [Cu2(CN)2(tmp)].

Identification code 	[Cu2(CN)2(tmp)]

Empirical formula 	C10H12Cu2N4

Formula weight 	315.32

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

# Space group 	P2(1)/n

Unit cell dimensions	a = 4.7242(11) Å	= 90.

b = 16.731(4) Å	= 94.020(5).

c = 7.4798(17) Å	 = 90.

Volume	589.7(2) Å3

Z	2

Density (calculated)	1.776 Mg/m3

Absorption coefficient	3.582 mm-1

F(000)	316

Crystal size	0.29 x 0.23 x 0.19 mm3

Theta range for data collection	2.43 to 28.25.

Index ranges	-5<=h<=6, -11<=k<=22, -9<=l<=9

Reflections collected	3800

Independent reflections	1406 [R(int) = 0.0341]

Completeness to theta = 28.25	96.0 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1406 / 0 / 74

Goodness-of-fit on F2	1.051

Final R indices [I>2sigma(I)]	R1 = 0.0414, wR2 = 0.0906

R indices (all data)	R1 = 0.0552, wR2 = 0.0962

Extinction coefficient	0.005(2)

Largest diff. peak and hole	0.940 and -0.611 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(tmp)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	1435(1)	1931(1)	3665(1)	14(1)

N(3)	816(6)	731(2)	4330(4)	11(1)

N(1)	3370(8)	2296(2)	1708(5)	22(1)

N(2)	-503(7)	2444(2)	5524(4)	12(1)

C(1)	3370(8)	2296(2)	1708(5)	22(1)

C(2)	-503(7)	2444(2)	5524(4)	12(1)

C(3)	4183(8)	971(2)	6909(5)	16(1)

C(4)	1978(7)	457(2)	5906(4)	12(1)

C(5)	-1119(7)	280(2)	3411(4)	11(1)

C(6)	-2353(8)	587(2)	1629(5)	17(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(tmp)].

_____________________________________________________

Cu(1)-N(1) 	1.881(4)

Cu(1)-N(2) 	1.920(3)

Cu(1)-N(3) 	2.093(3)

N(3)-C(5) 	1.338(4)

N(3)-C(4) 	1.345(4)

N(1)-C(2)#1 	1.151(5)

N(1)-N(2)#1 	1.151(5)

N(2)-C(1)#2 	1.151(5)

N(2)-N(1)#2 	1.151(5)

C(3)-C(4) 	1.509(5)

C(4)-C(5)#3 	1.406(5)

C(5)-C(4)#3 	1.406(5)

C(5)-C(6) 	1.507(5)

N(1)-Cu(1)-N(2)	134.49(14)

N(1)-Cu(1)-N(3)	125.44(13)

N(2)-Cu(1)-N(3)	100.06(12)

C(5)-N(3)-C(4)	118.7(3)

C(5)-N(3)-Cu(1)	121.4(2)

C(4)-N(3)-Cu(1)	118.7(2)

C(2)#1-N(1)-N(2)#1	0.0(3)

C(2)#1-N(1)-Cu(1)	176.6(3)

N(2)#1-N(1)-Cu(1)	176.6(3)

C(1)#2-N(2)-N(1)#2	0.0(3)

C(1)#2-N(2)-Cu(1)	175.3(3)

N(1)#2-N(2)-Cu(1)	175.3(3)

N(3)-C(4)-C(5)#3	120.4(3)

N(3)-C(4)-C(3)	117.8(3)

C(5)#3-C(4)-C(3)	121.7(3)

N(3)-C(5)-C(4)#3	120.8(3)

N(3)-C(5)-C(6)	118.1(3)

C(4)#3-C(5)-C(6)	121.1(3)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x+1/2,-y+1/2,z-1/2    #2 x-1/2,-y+1/2,z+1/2

#3 -x,-y,-z+1

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(tmp)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	20(1) 	9(1)	13(1) 	1(1)	8(1) 	0(1)

N(3)	13(1) 	6(1)	13(1) 	-1(1)	4(1) 	1(1)

N(1)	27(2) 	11(2)	27(2) 	-1(1)	6(2) 	5(1)

N(2)	18(2) 	5(1)	13(2) 	-1(1)	7(1) 	-1(1)

C(1)	27(2) 	11(2)	27(2) 	-1(1)	6(2) 	5(1)

C(2)	18(2) 	5(1)	13(2) 	-1(1)	7(1) 	-1(1)

C(3)	19(2) 	12(2)	18(2) 	-1(1)	1(1) 	-4(1)

C(4)	16(2) 	9(2)	12(2) 	-1(1)	3(1) 	1(1)

C(5)	12(2) 	10(2)	12(2) 	-1(1)	5(1) 	4(1)

C(6)	24(2) 	11(2)	15(2) 	1(1)	-1(1) 	-1(1)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(tmp)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(3A)	4487	1447	6231	25

H(3B)	5930	679	7079	25

H(3C)	3535	1114	8054	25

H(6A)	-1518	1094	1381	25

H(6B)	-4369	648	1667	25

H(6C)	-1960	214	704	25

______________________________________________________________________________