Table 1.  Crystal data and structure refinement for [Cu2(CN)2(qox)].

Identification code 	[Cu2(CN)2(qox)]

Empirical formula 	C20H12Cu4N8

Formula weight 	618.54

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 6.8433(14) Å	= 83.894(5).

b = 9.6049(19) Å	= 81.517(5).

c = 15.589(3) Å	 = 71.436(5).

Volume	958.8(3) Å3

Z	2

Density (calculated)	2.142 Mg/m3

Absorption coefficient	4.404 mm-1

F(000)	608

Crystal size	0.11 x 0.09 x 0.05 mm3

Theta range for data collection	1.32 to 28.27.

Index ranges	-8<=h<=7, -11<=k<=12, -20<=l<=18

Reflections collected	6175

Independent reflections	4247 [R(int) = 0.0345]

Completeness to theta = 28.27	89.3 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4247 / 0 / 290

Goodness-of-fit on F2	0.984

Final R indices [I>2sigma(I)]	R1 = 0.0498, wR2 = 0.1136

R indices (all data)	R1 = 0.0718, wR2 = 0.1236

Extinction coefficient	0.0005(5)

Largest diff. peak and hole	0.968 and -1.062 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(qox)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	-1892(1)	9801(1)	5577(1)	14(1)

Cu(2)	1464(1)	5971(1)	3517(1)	12(1)

Cu(3)	3720(1)	4052(1)	583(1)	13(1)

Cu(4)	9738(1)	-2364(1)	-1483(1)	13(1)

N(9)	-4095(7)	11619(5)	5104(3)	11(1)

N(10)	-6844(6)	14112(5)	4293(3)	9(1)

N(11)	5677(7)	2133(5)	88(3)	10(1)

N(12)	8041(6)	-489(4)	-724(3)	8(1)

N(1)	-1453(8)	8996(5)	6723(3)	16(1)

N(2)	-746(7)	8670(5)	4537(3)	10(1)

N(3)	-1(8)	7717(6)	4088(3)	16(1)

N(4)	2285(7)	5199(5)	2394(3)	8(1)

N(5)	2803(8)	4704(5)	1721(4)	19(1)

N(6)	2609(7)	5141(5)	-476(3)	10(1)

N(7)	8929(7)	-1528(5)	-2600(3)	9(1)

N(8)	11541(8)	-3961(6)	-910(3)	16(1)

C(1)	-1453(8)	8996(5)	6723(3)	16(1)

C(2)	-746(7)	8670(5)	4537(3)	10(1)

C(3)	-1(8)	7717(6)	4088(3)	16(1)

C(4)	2285(7)	5199(5)	2394(3)	8(1)

C(5)	2803(8)	4704(5)	1721(4)	19(1)

C(6)	2609(7)	5141(5)	-476(3)	10(1)

C(7)	8929(7)	-1528(5)	-2600(3)	9(1)

C(8)	11541(8)	-3961(6)	-910(3)	16(1)

C(9)	-4333(8)	11712(6)	4276(3)	11(1)

C(10)	-5678(8)	12931(6)	3870(3)	12(1)

C(11)	-6680(7)	14047(5)	5166(3)	9(1)

C(12)	-7904(8)	15221(5)	5671(3)	11(1)

C(13)	-7730(8)	15146(6)	6546(3)	10(1)

C(14)	-6372(8)	13921(6)	6947(3)	12(1)

C(15)	-5164(8)	12761(6)	6472(3)	11(1)

C(16)	-5300(7)	12805(5)	5575(3)	8(1)

C(17)	5998(8)	2055(6)	-760(3)	9(1)

C(18)	7175(8)	754(6)	-1168(3)	11(1)

C(19)	7803(8)	-445(5)	168(3)	10(1)

C(20)	8722(8)	-1716(5)	687(3)	10(1)

C(21)	8505(8)	-1659(6)	1572(3)	11(1)

C(22)	7383(8)	-337(6)	1979(3)	14(1)

C(23)	6444(8)	896(6)	1489(3)	12(1)

C(24)	6650(8)	880(5)	579(3)	8(1)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(qox)].

_____________________________________________________

Cu(1)-N(1) 	1.896(5)

Cu(1)-N(2) 	1.970(4)

Cu(1)-N(9) 	2.060(4)

Cu(1)-Cu(1)#1 	3.0324(14)

Cu(2)-N(3) 	1.895(5)

Cu(2)-N(4) 	1.911(4)

Cu(2)-N(10)#2 	2.152(4)

Cu(3)-N(5) 	1.895(6)

Cu(3)-N(6) 	1.974(5)

Cu(3)-N(11) 	2.052(4)

Cu(4)-N(8) 	1.872(5)

Cu(4)-N(7) 	1.920(4)

Cu(4)-N(12) 	2.170(4)

N(9)-C(9) 	1.315(6)

N(9)-C(16) 	1.384(6)

N(10)-C(10) 	1.336(7)

N(10)-C(11) 	1.376(6)

N(10)-Cu(2)#3 	2.152(4)

N(11)-C(17) 	1.314(6)

N(11)-C(24) 	1.386(6)

N(12)-C(18) 	1.323(6)

N(12)-C(19) 	1.379(6)

N(1)-C(7)#4 	1.150(7)

N(1)-N(7)#4 	1.150(7)

N(2)-N(3) 	1.150(7)

N(4)-N(5) 	1.159(7)

N(6)-C(8)#3 	1.164(7)

N(6)-N(8)#3 	1.164(7)

N(7)-C(1)#5 	1.150(7)

N(7)-N(1)#5 	1.150(7)

N(8)-C(6)#2 	1.164(7)

N(8)-N(6)#2 	1.164(7)

C(9)-C(10) 	1.395(7)

C(11)-C(12) 	1.409(7)

C(11)-C(16) 	1.421(7)

C(12)-C(13) 	1.378(7)

C(13)-C(14) 	1.399(7)

C(14)-C(15) 	1.372(7)

C(15)-C(16) 	1.410(7)

C(17)-C(18) 	1.411(7)

C(19)-C(20) 	1.412(7)

C(19)-C(24) 	1.427(7)

C(20)-C(21) 	1.370(7)

C(21)-C(22) 	1.419(7)

C(22)-C(23) 	1.367(7)

C(23)-C(24) 	1.406(7)

N(1)-Cu(1)-N(2)	123.4(2)

N(1)-Cu(1)-N(9)	132.10(19)

N(2)-Cu(1)-N(9)	102.33(18)

N(1)-Cu(1)-Cu(1)#1	115.87(16)

N(2)-Cu(1)-Cu(1)#1	59.35(14)

N(9)-Cu(1)-Cu(1)#1	98.29(12)

N(3)-Cu(2)-N(4)	142.6(2)

N(3)-Cu(2)-N(10)#2	117.31(19)

N(4)-Cu(2)-N(10)#2	99.74(17)

N(5)-Cu(3)-N(6)	124.4(2)

N(5)-Cu(3)-N(11)	134.1(2)

N(6)-Cu(3)-N(11)	101.12(18)

N(8)-Cu(4)-N(7)	144.2(2)

N(8)-Cu(4)-N(12)	116.64(19)

N(7)-Cu(4)-N(12)	98.53(17)

C(9)-N(9)-C(16)	116.2(4)

C(9)-N(9)-Cu(1)	118.1(3)

C(16)-N(9)-Cu(1)	125.6(3)

C(10)-N(10)-C(11)	116.0(4)

C(10)-N(10)-Cu(2)#3	116.7(3)

C(11)-N(10)-Cu(2)#3	127.1(3)

C(17)-N(11)-C(24)	116.6(4)

C(17)-N(11)-Cu(3)	118.1(3)

C(24)-N(11)-Cu(3)	125.2(3)

C(18)-N(12)-C(19)	116.6(4)

C(18)-N(12)-Cu(4)	116.3(3)

C(19)-N(12)-Cu(4)	127.2(3)

C(7)#4-N(1)-N(7)#4	0.0(5)

C(7)#4-N(1)-Cu(1)	176.1(5)

N(7)#4-N(1)-Cu(1)	176.1(5)

N(3)-N(2)-Cu(1)	162.5(4)

N(2)-N(3)-Cu(2)	170.0(5)

N(5)-N(4)-Cu(2)	178.7(5)

N(4)-N(5)-Cu(3)	174.7(5)

C(8)#3-N(6)-N(8)#3	0.0(9)

C(8)#3-N(6)-Cu(3)	159.3(4)

N(8)#3-N(6)-Cu(3)	159.3(4)

C(1)#5-N(7)-N(1)#5	0.0(6)

C(1)#5-N(7)-Cu(4)	176.0(4)

N(1)#5-N(7)-Cu(4)	176.0(4)

C(6)#2-N(8)-N(6)#2	0.0(5)

C(6)#2-N(8)-Cu(4)	172.6(4)

N(6)#2-N(8)-Cu(4)	172.6(4)

N(9)-C(9)-C(10)	123.4(5)

N(10)-C(10)-C(9)	122.7(5)

N(10)-C(11)-C(12)	120.0(5)

N(10)-C(11)-C(16)	121.1(4)

C(12)-C(11)-C(16)	119.0(5)

C(13)-C(12)-C(11)	119.6(5)

C(12)-C(13)-C(14)	121.4(5)

C(15)-C(14)-C(13)	120.3(5)

C(14)-C(15)-C(16)	119.7(5)

N(9)-C(16)-C(15)	119.2(5)

N(9)-C(16)-C(11)	120.7(5)

C(15)-C(16)-C(11)	120.1(5)

N(11)-C(17)-C(18)	122.9(5)

N(12)-C(18)-C(17)	122.5(5)

N(12)-C(19)-C(20)	120.1(4)

N(12)-C(19)-C(24)	120.9(5)

C(20)-C(19)-C(24)	119.0(5)

C(21)-C(20)-C(19)	119.8(5)

C(20)-C(21)-C(22)	121.1(5)

C(23)-C(22)-C(21)	119.9(5)

C(22)-C(23)-C(24)	120.4(5)

N(11)-C(24)-C(23)	119.9(4)

N(11)-C(24)-C(19)	120.3(4)

C(23)-C(24)-C(19)	119.7(5)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y+2,-z+1    #2 x+1,y-1,z    #3 x-1,y+1,z

#4 x-1,y+1,z+1    #5 x+1,y-1,z-1

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(qox)].  The anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	18(1) 	9(1)	10(1) 	-2(1)	-5(1) 	3(1)

Cu(2)	12(1) 	10(1)	10(1) 	-3(1)	-2(1) 	3(1)

Cu(3)	15(1) 	10(1)	9(1) 	-4(1)	-2(1) 	3(1)

Cu(4)	13(1) 	10(1)	10(1) 	-1(1)	-4(1) 	3(1)

N(9)	9(2) 	11(2)	11(2) 	-3(2)	-1(2) 	0(2)

N(10)	10(2) 	9(2)	7(2) 	-2(2)	0(2) 	-3(2)

N(11)	9(2) 	9(2)	9(2) 	-2(2)	0(2) 	-1(2)

N(12)	9(2) 	3(2)	9(2) 	-4(2)	-1(2) 	1(2)

N(1)	14(3) 	13(2)	18(3) 	-5(2)	0(2) 	-1(2)

N(2)	13(2) 	4(2)	8(2) 	-4(2)	1(2) 	3(2)

N(3)	11(2) 	18(3)	16(3) 	9(2)	-9(2) 	-3(2)

N(4)	7(2) 	6(2)	8(2) 	-3(2)	-4(2) 	4(2)

N(5)	17(3) 	9(2)	26(3) 	4(2)	-5(2) 	-1(2)

N(6)	11(2) 	9(2)	7(2) 	-2(2)	-2(2) 	4(2)

N(7)	14(2) 	7(2)	3(2) 	0(2)	-3(2) 	1(2)

N(8)	18(3) 	17(3)	12(2) 	-5(2)	4(2) 	-5(2)

C(1)	14(3) 	13(2)	18(3) 	-5(2)	0(2) 	-1(2)

C(2)	13(2) 	4(2)	8(2) 	-4(2)	1(2) 	3(2)

C(3)	11(2) 	18(3)	16(3) 	9(2)	-9(2) 	-3(2)

C(4)	7(2) 	6(2)	8(2) 	-3(2)	-4(2) 	4(2)

C(5)	17(3) 	9(2)	26(3) 	4(2)	-5(2) 	-1(2)

C(6)	11(2) 	9(2)	7(2) 	-2(2)	-2(2) 	4(2)

C(7)	14(2) 	7(2)	3(2) 	0(2)	-3(2) 	1(2)

C(8)	18(3) 	17(3)	12(2) 	-5(2)	4(2) 	-5(2)

C(9)	13(3) 	10(2)	10(3) 	-2(2)	-1(2) 	-2(2)

C(10)	14(3) 	12(3)	10(3) 	3(2)	-5(2) 	-2(2)

C(11)	7(2) 	9(2)	8(2) 	-1(2)	0(2) 	-1(2)

C(12)	7(2) 	5(2)	16(3) 	2(2)	-2(2) 	2(2)

C(13)	9(2) 	11(2)	9(2) 	-7(2)	2(2) 	-1(2)

C(14)	13(3) 	16(3)	6(2) 	-3(2)	3(2) 	-5(2)

C(15)	8(2) 	7(2)	15(3) 	-3(2)	-2(2) 	2(2)

C(16)	4(2) 	8(2)	10(2) 	1(2)	-2(2) 	-1(2)

C(17)	9(2) 	8(2)	10(2) 	-3(2)	-2(2) 	-1(2)

C(18)	14(3) 	12(3)	5(2) 	0(2)	1(2) 	-4(2)

C(19)	8(2) 	8(2)	12(2) 	-1(2)	-2(2) 	0(2)

C(20)	11(3) 	5(2)	11(2) 	3(2)	-3(2) 	-1(2)

C(21)	8(2) 	9(2)	15(3) 	2(2)	-4(2) 	0(2)

C(22)	15(3) 	21(3)	7(2) 	-4(2)	2(2) 	-6(2)

C(23)	14(3) 	16(3)	4(2) 	-3(2)	1(2) 	-5(2)

C(24)	9(2) 	8(2)	6(2) 	-1(2)	4(2) 	-1(2)

______________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(qox)].

______________________________________________________________________________

x 	y 	z 	U(eq)

______________________________________________________________________________

H(9)	-3565	10926	3944	13

H(10)	-5766	12921	3281	15

H(12)	-8822	16041	5416	13

H(13)	-8532	15926	6876	12

H(14)	-6287	13893	7539	14

H(15)	-4260	11950	6740	13

H(17)	5424	2894	-1107	11

H(18)	7350	771	-1771	13

H(20)	9472	-2590	430	12

H(21)	9104	-2502	1911	13

H(22)	7287	-309	2579	17

H(23)	5664	1752	1758	14

______________________________________________________________________________