Table 1.  Crystal data and structure refinement for [Cu2(CN)2(mpyr)].

Identification code 	[Cu2(CN)2(mpyr)]

Empirical formula 	C7H8Cu2N4

Formula weight 	275.25

Temperature 	115(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 14.1228(14) Å	= 90.

b = 8.7264(9) Å	= 98.125(2).

c = 7.2508(7) Å	 = 90.

Volume	884.63(15) Å3

Z	4

Density (calculated)	2.067 Mg/m3

Absorption coefficient	4.759 mm-1

F(000)	544

Crystal size	0.25 x 0.19 x 0.05 mm3

Theta range for data collection	2.75 to 28.28.

Index ranges	-16<=h<=18, -10<=k<=11, -9<=l<=9

Reflections collected	2867

Independent reflections	1063 [R(int) = 0.0351]

Completeness to theta = 28.28	96.7 %

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	1063 / 0 / 64

Goodness-of-fit on F2	1.067

Final R indices [I>2sigma(I)]	R1 = 0.0356, wR2 = 0.0898

R indices (all data)	R1 = 0.0505, wR2 = 0.0940

Largest diff. peak and hole	0.707 and -0.592 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for [Cu2(CN)2(mpyr)].  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

______________________________________________________________________________

x	y	z	U(eq)

______________________________________________________________________________

Cu(1)	2882(1)	1505(1)	1182(1)	13(1)

N(3)	4164(2)	651(4)	489(4)	15(1)

N(1)	2332(2)	-349(4)	2095(4)	12(1)

N(2)	2227(3)	-1471(4)	2854(5)	21(1)

C(1)	2332(2)	-349(4)	2095(4)	12(1)

C(2)	2227(3)	-1471(4)	2854(5)	21(1)

C(3)	4889(3)	1530(4)	66(5)	17(1)

C(4)	5714(3)	876(5)	-419(5)	16(1)

C(5)	4815(6)	3241(8)	4(11)	18(2)

______________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [] for  [Cu2(CN)2(mpyr)].

_____________________________________________________

Cu(1)-C(2)#1 	1.914(4)

Cu(1)-N(2)#1 	1.914(4)

Cu(1)-N(1) 	1.950(3)

Cu(1)-N(3) 	2.083(3)

Cu(1)-C(2)#2 	2.459(4)

Cu(1)-N(2)#2 	2.459(4)

Cu(1)-Cu(1)#3 	2.5682(8)

N(3)-C(4)#4 	1.345(5)

N(3)-C(3) 	1.349(5)

N(1)-N(2) 	1.143(5)

N(2)-Cu(1)#5 	1.914(4)

N(2)-Cu(1)#6 	2.459(4)

C(3)-C(4) 	1.387(5)

C(3)-C(5) 	1.496(7)

C(4)-N(3)#4 	1.345(5)

C(2)#1-Cu(1)-N(2)#1	0.0(3)

C(2)#1-Cu(1)-N(1)	125.80(14)

N(2)#1-Cu(1)-N(1)	125.80(14)

C(2)#1-Cu(1)-N(3)	122.39(14)

N(2)#1-Cu(1)-N(3)	122.39(14)

N(1)-Cu(1)-N(3)	100.75(13)

C(2)#1-Cu(1)-C(2)#2	109.31(12)

N(2)#1-Cu(1)-C(2)#2	109.31(12)

N(1)-Cu(1)-C(2)#2	102.17(12)

N(3)-Cu(1)-C(2)#2	88.76(11)

C(2)#1-Cu(1)-N(2)#2	109.31(12)

N(2)#1-Cu(1)-N(2)#2	109.31(12)

N(1)-Cu(1)-N(2)#2	102.17(12)

N(3)-Cu(1)-N(2)#2	88.76(11)

C(2)#2-Cu(1)-N(2)#2	0.00(19)

C(2)#1-Cu(1)-Cu(1)#3	64.62(11)

N(2)#1-Cu(1)-Cu(1)#3	64.62(11)

N(1)-Cu(1)-Cu(1)#3	129.62(9)

N(3)-Cu(1)-Cu(1)#3	112.24(8)

C(2)#2-Cu(1)-Cu(1)#3	44.69(9)

N(2)#2-Cu(1)-Cu(1)#3	44.69(9)

C(4)#4-N(3)-C(3)	116.7(3)

C(4)#4-N(3)-Cu(1)	119.0(3)

C(3)-N(3)-Cu(1)	124.4(3)

N(2)-N(1)-Cu(1)	163.5(3)

N(1)-N(2)-Cu(1)#5	171.5(3)

N(1)-N(2)-Cu(1)#6	115.2(3)

Cu(1)#5-N(2)-Cu(1)#6	70.69(12)

N(3)-C(3)-C(4)	121.0(4)

N(3)-C(3)-C(5)	121.5(4)

C(4)-C(3)-C(5)	117.4(4)

N(3)#4-C(4)-C(3)	122.3(4)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1/2,y+1/2,-z+1/2    #2 x,-y,z-1/2    #3 -x+1/2,-y+1/2,-z

#4 -x+1,-y,-z    #5 -x+1/2,y-1/2,-z+1/2    #6 x,-y,z+1/2

Table 4.   Anisotropic displacement parameters  (Å2x 103) for [Cu2(CN)2(mpyr.)].  Anisotropic displacement factor exponent takes the form:  -2p2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Cu(1)	17(1) 	10(1)	13(1) 	1(1)	3(1) 	2(1)

N(3)	18(2) 	15(2)	9(1) 	-2(1)	-3(1) 	4(1)

N(1)	15(2) 	9(2)	10(2) 	3(1)	-1(1) 	-3(1)

N(2)	16(2) 	26(2)	20(2) 	-7(2)	1(1) 	0(2)

C(1)	15(2) 	9(2)	10(2) 	3(1)	-1(1) 	-3(1)

C(2)	16(2) 	26(2)	20(2) 	-7(2)	1(1) 	0(2)

C(3)	17(2) 	18(2)	14(2) 	-3(1)	-1(1) 	3(2)

C(4)	16(2) 	19(2)	13(2) 	-1(1)	-1(1) 	2(2)

C(5)	14(4) 	21(4)	20(4) 	-2(3)	6(3) 	-4(3)

______________________________________________________________________________

Table 5  Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3)

for [Cu2(CN)2(mpyr)].

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(4A)	6199	1515	-706	19

H(5A)	4348	3542	-1024	27

H(5B)	5425	3670	-148	27

H(5C)	4625	3607	1145	27

________________________________________________________________________