Table 1.  Crystal data and structure refinement for Cu3(CN)3(2,2'-bpy).

Identification code 	[Cu3(CN)3(2,2'-bpy)]

Empirical formula 	C13H8Cu3N5O0.10

Formula weight 	426.46

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/n

Unit cell dimensions	a = 10.128(2) Å	= 90°.

b = 13.659(3) Å	= 109.663(5)°.

c = 11.012(2) Å	 = 90°.

Volume	1434.6(5) Å3

Z	4

Density (calculated)	1.975 Mg/m3

Absorption coefficient	4.404 mm-1

F(000)	835

Crystal size	0.40 x 0.19 x 0.19 mm3

Theta range for data collection	2.37 to 28.28°.

Index ranges	-13<=h<=6, -18<=k<=18, -12<=l<=14

Reflections collected	9304

Independent reflections	3430 [R(int) = 0.0323]

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3430 / 0 / 226

Goodness-of-fit on F2	1.048

Final R indices [I>2sigma(I)]	R1 = 0.0271, wR2 = 0.0694

R indices (all data)	R1 = 0.0319, wR2 = 0.0712

Largest diff. peak and hole	0.544 and -1.012 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for Cu3(CN)3(2,2'-bpy).  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________

Cu(1)	2703(1)	-2349(1)	4998(1)	18(1)

Cu(2)	5269(1)	-789(1)	2418(1)	15(1)

Cu(3)	4768(1)	2759(1)	2890(1)	17(1)

C(1)	1256(2)	-3478(1)	6522(2)	19(1)

C(2)	1790(2)	-3027(1)	5934(2)	17(1)

C(3)	3595(2)	-1739(2)	3990(2)	19(1)

C(4)	4221(2)	-1380(1)	3399(2)	16(1)

C(5)	5283(2)	634(1)	2498(2)	14(1)

C(6)	5113(2)	1462(2)	2594(2)	21(1)

C(7)	3091(3)	2781(2)	4752(2)	17(1)

C(8)	2267(2)	3207(2)	5382(2)	20(1)

C(9)	2055(2)	4215(2)	5276(2)	20(1)

C(10)	2671(2)	4752(2)	4552(2)	18(1)

C(11)	3479(2)	4272(1)	3930(2)	14(1)

C(12)	4151(2)	4777(1)	3100(2)	14(1)

C(13)	4070(2)	5789(2)	2891(2)	20(1)

C(14)	4779(3)	6209(2)	2142(2)	22(1)

C(15)	5550(3)	5610(2)	1606(2)	22(1)

C(16)	5565(3)	4609(2)	1830(2)	19(1)

N(1)	1256(2)	-3478(1)	6522(2)	19(1)

N(2)	1790(2)	-3027(1)	5934(2)	17(1)

N(3)	3595(2)	-1739(2)	3990(2)	19(1)

N(4)	4221(2)	-1380(1)	3399(2)	16(1)

N(5)	5283(2)	634(1)	2498(2)	14(1)

N(6)	5113(2)	1462(2)	2594(2)	21(1)

N(7)	3694(2)	3292(1)	4040(2)	15(1)

N(8)	4882(2)	4195(1)	2554(2)	15(1)

O(1)	7227(17)	-199(11)	4960(15)	19(3)

________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for Cu3(CN)3(2,2'-bpy).

_____________________________________________________

Cu(1)-N(3) 	1.848(2)

Cu(1)-C(3) 	1.848(2)

Cu(1)-C(2) 	1.848(2)

Cu(1)-N(2) 	1.848(2)

Cu(1)-Cu(3)#1 	2.8763(6)

Cu(2)-N(1)#2 	1.907(2)

Cu(2)-C(1)#2 	1.907(2)

Cu(2)-C(4) 	1.928(2)

Cu(2)-N(4) 	1.928(2)

Cu(2)-N(5) 	1.946(2)

Cu(2)-C(5) 	1.946(2)

Cu(3)-N(6) 	1.855(2)

Cu(3)-C(6) 	1.855(2)

Cu(3)-N(8) 	2.007(2)

Cu(3)-N(7) 	2.060(2)

Cu(3)-Cu(1)#1 	2.8763(6)

C(1)-N(2) 	1.152(3)

C(1)-C(2) 	1.152(3)

C(1)-Cu(2)#3 	1.907(2)

C(2)-N(1) 	1.152(3)

C(3)-N(4) 	1.159(3)

C(3)-C(4) 	1.159(3)

C(4)-N(3) 	1.159(3)

C(5)-N(6) 	1.154(3)

C(5)-C(6) 	1.154(3)

C(6)-N(5) 	1.154(3)

C(7)-N(7) 	1.340(3)

C(7)-C(8) 	1.381(3)

C(8)-C(9) 	1.392(3)

C(9)-C(10) 	1.378(3)

C(10)-C(11) 	1.395(3)

C(11)-N(7) 	1.355(2)

C(11)-C(12) 	1.480(3)

C(12)-N(8) 	1.357(3)

C(12)-C(13) 	1.399(3)

C(13)-C(14) 	1.387(3)

C(14)-C(15) 	1.392(3)

C(15)-C(16) 	1.389(3)

C(16)-N(8) 	1.344(3)

N(1)-N(2) 	1.152(3)

N(1)-Cu(2)#3 	1.907(2)

N(3)-N(4) 	1.159(3)

N(5)-N(6) 	1.154(3)

N(3)-Cu(1)-C(3)	0.0(2)

N(3)-Cu(1)-C(2)	176.30(9)

C(3)-Cu(1)-C(2)	176.30(9)

N(3)-Cu(1)-N(2)	176.30(9)

C(3)-Cu(1)-N(2)	176.30(9)

C(2)-Cu(1)-N(2)	0.0(2)

N(3)-Cu(1)-Cu(3)#1	95.23(7)

C(3)-Cu(1)-Cu(3)#1	95.23(7)

C(2)-Cu(1)-Cu(3)#1	85.88(7)

N(2)-Cu(1)-Cu(3)#1	85.88(7)

N(1)#2-Cu(2)-C(1)#2	0.0(2)

N(1)#2-Cu(2)-C(4)	123.60(8)

C(1)#2-Cu(2)-C(4)	123.60(8)

N(1)#2-Cu(2)-N(4)	123.60(8)

C(1)#2-Cu(2)-N(4)	123.60(8)

C(4)-Cu(2)-N(4)	0.0(2)

N(1)#2-Cu(2)-N(5)	123.42(8)

C(1)#2-Cu(2)-N(5)	123.42(8)

C(4)-Cu(2)-N(5)	112.93(8)

N(4)-Cu(2)-N(5)	112.93(8)

N(1)#2-Cu(2)-C(5)	123.42(8)

C(1)#2-Cu(2)-C(5)	123.42(8)

C(4)-Cu(2)-C(5)	112.93(8)

N(4)-Cu(2)-C(5)	112.93(8)

N(5)-Cu(2)-C(5)	0.0(2)

N(6)-Cu(3)-C(6)	0.0(2)

N(6)-Cu(3)-N(8)	151.02(9)

C(6)-Cu(3)-N(8)	151.02(9)

N(6)-Cu(3)-N(7)	127.98(8)

C(6)-Cu(3)-N(7)	127.98(8)

N(8)-Cu(3)-N(7)	80.95(7)

N(6)-Cu(3)-Cu(1)#1	77.71(7)

C(6)-Cu(3)-Cu(1)#1	77.71(7)

N(8)-Cu(3)-Cu(1)#1	104.38(5)

N(7)-Cu(3)-Cu(1)#1	94.71(5)

N(2)-C(1)-C(2)	0.0(3)

N(2)-C(1)-Cu(2)#3	176.6(2)

C(2)-C(1)-Cu(2)#3	176.6(2)

N(1)-C(2)-C(1)	0.0(3)

N(1)-C(2)-Cu(1)	177.4(2)

C(1)-C(2)-Cu(1)	177.4(2)

N(4)-C(3)-C(4)	0.0(3)

N(4)-C(3)-Cu(1)	176.3(2)

C(4)-C(3)-Cu(1)	176.3(2)

N(3)-C(4)-C(3)	0.0(3)

N(3)-C(4)-Cu(2)	179.7(2)

C(3)-C(4)-Cu(2)	179.7(2)

N(6)-C(5)-C(6)	0.0(4)

N(6)-C(5)-Cu(2)	169.8(2)

C(6)-C(5)-Cu(2)	169.8(2)

N(5)-C(6)-C(5)	0.0(3)

N(5)-C(6)-Cu(3)	173.8(2)

C(5)-C(6)-Cu(3)	173.8(2)

N(7)-C(7)-C(8)	123.1(2)

C(7)-C(8)-C(9)	118.5(2)

C(10)-C(9)-C(8)	119.2(2)

C(9)-C(10)-C(11)	119.3(2)

N(7)-C(11)-C(10)	121.5(2)

N(7)-C(11)-C(12)	115.0(2)

C(10)-C(11)-C(12)	123.5(2)

N(8)-C(12)-C(13)	121.1(2)

N(8)-C(12)-C(11)	115.7(2)

C(13)-C(12)-C(11)	123.3(2)

C(14)-C(13)-C(12)	119.6(2)

C(13)-C(14)-C(15)	119.1(2)

C(16)-C(15)-C(14)	118.5(2)

N(8)-C(16)-C(15)	122.9(2)

N(2)-N(1)-C(2)	0.0(3)

N(2)-N(1)-Cu(2)#3	176.6(2)

C(2)-N(1)-Cu(2)#3	176.6(2)

N(1)-N(2)-C(1)	0.0(3)

N(1)-N(2)-Cu(1)	177.4(2)

C(1)-N(2)-Cu(1)	177.4(2)

N(4)-N(3)-C(4)	0.0(3)

N(4)-N(3)-Cu(1)	176.3(2)

C(4)-N(3)-Cu(1)	176.3(2)

N(3)-N(4)-C(3)	0.0(3)

N(3)-N(4)-Cu(2)	179.7(2)

C(3)-N(4)-Cu(2)	179.7(2)

N(6)-N(5)-C(6)	0.0(4)

N(6)-N(5)-Cu(2)	169.8(2)

C(6)-N(5)-Cu(2)	169.8(2)

N(5)-N(6)-C(5)	0.0(3)

N(5)-N(6)-Cu(3)	173.8(2)

C(5)-N(6)-Cu(3)	173.8(2)

C(7)-N(7)-C(11)	118.4(2)

C(7)-N(7)-Cu(3)	127.87(14)

C(11)-N(7)-Cu(3)	113.34(14)

C(16)-N(8)-C(12)	118.9(2)

C(16)-N(8)-Cu(3)	126.43(15)

C(12)-N(8)-Cu(3)	114.64(14)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y,-z+1    #2 x+1/2,-y-1/2,z-1/2    #3 x-1/2,-y-1/2,z+1/2

Table 4.   Anisotropic displacement parameters  (Å2x 103) for Cu3(CN)3(2,2'-bpy).  The anisotropic displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

________________________________________________________________________

U11	U22 	U33	U23	U13	U12

________________________________________________________________________

Cu(1)	23(1) 	15(1)	23(1) 	4(1)	16(1) 	2(1)

Cu(2)	21(1) 	9(1)	19(1) 	1(1)	10(1) 	1(1)

Cu(3)	23(1) 	9(1)	19(1) 	-4(1)	7(1) 	2(1)

C(1)	23(1) 	13(1)	23(1) 	-3(1)	12(1) 	0(1)

C(2)	19(1) 	15(1)	20(1) 	0(1)	11(1) 	0(1)

C(3)	20(1) 	19(1)	18(1) 	3(1)	7(1) 	3(1)

C(4)	18(1) 	14(1)	15(1) 	2(1)	6(1) 	3(1)

C(5)	21(1) 	8(1)	14(1) 	-2(1)	9(1) 	0(1)

C(6)	24(1) 	22(1)	19(1) 	-4(1)	9(1) 	-1(1)

C(7)	20(1) 	14(1)	18(1) 	2(1)	5(1) 	2(1)

C(8)	19(1) 	24(1)	16(1) 	-1(1)	4(1) 	0(1)

C(9)	17(1) 	24(1)	19(1) 	-6(1)	6(1) 	3(1)

C(10)	19(1) 	15(1)	17(1) 	-4(1)	3(1) 	4(1)

C(11)	15(1) 	11(1)	12(1) 	-2(1)	1(1) 	1(1)

C(12)	16(1) 	11(1)	14(1) 	-2(1)	1(1) 	2(1)

C(13)	23(1) 	13(1)	20(1) 	-3(1)	3(1) 	2(1)

C(14)	27(1) 	13(1)	21(1) 	2(1)	3(1) 	0(1)

C(15)	27(1) 	19(1)	19(1) 	2(1)	5(1) 	-3(1)

C(16)	23(1) 	18(1)	17(1) 	-1(1)	8(1) 	0(1)

N(1)	23(1) 	13(1)	23(1) 	-3(1)	12(1) 	0(1)

N(2)	19(1) 	15(1)	20(1) 	0(1)	11(1) 	0(1)

N(3)	20(1) 	19(1)	18(1) 	3(1)	7(1) 	3(1)

N(4)	18(1) 	14(1)	15(1) 	2(1)	6(1) 	3(1)

N(5)	21(1) 	8(1)	14(1) 	-2(1)	9(1) 	0(1)

N(6)	24(1) 	22(1)	19(1) 	-4(1)	9(1) 	-1(1)

N(7)	18(1) 	11(1)	14(1) 	-2(1)	4(1) 	3(1)

N(8)	20(1) 	11(1)	14(1) 	-2(1)	5(1) 	0(1)

________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3) for Cu3(CN)3(2,2'-bpy).

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(7)	3271(34)	2183(24)	4752(31)	36(9)

H(8)	1827(27)	2753(18)	5908(25)	13(6)

H(9)	1572(31)	4450(22)	5627(26)	22(7)

H(10)	2477(28)	5414(21)	4464(24)	21(7)

H(13)	3500(33)	6256(24)	3350(29)	42(9)

H(14)	4823(29)	6855(23)	2049(26)	25(7)

H(15)	6107(27)	5852(19)	1044(25)	18(6)

H(16)	6027(28)	4216(19)	1463(24)	16(6)

________________________________________________________________________