Table 1.  Crystal data and structure refinement for Cu3(CN)3(1,10-phen).

Identification code 	[Cu3(CN)3(1,10-phen)]

Empirical formula 	C15H8Cu3N5

Formula weight 	448.88

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/c

Unit cell dimensions	a = 9.6979(2) Å	= 90°.

b = 23.5984(4) Å	= 99.2630(10)°.

c = 6.89890(10) Å	 = 90°.

Volume	1558.26(5) Å3

Z	4

Density (calculated)	1.913 Mg/m3

Absorption coefficient	4.060 mm-1

F(000)	880

Crystal size	0.29 x 0.23 x 0.18 mm3

Theta range for data collection	1.73 to 25.00°.

Index ranges	-11<=h<=11, -27<=k<=28, -8<=l<=7

Reflections collected	7963

Independent reflections	2715 [R(int) = 0.0856]

Completeness to theta = 25.00°	98.9 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2715 / 0 / 208

Goodness-of-fit on F2	1.109

Final R indices [I>2sigma(I)]	R1 = 0.0507, wR2 = 0.1089

R indices (all data)	R1 = 0.0710, wR2 = 0.1182

Largest diff. peak and hole	0.658 and -0.605 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for Cu3(CN)3(1,10-phen).  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________

Cu(1)	4897(1)	2939(1)	6407(1)	39(1)

Cu(2)	1718(1)	4437(1)	3483(1)	30(1)

Cu(3)	3444(1)	4636(1)	-2826(1)	38(1)

N(7)	6974(5)	3219(2)	7156(7)	31(1)

N(8)	5788(5)	2173(2)	6731(6)	29(1)

C(7)	7533(7)	3732(3)	7335(9)	38(2)

C(8)	8978(7)	3828(3)	7798(9)	41(2)

C(9)	9880(6)	3375(3)	8041(8)	38(2)

C(10)	9322(6)	2821(3)	7872(8)	32(1)

C(11)	7859(6)	2763(2)	7393(8)	28(1)

C(12)	10155(6)	2309(3)	8123(9)	37(1)

C(13)	9572(6)	1788(3)	7926(9)	38(2)

C(14)	8069(5)	1717(2)	7445(8)	28(1)

C(15)	7222(5)	2204(2)	7195(8)	26(1)

C(16)	7402(6)	1184(3)	7235(9)	35(1)

C(17)	5961(7)	1155(3)	6763(9)	40(2)

C(18)	5193(6)	1660(3)	6520(8)	35(1)

C(1)	3399(6)	3432(3)	5583(8)	41(1)

C(2)	2629(5)	3785(2)	4988(7)	24(1)

C(3)	2230(5)	4493(2)	917(8)	34(1)

C(4)	2649(5)	4540(2)	-556(8)	34(1)

C(5)	4621(6)	4912(2)	-4492(7)	35(1)

C(6)	420(5)	4871(2)	4666(7)	30(1)

N(1)	3399(6)	3432(3)	5583(8)	41(1)

N(2)	2629(5)	3785(2)	4988(7)	24(1)

N(3)	2230(5)	4493(2)	917(8)	34(1)

N(4)	2649(5)	4540(2)	-556(8)	34(1)

N(5)	4621(6)	4912(2)	-4492(7)	35(1)

N(6)	420(5)	4871(2)	4666(7)	30(1)

________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for Cu3(CN)3(1,10-phen).

_____________________________________________________

Cu(1)-C(1) 	1.876(7)

Cu(1)-N(8) 	2.000(5)

Cu(1)-N(7) 	2.103(5)

Cu(2)-C(6) 	1.905(5)

Cu(2)-C(3) 	1.918(6)

Cu(2)-C(2) 	1.983(5)

Cu(2)-Cu(3)#1 	2.8522(10)

Cu(3)-C(5) 	1.862(5)

Cu(3)-C(4) 	1.868(5)

Cu(3)-Cu(2)#2 	2.8522(10)

N(7)-C(7) 	1.323(8)

N(7)-C(11) 	1.371(7)

N(8)-C(18) 	1.340(8)

N(8)-C(15) 	1.378(7)

C(7)-C(8) 	1.404(9)

C(8)-C(9) 	1.375(9)

C(9)-C(10) 	1.412(9)

C(10)-C(11) 	1.411(8)

C(10)-C(12) 	1.448(9)

C(11)-C(15) 	1.452(8)

C(12)-C(13) 	1.351(9)

C(13)-C(14) 	1.452(8)

C(14)-C(15) 	1.408(8)

C(14)-C(16) 	1.410(8)

C(16)-C(17) 	1.384(8)

C(17)-C(18) 	1.399(9)

C(1)-C(2) 	1.150(7)

C(3)-C(4) 	1.159(7)

C(5)-N(5)#3 	1.171(10)

C(5)-C(5)#3 	1.171(10)

C(6)-N(6)#4 	1.170(10)

C(6)-C(6)#4 	1.170(10)

C(1)-Cu(1)-N(8)	153.3(2)

C(1)-Cu(1)-N(7)	123.0(2)

N(8)-Cu(1)-N(7)	82.95(18)

C(6)-Cu(2)-C(3)	130.2(2)

C(6)-Cu(2)-C(2)	117.5(2)

C(3)-Cu(2)-C(2)	112.2(2)

C(6)-Cu(2)-Cu(3)#1	82.08(16)

C(3)-Cu(2)-Cu(3)#1	127.65(16)

C(2)-Cu(2)-Cu(3)#1	60.81(14)

C(5)-Cu(3)-C(4)	159.5(2)

C(5)-Cu(3)-Cu(2)#2	80.58(16)

C(4)-Cu(3)-Cu(2)#2	117.80(16)

C(7)-N(7)-C(11)	117.9(5)

C(7)-N(7)-Cu(1)	132.2(4)

C(11)-N(7)-Cu(1)	109.8(4)

C(18)-N(8)-C(15)	118.3(5)

C(18)-N(8)-Cu(1)	129.4(4)

C(15)-N(8)-Cu(1)	112.3(4)

N(7)-C(7)-C(8)	123.1(6)

C(9)-C(8)-C(7)	119.7(6)

C(8)-C(9)-C(10)	118.8(6)

C(11)-C(10)-C(9)	117.9(5)

C(11)-C(10)-C(12)	117.9(5)

C(9)-C(10)-C(12)	124.2(5)

N(7)-C(11)-C(10)	122.6(5)

N(7)-C(11)-C(15)	116.9(5)

C(10)-C(11)-C(15)	120.5(5)

C(13)-C(12)-C(10)	122.0(5)

C(12)-C(13)-C(14)	121.2(5)

C(15)-C(14)-C(16)	117.8(5)

C(15)-C(14)-C(13)	118.5(5)

C(16)-C(14)-C(13)	123.7(5)

N(8)-C(15)-C(14)	122.1(5)

N(8)-C(15)-C(11)	117.9(5)

C(14)-C(15)-C(11)	119.9(5)

C(17)-C(16)-C(14)	119.8(5)

C(16)-C(17)-C(18)	118.9(6)

N(8)-C(18)-C(17)	123.0(5)

C(2)-C(1)-Cu(1)	169.8(5)

C(1)-C(2)-Cu(2)	163.4(4)

C(4)-C(3)-Cu(2)	174.3(5)

C(3)-C(4)-Cu(3)	175.8(5)

N(5)#3-C(5)-C(5)#3	0.0(6)

N(5)#3-C(5)-Cu(3)	178.7(7)

C(5)#3-C(5)-Cu(3)	178.7(7)

N(6)#4-C(6)-C(6)#4	0.0(5)

N(6)#4-C(6)-Cu(2)	177.2(7)

C(6)#4-C(6)-Cu(2)	177.2(7)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,y,z+1    #2 x,y,z-1    #3 -x+1,-y+1,-z-1    #4 -x,-y+1,-z+1

Table 4.   Anisotropic displacement parameters  (Å2x 103) for Cu3(CN)3(1,10-phen).  The anisotropic displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

________________________________________________________________________

U11	U22 	U33	U23	U13	U12

________________________________________________________________________

Cu(1)	32(1) 	47(1)	39(1) 	8(1)	5(1) 	16(1)

Cu(2)	27(1) 	29(1)	33(1) 	-1(1)	5(1) 	2(1)

Cu(3)	46(1) 	39(1)	31(1) 	-1(1)	12(1) 	-6(1)

N(7)	34(3) 	28(3)	29(3) 	7(2)	3(2) 	7(2)

N(8)	29(2) 	28(3)	28(3) 	2(2)	1(2) 	1(2)

C(7)	51(4) 	30(4)	32(3) 	8(3)	4(3) 	8(3)

C(8)	49(4) 	36(4)	39(4) 	4(3)	13(3) 	-7(3)

C(9)	38(3) 	45(4)	30(3) 	4(3)	4(3) 	-8(3)

C(10)	29(3) 	36(4)	29(3) 	5(2)	1(2) 	2(3)

C(11)	32(3) 	28(3)	22(3) 	4(2)	2(2) 	3(2)

C(12)	25(3) 	46(4)	38(3) 	1(3)	-2(2) 	5(3)

C(13)	33(3) 	38(4)	38(3) 	1(3)	-3(3) 	13(3)

C(14)	28(3) 	31(3)	23(3) 	5(2)	0(2) 	6(2)

C(15)	23(3) 	29(3)	26(3) 	4(2)	3(2) 	5(2)

C(16)	43(3) 	24(3)	37(3) 	5(2)	-1(3) 	7(3)

C(17)	52(4) 	34(4)	33(3) 	6(3)	2(3) 	-11(3)

C(18)	34(3) 	38(4)	32(3) 	8(3)	1(3) 	-5(3)

C(1)	36(3) 	48(4)	40(3) 	-12(3)	11(3) 	-17(3)

C(2)	20(2) 	19(3)	32(3) 	5(2)	1(2) 	7(2)

C(3)	33(3) 	37(3)	32(3) 	1(2)	6(2) 	4(2)

C(4)	31(3) 	34(3)	35(3) 	-2(2)	5(2) 	-2(2)

C(5)	41(3) 	34(3)	29(3) 	-5(2)	5(2) 	-11(3)

C(6)	41(3) 	26(3)	24(3) 	8(2)	6(2) 	9(2)

N(1)	36(3) 	48(4)	40(3) 	-12(3)	11(3) 	-17(3)

N(2)	20(2) 	19(3)	32(3) 	5(2)	1(2) 	7(2)

N(3)	33(3) 	37(3)	32(3) 	1(2)	6(2) 	4(2)

N(4)	31(3) 	34(3)	35(3) 	-2(2)	5(2) 	-2(2)

N(5)	41(3) 	34(3)	29(3) 	-5(2)	5(2) 	-11(3)

N(6)	41(3) 	26(3)	24(3) 	8(2)	6(2) 	9(2)

________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3) for Cu3(CN)3(1,10-phen).

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(1A)	6940	4044	7145	46

H(2A)	9322	4196	7939	49

H(3A)	10841	3432	8312	46

H(6A)	11122	2340	8430	44

H(7A)	10143	1470	8100	45

H(10A)	7928	854	7414	42

H(11A)	5511	807	6609	49

H(12A)	4226	1637	6198	42

________________________________________________________________________