Table 1.  Crystal data and structure refinement for Cu3(CN)3(2,2'-biquin)2.

Identification code 	[Cu3(CN)3(2,2'-biquin)2]

Empirical formula 	C39H24Cu3N7

Formula weight 	781.27

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/m

Unit cell dimensions	a = 13.6666(2) Å	= 90°.

b = 15.3303(2) Å	= 96.751(2)°.

c = 7.8477(2) Å	 = 90°.

Volume	1632.80(5) Å3

Z	2

Density (calculated)	1.589 Mg/m3

Absorption coefficient	1.977 mm-1

F(000)	788

Crystal size	0.17 x 0.11 x 0.05 mm3

Theta range for data collection	2.00 to 28.26°.

Index ranges	-18<=h<=15, -20<=k<=16, -9<=l<=10

Reflections collected	5322

Independent reflections	2003 [R(int) = 0.0314]

Completeness to theta = 28.26°	95.7 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2003 / 0 / 119

Goodness-of-fit on F2	1.166

Final R indices [I>2sigma(I)]	R1 = 0.0343, wR2 = 0.0734

R indices (all data)	R1 = 0.0404, wR2 = 0.0766

Largest diff. peak and hole	0.457 and -0.407 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for Cu3(CN)3(2,2'-biquin)2.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________

Cu(2)	0	0	0	26(1)

Cu(1)	3320(1)	0	-1732(1)	20(1)

N(4)	3539(1)	860(1)	-3727(2)	17(1)

C(4)	3678(2)	488(1)	-5211(3)	18(1)

C(5)	3851(2)	981(2)	-6669(3)	23(1)

C(6)	3878(2)	1871(2)	-6557(3)	25(1)

C(7)	3745(2)	2287(2)	-4997(3)	23(1)

C(8)	3779(2)	3209(2)	-4764(4)	29(1)

C(9)	3678(2)	3561(2)	-3196(4)	34(1)

C(10)	3532(2)	3023(2)	-1794(4)	34(1)

C(11)	3478(2)	2135(2)	-1981(3)	26(1)

C(12)	3581(2)	1750(2)	-3590(3)	20(1)

C(1)	1243(2)	0	-643(4)	23(1)

C(2)	2036(3)	0	-1024(4)	28(1)

C(3)	4599(2)	0	-340(4)	21(1)

N(1)	1243(2)	0	-643(4)	23(1)

N(2)	2036(3)	0	-1024(4)	28(1)

N(3)	4599(2)	0	-340(4)	21(1)

________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for Cu3(CN)3(2,2'-biquin)2.

_____________________________________________________

Cu(2)-N(1)#1 	1.828(3)

Cu(2)-C(1)#1 	1.828(3)

Cu(2)-C(1) 	1.828(3)

Cu(1)-C(2) 	1.902(4)

Cu(1)-C(3) 	1.950(3)

Cu(1)-N(4) 	2.0947(18)

Cu(1)-N(4)#2 	2.0947(18)

N(4)-C(4) 	1.330(3)

N(4)-C(12) 	1.369(3)

C(4)-C(5) 	1.415(3)

C(4)-C(4)#2 	1.495(4)

C(5)-C(6) 	1.367(3)

C(6)-C(7) 	1.411(3)

C(7)-C(12) 	1.416(3)

C(7)-C(8) 	1.425(3)

C(8)-C(9) 	1.365(4)

C(9)-C(10) 	1.408(4)

C(10)-C(11) 	1.370(4)

C(11)-C(12) 	1.417(3)

C(1)-C(2) 	1.157(4)

C(3)-N(3)#3 	1.161(6)

C(3)-C(3)#3 	1.161(6)

N(1)#1-Cu(2)-C(1)#1	0.00(18)

N(1)#1-Cu(2)-C(1)	180.00(5)

C(1)#1-Cu(2)-C(1)	180.00(5)

C(2)-Cu(1)-C(3)	129.33(13)

C(2)-Cu(1)-N(4)	115.87(9)

C(3)-Cu(1)-N(4)	102.76(8)

C(2)-Cu(1)-N(4)#2	115.87(9)

C(3)-Cu(1)-N(4)#2	102.76(8)

N(4)-Cu(1)-N(4)#2	77.99(10)

C(4)-N(4)-C(12)	119.1(2)

C(4)-N(4)-Cu(1)	115.59(15)

C(12)-N(4)-Cu(1)	125.24(16)

N(4)-C(4)-C(5)	122.2(2)

N(4)-C(4)-C(4)#2	115.40(12)

C(5)-C(4)-C(4)#2	122.32(13)

C(6)-C(5)-C(4)	119.2(2)

C(5)-C(6)-C(7)	120.1(2)

C(6)-C(7)-C(12)	117.5(2)

C(6)-C(7)-C(8)	123.7(2)

C(12)-C(7)-C(8)	118.8(2)

C(9)-C(8)-C(7)	120.2(2)

C(8)-C(9)-C(10)	120.8(2)

C(11)-C(10)-C(9)	120.6(3)

C(10)-C(11)-C(12)	120.0(2)

N(4)-C(12)-C(7)	121.8(2)

N(4)-C(12)-C(11)	118.5(2)

C(7)-C(12)-C(11)	119.6(2)

C(2)-C(1)-Cu(2)	179.0(3)

C(1)-C(2)-Cu(1)	178.0(3)

N(3)#3-C(3)-C(3)#3	0.0(3)

N(3)#3-C(3)-Cu(1)	173.4(4)

C(3)#3-C(3)-Cu(1)	173.4(4)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y,-z    #2 x,-y,z    #3 -x+1,-y,-z

Table 4.   Anisotropic displacement parameters  (Å2x 103) for Djc38.  The anisotropic

displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

________________________________________________________________________

U11	U22 	U33	U23	U13	U12

________________________________________________________________________

Cu(2)	17(1) 	29(1)	33(1) 	0	9(1) 	0

Cu(1)	19(1) 	22(1)	18(1) 	0	5(1) 	0

N(4)	13(1) 	19(1)	19(1) 	0(1)	1(1) 	0(1)

C(4)	13(1) 	22(1)	18(1) 	1(1)	1(1) 	0(1)

C(5)	24(1) 	26(1)	20(1) 	2(1)	6(1) 	3(1)

C(6)	22(1) 	25(1)	27(1) 	9(1)	6(1) 	1(1)

C(7)	15(1) 	20(1)	32(1) 	4(1)	0(1) 	-1(1)

C(8)	22(1) 	21(1)	44(2) 	7(1)	1(1) 	-1(1)

C(9)	29(1) 	18(1)	54(2) 	-3(1)	-3(1) 	-1(1)

C(10)	36(2) 	26(1)	38(1) 	-12(1)	-1(1) 	2(1)

C(11)	27(1) 	24(1)	27(1) 	-3(1)	-1(1) 	2(1)

C(12)	15(1) 	19(1)	27(1) 	-1(1)	-1(1) 	1(1)

C(1)	18(2) 	23(2)	29(2) 	0	8(1) 	0

C(2)	32(2) 	23(2)	28(2) 	0	4(1) 	0

C(3)	24(1) 	23(1)	16(1) 	0	6(1) 	0

N(1)	18(2) 	23(2)	29(2) 	0	8(1) 	0

N(2)	32(2) 	23(2)	28(2) 	0	4(1) 	0

N(3)	24(1) 	23(1)	16(1) 	0	6(1) 	0

________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3) for Cu3(CN)3(2,2'-biquin)2.

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(5)	3945	704	-7691	27

H(6)	3985	2202	-7511	29

H(8)	3870	3572	-5682	35

H(9)	3706	4163	-3053	41

H(10)	3472	3273	-732	40

H(11)	3373	1786	-1051	32

________________________________________________________________________