Table 1  Crystal data and structure refinement for Cu2(CN)2(dpdp).

Identification code 	[Cu2(CN)2(dpdp)]

Empirical formula 	C24H16Cu2N4

Formula weight 	487.49

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/c

Unit cell dimensions	a = 12.112(2) Å	= 90°.

b = 9.9414(18) Å	= 93.743(5)°.

c = 16.308(3) Å	 = 90°.

Volume	1959.5(7) Å3

Z	4

Density (calculated)	1.652 Mg/m3

Absorption coefficient	2.189 mm-1

F(000)	984

Crystal size	0.15 x 0.13 x 0.09 mm3

Theta range for data collection	1.68 to 28.33°.

Index ranges	-16<=h<=11, -13<=k<=13, -21<=l<=19

Reflections collected	11982

Independent reflections	4639 [R(int) = 0.0610]

Completeness to theta = 28.33°	94.9 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4639 / 0 / 271

Goodness-of-fit on F2	1.054

Final R indices [I>2sigma(I)]	R1 = 0.0560, wR2 = 0.0916

R indices (all data)	R1 = 0.0988, wR2 = 0.1038

Largest diff. peak and hole	0.633 and -0.524 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for Cu2(CN)2(dpdp).  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________

Cu(1)	2426(1)	10190(1)	4934(1)	17(1)

Cu(2)	2333(1)	7920(1)	2247(1)	23(1)

N(5)	1388(3)	11781(3)	5257(2)	13(1)

N(6)	3426(3)	11856(3)	4742(2)	14(1)

N(1)	2558(3)	8952(4)	5832(2)	27(1)

N(2)	2197(3)	9520(3)	3801(2)	14(1)

N(3)	2211(3)	8981(4)	3171(2)	22(1)

N(4)	2534(3)	6790(3)	1380(2)	16(1)

C(1)	2558(3)	8952(4)	5832(2)	27(1)

C(2)	2197(3)	9520(3)	3801(2)	14(1)

C(3)	2211(3)	8981(4)	3171(2)	22(1)

C(4)	2534(3)	6790(3)	1380(2)	16(1)

C(5)	168(3)	16504(4)	6193(2)	18(1)

C(6)	-332(4)	17578(4)	6573(2)	20(1)

C(7)	-1092(4)	17353(4)	7147(2)	21(1)

C(8)	-1354(3)	16048(4)	7357(2)	22(1)

C(9)	-869(3)	14968(4)	6981(2)	18(1)

C(10)	-100(3)	15176(4)	6390(2)	15(1)

C(11)	414(3)	14027(4)	5974(2)	14(1)

C(12)	-106(3)	12773(4)	5936(2)	16(1)

C(13)	414(3)	11695(4)	5598(2)	17(1)

C(14)	1424(3)	14118(4)	5621(2)	14(1)

C(15)	1880(3)	13005(4)	5253(2)	14(1)

C(16)	2921(3)	13062(4)	4827(2)	13(1)

C(17)	4377(3)	11861(4)	4368(2)	18(1)

C(18)	4837(3)	12995(4)	4046(2)	17(1)

C(19)	4300(3)	14234(4)	4096(2)	14(1)

C(20)	3329(3)	14242(4)	4501(2)	14(1)

C(21)	4763(3)	15463(4)	3725(2)	13(1)

C(22)	5601(3)	15382(4)	3178(2)	18(1)

C(23)	6064(4)	16514(4)	2852(2)	22(1)

C(24)	5696(4)	17778(4)	3060(2)	22(1)

C(25)	4848(3)	17886(4)	3581(2)	21(1)

C(26)	4383(3)	16750(4)	3906(2)	18(1)

________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for Cu2(CN)2(dpdp).

_____________________________________________________

Cu(1)-N(1) 	1.911(4)

Cu(1)-N(2) 	1.966(3)

Cu(1)-N(6) 	2.089(3)

Cu(1)-N(5) 	2.109(3)

Cu(2)-N(4) 	1.834(3)

Cu(2)-N(3) 	1.854(4)

N(5)-C(13) 	1.339(5)

N(5)-C(15) 	1.355(5)

N(6)-C(17) 	1.337(5)

N(6)-C(16) 	1.357(5)

N(1)-C(4)#1 	1.162(5)

N(1)-N(4)#1 	1.162(5)

N(2)-N(3) 	1.159(5)

N(4)-C(1)#2 	1.162(5)

N(4)-N(1)#2 	1.162(5)

C(5)-C(6) 	1.392(5)

C(5)-C(10) 	1.402(5)

C(6)-C(7) 	1.374(6)

C(7)-C(8) 	1.385(6)

C(8)-C(9) 	1.386(5)

C(9)-C(10) 	1.398(5)

C(10)-C(11) 	1.486(5)

C(11)-C(14) 	1.388(5)

C(11)-C(12) 	1.397(5)

C(12)-C(13) 	1.376(5)

C(14)-C(15) 	1.391(5)

C(15)-C(16) 	1.479(5)

C(16)-C(20) 	1.391(5)

C(17)-C(18) 	1.377(5)

C(18)-C(19) 	1.398(5)

C(19)-C(20) 	1.386(5)

C(19)-C(21) 	1.490(5)

C(21)-C(22) 	1.396(5)

C(21)-C(26) 	1.397(5)

C(22)-C(23) 	1.380(5)

C(23)-C(24) 	1.382(6)

C(24)-C(25) 	1.380(6)

C(25)-C(26) 	1.383(5)

N(1)-Cu(1)-N(2)	120.10(15)

N(1)-Cu(1)-N(6)	127.24(15)

N(2)-Cu(1)-N(6)	100.10(13)

N(1)-Cu(1)-N(5)	108.22(14)

N(2)-Cu(1)-N(5)	116.06(13)

N(6)-Cu(1)-N(5)	78.67(12)

N(4)-Cu(2)-N(3)	175.46(17)

C(13)-N(5)-C(15)	117.4(3)

C(13)-N(5)-Cu(1)	127.7(2)

C(15)-N(5)-Cu(1)	113.7(3)

C(17)-N(6)-C(16)	116.8(3)

C(17)-N(6)-Cu(1)	126.6(2)

C(16)-N(6)-Cu(1)	114.5(3)

C(4)#1-N(1)-N(4)#1	0.0(4)

C(4)#1-N(1)-Cu(1)	173.7(4)

N(4)#1-N(1)-Cu(1)	173.7(4)

N(3)-N(2)-Cu(1)	168.3(3)

N(2)-N(3)-Cu(2)	171.9(4)

C(1)#2-N(4)-N(1)#2	0.0(4)

C(1)#2-N(4)-Cu(2)	173.7(3)

N(1)#2-N(4)-Cu(2)	173.7(3)

C(6)-C(5)-C(10)	120.5(4)

C(7)-C(6)-C(5)	120.5(4)

C(6)-C(7)-C(8)	119.7(4)

C(7)-C(8)-C(9)	120.4(4)

C(8)-C(9)-C(10)	120.7(4)

C(9)-C(10)-C(5)	118.1(4)

C(9)-C(10)-C(11)	121.2(3)

C(5)-C(10)-C(11)	120.7(3)

C(14)-C(11)-C(12)	116.6(3)

C(14)-C(11)-C(10)	123.1(3)

C(12)-C(11)-C(10)	120.4(3)

C(13)-C(12)-C(11)	119.7(4)

N(5)-C(13)-C(12)	123.7(4)

C(11)-C(14)-C(15)	120.8(3)

N(5)-C(15)-C(14)	121.7(3)

N(5)-C(15)-C(16)	115.2(3)

C(14)-C(15)-C(16)	123.1(3)

N(6)-C(16)-C(20)	122.1(3)

N(6)-C(16)-C(15)	114.7(3)

C(20)-C(16)-C(15)	123.1(3)

N(6)-C(17)-C(18)	124.0(4)

C(17)-C(18)-C(19)	119.8(4)

C(20)-C(19)-C(18)	116.5(4)

C(20)-C(19)-C(21)	122.9(3)

C(18)-C(19)-C(21)	120.6(3)

C(19)-C(20)-C(16)	120.7(4)

C(22)-C(21)-C(26)	116.7(3)

C(22)-C(21)-C(19)	121.4(3)

C(26)-C(21)-C(19)	121.9(3)

C(23)-C(22)-C(21)	122.0(4)

C(22)-C(23)-C(24)	120.1(4)

C(25)-C(24)-C(23)	119.1(4)

C(24)-C(25)-C(26)	120.7(4)

C(25)-C(26)-C(21)	121.3(4)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 x,-y+3/2,z+1/2    #2 x,-y+3/2,z-1/2

Table 4.   Anisotropic displacement parameters  (Å2x 103) for Cu2(CN)2(dpdp).  The anisotropic displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

________________________________________________________________________

U11	U22 	U33	U23	U13	U12

________________________________________________________________________

Cu(1)	22(1) 	11(1)	18(1) 	0(1)	5(1) 	1(1)

Cu(2)	26(1) 	23(1)	20(1) 	-10(1)	9(1) 	-7(1)

N(5)	18(2) 	13(2)	8(2) 	0(1)	2(1) 	1(1)

N(6)	17(2) 	13(2)	13(2) 	-2(1)	3(1) 	2(1)

N(1)	21(2) 	27(2)	34(2) 	-6(2)	6(2) 	4(2)

N(2)	16(2) 	11(2)	15(2) 	-1(1)	2(2) 	-3(2)

N(3)	20(2) 	21(2)	25(2) 	1(2)	5(2) 	-3(2)

N(4)	16(2) 	18(2)	15(2) 	-12(2)	6(2) 	-6(2)

C(1)	21(2) 	27(2)	34(2) 	-6(2)	6(2) 	4(2)

C(2)	16(2) 	11(2)	15(2) 	-1(1)	2(2) 	-3(2)

C(3)	20(2) 	21(2)	25(2) 	1(2)	5(2) 	-3(2)

C(4)	16(2) 	18(2)	15(2) 	-12(2)	6(2) 	-6(2)

C(5)	21(2) 	20(2)	13(2) 	2(2)	1(2) 	-2(2)

C(6)	31(3) 	12(2)	17(2) 	-1(2)	-5(2) 	7(2)

C(7)	23(2) 	21(2)	17(2) 	-8(2)	-2(2) 	9(2)

C(8)	17(2) 	31(2)	19(2) 	-2(2)	6(2) 	6(2)

C(9)	19(2) 	14(2)	20(2) 	-2(2)	3(2) 	0(2)

C(10)	12(2) 	18(2)	15(2) 	-4(2)	-2(2) 	4(2)

C(11)	20(2) 	11(2)	11(2) 	2(2)	-2(2) 	-1(2)

C(12)	14(2) 	18(2)	16(2) 	-2(2)	4(2) 	0(2)

C(13)	23(2) 	12(2)	15(2) 	0(2)	-3(2) 	-3(2)

C(14)	16(2) 	7(2)	18(2) 	1(2)	0(2) 	-1(2)

C(15)	17(2) 	14(2)	11(2) 	3(2)	1(2) 	2(2)

C(16)	17(2) 	14(2)	9(2) 	0(2)	1(2) 	1(2)

C(17)	23(2) 	14(2)	16(2) 	-3(2)	4(2) 	4(2)

C(18)	16(2) 	21(2)	14(2) 	-3(2)	3(2) 	4(2)

C(19)	13(2) 	16(2)	12(2) 	-2(2)	-1(2) 	-1(2)

C(20)	19(2) 	10(2)	13(2) 	0(2)	-2(2) 	1(2)

C(21)	14(2) 	16(2)	10(2) 	-2(2)	0(2) 	-3(2)

C(22)	23(2) 	15(2)	16(2) 	-1(2)	4(2) 	-1(2)

C(23)	19(2) 	25(2)	23(2) 	5(2)	7(2) 	-2(2)

C(24)	22(2) 	23(2)	20(2) 	3(2)	-2(2) 	-4(2)

C(25)	23(2) 	14(2)	25(2) 	0(2)	-2(2) 	-2(2)

C(26)	18(2) 	18(2)	16(2) 	0(2)	2(2) 	-1(2)

________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3) for Cu2(CN)2(dpdp).

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(5)	682	16669	5807	21

H(6)	-149	18455	6436	24

H(7)	-1429	18075	7393	25

H(8)	-1859	15894	7752	27

H(9)	-1057	14095	7122	21

H(12)	-802	12666	6138	19

H(13)	69	10860	5606	20

H(14)	1800	14934	5631	17

H(17)	4750	11049	4324	21

H(18)	5504	12936	3795	20

H(20)	2946	15044	4556	17

H(22)	5854	14540	3029	22

H(23)	6624	16427	2492	26

H(24)	6017	18545	2851	26

H(25)	4586	18732	3715	25

H(26)	3807	16844	4251	21

________________________________________________________________________