Table 1.  Crystal data and structure refinement for Cu(CN)(dpphen).

Identification code 	[Cu(CN)(dpphen)]

Empirical formula 	C25H16CuN3

Formula weight 	421.95

Temperature 	293(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Cmc2(1)

Unit cell dimensions	a = 25.5335(6) Å	= 90°.

b = 9.7098(2) Å	= 90°.

c = 7.6381(2) Å	 = 90°.

Volume	1893.68(8) Å3

Z	4

Density (calculated)	1.480 Mg/m3

Absorption coefficient	1.169 mm-1

F(000)	864

Crystal size	0.11 x 0.05 x 0.03 mm3

Theta range for data collection	1.60 to 28.21°.

Index ranges	-29<=h<=33, -11<=k<=12, -10<=l<=9

Reflections collected	5991

Independent reflections	2256 [R(int) = 0.0661]

Completeness to theta = 28.21°	99.0 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2256 / 1 / 137

Goodness-of-fit on F2	1.258

Final R indices [I>2sigma(I)]	R1 = 0.0591, wR2 = 0.1241

R indices (all data)	R1 = 0.0781, wR2 = 0.1343

Absolute structure parameter	0.04(3)

Extinction coefficient	0.0079(10)

Largest diff. peak and hole	0.798 and -0.506 e.Å-3

Table 2.  Atomic coordinates  ( x 104) and equivalent  isotropic displacement parameters (Å2x 103) for Cu(CN)(dpphen).  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________

Cu(1)	5000	1639(1)	3804(1)	20(1)

N(3)	5521(1)	3277(3)	3918(7)	14(1)

N(1)	5000	593(8)	1693(9)	24(2)

N(2)	5000	320(7)	5672(9)	18(2)

C(1)	5000	593(8)	1693(9)	24(2)

C(2)	5000	320(7)	5672(9)	18(2)

C(3)	6043(2)	3272(4)	4029(7)	15(1)

C(4)	6342(2)	4464(4)	4019(6)	16(1)

C(5)	6115(1)	5756(3)	3862(8)	14(1)

C(6)	5559(2)	5796(4)	3663(7)	12(1)

C(7)	5282(1)	4532(3)	3772(8)	12(1)

C(8)	6440(2)	7017(4)	3940(8)	15(1)

C(9)	6921(2)	7088(5)	3043(6)	17(1)

C(10)	7241(2)	8238(5)	3205(6)	19(1)

C(11)	7093(2)	9324(5)	4267(6)	19(1)

C(12)	6621(2)	9280(5)	5168(6)	20(1)

C(13)	6292(2)	8129(4)	5003(6)	16(1)

C(14)	5265(2)	7028(4)	3346(5)	13(1)

________________________________________________________________________

Table 3.   Bond lengths [Å] and angles [°] for Cu(CN)(dpphen).

_____________________________________________________

Cu(1)-N(1) 	1.905(8)

Cu(1)-N(2) 	1.918(7)

Cu(1)-N(3) 	2.075(3)

Cu(1)-N(3)#1 	2.075(3)

N(3)-C(3) 	1.335(5)

N(3)-C(7) 	1.368(4)

N(1)-C(2)#2 	1.181(8)

N(1)-N(2)#2 	1.181(8)

N(2)-C(1)#3 	1.181(8)

N(2)-N(1)#3 	1.181(8)

C(3)-C(4) 	1.388(5)

C(4)-C(5) 	1.387(5)

C(5)-C(6) 	1.431(5)

C(5)-C(8) 	1.480(5)

C(6)-C(7) 	1.419(5)

C(6)-C(14) 	1.432(5)

C(7)-C(7)#1 	1.440(6)

C(8)-C(13) 	1.402(6)

C(8)-C(9) 	1.408(6)

C(9)-C(10) 	1.388(6)

C(10)-C(11) 	1.383(6)

C(11)-C(12) 	1.388(6)

C(12)-C(13) 	1.404(6)

C(14)-C(14)#1 	1.353(8)

N(1)-Cu(1)-N(2)	105.9(3)

N(1)-Cu(1)-N(3)	116.4(2)

N(2)-Cu(1)-N(3)	118.71(19)

N(1)-Cu(1)-N(3)#1	116.4(2)

N(2)-Cu(1)-N(3)#1	118.71(19)

N(3)-Cu(1)-N(3)#1	79.77(16)

C(3)-N(3)-C(7)	117.0(3)

C(3)-N(3)-Cu(1)	129.8(2)

C(7)-N(3)-Cu(1)	113.1(2)

C(2)#2-N(1)-N(2)#2	0.0(7)

C(2)#2-N(1)-Cu(1)	163.6(6)

N(2)#2-N(1)-Cu(1)	163.6(6)

C(1)#3-N(2)-N(1)#3	0.0(5)

C(1)#3-N(2)-Cu(1)	173.3(5)

N(1)#3-N(2)-Cu(1)	173.3(5)

N(3)-C(3)-C(4)	123.1(3)

C(5)-C(4)-C(3)	121.7(4)

C(4)-C(5)-C(6)	116.7(3)

C(4)-C(5)-C(8)	120.7(3)

C(6)-C(5)-C(8)	122.6(3)

C(7)-C(6)-C(5)	117.7(3)

C(7)-C(6)-C(14)	118.2(3)

C(5)-C(6)-C(14)	124.1(3)

N(3)-C(7)-C(6)	123.6(3)

N(3)-C(7)-C(7)#1	116.53(19)

C(6)-C(7)-C(7)#1	119.85(19)

C(13)-C(8)-C(9)	118.6(4)

C(13)-C(8)-C(5)	120.6(4)

C(9)-C(8)-C(5)	120.7(4)

C(10)-C(9)-C(8)	120.6(4)

C(11)-C(10)-C(9)	120.4(4)

C(10)-C(11)-C(12)	120.2(4)

C(11)-C(12)-C(13)	119.9(4)

C(8)-C(13)-C(12)	120.2(4)

C(14)#1-C(14)-C(6)	121.6(2)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,y,z    #2 -x+1,-y,z-1/2    #3 -x+1,-y,z+1/2

Table 4.   Anisotropic displacement parameters  (Å2x 103) for Cu(CN)(dpphen).  The anisotropic displacement factor exponent takes the form:  -22[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

________________________________________________________________________

U11	U22 	U33	U23	U13	U12

________________________________________________________________________

Cu(1)	26(1) 	9(1)	24(1) 	-2(1)	0 	0

N(3)	18(2) 	10(1)	12(2) 	-5(2)	-3(2) 	4(1)

N(1)	29(4) 	22(4)	20(4) 	11(3)	0 	0

N(2)	32(4) 	8(3)	14(3) 	-3(2)	0 	0

C(1)	29(4) 	22(4)	20(4) 	11(3)	0 	0

C(2)	32(4) 	8(3)	14(3) 	-3(2)	0 	0

C(3)	17(2) 	14(2)	16(3) 	1(2)	0(2) 	5(1)

C(4)	12(2) 	19(2)	15(3) 	0(2)	-2(2) 	3(1)

C(5)	16(2) 	15(2)	11(2) 	-1(3)	0(2) 	-1(1)

C(6)	19(2) 	9(2)	9(2) 	-1(2)	-2(2) 	1(1)

C(7)	13(2) 	12(2)	11(2) 	4(3)	1(2) 	1(1)

C(8)	13(2) 	14(2)	17(2) 	4(2)	-3(2) 	1(1)

C(9)	13(2) 	17(2)	21(2) 	2(2)	-2(2) 	4(2)

C(10)	8(2) 	28(3)	22(3) 	6(2)	1(2) 	0(2)

C(11)	15(2) 	25(2)	18(3) 	2(2)	-6(2) 	-6(2)

C(12)	25(2) 	16(2)	19(3) 	1(2)	-7(2) 	1(2)

C(13)	10(2) 	16(2)	21(2) 	2(2)	-4(2) 	-2(2)

C(14)	15(2) 	11(2)	13(3) 	2(1)	1(2) 	-2(2)

________________________________________________________________________

Table 5.   Hydrogen coordinates ( x 104) and isotropic  displacement parameters (Å2x 10 3) for Cu(CN)(dpphen).

________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________

H(3)	6214	2429	4117	19

H(4)	6704	4395	4121	19

H(9)	7026	6359	2336	20

H(10)	7555	8278	2596	23

H(11)	7311	10087	4379	23

H(12)	6523	10013	5880	24

H(13)	5975	8103	5601	19

H(14)	5443	7847	3135	16

________________________________________________________________________