data_ifn319

_database_code_CSD                  191318

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'C101 H176 N12 Ni10 O35 S4'

_chemical_formula_weight          2833.88

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'C'  'C'   0.0033   0.0016

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'H'  'H'   0.0000   0.0000

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'N'  'N'   0.0061   0.0033

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'S'  'S'   0.1246   0.1234

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ni'  'Ni'   0.3393   1.1124

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            Monoclinic

_symmetry_space_group_name_H-M    P2(1)/c

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y-1/2, z-1/2'

_cell_length_a                    15.730(4)

_cell_length_b                    20.540(4)

_cell_length_c                    41.061(8)

_cell_angle_alpha                 90.00

_cell_angle_beta                  91.314(5)

_cell_angle_gamma                 90.00

_cell_volume                      13264(5)

_cell_formula_units_Z             4

_cell_measurement_temperature     150(2)

_cell_measurement_reflns_used     3123

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           0.42

_exptl_crystal_size_mid           0.32

_exptl_crystal_size_min           0.22

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     1.419

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              5960

_exptl_absorpt_coefficient_mu     1.522

_exptl_absorpt_correction_type    empirical

_exptl_absorpt_correction_T_min   0.5673

_exptl_absorpt_correction_T_max   0.7306

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       150(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   'CCD area detector'

_diffrn_measurement_method        'phi and omega scans'

_diffrn_detector_area_resol_mean  ?

_diffrn_standards_number          ?

_diffrn_standards_interval_count  ?

_diffrn_standards_interval_time   ?

_diffrn_standards_decay_%         ?

_diffrn_reflns_number             55025

_diffrn_reflns_av_R_equivalents   0.2064

_diffrn_reflns_av_sigmaI/netI     0.2523

_diffrn_reflns_limit_h_min        -16

_diffrn_reflns_limit_h_max        16

_diffrn_reflns_limit_k_min        -22

_diffrn_reflns_limit_k_max        22

_diffrn_reflns_limit_l_min        -44

_diffrn_reflns_limit_l_max        38

_diffrn_reflns_theta_min          1.11

_diffrn_reflns_theta_max          22.50

_reflns_number_total              17333

_reflns_number_gt                 7166

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        'Bruker SMART'

_computing_cell_refinement        'Bruker SMART'

_computing_data_reduction         'Bruker SHELXTL'

_computing_structure_solution     'SHELXS-97 (Sheldrick, 1990)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 1997)'

_computing_molecular_graphics     'Bruker SHELXTL'

_computing_publication_material   'Bruker SHELXTL'

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.1022P)^2^+0.0000P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          17333

_refine_ls_number_parameters      1446

_refine_ls_number_restraints      25

_refine_ls_R_factor_all           0.2006

_refine_ls_R_factor_gt            0.0908

_refine_ls_wR_factor_ref          0.2513

_refine_ls_wR_factor_gt           0.2099

_refine_ls_goodness_of_fit_ref    0.943

_refine_ls_restrained_S_all       0.943

_refine_ls_shift/su_max           0.000

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

Ni1 Ni 0.67346(12) 0.09200(9) 0.37138(4) 0.0257(5) Uani 1 1 d . . .

Ni2 Ni 0.65916(12) 0.20979(9) 0.41281(5) 0.0326(6) Uani 1 1 d . . .

Ni3 Ni 0.57863(12) 0.24712(9) 0.34643(5) 0.0305(5) Uani 1 1 d . . .

Ni4 Ni 0.36239(13) 0.31258(9) 0.35135(5) 0.0363(6) Uani 1 1 d . . .

Ni5 Ni 0.42993(13) 0.23792(9) 0.29574(5) 0.0313(5) Uani 1 1 d . . .

Ni6 Ni -0.17574(12) 0.37215(9) 0.12176(5) 0.0289(5) Uani 1 1 d . . .

Ni7 Ni -0.16842(12) 0.26890(9) 0.07122(5) 0.0317(5) Uani 1 1 d . . .

Ni8 Ni -0.08785(12) 0.20822(9) 0.13377(5) 0.0329(6) Uani 1 1 d . . .

Ni9 Ni 0.12387(13) 0.13927(9) 0.12198(5) 0.0366(6) Uani 1 1 d . . .

Ni10 Ni 0.06579(12) 0.20133(9) 0.18266(5) 0.0345(6) Uani 1 1 d . . .

S1 S 0.3793(6) 0.2980(5) 0.4983(2) 0.159(4) Uani 1 1 d D . .

S2 S 0.4393(4) 0.0011(3) 0.20464(15) 0.090(2) Uani 1 1 d D . .

S3 S 0.1010(5) 0.1885(4) -0.01840(18) 0.127(3) Uani 1 1 d D . .

S4 S 0.0565(5) 0.4722(4) 0.23994(19) 0.126(3) Uani 1 1 d D . .

O1 O 0.6273(6) 0.1158(4) 0.4154(2) 0.027(2) Uani 1 1 d . . .

O2 O 0.6728(5) 0.1895(4) 0.3641(2) 0.024(2) Uani 1 1 d . . .

H20D H 0.7294 0.2048 0.3565 0.029 Uiso 1 1 calc R . .

O3 O 0.7948(6) 0.1002(5) 0.3885(2) 0.032(3) Uani 1 1 d . . .

O4 O 0.7871(6) 0.1884(5) 0.4209(2) 0.041(3) Uani 1 1 d . . .

O5 O 0.5463(6) 0.0857(4) 0.3555(2) 0.029(3) Uani 1 1 d . . .

O6 O 0.5031(6) 0.1708(5) 0.3266(2) 0.027(3) Uani 1 1 d . . .

O7 O 0.6402(6) 0.2563(5) 0.3030(3) 0.043(3) Uani 1 1 d . . .

O8 O 0.5326(7) 0.2481(5) 0.2674(2) 0.039(3) Uani 1 1 d . . .

O9 O 0.3314(7) 0.2332(4) 0.3246(2) 0.031(3) Uani 1 1 d . . .

O10 O 0.4761(6) 0.2996(4) 0.3313(2) 0.026(2) Uani 1 1 d . . .

H20E H 0.4953 0.3412 0.3211 0.032 Uiso 1 1 calc R . .

O11 O 0.3795(7) 0.3183(5) 0.2712(2) 0.043(3) Uani 1 1 d . . .

O12 O 0.3339(7) 0.3758(5) 0.3131(3) 0.045(3) Uani 1 1 d . . .

O13 O 0.3947(7) 0.2469(5) 0.3887(2) 0.038(3) Uani 1 1 d . . .

O14 O 0.5351(6) 0.2343(5) 0.3928(2) 0.033(3) Uani 1 1 d . . .

O15 O 0.6369(7) 0.3313(5) 0.3597(3) 0.049(3) Uani 1 1 d . . .

O16 O 0.6912(7) 0.3054(5) 0.4081(3) 0.052(4) Uani 1 1 d . . .

O17 O -0.1322(6) 0.3610(4) 0.0757(2) 0.032(3) Uani 1 1 d . . .

O18 O -0.1796(6) 0.2741(4) 0.1216(2) 0.031(3) Uani 1 1 d . . .

H20F H -0.2368 0.2582 0.1282 0.037 Uiso 1 1 calc R . .

O19 O -0.2992(6) 0.3719(5) 0.1041(3) 0.036(3) Uani 1 1 d . . .

O20 O -0.2940(6) 0.2960(5) 0.0648(2) 0.036(3) Uani 1 1 d . . .

O21 O -0.0501(6) 0.3710(4) 0.1370(2) 0.033(3) Uani 1 1 d . . .

O22 O -0.0069(6) 0.2756(5) 0.1577(2) 0.031(3) Uani 1 1 d . . .

O23 O -0.1449(6) 0.1831(5) 0.1764(3) 0.044(3) Uani 1 1 d . B .

O24 O -0.0367(7) 0.1827(5) 0.2119(2) 0.042(3) Uani 1 1 d . B .

O25 O 0.1607(6) 0.2114(4) 0.1521(2) 0.033(3) Uani 1 1 d . . .

O26 O 0.0117(6) 0.1504(5) 0.1446(2) 0.043(3) Uani 1 1 d . . .

H20G H -0.0089 0.1072 0.1525 0.051 Uiso 1 1 calc R . .

O27 O 0.1227(7) 0.1193(5) 0.2028(3) 0.040(3) Uani 1 1 d . . .

O28 O 0.1560(7) 0.0695(5) 0.1557(3) 0.047(3) Uani 1 1 d . . .

O29 O 0.0926(7) 0.2120(4) 0.0887(2) 0.034(3) Uani 1 1 d . . .

O30 O -0.0467(7) 0.2353(5) 0.0878(2) 0.037(3) Uani 1 1 d . . .

O31 O -0.1531(7) 0.1304(5) 0.1136(3) 0.046(3) Uani 1 1 d . . .

O32 O -0.2056(7) 0.1756(5) 0.0678(3) 0.048(3) Uani 1 1 d . . .

N1 N 0.6683(7) -0.0080(5) 0.3837(3) 0.028(3) Uani 1 1 d . . .

N2 N 0.7182(8) 0.0563(6) 0.3254(3) 0.039(4) Uani 1 1 d . . .

N3 N 0.6439(8) 0.2183(6) 0.4620(3) 0.038(4) Uani 1 1 d . . .

N4 N 0.2366(9) 0.3178(6) 0.3684(4) 0.044(4) Uani 1 1 d . . .

N5 N 0.3883(10) 0.3946(7) 0.3818(3) 0.056(4) Uani 1 1 d . . .

N6 N 0.3721(9) 0.1753(6) 0.2638(3) 0.036(3) Uani 1 1 d . . .

N7 N -0.1642(8) 0.4746(6) 0.1176(3) 0.035(3) Uani 1 1 d . . .

N8 N -0.2171(8) 0.3957(6) 0.1709(3) 0.035(3) Uani 1 1 d . . .

N9 N -0.1538(8) 0.2746(6) 0.0220(3) 0.033(3) Uani 1 1 d . . .

N10 N 0.2470(8) 0.1355(6) 0.1017(3) 0.039(4) Uani 1 1 d . . .

N11 N 0.0937(10) 0.0646(7) 0.0868(4) 0.057(4) Uani 1 1 d . . .

N12 N 0.1273(8) 0.2554(6) 0.2176(3) 0.034(3) Uani 1 1 d . . .

C1 C 0.6142(13) -0.0501(9) 0.5256(4) 0.075(6) Uani 1 1 d . . .

H1A H 0.6016 -0.0939 0.5173 0.113 Uiso 1 1 calc R . .

H1B H 0.5691 -0.0362 0.5401 0.113 Uiso 1 1 calc R . .

H1C H 0.6687 -0.0506 0.5376 0.113 Uiso 1 1 calc R . .

C2 C 0.6194(11) -0.0028(11) 0.4971(4) 0.056(6) Uani 1 1 d . . .

C3 C 0.6332(10) 0.0615(8) 0.4999(4) 0.035(4) Uani 1 1 d . . .

H3A H 0.6397 0.0798 0.5211 0.041 Uiso 1 1 calc R . .

C4 C 0.6383(9) 0.1025(8) 0.4728(4) 0.034(4) Uani 1 1 d . . .

C5 C 0.6235(9) 0.0785(7) 0.4415(4) 0.027(4) Uani 1 1 d . . .

C6 C 0.6102(9) 0.0113(7) 0.4379(3) 0.026(4) Uani 1 1 d . . .

C7 C 0.6058(9) -0.0278(8) 0.4656(4) 0.043(5) Uani 1 1 d . . .

H7A H 0.5932 -0.0727 0.4631 0.052 Uiso 1 1 calc R . .

C8 C 0.5961(10) -0.0173(7) 0.4049(3) 0.033(4) Uani 1 1 d . . .

H8A H 0.5849 -0.0645 0.4071 0.039 Uiso 1 1 calc R . .

H8B H 0.5451 0.0029 0.3946 0.039 Uiso 1 1 calc R . .

C9 C 0.7451(9) -0.0360(7) 0.4006(3) 0.033(4) Uani 1 1 d . . .

H9A H 0.7542 -0.0117 0.4212 0.040 Uiso 1 1 calc R . .

H9B H 0.7948 -0.0272 0.3869 0.040 Uiso 1 1 calc R . .

C10 C 0.7451(10) -0.1071(7) 0.4086(4) 0.050(5) Uani 1 1 d . . .

H10A H 0.7994 -0.1189 0.4192 0.075 Uiso 1 1 calc R . .

H10B H 0.7375 -0.1324 0.3884 0.075 Uiso 1 1 calc R . .

H10C H 0.6985 -0.1167 0.4232 0.075 Uiso 1 1 calc R . .

C11 C 0.6542(10) -0.0399(7) 0.3505(4) 0.036(4) Uani 1 1 d . . .

H11C H 0.6597 -0.0877 0.3526 0.043 Uiso 1 1 calc R . .

H11D H 0.5962 -0.0299 0.3421 0.043 Uiso 1 1 calc R . .

C12 C 0.7180(10) -0.0148(7) 0.3279(4) 0.034(4) Uani 1 1 d . . .

H12C H 0.7751 -0.0295 0.3354 0.041 Uiso 1 1 calc R . .

H12D H 0.7066 -0.0335 0.3060 0.041 Uiso 1 1 calc R . .

C13 C 0.6572(10) 0.0765(7) 0.2977(4) 0.042(5) Uani 1 1 d . . .

H13D H 0.6781 0.0599 0.2770 0.063 Uiso 1 1 calc R . .

H13E H 0.6537 0.1241 0.2968 0.063 Uiso 1 1 calc R . .

H13F H 0.6007 0.0584 0.3016 0.063 Uiso 1 1 calc R . .

C14 C 0.8029(9) 0.0841(9) 0.3179(4) 0.055(5) Uani 1 1 d . . .

H14D H 0.8216 0.0670 0.2970 0.082 Uiso 1 1 calc R . .

H14E H 0.8441 0.0719 0.3351 0.082 Uiso 1 1 calc R . .

H14F H 0.7987 0.1316 0.3167 0.082 Uiso 1 1 calc R . .

C15 C 0.6459(9) 0.1704(8) 0.4813(4) 0.033(4) Uani 1 1 d . . .

H15A H 0.6532 0.1801 0.5038 0.039 Uiso 1 1 calc R . .

C16 C 0.6395(13) 0.2853(9) 0.4782(5) 0.075(7) Uani 1 1 d . A .

H16C H 0.6604 0.2817 0.5010 0.090 Uiso 1 1 calc R . .

H16D H 0.6776 0.3156 0.4667 0.090 Uiso 1 1 calc R . .

C17 C 0.5515(16) 0.3129(11) 0.4778(5) 0.104(9) Uani 1 1 d D . .

H17A H 0.5233 0.3039 0.4564 0.125 Uiso 0.26(10) 1 calc PR A 1

H17B H 0.5543 0.3607 0.4807 0.125 Uiso 0.26(10) 1 calc PR A 1

H17C H 0.5267 0.3100 0.4560 0.125 Uiso 0.74(10) 1 d PR A 2

H17D H 0.5535 0.3584 0.4840 0.125 Uiso 0.74(10) 1 d PR A 2

C18 C 0.4959(19) 0.280(8) 0.507(3) 0.110(13) Uiso 0.26(10) 1 d PDU A 1

H18A H 0.5135 0.2988 0.5285 0.132 Uiso 0.26(10) 1 calc PR A 1

H18B H 0.5055 0.2324 0.5080 0.132 Uiso 0.26(10) 1 calc PR A 1

C18' C 0.4938(16) 0.270(3) 0.5031(11) 0.109(12) Uiso 0.74(10) 1 d PDU A 2

H18C H 0.5144 0.2764 0.5258 0.131 Uiso 0.74(10) 1 calc PR A 2

H18D H 0.4980 0.2228 0.4978 0.131 Uiso 0.74(10) 1 calc PR A 2

C19 C 0.327(2) 0.2277(16) 0.5197(8) 0.218(19) Uani 1 1 d . A .

H19A H 0.2653 0.2343 0.5195 0.326 Uiso 1 1 calc R . .

H19B H 0.3484 0.2255 0.5423 0.326 Uiso 1 1 calc R . .

H19C H 0.3402 0.1870 0.5084 0.326 Uiso 1 1 calc R . .

C20 C 0.0024(11) 0.1245(10) 0.3037(5) 0.080(7) Uani 1 1 d . . .

H20A H -0.0334 0.1362 0.3221 0.121 Uiso 1 1 calc R . .

H20B H 0.0062 0.0770 0.3021 0.121 Uiso 1 1 calc R . .

H20C H -0.0227 0.1422 0.2835 0.121 Uiso 1 1 calc R . .

C21 C 0.0921(11) 0.1532(9) 0.3093(5) 0.052(5) Uani 1 1 d . . .

C22 C 0.1540(11) 0.1430(7) 0.2863(4) 0.043(5) Uani 1 1 d . . .

H22A H 0.1400 0.1188 0.2672 0.051 Uiso 1 1 calc R . .

C23 C 0.2379(10) 0.1678(7) 0.2906(4) 0.028(4) Uani 1 1 d . . .

C24 C 0.2547(11) 0.2067(7) 0.3185(4) 0.039(4) Uani 1 1 d . . .

C25 C 0.1895(10) 0.2167(8) 0.3419(4) 0.038(4) Uani 1 1 d . . .

C26 C 0.1088(11) 0.1866(8) 0.3355(4) 0.049(5) Uani 1 1 d . . .

H26A H 0.0656 0.1913 0.3511 0.058 Uiso 1 1 calc R . .

C27 C 0.2044(11) 0.2521(8) 0.3736(4) 0.051(5) Uani 1 1 d . . .

H27A H 0.1503 0.2545 0.3854 0.061 Uiso 1 1 calc R . .

H27B H 0.2457 0.2274 0.3872 0.061 Uiso 1 1 calc R . .

C28 C 0.1753(10) 0.3554(8) 0.3475(4) 0.048(5) Uani 1 1 d . . .

H28A H 0.1690 0.3323 0.3265 0.057 Uiso 1 1 calc R . .

H28B H 0.2015 0.3982 0.3429 0.057 Uiso 1 1 calc R . .

C29 C 0.0877(12) 0.3678(10) 0.3600(5) 0.091(7) Uani 1 1 d . . .

H29D H 0.0541 0.3916 0.3435 0.136 Uiso 1 1 calc R . .

H29E H 0.0918 0.3938 0.3800 0.136 Uiso 1 1 calc R . .

H29F H 0.0600 0.3262 0.3646 0.136 Uiso 1 1 calc R . .

C30 C 0.2514(12) 0.3489(9) 0.3997(5) 0.063(6) Uani 1 1 d . . .

H30C H 0.2809 0.3180 0.4146 0.075 Uiso 1 1 calc R . .

H30D H 0.1961 0.3602 0.4092 0.075 Uiso 1 1 calc R . .

C31 C 0.3051(13) 0.4105(9) 0.3964(5) 0.064(6) Uani 1 1 d . . .

H31A H 0.2743 0.4424 0.3824 0.077 Uiso 1 1 calc R . .

H31B H 0.3147 0.4304 0.4181 0.077 Uiso 1 1 calc R . .

C32 C 0.4214(12) 0.4523(8) 0.3649(5) 0.073(6) Uani 1 1 d . . .

H32A H 0.4314 0.4875 0.3806 0.109 Uiso 1 1 calc R . .

H32B H 0.3799 0.4666 0.3482 0.109 Uiso 1 1 calc R . .

H32C H 0.4750 0.4411 0.3545 0.109 Uiso 1 1 calc R . .

C33 C 0.4468(11) 0.3783(8) 0.4096(4) 0.053(5) Uani 1 1 d . . .

H33A H 0.4567 0.4172 0.4230 0.079 Uiso 1 1 calc R . .

H33B H 0.5010 0.3627 0.4013 0.079 Uiso 1 1 calc R . .

H33C H 0.4212 0.3442 0.4229 0.079 Uiso 1 1 calc R . .

C34 C 0.2931(13) 0.1574(8) 0.2661(4) 0.049(5) Uani 1 1 d . . .

H34B H 0.2707 0.1337 0.2480 0.059 Uiso 1 1 calc R . .

C35 C 0.4177(12) 0.1547(8) 0.2352(4) 0.055(5) Uani 1 1 d . A .

H35A H 0.4452 0.1930 0.2253 0.066 Uiso 1 1 calc R . .

H35B H 0.3766 0.1366 0.2190 0.066 Uiso 1 1 calc R . .

C36 C 0.4849(11) 0.1038(8) 0.2431(4) 0.055(5) Uani 1 1 d . . .

H36A H 0.5280 0.1043 0.2259 0.067 Uiso 1 1 calc R A .

H36B H 0.5140 0.1155 0.2640 0.067 Uiso 1 1 calc R . .

C37 C 0.4511(13) 0.0391(9) 0.2457(4) 0.075(7) Uani 1 1 d . A .

H37A H 0.3951 0.0409 0.2561 0.090 Uiso 1 1 calc R . .

H37B H 0.4897 0.0123 0.2596 0.090 Uiso 1 1 calc R . .

C38 C 0.399(5) -0.072(4) 0.224(4) 0.086(11) Uiso 0.26(10) 1 d PDU A 1

H38A H 0.3865 -0.1047 0.2068 0.129 Uiso 0.26(10) 1 calc PR A 1

H38B H 0.3476 -0.0618 0.2354 0.129 Uiso 0.26(10) 1 calc PR A 1

H38C H 0.4425 -0.0892 0.2389 0.129 Uiso 0.26(10) 1 calc PR A 1

C38' C 0.4041(7) -0.0807(5) 0.2137(3) 0.086(10) Uiso 0.74(10) 1 d PDU A 2

H38D H 0.3960 -0.1051 0.1933 0.129 Uiso 0.74(10) 1 calc PR A 2

H38E H 0.3501 -0.0788 0.2251 0.129 Uiso 0.74(10) 1 calc PR A 2

H38F H 0.4470 -0.1026 0.2275 0.129 Uiso 0.74(10) 1 calc PR A 2

C39 C 0.8262(7) 0.1423(5) 0.4073(3) 0.034(4) Uani 1 1 d R . .

C40 C 0.9241(7) 0.1389(5) 0.4130(3) 0.061(6) Uani 1 1 d R . .

H40A H 0.9418 0.1734 0.4274 0.091 Uiso 1 1 d R . .

H40B H 0.9518 0.1435 0.3926 0.091 Uiso 1 1 d R . .

H40C H 0.9390 0.0978 0.4226 0.091 Uiso 1 1 d R . .

C41 C 0.4921(10) 0.1161(6) 0.3390(3) 0.023(3) Uani 1 1 d U . .

C42 C 0.4097(9) 0.0832(6) 0.3336(3) 0.026(3) Uani 1 1 d U . .

H42A H 0.4105 0.0409 0.3446 0.040 Uiso 1 1 calc R . .

H42B H 0.3994 0.0768 0.3102 0.040 Uiso 1 1 calc R . .

H42C H 0.3642 0.1102 0.3424 0.040 Uiso 1 1 calc R . .

C43 C 0.6102(12) 0.2564(8) 0.2750(4) 0.046(5) Uani 1 1 d . . .

C44 C 0.6697(11) 0.2679(10) 0.2474(4) 0.075(7) Uani 1 1 d . . .

H44A H 0.7278 0.2732 0.2561 0.112 Uiso 1 1 calc R . .

H44B H 0.6526 0.3074 0.2356 0.112 Uiso 1 1 calc R . .

H44C H 0.6676 0.2307 0.2325 0.112 Uiso 1 1 calc R . .

C45 C 0.3494(12) 0.3678(8) 0.2846(5) 0.042(5) Uani 1 1 d . . .

C46 C 0.3331(13) 0.4263(8) 0.2625(5) 0.076(7) Uani 1 1 d . . .

H46D H 0.3084 0.4617 0.2752 0.115 Uiso 1 1 calc R . .

H46E H 0.2934 0.4139 0.2448 0.115 Uiso 1 1 calc R . .

H46F H 0.3868 0.4408 0.2533 0.115 Uiso 1 1 calc R . .

C47 C 0.4617(14) 0.2222(7) 0.4014(4) 0.044(5) Uani 1 1 d . . .

C48 C 0.4446(10) 0.1760(8) 0.4287(4) 0.044(5) Uani 1 1 d . . .

H48A H 0.4986 0.1587 0.4374 0.066 Uiso 1 1 calc R . .

H48B H 0.4091 0.1401 0.4206 0.066 Uiso 1 1 calc R . .

H48C H 0.4150 0.1991 0.4460 0.066 Uiso 1 1 calc R . .

C49 C 0.6766(12) 0.3450(8) 0.3866(5) 0.050(5) Uani 1 1 d . . .

C50 C 0.7064(14) 0.4118(9) 0.3909(5) 0.090(8) Uani 1 1 d . . .

H50D H 0.7352 0.4162 0.4122 0.135 Uiso 1 1 calc R . .

H50E H 0.6578 0.4416 0.3896 0.135 Uiso 1 1 calc R . .

H50F H 0.7462 0.4225 0.3736 0.135 Uiso 1 1 calc R . .

C51 C -0.1099(11) 0.5600(7) -0.0208(4) 0.048(5) Uani 1 1 d . . .

H51A H -0.1210 0.5426 -0.0427 0.072 Uiso 1 1 calc R . .

H51B H -0.0528 0.5791 -0.0197 0.072 Uiso 1 1 calc R . .

H51C H -0.1521 0.5936 -0.0161 0.072 Uiso 1 1 calc R . .

C52 C -0.1161(10) 0.5048(8) 0.0044(4) 0.038(5) Uani 1 1 d . . .

C53 C -0.1375(10) 0.4434(9) -0.0026(4) 0.045(5) Uani 1 1 d . . .

H53A H -0.1532 0.4344 -0.0246 0.055 Uiso 1 1 calc R . .

C54 C -0.1392(9) 0.3920(7) 0.0185(4) 0.031(4) Uani 1 1 d . . .

C55 C -0.1285(8) 0.4060(7) 0.0526(4) 0.024(4) Uani 1 1 d . . .

C56 C -0.1083(9) 0.4710(7) 0.0615(3) 0.025(4) Uani 1 1 d . . .

C57 C -0.1039(9) 0.5183(7) 0.0378(4) 0.037(4) Uani 1 1 d . . .

H57A H -0.0922 0.5619 0.0442 0.044 Uiso 1 1 calc R . .

C58 C -0.0912(10) 0.4886(7) 0.0971(3) 0.037(4) Uani 1 1 d . . .

H58A H -0.0412 0.4639 0.1053 0.044 Uiso 1 1 calc R . .

H58B H -0.0774 0.5356 0.0986 0.044 Uiso 1 1 calc R . .

C59 C -0.2423(10) 0.5070(7) 0.1044(4) 0.037(4) Uani 1 1 d . . .

H59A H -0.2902 0.4954 0.1185 0.045 Uiso 1 1 calc R . .

H59B H -0.2551 0.4889 0.0825 0.045 Uiso 1 1 calc R . .

C60 C -0.2387(10) 0.5807(7) 0.1017(4) 0.044(5) Uani 1 1 d . . .

H60D H -0.2929 0.5969 0.0927 0.066 Uiso 1 1 calc R . .

H60E H -0.1926 0.5932 0.0873 0.066 Uiso 1 1 calc R . .

H60F H -0.2282 0.5996 0.1233 0.066 Uiso 1 1 calc R . .

C61 C -0.1459(10) 0.4951(7) 0.1514(4) 0.037(4) Uani 1 1 d . . .

H61A H -0.1468 0.5432 0.1528 0.044 Uiso 1 1 calc R . .

H61B H -0.0885 0.4800 0.1583 0.044 Uiso 1 1 calc R . .

C62 C -0.2110(10) 0.4673(8) 0.1740(4) 0.038(4) Uani 1 1 d . . .

H62A H -0.1951 0.4786 0.1968 0.045 Uiso 1 1 calc R . .

H62B H -0.2672 0.4869 0.1689 0.045 Uiso 1 1 calc R . .

C63 C -0.3055(10) 0.3739(9) 0.1762(4) 0.053(5) Uani 1 1 d . . .

H63A H -0.3220 0.3851 0.1983 0.080 Uiso 1 1 calc R . .

H63B H -0.3091 0.3266 0.1732 0.080 Uiso 1 1 calc R . .

H63C H -0.3439 0.3955 0.1604 0.080 Uiso 1 1 calc R . .

C64 C -0.1615(10) 0.3615(8) 0.1954(4) 0.049(5) Uani 1 1 d . . .

H64A H -0.1800 0.3721 0.2174 0.073 Uiso 1 1 calc R . .

H64B H -0.1024 0.3754 0.1930 0.073 Uiso 1 1 calc R . .

H64C H -0.1656 0.3143 0.1920 0.073 Uiso 1 1 calc R . .

C65 C -0.1525(9) 0.3267(7) 0.0061(4) 0.029(4) Uani 1 1 d . . .

H65B H -0.1614 0.3229 -0.0168 0.035 Uiso 1 1 calc R . .

C66 C -0.1549(12) 0.2167(9) 0.0006(4) 0.059(6) Uani 1 1 d . B .

H66A H -0.1732 0.2298 -0.0217 0.071 Uiso 1 1 calc R . .

H66B H -0.1967 0.1848 0.0087 0.071 Uiso 1 1 calc R . .

C67 C -0.0698(14) 0.1853(10) -0.0006(5) 0.078(7) Uani 1 1 d D . .

H67A H -0.0449 0.1824 0.0217 0.094 Uiso 0.37(3) 1 calc PR B 1

H67B H -0.0760 0.1405 -0.0092 0.094 Uiso 0.37(3) 1 calc PR B 1

H67C H -0.0447 0.1829 0.0211 0.094 Uiso 0.63(3) 1 d PR B 2

H67D H -0.0767 0.1412 -0.0087 0.094 Uiso 0.63(3) 1 d PR B 2

C68 C -0.012(3) 0.223(5) -0.022(3) 0.107(9) Uiso 0.37(3) 1 d PDU B 1

H68A H -0.0114 0.2690 -0.0148 0.128 Uiso 0.37(3) 1 calc PR B 1

H68B H -0.0325 0.2206 -0.0445 0.128 Uiso 0.37(3) 1 calc PR B 1

C68' C -0.012(2) 0.223(3) -0.022(2) 0.107(8) Uiso 0.63(3) 1 d PDU B 2

H68C H -0.0114 0.2690 -0.0148 0.128 Uiso 0.63(3) 1 calc PR B 2

H68D H -0.0325 0.2206 -0.0445 0.128 Uiso 0.63(3) 1 calc PR B 2

C69' C 0.083(3) 0.1035(12) -0.0347(10) 0.054(17) Uiso 0.37(3) 1 d PD B 1

H69A H 0.0556 0.0769 -0.0182 0.081 Uiso 0.37(3) 1 calc PR B 1

H69B H 0.1381 0.0840 -0.0400 0.081 Uiso 0.37(3) 1 calc PR B 1

H69C H 0.0469 0.1054 -0.0544 0.081 Uiso 0.37(3) 1 calc PR B 1

C69 C 0.1561(9) 0.2620(8) -0.0357(4) 0.20(3) Uiso 0.63(3) 1 d PD B 2

H69D H 0.1540 0.2980 -0.0201 0.307 Uiso 0.63(3) 1 calc PR B 2

H69E H 0.1275 0.2750 -0.0562 0.307 Uiso 0.63(3) 1 calc PR B 2

H69F H 0.2156 0.2512 -0.0399 0.307 Uiso 0.63(3) 1 calc PR B 2

C70 C 0.4929(9) 0.3140(8) 0.1753(4) 0.062(6) Uani 1 1 d R . .

H70D H 0.4963 0.3333 0.1966 0.093 Uiso 1 1 d R . .

H70E H 0.5034 0.3466 0.1591 0.093 Uiso 1 1 d R . .

H70F H 0.5346 0.2800 0.1738 0.093 Uiso 1 1 d R . .

C71 C 0.4047(11) 0.2851(7) 0.1694(4) 0.039(4) Uani 1 1 d . . .

C72 C 0.3459(11) 0.2869(7) 0.1937(4) 0.041(4) Uani 1 1 d . . .

H72B H 0.3610 0.3048 0.2144 0.049 Uiso 1 1 calc R . .

C73 C 0.2638(9) 0.2622(7) 0.1881(4) 0.031(4) Uani 1 1 d . . .

C74 C 0.2402(10) 0.2344(7) 0.1591(4) 0.028(4) Uani 1 1 d . . .

C75 C 0.3010(10) 0.2303(7) 0.1342(4) 0.036(4) Uani 1 1 d . . .

C76 C 0.3812(10) 0.2550(7) 0.1410(4) 0.039(4) Uani 1 1 d . . .

H76B H 0.4229 0.2508 0.1247 0.047 Uiso 1 1 calc R . .

C77 C 0.2806(10) 0.2019(8) 0.1004(4) 0.046(5) Uani 1 1 d . . .

H77C H 0.2384 0.2302 0.0890 0.055 Uiso 1 1 calc R . .

H77D H 0.3329 0.2020 0.0874 0.055 Uiso 1 1 calc R . .

C78 C 0.3082(10) 0.0932(8) 0.1198(4) 0.051(5) Uani 1 1 d . . .

H78A H 0.2822 0.0496 0.1220 0.061 Uiso 1 1 calc R . .

H78B H 0.3158 0.1111 0.1421 0.061 Uiso 1 1 calc R . .

C79 C 0.3958(11) 0.0847(9) 0.1055(5) 0.075(7) Uani 1 1 d . . .

H79A H 0.4301 0.0557 0.1195 0.113 Uiso 1 1 calc R . .

H79B H 0.4238 0.1272 0.1040 0.113 Uiso 1 1 calc R . .

H79C H 0.3899 0.0656 0.0836 0.113 Uiso 1 1 calc R . .

C80 C 0.2264(12) 0.1100(8) 0.0685(4) 0.061(6) Uani 1 1 d . . .

H80A H 0.2797 0.0996 0.0572 0.073 Uiso 1 1 calc R . .

H80B H 0.1956 0.1437 0.0557 0.073 Uiso 1 1 calc R . .

C81 C 0.1725(12) 0.0500(8) 0.0704(4) 0.056(5) Uani 1 1 d . . .

H81C H 0.1595 0.0336 0.0482 0.067 Uiso 1 1 calc R . .

H81D H 0.2040 0.0156 0.0825 0.067 Uiso 1 1 calc R . .

C82 C 0.0296(11) 0.0880(8) 0.0627(4) 0.052(5) Uani 1 1 d . . .

H82D H 0.0168 0.0534 0.0469 0.078 Uiso 1 1 calc R . .

H82E H 0.0518 0.1261 0.0513 0.078 Uiso 1 1 calc R . .

H82F H -0.0225 0.1001 0.0739 0.078 Uiso 1 1 calc R . .

C83 C 0.0608(12) 0.0046(8) 0.1022(4) 0.061(6) Uani 1 1 d . . .

H83D H 0.0486 -0.0281 0.0854 0.091 Uiso 1 1 calc R . .

H83E H 0.0085 0.0148 0.1137 0.091 Uiso 1 1 calc R . .

H83F H 0.1035 -0.0124 0.1177 0.091 Uiso 1 1 calc R . .

C84 C 0.2064(12) 0.2700(7) 0.2160(4) 0.043(5) Uani 1 1 d . . .

H84A H 0.2315 0.2882 0.2351 0.051 Uiso 1 1 calc R . .

C85 C 0.0860(10) 0.2715(8) 0.2483(4) 0.039(4) Uani 1 1 d . B .

H85C H 0.1297 0.2749 0.2660 0.047 Uiso 1 1 calc R . .

H85D H 0.0465 0.2359 0.2540 0.047 Uiso 1 1 calc R . .

C86 C 0.0371(11) 0.3350(8) 0.2458(4) 0.049(5) Uani 1 1 d D . .

H86A H 0.0090 0.3382 0.2240 0.059 Uiso 0.37(3) 1 calc PR B 1

H86B H -0.0077 0.3357 0.2624 0.059 Uiso 0.37(3) 1 calc PR B 1

H86C H -0.0030 0.3334 0.2275 0.059 Uiso 0.63(3) 1 d PR B 2

H86D H 0.0055 0.3416 0.2655 0.059 Uiso 0.63(3) 1 d PR B 2

C87 C 0.095(2) 0.3924(12) 0.251(3) 0.091(12) Uiso 0.37(3) 1 d PDU B 1

H87A H 0.1476 0.3843 0.2386 0.109 Uiso 0.37(3) 1 calc PR B 1

H87B H 0.1123 0.3935 0.2743 0.109 Uiso 0.37(3) 1 calc PR B 1

C87' C 0.0986(17) 0.3906(10) 0.2426(15) 0.090(11) Uiso 0.63(3) 1 d PDU B 2

H87C H 0.1322 0.3828 0.2229 0.109 Uiso 0.63(3) 1 calc PR B 2

H87D H 0.1387 0.3890 0.2615 0.109 Uiso 0.63(3) 1 calc PR B 2

C88 C 0.0171(14) 0.4884(13) 0.2806(5) 0.125(10) Uani 1 1 d . B .

H88A H -0.0089 0.5318 0.2810 0.188 Uiso 1 1 calc R . .

H88B H 0.0645 0.4866 0.2965 0.188 Uiso 1 1 calc R . .

H88C H -0.0254 0.4556 0.2861 0.188 Uiso 1 1 calc R . .

C89 C 0.1531(11) 0.0756(8) 0.1863(5) 0.039(5) Uani 1 1 d . . .

C90 C 0.2019(11) 0.0201(7) 0.2059(4) 0.054(5) Uani 1 1 d . . .

H90D H 0.2231 -0.0124 0.1906 0.082 Uiso 1 1 calc R . .

H90E H 0.1630 -0.0008 0.2210 0.082 Uiso 1 1 calc R . .

H90F H 0.2499 0.0392 0.2182 0.082 Uiso 1 1 calc R . .

C91 C -0.1105(12) 0.1734(8) 0.2050(4) 0.047(5) Uani 1 1 d D . .

C92 C -0.162(3) 0.164(2) 0.2360(7) 0.041(8) Uiso 0.37(3) 1 d PDU B 1

H92A H -0.1588 0.2040 0.2491 0.061 Uiso 0.37(3) 1 calc PR B 1

H92B H -0.1378 0.1278 0.2487 0.061 Uiso 0.37(3) 1 calc PR B 1

H92C H -0.2211 0.1547 0.2300 0.061 Uiso 0.37(3) 1 calc PR B 1

C92' C -0.1669(15) 0.1362(13) 0.2286(6) 0.038(7) Uiso 0.63(3) 1 d PDU B 2

H92D H -0.1785 0.0925 0.2200 0.057 Uiso 0.63(3) 1 calc PR B 2

H92E H -0.2206 0.1596 0.2311 0.057 Uiso 0.63(3) 1 calc PR B 2

H92F H -0.1376 0.1326 0.2498 0.057 Uiso 0.63(3) 1 calc PR B 2

C93 C 0.0033(9) 0.3330(8) 0.1490(3) 0.024(4) Uani 1 1 d . . .

C94 C 0.0915(10) 0.3631(7) 0.1548(4) 0.046(5) Uani 1 1 d . . .

H94D H 0.0914 0.4081 0.1469 0.069 Uiso 1 1 calc R . .

H94E H 0.1339 0.3378 0.1431 0.069 Uiso 1 1 calc R . .

H94F H 0.1056 0.3625 0.1782 0.069 Uiso 1 1 calc R . .

C95 C -0.3321(10) 0.3363(8) 0.0827(4) 0.034(4) Uani 1 1 d . . .

C96 C -0.4277(9) 0.3422(9) 0.0775(4) 0.052(5) Uani 1 1 d . . .

H96A H -0.4497 0.3758 0.0921 0.078 Uiso 1 1 calc R . .

H96B H -0.4547 0.3004 0.0824 0.078 Uiso 1 1 calc R . .

H96C H -0.4405 0.3543 0.0549 0.078 Uiso 1 1 calc R . .

C97 C -0.1905(13) 0.1264(9) 0.0854(6) 0.064(6) Uani 1 1 d . . .

C98 C -0.2235(14) 0.0618(8) 0.0751(5) 0.091(8) Uani 1 1 d . . .

H98D H -0.2512 0.0655 0.0535 0.136 Uiso 1 1 calc R . .

H98E H -0.2648 0.0463 0.0908 0.136 Uiso 1 1 calc R . .

H98F H -0.1762 0.0308 0.0740 0.136 Uiso 1 1 calc R . .

C99 C 0.0295(12) 0.2451(8) 0.0794(4) 0.037(4) Uani 1 1 d . . .

C100 C 0.0456(9) 0.2992(8) 0.0571(4) 0.041(4) Uani 1 1 d . . .

H100 H 0.1064 0.3010 0.0524 0.061 Uiso 1 1 calc R . .

H101 H 0.0282 0.3402 0.0672 0.061 Uiso 1 1 calc R . .

H102 H 0.0129 0.2927 0.0367 0.061 Uiso 1 1 calc R . .

O1S O -0.3148(10) 0.1996(8) 0.1603(4) 0.112(5) Uani 1 1 d D . .

H1S H -0.2544 0.2028 0.1533 0.134 Uiso 0.24(3) 1 d PR C 1

H1S' H -0.2711 0.2238 0.1478 0.134 Uiso 0.76(3) 1 d PR C 2

C1S C -0.296(8) 0.133(2) 0.167(3) 0.120(14) Uiso 0.24(3) 1 d PDU C 1

H1SA H -0.2461 0.1305 0.1823 0.181 Uiso 0.24(3) 1 calc PR C 1

H1SB H -0.2828 0.1099 0.1472 0.181 Uiso 0.24(3) 1 calc PR C 1

H1SC H -0.3445 0.1122 0.1776 0.181 Uiso 0.24(3) 1 calc PR C 1

C1S' C -0.367(2) 0.1475(15) 0.1479(8) 0.119(13) Uiso 0.76(3) 1 d PDU C 2

H1SD H -0.4116 0.1653 0.1335 0.179 Uiso 0.76(3) 1 calc PR C 2

H1SE H -0.3928 0.1245 0.1661 0.179 Uiso 0.76(3) 1 calc PR C 2

H1SF H -0.3317 0.1171 0.1357 0.179 Uiso 0.76(3) 1 calc PR C 2

O1W O 0.181(3) 0.5298(15) 0.3423(8) 0.074(6) Uiso 0.47(5) 1 d PU D 1

O1W' O 0.135(3) 0.5250(13) 0.3469(7) 0.074(6) Uiso 0.53(5) 1 d PU D 2

O2W O 0.844(3) 0.308(2) 0.3175(9) 0.066(5) Uiso 0.308(17) 1 d PU E 1

O2W' O 0.8079(12) 0.2563(9) 0.3213(4) 0.066(5) Uiso 0.692(17) 1 d PU E 2

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Ni1 0.0194(11) 0.0318(11) 0.0256(12) -0.0012(9) -0.0034(9) -0.0013(9)

Ni2 0.0260(12) 0.0339(11) 0.0374(13) -0.0052(10) -0.0088(10) -0.0031(10)

Ni3 0.0252(12) 0.0285(11) 0.0377(13) 0.0054(10) -0.0004(10) -0.0019(10)

Ni4 0.0342(13) 0.0319(12) 0.0427(14) 0.0052(10) 0.0005(11) 0.0070(10)

Ni5 0.0278(12) 0.0336(11) 0.0324(13) 0.0064(10) -0.0018(10) 0.0038(10)

Ni6 0.0188(12) 0.0344(11) 0.0334(13) 0.0061(10) -0.0028(9) 0.0018(10)

Ni7 0.0243(12) 0.0334(11) 0.0370(13) 0.0073(10) -0.0066(10) -0.0031(10)

Ni8 0.0243(12) 0.0332(11) 0.0409(14) 0.0123(10) -0.0049(10) -0.0030(10)

Ni9 0.0295(13) 0.0328(12) 0.0472(14) 0.0107(11) -0.0035(11) 0.0072(10)

Ni10 0.0247(12) 0.0395(12) 0.0390(14) 0.0158(11) -0.0046(10) 0.0015(10)

S1 0.117(7) 0.165(8) 0.194(9) -0.014(7) 0.006(6) 0.048(6)

S2 0.068(4) 0.105(5) 0.097(5) -0.046(4) -0.015(4) 0.018(4)

S3 0.092(6) 0.168(7) 0.121(6) -0.014(5) 0.004(5) 0.040(5)

S4 0.142(7) 0.101(5) 0.135(7) 0.019(5) 0.006(6) 0.008(5)

O1 0.016(6) 0.042(6) 0.023(6) -0.001(5) 0.001(5) -0.005(5)

O2 0.003(5) 0.031(6) 0.038(6) 0.006(5) -0.008(4) -0.004(4)

O3 0.016(6) 0.039(6) 0.040(7) -0.003(5) -0.006(5) -0.005(5)

O4 0.018(6) 0.060(8) 0.045(7) -0.010(6) -0.007(5) -0.009(6)

O5 0.024(6) 0.032(6) 0.032(6) 0.003(5) -0.006(5) 0.002(5)

O6 0.027(6) 0.036(6) 0.018(6) 0.010(5) -0.005(5) -0.004(5)

O7 0.031(7) 0.053(7) 0.043(8) 0.025(6) -0.003(6) 0.002(6)

O8 0.037(8) 0.053(7) 0.026(6) -0.002(5) 0.006(5) -0.005(6)

O9 0.034(7) 0.035(6) 0.024(6) 0.003(5) -0.004(5) 0.016(6)

O10 0.020(6) 0.012(5) 0.048(7) 0.011(5) 0.013(5) 0.001(4)

O11 0.064(9) 0.037(7) 0.029(7) 0.011(6) -0.006(6) 0.003(6)

O12 0.047(8) 0.038(7) 0.050(8) 0.016(6) -0.006(7) 0.005(6)

O13 0.035(7) 0.047(7) 0.032(7) 0.007(5) -0.006(5) 0.017(6)

O14 0.014(6) 0.036(6) 0.048(8) 0.003(5) 0.003(5) -0.005(5)

O15 0.046(8) 0.044(7) 0.058(8) 0.003(6) -0.001(7) -0.004(6)

O16 0.061(9) 0.031(7) 0.064(9) -0.007(7) -0.018(7) -0.026(6)

O17 0.025(6) 0.032(6) 0.039(7) 0.006(6) -0.007(5) -0.003(5)

O18 0.019(6) 0.036(6) 0.038(7) 0.008(5) 0.003(5) 0.004(5)

O19 0.019(6) 0.039(6) 0.050(7) 0.004(6) -0.006(6) 0.009(5)

O20 0.015(6) 0.049(7) 0.045(7) 0.004(6) -0.012(5) -0.004(6)

O21 0.020(6) 0.032(6) 0.047(7) 0.016(5) -0.012(5) 0.004(5)

O22 0.013(6) 0.033(6) 0.047(7) 0.014(6) -0.004(5) 0.002(5)

O23 0.023(7) 0.054(7) 0.053(8) 0.030(6) -0.005(6) -0.009(6)

O24 0.028(7) 0.055(7) 0.043(7) 0.023(6) 0.000(6) -0.007(6)

O25 0.033(7) 0.036(6) 0.030(6) 0.011(5) -0.001(5) 0.012(5)

O26 0.022(6) 0.043(6) 0.064(8) 0.033(6) -0.002(6) -0.009(5)

O27 0.042(8) 0.036(7) 0.041(7) 0.004(6) -0.014(6) 0.014(6)

O28 0.037(8) 0.047(7) 0.057(9) 0.015(7) -0.009(7) 0.003(6)

O29 0.039(7) 0.023(6) 0.041(7) 0.007(5) 0.001(6) 0.007(5)

O30 0.026(7) 0.046(7) 0.040(7) 0.005(6) -0.004(6) -0.004(6)

O31 0.043(8) 0.039(7) 0.054(8) 0.016(6) -0.012(6) -0.017(6)

O32 0.038(8) 0.036(7) 0.069(9) -0.007(7) -0.012(6) -0.005(6)

N1 0.020(8) 0.033(7) 0.031(8) -0.004(6) -0.007(6) 0.011(6)

N2 0.027(9) 0.044(8) 0.046(9) -0.005(7) -0.009(7) 0.026(7)

N3 0.034(9) 0.043(9) 0.037(9) -0.015(8) -0.010(7) 0.019(7)

N4 0.047(10) 0.027(8) 0.060(11) 0.013(8) 0.008(8) 0.003(7)

N5 0.068(12) 0.049(10) 0.049(10) -0.004(8) -0.009(9) 0.015(9)

N6 0.039(10) 0.054(9) 0.016(8) 0.002(7) 0.003(7) 0.008(8)

N7 0.031(9) 0.041(8) 0.033(9) 0.000(7) -0.009(7) 0.010(7)

N8 0.020(8) 0.058(9) 0.029(8) 0.017(7) -0.001(6) -0.001(7)

N9 0.031(8) 0.036(8) 0.032(8) 0.010(7) -0.012(7) 0.003(7)

N10 0.029(8) 0.028(8) 0.059(10) 0.012(7) 0.006(7) 0.000(7)

N11 0.047(11) 0.045(9) 0.079(12) 0.028(9) -0.003(9) 0.008(8)

N12 0.016(8) 0.032(8) 0.055(10) 0.022(7) 0.000(7) 0.001(7)

C1 0.075(16) 0.094(16) 0.056(14) 0.022(12) -0.009(12) -0.003(13)

C2 0.038(12) 0.114(18) 0.016(11) 0.015(12) 0.002(9) 0.008(12)

C3 0.030(10) 0.044(11) 0.029(11) -0.006(9) 0.000(8) 0.013(9)

C4 0.011(9) 0.042(10) 0.048(12) 0.008(10) -0.008(8) -0.002(8)

C5 0.021(9) 0.044(11) 0.016(10) -0.011(8) 0.002(7) 0.015(8)

C6 0.015(9) 0.042(10) 0.021(10) 0.007(8) 0.007(7) -0.005(8)

C7 0.024(10) 0.046(11) 0.060(14) 0.012(10) 0.000(9) 0.008(9)

C8 0.046(12) 0.018(8) 0.034(11) 0.003(8) 0.006(9) 0.004(8)

C9 0.031(10) 0.043(10) 0.027(10) -0.006(8) -0.001(8) -0.002(8)

C10 0.040(12) 0.042(11) 0.067(13) -0.013(10) -0.017(10) 0.023(9)

C11 0.029(10) 0.041(10) 0.036(11) 0.001(9) -0.012(9) 0.022(8)

C12 0.035(11) 0.039(10) 0.028(10) -0.010(8) -0.006(8) 0.022(9)

C13 0.040(11) 0.041(10) 0.044(11) 0.015(9) 0.007(9) 0.014(9)

C14 0.012(10) 0.099(15) 0.054(12) 0.002(11) 0.020(8) 0.004(10)

C15 0.013(9) 0.057(12) 0.028(10) -0.017(9) -0.005(8) 0.009(9)

C16 0.076(17) 0.073(15) 0.074(16) -0.013(12) -0.024(13) 0.010(13)

C17 0.12(2) 0.097(18) 0.093(19) -0.023(15) -0.044(17) 0.028(17)

C19 0.20(4) 0.23(4) 0.22(4) 0.02(3) 0.08(3) -0.14(3)

C20 0.043(13) 0.104(17) 0.094(17) 0.022(14) -0.002(12) -0.024(13)

C21 0.027(12) 0.073(14) 0.056(15) 0.023(12) -0.009(11) -0.005(11)

C22 0.045(12) 0.028(9) 0.054(13) 0.016(9) -0.029(11) -0.008(9)

C23 0.027(10) 0.032(9) 0.026(10) 0.003(8) -0.013(9) 0.002(8)

C24 0.039(12) 0.029(9) 0.048(12) 0.019(9) 0.008(10) 0.018(9)

C25 0.018(10) 0.049(11) 0.046(12) 0.015(9) -0.014(9) 0.008(9)

C26 0.046(13) 0.062(12) 0.039(12) 0.024(10) 0.014(10) -0.006(10)

C27 0.030(11) 0.057(12) 0.066(14) 0.029(11) 0.006(10) 0.003(9)

C28 0.037(12) 0.051(11) 0.055(12) 0.019(10) 0.000(9) 0.020(10)

C29 0.048(15) 0.121(19) 0.102(18) -0.005(15) -0.014(13) 0.030(14)

C30 0.043(13) 0.066(14) 0.080(16) 0.000(12) 0.010(11) 0.029(11)

C31 0.067(15) 0.059(13) 0.068(15) -0.030(11) 0.007(12) 0.028(12)

C32 0.064(15) 0.043(12) 0.111(18) -0.013(12) -0.008(13) -0.018(11)

C33 0.050(13) 0.044(11) 0.062(13) -0.022(10) -0.007(10) 0.004(10)

C34 0.052(14) 0.050(11) 0.044(13) 0.008(10) -0.018(11) -0.005(11)

C35 0.069(14) 0.052(11) 0.042(12) 0.010(10) -0.021(11) -0.009(11)

C36 0.049(13) 0.049(12) 0.067(14) 0.015(10) -0.023(10) 0.016(10)

C37 0.078(16) 0.066(14) 0.079(16) -0.027(12) -0.022(13) 0.031(13)

C39 0.015(9) 0.037(10) 0.048(12) 0.012(9) -0.010(8) 0.005(9)

C40 0.027(11) 0.077(13) 0.077(14) -0.027(11) -0.018(10) 0.016(10)

C41 0.038(8) 0.009(6) 0.023(7) -0.003(6) 0.011(6) 0.002(5)

C42 0.037(7) 0.015(6) 0.028(7) 0.002(6) 0.010(6) 0.002(5)

C43 0.038(12) 0.068(13) 0.032(12) 0.014(10) 0.006(10) -0.016(10)

C44 0.034(12) 0.14(2) 0.049(13) 0.013(13) 0.003(10) 0.019(13)

C45 0.054(13) 0.034(11) 0.038(12) 0.010(10) -0.013(10) -0.006(10)

C46 0.083(17) 0.063(13) 0.082(16) 0.016(12) -0.032(13) 0.008(12)

C47 0.085(17) 0.030(10) 0.016(10) 0.000(8) -0.007(11) 0.013(11)

C48 0.041(11) 0.056(11) 0.035(11) 0.001(9) -0.007(9) 0.013(9)

C49 0.046(13) 0.029(11) 0.075(16) -0.006(11) 0.001(12) -0.019(10)

C50 0.11(2) 0.074(15) 0.089(17) 0.008(13) -0.041(15) -0.033(14)

C51 0.057(13) 0.047(10) 0.040(11) 0.034(9) -0.007(9) -0.008(10)

C52 0.025(10) 0.042(11) 0.046(13) 0.022(9) -0.011(9) -0.013(8)

C53 0.031(11) 0.069(13) 0.037(11) 0.023(10) -0.013(9) -0.003(10)

C54 0.014(9) 0.045(11) 0.034(11) 0.009(9) -0.006(8) -0.006(8)

C55 0.005(8) 0.030(9) 0.037(11) 0.008(9) 0.003(7) 0.007(7)

C56 0.015(9) 0.039(10) 0.021(9) 0.007(8) 0.004(7) -0.009(7)

C57 0.027(10) 0.033(9) 0.049(12) 0.011(9) -0.005(9) -0.007(8)

C58 0.029(10) 0.046(10) 0.035(11) 0.004(9) -0.019(9) 0.006(9)

C59 0.033(10) 0.052(11) 0.026(10) 0.011(8) 0.000(8) 0.007(9)

C60 0.045(12) 0.048(11) 0.038(11) 0.013(9) -0.010(9) 0.021(9)

C61 0.050(12) 0.025(9) 0.036(11) 0.016(8) -0.013(9) 0.009(8)

C62 0.027(10) 0.061(12) 0.025(10) 0.006(9) 0.002(8) 0.009(9)

C63 0.032(11) 0.087(14) 0.041(12) 0.008(10) -0.001(9) -0.005(11)

C64 0.046(12) 0.072(12) 0.028(10) 0.010(9) -0.004(9) 0.016(10)

C65 0.028(10) 0.040(10) 0.018(9) -0.005(8) -0.020(8) 0.004(8)

C66 0.056(14) 0.061(13) 0.058(13) 0.001(11) -0.013(11) 0.024(11)

C67 0.079(17) 0.085(15) 0.069(15) 0.007(13) -0.009(13) 0.004(14)

C70 0.009(10) 0.074(13) 0.103(16) 0.028(12) -0.006(10) -0.010(9)

C71 0.034(11) 0.040(10) 0.043(12) 0.019(9) -0.013(10) 0.006(9)

C72 0.044(12) 0.044(11) 0.035(11) 0.018(9) 0.002(10) 0.009(10)

C73 0.016(10) 0.025(9) 0.053(12) 0.006(9) -0.017(9) 0.009(8)

C74 0.021(10) 0.026(9) 0.035(11) 0.009(8) -0.001(9) 0.003(8)

C75 0.026(11) 0.041(10) 0.040(11) 0.001(9) -0.009(9) 0.004(8)

C76 0.021(10) 0.043(10) 0.054(12) 0.024(10) 0.003(9) 0.001(8)

C77 0.026(10) 0.057(12) 0.054(12) 0.016(10) -0.003(9) 0.017(9)

C78 0.031(11) 0.048(11) 0.074(14) -0.006(10) 0.000(10) 0.020(9)

C79 0.033(12) 0.066(13) 0.126(19) 0.016(13) 0.000(12) 0.034(11)

C80 0.060(14) 0.055(12) 0.068(15) -0.002(11) 0.010(11) -0.008(11)

C81 0.059(14) 0.040(11) 0.068(14) -0.014(10) -0.006(11) -0.006(11)

C82 0.045(12) 0.060(12) 0.051(12) -0.002(10) -0.015(10) 0.005(10)

C83 0.074(15) 0.051(12) 0.057(13) 0.008(10) -0.005(11) -0.002(11)

C84 0.054(14) 0.039(10) 0.034(11) 0.007(9) -0.014(10) 0.003(10)

C85 0.031(10) 0.053(11) 0.032(11) -0.007(9) 0.002(9) -0.009(9)

C86 0.042(12) 0.059(12) 0.047(12) 0.006(10) 0.005(9) 0.004(10)

C88 0.069(18) 0.21(3) 0.10(2) -0.001(19) 0.067(15) 0.050(19)

C89 0.036(12) 0.036(11) 0.044(13) 0.010(10) -0.009(10) -0.011(9)

C90 0.050(12) 0.043(10) 0.069(13) 0.015(10) -0.013(10) 0.026(10)

C91 0.039(13) 0.064(12) 0.036(12) -0.001(10) -0.002(10) 0.025(11)

C93 0.023(10) 0.040(10) 0.010(9) 0.006(8) 0.004(7) -0.012(9)

C94 0.039(11) 0.033(9) 0.066(13) 0.009(9) -0.017(9) -0.021(9)

C95 0.019(10) 0.036(10) 0.048(12) 0.013(9) -0.003(9) -0.006(9)

C96 0.005(9) 0.092(14) 0.059(13) -0.007(11) -0.002(8) -0.012(9)

C97 0.056(14) 0.048(13) 0.087(17) -0.005(13) -0.014(13) -0.020(11)

C98 0.12(2) 0.038(12) 0.114(19) 0.006(12) -0.030(16) -0.038(13)

C99 0.046(13) 0.037(11) 0.028(11) -0.003(9) -0.009(9) -0.004(10)

C100 0.014(9) 0.059(11) 0.049(11) 0.015(10) -0.003(8) 0.007(9)

O1S 0.073(12) 0.130(14) 0.134(15) -0.013(12) 0.031(10) -0.006(11)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Ni1 O1 2.024(10) . ?

Ni1 O2 2.025(8) . ?

Ni1 O3 2.027(9) . ?

Ni1 O5 2.094(9) . ?

Ni1 N1 2.118(11) . ?

Ni1 N2 2.158(13) . ?

Ni1 Ni2 2.969(3) . ?

Ni1 Ni3 3.654(3) . ?

Ni2 O1 1.997(9) . ?

Ni2 O16 2.038(11) . ?

Ni2 N3 2.049(13) . ?

Ni2 O2 2.058(9) . ?

Ni2 O4 2.080(10) . ?

Ni2 O14 2.161(10) . ?

Ni2 Ni3 3.076(3) . ?

Ni3 O2 2.018(8) . ?

Ni3 O15 2.025(11) . ?

Ni3 O10 2.026(8) . ?

Ni3 O14 2.053(11) . ?

Ni3 O7 2.058(11) . ?

Ni3 O6 2.118(9) . ?

Ni3 Ni5 3.101(3) . ?

Ni3 Ni4 3.667(3) . ?

Ni4 O10 2.005(9) . ?

Ni4 O9 2.019(10) . ?

Ni4 O12 2.080(11) . ?

Ni4 O13 2.097(10) . ?

Ni4 N4 2.116(14) . ?

Ni4 N5 2.132(14) . ?

Ni4 Ni5 2.967(3) . ?

Ni5 O9 1.976(11) . ?

Ni5 O8 2.022(11) . ?

Ni5 N6 2.036(13) . ?

Ni5 O10 2.052(9) . ?

Ni5 O11 2.081(10) . ?

Ni5 O6 2.183(9) . ?

Ni6 O18 2.015(9) . ?

Ni6 O17 2.039(10) . ?

Ni6 O19 2.058(10) . ?

Ni6 O21 2.060(9) . ?

Ni6 N7 2.119(12) . ?

Ni6 N8 2.189(12) . ?

Ni6 Ni7 2.971(3) . ?

Ni6 Ni8 3.669(3) . ?

Ni7 O17 1.983(9) . ?

Ni7 O32 2.007(11) . ?

Ni7 N9 2.041(13) . ?

Ni7 O20 2.063(10) . ?

Ni7 O18 2.081(9) . ?

Ni7 O30 2.132(10) . ?

Ni7 Ni8 3.100(3) . ?

Ni8 O26 2.008(9) . ?

Ni8 O18 2.033(9) . ?

Ni8 O23 2.053(11) . ?

Ni8 O31 2.062(10) . ?

Ni8 O30 2.086(11) . ?

Ni8 O22 2.109(9) . ?

Ni8 Ni10 3.109(3) . ?

Ni8 Ni9 3.661(3) . ?

Ni9 O25 2.005(10) . ?

Ni9 O26 2.026(10) . ?

Ni9 O28 2.048(11) . ?

Ni9 O29 2.076(9) . ?

Ni9 N10 2.129(13) . ?

Ni9 N11 2.152(15) . ?

Ni9 Ni10 2.962(3) . ?

Ni10 O25 1.984(10) . ?

Ni10 N12 2.042(13) . ?

Ni10 O26 2.047(10) . ?

Ni10 O24 2.068(11) . ?

Ni10 O27 2.070(10) . ?

Ni10 O22 2.152(9) . ?

S1 C19 1.89(3) . ?

S1 C18' 1.90(3) . ?

S1 C18 1.90(3) . ?

S2 C38' 1.811(12) . ?

S2 C38 1.811(12) . ?

S2 C37 1.865(18) . ?

S3 C69' 1.889(16) . ?

S3 C69 1.889(16) . ?

S3 C68 1.91(2) . ?

S3 C68' 1.91(2) . ?

S4 C87 1.80(2) . ?

S4 C87' 1.80(2) . ?

S4 C88 1.82(2) . ?

O1 C5 1.322(16) . ?

O3 C39 1.251(13) . ?

O4 C39 1.264(14) . ?

O5 C41 1.244(15) . ?

O6 C41 1.247(15) . ?

O7 C43 1.233(17) . ?

O8 C43 1.265(18) . ?

O9 C24 1.342(18) . ?

O11 C45 1.254(19) . ?

O12 C45 1.212(19) . ?

O13 C47 1.270(19) . ?

O14 C47 1.24(2) . ?

O15 C49 1.289(19) . ?

O16 C49 1.218(19) . ?

O17 C55 1.326(15) . ?

O19 C95 1.246(17) . ?

O20 C95 1.267(18) . ?

O21 C93 1.239(16) . ?

O22 C93 1.245(16) . ?

O23 C91 1.294(17) . ?

O24 C91 1.206(18) . ?

O25 C74 1.361(16) . ?

O27 C89 1.227(19) . ?

O28 C89 1.264(18) . ?

O29 C99 1.254(17) . ?

O30 C99 1.271(19) . ?

O31 C97 1.29(2) . ?

O32 C97 1.26(2) . ?

N1 C8 1.459(18) . ?

N1 C9 1.495(16) . ?

N1 C11 1.520(17) . ?

N2 C12 1.463(17) . ?

N2 C14 1.488(19) . ?

N2 C13 1.526(16) . ?

N3 C15 1.262(18) . ?

N3 C16 1.53(2) . ?

N4 C30 1.45(2) . ?

N4 C27 1.461(18) . ?

N4 C28 1.489(17) . ?

N5 C32 1.48(2) . ?

N5 C31 1.49(2) . ?

N5 C33 1.488(18) . ?

N6 C34 1.30(2) . ?

N6 C35 1.45(2) . ?

N7 C58 1.468(19) . ?

N7 C61 1.474(17) . ?

N7 C59 1.489(17) . ?

N8 C62 1.478(18) . ?

N8 C63 1.481(19) . ?

N8 C64 1.495(16) . ?

N9 C65 1.256(17) . ?

N9 C66 1.481(19) . ?

N10 C77 1.464(18) . ?

N10 C78 1.485(18) . ?

N10 C80 1.488(19) . ?

N11 C81 1.45(2) . ?

N11 C82 1.477(18) . ?

N11 C83 1.483(19) . ?

N12 C84 1.28(2) . ?

N12 C85 1.469(19) . ?

C1 C2 1.52(2) . ?

C2 C3 1.34(2) . ?

C2 C7 1.40(2) . ?

C3 C4 1.40(2) . ?

C4 C5 1.388(19) . ?

C4 C15 1.44(2) . ?

C5 C6 1.403(19) . ?

C6 C7 1.397(19) . ?

C6 C8 1.489(18) . ?

C9 C10 1.498(19) . ?

C11 C12 1.48(2) . ?

C16 C17 1.50(3) . ?

C17 C18 1.65(3) . ?

C17 C18' 1.65(3) . ?

C20 C21 1.54(2) . ?

C21 C26 1.30(2) . ?

C21 C22 1.39(2) . ?

C22 C23 1.42(2) . ?

C23 C34 1.36(2) . ?

C23 C24 1.42(2) . ?

C24 C25 1.44(2) . ?

C25 C26 1.43(2) . ?

C25 C27 1.50(2) . ?

C28 C29 1.50(2) . ?

C30 C31 1.53(2) . ?

C35 C36 1.52(2) . ?

C36 C37 1.44(2) . ?

C39 C40 1.5536 . ?

C41 C42 1.475(19) . ?

C43 C44 1.50(2) . ?

C45 C46 1.52(2) . ?

C47 C48 1.50(2) . ?

C49 C50 1.46(2) . ?

C51 C52 1.540(19) . ?

C52 C53 1.33(2) . ?

C52 C57 1.41(2) . ?

C53 C54 1.36(2) . ?

C54 C55 1.437(19) . ?

C54 C65 1.45(2) . ?

C55 C56 1.418(19) . ?

C56 C57 1.380(18) . ?

C56 C58 1.522(18) . ?

C59 C60 1.520(19) . ?

C61 C62 1.51(2) . ?

C66 C67 1.49(2) . ?

C67 C68 1.48(3) . ?

C67 C68' 1.48(3) . ?

C70 C71 1.52(2) . ?

C71 C76 1.36(2) . ?

C71 C72 1.38(2) . ?

C72 C73 1.40(2) . ?

C73 C74 1.363(19) . ?

C73 C84 1.48(2) . ?

C74 C75 1.42(2) . ?

C75 C76 1.38(2) . ?

C75 C77 1.53(2) . ?

C78 C79 1.52(2) . ?

C80 C81 1.50(2) . ?

C85 C86 1.52(2) . ?

C86 C87' 1.51(3) . ?

C86 C87 1.51(3) . ?

C89 C90 1.58(2) . ?

C91 C92' 1.53(2) . ?

C91 C92 1.53(2) . ?

C93 C94 1.532(19) . ?

C95 C96 1.52(2) . ?

C97 C98 1.48(2) . ?

C99 C100 1.47(2) . ?

O1S C1S' 1.43(3) . ?

O1S C1S 1.43(3) . ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O1 Ni1 O2 83.8(4) . . ?

O1 Ni1 O3 91.3(4) . . ?

O2 Ni1 O3 88.3(4) . . ?

O1 Ni1 O5 86.2(4) . . ?

O2 Ni1 O5 90.8(3) . . ?

O3 Ni1 O5 177.5(4) . . ?

O1 Ni1 N1 90.3(4) . . ?

O2 Ni1 N1 174.1(4) . . ?

O3 Ni1 N1 92.2(4) . . ?

O5 Ni1 N1 88.4(4) . . ?

O1 Ni1 N2 174.0(4) . . ?

O2 Ni1 N2 102.0(4) . . ?

O3 Ni1 N2 90.5(4) . . ?

O5 Ni1 N2 91.9(4) . . ?

N1 Ni1 N2 83.9(5) . . ?

O1 Ni1 Ni2 42.1(3) . . ?

O2 Ni1 Ni2 43.8(3) . . ?

O3 Ni1 Ni2 79.4(3) . . ?

O5 Ni1 Ni2 98.4(3) . . ?

N1 Ni1 Ni2 130.6(3) . . ?

N2 Ni1 Ni2 144.0(4) . . ?

O1 Ni1 Ni3 83.5(3) . . ?

O2 Ni1 Ni3 25.3(2) . . ?

O3 Ni1 Ni3 113.6(3) . . ?

O5 Ni1 Ni3 65.5(3) . . ?

N1 Ni1 Ni3 153.5(3) . . ?

N2 Ni1 Ni3 101.0(3) . . ?

Ni2 Ni1 Ni3 54.16(6) . . ?

O1 Ni2 O16 177.6(4) . . ?

O1 Ni2 N3 89.7(5) . . ?

O16 Ni2 N3 92.7(5) . . ?

O1 Ni2 O2 83.6(4) . . ?

O16 Ni2 O2 94.1(4) . . ?

N3 Ni2 O2 173.2(5) . . ?

O1 Ni2 O4 91.7(4) . . ?

O16 Ni2 O4 88.8(5) . . ?

N3 Ni2 O4 89.8(4) . . ?

O2 Ni2 O4 89.4(4) . . ?

O1 Ni2 O14 91.2(4) . . ?

O16 Ni2 O14 87.8(4) . . ?

N3 Ni2 O14 103.4(5) . . ?

O2 Ni2 O14 77.9(4) . . ?

O4 Ni2 O14 166.6(4) . . ?

O1 Ni2 Ni1 42.7(3) . . ?

O16 Ni2 Ni1 135.1(4) . . ?

N3 Ni2 Ni1 130.3(4) . . ?

O2 Ni2 Ni1 42.9(2) . . ?

O4 Ni2 Ni1 80.4(3) . . ?

O14 Ni2 Ni1 92.9(3) . . ?

O1 Ni2 Ni3 100.9(3) . . ?

O16 Ni2 Ni3 76.9(3) . . ?

N3 Ni2 Ni3 142.9(4) . . ?

O2 Ni2 Ni3 40.5(2) . . ?

O4 Ni2 Ni3 124.8(3) . . ?

O14 Ni2 Ni3 41.8(3) . . ?

Ni1 Ni2 Ni3 74.36(7) . . ?

O2 Ni3 O15 94.6(4) . . ?

O2 Ni3 O10 174.4(4) . . ?

O15 Ni3 O10 88.9(4) . . ?

O2 Ni3 O14 81.3(4) . . ?

O15 Ni3 O14 91.1(4) . . ?

O10 Ni3 O14 94.2(4) . . ?

O2 Ni3 O7 90.5(4) . . ?

O15 Ni3 O7 86.3(4) . . ?

O10 Ni3 O7 94.1(4) . . ?

O14 Ni3 O7 171.2(4) . . ?

O2 Ni3 O6 96.1(3) . . ?

O15 Ni3 O6 168.9(4) . . ?

O10 Ni3 O6 80.8(3) . . ?

O14 Ni3 O6 93.7(4) . . ?

O7 Ni3 O6 90.4(4) . . ?

O2 Ni3 Ni2 41.5(3) . . ?

O15 Ni3 Ni2 78.5(3) . . ?

O10 Ni3 Ni2 135.6(3) . . ?

O14 Ni3 Ni2 44.5(3) . . ?

O7 Ni3 Ni2 126.7(3) . . ?

O6 Ni3 Ni2 111.8(2) . . ?

O2 Ni3 Ni5 137.9(2) . . ?

O15 Ni3 Ni5 124.2(3) . . ?

O10 Ni3 Ni5 40.8(3) . . ?

O14 Ni3 Ni5 110.6(3) . . ?

O7 Ni3 Ni5 77.7(3) . . ?

O6 Ni3 Ni5 44.7(2) . . ?

Ni2 Ni3 Ni5 150.28(9) . . ?

O2 Ni3 Ni1 25.4(2) . . ?

O15 Ni3 Ni1 119.3(3) . . ?

O10 Ni3 Ni1 150.1(3) . . ?

O14 Ni3 Ni1 76.8(3) . . ?

O7 Ni3 Ni1 97.2(3) . . ?

O6 Ni3 Ni1 71.6(2) . . ?

Ni2 Ni3 Ni1 51.48(5) . . ?

Ni5 Ni3 Ni1 115.58(7) . . ?

O2 Ni3 Ni4 150.4(3) . . ?

O15 Ni3 Ni4 95.0(3) . . ?

O10 Ni3 Ni4 24.4(3) . . ?

O14 Ni3 Ni4 70.5(3) . . ?

O7 Ni3 Ni4 118.0(3) . . ?

O6 Ni3 Ni4 77.2(3) . . ?

Ni2 Ni3 Ni4 113.97(8) . . ?

Ni5 Ni3 Ni4 51.17(6) . . ?

Ni1 Ni3 Ni4 132.64(7) . . ?

O10 Ni4 O9 82.9(4) . . ?

O10 Ni4 O12 87.2(4) . . ?

O9 Ni4 O12 92.8(4) . . ?

O10 Ni4 O13 90.7(4) . . ?

O9 Ni4 O13 86.0(4) . . ?

O12 Ni4 O13 177.7(5) . . ?

O10 Ni4 N4 173.0(5) . . ?

O9 Ni4 N4 90.2(5) . . ?

O12 Ni4 N4 91.7(5) . . ?

O13 Ni4 N4 90.2(5) . . ?

O10 Ni4 N5 100.8(5) . . ?

O9 Ni4 N5 176.0(6) . . ?

O12 Ni4 N5 89.1(5) . . ?

O13 Ni4 N5 92.2(5) . . ?

N4 Ni4 N5 86.2(6) . . ?

O10 Ni4 Ni5 43.6(3) . . ?

O9 Ni4 Ni5 41.5(3) . . ?

O12 Ni4 Ni5 79.4(3) . . ?

O13 Ni4 Ni5 98.4(3) . . ?

N4 Ni4 Ni5 129.4(4) . . ?

N5 Ni4 Ni5 142.5(5) . . ?

O10 Ni4 Ni3 24.7(2) . . ?

O9 Ni4 Ni3 83.5(3) . . ?

O12 Ni4 Ni3 111.8(3) . . ?

O13 Ni4 Ni3 66.1(3) . . ?

N4 Ni4 Ni3 155.8(3) . . ?

N5 Ni4 Ni3 99.0(4) . . ?

Ni5 Ni4 Ni3 54.50(6) . . ?

O9 Ni5 O8 176.5(4) . . ?

O9 Ni5 N6 90.6(5) . . ?

O8 Ni5 N6 92.6(5) . . ?

O9 Ni5 O10 82.7(4) . . ?

O8 Ni5 O10 94.1(4) . . ?

N6 Ni5 O10 173.3(5) . . ?

O9 Ni5 O11 91.9(4) . . ?

O8 Ni5 O11 86.6(4) . . ?

N6 Ni5 O11 91.7(4) . . ?

O10 Ni5 O11 88.8(4) . . ?

O9 Ni5 O6 91.7(4) . . ?

O8 Ni5 O6 89.0(4) . . ?

N6 Ni5 O6 101.4(4) . . ?

O10 Ni5 O6 78.7(3) . . ?

O11 Ni5 O6 166.4(4) . . ?

O9 Ni5 Ni4 42.6(3) . . ?

O8 Ni5 Ni4 133.9(3) . . ?

N6 Ni5 Ni4 131.3(4) . . ?

O10 Ni5 Ni4 42.4(3) . . ?

O11 Ni5 Ni4 79.8(3) . . ?

O6 Ni5 Ni4 94.1(3) . . ?

O9 Ni5 Ni3 101.0(3) . . ?

O8 Ni5 Ni3 77.3(3) . . ?

N6 Ni5 Ni3 142.2(4) . . ?

O10 Ni5 Ni3 40.2(2) . . ?

O11 Ni5 Ni3 123.4(3) . . ?

O6 Ni5 Ni3 43.0(2) . . ?

Ni4 Ni5 Ni3 74.33(7) . . ?

O18 Ni6 O17 84.0(4) . . ?

O18 Ni6 O19 88.2(4) . . ?

O17 Ni6 O19 90.4(4) . . ?

O18 Ni6 O21 91.1(4) . . ?

O17 Ni6 O21 86.6(4) . . ?

O19 Ni6 O21 176.9(4) . . ?

O18 Ni6 N7 174.1(5) . . ?

O17 Ni6 N7 90.3(4) . . ?

O19 Ni6 N7 93.2(4) . . ?

O21 Ni6 N7 87.2(4) . . ?

O18 Ni6 N8 102.4(4) . . ?

O17 Ni6 N8 173.3(4) . . ?

O19 Ni6 N8 91.6(4) . . ?

O21 Ni6 N8 91.5(4) . . ?

N7 Ni6 N8 83.2(5) . . ?

O18 Ni6 Ni7 44.4(3) . . ?

O17 Ni6 Ni7 41.7(3) . . ?

O19 Ni6 Ni7 78.7(3) . . ?

O21 Ni6 Ni7 98.7(3) . . ?

N7 Ni6 Ni7 130.4(4) . . ?

N8 Ni6 Ni7 145.0(3) . . ?

O18 Ni6 Ni8 25.1(3) . . ?

O17 Ni6 Ni8 83.6(3) . . ?

O19 Ni6 Ni8 113.3(3) . . ?

O21 Ni6 Ni8 66.0(3) . . ?

N7 Ni6 Ni8 152.8(3) . . ?

N8 Ni6 Ni8 101.4(3) . . ?

Ni7 Ni6 Ni8 54.43(6) . . ?

O17 Ni7 O32 178.6(5) . . ?

O17 Ni7 N9 89.9(5) . . ?

O32 Ni7 N9 91.5(5) . . ?

O17 Ni7 O20 91.5(4) . . ?

O32 Ni7 O20 88.4(4) . . ?

N9 Ni7 O20 89.3(4) . . ?

O17 Ni7 O18 83.7(4) . . ?

O32 Ni7 O18 95.0(4) . . ?

N9 Ni7 O18 173.6(4) . . ?

O20 Ni7 O18 90.5(4) . . ?

O17 Ni7 O30 91.4(4) . . ?

O32 Ni7 O30 88.4(4) . . ?

N9 Ni7 O30 102.3(4) . . ?

O20 Ni7 O30 168.0(4) . . ?

O18 Ni7 O30 78.2(4) . . ?

O17 Ni7 Ni6 43.1(3) . . ?

O32 Ni7 Ni6 135.6(4) . . ?

N9 Ni7 Ni6 131.1(4) . . ?

O20 Ni7 Ni6 81.0(3) . . ?

O18 Ni7 Ni6 42.6(2) . . ?

O30 Ni7 Ni6 93.3(3) . . ?

O17 Ni7 Ni8 101.3(3) . . ?

O32 Ni7 Ni8 77.7(3) . . ?

N9 Ni7 Ni8 142.2(4) . . ?

O20 Ni7 Ni8 125.8(3) . . ?

O18 Ni7 Ni8 40.5(2) . . ?

O30 Ni7 Ni8 42.1(3) . . ?

Ni6 Ni7 Ni8 74.33(7) . . ?

O26 Ni8 O18 174.0(4) . . ?

O26 Ni8 O23 90.9(4) . . ?

O18 Ni8 O23 93.2(4) . . ?

O26 Ni8 O31 90.6(4) . . ?

O18 Ni8 O31 94.2(4) . . ?

O23 Ni8 O31 85.7(4) . . ?

O26 Ni8 O30 95.9(4) . . ?

O18 Ni8 O30 80.4(4) . . ?

O23 Ni8 O30 172.2(4) . . ?

O31 Ni8 O30 90.3(4) . . ?

O26 Ni8 O22 79.9(4) . . ?

O18 Ni8 O22 95.5(4) . . ?

O23 Ni8 O22 92.1(4) . . ?

O31 Ni8 O22 170.2(4) . . ?

O30 Ni8 O22 92.9(4) . . ?

O26 Ni8 Ni7 136.4(3) . . ?

O18 Ni8 Ni7 41.7(3) . . ?

O23 Ni8 Ni7 129.0(3) . . ?

O31 Ni8 Ni7 77.8(3) . . ?

O30 Ni8 Ni7 43.3(3) . . ?

O22 Ni8 Ni7 110.7(3) . . ?

O26 Ni8 Ni10 40.4(3) . . ?

O18 Ni8 Ni10 136.6(3) . . ?

O23 Ni8 Ni10 77.6(3) . . ?

O31 Ni8 Ni10 126.6(3) . . ?

O30 Ni8 Ni10 110.1(3) . . ?

O22 Ni8 Ni10 43.7(2) . . ?

Ni7 Ni8 Ni10 148.24(9) . . ?

O26 Ni8 Ni9 24.9(3) . . ?

O18 Ni8 Ni9 150.2(3) . . ?

O23 Ni8 Ni9 115.6(3) . . ?

O31 Ni8 Ni9 95.3(3) . . ?

O30 Ni8 Ni9 71.4(3) . . ?

O22 Ni8 Ni9 77.0(3) . . ?

Ni7 Ni8 Ni9 113.70(8) . . ?

Ni10 Ni8 Ni9 51.09(6) . . ?

O26 Ni8 Ni6 149.6(3) . . ?

O18 Ni8 Ni6 24.9(3) . . ?

O23 Ni8 Ni6 100.0(3) . . ?

O31 Ni8 Ni6 118.3(3) . . ?

O30 Ni8 Ni6 76.0(3) . . ?

O22 Ni8 Ni6 71.4(2) . . ?

Ni7 Ni8 Ni6 51.24(5) . . ?

Ni10 Ni8 Ni6 114.42(7) . . ?

Ni9 Ni8 Ni6 132.71(7) . . ?

O25 Ni9 O26 82.9(4) . . ?

O25 Ni9 O28 92.1(4) . . ?

O26 Ni9 O28 88.4(4) . . ?

O25 Ni9 O29 86.3(4) . . ?

O26 Ni9 O29 91.5(4) . . ?

O28 Ni9 O29 178.4(4) . . ?

O25 Ni9 N10 90.9(5) . . ?

O26 Ni9 N10 173.8(5) . . ?

O28 Ni9 N10 91.5(5) . . ?

O29 Ni9 N10 88.4(4) . . ?

O25 Ni9 N11 174.7(5) . . ?

O26 Ni9 N11 102.0(5) . . ?

O28 Ni9 N11 90.1(5) . . ?

O29 Ni9 N11 91.5(4) . . ?

N10 Ni9 N11 84.2(6) . . ?

O25 Ni9 Ni10 41.8(3) . . ?

O26 Ni9 Ni10 43.6(3) . . ?

O28 Ni9 Ni10 79.0(4) . . ?

O29 Ni9 Ni10 99.8(3) . . ?

N10 Ni9 Ni10 130.3(4) . . ?

N11 Ni9 Ni10 143.5(4) . . ?

O25 Ni9 Ni8 83.3(3) . . ?

O26 Ni9 Ni8 24.7(3) . . ?

O28 Ni9 Ni8 113.1(3) . . ?

O29 Ni9 Ni8 66.8(3) . . ?

N10 Ni9 Ni8 154.8(3) . . ?

N11 Ni9 Ni8 100.2(4) . . ?

Ni10 Ni9 Ni8 54.78(6) . . ?

O25 Ni10 N12 92.1(5) . . ?

O25 Ni10 O26 82.9(4) . . ?

N12 Ni10 O26 174.8(5) . . ?

O25 Ni10 O24 174.3(4) . . ?

N12 Ni10 O24 93.1(5) . . ?

O26 Ni10 O24 91.9(4) . . ?

O25 Ni10 O27 90.7(4) . . ?

N12 Ni10 O27 88.2(4) . . ?

O26 Ni10 O27 93.2(4) . . ?

O24 Ni10 O27 87.3(4) . . ?

O25 Ni10 O22 91.4(4) . . ?

N12 Ni10 O22 100.8(4) . . ?

O26 Ni10 O22 78.0(4) . . ?

O24 Ni10 O22 89.7(4) . . ?

O27 Ni10 O22 170.7(4) . . ?

O25 Ni10 Ni9 42.3(3) . . ?

N12 Ni10 Ni9 132.5(4) . . ?

O26 Ni10 Ni9 43.1(3) . . ?

O24 Ni10 Ni9 132.0(3) . . ?

O27 Ni10 Ni9 81.2(3) . . ?

O22 Ni10 Ni9 94.4(3) . . ?

O25 Ni10 Ni8 99.9(3) . . ?

N12 Ni10 Ni8 141.1(3) . . ?

O26 Ni10 Ni8 39.5(3) . . ?

O24 Ni10 Ni8 77.3(3) . . ?

O27 Ni10 Ni8 128.1(3) . . ?

O22 Ni10 Ni8 42.6(3) . . ?

Ni9 Ni10 Ni8 74.13(7) . . ?

C19 S1 C18' 98.0(17) . . ?

C19 S1 C18 101(3) . . ?

C18' S1 C18 8(8) . . ?

C38' S2 C38 14(6) . . ?

C38' S2 C37 103.2(8) . . ?

C38 S2 C37 89(6) . . ?

C69' S3 C69 132.1(16) . . ?

C69' S3 C68 101(5) . . ?

C69 S3 C68 96.5(17) . . ?

C69' S3 C68' 101(3) . . ?

C69 S3 C68' 96.5(14) . . ?

C68 S3 C68' 0(10) . . ?

C87 S4 C87' 11(5) . . ?

C87 S4 C88 93(4) . . ?

C87' S4 C88 104(2) . . ?

C5 O1 Ni2 128.4(9) . . ?

C5 O1 Ni1 127.5(8) . . ?

Ni2 O1 Ni1 95.2(4) . . ?

Ni3 O2 Ni1 129.3(4) . . ?

Ni3 O2 Ni2 98.0(4) . . ?

Ni1 O2 Ni2 93.3(4) . . ?

C39 O3 Ni1 128.8(8) . . ?

C39 O4 Ni2 124.5(8) . . ?

C41 O5 Ni1 140.9(9) . . ?

C41 O6 Ni3 126.4(9) . . ?

C41 O6 Ni5 136.9(9) . . ?

Ni3 O6 Ni5 92.3(4) . . ?

C43 O7 Ni3 129.1(11) . . ?

C43 O8 Ni5 130.7(10) . . ?

C24 O9 Ni5 128.4(10) . . ?

C24 O9 Ni4 129.4(10) . . ?

Ni5 O9 Ni4 95.9(5) . . ?

Ni4 O10 Ni3 131.0(5) . . ?

Ni4 O10 Ni5 94.0(4) . . ?

Ni3 O10 Ni5 99.0(4) . . ?

C45 O11 Ni5 125.2(10) . . ?

C45 O12 Ni4 126.9(11) . . ?

C47 O13 Ni4 137.9(12) . . ?

C47 O14 Ni3 128.5(10) . . ?

C47 O14 Ni2 133.1(11) . . ?

Ni3 O14 Ni2 93.7(4) . . ?

C49 O15 Ni3 128.7(11) . . ?

C49 O16 Ni2 132.1(11) . . ?

C55 O17 Ni7 128.0(9) . . ?

C55 O17 Ni6 127.3(9) . . ?

Ni7 O17 Ni6 95.2(4) . . ?

Ni6 O18 Ni8 130.0(5) . . ?

Ni6 O18 Ni7 93.0(4) . . ?

Ni8 O18 Ni7 97.7(4) . . ?

C95 O19 Ni6 128.6(10) . . ?

C95 O20 Ni7 124.6(9) . . ?

C93 O21 Ni6 139.8(9) . . ?

C93 O22 Ni8 124.6(9) . . ?

C93 O22 Ni10 137.6(9) . . ?

Ni8 O22 Ni10 93.7(4) . . ?

C91 O23 Ni8 129.0(11) . . ?

C91 O24 Ni10 130.6(11) . . ?

C74 O25 Ni10 127.1(9) . . ?

C74 O25 Ni9 129.7(9) . . ?

Ni10 O25 Ni9 95.8(4) . . ?

Ni8 O26 Ni9 130.4(5) . . ?

Ni8 O26 Ni10 100.1(5) . . ?

Ni9 O26 Ni10 93.3(4) . . ?

C89 O27 Ni10 123.1(11) . . ?

C89 O28 Ni9 126.0(11) . . ?

C99 O29 Ni9 139.8(11) . . ?

C99 O30 Ni8 126.9(10) . . ?

C99 O30 Ni7 135.1(10) . . ?

Ni8 O30 Ni7 94.6(5) . . ?

C97 O31 Ni8 128.5(11) . . ?

C97 O32 Ni7 132.4(11) . . ?

C8 N1 C9 107.7(11) . . ?

C8 N1 C11 112.2(11) . . ?

C9 N1 C11 110.6(11) . . ?

C8 N1 Ni1 107.6(8) . . ?

C9 N1 Ni1 116.6(9) . . ?

C11 N1 Ni1 102.1(8) . . ?

C12 N2 C14 113.6(13) . . ?

C12 N2 C13 108.8(11) . . ?

C14 N2 C13 107.0(12) . . ?

C12 N2 Ni1 106.0(10) . . ?

C14 N2 Ni1 111.2(9) . . ?

C13 N2 Ni1 110.3(9) . . ?

C15 N3 C16 115.6(14) . . ?

C15 N3 Ni2 123.3(11) . . ?

C16 N3 Ni2 120.8(12) . . ?

C30 N4 C27 109.1(14) . . ?

C30 N4 C28 111.7(13) . . ?

C27 N4 C28 109.9(13) . . ?

C30 N4 Ni4 100.6(10) . . ?

C27 N4 Ni4 109.4(10) . . ?

C28 N4 Ni4 115.8(10) . . ?

C32 N5 C31 109.7(14) . . ?

C32 N5 C33 108.9(14) . . ?

C31 N5 C33 106.0(14) . . ?

C32 N5 Ni4 115.0(11) . . ?

C31 N5 Ni4 104.5(11) . . ?

C33 N5 Ni4 112.2(9) . . ?

C34 N6 C35 117.8(15) . . ?

C34 N6 Ni5 123.0(12) . . ?

C35 N6 Ni5 118.9(11) . . ?

C58 N7 C61 110.4(11) . . ?

C58 N7 C59 110.6(11) . . ?

C61 N7 C59 110.9(12) . . ?

C58 N7 Ni6 108.1(9) . . ?

C61 N7 Ni6 102.9(8) . . ?

C59 N7 Ni6 113.7(9) . . ?

C62 N8 C63 110.4(13) . . ?

C62 N8 C64 112.0(12) . . ?

C63 N8 C64 107.2(12) . . ?

C62 N8 Ni6 106.2(9) . . ?

C63 N8 Ni6 111.5(9) . . ?

C64 N8 Ni6 109.6(9) . . ?

C65 N9 C66 112.0(13) . . ?

C65 N9 Ni7 124.7(11) . . ?

C66 N9 Ni7 122.8(10) . . ?

C77 N10 C78 109.5(12) . . ?

C77 N10 C80 111.5(12) . . ?

C78 N10 C80 112.3(13) . . ?

C77 N10 Ni9 108.2(10) . . ?

C78 N10 Ni9 114.2(10) . . ?

C80 N10 Ni9 100.9(10) . . ?

C81 N11 C82 109.5(15) . . ?

C81 N11 C83 109.6(13) . . ?

C82 N11 C83 108.4(13) . . ?

C81 N11 Ni9 106.3(10) . . ?

C82 N11 Ni9 110.7(10) . . ?

C83 N11 Ni9 112.3(11) . . ?

C84 N12 C85 116.3(14) . . ?

C84 N12 Ni10 122.3(12) . . ?

C85 N12 Ni10 120.9(10) . . ?

C3 C2 C7 117.4(16) . . ?

C3 C2 C1 124.8(17) . . ?

C7 C2 C1 117.7(19) . . ?

C2 C3 C4 122.3(15) . . ?

C5 C4 C3 120.6(15) . . ?

C5 C4 C15 125.4(15) . . ?

C3 C4 C15 113.2(15) . . ?

O1 C5 C4 122.2(14) . . ?

O1 C5 C6 119.5(13) . . ?

C4 C5 C6 118.1(14) . . ?

C7 C6 C5 119.1(14) . . ?

C7 C6 C8 120.5(14) . . ?

C5 C6 C8 120.3(13) . . ?

C6 C7 C2 122.2(16) . . ?

N1 C8 C6 113.0(12) . . ?

N1 C9 C10 118.1(12) . . ?

C12 C11 N1 109.0(12) . . ?

N2 C12 C11 113.3(13) . . ?

N3 C15 C4 127.0(15) . . ?

C17 C16 N3 112.8(16) . . ?

C16 C17 C18 110(2) . . ?

C16 C17 C18' 108.1(18) . . ?

C18 C17 C18' 9(9) . . ?

C17 C18 S1 107.7(18) . . ?

C17 C18' S1 107.7(18) . . ?

C26 C21 C22 120.8(17) . . ?

C26 C21 C20 119(2) . . ?

C22 C21 C20 119.7(18) . . ?

C21 C22 C23 121.7(16) . . ?

C34 C23 C24 125.1(16) . . ?

C34 C23 C22 117.4(16) . . ?

C24 C23 C22 117.2(17) . . ?

O9 C24 C23 122.0(15) . . ?

O9 C24 C25 117.9(15) . . ?

C23 C24 C25 120.0(16) . . ?

C26 C25 C24 117.4(16) . . ?

C26 C25 C27 119.1(16) . . ?

C24 C25 C27 123.3(14) . . ?

C21 C26 C25 122.8(18) . . ?

N4 C27 C25 111.6(14) . . ?

N4 C28 C29 118.7(15) . . ?

N4 C30 C31 111.3(15) . . ?

N5 C31 C30 110.3(14) . . ?

N6 C34 C23 129.6(17) . . ?

N6 C35 C36 112.4(13) . . ?

C37 C36 C35 113.3(16) . . ?

C36 C37 S2 110.5(15) . . ?

O3 C39 O4 126.8(11) . . ?

O3 C39 C40 115.9(7) . . ?

O4 C39 C40 117.2(6) . . ?

O5 C41 O6 125.1(14) . . ?

O5 C41 C42 116.2(12) . . ?

O6 C41 C42 118.7(13) . . ?

O7 C43 O8 125.2(16) . . ?

O7 C43 C44 118.1(16) . . ?

O8 C43 C44 116.8(15) . . ?

O12 C45 O11 128.2(16) . . ?

O12 C45 C46 115.7(18) . . ?

O11 C45 C46 116.1(17) . . ?

O14 C47 O13 124.9(15) . . ?

O14 C47 C48 121.6(16) . . ?

O13 C47 C48 113.5(18) . . ?

O16 C49 O15 123.6(15) . . ?

O16 C49 C50 119.2(18) . . ?

O15 C49 C50 117.2(18) . . ?

C53 C52 C57 115.0(14) . . ?

C53 C52 C51 125.0(15) . . ?

C57 C52 C51 119.9(14) . . ?

C52 C53 C54 127.2(16) . . ?

C53 C54 C55 117.3(15) . . ?

C53 C54 C65 119.9(15) . . ?

C55 C54 C65 122.8(14) . . ?

O17 C55 C56 119.0(13) . . ?

O17 C55 C54 123.5(13) . . ?

C56 C55 C54 117.4(13) . . ?

C57 C56 C55 119.8(13) . . ?

C57 C56 C58 119.9(13) . . ?

C55 C56 C58 120.3(13) . . ?

C56 C57 C52 122.7(14) . . ?

N7 C58 C56 112.4(12) . . ?

N7 C59 C60 116.2(12) . . ?

N7 C61 C62 110.6(12) . . ?

N8 C62 C61 111.6(13) . . ?

N9 C65 C54 127.5(14) . . ?

N9 C66 C67 111.7(15) . . ?

C68 C67 C68' 0(5) . . ?

C68 C67 C66 111(2) . . ?

C68' C67 C66 111.1(18) . . ?

C67 C68 S3 110.5(16) . . ?

C67 C68' S3 110.5(16) . . ?

C76 C71 C72 117.3(16) . . ?

C76 C71 C70 122.7(17) . . ?

C72 C71 C70 119.9(16) . . ?

C71 C72 C73 120.1(16) . . ?

C74 C73 C72 121.8(17) . . ?

C74 C73 C84 124.1(14) . . ?

C72 C73 C84 114.0(15) . . ?

O25 C74 C73 124.1(15) . . ?

O25 C74 C75 117.2(13) . . ?

C73 C74 C75 118.7(15) . . ?

C76 C75 C74 117.4(15) . . ?

C76 C75 C77 119.6(16) . . ?

C74 C75 C77 123.0(14) . . ?

C71 C76 C75 124.5(17) . . ?

N10 C77 C75 112.9(13) . . ?

N10 C78 C79 117.0(15) . . ?

N10 C80 C81 110.7(15) . . ?

N11 C81 C80 110.1(14) . . ?

N12 C84 C73 128.6(15) . . ?

N12 C85 C86 111.6(13) . . ?

C87' C86 C87 13(6) . . ?

C87' C86 C85 109.5(15) . . ?

C87 C86 C85 111.0(16) . . ?

C86 C87 S4 118.3(19) . . ?

C86 C87' S4 118.3(19) . . ?

O27 C89 O28 130.0(16) . . ?

O27 C89 C90 115.9(16) . . ?

O28 C89 C90 113.9(16) . . ?

O24 C91 O23 124.8(17) . . ?

O24 C91 C92' 119.8(17) . . ?

O23 C91 C92' 114.5(17) . . ?

O24 C91 C92 110(2) . . ?

O23 C91 C92 124(2) . . ?

C92' C91 C92 24.6(19) . . ?

O21 C93 O22 128.3(13) . . ?

O21 C93 C94 114.3(13) . . ?

O22 C93 C94 117.3(13) . . ?

O19 C95 O20 126.6(15) . . ?

O19 C95 C96 116.4(16) . . ?

O20 C95 C96 116.9(15) . . ?

O32 C97 O31 122.7(16) . . ?

O32 C97 C98 119.5(18) . . ?

O31 C97 C98 117.6(18) . . ?

O29 C99 O30 125.2(15) . . ?

O29 C99 C100 117.0(16) . . ?

O30 C99 C100 117.8(15) . . ?

C1S' O1S C1S 58(4) . . ?

loop_

_geom_torsion_atom_site_label_1

_geom_torsion_atom_site_label_2

_geom_torsion_atom_site_label_3

_geom_torsion_atom_site_label_4

_geom_torsion

_geom_torsion_site_symmetry_1

_geom_torsion_site_symmetry_2

_geom_torsion_site_symmetry_3

_geom_torsion_site_symmetry_4

_geom_torsion_publ_flag

O2 Ni1 Ni2 O1 157.2(5) . . . . ?

O3 Ni1 Ni2 O1 -104.1(5) . . . . ?

O5 Ni1 Ni2 O1 74.8(5) . . . . ?

N1 Ni1 Ni2 O1 -20.3(6) . . . . ?

N2 Ni1 Ni2 O1 179.9(6) . . . . ?

Ni3 Ni1 Ni2 O1 126.3(4) . . . . ?

O1 Ni1 Ni2 O16 -178.4(6) . . . . ?

O2 Ni1 Ni2 O16 -21.2(6) . . . . ?

O3 Ni1 Ni2 O16 77.5(6) . . . . ?

O5 Ni1 Ni2 O16 -103.6(5) . . . . ?

N1 Ni1 Ni2 O16 161.3(6) . . . . ?

N2 Ni1 Ni2 O16 1.5(7) . . . . ?

Ni3 Ni1 Ni2 O16 -52.1(5) . . . . ?

O1 Ni1 Ni2 N3 21.8(6) . . . . ?

O2 Ni1 Ni2 N3 179.0(6) . . . . ?

O3 Ni1 Ni2 N3 -82.3(5) . . . . ?

O5 Ni1 Ni2 N3 96.6(5) . . . . ?

N1 Ni1 Ni2 N3 1.5(6) . . . . ?

N2 Ni1 Ni2 N3 -158.3(7) . . . . ?

Ni3 Ni1 Ni2 N3 148.1(5) . . . . ?

O1 Ni1 Ni2 O2 -157.2(5) . . . . ?

O3 Ni1 Ni2 O2 98.7(4) . . . . ?

O5 Ni1 Ni2 O2 -82.4(4) . . . . ?

N1 Ni1 Ni2 O2 -177.5(5) . . . . ?

N2 Ni1 Ni2 O2 22.6(6) . . . . ?

Ni3 Ni1 Ni2 O2 -30.9(3) . . . . ?

O1 Ni1 Ni2 O4 103.2(5) . . . . ?

O2 Ni1 Ni2 O4 -99.6(5) . . . . ?

O3 Ni1 Ni2 O4 -0.9(4) . . . . ?

O5 Ni1 Ni2 O4 178.0(4) . . . . ?

N1 Ni1 Ni2 O4 82.9(5) . . . . ?

N2 Ni1 Ni2 O4 -76.9(6) . . . . ?

Ni3 Ni1 Ni2 O4 -130.5(3) . . . . ?

O1 Ni1 Ni2 O14 -88.5(5) . . . . ?

O2 Ni1 Ni2 O14 68.7(4) . . . . ?

O3 Ni1 Ni2 O14 167.4(4) . . . . ?

O5 Ni1 Ni2 O14 -13.7(4) . . . . ?

N1 Ni1 Ni2 O14 -108.8(5) . . . . ?

N2 Ni1 Ni2 O14 91.3(6) . . . . ?

Ni3 Ni1 Ni2 O14 37.8(3) . . . . ?

O1 Ni1 Ni2 Ni3 -126.3(4) . . . . ?

O2 Ni1 Ni2 Ni3 30.9(3) . . . . ?

O3 Ni1 Ni2 Ni3 129.6(3) . . . . ?

O5 Ni1 Ni2 Ni3 -51.5(3) . . . . ?

N1 Ni1 Ni2 Ni3 -146.6(4) . . . . ?

N2 Ni1 Ni2 Ni3 53.5(5) . . . . ?

O1 Ni2 Ni3 O2 -66.4(5) . . . . ?

O16 Ni2 Ni3 O2 112.6(5) . . . . ?

N3 Ni2 Ni3 O2 -170.7(8) . . . . ?

O4 Ni2 Ni3 O2 33.5(5) . . . . ?

O14 Ni2 Ni3 O2 -145.7(5) . . . . ?

Ni1 Ni2 Ni3 O2 -32.6(4) . . . . ?

O1 Ni2 Ni3 O15 -177.1(4) . . . . ?

O16 Ni2 Ni3 O15 1.9(5) . . . . ?

N3 Ni2 Ni3 O15 78.7(7) . . . . ?

O2 Ni2 Ni3 O15 -110.7(5) . . . . ?

O4 Ni2 Ni3 O15 -77.2(5) . . . . ?

O14 Ni2 Ni3 O15 103.6(5) . . . . ?

Ni1 Ni2 Ni3 O15 -143.2(3) . . . . ?

O1 Ni2 Ni3 O10 106.6(5) . . . . ?

O16 Ni2 Ni3 O10 -74.4(5) . . . . ?

N3 Ni2 Ni3 O10 2.3(8) . . . . ?

O2 Ni2 Ni3 O10 173.0(5) . . . . ?

O4 Ni2 Ni3 O10 -153.5(5) . . . . ?

O14 Ni2 Ni3 O10 27.3(5) . . . . ?

Ni1 Ni2 Ni3 O10 140.4(4) . . . . ?

O1 Ni2 Ni3 O14 79.3(5) . . . . ?

O16 Ni2 Ni3 O14 -101.7(5) . . . . ?

N3 Ni2 Ni3 O14 -24.9(8) . . . . ?

O2 Ni2 Ni3 O14 145.7(5) . . . . ?

O4 Ni2 Ni3 O14 179.2(5) . . . . ?

Ni1 Ni2 Ni3 O14 113.2(4) . . . . ?

O1 Ni2 Ni3 O7 -100.6(5) . . . . ?

O16 Ni2 Ni3 O7 78.3(5) . . . . ?

N3 Ni2 Ni3 O7 155.1(7) . . . . ?

O2 Ni2 Ni3 O7 -34.3(5) . . . . ?

O4 Ni2 Ni3 O7 -0.8(5) . . . . ?

O14 Ni2 Ni3 O7 -180.0(5) . . . . ?

Ni1 Ni2 Ni3 O7 -66.8(4) . . . . ?

O1 Ni2 Ni3 O6 7.3(4) . . . . ?

O16 Ni2 Ni3 O6 -173.7(5) . . . . ?

N3 Ni2 Ni3 O6 -97.0(7) . . . . ?

O2 Ni2 Ni3 O6 73.7(5) . . . . ?

O4 Ni2 Ni3 O6 107.2(5) . . . . ?

O14 Ni2 Ni3 O6 -72.0(5) . . . . ?

Ni1 Ni2 Ni3 O6 41.1(3) . . . . ?

O1 Ni2 Ni3 Ni5 39.8(3) . . . . ?

O16 Ni2 Ni3 Ni5 -141.2(4) . . . . ?

N3 Ni2 Ni3 Ni5 -64.4(7) . . . . ?

O2 Ni2 Ni3 Ni5 106.2(4) . . . . ?

O4 Ni2 Ni3 Ni5 139.7(4) . . . . ?

O14 Ni2 Ni3 Ni5 -39.5(4) . . . . ?

Ni1 Ni2 Ni3 Ni5 73.66(18) . . . . ?

O1 Ni2 Ni3 Ni1 -33.8(3) . . . . ?

O16 Ni2 Ni3 Ni1 145.1(4) . . . . ?

N3 Ni2 Ni3 Ni1 -138.1(7) . . . . ?

O2 Ni2 Ni3 Ni1 32.6(4) . . . . ?

O4 Ni2 Ni3 Ni1 66.0(4) . . . . ?

O14 Ni2 Ni3 Ni1 -113.2(4) . . . . ?

O1 Ni2 Ni3 Ni4 92.6(3) . . . . ?

O16 Ni2 Ni3 Ni4 -88.4(4) . . . . ?

N3 Ni2 Ni3 Ni4 -11.7(7) . . . . ?

O2 Ni2 Ni3 Ni4 159.0(4) . . . . ?

O4 Ni2 Ni3 Ni4 -167.6(4) . . . . ?

O14 Ni2 Ni3 Ni4 13.2(4) . . . . ?

Ni1 Ni2 Ni3 Ni4 126.41(8) . . . . ?

O1 Ni1 Ni3 O2 89.1(7) . . . . ?

O3 Ni1 Ni3 O2 0.5(7) . . . . ?

O5 Ni1 Ni3 O2 177.9(7) . . . . ?

N1 Ni1 Ni3 O2 166.7(10) . . . . ?

N2 Ni1 Ni3 O2 -95.0(7) . . . . ?

Ni2 Ni1 Ni3 O2 56.2(6) . . . . ?

O1 Ni1 Ni3 O15 75.2(5) . . . . ?

O2 Ni1 Ni3 O15 -14.0(7) . . . . ?

O3 Ni1 Ni3 O15 -13.5(5) . . . . ?

O5 Ni1 Ni3 O15 164.0(5) . . . . ?

N1 Ni1 Ni3 O15 152.7(8) . . . . ?

N2 Ni1 Ni3 O15 -108.9(5) . . . . ?

Ni2 Ni1 Ni3 O15 42.3(4) . . . . ?

O1 Ni1 Ni3 O10 -83.6(6) . . . . ?

O2 Ni1 Ni3 O10 -172.7(8) . . . . ?

O3 Ni1 Ni3 O10 -172.2(6) . . . . ?

O5 Ni1 Ni3 O10 5.2(6) . . . . ?

N1 Ni1 Ni3 O10 -6.1(9) . . . . ?

N2 Ni1 Ni3 O10 92.3(6) . . . . ?

Ni2 Ni1 Ni3 O10 -116.5(6) . . . . ?

O1 Ni1 Ni3 O14 -8.5(4) . . . . ?

O2 Ni1 Ni3 O14 -97.7(7) . . . . ?

O3 Ni1 Ni3 O14 -97.2(4) . . . . ?

O5 Ni1 Ni3 O14 80.3(4) . . . . ?

N1 Ni1 Ni3 O14 69.0(8) . . . . ?

N2 Ni1 Ni3 O14 167.4(4) . . . . ?

Ni2 Ni1 Ni3 O14 -41.4(3) . . . . ?

O1 Ni1 Ni3 O7 165.0(4) . . . . ?

O2 Ni1 Ni3 O7 75.8(7) . . . . ?

O3 Ni1 Ni3 O7 76.3(4) . . . . ?

O5 Ni1 Ni3 O7 -106.2(4) . . . . ?

N1 Ni1 Ni3 O7 -117.5(8) . . . . ?

N2 Ni1 Ni3 O7 -19.1(5) . . . . ?

Ni2 Ni1 Ni3 O7 132.1(3) . . . . ?

O1 Ni1 Ni3 O6 -107.0(4) . . . . ?

O2 Ni1 Ni3 O6 163.8(7) . . . . ?

O3 Ni1 Ni3 O6 164.3(4) . . . . ?

O5 Ni1 Ni3 O6 -18.2(4) . . . . ?

N1 Ni1 Ni3 O6 -29.5(8) . . . . ?

N2 Ni1 Ni3 O6 68.9(4) . . . . ?

Ni2 Ni1 Ni3 O6 -139.9(3) . . . . ?

O1 Ni1 Ni3 Ni2 32.9(3) . . . . ?

O2 Ni1 Ni3 Ni2 -56.2(6) . . . . ?

O3 Ni1 Ni3 Ni2 -55.7(3) . . . . ?

O5 Ni1 Ni3 Ni2 121.7(3) . . . . ?

N1 Ni1 Ni3 Ni2 110.4(7) . . . . ?

N2 Ni1 Ni3 Ni2 -151.2(4) . . . . ?

O1 Ni1 Ni3 Ni5 -115.3(3) . . . . ?

O2 Ni1 Ni3 Ni5 155.6(6) . . . . ?

O3 Ni1 Ni3 Ni5 156.1(3) . . . . ?

O5 Ni1 Ni3 Ni5 -26.5(3) . . . . ?

N1 Ni1 Ni3 Ni5 -37.7(8) . . . . ?

N2 Ni1 Ni3 Ni5 60.6(4) . . . . ?

Ni2 Ni1 Ni3 Ni5 -148.17(10) . . . . ?

O1 Ni1 Ni3 Ni4 -55.5(3) . . . . ?

O2 Ni1 Ni3 Ni4 -144.7(6) . . . . ?

O3 Ni1 Ni3 Ni4 -144.2(3) . . . . ?

O5 Ni1 Ni3 Ni4 33.3(3) . . . . ?

N1 Ni1 Ni3 Ni4 22.0(8) . . . . ?

N2 Ni1 Ni3 Ni4 120.4(4) . . . . ?

Ni2 Ni1 Ni3 Ni4 -88.44(10) . . . . ?

O2 Ni3 Ni4 O10 -175.5(8) . . . . ?

O15 Ni3 Ni4 O10 76.2(7) . . . . ?

O14 Ni3 Ni4 O10 165.6(7) . . . . ?

O7 Ni3 Ni4 O10 -12.3(7) . . . . ?

O6 Ni3 Ni4 O10 -95.8(6) . . . . ?

Ni2 Ni3 Ni4 O10 155.8(6) . . . . ?

Ni5 Ni3 Ni4 O10 -54.7(6) . . . . ?

Ni1 Ni3 Ni4 O10 -145.4(6) . . . . ?

O2 Ni3 Ni4 O9 -88.5(6) . . . . ?

O15 Ni3 Ni4 O9 163.2(4) . . . . ?

O10 Ni3 Ni4 O9 87.0(6) . . . . ?

O14 Ni3 Ni4 O9 -107.4(4) . . . . ?

O7 Ni3 Ni4 O9 74.8(4) . . . . ?

O6 Ni3 Ni4 O9 -8.8(4) . . . . ?

Ni2 Ni3 Ni4 O9 -117.2(3) . . . . ?

Ni5 Ni3 Ni4 O9 32.3(3) . . . . ?

Ni1 Ni3 Ni4 O9 -58.4(3) . . . . ?

O2 Ni3 Ni4 O12 -178.9(6) . . . . ?

O15 Ni3 Ni4 O12 72.8(5) . . . . ?

O10 Ni3 Ni4 O12 -3.4(7) . . . . ?

O14 Ni3 Ni4 O12 162.2(4) . . . . ?

O7 Ni3 Ni4 O12 -15.6(5) . . . . ?

O6 Ni3 Ni4 O12 -99.2(4) . . . . ?

Ni2 Ni3 Ni4 O12 152.4(3) . . . . ?

Ni5 Ni3 Ni4 O12 -58.1(3) . . . . ?

Ni1 Ni3 Ni4 O12 -148.8(3) . . . . ?

O2 Ni3 Ni4 O13 0.0(6) . . . . ?

O15 Ni3 Ni4 O13 -108.3(4) . . . . ?

O10 Ni3 Ni4 O13 175.5(7) . . . . ?

O14 Ni3 Ni4 O13 -19.0(4) . . . . ?

O7 Ni3 Ni4 O13 163.2(5) . . . . ?

O6 Ni3 Ni4 O13 79.7(4) . . . . ?

Ni2 Ni3 Ni4 O13 -28.8(3) . . . . ?

Ni5 Ni3 Ni4 O13 120.8(3) . . . . ?

Ni1 Ni3 Ni4 O13 30.1(3) . . . . ?

O2 Ni3 Ni4 N4 -12.5(11) . . . . ?

O15 Ni3 Ni4 N4 -120.9(10) . . . . ?

O10 Ni3 Ni4 N4 162.9(12) . . . . ?

O14 Ni3 Ni4 N4 -31.5(10) . . . . ?

O7 Ni3 Ni4 N4 150.7(10) . . . . ?

O6 Ni3 Ni4 N4 67.1(10) . . . . ?

Ni2 Ni3 Ni4 N4 -41.3(10) . . . . ?

Ni5 Ni3 Ni4 N4 108.3(10) . . . . ?

Ni1 Ni3 Ni4 N4 17.6(10) . . . . ?

O2 Ni3 Ni4 N5 88.4(6) . . . . ?

O15 Ni3 Ni4 N5 -19.9(5) . . . . ?

O10 Ni3 Ni4 N5 -96.1(7) . . . . ?

O14 Ni3 Ni4 N5 69.5(5) . . . . ?

O7 Ni3 Ni4 N5 -108.4(5) . . . . ?

O6 Ni3 Ni4 N5 168.1(5) . . . . ?

Ni2 Ni3 Ni4 N5 59.7(4) . . . . ?

Ni5 Ni3 Ni4 N5 -150.8(4) . . . . ?

Ni1 Ni3 Ni4 N5 118.5(4) . . . . ?

O2 Ni3 Ni4 Ni5 -120.8(5) . . . . ?

O15 Ni3 Ni4 Ni5 130.9(3) . . . . ?

O10 Ni3 Ni4 Ni5 54.7(6) . . . . ?

O14 Ni3 Ni4 Ni5 -139.8(3) . . . . ?

O7 Ni3 Ni4 Ni5 42.4(3) . . . . ?

O6 Ni3 Ni4 Ni5 -41.1(2) . . . . ?

Ni2 Ni3 Ni4 Ni5 -149.57(9) . . . . ?

Ni1 Ni3 Ni4 Ni5 -90.71(10) . . . . ?

O10 Ni4 Ni5 O9 156.2(5) . . . . ?

O12 Ni4 Ni5 O9 -106.6(5) . . . . ?

O13 Ni4 Ni5 O9 74.1(5) . . . . ?

N4 Ni4 Ni5 O9 -23.2(6) . . . . ?

N5 Ni4 Ni5 O9 179.0(7) . . . . ?

Ni3 Ni4 Ni5 O9 126.6(4) . . . . ?

O10 Ni4 Ni5 O8 -24.4(5) . . . . ?

O9 Ni4 Ni5 O8 179.4(5) . . . . ?

O12 Ni4 Ni5 O8 72.7(5) . . . . ?

O13 Ni4 Ni5 O8 -106.5(5) . . . . ?

N4 Ni4 Ni5 O8 156.2(6) . . . . ?

N5 Ni4 Ni5 O8 -1.7(7) . . . . ?

Ni3 Ni4 Ni5 O8 -54.0(4) . . . . ?

O10 Ni4 Ni5 N6 177.2(6) . . . . ?

O9 Ni4 Ni5 N6 21.0(6) . . . . ?

O12 Ni4 Ni5 N6 -85.6(6) . . . . ?

O13 Ni4 Ni5 N6 95.1(5) . . . . ?

N4 Ni4 Ni5 N6 -2.1(6) . . . . ?

N5 Ni4 Ni5 N6 -160.0(8) . . . . ?

Ni3 Ni4 Ni5 N6 147.7(5) . . . . ?

O9 Ni4 Ni5 O10 -156.2(5) . . . . ?

O12 Ni4 Ni5 O10 97.2(5) . . . . ?

O13 Ni4 Ni5 O10 -82.1(5) . . . . ?

N4 Ni4 Ni5 O10 -179.4(6) . . . . ?

N5 Ni4 Ni5 O10 22.8(7) . . . . ?

Ni3 Ni4 Ni5 O10 -29.6(3) . . . . ?

O10 Ni4 Ni5 O11 -99.5(5) . . . . ?

O9 Ni4 Ni5 O11 104.3(5) . . . . ?

O12 Ni4 Ni5 O11 -2.4(4) . . . . ?

O13 Ni4 Ni5 O11 178.4(4) . . . . ?

N4 Ni4 Ni5 O11 81.1(5) . . . . ?

N5 Ni4 Ni5 O11 -76.8(7) . . . . ?

Ni3 Ni4 Ni5 O11 -129.1(3) . . . . ?

O10 Ni4 Ni5 O6 68.2(4) . . . . ?

O9 Ni4 Ni5 O6 -88.0(4) . . . . ?

O12 Ni4 Ni5 O6 165.3(4) . . . . ?

O13 Ni4 Ni5 O6 -13.9(4) . . . . ?

N4 Ni4 Ni5 O6 -111.2(5) . . . . ?

N5 Ni4 Ni5 O6 90.9(7) . . . . ?

Ni3 Ni4 Ni5 O6 38.6(2) . . . . ?

O10 Ni4 Ni5 Ni3 29.6(3) . . . . ?

O9 Ni4 Ni5 Ni3 -126.6(4) . . . . ?

O12 Ni4 Ni5 Ni3 126.7(3) . . . . ?

O13 Ni4 Ni5 Ni3 -52.5(3) . . . . ?

N4 Ni4 Ni5 Ni3 -149.8(4) . . . . ?

N5 Ni4 Ni5 Ni3 52.3(6) . . . . ?

O2 Ni3 Ni5 O9 107.1(5) . . . . ?

O15 Ni3 Ni5 O9 -99.2(5) . . . . ?

O10 Ni3 Ni5 O9 -64.6(5) . . . . ?

O14 Ni3 Ni5 O9 7.0(4) . . . . ?

O7 Ni3 Ni5 O9 -176.0(4) . . . . ?

O6 Ni3 Ni5 O9 80.6(5) . . . . ?

Ni2 Ni3 Ni5 O9 35.4(3) . . . . ?

Ni1 Ni3 Ni5 O9 91.8(3) . . . . ?

Ni4 Ni3 Ni5 O9 -33.6(3) . . . . ?

O2 Ni3 Ni5 O8 -76.0(5) . . . . ?

O15 Ni3 Ni5 O8 77.7(5) . . . . ?

O10 Ni3 Ni5 O8 112.3(5) . . . . ?

O14 Ni3 Ni5 O8 -176.1(4) . . . . ?

O7 Ni3 Ni5 O8 0.9(4) . . . . ?

O6 Ni3 Ni5 O8 -102.4(5) . . . . ?

Ni2 Ni3 Ni5 O8 -147.7(3) . . . . ?

Ni1 Ni3 Ni5 O8 -91.3(3) . . . . ?

Ni4 Ni3 Ni5 O8 143.3(3) . . . . ?

O2 Ni3 Ni5 N6 1.6(8) . . . . ?

O15 Ni3 Ni5 N6 155.3(8) . . . . ?

O10 Ni3 Ni5 N6 -170.1(8) . . . . ?

O14 Ni3 Ni5 N6 -98.5(7) . . . . ?

O7 Ni3 Ni5 N6 78.5(7) . . . . ?

O6 Ni3 Ni5 N6 -24.8(7) . . . . ?

Ni2 Ni3 Ni5 N6 -70.0(7) . . . . ?

Ni1 Ni3 Ni5 N6 -13.7(7) . . . . ?

Ni4 Ni3 Ni5 N6 -139.1(7) . . . . ?

O2 Ni3 Ni5 O10 171.7(6) . . . . ?

O15 Ni3 Ni5 O10 -34.6(6) . . . . ?

O14 Ni3 Ni5 O10 71.6(5) . . . . ?

O7 Ni3 Ni5 O10 -111.4(5) . . . . ?

O6 Ni3 Ni5 O10 145.3(5) . . . . ?

Ni2 Ni3 Ni5 O10 100.0(4) . . . . ?

Ni1 Ni3 Ni5 O10 156.4(4) . . . . ?

Ni4 Ni3 Ni5 O10 31.0(4) . . . . ?

O2 Ni3 Ni5 O11 -153.2(6) . . . . ?

O15 Ni3 Ni5 O11 0.5(6) . . . . ?

O10 Ni3 Ni5 O11 35.1(6) . . . . ?

O14 Ni3 Ni5 O11 106.7(5) . . . . ?

O7 Ni3 Ni5 O11 -76.3(5) . . . . ?

O6 Ni3 Ni5 O11 -179.7(6) . . . . ?

Ni2 Ni3 Ni5 O11 135.1(4) . . . . ?

Ni1 Ni3 Ni5 O11 -168.5(4) . . . . ?

Ni4 Ni3 Ni5 O11 66.1(4) . . . . ?

O2 Ni3 Ni5 O6 26.5(5) . . . . ?

O15 Ni3 Ni5 O6 -179.9(6) . . . . ?

O10 Ni3 Ni5 O6 -145.3(5) . . . . ?

O14 Ni3 Ni5 O6 -73.7(5) . . . . ?

O7 Ni3 Ni5 O6 103.3(5) . . . . ?

Ni2 Ni3 Ni5 O6 -45.2(4) . . . . ?

Ni1 Ni3 Ni5 O6 11.1(4) . . . . ?

Ni4 Ni3 Ni5 O6 -114.2(4) . . . . ?

O2 Ni3 Ni5 Ni4 140.7(4) . . . . ?

O15 Ni3 Ni5 Ni4 -65.6(4) . . . . ?

O10 Ni3 Ni5 Ni4 -31.0(4) . . . . ?

O14 Ni3 Ni5 Ni4 40.6(3) . . . . ?

O7 Ni3 Ni5 Ni4 -142.5(3) . . . . ?

O6 Ni3 Ni5 Ni4 114.2(4) . . . . ?

Ni2 Ni3 Ni5 Ni4 69.01(18) . . . . ?

Ni1 Ni3 Ni5 Ni4 125.36(8) . . . . ?

O18 Ni6 Ni7 O17 -157.3(5) . . . . ?

O19 Ni6 Ni7 O17 103.7(5) . . . . ?

O21 Ni6 Ni7 O17 -74.7(5) . . . . ?

N7 Ni6 Ni7 O17 19.1(6) . . . . ?

N8 Ni6 Ni7 O17 179.9(7) . . . . ?

Ni8 Ni6 Ni7 O17 -126.6(4) . . . . ?

O18 Ni6 Ni7 O32 22.4(6) . . . . ?

O17 Ni6 Ni7 O32 179.6(6) . . . . ?

O19 Ni6 Ni7 O32 -76.7(5) . . . . ?

O21 Ni6 Ni7 O32 104.9(5) . . . . ?

N7 Ni6 Ni7 O32 -161.3(6) . . . . ?

N8 Ni6 Ni7 O32 -0.4(7) . . . . ?

Ni8 Ni6 Ni7 O32 53.0(4) . . . . ?

O18 Ni6 Ni7 N9 -178.1(6) . . . . ?

O17 Ni6 Ni7 N9 -20.9(6) . . . . ?

O19 Ni6 Ni7 N9 82.8(5) . . . . ?

O21 Ni6 Ni7 N9 -95.5(5) . . . . ?

N7 Ni6 Ni7 N9 -1.7(6) . . . . ?

N8 Ni6 Ni7 N9 159.1(7) . . . . ?

Ni8 Ni6 Ni7 N9 -147.5(5) . . . . ?

O18 Ni6 Ni7 O20 100.7(5) . . . . ?

O17 Ni6 Ni7 O20 -102.0(5) . . . . ?

O19 Ni6 Ni7 O20 1.6(4) . . . . ?

O21 Ni6 Ni7 O20 -176.7(4) . . . . ?

N7 Ni6 Ni7 O20 -82.9(5) . . . . ?

N8 Ni6 Ni7 O20 77.9(6) . . . . ?

Ni8 Ni6 Ni7 O20 131.3(3) . . . . ?

O17 Ni6 Ni7 O18 157.3(5) . . . . ?

O19 Ni6 Ni7 O18 -99.1(5) . . . . ?

O21 Ni6 Ni7 O18 82.6(5) . . . . ?

N7 Ni6 Ni7 O18 176.4(6) . . . . ?

N8 Ni6 Ni7 O18 -22.8(6) . . . . ?

Ni8 Ni6 Ni7 O18 30.6(4) . . . . ?

O18 Ni6 Ni7 O30 -68.6(5) . . . . ?

O17 Ni6 Ni7 O30 88.6(5) . . . . ?

O19 Ni6 Ni7 O30 -167.7(4) . . . . ?

O21 Ni6 Ni7 O30 13.9(4) . . . . ?

N7 Ni6 Ni7 O30 107.7(5) . . . . ?

N8 Ni6 Ni7 O30 -91.4(6) . . . . ?

Ni8 Ni6 Ni7 O30 -38.0(3) . . . . ?

O18 Ni6 Ni7 Ni8 -30.6(4) . . . . ?

O17 Ni6 Ni7 Ni8 126.6(4) . . . . ?

O19 Ni6 Ni7 Ni8 -129.7(3) . . . . ?

O21 Ni6 Ni7 Ni8 51.9(3) . . . . ?

N7 Ni6 Ni7 Ni8 145.8(5) . . . . ?

N8 Ni6 Ni7 Ni8 -53.4(5) . . . . ?

O17 Ni7 Ni8 O26 -105.5(5) . . . . ?

O32 Ni7 Ni8 O26 75.4(5) . . . . ?

N9 Ni7 Ni8 O26 -0.8(7) . . . . ?

O20 Ni7 Ni8 O26 154.2(5) . . . . ?

O18 Ni7 Ni8 O26 -171.5(6) . . . . ?

O30 Ni7 Ni8 O26 -26.0(6) . . . . ?

Ni6 Ni7 Ni8 O26 -139.5(4) . . . . ?

O17 Ni7 Ni8 O18 66.0(5) . . . . ?

O32 Ni7 Ni8 O18 -113.1(5) . . . . ?

N9 Ni7 Ni8 O18 170.7(7) . . . . ?

O20 Ni7 Ni8 O18 -34.2(5) . . . . ?

O30 Ni7 Ni8 O18 145.5(6) . . . . ?

Ni6 Ni7 Ni8 O18 32.0(4) . . . . ?

O17 Ni7 Ni8 O23 102.7(5) . . . . ?

O32 Ni7 Ni8 O23 -76.4(5) . . . . ?

N9 Ni7 Ni8 O23 -152.6(7) . . . . ?

O20 Ni7 Ni8 O23 2.4(5) . . . . ?

O18 Ni7 Ni8 O23 36.7(5) . . . . ?

O30 Ni7 Ni8 O23 -177.8(6) . . . . ?

Ni6 Ni7 Ni8 O23 68.7(4) . . . . ?

O17 Ni7 Ni8 O31 176.8(5) . . . . ?

O32 Ni7 Ni8 O31 -2.3(5) . . . . ?

N9 Ni7 Ni8 O31 -78.5(7) . . . . ?

O20 Ni7 Ni8 O31 76.5(5) . . . . ?

O18 Ni7 Ni8 O31 110.7(5) . . . . ?

O30 Ni7 Ni8 O31 -103.7(5) . . . . ?

Ni6 Ni7 Ni8 O31 142.8(3) . . . . ?

O17 Ni7 Ni8 O30 -79.5(5) . . . . ?

O32 Ni7 Ni8 O30 101.4(5) . . . . ?

N9 Ni7 Ni8 O30 25.2(7) . . . . ?

O20 Ni7 Ni8 O30 -179.8(5) . . . . ?

O18 Ni7 Ni8 O30 -145.5(6) . . . . ?

Ni6 Ni7 Ni8 O30 -113.5(4) . . . . ?

O17 Ni7 Ni8 O22 -8.3(4) . . . . ?

O32 Ni7 Ni8 O22 172.6(5) . . . . ?

N9 Ni7 Ni8 O22 96.4(7) . . . . ?

O20 Ni7 Ni8 O22 -108.5(5) . . . . ?

O18 Ni7 Ni8 O22 -74.3(5) . . . . ?

O30 Ni7 Ni8 O22 71.2(5) . . . . ?

Ni6 Ni7 Ni8 O22 -42.3(3) . . . . ?

O17 Ni7 Ni8 Ni10 -39.2(4) . . . . ?

O32 Ni7 Ni8 Ni10 141.7(4) . . . . ?

N9 Ni7 Ni8 Ni10 65.5(6) . . . . ?

O20 Ni7 Ni8 Ni10 -139.4(4) . . . . ?

O18 Ni7 Ni8 Ni10 -105.2(4) . . . . ?

O30 Ni7 Ni8 Ni10 40.4(4) . . . . ?

Ni6 Ni7 Ni8 Ni10 -73.16(17) . . . . ?

O17 Ni7 Ni8 Ni9 -92.7(3) . . . . ?

O32 Ni7 Ni8 Ni9 88.2(4) . . . . ?

N9 Ni7 Ni8 Ni9 12.0(6) . . . . ?

O20 Ni7 Ni8 Ni9 167.0(4) . . . . ?

O18 Ni7 Ni8 Ni9 -158.7(4) . . . . ?

O30 Ni7 Ni8 Ni9 -13.2(4) . . . . ?

Ni6 Ni7 Ni8 Ni9 -126.70(8) . . . . ?

O17 Ni7 Ni8 Ni6 34.0(3) . . . . ?

O32 Ni7 Ni8 Ni6 -145.1(4) . . . . ?

N9 Ni7 Ni8 Ni6 138.7(6) . . . . ?

O20 Ni7 Ni8 Ni6 -66.3(4) . . . . ?

O18 Ni7 Ni8 Ni6 -32.0(4) . . . . ?

O30 Ni7 Ni8 Ni6 113.5(4) . . . . ?

O18 Ni6 Ni8 O26 174.9(9) . . . . ?

O17 Ni6 Ni8 O26 85.4(7) . . . . ?

O19 Ni6 Ni8 O26 173.1(7) . . . . ?

O21 Ni6 Ni8 O26 -3.7(7) . . . . ?

N7 Ni6 Ni8 O26 7.3(10) . . . . ?

N8 Ni6 Ni8 O26 -90.2(7) . . . . ?

Ni7 Ni6 Ni8 O26 117.8(6) . . . . ?

O17 Ni6 Ni8 O18 -89.5(7) . . . . ?

O19 Ni6 Ni8 O18 -1.8(7) . . . . ?

O21 Ni6 Ni8 O18 -178.6(7) . . . . ?

N7 Ni6 Ni8 O18 -167.6(10) . . . . ?

N8 Ni6 Ni8 O18 94.9(7) . . . . ?

Ni7 Ni6 Ni8 O18 -57.0(6) . . . . ?

O18 Ni6 Ni8 O23 -75.7(7) . . . . ?

O17 Ni6 Ni8 O23 -165.2(4) . . . . ?

O19 Ni6 Ni8 O23 -77.5(4) . . . . ?

O21 Ni6 Ni8 O23 105.8(4) . . . . ?

N7 Ni6 Ni8 O23 116.8(8) . . . . ?

N8 Ni6 Ni8 O23 19.3(4) . . . . ?

Ni7 Ni6 Ni8 O23 -132.7(3) . . . . ?

O18 Ni6 Ni8 O31 14.8(7) . . . . ?

O17 Ni6 Ni8 O31 -74.7(5) . . . . ?

O19 Ni6 Ni8 O31 13.0(5) . . . . ?

O21 Ni6 Ni8 O31 -163.7(5) . . . . ?

N7 Ni6 Ni8 O31 -152.7(8) . . . . ?

N8 Ni6 Ni8 O31 109.8(5) . . . . ?

Ni7 Ni6 Ni8 O31 -42.2(4) . . . . ?

O18 Ni6 Ni8 O30 97.4(7) . . . . ?

O17 Ni6 Ni8 O30 7.9(4) . . . . ?

O19 Ni6 Ni8 O30 95.6(4) . . . . ?

O21 Ni6 Ni8 O30 -81.2(4) . . . . ?

N7 Ni6 Ni8 O30 -70.1(8) . . . . ?

N8 Ni6 Ni8 O30 -167.6(4) . . . . ?

Ni7 Ni6 Ni8 O30 40.4(3) . . . . ?

O18 Ni6 Ni8 O22 -164.5(7) . . . . ?

O17 Ni6 Ni8 O22 106.0(4) . . . . ?

O19 Ni6 Ni8 O22 -166.4(4) . . . . ?

O21 Ni6 Ni8 O22 16.9(4) . . . . ?

N7 Ni6 Ni8 O22 27.9(8) . . . . ?

N8 Ni6 Ni8 O22 -69.6(4) . . . . ?

Ni7 Ni6 Ni8 O22 138.4(3) . . . . ?

O18 Ni6 Ni8 Ni7 57.0(6) . . . . ?

O17 Ni6 Ni8 Ni7 -32.5(3) . . . . ?

O19 Ni6 Ni8 Ni7 55.2(3) . . . . ?

O21 Ni6 Ni8 Ni7 -121.5(3) . . . . ?

N7 Ni6 Ni8 Ni7 -110.5(8) . . . . ?

N8 Ni6 Ni8 Ni7 152.0(3) . . . . ?

O18 Ni6 Ni8 Ni10 -156.6(6) . . . . ?

O17 Ni6 Ni8 Ni10 113.9(3) . . . . ?

O19 Ni6 Ni8 Ni10 -158.4(3) . . . . ?

O21 Ni6 Ni8 Ni10 24.9(3) . . . . ?

N7 Ni6 Ni8 Ni10 35.9(8) . . . . ?

N8 Ni6 Ni8 Ni10 -61.6(3) . . . . ?

Ni7 Ni6 Ni8 Ni10 146.41(10) . . . . ?

O18 Ni6 Ni8 Ni9 144.8(6) . . . . ?

O17 Ni6 Ni8 Ni9 55.3(3) . . . . ?

O19 Ni6 Ni8 Ni9 142.9(3) . . . . ?

O21 Ni6 Ni8 Ni9 -33.8(3) . . . . ?

N7 Ni6 Ni8 Ni9 -22.8(8) . . . . ?

N8 Ni6 Ni8 Ni9 -120.3(3) . . . . ?

Ni7 Ni6 Ni8 Ni9 87.73(10) . . . . ?

O26 Ni8 Ni9 O25 -87.5(7) . . . . ?

O18 Ni8 Ni9 O25 84.7(6) . . . . ?

O23 Ni8 Ni9 O25 -79.4(4) . . . . ?

O31 Ni8 Ni9 O25 -167.2(4) . . . . ?

O30 Ni8 Ni9 O25 104.3(4) . . . . ?

O22 Ni8 Ni9 O25 6.6(4) . . . . ?

Ni7 Ni8 Ni9 O25 113.8(3) . . . . ?

Ni10 Ni8 Ni9 O25 -33.3(3) . . . . ?

Ni6 Ni8 Ni9 O25 55.5(3) . . . . ?

O18 Ni8 Ni9 O26 172.2(9) . . . . ?

O23 Ni8 Ni9 O26 8.0(8) . . . . ?

O31 Ni8 Ni9 O26 -79.8(7) . . . . ?

O30 Ni8 Ni9 O26 -168.3(7) . . . . ?

O22 Ni8 Ni9 O26 94.1(7) . . . . ?

Ni7 Ni8 Ni9 O26 -158.8(7) . . . . ?

Ni10 Ni8 Ni9 O26 54.2(7) . . . . ?

Ni6 Ni8 Ni9 O26 142.9(7) . . . . ?

O26 Ni8 Ni9 O28 2.0(8) . . . . ?

O18 Ni8 Ni9 O28 174.2(6) . . . . ?

O23 Ni8 Ni9 O28 10.0(5) . . . . ?

O31 Ni8 Ni9 O28 -77.8(5) . . . . ?

O30 Ni8 Ni9 O28 -166.3(5) . . . . ?

O22 Ni8 Ni9 O28 96.1(4) . . . . ?

Ni7 Ni8 Ni9 O28 -156.8(4) . . . . ?

Ni10 Ni8 Ni9 O28 56.2(4) . . . . ?

Ni6 Ni8 Ni9 O28 144.9(4) . . . . ?

O26 Ni8 Ni9 O29 -176.2(8) . . . . ?

O18 Ni8 Ni9 O29 -4.0(6) . . . . ?

O23 Ni8 Ni9 O29 -168.2(4) . . . . ?

O31 Ni8 Ni9 O29 104.0(4) . . . . ?

O30 Ni8 Ni9 O29 15.5(4) . . . . ?

O22 Ni8 Ni9 O29 -82.1(4) . . . . ?

Ni7 Ni8 Ni9 O29 25.0(3) . . . . ?

Ni10 Ni8 Ni9 O29 -122.0(3) . . . . ?

Ni6 Ni8 Ni9 O29 -33.3(3) . . . . ?

O26 Ni8 Ni9 N10 -165.2(11) . . . . ?

O18 Ni8 Ni9 N10 7.0(10) . . . . ?

O23 Ni8 Ni9 N10 -157.2(9) . . . . ?

O31 Ni8 Ni9 N10 115.0(9) . . . . ?

O30 Ni8 Ni9 N10 26.5(9) . . . . ?

O22 Ni8 Ni9 N10 -71.1(9) . . . . ?

Ni7 Ni8 Ni9 N10 36.0(9) . . . . ?

Ni10 Ni8 Ni9 N10 -111.0(9) . . . . ?

Ni6 Ni8 Ni9 N10 -22.3(9) . . . . ?

O26 Ni8 Ni9 N11 96.6(8) . . . . ?

O18 Ni8 Ni9 N11 -91.3(6) . . . . ?

O23 Ni8 Ni9 N11 104.6(5) . . . . ?

O31 Ni8 Ni9 N11 16.8(5) . . . . ?

O30 Ni8 Ni9 N11 -71.7(5) . . . . ?

O22 Ni8 Ni9 N11 -169.4(5) . . . . ?

Ni7 Ni8 Ni9 N11 -62.2(4) . . . . ?

Ni10 Ni8 Ni9 N11 150.8(4) . . . . ?

Ni6 Ni8 Ni9 N11 -120.5(4) . . . . ?

O26 Ni8 Ni9 Ni10 -54.2(7) . . . . ?

O18 Ni8 Ni9 Ni10 118.0(5) . . . . ?

O23 Ni8 Ni9 Ni10 -46.2(3) . . . . ?

O31 Ni8 Ni9 Ni10 -134.0(3) . . . . ?

O30 Ni8 Ni9 Ni10 137.5(3) . . . . ?

O22 Ni8 Ni9 Ni10 39.9(3) . . . . ?

Ni7 Ni8 Ni9 Ni10 147.04(9) . . . . ?

Ni6 Ni8 Ni9 Ni10 88.73(10) . . . . ?

O26 Ni9 Ni10 O25 -154.6(5) . . . . ?

O28 Ni9 Ni10 O25 105.9(5) . . . . ?

O29 Ni9 Ni10 O25 -72.9(5) . . . . ?

N10 Ni9 Ni10 O25 23.4(6) . . . . ?

N11 Ni9 Ni10 O25 -179.1(7) . . . . ?

Ni8 Ni9 Ni10 O25 -125.2(4) . . . . ?

O25 Ni9 Ni10 N12 -21.6(6) . . . . ?

O26 Ni9 Ni10 N12 -176.2(6) . . . . ?

O28 Ni9 Ni10 N12 84.4(5) . . . . ?

O29 Ni9 Ni10 N12 -94.5(5) . . . . ?

N10 Ni9 Ni10 N12 1.8(6) . . . . ?

N11 Ni9 Ni10 N12 159.3(7) . . . . ?

Ni8 Ni9 Ni10 N12 -146.8(4) . . . . ?

O25 Ni9 Ni10 O26 154.6(5) . . . . ?

O28 Ni9 Ni10 O26 -99.5(5) . . . . ?

O29 Ni9 Ni10 O26 81.7(5) . . . . ?

N10 Ni9 Ni10 O26 178.0(6) . . . . ?

N11 Ni9 Ni10 O26 -24.5(7) . . . . ?

Ni8 Ni9 Ni10 O26 29.4(4) . . . . ?

O25 Ni9 Ni10 O24 -179.2(5) . . . . ?

O26 Ni9 Ni10 O24 26.2(5) . . . . ?

O28 Ni9 Ni10 O24 -73.2(5) . . . . ?

O29 Ni9 Ni10 O24 107.9(5) . . . . ?

N10 Ni9 Ni10 O24 -155.8(6) . . . . ?

N11 Ni9 Ni10 O24 1.7(7) . . . . ?

Ni8 Ni9 Ni10 O24 55.6(4) . . . . ?

O25 Ni9 Ni10 O27 -100.9(5) . . . . ?

O26 Ni9 Ni10 O27 104.5(5) . . . . ?

O28 Ni9 Ni10 O27 5.0(4) . . . . ?

O29 Ni9 Ni10 O27 -173.8(4) . . . . ?

N10 Ni9 Ni10 O27 -77.5(5) . . . . ?

N11 Ni9 Ni10 O27 80.0(7) . . . . ?

Ni8 Ni9 Ni10 O27 133.9(3) . . . . ?

O25 Ni9 Ni10 O22 87.3(4) . . . . ?

O26 Ni9 Ni10 O22 -67.3(5) . . . . ?

O28 Ni9 Ni10 O22 -166.8(4) . . . . ?

O29 Ni9 Ni10 O22 14.4(4) . . . . ?

N10 Ni9 Ni10 O22 110.7(5) . . . . ?

N11 Ni9 Ni10 O22 -91.8(6) . . . . ?

Ni8 Ni9 Ni10 O22 -37.9(3) . . . . ?

O25 Ni9 Ni10 Ni8 125.2(4) . . . . ?

O26 Ni9 Ni10 Ni8 -29.4(4) . . . . ?

O28 Ni9 Ni10 Ni8 -128.9(3) . . . . ?

O29 Ni9 Ni10 Ni8 52.3(3) . . . . ?

N10 Ni9 Ni10 Ni8 148.6(4) . . . . ?

N11 Ni9 Ni10 Ni8 -53.9(6) . . . . ?

O26 Ni8 Ni10 O25 65.8(5) . . . . ?

O18 Ni8 Ni10 O25 -106.4(5) . . . . ?

O23 Ni8 Ni10 O25 172.2(4) . . . . ?

O31 Ni8 Ni10 O25 97.2(5) . . . . ?

O30 Ni8 Ni10 O25 -9.0(4) . . . . ?

O22 Ni8 Ni10 O25 -81.2(5) . . . . ?

Ni7 Ni8 Ni10 O25 -37.2(3) . . . . ?

Ni9 Ni8 Ni10 O25 34.0(3) . . . . ?

Ni6 Ni8 Ni10 O25 -92.3(3) . . . . ?

O26 Ni8 Ni10 N12 171.8(8) . . . . ?

O18 Ni8 Ni10 N12 -0.4(7) . . . . ?

O23 Ni8 Ni10 N12 -81.8(7) . . . . ?

O31 Ni8 Ni10 N12 -156.8(7) . . . . ?

O30 Ni8 Ni10 N12 97.0(7) . . . . ?

O22 Ni8 Ni10 N12 24.8(7) . . . . ?

Ni7 Ni8 Ni10 N12 68.8(6) . . . . ?

Ni9 Ni8 Ni10 N12 140.0(6) . . . . ?

Ni6 Ni8 Ni10 N12 13.7(6) . . . . ?

O18 Ni8 Ni10 O26 -172.2(6) . . . . ?

O23 Ni8 Ni10 O26 106.4(5) . . . . ?

O31 Ni8 Ni10 O26 31.4(6) . . . . ?

O30 Ni8 Ni10 O26 -74.8(5) . . . . ?

O22 Ni8 Ni10 O26 -147.1(6) . . . . ?

Ni7 Ni8 Ni10 O26 -103.0(5) . . . . ?

Ni9 Ni8 Ni10 O26 -31.8(4) . . . . ?

Ni6 Ni8 Ni10 O26 -158.1(4) . . . . ?

O26 Ni8 Ni10 O24 -109.2(5) . . . . ?

O18 Ni8 Ni10 O24 78.6(5) . . . . ?

O23 Ni8 Ni10 O24 -2.8(4) . . . . ?

O31 Ni8 Ni10 O24 -77.8(5) . . . . ?

O30 Ni8 Ni10 O24 176.0(4) . . . . ?

O22 Ni8 Ni10 O24 103.8(5) . . . . ?

Ni7 Ni8 Ni10 O24 147.8(3) . . . . ?

Ni9 Ni8 Ni10 O24 -141.0(3) . . . . ?

Ni6 Ni8 Ni10 O24 92.7(3) . . . . ?

O26 Ni8 Ni10 O27 -32.9(6) . . . . ?

O18 Ni8 Ni10 O27 154.9(6) . . . . ?

O23 Ni8 Ni10 O27 73.4(5) . . . . ?

O31 Ni8 Ni10 O27 -1.6(6) . . . . ?

O30 Ni8 Ni10 O27 -107.8(5) . . . . ?

O22 Ni8 Ni10 O27 180.0(6) . . . . ?

Ni7 Ni8 Ni10 O27 -136.0(4) . . . . ?

Ni9 Ni8 Ni10 O27 -64.8(4) . . . . ?

Ni6 Ni8 Ni10 O27 169.0(4) . . . . ?

O26 Ni8 Ni10 O22 147.1(6) . . . . ?

O18 Ni8 Ni10 O22 -25.1(6) . . . . ?

O23 Ni8 Ni10 O22 -106.6(5) . . . . ?

O31 Ni8 Ni10 O22 178.4(6) . . . . ?

O30 Ni8 Ni10 O22 72.3(5) . . . . ?

Ni7 Ni8 Ni10 O22 44.0(4) . . . . ?

Ni9 Ni8 Ni10 O22 115.2(4) . . . . ?

Ni6 Ni8 Ni10 O22 -11.0(4) . . . . ?

O26 Ni8 Ni10 Ni9 31.8(4) . . . . ?

O18 Ni8 Ni10 Ni9 -140.3(4) . . . . ?

O23 Ni8 Ni10 Ni9 138.2(3) . . . . ?

O31 Ni8 Ni10 Ni9 63.2(4) . . . . ?

O30 Ni8 Ni10 Ni9 -43.0(3) . . . . ?

O22 Ni8 Ni10 Ni9 -115.2(4) . . . . ?

Ni7 Ni8 Ni10 Ni9 -71.17(17) . . . . ?

Ni6 Ni8 Ni10 Ni9 -126.22(8) . . . . ?

O16 Ni2 O1 C5 176(100) . . . . ?

N3 Ni2 O1 C5 -15.2(11) . . . . ?

O2 Ni2 O1 C5 163.7(11) . . . . ?

O4 Ni2 O1 C5 74.5(11) . . . . ?

O14 Ni2 O1 C5 -118.6(11) . . . . ?

Ni1 Ni2 O1 C5 148.3(12) . . . . ?

Ni3 Ni2 O1 C5 -159.5(10) . . . . ?

O16 Ni2 O1 Ni1 28(11) . . . . ?

N3 Ni2 O1 Ni1 -163.6(4) . . . . ?

O2 Ni2 O1 Ni1 15.4(3) . . . . ?

O4 Ni2 O1 Ni1 -73.8(4) . . . . ?

O14 Ni2 O1 Ni1 93.1(4) . . . . ?

Ni3 Ni2 O1 Ni1 52.2(3) . . . . ?

O2 Ni1 O1 C5 -164.4(11) . . . . ?

O3 Ni1 O1 C5 -76.2(11) . . . . ?

O5 Ni1 O1 C5 104.4(11) . . . . ?

N1 Ni1 O1 C5 16.0(11) . . . . ?

N2 Ni1 O1 C5 32(4) . . . . ?

Ni2 Ni1 O1 C5 -148.7(12) . . . . ?

Ni3 Ni1 O1 C5 170.2(11) . . . . ?

O2 Ni1 O1 Ni2 -15.6(3) . . . . ?

O3 Ni1 O1 Ni2 72.5(4) . . . . ?

O5 Ni1 O1 Ni2 -106.9(4) . . . . ?

N1 Ni1 O1 Ni2 164.7(4) . . . . ?

N2 Ni1 O1 Ni2 -179(100) . . . . ?

Ni3 Ni1 O1 Ni2 -41.1(3) . . . . ?

O15 Ni3 O2 Ni1 167.8(6) . . . . ?

O10 Ni3 O2 Ni1 40(4) . . . . ?

O14 Ni3 O2 Ni1 77.4(6) . . . . ?

O7 Ni3 O2 Ni1 -105.9(6) . . . . ?

O6 Ni3 O2 Ni1 -15.4(6) . . . . ?

Ni2 Ni3 O2 Ni1 100.9(7) . . . . ?

Ni5 Ni3 O2 Ni1 -33.8(8) . . . . ?

Ni4 Ni3 O2 Ni1 59.4(9) . . . . ?

O15 Ni3 O2 Ni2 66.9(4) . . . . ?

O10 Ni3 O2 Ni2 -61(4) . . . . ?

O14 Ni3 O2 Ni2 -23.5(4) . . . . ?

O7 Ni3 O2 Ni2 153.2(4) . . . . ?

O6 Ni3 O2 Ni2 -116.4(4) . . . . ?

Ni5 Ni3 O2 Ni2 -134.7(2) . . . . ?

Ni1 Ni3 O2 Ni2 -100.9(7) . . . . ?

Ni4 Ni3 O2 Ni2 -41.6(6) . . . . ?

O1 Ni1 O2 Ni3 -88.0(6) . . . . ?

O3 Ni1 O2 Ni3 -179.5(6) . . . . ?

O5 Ni1 O2 Ni3 -1.9(6) . . . . ?

N1 Ni1 O2 Ni3 -84(4) . . . . ?

N2 Ni1 O2 Ni3 90.3(7) . . . . ?

Ni2 Ni1 O2 Ni3 -103.1(7) . . . . ?

O1 Ni1 O2 Ni2 15.1(3) . . . . ?

O3 Ni1 O2 Ni2 -76.4(4) . . . . ?

O5 Ni1 O2 Ni2 101.2(4) . . . . ?

N1 Ni1 O2 Ni2 19(4) . . . . ?

N2 Ni1 O2 Ni2 -166.6(4) . . . . ?

Ni3 Ni1 O2 Ni2 103.1(7) . . . . ?

O1 Ni2 O2 Ni3 115.1(4) . . . . ?

O16 Ni2 O2 Ni3 -64.4(4) . . . . ?

N3 Ni2 O2 Ni3 124(4) . . . . ?

O4 Ni2 O2 Ni3 -153.1(4) . . . . ?

O14 Ni2 O2 Ni3 22.6(4) . . . . ?

Ni1 Ni2 O2 Ni3 130.5(5) . . . . ?

O1 Ni2 O2 Ni1 -15.3(4) . . . . ?

O16 Ni2 O2 Ni1 165.2(4) . . . . ?

N3 Ni2 O2 Ni1 -6(4) . . . . ?

O4 Ni2 O2 Ni1 76.5(4) . . . . ?

O14 Ni2 O2 Ni1 -107.9(4) . . . . ?

Ni3 Ni2 O2 Ni1 -130.5(5) . . . . ?

O1 Ni1 O3 C39 -41.2(11) . . . . ?

O2 Ni1 O3 C39 42.6(11) . . . . ?

O5 Ni1 O3 C39 -27(10) . . . . ?

N1 Ni1 O3 C39 -131.5(11) . . . . ?

N2 Ni1 O3 C39 144.6(11) . . . . ?

Ni2 Ni1 O3 C39 -0.6(10) . . . . ?

Ni3 Ni1 O3 C39 42.4(11) . . . . ?

O1 Ni2 O4 C39 44.1(11) . . . . ?

O16 Ni2 O4 C39 -133.5(11) . . . . ?

N3 Ni2 O4 C39 133.8(11) . . . . ?

O2 Ni2 O4 C39 -39.5(10) . . . . ?

O14 Ni2 O4 C39 -58(2) . . . . ?

Ni1 Ni2 O4 C39 2.7(10) . . . . ?

Ni3 Ni2 O4 C39 -60.5(11) . . . . ?

O1 Ni1 O5 C41 104.7(15) . . . . ?

O2 Ni1 O5 C41 21.0(15) . . . . ?

O3 Ni1 O5 C41 90(9) . . . . ?

N1 Ni1 O5 C41 -164.9(15) . . . . ?

N2 Ni1 O5 C41 -81.0(15) . . . . ?

Ni2 Ni1 O5 C41 64.3(15) . . . . ?

Ni3 Ni1 O5 C41 20.1(14) . . . . ?

O2 Ni3 O6 C41 38.1(12) . . . . ?

O15 Ni3 O6 C41 -159(2) . . . . ?

O10 Ni3 O6 C41 -137.3(12) . . . . ?

O14 Ni3 O6 C41 -43.6(12) . . . . ?

O7 Ni3 O6 C41 128.6(12) . . . . ?

Ni2 Ni3 O6 C41 -1.7(12) . . . . ?

Ni5 Ni3 O6 C41 -159.4(13) . . . . ?

Ni1 Ni3 O6 C41 31.2(11) . . . . ?

Ni4 Ni3 O6 C41 -112.7(12) . . . . ?

O2 Ni3 O6 Ni5 -162.5(4) . . . . ?

O15 Ni3 O6 Ni5 1(2) . . . . ?

O10 Ni3 O6 Ni5 22.2(4) . . . . ?

O14 Ni3 O6 Ni5 115.8(4) . . . . ?

O7 Ni3 O6 Ni5 -71.9(4) . . . . ?

Ni2 Ni3 O6 Ni5 157.73(19) . . . . ?

Ni1 Ni3 O6 Ni5 -169.4(4) . . . . ?

Ni4 Ni3 O6 Ni5 46.8(2) . . . . ?

O9 Ni5 O6 C41 51.3(13) . . . . ?

O8 Ni5 O6 C41 -132.2(13) . . . . ?

N6 Ni5 O6 C41 -39.7(14) . . . . ?

O10 Ni5 O6 C41 133.5(14) . . . . ?

O11 Ni5 O6 C41 156.8(18) . . . . ?

Ni4 Ni5 O6 C41 93.9(13) . . . . ?

Ni3 Ni5 O6 C41 155.5(15) . . . . ?

O9 Ni5 O6 Ni3 -104.3(4) . . . . ?

O8 Ni5 O6 Ni3 72.3(4) . . . . ?

N6 Ni5 O6 Ni3 164.8(5) . . . . ?

O10 Ni5 O6 Ni3 -22.0(3) . . . . ?

O11 Ni5 O6 Ni3 1(2) . . . . ?

Ni4 Ni5 O6 Ni3 -61.7(3) . . . . ?

O2 Ni3 O7 C43 139.8(14) . . . . ?

O15 Ni3 O7 C43 -125.7(14) . . . . ?

O10 Ni3 O7 C43 -37.1(14) . . . . ?

O14 Ni3 O7 C43 162(2) . . . . ?

O6 Ni3 O7 C43 43.7(14) . . . . ?

Ni2 Ni3 O7 C43 161.7(13) . . . . ?

Ni5 Ni3 O7 C43 0.5(13) . . . . ?

Ni1 Ni3 O7 C43 115.2(14) . . . . ?

Ni4 Ni3 O7 C43 -32.0(15) . . . . ?

O9 Ni5 O8 C43 57(7) . . . . ?

N6 Ni5 O8 C43 -146.0(14) . . . . ?

O10 Ni5 O8 C43 33.9(15) . . . . ?

O11 Ni5 O8 C43 122.5(15) . . . . ?

O6 Ni5 O8 C43 -44.7(14) . . . . ?

Ni4 Ni5 O8 C43 50.1(16) . . . . ?

Ni3 Ni5 O8 C43 -2.9(14) . . . . ?

O8 Ni5 O9 C24 146(6) . . . . ?

N6 Ni5 O9 C24 -10.6(11) . . . . ?

O10 Ni5 O9 C24 169.6(11) . . . . ?

O11 Ni5 O9 C24 81.1(11) . . . . ?

O6 Ni5 O9 C24 -112.0(11) . . . . ?

Ni4 Ni5 O9 C24 153.7(12) . . . . ?

Ni3 Ni5 O9 C24 -154.4(10) . . . . ?

O8 Ni5 O9 Ni4 -8(7) . . . . ?

N6 Ni5 O9 Ni4 -164.4(4) . . . . ?

O10 Ni5 O9 Ni4 15.9(3) . . . . ?

O11 Ni5 O9 Ni4 -72.6(4) . . . . ?

O6 Ni5 O9 Ni4 94.2(4) . . . . ?

Ni3 Ni5 O9 Ni4 51.9(3) . . . . ?

O10 Ni4 O9 C24 -169.6(11) . . . . ?

O12 Ni4 O9 C24 -82.8(12) . . . . ?

O13 Ni4 O9 C24 99.2(11) . . . . ?

N4 Ni4 O9 C24 9.0(12) . . . . ?

N5 Ni4 O9 C24 36(7) . . . . ?

Ni5 Ni4 O9 C24 -153.3(13) . . . . ?

Ni3 Ni4 O9 C24 165.6(11) . . . . ?

O10 Ni4 O9 Ni5 -16.3(4) . . . . ?

O12 Ni4 O9 Ni5 70.5(4) . . . . ?

O13 Ni4 O9 Ni5 -107.5(4) . . . . ?

N4 Ni4 O9 Ni5 162.3(4) . . . . ?

N5 Ni4 O9 Ni5 -171(6) . . . . ?

Ni3 Ni4 O9 Ni5 -41.1(3) . . . . ?

O9 Ni4 O10 Ni3 -90.0(6) . . . . ?

O12 Ni4 O10 Ni3 176.9(6) . . . . ?

O13 Ni4 O10 Ni3 -4.1(6) . . . . ?

N4 Ni4 O10 Ni3 -102(3) . . . . ?

N5 Ni4 O10 Ni3 88.3(7) . . . . ?

Ni5 Ni4 O10 Ni3 -105.6(6) . . . . ?

O9 Ni4 O10 Ni5 15.6(3) . . . . ?

O12 Ni4 O10 Ni5 -77.5(4) . . . . ?

O13 Ni4 O10 Ni5 101.5(4) . . . . ?

N4 Ni4 O10 Ni5 4(4) . . . . ?

N5 Ni4 O10 Ni5 -166.1(4) . . . . ?

Ni3 Ni4 O10 Ni5 105.6(6) . . . . ?

O2 Ni3 O10 Ni4 23(4) . . . . ?

O15 Ni3 O10 Ni4 -104.6(6) . . . . ?

O14 Ni3 O10 Ni4 -13.6(6) . . . . ?

O7 Ni3 O10 Ni4 169.2(6) . . . . ?

O6 Ni3 O10 Ni4 79.4(6) . . . . ?

Ni2 Ni3 O10 Ni4 -32.4(8) . . . . ?

Ni5 Ni3 O10 Ni4 103.4(7) . . . . ?

Ni1 Ni3 O10 Ni4 57.0(9) . . . . ?

O2 Ni3 O10 Ni5 -80(4) . . . . ?

O15 Ni3 O10 Ni5 152.0(5) . . . . ?

O14 Ni3 O10 Ni5 -117.0(4) . . . . ?

O7 Ni3 O10 Ni5 65.8(4) . . . . ?

O6 Ni3 O10 Ni5 -24.0(4) . . . . ?

Ni2 Ni3 O10 Ni5 -135.8(2) . . . . ?

Ni1 Ni3 O10 Ni5 -46.4(7) . . . . ?

Ni4 Ni3 O10 Ni5 -103.4(7) . . . . ?

O9 Ni5 O10 Ni4 -16.0(3) . . . . ?

O8 Ni5 O10 Ni4 162.6(4) . . . . ?

N6 Ni5 O10 Ni4 -18(4) . . . . ?

O11 Ni5 O10 Ni4 76.1(4) . . . . ?

O6 Ni5 O10 Ni4 -109.2(4) . . . . ?

Ni3 Ni5 O10 Ni4 -132.6(5) . . . . ?

O9 Ni5 O10 Ni3 116.6(4) . . . . ?

O8 Ni5 O10 Ni3 -64.8(4) . . . . ?

N6 Ni5 O10 Ni3 114(4) . . . . ?

O11 Ni5 O10 Ni3 -151.3(4) . . . . ?

O6 Ni5 O10 Ni3 23.4(4) . . . . ?

Ni4 Ni5 O10 Ni3 132.6(5) . . . . ?

O9 Ni5 O11 C45 47.6(13) . . . . ?

O8 Ni5 O11 C45 -129.2(13) . . . . ?

N6 Ni5 O11 C45 138.3(14) . . . . ?

O10 Ni5 O11 C45 -35.1(13) . . . . ?

O6 Ni5 O11 C45 -58(3) . . . . ?

Ni4 Ni5 O11 C45 6.6(13) . . . . ?

Ni3 Ni5 O11 C45 -56.9(14) . . . . ?

O10 Ni4 O12 C45 42.6(14) . . . . ?

O9 Ni4 O12 C45 -40.1(14) . . . . ?

O13 Ni4 O12 C45 18(11) . . . . ?

N4 Ni4 O12 C45 -130.4(14) . . . . ?

N5 Ni4 O12 C45 143.5(15) . . . . ?

Ni5 Ni4 O12 C45 -0.6(13) . . . . ?

Ni3 Ni4 O12 C45 44.1(14) . . . . ?

O10 Ni4 O13 C47 19.2(14) . . . . ?

O9 Ni4 O13 C47 102.0(14) . . . . ?

O12 Ni4 O13 C47 44(11) . . . . ?

N4 Ni4 O13 C47 -167.8(15) . . . . ?

N5 Ni4 O13 C47 -81.6(15) . . . . ?

Ni5 Ni4 O13 C47 62.3(14) . . . . ?

Ni3 Ni4 O13 C47 17.3(13) . . . . ?

O2 Ni3 O14 C47 -135.7(13) . . . . ?

O15 Ni3 O14 C47 129.9(13) . . . . ?

O10 Ni3 O14 C47 40.9(13) . . . . ?

O7 Ni3 O14 C47 -158(2) . . . . ?

O6 Ni3 O14 C47 -40.1(13) . . . . ?

Ni2 Ni3 O14 C47 -157.9(15) . . . . ?

Ni5 Ni3 O14 C47 2.4(14) . . . . ?

Ni1 Ni3 O14 C47 -110.2(13) . . . . ?

Ni4 Ni3 O14 C47 35.0(13) . . . . ?

O2 Ni3 O14 Ni2 22.2(3) . . . . ?

O15 Ni3 O14 Ni2 -72.3(4) . . . . ?

O10 Ni3 O14 Ni2 -161.2(4) . . . . ?

O7 Ni3 O14 Ni2 0(3) . . . . ?

O6 Ni3 O14 Ni2 117.8(4) . . . . ?

Ni5 Ni3 O14 Ni2 160.3(2) . . . . ?

Ni1 Ni3 O14 Ni2 47.6(2) . . . . ?

Ni4 Ni3 O14 Ni2 -167.2(4) . . . . ?

O1 Ni2 O14 C47 51.0(14) . . . . ?

O16 Ni2 O14 C47 -131.2(15) . . . . ?

N3 Ni2 O14 C47 -38.9(15) . . . . ?

O2 Ni2 O14 C47 134.2(14) . . . . ?

O4 Ni2 O14 C47 153.4(17) . . . . ?

Ni1 Ni2 O14 C47 93.8(14) . . . . ?

Ni3 Ni2 O14 C47 156.2(16) . . . . ?

O1 Ni2 O14 Ni3 -105.2(4) . . . . ?

O16 Ni2 O14 Ni3 72.6(5) . . . . ?

N3 Ni2 O14 Ni3 164.9(5) . . . . ?

O2 Ni2 O14 Ni3 -22.0(3) . . . . ?

O4 Ni2 O14 Ni3 -2.8(19) . . . . ?

Ni1 Ni2 O14 Ni3 -62.4(3) . . . . ?

O2 Ni3 O15 C49 -43.1(15) . . . . ?

O10 Ni3 O15 C49 132.4(15) . . . . ?

O14 Ni3 O15 C49 38.3(15) . . . . ?

O7 Ni3 O15 C49 -133.4(15) . . . . ?

O6 Ni3 O15 C49 154(2) . . . . ?

Ni2 Ni3 O15 C49 -4.7(14) . . . . ?

Ni5 Ni3 O15 C49 154.2(13) . . . . ?

Ni1 Ni3 O15 C49 -37.1(16) . . . . ?

Ni4 Ni3 O15 C49 108.8(14) . . . . ?

O1 Ni2 O16 C49 24(12) . . . . ?

N3 Ni2 O16 C49 -144.3(17) . . . . ?

O2 Ni2 O16 C49 36.7(18) . . . . ?

O4 Ni2 O16 C49 126.0(18) . . . . ?

O14 Ni2 O16 C49 -41.0(18) . . . . ?

Ni1 Ni2 O16 C49 51.0(19) . . . . ?

Ni3 Ni2 O16 C49 -0.2(17) . . . . ?

O32 Ni7 O17 C55 -159(18) . . . . ?

N9 Ni7 O17 C55 16.9(11) . . . . ?

O20 Ni7 O17 C55 -72.5(11) . . . . ?

O18 Ni7 O17 C55 -162.8(11) . . . . ?

O30 Ni7 O17 C55 119.2(11) . . . . ?

Ni6 Ni7 O17 C55 -147.6(12) . . . . ?

Ni8 Ni7 O17 C55 160.5(10) . . . . ?

O32 Ni7 O17 Ni6 -12(18) . . . . ?

N9 Ni7 O17 Ni6 164.4(4) . . . . ?

O20 Ni7 O17 Ni6 75.1(4) . . . . ?

O18 Ni7 O17 Ni6 -15.3(4) . . . . ?

O30 Ni7 O17 Ni6 -93.3(4) . . . . ?

Ni8 Ni7 O17 Ni6 -52.0(3) . . . . ?

O18 Ni6 O17 C55 163.7(10) . . . . ?

O19 Ni6 O17 C55 75.6(10) . . . . ?

O21 Ni6 O17 C55 -104.9(10) . . . . ?

N7 Ni6 O17 C55 -17.7(11) . . . . ?

N8 Ni6 O17 C55 -32(4) . . . . ?

Ni7 Ni6 O17 C55 147.9(12) . . . . ?

Ni8 Ni6 O17 C55 -171.1(10) . . . . ?

O18 Ni6 O17 Ni7 15.8(4) . . . . ?

O19 Ni6 O17 Ni7 -72.3(4) . . . . ?

O21 Ni6 O17 Ni7 107.2(4) . . . . ?

N7 Ni6 O17 Ni7 -165.5(4) . . . . ?

N8 Ni6 O17 Ni7 -180(100) . . . . ?

Ni8 Ni6 O17 Ni7 41.1(3) . . . . ?

O17 Ni6 O18 Ni8 87.7(6) . . . . ?

O19 Ni6 O18 Ni8 178.3(6) . . . . ?

O21 Ni6 O18 Ni8 1.3(7) . . . . ?

N7 Ni6 O18 Ni8 75(4) . . . . ?

N8 Ni6 O18 Ni8 -90.5(7) . . . . ?

Ni7 Ni6 O18 Ni8 102.7(7) . . . . ?

O17 Ni6 O18 Ni7 -15.0(4) . . . . ?

O19 Ni6 O18 Ni7 75.6(4) . . . . ?

O21 Ni6 O18 Ni7 -101.4(4) . . . . ?

N7 Ni6 O18 Ni7 -28(4) . . . . ?

N8 Ni6 O18 Ni7 166.8(4) . . . . ?

Ni8 Ni6 O18 Ni7 -102.7(7) . . . . ?

O26 Ni8 O18 Ni6 -25(4) . . . . ?

O23 Ni8 O18 Ni6 107.2(6) . . . . ?

O31 Ni8 O18 Ni6 -166.9(6) . . . . ?

O30 Ni8 O18 Ni6 -77.4(6) . . . . ?

O22 Ni8 O18 Ni6 14.7(7) . . . . ?

Ni7 Ni8 O18 Ni6 -100.5(7) . . . . ?

Ni10 Ni8 O18 Ni6 31.8(9) . . . . ?

Ni9 Ni8 O18 Ni6 -58.6(9) . . . . ?

O26 Ni8 O18 Ni7 75(4) . . . . ?

O23 Ni8 O18 Ni7 -152.3(4) . . . . ?

O31 Ni8 O18 Ni7 -66.4(4) . . . . ?

O30 Ni8 O18 Ni7 23.2(4) . . . . ?

O22 Ni8 O18 Ni7 115.2(4) . . . . ?

Ni10 Ni8 O18 Ni7 132.3(3) . . . . ?

Ni9 Ni8 O18 Ni7 41.9(7) . . . . ?

Ni6 Ni8 O18 Ni7 100.5(7) . . . . ?

O17 Ni7 O18 Ni6 15.4(4) . . . . ?

O32 Ni7 O18 Ni6 -164.5(4) . . . . ?

N9 Ni7 O18 Ni6 13(4) . . . . ?

O20 Ni7 O18 Ni6 -76.1(4) . . . . ?

O30 Ni7 O18 Ni6 108.2(4) . . . . ?

Ni8 Ni7 O18 Ni6 131.0(5) . . . . ?

O17 Ni7 O18 Ni8 -115.6(4) . . . . ?

O32 Ni7 O18 Ni8 64.5(4) . . . . ?

N9 Ni7 O18 Ni8 -118(4) . . . . ?

O20 Ni7 O18 Ni8 152.9(4) . . . . ?

O30 Ni7 O18 Ni8 -22.8(4) . . . . ?

Ni6 Ni7 O18 Ni8 -131.0(5) . . . . ?

O18 Ni6 O19 C95 -41.9(13) . . . . ?

O17 Ni6 O19 C95 42.1(13) . . . . ?

O21 Ni6 O19 C95 34(8) . . . . ?

N7 Ni6 O19 C95 132.4(13) . . . . ?

N8 Ni6 O19 C95 -144.3(13) . . . . ?

Ni7 Ni6 O19 C95 1.8(12) . . . . ?

Ni8 Ni6 O19 C95 -41.1(13) . . . . ?

O17 Ni7 O20 C95 -47.7(12) . . . . ?

O32 Ni7 O20 C95 130.9(12) . . . . ?

N9 Ni7 O20 C95 -137.6(12) . . . . ?

O18 Ni7 O20 C95 36.0(12) . . . . ?

O30 Ni7 O20 C95 57(2) . . . . ?

Ni6 Ni7 O20 C95 -5.7(11) . . . . ?

Ni8 Ni7 O20 C95 57.4(12) . . . . ?

O18 Ni6 O21 C93 -15.4(15) . . . . ?

O17 Ni6 O21 C93 -99.3(15) . . . . ?

O19 Ni6 O21 C93 -91(7) . . . . ?

N7 Ni6 O21 C93 170.2(15) . . . . ?

N8 Ni6 O21 C93 87.1(15) . . . . ?

Ni7 Ni6 O21 C93 -59.3(15) . . . . ?

Ni8 Ni6 O21 C93 -14.8(14) . . . . ?

O26 Ni8 O22 C93 139.7(12) . . . . ?

O18 Ni8 O22 C93 -36.3(12) . . . . ?

O23 Ni8 O22 C93 -129.8(12) . . . . ?

O31 Ni8 O22 C93 153(2) . . . . ?

O30 Ni8 O22 C93 44.3(12) . . . . ?

Ni7 Ni8 O22 C93 3.7(12) . . . . ?

Ni10 Ni8 O22 C93 160.7(14) . . . . ?

Ni9 Ni8 O22 C93 114.4(12) . . . . ?

Ni6 Ni8 O22 C93 -29.9(11) . . . . ?

O26 Ni8 O22 Ni10 -21.0(4) . . . . ?

O18 Ni8 O22 Ni10 163.0(4) . . . . ?

O23 Ni8 O22 Ni10 69.6(4) . . . . ?

O31 Ni8 O22 Ni10 -7(3) . . . . ?

O30 Ni8 O22 Ni10 -116.4(4) . . . . ?

Ni7 Ni8 O22 Ni10 -157.0(2) . . . . ?

Ni9 Ni8 O22 Ni10 -46.3(3) . . . . ?

Ni6 Ni8 O22 Ni10 169.4(4) . . . . ?

O25 Ni10 O22 C93 -53.1(15) . . . . ?

N12 Ni10 O22 C93 39.3(15) . . . . ?

O26 Ni10 O22 C93 -135.5(15) . . . . ?

O24 Ni10 O22 C93 132.5(15) . . . . ?

O27 Ni10 O22 C93 -156(2) . . . . ?

Ni9 Ni10 O22 C93 -95.4(14) . . . . ?

Ni8 Ni10 O22 C93 -156.2(16) . . . . ?

O25 Ni10 O22 Ni8 103.1(4) . . . . ?

N12 Ni10 O22 Ni8 -164.5(5) . . . . ?

O26 Ni10 O22 Ni8 20.7(4) . . . . ?

O24 Ni10 O22 Ni8 -71.3(4) . . . . ?

O27 Ni10 O22 Ni8 0(3) . . . . ?

Ni9 Ni10 O22 Ni8 60.8(3) . . . . ?

O26 Ni8 O23 C91 38.2(13) . . . . ?

O18 Ni8 O23 C91 -137.4(13) . . . . ?

O31 Ni8 O23 C91 128.7(13) . . . . ?

O30 Ni8 O23 C91 -172(3) . . . . ?

O22 Ni8 O23 C91 -41.8(13) . . . . ?

Ni7 Ni8 O23 C91 -160.8(11) . . . . ?

Ni10 Ni8 O23 C91 -0.3(12) . . . . ?

Ni9 Ni8 O23 C91 34.8(14) . . . . ?

Ni6 Ni8 O23 C91 -113.3(13) . . . . ?

O25 Ni10 O24 C91 -52(5) . . . . ?

N12 Ni10 O24 C91 150.1(15) . . . . ?

O26 Ni10 O24 C91 -28.7(15) . . . . ?

O27 Ni10 O24 C91 -121.8(15) . . . . ?

O22 Ni10 O24 C91 49.3(15) . . . . ?

Ni9 Ni10 O24 C91 -46.3(16) . . . . ?

Ni8 Ni10 O24 C91 8.2(14) . . . . ?

N12 Ni10 O25 C74 12.5(10) . . . . ?

O26 Ni10 O25 C74 -169.0(10) . . . . ?

O24 Ni10 O25 C74 -146(4) . . . . ?

O27 Ni10 O25 C74 -75.8(10) . . . . ?

O22 Ni10 O25 C74 113.3(10) . . . . ?

Ni9 Ni10 O25 C74 -151.8(12) . . . . ?

Ni8 Ni10 O25 C74 155.3(10) . . . . ?

N12 Ni10 O25 Ni9 164.3(4) . . . . ?

O26 Ni10 O25 Ni9 -17.2(4) . . . . ?

O24 Ni10 O25 Ni9 6(4) . . . . ?

O27 Ni10 O25 Ni9 76.0(4) . . . . ?

O22 Ni10 O25 Ni9 -94.9(4) . . . . ?

Ni8 Ni10 O25 Ni9 -52.9(3) . . . . ?

O26 Ni9 O25 C74 168.0(11) . . . . ?

O28 Ni9 O25 C74 79.8(11) . . . . ?

O29 Ni9 O25 C74 -100.1(11) . . . . ?

N10 Ni9 O25 C74 -11.7(11) . . . . ?

N11 Ni9 O25 C74 -35(5) . . . . ?

Ni10 Ni9 O25 C74 150.7(12) . . . . ?

Ni8 Ni9 O25 C74 -167.1(11) . . . . ?

O26 Ni9 O25 Ni10 17.3(4) . . . . ?

O28 Ni9 O25 Ni10 -70.8(4) . . . . ?

O29 Ni9 O25 Ni10 109.3(4) . . . . ?

N10 Ni9 O25 Ni10 -162.4(4) . . . . ?

N11 Ni9 O25 Ni10 174(5) . . . . ?

Ni8 Ni9 O25 Ni10 42.2(3) . . . . ?

O18 Ni8 O26 Ni9 -40(4) . . . . ?

O23 Ni8 O26 Ni9 -172.8(7) . . . . ?

O31 Ni8 O26 Ni9 101.5(7) . . . . ?

O30 Ni8 O26 Ni9 11.2(7) . . . . ?

O22 Ni8 O26 Ni9 -80.8(7) . . . . ?

Ni7 Ni8 O26 Ni9 28.8(9) . . . . ?

Ni10 Ni8 O26 Ni9 -103.2(7) . . . . ?

Ni6 Ni8 O26 Ni9 -61.0(10) . . . . ?

O18 Ni8 O26 Ni10 63(4) . . . . ?

O23 Ni8 O26 Ni10 -69.6(4) . . . . ?

O31 Ni8 O26 Ni10 -155.3(5) . . . . ?

O30 Ni8 O26 Ni10 114.4(4) . . . . ?

O22 Ni8 O26 Ni10 22.4(4) . . . . ?

Ni7 Ni8 O26 Ni10 131.9(3) . . . . ?

Ni9 Ni8 O26 Ni10 103.2(7) . . . . ?

Ni6 Ni8 O26 Ni10 42.2(8) . . . . ?

O25 Ni9 O26 Ni8 89.5(7) . . . . ?

O28 Ni9 O26 Ni8 -178.2(7) . . . . ?

O29 Ni9 O26 Ni8 3.5(7) . . . . ?

N10 Ni9 O26 Ni8 92(4) . . . . ?

N11 Ni9 O26 Ni8 -88.4(7) . . . . ?

Ni10 Ni9 O26 Ni8 106.3(8) . . . . ?

O25 Ni9 O26 Ni10 -16.7(3) . . . . ?

O28 Ni9 O26 Ni10 75.6(4) . . . . ?

O29 Ni9 O26 Ni10 -102.8(4) . . . . ?

N10 Ni9 O26 Ni10 -14(4) . . . . ?

N11 Ni9 O26 Ni10 165.4(4) . . . . ?

Ni8 Ni9 O26 Ni10 -106.3(8) . . . . ?

O25 Ni10 O26 Ni8 -115.1(4) . . . . ?

N12 Ni10 O26 Ni8 -99(5) . . . . ?

O24 Ni10 O26 Ni8 67.2(4) . . . . ?

O27 Ni10 O26 Ni8 154.6(5) . . . . ?

O22 Ni10 O26 Ni8 -22.1(4) . . . . ?

Ni9 Ni10 O26 Ni8 -132.0(5) . . . . ?

O25 Ni10 O26 Ni9 16.9(4) . . . . ?

N12 Ni10 O26 Ni9 33(5) . . . . ?

O24 Ni10 O26 Ni9 -160.8(4) . . . . ?

O27 Ni10 O26 Ni9 -73.4(4) . . . . ?

O22 Ni10 O26 Ni9 109.9(4) . . . . ?

Ni8 Ni10 O26 Ni9 132.0(5) . . . . ?

O25 Ni10 O27 C89 -45.4(12) . . . . ?

N12 Ni10 O27 C89 -137.5(13) . . . . ?

O26 Ni10 O27 C89 37.5(13) . . . . ?

O24 Ni10 O27 C89 129.2(13) . . . . ?

O22 Ni10 O27 C89 58(3) . . . . ?

Ni9 Ni10 O27 C89 -4.0(12) . . . . ?

Ni8 Ni10 O27 C89 57.7(13) . . . . ?

O25 Ni9 O28 C89 31.4(13) . . . . ?

O26 Ni9 O28 C89 -51.4(13) . . . . ?

O29 Ni9 O28 C89 35(17) . . . . ?

N10 Ni9 O28 C89 122.3(13) . . . . ?

N11 Ni9 O28 C89 -153.4(13) . . . . ?

Ni10 Ni9 O28 C89 -8.5(12) . . . . ?

Ni8 Ni9 O28 C89 -52.3(13) . . . . ?

O25 Ni9 O29 C99 -94.7(15) . . . . ?

O26 Ni9 O29 C99 -11.9(15) . . . . ?

O28 Ni9 O29 C99 -98(16) . . . . ?

N10 Ni9 O29 C99 174.3(15) . . . . ?

N11 Ni9 O29 C99 90.1(15) . . . . ?

Ni10 Ni9 O29 C99 -55.0(15) . . . . ?

Ni8 Ni9 O29 C99 -10.4(14) . . . . ?

O26 Ni8 O30 C99 -35.9(13) . . . . ?

O18 Ni8 O30 C99 139.4(13) . . . . ?

O23 Ni8 O30 C99 174(3) . . . . ?

O31 Ni8 O30 C99 -126.5(13) . . . . ?

O22 Ni8 O30 C99 44.3(13) . . . . ?

Ni7 Ni8 O30 C99 161.8(15) . . . . ?

Ni10 Ni8 O30 C99 3.1(13) . . . . ?

Ni9 Ni8 O30 C99 -30.9(12) . . . . ?

Ni6 Ni8 O30 C99 114.3(13) . . . . ?

O26 Ni8 O30 Ni7 162.3(4) . . . . ?

O18 Ni8 O30 Ni7 -22.4(4) . . . . ?

O23 Ni8 O30 Ni7 13(3) . . . . ?

O31 Ni8 O30 Ni7 71.7(4) . . . . ?

O22 Ni8 O30 Ni7 -117.5(4) . . . . ?

Ni10 Ni8 O30 Ni7 -158.7(2) . . . . ?

Ni9 Ni8 O30 Ni7 167.3(4) . . . . ?

Ni6 Ni8 O30 Ni7 -47.5(3) . . . . ?

O17 Ni7 O30 C99 -54.0(14) . . . . ?

O32 Ni7 O30 C99 127.3(14) . . . . ?

N9 Ni7 O30 C99 36.2(15) . . . . ?

O20 Ni7 O30 C99 -158.4(18) . . . . ?

O18 Ni7 O30 C99 -137.2(15) . . . . ?

Ni6 Ni7 O30 C99 -97.1(14) . . . . ?

Ni8 Ni7 O30 C99 -159.3(16) . . . . ?

O17 Ni7 O30 Ni8 105.3(4) . . . . ?

O32 Ni7 O30 Ni8 -73.4(5) . . . . ?

N9 Ni7 O30 Ni8 -164.5(4) . . . . ?

O20 Ni7 O30 Ni8 1(2) . . . . ?

O18 Ni7 O30 Ni8 22.1(4) . . . . ?

Ni6 Ni7 O30 Ni8 62.2(3) . . . . ?

O26 Ni8 O31 C97 -129.2(16) . . . . ?

O18 Ni8 O31 C97 47.1(16) . . . . ?

O23 Ni8 O31 C97 140.0(16) . . . . ?

O30 Ni8 O31 C97 -33.3(16) . . . . ?

O22 Ni8 O31 C97 -143(2) . . . . ?

Ni7 Ni8 O31 C97 8.5(15) . . . . ?

Ni10 Ni8 O31 C97 -148.9(14) . . . . ?

Ni9 Ni8 O31 C97 -104.6(15) . . . . ?

Ni6 Ni8 O31 C97 40.9(16) . . . . ?

O17 Ni7 O32 C97 -43(19) . . . . ?

N9 Ni7 O32 C97 140.7(18) . . . . ?

O20 Ni7 O32 C97 -130.0(18) . . . . ?

O18 Ni7 O32 C97 -39.6(18) . . . . ?

O30 Ni7 O32 C97 38.4(18) . . . . ?

Ni6 Ni7 O32 C97 -54.6(19) . . . . ?

Ni8 Ni7 O32 C97 -2.7(17) . . . . ?

O1 Ni1 N1 C8 32.5(9) . . . . ?

O2 Ni1 N1 C8 29(4) . . . . ?

O3 Ni1 N1 C8 123.9(9) . . . . ?

O5 Ni1 N1 C8 -53.7(9) . . . . ?

N2 Ni1 N1 C8 -145.8(9) . . . . ?

Ni2 Ni1 N1 C8 45.9(10) . . . . ?

Ni3 Ni1 N1 C8 -43.5(13) . . . . ?

O1 Ni1 N1 C9 -88.5(10) . . . . ?

O2 Ni1 N1 C9 -92(4) . . . . ?

O3 Ni1 N1 C9 2.8(10) . . . . ?

O5 Ni1 N1 C9 -174.7(10) . . . . ?

N2 Ni1 N1 C9 93.1(10) . . . . ?

Ni2 Ni1 N1 C9 -75.1(11) . . . . ?

Ni3 Ni1 N1 C9 -164.5(7) . . . . ?

O1 Ni1 N1 C11 150.8(8) . . . . ?

O2 Ni1 N1 C11 147(3) . . . . ?

O3 Ni1 N1 C11 -117.8(8) . . . . ?

O5 Ni1 N1 C11 64.6(8) . . . . ?

N2 Ni1 N1 C11 -27.5(8) . . . . ?

Ni2 Ni1 N1 C11 164.2(7) . . . . ?

Ni3 Ni1 N1 C11 74.8(11) . . . . ?

O1 Ni1 N2 C12 -15(4) . . . . ?

O2 Ni1 N2 C12 -178.1(8) . . . . ?

O3 Ni1 N2 C12 93.5(9) . . . . ?

O5 Ni1 N2 C12 -86.9(9) . . . . ?

N1 Ni1 N2 C12 1.3(9) . . . . ?

Ni2 Ni1 N2 C12 166.1(7) . . . . ?

Ni3 Ni1 N2 C12 -152.3(8) . . . . ?

O1 Ni1 N2 C14 -139(4) . . . . ?

O2 Ni1 N2 C14 58.0(10) . . . . ?

O3 Ni1 N2 C14 -30.4(10) . . . . ?

O5 Ni1 N2 C14 149.2(10) . . . . ?

N1 Ni1 N2 C14 -122.6(10) . . . . ?

Ni2 Ni1 N2 C14 42.2(12) . . . . ?

Ni3 Ni1 N2 C14 83.8(10) . . . . ?

O1 Ni1 N2 C13 103(4) . . . . ?

O2 Ni1 N2 C13 -60.6(10) . . . . ?

O3 Ni1 N2 C13 -148.9(9) . . . . ?

O5 Ni1 N2 C13 30.7(10) . . . . ?

N1 Ni1 N2 C13 118.9(10) . . . . ?

Ni2 Ni1 N2 C13 -76.4(11) . . . . ?

Ni3 Ni1 N2 C13 -34.8(10) . . . . ?

O1 Ni2 N3 C15 20.8(13) . . . . ?

O16 Ni2 N3 C15 -159.7(13) . . . . ?

O2 Ni2 N3 C15 12(4) . . . . ?

O4 Ni2 N3 C15 -71.0(13) . . . . ?

O14 Ni2 N3 C15 111.9(13) . . . . ?

Ni1 Ni2 N3 C15 6.2(15) . . . . ?

Ni3 Ni2 N3 C15 128.6(11) . . . . ?

O1 Ni2 N3 C16 -166.4(12) . . . . ?

O16 Ni2 N3 C16 13.1(13) . . . . ?

O2 Ni2 N3 C16 -175(3) . . . . ?

O4 Ni2 N3 C16 101.9(12) . . . . ?

O14 Ni2 N3 C16 -75.3(12) . . . . ?

Ni1 Ni2 N3 C16 179.0(10) . . . . ?

Ni3 Ni2 N3 C16 -58.5(15) . . . . ?

O10 Ni4 N4 C30 164(3) . . . . ?

O9 Ni4 N4 C30 152.0(9) . . . . ?

O12 Ni4 N4 C30 -115.2(10) . . . . ?

O13 Ni4 N4 C30 66.1(9) . . . . ?

N5 Ni4 N4 C30 -26.1(10) . . . . ?

Ni5 Ni4 N4 C30 167.1(8) . . . . ?

Ni3 Ni4 N4 C30 77.5(13) . . . . ?

O10 Ni4 N4 C27 49(4) . . . . ?

O9 Ni4 N4 C27 37.4(11) . . . . ?

O12 Ni4 N4 C27 130.2(11) . . . . ?

O13 Ni4 N4 C27 -48.6(11) . . . . ?

N5 Ni4 N4 C27 -140.8(11) . . . . ?

Ni5 Ni4 N4 C27 52.5(12) . . . . ?

Ni3 Ni4 N4 C27 -37.2(17) . . . . ?

O10 Ni4 N4 C28 -76(4) . . . . ?

O9 Ni4 N4 C28 -87.5(11) . . . . ?

O12 Ni4 N4 C28 5.3(11) . . . . ?

O13 Ni4 N4 C28 -173.4(11) . . . . ?

N5 Ni4 N4 C28 94.4(11) . . . . ?

Ni5 Ni4 N4 C28 -72.3(11) . . . . ?

Ni3 Ni4 N4 C28 -162.0(8) . . . . ?

O10 Ni4 N5 C32 56.3(12) . . . . ?

O9 Ni4 N5 C32 -149(6) . . . . ?

O12 Ni4 N5 C32 -30.7(12) . . . . ?

O13 Ni4 N5 C32 147.4(12) . . . . ?

N4 Ni4 N5 C32 -122.5(12) . . . . ?

Ni5 Ni4 N5 C32 40.5(15) . . . . ?

Ni3 Ni4 N5 C32 81.2(12) . . . . ?

O10 Ni4 N5 C31 176.6(10) . . . . ?

O9 Ni4 N5 C31 -29(7) . . . . ?

O12 Ni4 N5 C31 89.6(11) . . . . ?

O13 Ni4 N5 C31 -92.2(11) . . . . ?

N4 Ni4 N5 C31 -2.2(11) . . . . ?

Ni5 Ni4 N5 C31 160.9(9) . . . . ?

Ni3 Ni4 N5 C31 -158.4(10) . . . . ?

O10 Ni4 N5 C33 -68.9(12) . . . . ?

O9 Ni4 N5 C33 85(7) . . . . ?

O12 Ni4 N5 C33 -155.9(13) . . . . ?

O13 Ni4 N5 C33 22.2(12) . . . . ?

N4 Ni4 N5 C33 112.3(13) . . . . ?

Ni5 Ni4 N5 C33 -84.7(13) . . . . ?

Ni3 Ni4 N5 C33 -44.0(12) . . . . ?

O9 Ni5 N6 C34 9.6(13) . . . . ?

O8 Ni5 N6 C34 -169.0(13) . . . . ?

O10 Ni5 N6 C34 12(4) . . . . ?

O11 Ni5 N6 C34 -82.3(13) . . . . ?

O6 Ni5 N6 C34 101.5(13) . . . . ?

Ni4 Ni5 N6 C34 -4.5(15) . . . . ?

Ni3 Ni5 N6 C34 118.5(12) . . . . ?

O9 Ni5 N6 C35 -177.0(11) . . . . ?

O8 Ni5 N6 C35 4.3(11) . . . . ?

O10 Ni5 N6 C35 -175(3) . . . . ?

O11 Ni5 N6 C35 91.0(11) . . . . ?

O6 Ni5 N6 C35 -85.2(11) . . . . ?

Ni4 Ni5 N6 C35 168.9(9) . . . . ?

Ni3 Ni5 N6 C35 -68.2(13) . . . . ?

O18 Ni6 N7 C58 -20(4) . . . . ?

O17 Ni6 N7 C58 -33.1(8) . . . . ?

O19 Ni6 N7 C58 -123.5(8) . . . . ?

O21 Ni6 N7 C58 53.5(9) . . . . ?

N8 Ni6 N7 C58 145.3(9) . . . . ?

Ni7 Ni6 N7 C58 -45.7(10) . . . . ?

Ni8 Ni6 N7 C58 43.4(13) . . . . ?

O18 Ni6 N7 C61 -137(4) . . . . ?

O17 Ni6 N7 C61 -149.9(9) . . . . ?

O19 Ni6 N7 C61 119.7(9) . . . . ?

O21 Ni6 N7 C61 -63.3(9) . . . . ?

N8 Ni6 N7 C61 28.5(9) . . . . ?

Ni7 Ni6 N7 C61 -162.5(7) . . . . ?

Ni8 Ni6 N7 C61 -73.4(13) . . . . ?

O18 Ni6 N7 C59 103(4) . . . . ?

O17 Ni6 N7 C59 90.1(10) . . . . ?

O19 Ni6 N7 C59 -0.3(10) . . . . ?

O21 Ni6 N7 C59 176.7(10) . . . . ?

N8 Ni6 N7 C59 -91.5(10) . . . . ?

Ni7 Ni6 N7 C59 77.5(11) . . . . ?

Ni8 Ni6 N7 C59 166.6(7) . . . . ?

O18 Ni6 N8 C62 176.5(8) . . . . ?

O17 Ni6 N8 C62 12(4) . . . . ?

O19 Ni6 N8 C62 -95.0(9) . . . . ?

O21 Ni6 N8 C62 85.1(9) . . . . ?

N7 Ni6 N8 C62 -2.0(9) . . . . ?

Ni7 Ni6 N8 C62 -167.4(6) . . . . ?

Ni8 Ni6 N8 C62 150.8(8) . . . . ?

O18 Ni6 N8 C63 -63.2(10) . . . . ?

O17 Ni6 N8 C63 133(3) . . . . ?

O19 Ni6 N8 C63 25.3(10) . . . . ?

O21 Ni6 N8 C63 -154.6(10) . . . . ?

N7 Ni6 N8 C63 118.3(10) . . . . ?

Ni7 Ni6 N8 C63 -47.1(13) . . . . ?

Ni8 Ni6 N8 C63 -88.9(10) . . . . ?

O18 Ni6 N8 C64 55.4(10) . . . . ?

O17 Ni6 N8 C64 -109(3) . . . . ?

O19 Ni6 N8 C64 143.8(10) . . . . ?

O21 Ni6 N8 C64 -36.1(10) . . . . ?

N7 Ni6 N8 C64 -123.1(10) . . . . ?

Ni7 Ni6 N8 C64 71.5(11) . . . . ?

Ni8 Ni6 N8 C64 29.7(10) . . . . ?

O17 Ni7 N9 C65 -20.2(12) . . . . ?

O32 Ni7 N9 C65 159.7(12) . . . . ?

O20 Ni7 N9 C65 71.3(12) . . . . ?

O18 Ni7 N9 C65 -18(5) . . . . ?

O30 Ni7 N9 C65 -111.7(12) . . . . ?

Ni6 Ni7 N9 C65 -6.1(15) . . . . ?

Ni8 Ni7 N9 C65 -128.7(11) . . . . ?

O17 Ni7 N9 C66 168.2(12) . . . . ?

O32 Ni7 N9 C66 -11.9(12) . . . . ?

O20 Ni7 N9 C66 -100.2(12) . . . . ?

O18 Ni7 N9 C66 171(3) . . . . ?

O30 Ni7 N9 C66 76.8(12) . . . . ?

Ni6 Ni7 N9 C66 -177.7(10) . . . . ?

Ni8 Ni7 N9 C66 59.8(13) . . . . ?

O25 Ni9 N10 C77 -35.9(10) . . . . ?

O26 Ni9 N10 C77 -38(4) . . . . ?

O28 Ni9 N10 C77 -128.0(10) . . . . ?

O29 Ni9 N10 C77 50.4(10) . . . . ?

N11 Ni9 N10 C77 142.0(10) . . . . ?

Ni10 Ni9 N10 C77 -51.2(11) . . . . ?

Ni8 Ni9 N10 C77 40.3(15) . . . . ?

O25 Ni9 N10 C78 86.3(10) . . . . ?

O26 Ni9 N10 C78 84(4) . . . . ?

O28 Ni9 N10 C78 -5.8(11) . . . . ?

O29 Ni9 N10 C78 172.5(11) . . . . ?

N11 Ni9 N10 C78 -95.8(11) . . . . ?

Ni10 Ni9 N10 C78 71.0(11) . . . . ?

Ni8 Ni9 N10 C78 162.4(8) . . . . ?

O25 Ni9 N10 C80 -153.0(9) . . . . ?

O26 Ni9 N10 C80 -156(4) . . . . ?

O28 Ni9 N10 C80 114.9(9) . . . . ?

O29 Ni9 N10 C80 -66.8(9) . . . . ?

N11 Ni9 N10 C80 24.9(9) . . . . ?

Ni10 Ni9 N10 C80 -168.3(7) . . . . ?

Ni8 Ni9 N10 C80 -76.9(12) . . . . ?

O25 Ni9 N11 C81 27(5) . . . . ?

O26 Ni9 N11 C81 -176.5(10) . . . . ?

O28 Ni9 N11 C81 -88.1(11) . . . . ?

O29 Ni9 N11 C81 91.7(11) . . . . ?

N10 Ni9 N11 C81 3.4(10) . . . . ?

Ni10 Ni9 N11 C81 -159.5(8) . . . . ?

Ni8 Ni9 N11 C81 158.4(10) . . . . ?

O25 Ni9 N11 C82 -92(5) . . . . ?

O26 Ni9 N11 C82 64.7(12) . . . . ?

O28 Ni9 N11 C82 153.1(12) . . . . ?

O29 Ni9 N11 C82 -27.1(12) . . . . ?

N10 Ni9 N11 C82 -115.4(12) . . . . ?

Ni10 Ni9 N11 C82 81.7(12) . . . . ?

Ni8 Ni9 N11 C82 39.6(12) . . . . ?

O25 Ni9 N11 C83 147(4) . . . . ?

O26 Ni9 N11 C83 -56.7(11) . . . . ?

O28 Ni9 N11 C83 31.7(11) . . . . ?

O29 Ni9 N11 C83 -148.5(11) . . . . ?

N10 Ni9 N11 C83 123.3(11) . . . . ?

Ni10 Ni9 N11 C83 -39.7(14) . . . . ?

Ni8 Ni9 N11 C83 -81.8(11) . . . . ?

O25 Ni10 N12 C84 -13.1(12) . . . . ?

O26 Ni10 N12 C84 -29(5) . . . . ?

O24 Ni10 N12 C84 164.7(12) . . . . ?

O27 Ni10 N12 C84 77.5(12) . . . . ?

O22 Ni10 N12 C84 -105.0(12) . . . . ?

Ni9 Ni10 N12 C84 1.2(14) . . . . ?

Ni8 Ni10 N12 C84 -121.8(11) . . . . ?

O25 Ni10 N12 C85 175.9(10) . . . . ?

O26 Ni10 N12 C85 160(4) . . . . ?

O24 Ni10 N12 C85 -6.3(11) . . . . ?

O27 Ni10 N12 C85 -93.5(11) . . . . ?

O22 Ni10 N12 C85 84.0(11) . . . . ?

Ni9 Ni10 N12 C85 -169.8(8) . . . . ?

Ni8 Ni10 N12 C85 67.2(12) . . . . ?

C7 C2 C3 C4 -3(3) . . . . ?

C1 C2 C3 C4 179.2(15) . . . . ?

C2 C3 C4 C5 4(2) . . . . ?

C2 C3 C4 C15 174.9(15) . . . . ?

Ni2 O1 C5 C4 3.4(19) . . . . ?

Ni1 O1 C5 C4 142.2(11) . . . . ?

Ni2 O1 C5 C6 -171.9(10) . . . . ?

Ni1 O1 C5 C6 -33.1(18) . . . . ?

C3 C4 C5 O1 179.6(13) . . . . ?

C15 C4 C5 O1 10(2) . . . . ?

C3 C4 C5 C6 -5(2) . . . . ?

C15 C4 C5 C6 -174.4(14) . . . . ?

O1 C5 C6 C7 -179.7(12) . . . . ?

C4 C5 C6 C7 5(2) . . . . ?

O1 C5 C6 C8 -3(2) . . . . ?

C4 C5 C6 C8 -178.5(13) . . . . ?

C5 C6 C7 C2 -4(2) . . . . ?

C8 C6 C7 C2 179.4(14) . . . . ?

C3 C2 C7 C6 3(2) . . . . ?

C1 C2 C7 C6 -179.2(15) . . . . ?

C9 N1 C8 C6 55.8(15) . . . . ?

C11 N1 C8 C6 177.7(11) . . . . ?

Ni1 N1 C8 C6 -70.7(12) . . . . ?

C7 C6 C8 N1 -121.7(14) . . . . ?

C5 C6 C8 N1 61.7(18) . . . . ?

C8 N1 C9 C10 61.3(17) . . . . ?

C11 N1 C9 C10 -61.7(18) . . . . ?

Ni1 N1 C9 C10 -177.7(11) . . . . ?

C8 N1 C11 C12 165.5(12) . . . . ?

C9 N1 C11 C12 -74.2(14) . . . . ?

Ni1 N1 C11 C12 50.5(11) . . . . ?

C14 N2 C12 C11 150.3(13) . . . . ?

C13 N2 C12 C11 -90.7(15) . . . . ?

Ni1 N2 C12 C11 27.8(13) . . . . ?

N1 C11 C12 N2 -55.3(15) . . . . ?

C16 N3 C15 C4 170.7(15) . . . . ?

Ni2 N3 C15 C4 -16(2) . . . . ?

C5 C4 C15 N3 -3(3) . . . . ?

C3 C4 C15 N3 -173.1(15) . . . . ?

C15 N3 C16 C17 -100(2) . . . . ?

Ni2 N3 C16 C17 87(2) . . . . ?

N3 C16 C17 C18 80(8) . . . . ?

N3 C16 C17 C18' 70(3) . . . . ?

C16 C17 C18 S1 -164(6) . . . . ?

C18' C17 C18 S1 -84(5) . . . . ?

C19 S1 C18 C17 154(8) . . . . ?

C18' S1 C18 C17 84(6) . . . . ?

C16 C17 C18' S1 -173(3) . . . . ?

C18 C17 C18' S1 84(5) . . . . ?

C19 S1 C18' C17 165(3) . . . . ?

C18 S1 C18' C17 -84(6) . . . . ?

C26 C21 C22 C23 1(3) . . . . ?

C20 C21 C22 C23 -179.2(14) . . . . ?

C21 C22 C23 C34 -177.5(15) . . . . ?

C21 C22 C23 C24 -4(2) . . . . ?

Ni5 O9 C24 C23 10.3(19) . . . . ?

Ni4 O9 C24 C23 155.5(10) . . . . ?

Ni5 O9 C24 C25 -172.1(9) . . . . ?

Ni4 O9 C24 C25 -26.8(18) . . . . ?

C34 C23 C24 O9 -6(2) . . . . ?

C22 C23 C24 O9 -179.1(12) . . . . ?

C34 C23 C24 C25 176.7(15) . . . . ?

C22 C23 C24 C25 3(2) . . . . ?

O9 C24 C25 C26 -178.3(12) . . . . ?

C23 C24 C25 C26 -1(2) . . . . ?

O9 C24 C25 C27 -3(2) . . . . ?

C23 C24 C25 C27 174.3(13) . . . . ?

C22 C21 C26 C25 2(3) . . . . ?

C20 C21 C26 C25 -177.7(15) . . . . ?

C24 C25 C26 C21 -2(2) . . . . ?

C27 C25 C26 C21 -177.4(16) . . . . ?

C30 N4 C27 C25 -178.7(13) . . . . ?

C28 N4 C27 C25 58.5(17) . . . . ?

Ni4 N4 C27 C25 -69.7(14) . . . . ?

C26 C25 C27 N4 -128.3(15) . . . . ?

C24 C25 C27 N4 57.0(19) . . . . ?

C30 N4 C28 C29 -59(2) . . . . ?

C27 N4 C28 C29 63(2) . . . . ?

Ni4 N4 C28 C29 -173.0(14) . . . . ?

C27 N4 C30 C31 165.9(14) . . . . ?

C28 N4 C30 C31 -72.3(17) . . . . ?

Ni4 N4 C30 C31 51.0(14) . . . . ?

C32 N5 C31 C30 153.7(15) . . . . ?

C33 N5 C31 C30 -88.9(17) . . . . ?

Ni4 N5 C31 C30 29.8(16) . . . . ?

N4 C30 C31 N5 -58.7(19) . . . . ?

C35 N6 C34 C23 177.1(16) . . . . ?

Ni5 N6 C34 C23 -9(2) . . . . ?

C24 C23 C34 N6 6(3) . . . . ?

C22 C23 C34 N6 179.3(15) . . . . ?

C34 N6 C35 C36 -109.6(17) . . . . ?

Ni5 N6 C35 C36 76.7(16) . . . . ?

N6 C35 C36 C37 81(2) . . . . ?

C35 C36 C37 S2 83.4(18) . . . . ?

C38' S2 C37 C36 175.9(12) . . . . ?

C38 S2 C37 C36 179(3) . . . . ?

Ni1 O3 C39 O4 3.1(19) . . . . ?

Ni1 O3 C39 C40 -173.9(5) . . . . ?

Ni2 O4 C39 O3 -4.3(18) . . . . ?

Ni2 O4 C39 C40 172.6(5) . . . . ?

Ni1 O5 C41 O6 -4(2) . . . . ?

Ni1 O5 C41 C42 174.9(10) . . . . ?

Ni3 O6 C41 O5 -34(2) . . . . ?

Ni5 O6 C41 O5 177.4(9) . . . . ?

Ni3 O6 C41 C42 147.5(10) . . . . ?

Ni5 O6 C41 C42 -2(2) . . . . ?

Ni3 O7 C43 O8 -3(3) . . . . ?

Ni3 O7 C43 C44 176.5(12) . . . . ?

Ni5 O8 C43 O7 4(3) . . . . ?

Ni5 O8 C43 C44 -174.9(12) . . . . ?

Ni4 O12 C45 O11 6(3) . . . . ?

Ni4 O12 C45 C46 -171.4(11) . . . . ?

Ni5 O11 C45 O12 -10(3) . . . . ?

Ni5 O11 C45 C46 167.6(11) . . . . ?

Ni3 O14 C47 O13 -40(2) . . . . ?

Ni2 O14 C47 O13 171.3(9) . . . . ?

Ni3 O14 C47 C48 141.0(12) . . . . ?

Ni2 O14 C47 C48 -8(2) . . . . ?

Ni4 O13 C47 O14 1(3) . . . . ?

Ni4 O13 C47 C48 -180.0(10) . . . . ?

Ni2 O16 C49 O15 -3(3) . . . . ?

Ni2 O16 C49 C50 177.9(14) . . . . ?

Ni3 O15 C49 O16 6(3) . . . . ?

Ni3 O15 C49 C50 -174.7(14) . . . . ?

C57 C52 C53 C54 -8(3) . . . . ?

C51 C52 C53 C54 176.0(15) . . . . ?

C52 C53 C54 C55 9(3) . . . . ?

C52 C53 C54 C65 -171.4(17) . . . . ?

Ni7 O17 C55 C56 174.1(9) . . . . ?

Ni6 O17 C55 C56 36.3(17) . . . . ?

Ni7 O17 C55 C54 -9.5(18) . . . . ?

Ni6 O17 C55 C54 -147.3(10) . . . . ?

C53 C54 C55 O17 177.3(13) . . . . ?

C65 C54 C55 O17 -2(2) . . . . ?

C53 C54 C55 C56 -6.3(19) . . . . ?

C65 C54 C55 C56 174.5(13) . . . . ?

O17 C55 C56 C57 179.8(12) . . . . ?

C54 C55 C56 C57 3(2) . . . . ?

O17 C55 C56 C58 0(2) . . . . ?

C54 C55 C56 C58 -176.7(12) . . . . ?

C55 C56 C57 C52 -2(2) . . . . ?

C58 C56 C57 C52 177.7(14) . . . . ?

C53 C52 C57 C56 4(2) . . . . ?

C51 C52 C57 C56 -179.8(14) . . . . ?

C61 N7 C58 C56 -177.6(11) . . . . ?

C59 N7 C58 C56 -54.5(16) . . . . ?

Ni6 N7 C58 C56 70.6(12) . . . . ?

C57 C56 C58 N7 120.5(15) . . . . ?

C55 C56 C58 N7 -59.7(18) . . . . ?

C58 N7 C59 C60 -59.7(17) . . . . ?

C61 N7 C59 C60 63.1(17) . . . . ?

Ni6 N7 C59 C60 178.5(11) . . . . ?

C58 N7 C61 C62 -167.0(12) . . . . ?

C59 N7 C61 C62 70.1(15) . . . . ?

Ni6 N7 C61 C62 -51.8(13) . . . . ?

C63 N8 C62 C61 -146.6(12) . . . . ?

C64 N8 C62 C61 94.0(15) . . . . ?

Ni6 N8 C62 C61 -25.6(13) . . . . ?

N7 C61 C62 N8 54.5(15) . . . . ?

C66 N9 C65 C54 -170.6(15) . . . . ?

Ni7 N9 C65 C54 17(2) . . . . ?

C53 C54 C65 N9 178.2(16) . . . . ?

C55 C54 C65 N9 -3(2) . . . . ?

C65 N9 C66 C67 102.6(17) . . . . ?

Ni7 N9 C66 C67 -84.9(18) . . . . ?

N9 C66 C67 C68 -76(7) . . . . ?

N9 C66 C67 C68' -76(5) . . . . ?

C68' C67 C68 S3 90(100) . . . . ?

C66 C67 C68 S3 172(6) . . . . ?

C69' S3 C68 C67 62(10) . . . . ?

C69 S3 C68 C67 -163(9) . . . . ?

C68' S3 C68 C67 -91(100) . . . . ?

C68 C67 C68' S3 -90(100) . . . . ?

C66 C67 C68' S3 172(4) . . . . ?

C69' S3 C68' C67 62(6) . . . . ?

C69 S3 C68' C67 -163(5) . . . . ?

C68 S3 C68' C67 89(100) . . . . ?

C76 C71 C72 C73 -4(2) . . . . ?

C70 C71 C72 C73 178.0(13) . . . . ?

C71 C72 C73 C74 2(2) . . . . ?

C71 C72 C73 C84 -177.4(13) . . . . ?

Ni10 O25 C74 C73 -8.7(19) . . . . ?

Ni9 O25 C74 C73 -151.1(11) . . . . ?

Ni10 O25 C74 C75 173.0(9) . . . . ?

Ni9 O25 C74 C75 30.6(17) . . . . ?

C72 C73 C74 O25 -178.1(13) . . . . ?

C84 C73 C74 O25 1(2) . . . . ?

C72 C73 C74 C75 0(2) . . . . ?

C84 C73 C74 C75 179.4(13) . . . . ?

O25 C74 C75 C76 178.5(12) . . . . ?

C73 C74 C75 C76 0(2) . . . . ?

O25 C74 C75 C77 0(2) . . . . ?

C73 C74 C75 C77 -178.1(13) . . . . ?

C72 C71 C76 C75 5(2) . . . . ?

C70 C71 C76 C75 -177.6(14) . . . . ?

C74 C75 C76 C71 -3(2) . . . . ?

C77 C75 C76 C71 175.6(14) . . . . ?

C78 N10 C77 C75 -56.2(17) . . . . ?

C80 N10 C77 C75 178.9(13) . . . . ?

Ni9 N10 C77 C75 68.8(13) . . . . ?

C76 C75 C77 N10 126.0(15) . . . . ?

C74 C75 C77 N10 -55.9(19) . . . . ?

C77 N10 C78 C79 -62.4(19) . . . . ?

C80 N10 C78 C79 62.0(19) . . . . ?

Ni9 N10 C78 C79 176.1(12) . . . . ?

C77 N10 C80 C81 -165.6(14) . . . . ?

C78 N10 C80 C81 71.1(18) . . . . ?

Ni9 N10 C80 C81 -50.9(15) . . . . ?

C82 N11 C81 C80 87.5(17) . . . . ?

C83 N11 C81 C80 -153.7(14) . . . . ?

Ni9 N11 C81 C80 -32.2(16) . . . . ?

N10 C80 C81 N11 59.4(19) . . . . ?

C85 N12 C84 C73 -177.5(14) . . . . ?

Ni10 N12 C84 C73 11(2) . . . . ?

C74 C73 C84 N12 -3(3) . . . . ?

C72 C73 C84 N12 176.3(15) . . . . ?

C84 N12 C85 C86 98.5(15) . . . . ?

Ni10 N12 C85 C86 -90.0(13) . . . . ?

N12 C85 C86 C87' -68(3) . . . . ?

N12 C85 C86 C87 -82(5) . . . . ?

C87' C86 C87 S4 80(5) . . . . ?

C85 C86 C87 S4 166(5) . . . . ?

C87' S4 C87 C86 -79(5) . . . . ?

C88 S4 C87 C86 92(7) . . . . ?

C87 C86 C87' S4 -80(5) . . . . ?

C85 C86 C87' S4 -179(3) . . . . ?

C87 S4 C87' C86 79(5) . . . . ?

C88 S4 C87' C86 70(4) . . . . ?

Ni10 O27 C89 O28 -1(2) . . . . ?

Ni10 O27 C89 C90 174.2(10) . . . . ?

Ni9 O28 C89 O27 9(3) . . . . ?

Ni9 O28 C89 C90 -166.3(10) . . . . ?

Ni10 O24 C91 O23 -12(3) . . . . ?

Ni10 O24 C91 C92' 156.9(15) . . . . ?

Ni10 O24 C91 C92 -178(2) . . . . ?

Ni8 O23 C91 O24 6(2) . . . . ?

Ni8 O23 C91 C92' -162.7(14) . . . . ?

Ni8 O23 C91 C92 171(3) . . . . ?

Ni6 O21 C93 O22 -4(3) . . . . ?

Ni6 O21 C93 C94 179.5(11) . . . . ?

Ni8 O22 C93 O21 36(2) . . . . ?

Ni10 O22 C93 O21 -172.9(10) . . . . ?

Ni8 O22 C93 C94 -146.7(10) . . . . ?

Ni10 O22 C93 C94 4(2) . . . . ?

Ni6 O19 C95 O20 -7(2) . . . . ?

Ni6 O19 C95 C96 173.1(10) . . . . ?

Ni7 O20 C95 O19 10(2) . . . . ?

Ni7 O20 C95 C96 -170.8(10) . . . . ?

Ni7 O32 C97 O31 10(3) . . . . ?

Ni7 O32 C97 C98 -175.9(14) . . . . ?

Ni8 O31 C97 O32 -13(3) . . . . ?

Ni8 O31 C97 C98 172.2(14) . . . . ?

Ni9 O29 C99 O30 -9(3) . . . . ?

Ni9 O29 C99 C100 171.2(10) . . . . ?

Ni8 O30 C99 O29 39(2) . . . . ?

Ni7 O30 C99 O29 -167.1(10) . . . . ?

Ni8 O30 C99 C100 -141.0(11) . . . . ?

Ni7 O30 C99 C100 13(2) . . . . ?

_diffrn_measured_fraction_theta_max    1.000

_diffrn_reflns_theta_full              22.50

_diffrn_measured_fraction_theta_full   1.000

_refine_diff_density_max    1.538

_refine_diff_density_min   -0.771

_refine_diff_density_rms    0.140