Fig. S2	Scanning electron micrographs for La phosphate particles prepared via the ELM system, following calcination for 2 h at temperatures of (a) 573 K and (b) 1373 K.  [EHPNA]feed = 0.5 mol l–1, [Ln]feed = 0.01 mol l–1, [Span 83]feed = 5 wt%, and [H3PO4]feed = 0.3 mol l–1.