Supporting Information

The Au(111) surface has been visualized with STM (see image below).  It exhibits atomically flat terraces with a size of a few hundreds of nanometers across. These crystals are proper supports for the growth of ordered architectures of fullerene.

Constant current STM image of a Au(111) surface, onto which the C60 is adsorbed.  By using slightly invasive tunneling parameters (tip bias=500 mV ; average tunneling current=200 pA) the structure of the bare substrate is visible.  The small visualized roughness can be ascribed to the layer of C60 above. Height range: 8.5 nm.