[meso-Tetrakis(pentafluorophenyl)porphyrinato] Platinum(II) as an Efficient, Oxidation-Resistant Red Phosphor: Spectroscopic Properties and Applications in Organic Light-Emitting Diodes

Prof. Y. Wang

Key Laboratory for Supramolecular Structure and Spectroscopy of Ministry of Education, Jilin University, Changchun 130023 (China)

Details of photoluminescence measurements; transient absorption spectra of PtF20TPP; photophysical properties of PtF20TPP in different solvents; EL spectra and performances of OLEDs using PtF20TPP as emitters at various doping levels; crystallographic data for PtF20TPP.

Transient absorption spectra for PtF20TPP in acetonitrile following 355 nm excitation

Table. Photophysical Properties of PtF20TPP in different solvents

| Solvent | em (nm) |  |  (s) |
| --- | --- | --- | --- |
| Hexane | 647 | 0.081 | 52 |
| CH2Cl2 | 648 | 0.088 | 60 |
| ## Acetonitrile | 647 | 0.084 | 55 |
| MeOH | 647 | 0.045 | 26 |

EL spectra of Devices 2 (top) and 4 (bottom) at various voltages

EL spectra of Devices 14 recorded at 8 V

Current-voltage and luminance-voltage characteristics of Devices 2 (top) and 4 (bottom)

Crystal data: Formula: [PtF20TPP](H2O)0.33, [C44 H8.67 F20 N4 O0.33 Pt];  formula weight  = 1173.64, rhombohedral, R -3, a = 14.2727(16) Å,= 88.309(17)°,V = 2903.8(6) Å3, Z = 3, Dc = 2.013 g cm-3, (Mo-K) = 3.764  mm-1, F(000) = 1684, T = 301 K.

Data collection: A crystal of dimensions 0.4 × 0.3 × 0.1 mm mounted in a glass capillary was used for data collection at 28oC on a MAR diffractometer with a 300 mm image plate detector using graphite monochromatized Mo-K radiation ( = 0.71073 Å). Data collection was made with 2o oscillation steps of , 300 seconds exposure time and scanner distance at 120 mm. 100 images were collected.

Data reduction: The images were interpreted and intensities integrated using program DENZO  .

Structure solution: The structure was solved by direct methods employing SHELXS-97 program on PC. Almost all atoms except the water molecule were located according to the direct methods. The position of the O atom was found after successful refinement by full-matrix least-squares using program SHELXL-97  on PC.

Structure refinement: According to the SHELXL-97 program,3 all 3553 independent reflections (Rint  equal to 0.0697, 2780 reflections larger than 4(Fo)) from a total 19190 reflections were participated in the full-matrix least-square refinement against F2. These reflections were in the range -17<=h<= 17, -17<=k<= 17, -15<=l<= 15 with 2 max equal to 51.06o.

One crystallographic asymmetric unit consists of one half of formula unit, inclusive one third of water molecule. In the final stage of least-squares refinement, all non-hydrogen atoms were refined anisotropically. H atoms except those on O of water molecule are generated by program SHELXL-97. The positions of H atoms are calculated based on riding mode with thermal parameters equal to 1.2 times that of the associated C atoms, and participated in the calculation of final R-indices.

Convergence (( /)max = 0.001, av. 0.001) for 315 variable parameters by full-matrix least-squares refinement on F2 reaches to R1 = 0.0336 and wR2 = 0.0848 with a goodness-of-fit of 0.994, the parameters a and b for weighting scheme are 0.0639 and 0.0. The final difference Fourier map shows maximum rest peaks and holes of 0.482 and -1.037 eÅ-3 respectively.

Drawing: The ORTEP  drawing of the molecule was made with thermal ellipsoids at the 30 % probability level.

Otwinowski, Z. and Minor, W., “Processing of X-ray Diffraction Data Collected in Oscillation Mode”, Methods in Enzymology, Volume 276: Macromolecular Crystallography, part A, p. 307-326, 1997. Carter C. W., Sweet Jr. & R. M., Eds., Academic Press.

SHELXS97, Sheldrick, G. M. (1997). SHELX97. Programs for Crystal Structure Analysis (Release 97-2). University of Goetingen, Germany.

SHELXL97, Sheldrick, G. M. (1997). SHELX97. Programs for Crystal Structure Analysis (Release 97-2). University of Goetingen, Germany.

Rint = | Fo2- Fo2(mean) | / [ Fo2]

Since the structure refinements are against F2, R-indices based on F2 are larger than (more than double) those based on F.  For comparison with older refinements based on F and an OMIT threshold, a conventional index R1 based on observed F values larger than 4(Fo) is also given (corresponding to Intensity2(I)). wR2 = { [ w( Fo2– Fc2)2] / [ w(Fo2)2] }1/2, R1 = ||Fo| – |Fc|| / |Fo|, The Goodness of Fit is always based on F2: GooF = S = { [ w( Fo2– Fc2)2] / ( n– p) }1/2, where n is the number of reflections and p is the total number of parameters refined. The weighting scheme is: w = 1/[2(Fo2) + (aP)2+ bP ], where P is [ 2 Fc2+ Max( Fo2,0) ]/3.

ORTEP3 for Windows - Farrugia, L. J. (1997) J. Appl. Cryst. 30, 565.