Online Supporting Information for

# Mechanisms of Charge Accumulation in the Dark Operation of Perovskite Solar Cells

Teresa S. Ripolles,*1 Ajay K. Baranwal,1 Koji Nishinaka,1 Yuhei Ogomi,1 Germà Garcia-Belmonte,*2 and Shuzi Hayase*1

1Graduate School of Life Science and Systems Engineering, Kyushu Institute of Technology, 2-4 Hibikino, Wakamatsu-ku, Kitakyushu, Fukuoka 808-0196, Japan.

2Institute of Advance Materials (INAM), Universitat Jaume I, ES-12006 Castelló, Spain.

Results and discussion

Figure SI 1. Current density-voltage curves under dark at reverse sweep for devices with architecture glass/FTO/c-TiO2/mp-TiO2/MAPbI3/spiro-OMeTAD/Au. The scan rate was 0.1 V/s. Between FS-RS measurements, the device remained at +3.5 V for several seconds, 0, 5, 10, 20, 30, and 60 s.

Figure SI 2. Current density-voltage curves of an additional MAPbI3/Spiro-OMeTAD device (a) at simulated 1 sun illumination from short-circuit to forward conditions (forward sweep, FS) and forward to short-circuit conditions (reverse sweep, RS); (b) under dark conditions at FS and RS, the solar cell remains at +3.5 V or short-circuit conditions for 0 s or 30 s between the measurements FS and RS; and, (c) under dark at RS and at different delay times between FS and RS measurements. The scan rate was 0.1 V/s for all measurements.

Table SI 1. The relative percentage of the charge accumulation and the capacitance were included. The C was measured under dark from the difference of currents at FS and RS at backward voltage with a delay time of 60 s at 0.01 V/s of scan rate in different photovoltaic devices.

| Device | % Charge accumulation | C (mF cm-2) |
| --- | --- | --- |
| MAPbI3/spiro-OMeTAD | 14.8 | 452.9 |
| MAPbI3/spiro-OMeTAD+Add. | 18.0 | 515.0 |
| MAPbI3/P3HT | 10.9 | 45.1 |
| MAPbI3/P3HT+Add. | 8.9 | 40.0 |
| CsPbI3/P3HT | 18.6 | 8.3 |
| CsPbI3/P3HT/MoO3 | 37.6 | 54.0 |

Figure SI 3. Current density-voltage curves under dark at reverse sweep for devices with architecture glass/FTO/c-TiO2/mp-TiO2/MAPbI3/spiro-OMeTAD+Additives/Au. The scan rate was 0.1 V/s (solid lines) and 0.01 V/s (dash lines). Between FS-RS measurements, the devices were short-circuited for several seconds, 0, 20, and 60 s. Figure (b) is the zoom of Figure (a).

Figure SI 4. Current density-voltage curves under dark at reverse sweep for devices with architecture glass/FTO/c-TiO2/mp-TiO2/MAPbI3/P3HT/Au. The scan rate was 0.1 V/s (solid lines) and 0.01 V/s (dash lines). Between FS-RS measurements, the devices were short-circuited for several seconds, 0, 20, and 60 s. Figure (b) is the zoom of Figure (a).

Figure SI 5. Current density-voltage curves under dark at reverse sweep for devices with architecture glass/FTO/c-TiO2/mp-TiO2/MAPbI3/P3HT+Additives/Au. The scan rate was 0.1 V/s (solid lines) and 0.01 V/s (dash lines). Between FS-RS measurements, the devices were short-circuited for several seconds, 0, 20, and 60 s. Figure (b) is the zoom of Figure (a).