Supporting Information

Hydrodynamic trapping for rapid assembly and in situ electrical characterization of droplet interface bilayer arrays

Mary-Anne Nguyena, Bernadeta Srijantob, C. Patrick Collierb, Scott T. Rettererc, Stephen A. Sarlesa*

a University of Tennessee, Department of Mechanical, Aerospace, and Biomedical Engineering

b Oak Ridge National Laboratory, Center for Nanophase Materials Sciences

c UT-Battelle, LLC, Biosciences and Center for Nanophase Materials Sciences

*corresponding author: ssarles@utk.edu

Bioinspired Materials and Transduction Laboratory

Department of Mechanical, Aerospace, and Biomedical Engineering

University of Tennessee, Knoxville

Knoxville, TN 37996, United States

S1. Derivation of network models for trap arrays

Figure S1 shows an electrical circuit model for a 3-trap Model 1 array, which will be used to demonstrate the process for developing a system of equations as given in manuscript in Equation 4.

Figure S1: Electrical circuit layout of a three-trap, Model 1 array with parallel traps and a return channel. Q is the total input fluid flow rate, Ri is resistance of the ith channel section, and Pi is the absolute pressure at the ith node.

Using Kirchoff’s Current Law (KCL) for fluid flow at each channel intersection, a matrix of equations is developed to describe the relationship between absolute node pressure, channel resistances, and input fluid flow rate. For example, applying KCL at nodes 1 and 2 yield:

Following the same procedure for the remaining 4 nodes within this 3-trap array yields a total of 6 linear equations in terms of the 6 unknown pressures at all nodes. These equations can be rewritten in matrix form as follows

.

The same KCL procedure is also applied for 3-trap arrays in the form of both Model 2 and Model 3 as shown in Figure 2B,C, respectively. For Model 2, this process yields are a total of 7 linear equations as written in the following matrix form:

.

Finally, a 3-trap version of Model 3 with 9 pressure nodes yields a total of 9 linear equations, which can be written in the following matrix form

.

These matrix expressions can be solved numerically in MATLAB to determine the values of absolute pressures at all nodes, which can then be used to evaluate relative flow rates in traps versus the main channel (Figure 3D) or compute the pressure drop across all traps in a filled array (Figure 3E).

S2. Droplet size based on flow rates of aqueous buffer and oil

Figure S2: Average droplet diameter versus the aqueous buffer/oil flow rate ratio.

A series of experiments varying the flow rates of the oil and the aqueous buffer was performed to determine the range of the droplet sizes the device can produce and to identify the flow rates required to generate ~100 µm diameter droplets used in the trapping experiments. Figure S2 shows the corresponding droplet diameters based on the flow rate ratio of buffer to oil. Note, the same flow rate ratios can give different sizes since different flow rates of oil and buffer can produce the same ratios.

S3. Nominal capacitance and membrane resistance determined for an 8-DIB array

Raw current measurements as shown in Figure 7C is used to calculate bilayer capacitance, which is then plotted against time in Figure S3A The capacitances of all 8 pairs correspond to the growing membrane area. Furthermore, the resistivity is plotted in Figure S2B using the interface area and resistance of the membrane, which is calculated from the slope of the current at the peaks of the square-like waveform.

Figure S3: (A) Membrane capacitance increases upon DIB formation, corresponding to a growing membrane area, while (B) normalized resistances does not change significantly for all eight pairs of DIBs. Note start time is relative to each DIB pair.

S4. Electrical measurements from 2 additional trials

Below are tabulated results from two separate experiments using electrical measurements to simultaneously characterize a set of 8 GMO DIBs.

Table S1: Capacitance, resistance, area, specific capacitance, and normalized resistance for GMO DIBs obtained during Trial 2.

| DIB # | Capacitance final (CF) – pF | Resistance final (RF) – GΩ | Area final (AF) – µm2 | Specific capacitance (CM) - µF/cm2 | Normalized resistance (RN) - MΩcm2 |
| --- | --- | --- | --- | --- | --- |
| Pair 1 | 16.7 | 8.0 | 2173 | 0.769 | 0.17 |
| Pair 2 | 16.8 | 8.5 | 2181 | 0.770 | 0.19 |
| Pair 3 | 16.8 | 8.0 | 2181 | 0.770 | 0.17 |
| Pair 4 | 16.7 | 8.1 | 2181 | 0.766 | 0.18 |
| Pair 5 | 16.7 | 8.1 | 2173 | 0.769 | 0.18 |
| Pair 6 | 16.7 | 8.0 | 2173 | 0.769 | 0.17 |
| Pair 7 | 16.7 | 8.1 | 2173 | 0.769 | 0.18 |
| Pair 8 | 16.7 | 8.1 | 2173 | 0.769 | 0.18 |
| Averages | 16.7±0.05 | 8.1±0.2 | 2176±4 | 0.769±0.001 | 0.18±0.004 |

Table S2: Capacitance, resistance, area, specific capacitance, and normalized resistance for GMO DIBs obtained during Trial 3.

| DIB # | Capacitance final (CF) – pF | Resistance final (RF) – GΩ | Area final (AF) – µm2 | Specific capacitance (CM) - µF/cm2 | Normalized resistance (RN) - MΩcm2 |
| --- | --- | --- | --- | --- | --- |
| Pair 1 | 12.8 | 8.1 | 1662 | 0.770 | 0.13 |
| Pair 2 | 12.8 | 8.8 | 1662 | 0.770 | 0.15 |
| Pair 3 | 13.1 | 8.0 | 1684 | 0.778 | 0.14 |
| Pair 4 | 13.1 | 8.1 | 1684 | 0.778 | 0.14 |
| Pair 5 | 12.8 | 8.1 | 1662 | 0.770 | 0.13 |
| Pair 6 | 12.9 | 8.8 | 1669 | 0.773 | 0.15 |
| Pair 7 | 13.0 | 8.2 | 1676 | 0.775 | 0.14 |
| Pair 8 | 12.9 | 8.1 | 1669 | 0.773 | 0.13 |
| Averages | 12.9±0.13 | 8.3±0.4 | 1671±9 | 0.773±0.003 | 0.14±0.01 |

S5. Experimental set-up of microchip operation

Experiments are performed on an inverted microscope on top of a vibration isolation table as seen in Figure S5. Copper wires soldered to the microchip are attached to the 8-channel patch clamp amplifier. Liquids are pumped into microchip via a dual syringe pump.

Figure S5: Experimental set-up of microchip with electrodes attached to a patch clamp amplifier.