## Slide 1
Supplementary Material
Anomalous Lattice Behavior of Vanadium Pentaoxide (V2O5): X- Ray Diffraction, Inelastic Neutron Scattering and ab-initio Lattice Dynamics
Baltej Singha,b, Mayanak Kumar Guptaa, Sanjay Kumar Mishraa, Ranjan Mittala,b, P. U. Sastrya,b Stephane Rolsc and Samrath Lal Chaplota,b
aSolid State Physics Division, Bhabha Atomic Research Centre, Mumbai, 400085, India
bHomi Bhabha National Institute, Mumbai 400094, India
cInstitut Laue-Langevin, BP 156, 38042 Grenoble Cedex 9, France
The following shows the animations of selected low energy phonon modes responsible for the negative thermal expansion behaviour in the ab plane of α-V2O5.

## Slide 2:  Point (0 0 0), 9.0 meV αa= -1.2 ×10-6 K-1, αb= 2.3 ×10-6 K-1, αc=6.8 ×10-6 K-1
This phonon mode involves the in-phase bending of VO5 polyhedral chains about the O1 atoms in the ac - plane. All the atoms in the chain show in-phase motion.
O1
O2
O3
V
Supercell
2×1×3

## Slide 3
Z Point (0 0 0.5), 8.8 meV
αa= -3.0 ×10-6 K-1, αb= -0.8 ×10-6 K-1, αc=14.5 ×10-6 K-1
This phonon mode involves the out-of-phase breathing of VO5 polyhedral units in two consecutive layers. All the atoms in a chain show out-of-phase motion along c-axis.
O1
O2
O3
V
Supercell
2×1×3

## Slide 4
T Point (0 0.5 0.5), 9.5 meV
αa= 4.0 ×10-6 K-1, αb= -4.6 ×10-6 K-1, αc=2.1 ×10-6 K-1
In this phonon mode the rotation and translation vibrations of VO5 polyhedra create buckling in the ab plane. The successive layers show out-of-phase buckling.
O1
O2
O3
V
Supercell
1×3×3

## Slide 5
R Point (0.5 0.5 0.5), 10 meV
αa= 3.8 ×10-6 K-1, αb= -3.3 ×10-6 K-1, αc=-0.2 ×10-6 K-1
This phonon mode involves the out-of-phase bending of successive layers containing VO5 polyhedra in ab plane.
O1
O2
O3
V
Supercell
1×3×3