Electronic Supplementary Information #2 for

Insights into the origin of the excited transitions in graphene quantum dots interacted with heavy metals in different media

Ivan Shtepliuk, Volodymyr Khranovskyy and Rositsa Yakimova

Department of Physics, Chemistry and Biology, Linköping University, SE-58183, Linköping, Sweden

*Corresponding author: e-mail: ivan.shtepliuk@liu.se

Figure S1. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in GQDs.  (a) and (b) represent molecular orbitals of zigzag-edged GQDs in gas-phase and water, respectively. (c) and (d) show molecular orbitals of armchair-edged GQDs in the gas-phase and water, respectively. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Table S1. Electronic transitions in ZZ-GQDs

| No. | Wavelength (nm) | Osc. Strength | Symmetry | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- | --- |
| Gas-phase |  |  |  |  |  |
| 3 | 414.91 | 0.9971 | Singlet-A' | H-1->LUMO (48%), HOMO->L+1 (48%) |  |
| 4 | 414.89 | 0.9977 | Singlet-A' | H-1->L+1 (48%), HOMO->LUMO (48%) |  |
| Acetic Acid |  |  |  |  |  |
| 3 | 427.82 | 1.4196 | Singlet-A' | H-1->LUMO (49%), HOMO->L+1 (49%) |  |
| 4 | 427.78 | 1.4184 | Singlet-A' | H-1->L+1 (49%), HOMO->LUMO (49%) |  |
| Ethanol |  |  |  |  |  |
| 3 | 427.69 | 1.4043 | Singlet-A' | H-1->LUMO (49%), HOMO->L+1 (49%) |  |
| 4 | 427.64 | 1.4031 | Singlet-A' | H-1->L+1 (49%), HOMO->LUMO (48%) |  |
| DMF |  |  |  |  |  |
| 3 | 429.68 | 1.4696 | Singlet-A' | H-1->LUMO (49%), HOMO->L+1 (49%) |  |
| 4 | 429.63 | 1.4682 | Singlet-A' | H-1->L+1 (49%), HOMO->LUMO (49%) |  |
| Water |  |  |  |  |  |
| 3 | 426.94 | 1.3752 | Singlet-A' | H-1->LUMO (49%), HOMO->L+1 (49%) |  |
| 4 | 426.89 | 1.3741 | Singlet-A' | H-1->L+1 (49%), HOMO->LUMO (48%) |  |

Table S2. Electronic transitions in AC-GQDs

| No. | Wavelength (nm) | Osc. Strength | Symmetry | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- | --- |
| Gas-phase |  |  |  |  |  |
| 2 | 441.68 | 0.2693 | Singlet-A | H-1->L+1 (14%), HOMO->LUMO (86%) |  |
| 4 | 371.87 | 0.7896 | Singlet-A | H-1->L+1 (75%), HOMO->LUMO (16%) | H-2->LUMO (6%) |
| 5 | 369.68 | 0.8535 | Singlet-A | H-1->LUMO (46%), HOMO->L+1 (48%) | H-1->L+2 (2%) |
| 7 | 350.54 | 0.326 | Singlet-A | H-2->LUMO (58%), HOMO->L+2 (32%) | H-1->L+1 (4%) |
| 9 | 328.06 | 0.0143 | Singlet-A | HOMO->L+3 (93%) | H-2->LUMO (3%) |
| Acetic Acid |  |  |  |  |  |
| 2 | 441.66 | 0.274 | Singlet-A | H-1->L+1 (13%), HOMO->LUMO (86%) |  |
| 4 | 378.47 | 1.1327 | Singlet-A | H-1->L+1 (82%), HOMO->LUMO (13%) | H-2->LUMO (3%) |
| 5 | 378.21 | 1.2172 | Singlet-A | H-1->LUMO (48%), HOMO->L+1 (49%) |  |
| 7 | 355.17 | 0.3157 | Singlet-A | H-2->LUMO (55%), HOMO->L+2 (40%) |  |
| Ethanol |  |  |  |  |  |
| 2 | 441.68 | 0.2693 | Singlet-A | H-1->L+1 (14%), HOMO->LUMO (86%) |  |
| 4 | 378.56 | 1.1295 | Singlet-A | H-1->L+1 (83%), HOMO->LUMO (13%) |  |
| 5 | 378.13 | 1.2046 | Singlet-A | H-1->LUMO (48%), HOMO->L+1 (49%) |  |
| 7 | 355.26 | 0.3177 | Singlet-A | H-2->LUMO (52%), HOMO->L+2 (43%) |  |
| DMF |  |  |  |  |  |
| 2 | 442.07 | 0.2901 | Singlet-A | H-1->L+1 (13%), HOMO->LUMO (86%) |  |
| 4 | 379.50 | 1.176 | Singlet-A | H-1->L+1 (84%), HOMO->LUMO (13%) |  |
| 5 | 379.44 | 1.2586 | Singlet-A | H-1->LUMO (48%), HOMO->L+1 (49%) |  |
| 7 | 355.85 | 0.3123 | Singlet-A | H-2->LUMO (52%), HOMO->L+2 (44%) |  |
| Water |  |  |  |  |  |
| 2 | 441.55 | 0.2604 | Singlet-A | H-1->L+1 (14%), HOMO->LUMO (85%) |  |
| 4 | 378.24 | 1.1099 | Singlet-A | H-1->L+1 (83%), HOMO->LUMO (13%) |  |
| 5 | 377.64 | 1.1803 | Singlet-A | H-1->LUMO (48%), HOMO->L+1 (49%) |  |
| 7 | 355.07 | 0.3198 | Singlet-A | H-2->LUMO (51%), HOMO->L+2 (44%) |  |

Table S3. Top view and side view of the optimized geometries of the Cd adatom adsorbed on surface of GQD

| Dielectric Media | Cd0@GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Gas-phase |  |  |
| Acetic Acid |  |  |
| Ethanol |  |  |
| DMF |  |  |
| Water |  |  |

Figure S2. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in GQDs after complexation with Cd0.  (a) and (b) represent molecular orbitals of Cd0@ZZ-GQDs in gas-phase and water, respectively. (c) and (d) show molecular orbitals of Cd0@AC-GQDs in the gas-phase and water, respectively. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Dataset S1. Electronic transitions in Cd0@GQD

Zigzag GQDs with Cd0 in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 5 | 415.62 | 0.9474 | H-1->LUMO (27%), H-1->L+1 (21%), HOMO->LUMO (20%), HOMO->L+1 (27%) |
| 6 | 415.60 | 0.9481 | H-1->LUMO (21%), H-1->L+1 (27%), HOMO->LUMO (27%), HOMO->L+1 (21%) |

Zigzag GQDs with Cd0 in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 7 | 428.59 | 1.3411 | H-2->LUMO (20%), H-2->L+1 (29%), H-1->LUMO (29%), H-1->L+1 (20%) |
| 8 | 428.566 | 1.3402 | H-2->LUMO (29%), H-2->L+1 (20%), H-1->LUMO (20%), H-1->L+1 (29%) |

Zigzag GQDs with Cd0 in Ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 7 | 428.52 | 1.3235 | H-2->LUMO (22%), H-2->L+1 (27%), H-1->LUMO (27%), H-1->L+1 (22%) |
| 8 | 428.52 | 1.321 | H-2->LUMO (27%), H-2->L+1 (22%), H-1->LUMO (22%), H-1->L+1 (27%) |

Zigzag GQDs with Cd0 in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 7 | 430.47 | 1.3877 | H-2->LUMO (37%), H-2->L+1 (12%), H-1->LUMO (12%), H-1->L+1 (37%) |
| 8 | 430.45 | 1.3871 | H-2->LUMO (12%), H-2->L+1 (37%), H-1->LUMO (37%), H-1->L+1 (12%) |

Zigzag GQDs with Cd0 in H2O

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 7 | 427.73 | 1.2946 | H-2->LUMO (20%), H-2->L+1 (29%), H-1->LUMO (29%), H-1->L+1 (20%) |
| 8 | 427.69 | 1.2932 | H-2->LUMO (29%), H-2->L+1 (20%), H-1->LUMO (20%), H-1->L+1 (29%) |

Armchair GQDs with Cd0 in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 2 | 439.48 | 0.152 | H-1Cd-GQD ->L+1 (12%), HOMO->LUMO (82%) | H-2 Cd-GQD ->L+1 (5%) |
| 6 | 372.51 | 0.7191 | H-2Cd-GQD ->L+1(39%),H-1Cd-GQD ->L+1 (37%),HOMO->LUMO(15%) | H-3->LUMO (6%) |
| 7 | 370.83 | 0.7966 | H-2Cd-GQD->LUMO(22%),H-1CdGQD ->LUMO(25%),HOMO>L+1(48%) |  |
| 10 | 350.78 | 0.3272 | H-3->LUMO (54%), HOMO->L+2 (36%) | H-2 Cd-GQD ->L+1 (2%) |

Armchair GQDs with Cd0 in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 5 | 441.86 | 0.2645 | H-2->L+1 (13%), H-1->LUMO (86%) |  |
| 8 | 379.27 | 1.1099 | H-2->LUMO (47%), H-1->L+1 (49%) |  |
| 9 | 379.11 | 1.0382 | H-2->L+1 (82%), H-1->LUMO (12%) | H-3->LUMO (3%) |

Armchair GQDs with Cd0 in Ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 5 | 441.86 | 0.2597 | H-2->L+1 (13%), H-1->LUMO (86%) |  |
| 10 | 379.23 | 1.0972 | H-2->LUMO (48%), H-1->L+1 (49%) |  |
| 11 | 379.19 | 1.0339 | H-2->L+1 (83%), H-1->LUMO (13%) | H-3->LUMO (3%) |

Armchair GQDs with Cd0 in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 5 | 442.27 | 0.2796 | H-2->L+1 (12%), H-1->LUMO (87%) |  |
| 10 | 380.49 | 1.1465 | H-2->LUMO (48%), H-1->L+1 (49%) |  |
| 11 | 380.08 | 1.0718 | H-2->L+1 (83%), H-1->LUMO (12%) | H-3->LUMO (3%) |

Armchair GQDs with Cd0 in H2O

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 5 | 441.743 | 0.2511 | H-2->L+1 (13%), H-1->LUMO (86%) |  |
| 10 | 378.890 | 1.0151 | H-2->L+1 (83%), H-1->LUMO (13%) | H-3->LUMO (2%) |
| 11 | 378.774 | 1.0734 | H-2->LUMO (48%), H-1->L+1 (49%) |  |

Table S4. Top view and side view of the optimized geometries of the Hg adatom adsorbed on surface of GQD

| Dielectric Media | Hg0@GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Gas-phase |  |  |
| Acetic Acid |  |  |
| Ethanol |  |  |
| DMF |  |  |
| Water |  |  |

Figure S3 Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in GQDs after complexation with Hg0. (a) and (b) represent molecular orbitals of Hg0@ZZ-GQDs in gas-phase and water, respectively. (c) and (d) show molecular orbitals of Hg0@AC-GQDs in the gas-phase and water, respectively. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Dataset S2. Electronic transitions in Hg0@GQD

Zigzag GQDs with Hg0 in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 3 | 415.34 | 0.9655 | H-1->LUMO (28%), H-1->L+1 (19%), HOMO->LUMO (19%), HOMO->L+1 (28%) |
| 4 | 415.34 | 0.9656 | H-1->LUMO (19%), H-1->L+1 (29%), HOMO->LUMO (28%), HOMO->L+1 (19%) |

Zigzag GQDs with Hg0 in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 5 | 428.29 | 1.3713 | H-1->LUMO (48%), HOMO->L+1 (48%) |
| 6 | 428.25 | 1.3702 | H-1->L+1 (48%), HOMO->LUMO (48%) |

Zigzag GQDs with Hg0 in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 5 | 428.18 | 1.3548 | H-1->LUMO (34%), H-1->L+1 (15%), HOMO->LUMO (15%), HOMO->L+1 (34%) |
| 6 | 428.16 | 1.3534 | H-1->LUMO (15%), H-1->L+1 (34%), HOMO->LUMO (33%), HOMO->L+1 (15%) |

Zigzag GQDs with Hg0 in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 5 | 430.17 | 1.4208 | H-1->L+1 (49%), HOMO->LUMO (49%) |
| 6 | 430.15 | 1.4203 | H-1->LUMO (49%), HOMO->L+1 (49%) |

Zigzag GQDs with Hg0 in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 5 | 427.47 | 1.3272 | H-1->LUMO (33%), H-1->L+1 (16%), HOMO->LUMO (16%), HOMO->L+1 (33%) |
| 6 | 427.443 | 1.3267 | H-1->LUMO (16%), H-1->L+1 (33%), HOMO->LUMO (33%), HOMO->L+1 (16%) |

Armchair GQDs with Hg0 in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 2 | 439.41 | 0.1559 | H-1->L+1 (17%), HOMO->LUMO (82%) |  |
| 4 | 372.49 | 0.7536 | H-1->L+1 (76%), HOMO->LUMO (16%) | H-2->LUMO (6%) |
| 5 | 370.51 | 0.8206 | H-1->LUMO (47%), HOMO->L+1 (48%) |  |
| 7 | 350.86 | 0.3218 | H-2->LUMO (55%), HOMO->L+2 (35%) | H-1->L+1 (4%) |

Armchair GQDs with Hg0 in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 2 | 441.94 | 0.2681 | H-1 Hg -GQD ->L+1 (12%), HOMO->LUMO (86%) |  |
| 6 | 378.95 | 1.1619 | H-1 Hg -GQD ->LUMO (44%), HOMO->L+1 (49%) | H-2 Cd-GQD ->LUMO (4%) |
| 7 | 378.84 | 1.0792 | H-1 Hg -GQD ->L+1 (73%), HOMO->LUMO (12%) | H-3->LUMO (3%), H-2 Hg -GQD ->L+1 (9%) |
| 9 | 355.17 | 0.3086 | H-3->LUMO (56%), HOMO->L+2 (39%) |  |

Armchair GQDs with Hg0 in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 441.97 | 0.2617 | H-2->L+1 (13%), HOMO->LUMO (86%) |  |
| 6 | 378.95 | 1.0766 | H-2->L+1 (83%), HOMO->LUMO (13%) | H-3->LUMO (2%) |
| 7 | 378.89 | 1.1476 | H-2->LUMO (48%), HOMO->L+1 (49%) |  |
| 10 | 355.25 | 0.3096 | H-3->LUMO (54%), HOMO->L+2 (41%) |  |

Armchair GQDs with Hg0 in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 442.37 | 0.2811 | H-2->L+1 (12%), HOMO->LUMO (86%) |  |
| 6 | 380.15 | 1.2 | H-2->LUMO (48%), HOMO->L+1 (49%) |  |
| 7 | 379.86 | 1.1186 | H-2->L+1 (83%), HOMO->LUMO (12%) | H-3->LUMO (3%) |
| 10 | 355.83 | 0.3052 | H-3->LUMO (54%), HOMO->L+2 (41%) |  |

Armchair GQDs with Hg0 in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 441.88 | 0.249 | H-2->L+1 (13%), HOMO->LUMO (84%) |  |
| 6 | 378.65 | 1.0583 | H-2->L+1 (83%), HOMO->LUMO (13%) | H-3->LUMO (2%) |
| 7 | 378.40 | 1.1168 | H-2->LUMO (47%), HOMO->L+1 (49%) |  |
| 10 | 355.06 | 0.3112 | H-3->LUMO (53%), HOMO->L+2 (42%) |  |

Table S5. Top view and side view of the optimized geometries of the Pb adatom adsorbed on surface of GQD

| Dielectric Media | Pb0@GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Gas-phase |  |  |
| Acetic Acid |  |  |
| Ethanol |  |  |
| DMF |  |  |
| Water |  |  |

Figure S4 Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in zigzag-edged GQDs after complexation with Pb0 in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Figure S5 Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in armchair-edged GQDs after complexation with Pb0 in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Dataset S3. Electronic transitions in Pb0@GQD

Zigzag GQDs with Pb0 in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1468.83 | 0.0185 | HOMO Pb-GQD ->L+1 Pb-GQD (72%), HOMO Pb-GQD ->L+3 Pb-GQD (33%) |  |
| 7 | 729.27 | 0.0259 | HOMO Pb-GQD ->L+6 (97%) |  |
| 11 | 571.69 | 0.0143 | H-1->LUMO Pb-GQD (11%), HOMO Pb-GQD ->L+9 (46%), HOMO Pb-GQD ->L+10 (34%) | HOMO Pb-GQD ->L+7 (5%) |
| 12 | 555.48 | 0.024 | H-2->LUMO Pb-GQD (23%), H-2->L+1 Pb-GQD (12%), H-1->LUMO Pb-GQD (42%), HOMO Pb-GQD ->L+10 (15%) | HOMO Pb-GQD ->L+7 (4%) |

Zigzag GQDs with Pb0 in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 2197.13 | 0.0086 | HOMO Pb-GQD ->L+1 Pb-GQD (64%), HOMO Pb-GQD ->L+3 Pb-GQD (36%) |  |
| 7 | 725.35 | 0.0065 | HOMO Pb-GQD ->L+6 (99%) |  |
| 9 | 633.70 | 0.0074 | HOMO Pb-GQD ->L+8 (92%) | HOMO Pb-GQD ->L+10 (5%) |
| 10 | 594.36 | 0.0287 | HOMO Pb-GQD ->L+10 (85%) | HOMO Pb-GQD ->L+8 (7%), HOMO Pb-GQD ->L+9 (8%) |

Zigzag GQDs with Pb0 in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1802.88 | 0.0207 | HOMO Pb-GQD ->L+1 Pb-GQD (100%) |  |
| 6 | 868.54 | 0.0048 | HOMO Pb-GQD ->L+4 (99%) |  |
| 7 | 667.47 | 0.0074 | HOMO Pb-GQD ->L+6 (99%) |  |
| 9 | 596.13 | 0.0174 | HOMO Pb-GQD ->L+7 (100%) |  |

Zigzag GQDs with Pb0 in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1792.71 | 0.0206 | HOMO Pb-GQD ->L+1 Pb-GQD (100%) |  |
| 6 | 860.22 | 0.0047 | HOMO Pb-GQD ->L+4 (100%) |  |
| 7 | 661.49 | 0.0073 | HOMO Pb-GQD ->L+6 (99%) |  |
| 9 | 592.60 | 0.0174 | HOMO Pb-GQD ->L+7 (100%) |  |
| 12 | 536.86 | 0.0014 | HOMO Pb-GQD ->L+10 (96%) | HOMO Pb-GQD ->L+9 (2%) |

Zigzag GQDs with Pb0 in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1749.45 | 0.0191 | HOMO Pb-GQD ->L+1 (100%) |  |
| 6 | 850.08 | 0.0042 | HOMO Pb-GQD ->L+4 (100%) |  |
| 7 | 654.61 | 0.006 | HOMO Pb-GQD ->L+6 (99%) |  |
| 9 | 587.60 | 0.0165 | HOMO Pb-GQD ->L+7 (99%) |  |

Armchair GQDs with Pb0 in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1220.79 | 0.0222 | HOMO Pb-GQD ->L+1 (83%), HOMO->L+3 (14%) | HOMOPb-GQD ->L+4 Pb-GQD (4%), HOMOPb-GQD ->L+7 (2%) |
| 5 | 994.97 | 0.0165 | HOMO Pb-GQD ->L+3 Pb-GQD (48%), HOMO Pb-GQD ->L+4Pb-GQD (49%) | HOMOPb-GQD ->L+1 Pb-GQD (2%) |
| 8 | 621.47 | 0.0219 | HOMO Pb-GQD ->L+8 (94%) | HOMOPb-GQD ->L+10 (3%) |
| 9 | 613.20 | 0.0287 | HOMO Pb-GQD ->L+7 Pb-GQD (84%) | H-1->LUMO Pb-GQD (4%), HOMO Pb-GQD ->L+1 (2%), HOMOPb-GQD ->L+5 Pb-GQD (8%) |
| 10 | 552.14 | 0.0231 | HOMO Pb-GQD ->L+9 (91%) | H-1->LUMO Cd-GQD (6%) |
| 11 | 512.54 | 0.0569 | H-1->LUMO Pb-GQD (81%) | H-2->L+1 Pb-GQD (2%), HOMOPb-GQD ->L+5 Pb-GQD (2%), HOMO Pb-GQD ->L+9 (6%), HOMO Pb-GQD ->L+10 (3%) |
| 12 | 504.51 | 0.0135 | HOMO Pb-GQD ->L+10 (90%) | H-1->LUMOPb-GQD (3%), HOMO Pb-GQD ->L+8 (3%) |

Armchair GQDs with Pb0 in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 1796.61 | 0.014 | HOMO Pb-GQD ->L+1 Pb-GQD (63%), HOMO->L+3 Pb-GQD (25%) | HOMO Pb-GQD ->LUMO Pb-GQD (9%), HOMO Pb-GQD ->L+2 Pb-GQD (3%) |
| 8 | 661.39 | 0.0307 | HOMO Pb-GQD ->L+7 (96%) | HOMO Pb-GQD ->L+5 Pb-GQD (2%) |
| 10 | 577.82 | 0.0139 | HOMO Pb-GQD ->L+9 (99%) |  |
| 12 | 470.93 | 0.0282 | H-2->L+1 Pb-GQD (14%), H-1->LUMO Pb-GQD (77%) | H-1->L+1 Pb-GQD (7%) |

Armchair GQDs with Pb0 in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 3 | 1687.77 | 0.0089 | HOMO Pb ->LUMO (78%), HOMO Pb ->L+3 Pb-GQD (22%) |
| 8 | 629.26 | 0.0244 | HOMO Pb ->L+7 (97%) |
| 10 | 549.69 | 0.0092 | HOMO Pb ->L+9 (98%) |
| 12 | 466.73 | 0.0189 | H-2->LUMO (19%), H-1->L+1 Pb-GQD (80%) |

Armchair GQDs with Pb0 in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 3 | 1667.12 | 0.0087 | HOMO Pb ->LUMO (80%), HOMO Pb ->L+3 Pb-GQD (20%) |
| 5 | 924.35 | 0.0024 | HOMO Pb ->L+4 (99%) |
| 8 | 624.79 | 0.0244 | HOMO Pb ->L+7 (97%) |
| 10 | 545.53 | 0.0089 | HOMO Pb ->L+9 (98%) |
| 12 | 466.57 | 0.0198 | H-2->LUMO (19%), H-1->L+1 Pb-GQD (80%) |

Armchair GQDs with Pb0 in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 3 | 1626.44 | 0.0078 | HOMO Pb ->LUMO (79%), HOMO Pb ->L+3 Pb-GQD (20%) |
| 5 | 909.17 | 0.0021 | HOMO Pb ->L+4 (99%) |
| 8 | 618.15 | 0.0229 | HOMO Pb ->L+7 (97%) |
| 10 | 540.49 | 0.0082 | HOMO Pb ->L+9 (98%) |
| 12 | 466.29 | 0.0171 | H-2->LUMO (19%), H-1->L+1 Pb-GQD (80%) |

Figure S6. The equilibrium distances (in Å) between metal atom (Cd, Hg, and Pb) and the zigzag-edged GQD calculated in the gas-phase by different methods. Note: due to the “convergence failure” the using of the PBE functional is not appropriate approach to optimize the Pb@GQD geometry using Gaussian 09 software. Here and further we are comparing only the M06-2X and B3LYP functional predictions for interaction strength between neutral Pb species and GQDs.

Figure S7. The equilibrium distances (in Å) between metal atom (Cd, Hg, and Pb) and the armchair-edged GQD calculated in the gas-phase by different methods.

Figure S8. Dependence of the binding energy of the Cd@GQD complex on the dielectric permittivity. Left panel represents the case of zigzag-edged GQDs. Right panel shows the results for the armchair-edged GQDs.

Figure S9. Dependence of the binding energy of the Hg@GQD complex on the dielectric permittivity. Left panel represents the case of zigzag-edged GQDs. Right panel shows the results for the armchair-edged GQDs.

Figure S10. Dependence of the binding energy of the Pb@GQD complex on the dielectric permittivity. Left panel represents the case of zigzag-edged GQDs. Right panel shows the results for the armchair-edged GQDs.

Figure S11. Dependence of the HOMO-LUMO gap of the Cd@GQD complex on the dielectric permittivity. Left panel represents the case of zigzag-edged GQDs. Right panel shows the results for the armchair-edged GQDs.

Figure S12. Dependence of the HOMO-LUMO gap of the Hg@GQD complex on the dielectric permittivity. Left panel represents the case of zigzag-edged GQDs. Right panel shows the results for the armchair-edged GQDs.

Figure S13. Dependence of the HOMO-LUMO gap of the Pb@GQD complex on the dielectric permittivity. Left panel represents the case of zigzag-edged GQDs. Right panel shows the results for the armchair-edged GQDs.

Figure S14. A comparison of the absorption spectra of the GQDs obtained in different dielectric media by using the PCM/TD-DFT/B3LYP/6-31G (solid curves), PCM/TD-DFT/M06-2X/6-311G(d,p) (dash-dot curves) and PCM/TD-DFT/PBE-D3/6-311G(d,p) (dotted curves) calculations of excited transitions: (a) zigzag edge termination and (b) armchair edge termination. Colour represents of dielectric medium.

Figure S15. A comparison of the absorption spectra of the GQDs after complexation with Cd0 obtained in different dielectric media by using the PCM/TD-DFT/B3LYP/6-31G (solid curves), PCM/TD-DFT/M06-2X/6-311G(d,p) (dash-dot curves) and PCM/TD-DFT/PBE-D3/6-311G(d,p) (dotted curves) calculations of excited transitions: (a) zigzag edge termination and (b) armchair edge termination. Colour represents of dielectric medium.

Figure S16. A comparison of the absorption spectra of the GQDs after complexation with Hg0 obtained in different dielectric media by using the PCM/TD-DFT/B3LYP/6-31G (solid curves), PCM/TD-DFT/M06-2X/6-311G(d,p) (dash-dot curves) and PCM/TD-DFT/PBE-D3/6-311G(d,p) (dotted curves) calculations of excited transitions: (a) zigzag edge termination and (b) armchair edge termination. Colour represents of dielectric medium.

Figure S17. A comparison of the absorption spectra of the zigzag-edged GQDs after complexation with Pb0 obtained in different dielectric media by using the (a) PCM/TD-DFT/B3LYP/6-31G, PCM/TD-DFT/M06-2X/6-311G(d,p) and (b) PCM/TD-DFT/PBE-D3/6-311G(d,p) calculations of excited transitions.

Figure S18. A comparison of the absorption spectra of the armchair-edged GQDs after complexation with Pb0 obtained in different dielectric media by using the (a) PCM/TD-DFT/B3LYP/6-31G, PCM/TD-DFT/M06-2X/6-311G(d,p) and (b) PCM/TD-DFT/PBE-D3/6-311G(d,p) calculations of excited transitions.

Table S6. Top view and side view of the optimized geometries of the Cd2+ ion adsorbed on surface of GQD

| Dielectric Media | Cd2+@GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Gas-phase |  |  |
| Acetic Acid |  |  |
| Ethanol |  |  |
| DMF |  |  |
| Water |  |  |

Figure S19.  Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in zigzag-edged GQDs after complexation with Cd2+ in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Figure S20. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in armchair-edged GQDs after complexation with Cd2+ in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Dataset S4. Electronic transitions in Cd2+@GQD

Zigzag GQDs with Cd2+ in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1010.13 | 0.0484 | H-4->LUMO Cd-GQD (94%) | H-5->LUMO Cd-GQD (5%) |
| 5 | 832.22 | 0.2318 | H-2->LUMOCd-GQD(90%),HOMO>L+1(11%) |  |
| 6 | 632.41 | 0.1198 | H-5->LUMO Cd-GQD (90%) | H-4->LUMO Cd-GQD (4%), HOMO->L+2 (4%) |
| 12 | 489.93 | 0.1804 | H-1Cd-GQD ->L+2(59%),HOMO>L+1(37%) | H-2->LUMO (3%) |

Zigzag GQDs with Cd2+ in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 817.51 | 0.0421 | H-2->LUMO Cd-GQD (98%) |  |
| 7 | 543.88 | 0.0418 | H-1 Cd-GQD ->L+2 (35%), HOMO->L+1 (62%) |  |
| 12 | 444.91 | 0.3557 | H-9->LUMO Cd-GQD (66%), H-1 Cd-GQD ->L+2 (15%) | H-1 Cd-GQD ->L+1 (2%), HOMO->L+1 (8%), HOMO->L+2 (5%) |

Zigzag GQDs with Cd2+ in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 9 | 438.04 | 0.1388 | H-6->LUMO Cd (87%) | H-1>L+1(6%),HOMO>L+2(6%) |
| 10 | 433.58 | 0.2032 | H-7->LUMO Cd (85%) | H-1>L+2(7%),HOMO>L+1(7%) |
| 11 | 429.05 | 0.6503 | H-8->LUMOCd(43%),H-1->L+1(23%),HOMO->L+2(24%) | H-6->LUMO Cd (9%) |
| 12 | 428.09 | 1.1793 | H-7->LUMOCd(14%),H-1->L+2(42%), HOMO->L+1(41%) |  |

Zigzag GQDs with Cd2+ in gas DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 9 | 430.81 | 1.3897 | H-1->L+1 (47%), HOMO->L+2 (47%) |  |
| 10 | 430.62 | 1.436 | H-1->L+2 (49%), HOMO->L+1 (48%) |  |
| 11 | 410.20 | 0.0395 | H-6->LUMO Cd (97%) |  |

Zigzag GQDs with Cd2+ in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 8 | 428.81 | 1.3263 | H-1->L+1 (48%), HOMO->L+2 (49%) |  |
| 9 | 428.49 | 1.3406 | H-1->L+2 (50%), HOMO->L+1 (46%) |  |

Armchair GQDs with Cd2+ in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 1508.50 | 0.0498 | H-2->LUMO Cd-GQD (93%) | H-4->LUMO Cd-GQD (7%) |
| 5 | 835.36 | 0.1191 | H-4->LUMO Cd-GQD (86%) | H-6->LUMO Cd-GQD (3%), H-2->LUMO Cd-GQD (7%), H-1->L+1 (3%) |
| 6 | 754.52 | 0.5419 | H-5->LUMO Cd-GQD (12%), H-3->LUMO Cd-GQD(85%) |  |

Armchair GQDs with Cd2+ in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 9 | 477.06 | 0.0942 | H-8->LUMO Cd-GQD (48%), HOMO Cd-GQD ->L+1 (39%) | H-9->LUMOCd-GQD(5%),H-1->L+2(3%) |
| 10 | 467.95 | 0.1481 | H-8->LUMO Cd-GQD (35%), HOMO Cd-GQD ->L+1 (41%) | H-1->L+1 (9%), H-1->L+2 (4%), HOMO Cd-GQD ->L+2 (6%) |
| 11 | 463.16 | 0.0671 | H-1->L+1 (57%), HOMO Cd-GQD ->L+2 (23%) | H-8->LUMO Cd-GQD (6%), HOMO Cd-GQD ->L+1 (9%) |

Armchair GQDs with Cd2+ in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 9 | 447.96 | 0.0126 | H-7->LUMO Cd (86%) | H-8->LUMO Cd (8%), HOMO->L+1 (3%) |
| 10 | 442.29 | 0.2527 | H-1->L+2 (13%), HOMO->L+1(82%) | H-7->LUMO Cd (4%) |
| 12 | 383.74 | 0.1387 | H-2->L+1 (42%), HOMO->L+3(32%) | H-9->LUMO Cd (8%), H-1->L+1 (7%), HOMO->L+2 (7%) |

Armchair GQDs with Cd2+ in gas DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 8 | 445.68 | 0.0091 | H-6->LUMO Cd (90%) | HOMO->L+1 (4%) |
| 9 | 442.53 | 0.2768 | H-1->L+2 (12%), HOMO->L+1 (82%) | H-6->LUMO Cd (4%) |
| 12 | 383.30 | 0.1322 | H-2->L+1 (45%), HOMO->L+3 (39%) | H-1->L+1 (6%), HOMO->L+2 (6%) |

Armchair GQDs with Cd2+ in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 7 | 442.20 | 0.255 | H-1->L+2 (14%), HOMO->L+1 (85%) |  |
| 10 | 390.64 | 0.0072 | H-7->LUMO Cd (96%) |  |
| 12 | 378.72 | 1.102 | H-1->L+2 (81%), HOMO->L+1 (14%) |  |

Table S7. Top view and side view of the optimized geometries of the Hg2+ ion adsorbed on surface of GQD

| Dielectric Media | Hg2+@GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Gas-phase |  |  |
| Acetic Acid |  |  |
| Ethanol |  |  |
| DMF |  |  |
| Water |  |  |

Figure S21. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in zigzag-edged GQDs after complexation with Hg2+ in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Figure S22. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in armchair-edged GQDs after complexation with Hg2+ in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Dataset S5. Electronic transitions in Hg2+@GQD

Zigzag GQDs with Hg2+ in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1010.05 | 0.0536 | H-4->LUMO (93%) | H-5->LUMO (6%) |
| 5 | 820.10 | 0.2465 | H-2->LUMO (88%), HOMO->L+1 (12%) |  |
| 6 | 625.77 | 0.1457 | H-5->LUMO (89%) | H-4->LUMO (5%), HOMO->L+2 (5%) |
| 11 | 466.03 | 0.824 | H-2->LUMO (12%), HOMO->L+1 (85%) |  |

Zigzag GQDs with Hg2+ in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 1046.63 | 0.0525 | H-4->LUMO Hg-GQD (69%), H-3->LUMO Hg-GQD (20%) | H-5->LUMO Hg-GQD (3%), H-2->LUMO Hg-GQD (6%) |
| 5 | 862.73 | 0.3714 | H-2->LUMO Hg-GQD (89%) | H-4->LUMO Hg-GQD (4%), H-3->LUMO Hg-GQD (3%), H-1 Hg-GQD ->L+1 (4%) |
| 6 | 645.88 | 0.1299 | H-5->LUMO Hg-GQD (92%) | HOMO Hg-GQD ->L+1 (3%) |
| 12 | 509.61 | 0.1697 | H-1 Hg-GQD ->L+1 (39%), HOMO Hg-GQD ->L+2 (45%) | H-1 Hg-GQD ->L+2 (8%), HOMO Hg-GQD ->L+1 (5%) |

Zigzag GQDs with Hg2+ in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 2 | 2739.98 | 0.0239 | H-1 Hg-GQD ->LUMO Hg-GQD (120%) |  |
| 5 | 960.96 | 0.0315 | H-2->LUMO Hg-GQD (99%) |  |
| 6 | 660.33 | 0.0114 | H-5->LUMO Hg-GQD (99%) |  |

Zigzag GQDs with Hg2+ in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs |
| --- | --- | --- | --- |
| 2 | 2785.53 | 0.0106 | H-1->LUMO Hg (101%) |
| 5 | 856.65 | 0.0061 | H-2->LUMO Hg (100%) |
| 8 | 538.85 | 0.0102 | H-7->LUMO Hg (98%) |

Zigzag GQDs with Hg2+ in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 2 | 2017.97 | 0.0039 | H-1->LUMO Hg (100%) |  |
| 5 | 735.59 | 0.001 | H-4->LUMO Hg (99%) |  |
| 10 | 493.86 | 0.007 | H-7->LUMO Hg (98%) |  |

Armchair GQDs with Hg2+ in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 1474.07 | 0.0532 | H-4->LUMO (10%), H-1->LUMO (92%) |  |
| 5 | 834.06 | 0.1348 | H-4->LUMO (84%), H-1->LUMO (10%) | H-6->LUMO (3%), HOMO->L+1 (3%) |
| 6 | 734.63 | 0.63 | H-3->LUMO (90%) | H-5->LUMO (7%), HOMO->L+2 (2%) |
| 12 | 478.64 | 0.021 | H-11->LUMO (90%) | H-1->L+1 (5%) |

Armchair GQDs with Hg2+ in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 851.24 | 0.1442 | H-4->LUMO Hg-GQD (89%) | H-6->LUMO Hg-GQD(3%),H-2->LUMO Hg-GQD(5%) |
| 6 | 776.98 | 0.637 | H-5->LUMO Hg-GQD(13%),H-3->LUMOHgGQD(85%) |  |
| 10 | 536.35 | 0.1239 | HOMO Hg-GQD ->L+1 (95%) |  |

Armchair GQDs with Hg2+ in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 9 | 578.50 | 0.0037 | H-8->LUMO Hg (99%) |  |
| 10 | 502.38 | 0.0023 | H-9->LUMO Hg (98%) |  |
| 12 | 460.34 | 0.0055 | H-11->LUMO Hg (99%) |  |

Armchair GQDs with Hg2+ in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 5 | 703.01 | 0.0016 | H-3->LUMO Hg (90%) | H-5->LUMO Hg (9%) |
| 9 | 529.37 | 0.0034 | H-8->LUMO Hg (99%) |  |
| 10 | 463.83 | 0.002 | H-9->LUMO Hg (98%) |  |

Armchair GQDs with Hg2+ in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 5 | 622.94 | 0.0013 | H-3->LUMO Hg (91%) | H-5->LUMO Hg (8%) |
| 9 | 484.02 | 0.0029 | H-8->LUMO Hg (99%) |  |
| 11 | 442.32 | 0.2571 | H-1->L+2 (14%), HOMO->L+1 (85%) |  |

Table S8. Top view and side view of the optimized geometries of the Pb2+ ion adsorbed on surface of GQD

| Dielectric Media | Pb2+@GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Gas-phase |  |  |
| Acetic Acid |  |  |
| Ethanol |  |  |
| DMF |  |  |
| Water |  |  |

Figure S23. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in zigzag-edged GQDs after complexation with Pb2+ in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Figure S24. Images showing the spatial distribution of wave-functions corresponding to occupied and unoccupied orbitals, which are involved in electronic transitions in armchair-edged GQDs after complexation with Pb2+ in different media. The red and green colours indicate positive and negative phases in the wave function, respectively. The orbitals are drawn at an isosurface value of 0.02.

Dataset S6. Electronic transitions in Pb2+@GQD

Zigzag GQDs with Pb2+ in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 1383.90 | 0.0085 | H-1->LUMO(11%),HOMO->L+1(88%) |  |
| 4 | 1188.27 | 0.0314 | H-1->L+1 (96%) |  |
| 12 | 595.70 | 0.0088 | H-3->LUMO (69%),HOMO>L+3(12%) | H-4->L+1(8%),H-2->L+1(6%),H-1>L+4(4%) |

Zigzag GQDs with Pb2+ in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 803.31 | 0.0305 | H-1->L+1 (68%), HOMO->LUMO (30%) |  |
| 4 | 786.85 | 0.0495 | H-1->LUMO (96%) |  |
| 8 | 514.62 | 0.0187 | H-1->L+3 (55%), HOMO->L+4 (38%) | H-2->L+1 (4%) |
| 11 | 479.88 | 0.0796 | H-4->LUMO (59%), H-3->L+1 (16%), HOMO->L+4 (12%) | H-1->L+3 (8%) |

Zigzag GQDs with Pb2+ in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 687.76 | 0.0586 | H-1->L+1 (87%) | HOMO->LUMO (8%), HOMO->L+2 (3%) |
| 9 | 456.69 | 0.2759 | H-2->LUMO (35%), H-1->L+2 (14%), HOMO->L+4 (29%) | H-4->L+1 (8%), H-3->LUMO (6%), HOMO->L+5 (5%) |
| 11 | 449.96 | 0.1747 | H-2->LUMO (62%), H-1->L+2 (10%) | H-4->L+1 (7%), H-3->LUMO (7%), HOMO->L+4 (8%), HOMO->L+5 (4%) |
| 12 | 443.92 | 0.6543 | H-3->L+1 (18%), H-1->L+4 (38%), HOMO->L+2 (26%) | H-4->LUMO (8%), H-1->L+5 (4%) |

Zigzag GQDs with Pb2+ in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 3 | 681.90 | 0.052 | H-1->LUMO (56%), HOMO->L+1 (38%) | H-1->L+2 (2%) |
| 4 | 675.62 | 0.065 | H-1->L+1 (84%), HOMO->LUMO (10%) | HOMO->L+2 (3%) |
| 9 | 454.18 | 0.4577 | H-2->LUMO (16%), H-1->L+2 (21%), HOMO->L+4 (36%) | H-4->L+1 (8%), H-3->LUMO (6%), HOMO->L+5 (7%) |
| 11 | 445.15 | 0.1071 | H-2->LUMO (80%) | H-4->L+1 (3%), H-3->LUMO (4%), H-1->L+2 (6%), HOMO->L+4 (3%), HOMO->L+5 (2%) |
| 12 | 443.40 | 0.8517 | H-1->L+4 (44%), HOMO->L+2 (31%) | H-4->LUMO (2%), H-3->L+1 (6%), H-2->L+1 (4%), H-1->L+1 (2%), H-1->L+5 (4%) |

Zigzag GQDs with Pb2+ in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 9 | 450.19 | 0.4794 | H-2->LUMO (10%), H-1->L+2 (23%), HOMO->L+4 (31%) | H-4->L+1 (8%), H-3->LUMO (6%), HOMO->L+3 (7%), HOMO->L+5 (9%) |
| 10 | 440.30 | 0.7238 | H-2->L+1 (10%), H-1->L+3 (10%), H-1->L+4 (36%), HOMO->L+2 (29%) | H-4->LUMO (2%), H-1->L+5 (5%) |
| 11 | 439.02 | 0.0687 | H-2->LUMO (84%) | H-3->LUMO (3%), H-1->L+2 (4%) |
| 12 | 438.66 | 0.1126 | H-2->L+1 (83%) | H-3->L+1 (5%), H-1->L+4 (3%), HOMO->L+2 (3%) |

Armchair GQDs with Pb2+ in gas phase

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 796.60 | 0.0203 | H-2->LUMO (96%) | HOMO->LUMO (3%) |
| 6 | 737.91 | 0.024 | H-2->L+1 (11%), H-1->LUMO (68%), HOMO->L+1 (20%) |  |
| 8 | 593.68 | 0.0191 | H-3->L+1 (97%) |  |
| 10 | 529.75 | 0.066 | H-4->LUMO (10%), H-1->L+4 (12%), HOMO->L+3 (73%) |  |
| 12 | 520.30 | 0.0184 | H-4->LUMO (83%), HOMO->L+3 (12%) |  |

Armchair GQDs with Pb2+ in acetic acid

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 552.63 | 0.0329 | H-1->LUMO (85%), HOMO->L+1 (14%) |  |
| 5 | 542.29 | 0.0205 | H-2->LUMO (98%) |  |
| 7 | 483.76 | 0.1889 | H-1->L+3 (13%), HOMO->L+2 (85%) |  |
| 12 | 429.54 | 0.3302 | H-3->LUMO (33%), H-1->L+2 (39%), HOMO->L+3 (22%) |  |

Armchair GQDs with Pb2+ in ethanol

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 504.41 | 0.0301 | H-1->LUMO (85%), HOMO->L+1 (12%) | HOMO->L+3 (2%) |
| 7 | 472.78 | 0.0199 | H-1->L+2 (36%), HOMO->L+3 (58%) |  |
| 8 | 471.79 | 0.2056 | H-1->L+3 (13%), HOMO->L+2 (82%) | H-2->LUMO (3%) |
| 12 | 415.38 | 0.6156 | H-1->L+2 (55%), HOMO->L+3 (32%) | H-2->L+3 (2%), H-1->L+4 (4%) |

Armchair GQDs with Pb2+ in DMF

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 499.79 | 0.0306 | H-1->LUMO (85%), HOMO->L+1 (11%) | HOMO->L+3 (2%) |
| 8 | 470.47 | 0.2269 | H-1->L+3 (13%), HOMO->L+2 (80%) | H-2->LUMO (5%) |
| 10 | 422.08 | 0.0268 | H-1->L+4 (91%) | H-1->L+2 (5%), HOMO->L+3 (2%) |
| 12 | 414.62 | 0.6519 | H-1->L+2 (54%), HOMO->L+3 (31%) | H-2->L+3 (3%), H-1->L+4 (7%) |

Armchair GQDs with Pb2+ in water

| No. | Wavelength (nm) | Osc. Strength | Major contribs | Minor contribs |
| --- | --- | --- | --- | --- |
| 4 | 493.60 | 0.0276 | H-1->LUMO (84%), HOMO->L+1 (11%) | HOMO->L+3 (4%) |
| 7 | 469.28 | 0.0237 | H-2->L+1 (19%), H-1->L+2 (32%), HOMO->L+3 (44%) | H-1->LUMO (3%) |
| 8 | 467.95 | 0.2069 | H-2->LUMO (13%), H-1->L+3 (13%), HOMO->L+2 (72%) |  |
| 12 | 411.64 | 0.6239 | H-1->L+2 (54%), HOMO->L+3 (32%) | H-2->L+3 (3%), H-1->L+4 (5%) |

Table S9. Top view and side view of the optimized geometries of the HM species adsorbed on surface of GQD. Prior to optimization the metal species were located at the edges of the GQD

| Metal | GQD |  |
| --- | --- | --- |
|  | ZZ | AC |
| Cd0 |  |  |
| Hg0 |  |  |
| Pb0 |  |  |
| Cd2+ |  |  |
| Hg2+ |  |  |
| Pb2+ |  |  |