Supplementary Information

Quantitative analysis of metals ins steel using handheld µ-LIBS instrument
Muhammad Sher Afgan, Zongyu Hou and Zhe Wang
Department of Thermal Engineering, Tsinghua-BP Clean Energy Center, Tsinghua University, Beijing 100084, China.
Corresponding author E-mail: zhewang@tsinghua.edu.cn

Table S1 Certified value of C, Cr, Si, Cu, Mn, Ni, Mo and V in eigthy four steel samples
Sample number	C	Cr	Si	Cu	Mn	Ni	Mo	V	
P1	0.887	0.318	0.346	0.258	0.425	0.301			
P2	0.637	0.17	0.302	0.148	0.588	0.166			
P3	0.081	0.07	0.215	0.008	0.422	0.0064	0.0012		
P4	0.144	12.07	0.56	0.207	0.71	0.184			
P5	0.055	12.58	0.115	0.295	0.44	0.39	0.052	0.031	
P6	1.68	11.29	0.235	0.058	0.242	0.106	0.386	0.195	
P7	0.134	17.01	1.06	0.16	1.51	8.56	0.062		
P8	0.15	0.944	0.208	0.062	0.571	0.027	0.439		
P9	0.178	1.3	0.299	0.019	1.14	0.038	0.233	0.022	
P10	0.173	0.028	0.535	0.019	1.15	0.017		0.054	
P11	0.123	4.48	0.295	0.144	0.433	0.075	0.506		
P12	0.164	0.1	0.204	0.016	0.654	0.038	<0.02		
P13	0.157	0.03	0.22	0.01	1.28	0.02		0.067	
P14	0.122	0.062	0.253	0.135	0.447	0.053			
P15	0.22	0.065	0.291	0.016	0.576	0.088			
P16	0.289	0.032	0.31	0.038	0.613	0.022			
P17	0.138		0.073	0.029	0.71				
P18	0.116	1.08	0.303	0.016	0.567	0.015	0.351	0.291	
P19	0.164	0.011	0.39	0.029	1.34	0.022	<0.01		
P20	0.099	2.2	0.35	0.128	0.54	0.073	1.03	0.0155	
P21	0.133	1.16	0.69	0.17	0.46	0.15	0.52	0.004	
P22	0.121	8.75	0.68	0.133	0.43	0.29	0.95	0.014	
P23	0.49	0.044	0.292	0.038	0.663	0.03			
P24	0.682	0.148	0.206	0.109	0.22	0.057	0.034	0.0049	
P25	0.249	1.64	0.464	0.097	0.444	1.73		0.218	
P26	0.029	17.4	0.383	0.205	1.27	9.15	0.156	0.061	
P27	0.66	0.119	0.297	0.075	1.01	0.032			
P28	0.379	5.14	1.03	0.097	0.292	0.152	1.24	0.844	
P29	1.15	0.127	0.201	0.119	0.366	0.115	0.037		
P30	0.75	4.2	0.282	0.137	0.16	0.041	0.1	1.17	
P31	0.286	0.952	0.226	0.096	0.446	0.04	0.172		
P32	0.374	0.034	0.212	0.082	1.505	0.029			
P33	0.611	0.03	0.361	0.02	1.09	0.016			
P34	0.569	0.976	1.8	0.114	0.724	0.199	0.098	0.081	
P35	0.423	0.927	0.28	0.03	0.591	1.17	0.24		
P36	0.492	0.872	0.252	0.207	0.572	0.06		0.153	
P37	0.394	0.933	0.201	0.092	0.861	0.045	0.178		
P38	0.979	1.13	0.264	0.131	0.935	0.092	0.035		
P39	0.992	1.47	0.576	0.15	0.994	0.053	0.029		
P40	0.61	0.064	1.82	0.136	0.686	0.036			
P41	0.35	0.92	0.196	0.028	0.54	0.021	0.16	0.006	
P42	0.118	16.14	0.48	0.132	0.149	1.71	0.048	0.024	
P43	0.586	0.163	1.75	0.06	0.685	0.076		0.026	
P44	0.987	0.075	0.236	0.139	0.226	0.045	0.016	0.0017	
P45	0.72	4.09	0.3	0.107	0.227	0.074	0.076	1.12	
P46	1.03	0.063	0.176	0.122	1.63	0.324		0.031	
P47	0	0	0	0	0	0	0	0	
P48	0.21		0.25	0.11	0.54				
P49	0.21		0.25	0.11	0.54				
P50	0.79	0.1	0.23	0.065	0.21	0.073			
P51	0.42	0.92	0.3		0.62				
P52	0.4	1.46	0.34		0.45		0.2		
P53	0.3	0.77	0.29		0.49	2.24	0.25	0.19	
P54	0.58		1.66		0.74				
P55	0.97	1.02	0.23		0.91				
P56	0.38	2.38						0.33	
P57		4.14					4.77	2.07	
P58		3.88						1.13	
P59	0.2	13.08							
P60	0	0	0	0	0	0	0	0	
P61	0.376	1	0.283	0.096	0.534	0.11	0.197		
P62	0.11	0.059	0.342	0.025	1.43	0.017	0.033	0.016	
P63	0.214	0.083	0.238	0.024	0.42	0.011			
P64	0.657	0.13	0.212	0.022	1	0.01	0.0076	0.0017	
P65	0.157	0.026	0.314	0.012	1.41	0.0068	0.0008	0.0049	
P66	0.379	5.14	1.03	0.097	0.292	0.152	1.24	0.844	
P67	0.164	0.98	0.222	0.04	0.54	0.045	0.472	0.0067	
P68	0.121	1.06	0.28	0.065	0.396	0.12	0.31	0.204	
P69	0.04	18.21	0.452	0.023	1.02	8.05	0.024	0.072	
P70	0.103	8.67	0.293	0.073	0.386	0.081	0.908	0.191	
P71	0.111	2.09	0.388	0.062	0.471	0.04	0.981		
P72	0.103	0.56	0.3	0.032	0.604	0.018	0.311	0.223	
P73	0.165	0.111	0.275	0.033	1.48	0.096	0.056	0.078	
P74	0.053	24.5	0.569	0.197	1.06	19.33	0.133	0.061	
P75	0.021	17.19	0.51	0.34	1.87	8.24	0.069	0.096	
P76	0.176	0.45	0.083	0.086	1.25	0.107	0.563	0.434	
P77	0.207	14.27	0.472	0.077	0.594	0.867	0.026	0.021	
P78	0.178	0.144	0.247	0.11	1.37	0.126	0.006	0.0017	
P79	0.82	4.03	0.41	0.098	0.23	0.108	2.64	1.39	
P80	0.134	0.979	0.239	0.074	0.5	0.046	0.444		
P81	0.111	2.09	0.388	0.062	0.471	0.04	0.981		
P82	0.05	17.93	0.484	0.165	1.12	9.66	0.245	0.099	
P83	0.142	1.2	0.666	0.152	0.49	0.129	0.47	0.004	
P84	0.107	8.22	0.327	0.115	0.333	0.123	0.9	0.236	

Table S2 Number of samples containing or missing an element
Element	Present in samples	Missing or not reported	
Cr	79	5	
Si	78	6	
Cu	73	11	
Mn	78	6	
Ni	71	13	
Mo	55	29	
V	45	39