Electronic Supplementary Information

Face-centered cubic MoS2: A novel superconducting three-dimensional crystal more stable than layered T-MoS2

Peng-Fei Liu,a,b and Bao-Tian Wanga,b*

aInstitute of High Energy Physics, Chinese Academy of Sciences (CAS), Beijing 100049, China.

bDongguan Neutron Science Center, Dongguan 523803, China.

FIG. S1. Schematic of the crystal structures for (a) graphite, (b) diamond, (c) T-MoS2, and (d) FCC-MoS2. The octahedrons of [MoS6] in FCC-MoS2 are emphasized by red and blue colors for the adjacent layers.

FIG. S2. Schematic of the structures for FCC-MoS2 in the primitive lattice.

FIG. S3. The Calculated orientation-dependent 3D elastic properties for FCC-MoS2. (a) Young’s modulus (GPa). (b) Maximum and (c) minimum Shear modulus (GPa). (d) Linear compressibility (TPa-1). (e) Maximum and (f) minimum Poisson’s ratio.

FIG. S4. The ﬁrst Brillouin zone with high-symmetry points indicated.

FIG. S5. The Fermi surfaces of FCC-MoS2. The colors in this figure are meaningless.

FIG. S6. Evaluated superconducting transition temperature Tc of FCC-MoS2 as a function of Coulomb pseudopotential μ∗. Vertical line marks the value μ∗ = 0.10 used in this work.

Table S1. Variations of the elastic moduli of cubic MoS2

| Young's modulus (GPa) |  | Linear compressibility (TPa–1) |  | Shear modulus (GPa) |  | Poisson's ratio |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Emin | Emax | βmin | βmax | Gmin | Gmax | νmin | νmax |
| 103.63 | 154.11 | 2.6147 | 2.6147 | 37.974 | 59.339 | 0.15757 | 0.48323 |