PCL-DOX Macro drops: Evaluation of enhanced intracellular delivery of doxorubicin in metastatic cancer cells by in-silico and in-vitro approach

Aman Chandra Kaushik1#, Ajay Kumar2,3#, Chun-Yen Yu4#, Shiao-Wei Kuo5 , Shih-Shin Liang6, ,Satya P Singh7, Xiangeng Wang1, Yan-Jing Wang1, Chung-Kun Yen3, Xiaofeng Dai9, Dong-Qing Wei1*, Cheng-Tang Pan3,8*, Yow-Ling Shiue2*

Equal contribution-#

Corresponding Author-*

1College of Life Sciences and Biotechnology, The State Key Laboratory of Microbial Metabolism, Shanghai Jio Tong University, Shanghai, China, 200240

2Institute of Biomedical Sciences, National Sun Yat-Sen University, Kaohsiung City, 804, Taiwan

3Department of Mechanical and Electro-Mechanical Engineering, National Sun Yat-sen University, Kaohsiung City 804, Taiwan

4From the Liver Transplantation Program and Departments of Diagnostic Radiology, Kaohsiung Chang Gung Memorial Hospital and Chang Gung University College of Medicine, Kaohsiung, Taiwan

5Department of Materials and Optoelectronic Science, National Sun Yat-Sen University, Kaohsiung 80424, Taiwan

6Department of Biotechnology, College of Life Science, Kaohsiung Medical, University, Kaohsiung, Taiwan

7 School of Electrical and Electronic Engineering, Nanyang Technological University, Singapore

8Institute of Medical Science and Technology, National Sun Yat-Sen University, Kaohsiung City 804, Taiwan

9Wuxi School of Medicine, Jiangnan University, Wuxi, China

Figure S1: The syringe with a built-in stirring component to create an even W1/O emulsion: a stirring component was equipped inside the syringe to avoid uneven dispersion of W1/O emulsion; W1: Dox, Oil: PCL, W2: PVA. Schematic of atomization of W1/O emulsion droplets. (B) Dox original powder, of which particle size was ~ 5-20 µm observed by Scanning electron microscope (SEM).

Figure S2: Schematic of W1/O/W2, the solvent EA and Dox solution diffused into the PVA solution, by which DLPM were fabricated with some drug crystallizations.  W1: Dox, O: PCL, W2: PVA.

(a) Storage of DLPM dry powder, avoiding degradation by hydrolysis;

(b) View of DLPM by OM, uneven EE and aggregation of DLPM were observed;

(c) Matrix structure of DLPM with Dox crystallization and rough surface.

Figure S3: Fluorescence reaction of DLPM: the spectrum of Dox was corresponded with UV light of 100-400 nm wavelength.

Figure S4: A indicates different histogram represent MD simulation (RMSD) analysis for the Polycaprolactone and Doxorubicin hydrochloride compounds in 10ns time for 5 clusters. X-axis represent the RMSD in nanosecond (50 ns) and Y-axis represents the Frequency while B indicates different histogram represent MD simulation (Radius of Gyration) analysis for the Polycaprolactone and Doxorubicin hydrochloride compounds in 10ns time for 5 clusters. X-axis represent the Radius of gyration and Y-axis represents the Frequency and C indicates different histogram represent MD simulation (H-Bond) analysis for the Polycaprolactone and Doxorubicin hydrochloride compounds in 10ns time for 5 clusters. X-axis represents the H-Bond and Y-axis represents the Frequency.

Figure S5: Correlation coefficient heat map representation of radius of gyration and RMSD analysis for the Polycaprolactone and Doxorubicin hydrochloride compounds in 10ns time for 5 clusters where red indicate RMSD and blue indicate radius of gyration during 50ns simulations.

Figure S6: Representation of Stochastic simulation of the entire pathway in presence of polycaprolactone interaction with Doxorubicin hydrochloride.

Table S1: DLE under different HLB of surfactant

| Formulation (W1/O/W2) | Value |
| --- | --- |
| DLE | 38.2-42.2% |
| EE (5-30 µm) | 3.21% |
| EE (30-50 µm) | 1.54% |
| EE (50-100 µm) | 0.97% |
| EE (100-200 µm) | 0.97% |
| EE (200-500 µm) | 0.5% |