Supplementary Data

The static magnetic susceptibility of a powdered sample of Mn2(OH)2(C4O4) was measured in an applied field of 100 G in the range 2 to 300 K.  The data can be found in table S1 and the magnetisation as a function of temperature in Fig. 1 of the printed communication.  The paramagnetic susceptibility para was calculated by subtracting the diamagnetic component, dia, which was calculated from Pascal's constants to be -71.8 × 10-6 
cm3 mol-1.

Table S1

Temperature	Temperature	Magnetisation	SD of	para/	para-1/
	stability		magnetisation		
/K	/K	/G cm3 mol-1	/G cm3 mol-1	cm3 mol-1	mol cm-3

2	0	11.33788	8.5932E-4	0.11345	8.81441
2.5	0	11.35907	4.8439E-4	0.11366	8.79797
3	0	11.39447	1.9096E-3	0.11402	8.77066
3.5	0	11.43825	8.2904E-4	0.11445	8.73711
4	0.01	11.48809	2.2869E-3	0.11495	8.69923
4.77	0.32	11.58147	1.5719E-2	0.11589	8.62913
4.98	0.03	11.60639	7.7315E-4	0.11614	8.61062
5.5	0.03	11.66973	9.3617E-4	0.11677	8.56391
5.99	0.03	11.73331	5.985E-4	0.1174	8.51753
6.49	0.03	11.79851	1.7047E-3	0.11806	8.47049
6.98	0.05	11.86325	2.7712E-3	0.1187	8.42429
7.49	0.05	11.92939	2.3754E-3	0.11937	8.37761
7.98	0.06	11.99367	2.3986E-3	0.12001	8.33275
8.49	0.05	12.05957	2.3241E-3	0.12067	8.28724
8.99	0.05	12.12384	1.7908E-3	0.12131	8.24333
9.48	0.06	12.18858	2.033E-3	0.12196	8.19957
9.99	0.05	12.25449	2.4452E-3	0.12262	8.1555
10.99	0.04	12.39352	1.863E-3	0.12401	8.06406
12	0.02	12.56189	1.204E-3	0.12569	7.95604
13	0.02	12.7249	1.1062E-3	0.12732	7.85418
14.01	0.01	12.78219	1.1318E-3	0.12789	7.81899
15.01	0.01	12.81805	8.1507E-4	0.12825	7.79713
16.02	0.01	12.83435	1.0899E-3	0.12842	7.78723
17.04	0.01	12.8297	7.5918E-4	0.12837	7.79006
18.04	0	12.80408	1.1318E-3	0.12811	7.80563
19.02	0.01	12.75913	1.558E-3	0.12766	7.83311
20.05	0.02	12.69137	1.7233E-3	0.12699	7.87492
21.04	0.03	12.60567	1.8723E-3	0.12613	7.92842
22.05	0.03	12.49575	2.4452E-3	0.12503	7.99813
23.04	0.04	12.36697	2.7247E-3	0.12374	8.08136
24.04	0.04	12.21863	3.4233E-3	0.12226	8.17942
25.04	0.05	12.04327	5.0302E-3	0.1205	8.29845
26.04	0.05	11.8586	5.5891E-3	0.11866	8.4276
27.04	0.06	11.62805	6.9863E-3	0.11635	8.59459
28.04	0.04	11.3465	5.3329E-3	0.11354	8.80772
29.04	0.06	11.00976	1.0293E-2	0.11017	9.07693
30.03	0.05	10.59151	1.1597E-2	0.10599	9.43513
32.05	0.07	9.29811	2.6082E-2	0.09305	10.74658
34.06	0.06	7.72642	2.4219E-2	0.07734	12.9306
36.07	0.07	7.42577	3.0507E-3	0.07433	13.45361
38.06	0.04	7.2765	2.0307E-3	0.07284	13.72933
40.01	0.02	7.12559	4.1219E-4	0.07133	14.0198
42.02	0.03	6.9854	1.1877E-3	0.06993	14.30088
44	0.03	6.77627	1.5556E-3	0.06783	14.74175
46.01	0.04	6.66449	7.3589E-4	0.06672	14.98874
48	0.06	6.56133	1.3786E-3	0.06569	15.22416
50.01	0.14	6.45467	7.8014E-4	0.06462	15.47544
53.97	0.11	6.25766	1.8188E-3	0.06265	15.96211
57.96	0.15	6.06786	9.9672E-4	0.06075	16.4608
61.96	0.25	5.89204	1.2319E-3	0.05899	16.9514
65.96	0.29	5.71901	1.3367E-3	0.05726	17.46362
69.95	0.37	5.55227	8.1973E-4	0.05559	17.98739
73.96	0.44	5.39508	7.2425E-4	0.05402	18.51078
78	0.5	5.24324	9.7576E-4	0.0525	19.04609
82.01	0.57	5.0956	1.2319E-3	0.05103	19.59718
86.04	0.64	4.95284	7.0096E-4	0.0496	20.1612
90.13	0.68	4.81614	2.2892E-4	0.04823	20.73259
94.16	0.7	4.68899	7.0329E-4	0.04696	21.29394
98.2	0.72	4.56766	2.5849E-4	0.04575	21.85868
102.29	0.74	4.44866	5.5192E-4	0.04456	22.44245
106.33	0.74	4.33618	9.5713E-4	0.04343	23.02364
109.83	0.18	4.23209	1.1411E-3	0.04239	23.58899
118.2	0.86	3.87928	2.0447E-1	0.03886	25.73038
126.29	0.91	3.86158	1.027E-3	0.03869	25.84809
134.39	0.98	3.70206	5.7055E-4	0.03709	26.95973
142.47	0.96	3.56093	9.6877E-4	0.03568	28.02602
150.46	0.89	3.4233	8.9658E-4	0.0343	29.15042
158.51	0.91	3.28707	8.1507E-4	0.03294	30.35594
166.58	0.95	3.15712	4.7507E-4	0.03164	31.60254
174.71	0.94	3.04092	1.7489E-3	0.03048	32.80736
182.71	1	2.93472	7.3822E-4	0.02942	33.99159
190.79	0.99	2.83296	1.1038E-3	0.0284	35.20957
198.91	0.94	2.73818	8.1274E-4	0.02745	36.42515
206.92	1.01	2.65131	8.5466E-4	0.02658	37.61531
215.01	0.99	2.56887	9.4548E-4	0.02576	38.81907
223.1	0.99	2.49179	1.1923E-3	0.02499	40.01647
231.19	0.99	2.42076	9.5247E-3	0.02428	41.18712
238.08	0.95	2.35346	4.1685E-3	0.02361	42.36136
247.35	1.02	2.287	9.874E-4	0.02294	43.58859
255.63	0.87	2.22312	3.0041E-3	0.0223	44.83702
263.72	0.54	2.16378	4.6343E-3	0.02171	46.06251
271.59	1.05	2.10906	1.8654E-3	0.02116	47.2537
279.48	0.89	2.05834	3.7959E-3	0.02066	48.41406
287.48	0.96	2.00713	4.5178E-3	0.02014	49.64489
295.42	1.06	1.96178	4.8904E-3	0.01969	50.78811

# Table S2 Crystal data obtained at various temperatures

| Parameter | 10 K | 20 K | 45 K | 120 K | Room Temp. |
| --- | --- | --- | --- | --- | --- |
| a, Å | 3.3760(7) | 3.3770(7) | 3.3770(7) | 3.381(1) | 3.396(1) |
| b, Å | 10.268(2) | 10.268(2) | 10.269(2) | 10.268(5) | 10.270(1) |
| c, Å | 8.575(2) | 8.576(2) | 8.573(2) | 8.579(4) | 8.601(1) |
| , ° | 99.82(3) | 99.81 (3) | 99.80(3) | 99.85(3) | 99.95(1) |
| U, Å3 | 292.9(1) | 293.0(1) | 293.0(1) | 293.4(1) | 295.5(1) |
| Space group | Monoclinic, P21/c , Z = 2 |  |  |  |  |
| Dc, g cm-1 | 2.902 | 2.902 | 2.902 | 2.897 | 2.868 |
| Data/parameters | 2588/60 | 504/60 | 504/60 | 504/60 |  |
| Residual density | 0.651/-0.806 | 0.301/-0.230 | 0.399/-0.219 | 0.417/-0.471 |  |
| Theta max, ° | 47.51 | 25.00 | 25.00 | 25.00 |  |
| R (I  2) | 0.0234 | 0.0138 | 0.0144 | 0.0189 |  |
| GOF | 1.026 | 1.052 | 1.093 | 1.048 |  |