Neutron powder and ab initio structure of ortho xylene:  the influence of crystal packing on phenyl ring geometry at 2 K

Richard M. Ibberson,a Carole Morrisonb and Michael Prager.c

- ISIS Facility, CCLRC - Rutherford Appleton Laboratory, Chilton, Didcot, Oxfordshire, OX11 0QX, UK

- Department of Chemistry, The University of Edinburgh, King’s Buildings, West Mains Road, Edinburgh, EH9 3JJ, UK.

- Institut für Festköperforschung, Forschungszentrum Jülich, 52425 Jülich, Germany.

Supplementary information

Table A1 – Refined structural co-ordinates for o-xylene-d10 at 2 K.

Table A2 - Anisotropic displacement parameters (Å2 x 103) for o-xylene at 2 K.

Table A3 – Intramolecular distances (Å) and angles (º) for o-xylene-d10 at 2 K.

Table A4 – Comparison of intramolecular distances (Å) and angles (º) for 
o-xylene determined by ab initio calculation and from neutron powder diffraction (present study).

Table A1 – Refined structural co-ordinatesa for o-xylene-d10 at 2 K.

Space group: P21/a (No. 14)

Lattice constants: a = 12.51135(5) Å; b = 6.071416(23) Å;  c = 8.815672(35) Å; 
 =  108.6847(4) ; Vc =  634.3591(46)Å3.

| Atom | x/a | y/b | z/c | bUiso*100 |
| --- | --- | --- | --- | --- |
| C(1) | 0.85584(20) | 0.0294(4) | 0.25904(29) | 0.47(7) |
| C(2) | 0.73494(22) | 0.0346(4) | 0.20270(29) | 0.90(7) |
| C(3) | 0.67816(22) | 0.1967(4) | 0.25842(30) | 0.93(7) |
| C(4) | 0.73681(19) | 0.3524(5) | 0.36924(30) | 0.99(7) |
| C(5) | 0.85521(20) | 0.3502(4) | 0.42491(30) | 0.69(7) |
| C(6) | 0.91222(23) | 0.1884(4) | 0.36995(29) | 1.15(8) |
| C(1M) | 0.92009(23) | -0.1385(5) | 0.19852(33) | 1.12(7) |
| C(2M) | 0.67222(25) | -0.1354(5) | 0.08124(35) | 0.98(7) |
| D(3) | 0.58623(23) | 0.1972(4) | 0.21287(35) | 2.11* |
| D(4) | 0.69194(22) | 0.4751(4) | 0.41519(32) | 2.01* |
| D(5) | 0.90048(23) | 0.4682(4) | 0.51426(36) | 2.20* |
| D(6) | 1.00384(23) | 0.1865(5) | 0.41440(36) | 2.50* |
| D(11) | 1.01087(24) | -0.1127(4) | 0.25109(36) | 2.59* |
| D(12) | 0.89980(26) | -0.3069(5) | 0.22787(38) | 2.89* |
| D(13) | 0.89891(27) | -0.1282(5) | 0.06964(34) | 2.77* |
| D(21) | 0.68948(26) | -0.1253(5) | -0.02813(37) | 2.89* |
| D(22) | 0.58288(22) | -0.1151(5) | 0.05319(37) | 2.36* |
| D(23) | 0.69333(26) | -0.3039(4) | 0.12611(32) | 2.66* |

a Estimated standard deviations in parentheses.

b * denotes Ueq values which are one third of the trace of the diagonalized matrix.

Table A2 - Anisotropic displacement parameters (Å2 x 103) for o-xylene at 2 K.  The anisotropic displacement factor exponent takes the form: -2 2 [ h2 a*2 U11 + ... + 2 h k a* b* U12 ]

| Atom | U11 | U22 | U33 | U12 | U13 | U23 |
| --- | --- | --- | --- | --- | --- | --- |
| D(3) | 1.28(16) | 0.95(16) | 3.73(20) | 0.28(11) | 0.41(14) | -0.25(13) |
| D(4) | 1.81(15) | 2.24(16) | 2.50(17) | 0.02(14) | 1.35(13) | -1.09(13) |
| D(5) | 2.07(15) | 0.81(14) | 3.44(18) | 0.28(13) | 0.44(14) | -0.07(14) |
| D(6) | 0.84(16) | 2.64(21) | 3.58(19) | -0.14(13) | 0.27(13) | -0.62(14) |
| D(11) | 1.42(17) | 1.51(15) | 3.97(20) | 0.12(12) | -0.27(16) | -1.20(14) |
| D(12) | 3.22(17) | 1.40(18) | 4.74(21) | 0.25(14) | 2.16(16) | 0.30(14) |
| D(13) | 3.87(19) | 2.09(15) | 2.48(20) | 1.67(15) | 0.79(15) | -0.61(14) |
| D(21) | 3.60(20) | 3.02(18) | 2.40(19) | -0.47(16) | 1.07(16) | -0.93(15) |
| D(22) | 0.44(14) | 2.53(17) | 3.44(20) | 0.12(12) | -0.13(13) | -0.55(14) |
| D(23) | 4.28(19) | 0.13(14) | 2.66(18) | -0.30(13) | -0.66(15) | 0.38(13) |

Table A3 – Intramolecular distancesa (Å) and anglesa (º) for o-xylene-d10 at 2 K.  (The atomic labelling scheme is shown in Fig 1.)

| C(1)-C(2) | 1.4333(33) | C(3)-D(3) | 1.0900(35) |
| --- | --- | --- | --- |
| C(2)-C(3) | 1.3920(35) | C(4)-D(4) | 1.0864(30) |
| C(3)-C(4) | 1.388(4) | C(5)-D(5) | 1.0811(31) |
| C(4)-C(5) | 1.4033(33) | C(6)-D(6) | 1.0862(32) |
| C(5)-C(6) | 1.3894(33) | C(1M)-D(11) | 1.0917(34) |
| C(6)-C(1) | 1.3942(35) | C(1M)-D(12) | 1.1039(34) |
| C(1)-C(1M) | 1.498(4) | C(1M)-D(13) | 1.0827(30) |
| C(2)-C(2M) | 1.5133(35) | C(2M)-D(21) | 1.0551(33) |
|  |  | C(2M)-D(22) | 1.072(4) |
|  |  | C(2M)-D(23) | 1.0980(34) |
| C(1)-C(2)-C(2M) | 118.72(23) | C(4)-C(5)-C(6) | 119.13(27) |
| C(1)-C(2)-C(3) | 119.64(21) | C(4)-C(5)-D(5) | 119.78(28) |
| C(2M)-C(2)-C(3) | 121.63(23) | D(5)-C(5)-C(6) | 121.00(27) |
| C(2)-C(3)-C(4) | 121.01(23) | C(5)-C(6)-C(1) | 122.23(24) |
| C(2)-C(3)-D(3) | 118.01(27) | C(5)-C(6)-D(6) | 118.81(26) |
| D(3)-C(3)-C(4) | 120.98(27) | D(6)-C(6)-C(1) | 118.96(27) |
| C(3)-C(4)-C(5) | 120.04(26) | C(6)-C(1)-C(2) | 117.93(21) |
| C(3)-C(4)-D(4) | 120.64(26) | C(2)-C(1)-C(1M) | 121.25(23) |
| D(4)-C(4)-C(5) | 119.31(28) | C(6)-C(1)-C(1M) | 120.81(22) |
| C(1)-C(1M)-D(11) | 110.81(28) | C(2)-C(2M)-D(21) | 113.29(31) |
| C(1)-C(1M)-D(12) | 110.89(27) | C(2)-C(2M)-D(22) | 110.54(32) |
| C(1)-C(1M)-D(13) | 110.82(27) | C(2)-C(2M)-D(23) | 111.74(27) |
| D(11)-C(1M)-D(12) | 108.62(32) | D(21)-C(2M)-D(22) | 106.6(4) |
| D(11)-C(1M)-D(13) | 107.98(35) | D(21)-C(2M)-D(23) | 106.69(34) |
| D(12)-C(1M)-D(13) | 107.59(33) | D(22)-C(2M)-D(23) | 107.6(4) |

a Estimated standard deviations in parentheses.

Table A4 – Comparison of intramolecular distances (Å) and angles (º) for 
o-xylene determined by ab initio calculation and from neutron powder diffraction (present study).

| Parameter | HF/3-21G* | HF/6-31G* | MP2/6-31G* | MP2/6-311G* | NPD (2 K) |
| --- | --- | --- | --- | --- | --- |
| Bond lengths |  |  |  |  |  |
| rC1-C2 | 1.3967 | 1.4008 | 1.41 | 1.4117 | 1.4334(33) |
| rC2-C3 | 1.3859 | 1.3876 | 1.3992 | 1.4021 | 1.3919(35) |
| rC6-C1 | " | " | " | " | 1.3941(35) |
| rC3-C4 | 1.3842 | 1.3863 | 1.396 | 1.3978 | 1.388(4) |
| rC5-C6 | " | " | " | " | 1.3894(33) |
| rC4-C5 | 1.3806 | 1.3811 | 1.3941 | 1.3969 | 1.4032(33) |
| rC2-C2m | 1.5172 | 1.512 | 1.5065 | 1.5078 | 1.5133(35) |
| rC1-C1m | " | " | " | " | 1.498(4) |
| rC3-D3 | 1.073 | 1.0763 | 1.089 | 1.0889 | 1.0900(35) |
| rC6-D6 | " | " | " | " | 1.0862(23) |
| rC4-D4 | 1.0721 | 1.0755 | 1.0875 | 1.0874 | 1.0865(30) |
| rC5-D5 | " | " | " | " | 1.0811(30) |
| rC1m-D11 | 1.0853 | 1.0864 | 1.0956 | 1.095 | 1.0917(34) |
| rC2m-D21 | " | " | " | " | 1.0550(33) |
| rC1m-D12 | 1.0827 | 1.0835 | 1.0933 | 1.0925 | 1.1040(34) |
| rC2m-D22 | " | " | " | " | 1.072(4) |
| rC1m-D13 | 1.0853 | 1.0864 | 1.0956 | 1.095 | 1.0828(30) |
| rC2m-D23 | " | " | " | " | 1.0980(34) |
| Angles |  |  |  |  |  |
| <C1-C2-C3 | 119.19 | 119.01 | 119.12 | 119.11 | 119.64(21) |
| <C2-C1-C6 | " | " | " | " | 117.93(21) |
| <C2-C3-C4 | 121.2 | 121.47 | 121.31 | 121.33 | 121.01(23) |
| <C1-C6-C5 | " | " | " | " | 122.23(24) |
| <C3-C4-C5 | 119.61 | 119.51 | 119.57 | 119.56 | 120.04(26) |
| <C4-C5-C6 | " | " | " | " | 119.13(27) |
| <C3-C2-C2m | 120.22 | 120.04 | 120.32 | 120.38 | 121.63(23) |
| <C6-C1-C1m | " | " | " | " | 120.81(22) |
| <C1-C2-C2m | 120.59 | 120.94 | 120.56 | 120.51 | 118.73(23) |
| <C2-C1-C1m | " | " | " | " | 121.23(23) |
| <C2-C2m-D21 | 111.05 | 111.61 | 111.53 | 111.47 | 113.29(31) |
| <C1-C1m-D11 | " | " | " | " | 110.82(28) |
| <C2-C2m-D22 | 110.7 | 110.95 | 110.7 | 110.88 | 110.54(32) |
| <C1-C1m-D12 | " | " | " | " | 110.90(27) |
| <C2-C2m-D23 | 111.05 | 111.61 | 111.53 | 111.47 | 111.74(27) |
| <C1-C1m-D13 | " | " | " | " | 110.83(27) |
| <C2-C3-D3 | 119.22 | 119.18 | 119.11 | 119.12 | 118.02(27) |
| <C1-C6-D6 | " | " | " | " | 118.96(27) |
| <C3-C4-D4 | 120.01 | 120.01 | 120.04 | 120.05 | 120.63(26) |
| <C6-C5-D5 | " | " | " | " | 121.01(27) |
| <C4-C3-D3 | 119.58 | 119.35 | 119.58 | 119.54 | 120.97(27) |
| <C5-C6-D6 | " | " | " | " | 118.81(26) |
| <C5-C4-D4 | 120.38 | 120.48 | 120.39 | 120.39 | 119.32(28) |
| <C4-C5-D5 | " | " | " | " | 119.77(28) |
| Energy | -307.06049 | -308.77622 | -309.79946 | -309.903967 |  |