Supplementary information

1.  Polymer synthesis.  1 - 3 were synthesized according to the normal Wurtz coupling technique for polysilanes.  The synthesis of 1 is representative:  poly[{bis-3-(S)-2-methylbutylphenyl}0.2-co-(bis-4-butylphenyl)0.8]silylene, 1, was prepared by addition of a mixture of the comonomers, dichloro-bis[3-(S)-2-methylbutylphenyl]silaneS1 (0.2 equivs.) and dichloro-bis(4-butylphenyl)silane (0.8 equivs.), to a flask containing 2.5 equivalents of sodium dispersed in toluene with stirring at 70C.  After 2.5 hours, the viscous purple mixture was diluted with toluene and filtered through a 10m Teflon filter.  The high molecular weight (Mw) fraction (Mw = 474,000; yield 5.9%) was isolated by centrifugation after fractional precipitation in a mixed isopropanol-toluene solution and vacuum dried at 80C for 24 hours.

2.  Table of fluorescence excitation and NMRS2 data for 1 - 3.

| Cmpd | FL-EX max /nm | NMR  (ppm) |  |
| --- | --- | --- | --- |
|  |  | 29Si | 13C |
| 1 | 398.5 | -31.4 | 11.5, 14.3, 19.2, 22.8, 29.8, 34.1, 36.2, 36.7, 43.8 |
| 2 | 400.5 | -32.9 | 11.5, 14.2, 19.1, 22.8, 29.7, 33.9, 36.1, 36.7, 43.7 |
| 3 | 396.0 | -34.4 | 11.5, 14.0, 19.2, 22.8, 29.7, 33.7, 36.2, 36.7, 43.8 |

References

S1  J. R. Koe, M. Fujiki and H. Nakashima, J. Am. Chem. Soc., 1999, 121, 9734.

S2  NMR spectra were recorded on a Varian  Unity 300 spectrometer at 80C relative to internal TMS in toluene-d8 for silicon-29 at 59.591 MHz and for carbon-13 at 75.431 MHz for low Mw fractions of 1 and 3, and for the high Mw fraction of 2.  Peak integrations indicate correlation of copolymer compositions and nominal addition ratios.