Fig. S1  Normalised optical absorption, photoluminescence (PL) and electroluminescence (EL) spectra of BDMOS-DB-PPV.  PL and absorption spectra were measured on spin-coated films on quartz.  EL spectra are for devices in the configuration ITO/PEDOT (80 nm) /BDMOS-DB-PPV (80 nm)/Ca devices.

Fig. S2  Cyclic voltammograms of BDMOS-DB-PPV were measured as thin films on Pt disk electrodes in MeCN using n-Bu4NClO4 (0.10 mol l-1) as conducting electrolyte at room temp. (scan rate: 100 mV s-1).  Ag/AgCl was used as a reference electrode, which was referenced against Fc/Fc+ (+0.43 V).  The right hand CV is for oxidation, whereas the left hand is for reduction.