Figure 1	Effect of adding ZnCl2 on EuL2 (upper, 0.1 mM) and TbL2 (0.08 mM) absorption spectra (295K, 10 mM HEPES, 20 mM NaCl, 115 mM KCl, pH 7.4).

Figure 2	Iterative least-square fitting to a 1:1 model of Zn(II)-TbL2 complex. Inset: Hill plot analysis of the dependence of TbL2 absorption (max = 240 nm) as a function of pZn2+ at pH 7.4.

LogML = 5.30

logML = 5.48

Figure 3	Upper: Effect of Zn2+ ions on the intensity of terbium luminescence ([TbL2]=0.08 mM; exc 262 nm, 295 K, 10 mM HEPES, 20 mM NaCl, 115 mM KCl, pH 7.4; spectra were acquired using Fluorolog3-11 spectrofluorimeter). Lower: Hill plot analysis of the enhancement terbium emission (em = 545 nm) in TbL2+ upon addition of Zn2+ (logML=6.35).