Chem Comm b005327i

Gold Nanoparticles from Self-assembled Gold(I) Amine Precursors

Silvia Gomeza, Karine Philippota, Vincent Collièrea, Bruno Chaudret*a, François Senocqb, Pierre Lecantec

aLaboratoire de Chimie de Coordination du CNRS, 205, route de Narbonne, 31077 Toulouse Cédex 04, France.

bCIRIMAT, UMR CNRS 5085, E.N.S.C.T., 118, route de Narbonne, 31077 Toulouse Cédex 04, France.

cCentre d’Elaboration des Matériaux et d’Etudes Structurales du CNRS, 29, rue Jeanne Marvig BP 4347, 31055 Toulouse Cédex 04, France.

##### Supplementary Material

Experimental details and characterization of complexes 2-4.

All the reactions were carried out under an argon atmosphere using classical schlenk techniques.

WAXS Study: Samples 2, 3 and 4 were sealed in a Lindeman capillary. The scattering spectrum produced by the sample irradiated with graphite-monochromatized silver K radiation ( = 0,56083 Å) was obtained using a dedicated diffractometer. The experimental reduced radial distribution function (RDF), which shows the distribution of the interatomic distances, was calculated for each case.

TEM Study: The morphologies of 2, 3 and 4 were studied on a JEOL 200 CX-T electron microscope operating at 200 kV. The powder was dissolved, or suspended, in THF and the resulting solution was poured onto a copper grid covered by a thin carbon film.

TGA Study: The temperatures were controlled from 20 to 800°C at 20°C/min. and the experiments were carried out under an helium atmosphere.

XRD Studies : XRD diagrams were collected with a Seifert XRD 3000 TT diffractometer, using Cu K ( radiation, fitted with a back graphite monochromator.

## Evolution vs. temperature: The sample was introduced in a glass tube connected to a mercury diffusion vacuum pump and evacuated. The tube was then heated with a regulated oil bath for periods of 1 hour at the requested temperature and allowed to cool to room temperature under dynamic vacuum (( 10-4 Torr). XRD diagrams were then collected, the sample re-introduced in the glass tube and heated to the next temperature, following the same procedure, until complete evolution.

Selected data for 2: IR (KBr/cm-1): 3251 and 3211 ( N-H of coordinated amine), 2951-2848 ( C-H alkyl groups); 1H NMR (298 K, CD3COCD3, 300 MHz):  4.86 (-NH2, 2H), 3.04 (m, -CH2-NH2, 2H), 1.75 (m, CH2-CH2-NH2, 2H), 1.36-1.29 (m, -(CH2)5-(CH2)2-NH2, 10H), 0.88 (t, CH3-, 3H); 13C NMR (298 K, CD3COCD3, 300 MHz):  56.98 (-CH2-NH2), 32.01 (-CH2-CH2-NH2), 30.89 (-CH2-(CH2)2-NH2), 29.50 (-CH2-(CH2)3-NH2), 29.35 (-CH2-(CH2)4-NH2), 26.75 (-CH2-(CH2)5-NH2), 22.79 (-CH2-(CH2)6-NH2), 13.84 (CH3-); TGA : 43 ± 3 % weight loss between 22 and 400°C; expected : 45.5 % corresponding to successive loss of Cl and amine ligands ; Elemental analysis: Calcd. for C8H19NClAu: C, 26.56; H, 5.25; N, 3.87; Cl, 9.81. Found: C, 26.59; H, 4.79; N, 3.86; Cl, 9.79.

For 3: IR (KBr/ cm-1): 3247 and 3213 ( N-H of coordinated amine), 2954-2848 ( C-H alkyl groups); 1H NMR (298 K, THF-d8, 300 MHz):  4.76 (-NH2, 2H), 2.93 (m, -CH2-NH2, 2H), 1.69 (m, CH2-CH2-NH2, 2H), 1.37-1.32 (m, -(CH2)9-(CH2)2-NH2, 18H), 0.92 (t, CH3-, 3H); 13C NMR (298 K, THF-d8, 300 MHz):  47.33 (-CH2-NH2), 32.57 (-CH2-CH2-NH2), 32.29 (-CH2-(CH2)2-NH2), 30.02-29.72 (-(CH2)6-(CH2)3-NH2), 26.79 (-CH2-(CH2)9-NH2), 22.98 (-CH2-(CH2)10-NH2), 13.85 (CH3-); TGA : 51 ± 3 % weight loss between 22 and 500°C; expected : 52.8 % corresponding to loss of Cl and amine ligands ; Elemental analysis: Calcd. for C12H27NClAu: C, 34.49; H, 6.47; N, 3.35; Cl, 8.49. Found: C, 34.50; H, 6.44; N, 3.25; Cl, 8.47.

For 4: IR (KBr/ cm-1): 3245 and 3212 ( N-H of coordinated amine), 2952-2848 ( C-H alkyl groups); 1H NMR (298 K, THF-d8, 300 MHz):  4.76 (-NH2, 2H), 2.93 (m, -CH2-NH2, 2H), 1.68 (m, CH2-CH2-NH2, 2H), 1.37-1.33 (m, -(CH2)13-(CH2)2-NH2, 26H), 0.92 (t, CH3-, 3H); 13C NMR (298 K, THF-d8, 300 MHz):  47.32 (-CH2-NH2), 32.57 (-CH2-CH2-NH2), 32.28 (-CH2-(CH2)2-NH2), 30.02-29.71 (-(CH2)10-(CH2)3-NH2), 26.78 (-CH2-(CH2)13-NH2), 22.98 (-CH2-(CH2)14-NH2), 13.85 (CH3-); TGA : 60 ± 3 % weight loss between 22 and 600°C; expected : 58.4 % corresponding to loss of Cl and amine ligands ; Elemental analysis: Calcd. for C16H35NClAu: C, 40.55; H, 7.39; N, 2.95; Cl, 7.49. Found: C, 40.33; H, 7.17; N, 2.84; Cl, 6.64.