SUPPLEMENTARY DATA

Direct-space structure solution from laboratory powder diffraction data of an organic cocrystal:  1,2,3-trihydroxybenzene-HMTA (1/1).

M.Tremayne & C.Glidewell

Fractional atomic coordinates and isotropic displacement parameters (Å2) for the refined crystal structure of the 1:1 adduct of 1,2,3-trihydroxybenzene:HMTA.

| Atom | x | y | z | Uiso |
| --- | --- | --- | --- | --- |
| C11 | 0.156(1) | -0.084(2) | 0.150(1) | 0.024(3) |
| C12 | 0.217(1) | 0.061(2) | 0.110(1) | 0.024(3) |
| C13 | 0.347(1) | 0.053(2) | 0.103(1) | 0.024(3) |
| C14 | 0.411(1) | -0.086(2) | 0.149(1) | 0.024(3) |
| C15 | 0.348(1) | -0.225(2) | 0.190(1) | 0.024(3) |
| C16 | 0.220(1) | -0.222(2) | 0.191(1) | 0.024(3) |
| O11 | 0.0315(7) | -0.066(1) | 0.1603(6) | 0.026(2) |
| O12 | 0.1508(7) | 0.196(2) | 0.0648(6) | 0.026(2) |
| O13 | 0.4031(7) | 0.176(1) | 0.0537(6) | 0.026(2) |
| H11 | -0.003 | 0.060 | 0.153 | a |
| H12 | 0.198 | 0.273 | 0.029 | a |
| H13 | 0.488 | 0.199 | 0.070 | a |
| H14 | 0.515(2) | -0.084(10) | 0.150(5) | 0.05 |
| H15 | 0.399(3) | -0.337(10) | 0.222(2) | 0.05 |
| H16 | 0.170(3) | -0.330(10) | 0.225(3) | 0.05 |
| C21 | 0.890(1) | 0.356(2) | 0.0426(7) | 0.032(2) |
| N21 | 0.866(1) | 0.244(2) | 0.1144(7) | 0.033(2) |
| C22 | 0.665(1) | 0.396(2) | 0.0205(6) | 0.032(2) |
| N22 | 0.784(1) | 0.499(2) | 0.0327(7) | 0.033(2) |
| C23 | 0.744(1) | 0.145(1) | 0.1006(8) | 0.032(2) |
| N23 | 0.638(1) | 0.281(2) | 0.0900(7) | 0.033(2) |
| C24 | 0.862(1) | 0.353(2) | 0.1887(6) | 0.032(2) |
| N24 | 0.755(1) | 0.490(2) | 0.1808(6) | 0.033(2) |
| C25 | 0.777(1) | 0.602(1) | 0.1097(8) | 0.032(2) |
| C26 | 0.639(1) | 0.385(2) | 0.1648(7) | 0.032(2) |
| H211 | 0.976(2) | 0.435(5) | 0.053(3) | 0.07 |
| H212 | 0.891(4) | 0.274(5) | -0.011(1) | 0.07 |
| H221 | 0.590(2) | 0.504(5) | 0.017(3) | 0.07 |
| H222 | 0.670(4) | 0.321(6) | -0.036(1) | 0.07 |
| H231 | 0.724(3) | 0.062(5) | 0.154(2) | 0.07 |
| H232 | 0.751(3) | 0.061(5) | 0.047(2) | 0.07 |
| H241 | 0.846(4) | 0.268(5) | 0.242(1) | 0.07 |
| H242 | 0.948(2) | 0.431(5) | 0.199(3) | 0.07 |
| H251 | 0.693(4) | 0.699(6) | 0.104(2) | 0.07 |
| H252 | 0.859(4) | 0.693(6) | 0.118(2) | 0.07 |
| H261 | 0.558(2) | 0.483(5) | 0.164(3) | 0.07 |
| H262 | 0.632(4) | 0.287(5) | 0.216(1) | 0.07 |

a denotes hydroxyl H atoms placed in positions calculated from the coordinates of the hydrogen-bond donor and acceptors.  These atoms were not included in the refinement.

Interatomic bond distances (Å) and angles (º) in the refined crystal structure of the 1:1 adduct of 1,2,3-trihydroxybenzene:HMTA.

| C11—O11 | 1.361(8) |  | C14—H14 | 1.11(2) |
| --- | --- | --- | --- | --- |
| C11—C12 | 1.395(9) |  | C15—H15 | 1.09(2) |
| C11—C16 | 1.363(9) |  | C16—H16 | 1.10(2) |
| C12—O12 | 1.391(8) |  |  |  |
| C12—C13 | 1.410(8) |  |  |  |
| C13—O13 | 1.347(8) |  |  |  |
| C13—C14 | 1.414(9) |  |  |  |
| C14—C15 | 1.384(9) |  |  |  |
| C15—C16 | 1.376(9) |  |  |  |
| C21—N21 | 1.466(9) |  | C21—H211 | 1.09(2) |
| C21—N22 | 1.523(9) |  | C21—H212 | 1.08(2) |
| C22—N22 | 1.477(9) |  | C22—H221 | 1.11(2) |
| C22—N23 | 1.456(9) |  | C22—H222 | 1.09(2) |
| C23—N21 | 1.492(9) |  | C23—H231 | 1.10(2) |
| C23—N23 | 1.498(9) |  | C23—H232 | 1.08(2) |
| C24—N21 | 1.464(9) |  | C24—H241 | 1.09(2) |
| C24—N24 | 1.505(9) |  | C24—H242 | 1.09(2) |
| C25—N22 | 1.481(9) |  | C25—H251 | 1.14(2) |
| C25—N24 | 1.454(10) |  | C25—H252 | 1.09(2) |
| C26—N23 | 1.456(9) |  | C26—H261 | 1.10(2) |
| C26—N24 | 1.463(9) |  | C26—H262 | 1.11(2) |
| O11—C11—C12 | 118(1) |  | C13—C14—H14 | 118(2) |
| O11—C11—C16 | 119(1) |  | C15—C14—H14 | 121(2) |
| C12—C11—C16 | 122(1) |  | C14—C15—H15 | 120(2) |
| O12—C12—C11 | 121(1) |  | C16—C15—H15 | 120(2) |
| O12—C12—C13 | 119(1) |  | C11—C16—H16 | 120(2) |
| C11—C12—C13 | 119(1) |  | C15—C16—H16 | 120(2) |
| O13—C13—C12 | 119(1) |  |  |  |
| O13—C13—C14 | 124(1) |  |  |  |
| C12—C13—C14 | 118(1) |  |  |  |
| C13—C14—C15 | 121(1) |  |  |  |
| C14—C15—C16 | 120(1) |  |  |  |
| C11—C16—C15 | 120(1) |  |  |  |
| N21—C21—N22 | 108(1) |  | N21—C21—H211 | 108(2) |
| C21—N21—C23 | 107(1) |  | N21—C21—H212 | 114(2) |
| C21—N21—C24 | 115(1) |  | N22—C21—H211 | 108(2) |
| C23—N21—C24 | 109(1) |  | N22—C21—H212 | 107(2) |
| N22—C22—N23 | 111(1) |  | H211—C21—H212 | 112(2) |
| C21—N22—C22 | 109(1) |  | N22—C22—H221 | 108(2) |
| C21—N22—C25 | 106(1) |  | N23—C22—H221 | 104(2) |
| C22—N22—C25 | 108(1) |  | N22—C22—H222 | 108(2) |
| N21—C23—N23 | 113(1) |  | N23—C22—H222 | 116(2) |
| C22—N23—C23 | 106(1) |  | H221—C22—H222 | 110(2) |
| C22—N23—C26 | 114(1) |  | N21—C23—H231 | 109(2) |
| C23—N23—C26 | 103(1) |  | N21—C23—H232 | 108(2) |
| N21—C24—N24 | 107(1) |  | N23—C23—H231 | 105(2) |
| C24—N24—C25 | 106(1) |  | N23—C23—H232 | 108(2) |
| C24—N24—C26 | 110(1) |  | H231—C23—H232 | 114(2) |
| C25—N24—C26 | 106(1) |  | N21—C24—H241 | 115(2) |
| N22—C25—N24 | 118(1) |  | N24—C24—H241 | 107(2) |
| N23—C26—N24 | 114(1) |  | N21—C24—H242 | 111(2) |
|  |  |  | N24—C24—H242 | 110(2) |
|  |  |  | H241—C24—H242 | 107(2) |
|  |  |  | N22—C25—H251 | 106(2) |
|  |  |  | N22—C25—H252 | 110(2) |
|  |  |  | N24—C25—H252 | 111(2) |
|  |  |  | N24—C25—H251 | 104(2) |
|  |  |  | H251—C25—H252 | 108(2) |
|  |  |  | N23—C26—H261 | 108(2) |
|  |  |  | N23—C26—H262 | 110(2) |
|  |  |  | N24—C26—H261 | 111(2) |
|  |  |  | N24—C26—H262 | 104(2) |
|  |  |  | H261—C26—H262 | 109(2) |

Selected intermolecular distances (Å) and angles (º) in the refined crystal structure of the 1:1 adduct of 1,2,3-trihydroxybenzene:HMTA.

| D—H…...A | D …...A | D—H…...A |
| --- | --- | --- |
| O11—H11…...N21i | 2.90(1) | 153(1) |
| O12—H12…...N22ii | 2.79(1) | 150(1) |
| O13—H13…...N23iii | 2.69(1) | 169(1) |
| C16—H16…...Cgiv | 3.69(1) | 139(1) |
| C22—H222…...Cgv | 3.64(1) | 165(1) |

Cg denotes the centroid of the trihydroxybenzene ring.

# Symmetry codes

i)	1-x,y,z

ii)	1-x,1-y,-z

iii)	x,y,z

- 0.5-x,-0.5+y,0.5-z

- -x,-y,-z