Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2001


Supplementary Information

Figure S1.

[image: image1.wmf]0

0.2

0.4

0.6

0.8

1

1.2

1.4

200

400

600

800

1000

wavelength (nm)

Abs


Figure S1. UV-vis spectra of silver nanorods: Effect of changing amount of 4 nm seed. (1) = 2.0 mL, (2) = 1.0 mL, (3) = 0.5 mL, (4) = 0.25 mL, (5) = 0.125 mL and (6) = 0.06 mL of seed solution.  See ref 14 for experimental details.  



6





5





4





3





2





1





� EMBED Excel.Sheet.8  ���








1

[image: image2.wmf]0

0.2

0.4

0.6

0.8

1

1.2

1.4

200

400

600

800

1000

wavelength (nm)

Abs

_1040554297.xls
Chart1

		1260		1260		1260		1260		1260		1260

		1259		1259		1259		1259		1259		1259

		1258		1258		1258		1258		1258		1258

		1257		1257		1257		1257		1257		1257

		1256		1256		1256		1256		1256		1256

		1255		1255		1255		1255		1255		1255

		1254		1254		1254		1254		1254		1254

		1253		1253		1253		1253		1253		1253

		1252		1252		1252		1252		1252		1252

		1251		1251		1251		1251		1251		1251

		1250		1250		1250		1250		1250		1250

		1249		1249		1249		1249		1249		1249

		1248		1248		1248		1248		1248		1248

		1247		1247		1247		1247		1247		1247

		1246		1246		1246		1246		1246		1246

		1245		1245		1245		1245		1245		1245

		1244		1244		1244		1244		1244		1244

		1243		1243		1243		1243		1243		1243

		1242		1242		1242		1242		1242		1242

		1241		1241		1241		1241		1241		1241

		1240		1240		1240		1240		1240		1240

		1239		1239		1239		1239		1239		1239

		1238		1238		1238		1238		1238		1238

		1237		1237		1237		1237		1237		1237

		1236		1236		1236		1236		1236		1236

		1235		1235		1235		1235		1235		1235

		1234		1234		1234		1234		1234		1234

		1233		1233		1233		1233		1233		1233

		1232		1232		1232		1232		1232		1232

		1231		1231		1231		1231		1231		1231

		1230		1230		1230		1230		1230		1230

		1229		1229		1229		1229		1229		1229

		1228		1228		1228		1228		1228		1228

		1227		1227		1227		1227		1227		1227

		1226		1226		1226		1226		1226		1226

		1225		1225		1225		1225		1225		1225

		1224		1224		1224		1224		1224		1224

		1223		1223		1223		1223		1223		1223

		1222		1222		1222		1222		1222		1222

		1221		1221		1221		1221		1221		1221

		1220		1220		1220		1220		1220		1220

		1219		1219		1219		1219		1219		1219

		1218		1218		1218		1218		1218		1218

		1217		1217		1217		1217		1217		1217

		1216		1216		1216		1216		1216		1216

		1215		1215		1215		1215		1215		1215

		1214		1214		1214		1214		1214		1214

		1213		1213		1213		1213		1213		1213

		1212		1212		1212		1212		1212		1212

		1211		1211		1211		1211		1211		1211

		1210		1210		1210		1210		1210		1210

		1209		1209		1209		1209		1209		1209

		1208		1208		1208		1208		1208		1208

		1207		1207		1207		1207		1207		1207

		1206		1206		1206		1206		1206		1206

		1205		1205		1205		1205		1205		1205

		1204		1204		1204		1204		1204		1204

		1203		1203		1203		1203		1203		1203

		1202		1202		1202		1202		1202		1202

		1201		1201		1201		1201		1201		1201

		1200		1200		1200		1200		1200		1200

		1199		1199		1199		1199		1199		1199

		1198		1198		1198		1198		1198		1198

		1197		1197		1197		1197		1197		1197

		1196		1196		1196		1196		1196		1196

		1195		1195		1195		1195		1195		1195

		1194		1194		1194		1194		1194		1194

		1193		1193		1193		1193		1193		1193

		1192		1192		1192		1192		1192		1192

		1191		1191		1191		1191		1191		1191

		1190		1190		1190		1190		1190		1190

		1189		1189		1189		1189		1189		1189

		1188		1188		1188		1188		1188		1188

		1187		1187		1187		1187		1187		1187

		1186		1186		1186		1186		1186		1186

		1185		1185		1185		1185		1185		1185

		1184		1184		1184		1184		1184		1184

		1183		1183		1183		1183		1183		1183

		1182		1182		1182		1182		1182		1182

		1181		1181		1181		1181		1181		1181

		1180		1180		1180		1180		1180		1180

		1179		1179		1179		1179		1179		1179

		1178		1178		1178		1178		1178		1178

		1177		1177		1177		1177		1177		1177

		1176		1176		1176		1176		1176		1176

		1175		1175		1175		1175		1175		1175

		1174		1174		1174		1174		1174		1174

		1173		1173		1173		1173		1173		1173

		1172		1172		1172		1172		1172		1172

		1171		1171		1171		1171		1171		1171

		1170		1170		1170		1170		1170		1170

		1169		1169		1169		1169		1169		1169

		1168		1168		1168		1168		1168		1168

		1167		1167		1167		1167		1167		1167

		1166		1166		1166		1166		1166		1166

		1165		1165		1165		1165		1165		1165

		1164		1164		1164		1164		1164		1164

		1163		1163		1163		1163		1163		1163

		1162		1162		1162		1162		1162		1162

		1161		1161		1161		1161		1161		1161

		1160		1160		1160		1160		1160		1160

		1159		1159		1159		1159		1159		1159

		1158		1158		1158		1158		1158		1158

		1157		1157		1157		1157		1157		1157

		1156		1156		1156		1156		1156		1156

		1155		1155		1155		1155		1155		1155

		1154		1154		1154		1154		1154		1154

		1153		1153		1153		1153		1153		1153

		1152		1152		1152		1152		1152		1152

		1151		1151		1151		1151		1151		1151

		1150		1150		1150		1150		1150		1150

		1149		1149		1149		1149		1149		1149

		1148		1148		1148		1148		1148		1148

		1147		1147		1147		1147		1147		1147

		1146		1146		1146		1146		1146		1146

		1145		1145		1145		1145		1145		1145

		1144		1144		1144		1144		1144		1144

		1143		1143		1143		1143		1143		1143

		1142		1142		1142		1142		1142		1142

		1141		1141		1141		1141		1141		1141

		1140		1140		1140		1140		1140		1140

		1139		1139		1139		1139		1139		1139

		1138		1138		1138		1138		1138		1138

		1137		1137		1137		1137		1137		1137

		1136		1136		1136		1136		1136		1136

		1135		1135		1135		1135		1135		1135

		1134		1134		1134		1134		1134		1134

		1133		1133		1133		1133		1133		1133

		1132		1132		1132		1132		1132		1132

		1131		1131		1131		1131		1131		1131

		1130		1130		1130		1130		1130		1130

		1129		1129		1129		1129		1129		1129

		1128		1128		1128		1128		1128		1128

		1127		1127		1127		1127		1127		1127

		1126		1126		1126		1126		1126		1126

		1125		1125		1125		1125		1125		1125

		1124		1124		1124		1124		1124		1124

		1123		1123		1123		1123		1123		1123

		1122		1122		1122		1122		1122		1122

		1121		1121		1121		1121		1121		1121

		1120		1120		1120		1120		1120		1120

		1119		1119		1119		1119		1119		1119

		1118		1118		1118		1118		1118		1118

		1117		1117		1117		1117		1117		1117

		1116		1116		1116		1116		1116		1116

		1115		1115		1115		1115		1115		1115

		1114		1114		1114		1114		1114		1114

		1113		1113		1113		1113		1113		1113

		1112		1112		1112		1112		1112		1112

		1111		1111		1111		1111		1111		1111

		1110		1110		1110		1110		1110		1110

		1109		1109		1109		1109		1109		1109

		1108		1108		1108		1108		1108		1108

		1107		1107		1107		1107		1107		1107

		1106		1106		1106		1106		1106		1106

		1105		1105		1105		1105		1105		1105

		1104		1104		1104		1104		1104		1104

		1103		1103		1103		1103		1103		1103

		1102		1102		1102		1102		1102		1102

		1101		1101		1101		1101		1101		1101

		1100		1100		1100		1100		1100		1100

		1099		1099		1099		1099		1099		1099

		1098		1098		1098		1098		1098		1098

		1097		1097		1097		1097		1097		1097

		1096		1096		1096		1096		1096		1096

		1095		1095		1095		1095		1095		1095

		1094		1094		1094		1094		1094		1094

		1093		1093		1093		1093		1093		1093

		1092		1092		1092		1092		1092		1092

		1091		1091		1091		1091		1091		1091

		1090		1090		1090		1090		1090		1090

		1089		1089		1089		1089		1089		1089

		1088		1088		1088		1088		1088		1088

		1087		1087		1087		1087		1087		1087

		1086		1086		1086		1086		1086		1086

		1085		1085		1085		1085		1085		1085

		1084		1084		1084		1084		1084		1084

		1083		1083		1083		1083		1083		1083

		1082		1082		1082		1082		1082		1082

		1081		1081		1081		1081		1081		1081

		1080		1080		1080		1080		1080		1080

		1079		1079		1079		1079		1079		1079

		1078		1078		1078		1078		1078		1078

		1077		1077		1077		1077		1077		1077

		1076		1076		1076		1076		1076		1076

		1075		1075		1075		1075		1075		1075

		1074		1074		1074		1074		1074		1074

		1073		1073		1073		1073		1073		1073

		1072		1072		1072		1072		1072		1072

		1071		1071		1071		1071		1071		1071

		1070		1070		1070		1070		1070		1070

		1069		1069		1069		1069		1069		1069

		1068		1068		1068		1068		1068		1068

		1067		1067		1067		1067		1067		1067

		1066		1066		1066		1066		1066		1066

		1065		1065		1065		1065		1065		1065

		1064		1064		1064		1064		1064		1064

		1063		1063		1063		1063		1063		1063

		1062		1062		1062		1062		1062		1062

		1061		1061		1061		1061		1061		1061

		1060		1060		1060		1060		1060		1060

		1059		1059		1059		1059		1059		1059

		1058		1058		1058		1058		1058		1058

		1057		1057		1057		1057		1057		1057

		1056		1056		1056		1056		1056		1056

		1055		1055		1055		1055		1055		1055

		1054		1054		1054		1054		1054		1054

		1053		1053		1053		1053		1053		1053

		1052		1052		1052		1052		1052		1052

		1051		1051		1051		1051		1051		1051

		1050		1050		1050		1050		1050		1050

		1049		1049		1049		1049		1049		1049

		1048		1048		1048		1048		1048		1048

		1047		1047		1047		1047		1047		1047

		1046		1046		1046		1046		1046		1046

		1045		1045		1045		1045		1045		1045

		1044		1044		1044		1044		1044		1044

		1043		1043		1043		1043		1043		1043

		1042		1042		1042		1042		1042		1042

		1041		1041		1041		1041		1041		1041

		1040		1040		1040		1040		1040		1040

		1039		1039		1039		1039		1039		1039

		1038		1038		1038		1038		1038		1038

		1037		1037		1037		1037		1037		1037

		1036		1036		1036		1036		1036		1036

		1035		1035		1035		1035		1035		1035

		1034		1034		1034		1034		1034		1034

		1033		1033		1033		1033		1033		1033

		1032		1032		1032		1032		1032		1032

		1031		1031		1031		1031		1031		1031

		1030		1030		1030		1030		1030		1030

		1029		1029		1029		1029		1029		1029

		1028		1028		1028		1028		1028		1028

		1027		1027		1027		1027		1027		1027

		1026		1026		1026		1026		1026		1026

		1025		1025		1025		1025		1025		1025

		1024		1024		1024		1024		1024		1024

		1023		1023		1023		1023		1023		1023

		1022		1022		1022		1022		1022		1022

		1021		1021		1021		1021		1021		1021

		1020		1020		1020		1020		1020		1020

		1019		1019		1019		1019		1019		1019

		1018		1018		1018		1018		1018		1018

		1017		1017		1017		1017		1017		1017

		1016		1016		1016		1016		1016		1016

		1015		1015		1015		1015		1015		1015

		1014		1014		1014		1014		1014		1014

		1013		1013		1013		1013		1013		1013

		1012		1012		1012		1012		1012		1012

		1011		1011		1011		1011		1011		1011

		1010		1010		1010		1010		1010		1010

		1009		1009		1009		1009		1009		1009

		1008		1008		1008		1008		1008		1008

		1007		1007		1007		1007		1007		1007

		1006		1006		1006		1006		1006		1006

		1005		1005		1005		1005		1005		1005

		1004		1004		1004		1004		1004		1004

		1003		1003		1003		1003		1003		1003

		1002		1002		1002		1002		1002		1002

		1001		1001		1001		1001		1001		1001

		1000		1000		1000		1000		1000		1000

		999		999		999		999		999		999

		998		998		998		998		998		998

		997		997		997		997		997		997

		996		996		996		996		996		996

		995		995		995		995		995		995

		994		994		994		994		994		994

		993		993		993		993		993		993

		992		992		992		992		992		992

		991		991		991		991		991		991

		990		990		990		990		990		990

		989		989		989		989		989		989

		988		988		988		988		988		988

		987		987		987		987		987		987

		986		986		986		986		986		986

		985		985		985		985		985		985

		984		984		984		984		984		984

		983		983		983		983		983		983

		982		982		982		982		982		982

		981		981		981		981		981		981

		980		980		980		980		980		980

		979		979		979		979		979		979

		978		978		978		978		978		978

		977		977		977		977		977		977

		976		976		976		976		976		976

		975		975		975		975		975		975

		974		974		974		974		974		974

		973		973		973		973		973		973

		972		972		972		972		972		972

		971		971		971		971		971		971

		970		970		970		970		970		970

		969		969		969		969		969		969

		968		968		968		968		968		968

		967		967		967		967		967		967

		966		966		966		966		966		966

		965		965		965		965		965		965

		964		964		964		964		964		964

		963		963		963		963		963		963

		962		962		962		962		962		962

		961		961		961		961		961		961

		960		960		960		960		960		960

		959		959		959		959		959		959

		958		958		958		958		958		958

		957		957		957		957		957		957

		956		956		956		956		956		956

		955		955		955		955		955		955

		954		954		954		954		954		954

		953		953		953		953		953		953

		952		952		952		952		952		952

		951		951		951		951		951		951

		950		950		950		950		950		950

		949		949		949		949		949		949

		948		948		948		948		948		948

		947		947		947		947		947		947

		946		946		946		946		946		946

		945		945		945		945		945		945

		944		944		944		944		944		944

		943		943		943		943		943		943

		942		942		942		942		942		942

		941		941		941		941		941		941

		940		940		940		940		940		940

		939		939		939		939		939		939

		938		938		938		938		938		938

		937		937		937		937		937		937

		936		936		936		936		936		936

		935		935		935		935		935		935

		934		934		934		934		934		934

		933		933		933		933		933		933

		932		932		932		932		932		932

		931		931		931		931		931		931

		930		930		930		930		930		930

		929		929		929		929		929		929

		928		928		928		928		928		928

		927		927		927		927		927		927

		926		926		926		926		926		926

		925		925		925		925		925		925

		924		924		924		924		924		924

		923		923		923		923		923		923

		922		922		922		922		922		922

		921		921		921		921		921		921

		920		920		920		920		920		920

		919		919		919		919		919		919

		918		918		918		918		918		918

		917		917		917		917		917		917

		916		916		916		916		916		916

		915		915		915		915		915		915

		914		914		914		914		914		914

		913		913		913		913		913		913

		912		912		912		912		912		912

		911		911		911		911		911		911

		910		910		910		910		910		910

		909		909		909		909		909		909

		908		908		908		908		908		908

		907		907		907		907		907		907

		906		906		906		906		906		906

		905		905		905		905		905		905

		904		904		904		904		904		904

		903		903		903		903		903		903

		902		902		902		902		902		902

		901		901		901		901		901		901

		900		900		900		900		900		900

		899		899		899		899		899		899

		898		898		898		898		898		898

		897		897		897		897		897		897

		896		896		896		896		896		896

		895		895		895		895		895		895

		894		894		894		894		894		894

		893		893		893		893		893		893

		892		892		892		892		892		892

		891		891		891		891		891		891

		890		890		890		890		890		890

		889		889		889		889		889		889

		888		888		888		888		888		888

		887		887		887		887		887		887

		886		886		886		886		886		886

		885		885		885		885		885		885

		884		884		884		884		884		884

		883		883		883		883		883		883

		882		882		882		882		882		882

		881		881		881		881		881		881

		880		880		880		880		880		880

		879		879		879		879		879		879

		878		878		878		878		878		878

		877		877		877		877		877		877

		876		876		876		876		876		876

		875		875		875		875		875		875

		874		874		874		874		874		874

		873		873		873		873		873		873

		872		872		872		872		872		872

		871		871		871		871		871		871

		870		870		870		870		870		870

		869		869		869		869		869		869

		868		868		868		868		868		868

		867		867		867		867		867		867

		866		866		866		866		866		866

		865		865		865		865		865		865

		864		864		864		864		864		864

		863		863		863		863		863		863

		862		862		862		862		862		862

		861		861		861		861		861		861

		860		860		860		860		860		860

		859		859		859		859		859		859

		858		858		858		858		858		858

		857		857		857		857		857		857

		856		856		856		856		856		856

		855		855		855		855		855		855

		854		854		854		854		854		854

		853		853		853		853		853		853

		852		852		852		852		852		852

		851		851		851		851		851		851

		850		850		850		850		850		850

		849		849		849		849		849		849

		848		848		848		848		848		848

		847		847		847		847		847		847

		846		846		846		846		846		846

		845		845		845		845		845		845

		844		844		844		844		844		844

		843		843		843		843		843		843

		842		842		842		842		842		842

		841		841		841		841		841		841

		840		840		840		840		840		840

		839		839		839		839		839		839

		838		838		838		838		838		838

		837		837		837		837		837		837

		836		836		836		836		836		836

		835		835		835		835		835		835

		834		834		834		834		834		834

		833		833		833		833		833		833

		832		832		832		832		832		832

		831		831		831		831		831		831

		830		830		830		830		830		830

		829		829		829		829		829		829

		828		828		828		828		828		828

		827		827		827		827		827		827

		826		826		826		826		826		826

		825		825		825		825		825		825

		824		824		824		824		824		824

		823		823		823		823		823		823

		822		822		822		822		822		822

		821		821		821		821		821		821

		820		820		820		820		820		820

		819		819		819		819		819		819

		818		818		818		818		818		818

		817		817		817		817		817		817

		816		816		816		816		816		816

		815		815		815		815		815		815

		814		814		814		814		814		814

		813		813		813		813		813		813

		812		812		812		812		812		812

		811		811		811		811		811		811

		810		810		810		810		810		810

		809		809		809		809		809		809

		808		808		808		808		808		808

		807		807		807		807		807		807

		806		806		806		806		806		806

		805		805		805		805		805		805

		804		804		804		804		804		804

		803		803		803		803		803		803

		802		802		802		802		802		802

		801		801		801		801		801		801

		800		800		800		800		800		800

		799		799		799		799		799		799

		798		798		798		798		798		798

		797		797		797		797		797		797

		796		796		796		796		796		796

		795		795		795		795		795		795

		794		794		794		794		794		794

		793		793		793		793		793		793

		792		792		792		792		792		792

		791		791		791		791		791		791

		790		790		790		790		790		790

		789		789		789		789		789		789

		788		788		788		788		788		788

		787		787		787		787		787		787

		786		786		786		786		786		786

		785		785		785		785		785		785

		784		784		784		784		784		784

		783		783		783		783		783		783

		782		782		782		782		782		782

		781		781		781		781		781		781

		780		780		780		780		780		780

		779		779		779		779		779		779

		778		778		778		778		778		778

		777		777		777		777		777		777

		776		776		776		776		776		776

		775		775		775		775		775		775

		774		774		774		774		774		774

		773		773		773		773		773		773

		772		772		772		772		772		772

		771		771		771		771		771		771

		770		770		770		770		770		770

		769		769		769		769		769		769

		768		768		768		768		768		768

		767		767		767		767		767		767

		766		766		766		766		766		766

		765		765		765		765		765		765

		764		764		764		764		764		764

		763		763		763		763		763		763

		762		762		762		762		762		762

		761		761		761		761		761		761

		760		760		760		760		760		760

		759		759		759		759		759		759

		758		758		758		758		758		758

		757		757		757		757		757		757

		756		756		756		756		756		756

		755		755		755		755		755		755

		754		754		754		754		754		754

		753		753		753		753		753		753

		752		752		752		752		752		752

		751		751		751		751		751		751

		750		750		750		750		750		750

		749		749		749		749		749		749

		748		748		748		748		748		748

		747		747		747		747		747		747

		746		746		746		746		746		746

		745		745		745		745		745		745

		744		744		744		744		744		744

		743		743		743		743		743		743

		742		742		742		742		742		742

		741		741		741		741		741		741

		740		740		740		740		740		740

		739		739		739		739		739		739

		738		738		738		738		738		738

		737		737		737		737		737		737

		736		736		736		736		736		736

		735		735		735		735		735		735

		734		734		734		734		734		734

		733		733		733		733		733		733

		732		732		732		732		732		732

		731		731		731		731		731		731

		730		730		730		730		730		730

		729		729		729		729		729		729

		728		728		728		728		728		728

		727		727		727		727		727		727

		726		726		726		726		726		726

		725		725		725		725		725		725

		724		724		724		724		724		724

		723		723		723		723		723		723

		722		722		722		722		722		722

		721		721		721		721		721		721

		720		720		720		720		720		720

		719		719		719		719		719		719

		718		718		718		718		718		718

		717		717		717		717		717		717

		716		716		716		716		716		716

		715		715		715		715		715		715

		714		714		714		714		714		714

		713		713		713		713		713		713

		712		712		712		712		712		712

		711		711		711		711		711		711

		710		710		710		710		710		710

		709		709		709		709		709		709

		708		708		708		708		708		708

		707		707		707		707		707		707

		706		706		706		706		706		706

		705		705		705		705		705		705

		704		704		704		704		704		704

		703		703		703		703		703		703

		702		702		702		702		702		702

		701		701		701		701		701		701

		700		700		700		700		700		700

		699		699		699		699		699		699

		698		698		698		698		698		698

		697		697		697		697		697		697

		696		696		696		696		696		696

		695		695		695		695		695		695

		694		694		694		694		694		694

		693		693		693		693		693		693

		692		692		692		692		692		692

		691		691		691		691		691		691

		690		690		690		690		690		690

		689		689		689		689		689		689

		688		688		688		688		688		688

		687		687		687		687		687		687

		686		686		686		686		686		686

		685		685		685		685		685		685

		684		684		684		684		684		684

		683		683		683		683		683		683

		682		682		682		682		682		682

		681		681		681		681		681		681

		680		680		680		680		680		680

		679		679		679		679		679		679

		678		678		678		678		678		678

		677		677		677		677		677		677

		676		676		676		676		676		676

		675		675		675		675		675		675

		674		674		674		674		674		674

		673		673		673		673		673		673

		672		672		672		672		672		672

		671		671		671		671		671		671

		670		670		670		670		670		670

		669		669		669		669		669		669

		668		668		668		668		668		668

		667		667		667		667		667		667

		666		666		666		666		666		666

		665		665		665		665		665		665

		664		664		664		664		664		664

		663		663		663		663		663		663

		662		662		662		662		662		662

		661		661		661		661		661		661

		660		660		660		660		660		660

		659		659		659		659		659		659

		658		658		658		658		658		658

		657		657		657		657		657		657

		656		656		656		656		656		656

		655		655		655		655		655		655

		654		654		654		654		654		654

		653		653		653		653		653		653

		652		652		652		652		652		652

		651		651		651		651		651		651

		650		650		650		650		650		650

		649		649		649		649		649		649

		648		648		648		648		648		648

		647		647		647		647		647		647

		646		646		646		646		646		646

		645		645		645		645		645		645

		644		644		644		644		644		644

		643		643		643		643		643		643

		642		642		642		642		642		642

		641		641		641		641		641		641

		640		640		640		640		640		640

		639		639		639		639		639		639

		638		638		638		638		638		638

		637		637		637		637		637		637

		636		636		636		636		636		636

		635		635		635		635		635		635

		634		634		634		634		634		634

		633		633		633		633		633		633

		632		632		632		632		632		632

		631		631		631		631		631		631

		630		630		630		630		630		630

		629		629		629		629		629		629

		628		628		628		628		628		628

		627		627		627		627		627		627

		626		626		626		626		626		626

		625		625		625		625		625		625

		624		624		624		624		624		624

		623		623		623		623		623		623

		622		622		622		622		622		622

		621		621		621		621		621		621

		620		620		620		620		620		620

		619		619		619		619		619		619

		618		618		618		618		618		618

		617		617		617		617		617		617

		616		616		616		616		616		616

		615		615		615		615		615		615

		614		614		614		614		614		614

		613		613		613		613		613		613

		612		612		612		612		612		612

		611		611		611		611		611		611

		610		610		610		610		610		610

		609		609		609		609		609		609

		608		608		608		608		608		608

		607		607		607		607		607		607

		606		606		606		606		606		606

		605		605		605		605		605		605

		604		604		604		604		604		604

		603		603		603		603		603		603

		602		602		602		602		602		602

		601		601		601		601		601		601

		600		600		600		600		600		600

		599		599		599		599		599		599

		598		598		598		598		598		598

		597		597		597		597		597		597

		596		596		596		596		596		596

		595		595		595		595		595		595

		594		594		594		594		594		594

		593		593		593		593		593		593

		592		592		592		592		592		592

		591		591		591		591		591		591

		590		590		590		590		590		590

		589		589		589		589		589		589

		588		588		588		588		588		588

		587		587		587		587		587		587

		586		586		586		586		586		586

		585		585		585		585		585		585

		584		584		584		584		584		584

		583		583		583		583		583		583

		582		582		582		582		582		582

		581		581		581		581		581		581

		580		580		580		580		580		580

		579		579		579		579		579		579

		578		578		578		578		578		578

		577		577		577		577		577		577

		576		576		576		576		576		576

		575		575		575		575		575		575

		574		574		574		574		574		574

		573		573		573		573		573		573

		572		572		572		572		572		572

		571		571		571		571		571		571

		570		570		570		570		570		570

		569		569		569		569		569		569

		568		568		568		568		568		568

		567		567		567		567		567		567

		566		566		566		566		566		566

		565		565		565		565		565		565

		564		564		564		564		564		564

		563		563		563		563		563		563

		562		562		562		562		562		562

		561		561		561		561		561		561

		560		560		560		560		560		560

		559		559		559		559		559		559

		558		558		558		558		558		558

		557		557		557		557		557		557

		556		556		556		556		556		556

		555		555		555		555		555		555

		554		554		554		554		554		554

		553		553		553		553		553		553

		552		552		552		552		552		552

		551		551		551		551		551		551

		550		550		550		550		550		550

		549		549		549		549		549		549

		548		548		548		548		548		548

		547		547		547		547		547		547

		546		546		546		546		546		546

		545		545		545		545		545		545

		544		544		544		544		544		544

		543		543		543		543		543		543

		542		542		542		542		542		542

		541		541		541		541		541		541

		540		540		540		540		540		540

		539		539		539		539		539		539

		538		538		538		538		538		538

		537		537		537		537		537		537

		536		536		536		536		536		536

		535		535		535		535		535		535

		534		534		534		534		534		534

		533		533		533		533		533		533

		532		532		532		532		532		532

		531		531		531		531		531		531

		530		530		530		530		530		530

		529		529		529		529		529		529

		528		528		528		528		528		528

		527		527		527		527		527		527

		526		526		526		526		526		526

		525		525		525		525		525		525

		524		524		524		524		524		524

		523		523		523		523		523		523

		522		522		522		522		522		522

		521		521		521		521		521		521

		520		520		520		520		520		520

		519		519		519		519		519		519

		518		518		518		518		518		518

		517		517		517		517		517		517

		516		516		516		516		516		516

		515		515		515		515		515		515

		514		514		514		514		514		514

		513		513		513		513		513		513

		512		512		512		512		512		512

		511		511		511		511		511		511

		510		510		510		510		510		510

		509		509		509		509		509		509

		508		508		508		508		508		508

		507		507		507		507		507		507

		506		506		506		506		506		506

		505		505		505		505		505		505

		504		504		504		504		504		504

		503		503		503		503		503		503

		502		502		502		502		502		502

		501		501		501		501		501		501

		500		500		500		500		500		500

		499		499		499		499		499		499

		498		498		498		498		498		498

		497		497		497		497		497		497

		496		496		496		496		496		496

		495		495		495		495		495		495

		494		494		494		494		494		494

		493		493		493		493		493		493

		492		492		492		492		492		492

		491		491		491		491		491		491

		490		490		490		490		490		490

		489		489		489		489		489		489

		488		488		488		488		488		488

		487		487		487		487		487		487

		486		486		486		486		486		486

		485		485		485		485		485		485

		484		484		484		484		484		484

		483		483		483		483		483		483

		482		482		482		482		482		482

		481		481		481		481		481		481

		480		480		480		480		480		480

		479		479		479		479		479		479

		478		478		478		478		478		478

		477		477		477		477		477		477

		476		476		476		476		476		476

		475		475		475		475		475		475

		474		474		474		474		474		474

		473		473		473		473		473		473

		472		472		472		472		472		472

		471		471		471		471		471		471

		470		470		470		470		470		470

		469		469		469		469		469		469

		468		468		468		468		468		468

		467		467		467		467		467		467

		466		466		466		466		466		466

		465		465		465		465		465		465

		464		464		464		464		464		464

		463		463		463		463		463		463

		462		462		462		462		462		462

		461		461		461		461		461		461

		460		460		460		460		460		460

		459		459		459		459		459		459

		458		458		458		458		458		458

		457		457		457		457		457		457

		456		456		456		456		456		456

		455		455		455		455		455		455

		454		454		454		454		454		454

		453		453		453		453		453		453

		452		452		452		452		452		452

		451		451		451		451		451		451

		450		450		450		450		450		450

		449		449		449		449		449		449

		448		448		448		448		448		448

		447		447		447		447		447		447

		446		446		446		446		446		446

		445		445		445		445		445		445

		444		444		444		444		444		444

		443		443		443		443		443		443

		442		442		442		442		442		442

		441		441		441		441		441		441

		440		440		440		440		440		440

		439		439		439		439		439		439

		438		438		438		438		438		438

		437		437		437		437		437		437

		436		436		436		436		436		436

		435		435		435		435		435		435

		434		434		434		434		434		434

		433		433		433		433		433		433

		432		432		432		432		432		432

		431		431		431		431		431		431

		430		430		430		430		430		430

		429		429		429		429		429		429

		428		428		428		428		428		428

		427		427		427		427		427		427

		426		426		426		426		426		426

		425		425		425		425		425		425

		424		424		424		424		424		424

		423		423		423		423		423		423

		422		422		422		422		422		422

		421		421		421		421		421		421

		420		420		420		420		420		420

		419		419		419		419		419		419

		418		418		418		418		418		418

		417		417		417		417		417		417

		416		416		416		416		416		416

		415		415		415		415		415		415

		414		414		414		414		414		414

		413		413		413		413		413		413

		412		412		412		412		412		412

		411		411		411		411		411		411

		410		410		410		410		410		410

		409		409		409		409		409		409

		408		408		408		408		408		408

		407		407		407		407		407		407

		406		406		406		406		406		406

		405		405		405		405		405		405

		404		404		404		404		404		404

		403		403		403		403		403		403

		402		402		402		402		402		402

		401		401		401		401		401		401

		400		400		400		400		400		400

		399		399		399		399		399		399

		398		398		398		398		398		398

		397		397		397		397		397		397

		396		396		396		396		396		396

		395		395		395		395		395		395

		394		394		394		394		394		394

		393		393		393		393		393		393

		392		392		392		392		392		392

		391		391		391		391		391		391

		390		390		390		390		390		390

		389		389		389		389		389		389

		388		388		388		388		388		388

		387		387		387		387		387		387

		386		386		386		386		386		386

		385		385		385		385		385		385

		384		384		384		384		384		384

		383		383		383		383		383		383

		382		382		382		382		382		382

		381		381		381		381		381		381

		380		380		380		380		380		380

		379		379		379		379		379		379

		378		378		378		378		378		378

		377		377		377		377		377		377

		376		376		376		376		376		376

		375		375		375		375		375		375

		374		374		374		374		374		374

		373		373		373		373		373		373

		372		372		372		372		372		372

		371		371		371		371		371		371

		370		370		370		370		370		370

		369		369		369		369		369		369

		368		368		368		368		368		368

		367		367		367		367		367		367

		366		366		366		366		366		366

		365		365		365		365		365		365

		364		364		364		364		364		364

		363		363		363		363		363		363

		362		362		362		362		362		362

		361		361		361		361		361		361

		360		360		360		360		360		360

		359		359		359		359		359		359

		358		358		358		358		358		358

		357		357		357		357		357		357

		356		356		356		356		356		356

		355		355		355		355		355		355

		354		354		354		354		354		354

		353		353		353		353		353		353

		352		352		352		352		352		352

		351		351		351		351		351		351

		350		350		350		350		350		350

		349		349		349		349		349		349

		348		348		348		348		348		348

		347		347		347		347		347		347

		346		346		346		346		346		346

		345		345		345		345		345		345

		344		344		344		344		344		344

		343		343		343		343		343		343

		342		342		342		342		342		342

		341		341		341		341		341		341

		340		340		340		340		340		340

		339		339		339		339		339		339

		338		338		338		338		338		338

		337		337		337		337		337		337

		336		336		336		336		336		336

		335		335		335		335		335		335

		334		334		334		334		334		334

		333		333		333		333		333		333

		332		332		332		332		332		332

		331		331		331		331		331		331

		330		330		330		330		330		330

		329		329		329		329		329		329

		328		328		328		328		328		328

		327		327		327		327		327		327

		326		326		326		326		326		326

		325		325		325		325		325		325

		324		324		324		324		324		324

		323		323		323		323		323		323

		322		322		322		322		322		322

		321		321		321		321		321		321

		320		320		320		320		320		320

		319		319		319		319		319		319

		318		318		318		318		318		318

		317		317		317		317		317		317

		316		316		316		316		316		316

		315		315		315		315		315		315

		314		314		314		314		314		314

		313		313		313		313		313		313

		312		312		312		312		312		312

		311		311		311		311		311		311

		310		310		310		310		310		310

		309		309		309		309		309		309

		308		308		308		308		308		308

		307		307		307		307		307		307

		306		306		306		306		306		306

		305		305		305		305		305		305

		304		304		304		304		304		304

		303		303		303		303		303		303

		302		302		302		302		302		302

		301		301		301		301		301		301

		300		300		300		300		300		300

		299		299		299		299		299		299

		298		298		298		298		298		298

		297		297		297		297		297		297

		296		296		296		296		296		296

		295		295		295		295		295		295

		294		294		294		294		294		294

		293		293		293		293		293		293

		292		292		292		292		292		292

		291		291		291		291		291		291

		290		290		290		290		290		290

		289		289		289		289		289		289

		288		288		288		288		288		288

		287		287		287		287		287		287

		286		286		286		286		286		286

		285		285		285		285		285		285

		284		284		284		284		284		284

		283		283		283		283		283		283

		282		282		282		282		282		282

		281		281		281		281		281		281

		280		280		280		280		280		280

		279		279		279		279		279		279

		278		278		278		278		278		278

		277		277		277		277		277		277

		276		276		276		276		276		276

		275		275		275		275		275		275

		274		274		274		274		274		274

		273		273		273		273		273		273

		272		272		272		272		272		272

		271		271		271		271		271		271

		270		270		270		270		270		270

		269		269		269		269		269		269

		268		268		268		268		268		268

		267		267		267		267		267		267

		266		266		266		266		266		266

		265		265		265		265		265		265

		264		264		264		264		264		264

		263		263		263		263		263		263

		262		262		262		262		262		262

		261		261		261		261		261		261

		260		260		260		260		260		260

		259		259		259		259		259		259

		258		258		258		258		258		258

		257		257		257		257		257		257

		256		256		256		256		256		256

		255		255		255		255		255		255

		254		254		254		254		254		254

		253		253		253		253		253		253

		252		252		252		252		252		252

		251		251		251		251		251		251

		250		250		250		250		250		250

		249		249		249		249		249		249

		248		248		248		248		248		248

		247		247		247		247		247		247

		246		246		246		246		246		246

		245		245		245		245		245		245

		244		244		244		244		244		244

		243		243		243		243		243		243

		242		242		242		242		242		242

		241		241		241		241		241		241

		240		240		240		240		240		240

		239		239		239		239		239		239

		238		238		238		238		238		238

		237		237		237		237		237		237

		236		236		236		236		236		236

		235		235		235		235		235		235

		234		234		234		234		234		234

		233		233		233		233		233		233

		232		232		232		232		232		232

		231		231		231		231		231		231

		230		230		230		230		230		230

		229		229		229		229		229		229

		228		228		228		228		228		228

		227		227		227		227		227		227

		226		226		226		226		226		226

		225		225		225		225		225		225

		224		224		224		224		224		224

		223		223		223		223		223		223

		222		222		222		222		222		222

		221		221		221		221		221		221

		220		220		220		220		220		220

		219		219		219		219		219		219

		218		218		218		218		218		218

		217		217		217		217		217		217

		216		216		216		216		216		216

		215		215		215		215		215		215

		214		214		214		214		214		214

		213		213		213		213		213		213

		212		212		212		212		212		212

		211		211		211		211		211		211

		210		210		210		210		210		210

		209		209		209		209		209		209

		208		208		208		208		208		208

		207		207		207		207		207		207

		206		206		206		206		206		206

		205		205		205		205		205		205

		204		204		204		204		204		204

		203		203		203		203		203		203

		202		202		202		202		202		202

		201		201		201		201		201		201

		200		200		200		200		200		200



wavelength (nm)

Abs

0.0022825552

0.0081941932

0.0169226117

0.038249433

0.0415504202

0.0556665249

0.0056957039

0.0095049646

0.0179543942

0.0388209038

0.0448219553

0.0582381859

0.0018327052

0.0085996436

0.0175968856

0.0385809876

0.0415023118

0.0547540113

0.0063131489

0.0096747829

0.0182958599

0.0391402356

0.0449937321

0.0593983643

0.0025765775

0.0088061951

0.0178378895

0.0384146981

0.0420078747

0.0547523685

0.0044317176

0.0088808807

0.0171710234

0.0389175527

0.043499738

0.058583498

0.0051449044

0.0090472838

0.0191339329

0.038655512

0.0436244533

0.0573684387

0.0021277235

0.0088054817

0.016824061

0.0386196636

0.0418910645

0.0562794581

0.0062308158

0.0096808448

0.0187618565

0.0390116461

0.0452196933

0.0591210946

0.0023813734

0.0088975523

0.0180160981

0.0390838385

0.0417150371

0.0555765182

0.0060452758

0.0096245212

0.0177183412

0.0388173945

0.0448068008

0.0594194382

0.0034029353

0.0091921231

0.0186190605

0.0385405347

0.0426827483

0.0560164228

0.0049648024

0.0091795642

0.0173552353

0.0388057344

0.0429075398

0.0590683296

0.0048657088

0.0096779857

0.018824704

0.0388419665

0.0445883684

0.0573856607

0.0034402972

0.0095964419

0.0177377295

0.039097406

0.0424615555

0.0576056354

0.0067930394

0.009620578

0.0191163216

0.0392066389

0.0454528742

0.0596416891

0.0023993594

0.0095598958

0.0178298783

0.0392277464

0.0425362624

0.0560784191

0.00752621

0.0109101841

0.0194943044

0.0397375003

0.0458519086

0.0612205826

0.0032054558

0.0089961169

0.0187125597

0.0391466096

0.042942144

0.0561399497

0.0057682293

0.0111717796

0.0185976066

0.0398774259

0.0446247719

0.0604085065

0.0050143972

0.0096224565

0.0195733421

0.0393502451

0.0449143536

0.0582708344

0.0046092439

0.0108391829

0.0190193281

0.0404070616

0.0436691344

0.0592940226

0.0070009963

0.0105333356

0.0194734857

0.0395829044

0.0464792252

0.0601720959

0.0047470098

0.0119845737

0.0204914082

0.0412787311

0.0445461199

0.0588944256

0.0076095532

0.0109320572

0.0199733526

0.0401990674

0.0461512618

0.0621577911

0.0045549348

0.0116210962

0.0205354523

0.0410083234

0.0455737226

0.0584766269

0.0077184183

0.012755624

0.0203463044

0.041549027

0.046299547

0.0626196042

0.0064920243

0.0117136324

0.0218295939

0.0413087644

0.0474730134

0.0604265966

0.006577061

0.0132266786

0.0206745639

0.0421906635

0.0459316634

0.0613925308

0.0089173689

0.0132657224

0.0227265861

0.0425462834

0.0487950891

0.0635156706

0.0064133615

0.0135351764

0.0223272759

0.0430881083

0.0466693267

0.061395213

0.0102244439

0.0144976117

0.0226290002

0.0435010567

0.0495264679

0.0653996319

0.0069301319

0.0141989933

0.0233341064

0.043906033

0.0483341999

0.0620812401

0.0101485476

0.0153723312

0.0228370987

0.0441270173

0.0491907448

0.065716356

0.0092854388

0.0155251706

0.0254164115

0.0459293909

0.0516750738

0.0641775355

0.0102019701

0.0167677999

0.0244175065

0.0454701781

0.0498056337

0.0661295801

0.011935507

0.0164605193

0.0265469588

0.0467541628

0.0531821437

0.0674508214

0.0108097773

0.0189494509

0.02625845

0.047979217

0.0521501228

0.0668091252

0.0140718864

0.0187590197

0.0277727842

0.047540471

0.054072503

0.0702618658

0.0119323675

0.0193725694

0.0287944917

0.0502076745

0.0545636564

0.0684867054

0.0151840523

0.0216396097

0.0292300005

0.0501020886

0.0558079369

0.0722785667

0.0134751741

0.0201993808

0.0308890026

0.0509127974

0.0565147921

0.0702364892

0.016165385

0.0241890829

0.0311631393

0.0525458083

0.0571373105

0.0740301534

0.0160007719

0.0217402372

0.0321501829

0.052305609

0.058960896

0.0726855323

0.0153632136

0.0240526721

0.0321252942

0.0533888154

0.0579395853

0.0738785118

0.0185139123

0.0236836318

0.0330501422

0.0533282869

0.0594073571

0.0756104812

0.0155539587

0.0240717959

0.0329107493

0.0543918386

0.059780661

0.0732971206

0.0191303343

0.0260243006

0.033591032

0.054224018

0.0595940612

0.0777025893

0.0171167888

0.0236910135

0.0343964361

0.0551066734

0.0610347614

0.0742073134

0.0185058881

0.0274833217

0.033914905

0.0558795594

0.0607969649

0.0776860267

0.0182593577

0.0235552769

0.0344773084

0.0539526381

0.0604558401

0.0755137205

0.0170905367

0.0263477229

0.0339374952

0.0559834987

0.0606133491

0.0762063637

0.0187046677

0.0249955375

0.0341695659

0.0541807041

0.0603108518

0.0767969713

0.0156740658

0.0241183955

0.0339278951

0.0549286455

0.0603930987

0.074784264

0.0193794444

0.0258066785

0.033080142

0.0540316068

0.0597853251

0.0777249411

0.0149381943

0.0227308404

0.0333194137

0.0543502942

0.0598527044

0.0732929483

0.0182200242

0.0262124743

0.0328969546

0.0541168638

0.0591778122

0.0777827203

0.0163890626

0.022263648

0.0332005843

0.0531551987

0.0589517951

0.073992826

0.0154398931

0.0245835614

0.0316963941

0.0536124222

0.0585988723

0.0748915076

0.016917685

0.0232328363

0.0330014564

0.0521509089

0.058260683

0.075923577

0.0147649124

0.0222184192

0.0316875689

0.0534347743

0.0586494468

0.0728754327

0.0160618499

0.0238910317

0.0314385332

0.0516691543

0.0577142723

0.0756076723

0.0135814594

0.0210902095

0.0312694758

0.0516831502

0.0575504527

0.0722362846

0.016921347

0.0241378248

0.0315773413

0.05143952

0.0577813312

0.0764189139

0.0139849419

0.0207015499

0.0315121226

0.0509495586

0.0565829016

0.0720014796

0.0150328865

0.0231301952

0.0310448725

0.0513496287

0.0583023056

0.0754506141

0.0159206893

0.0218391474

0.0317972638

0.0503919721

0.0558781177

0.0737841576

0.0133357067

0.0209569149

0.0302941427

0.0511573255

0.0582453497

0.0731206685

0.0163084529

0.0235134661

0.032444559

0.050794702

0.0567551181

0.0759031996

0.013133713

0.0195657332

0.0304486882

0.0504694842

0.0566576012

0.0718341991

0.0158185549

0.0236459635

0.0314196683

0.0511448607

0.0580606759

0.076365985

0.0140374489

0.021271009

0.0320186354

0.0507027358

0.0562801659

0.0729954019

0.0141516281

0.0217507705

0.0294931736

0.0502467006

0.0574594662

0.0746311843

0.015330228

0.0225180238

0.0324323438

0.0510109216

0.0567027889

0.0749946758

0.0129267462

0.0209357794

0.0303946305

0.0508128293

0.0577941947

0.0737913698

0.0163362976

0.0231000539

0.031744875

0.0499659181

0.0565644726

0.0757757053

0.012539885

0.0204062332

0.0309461225

0.0511370264

0.0575216971

0.072809279

0.0158142056

0.0230896268

0.0315547101

0.0500541292

0.0574425943

0.07682129

0.0130416742

0.0208479389

0.0310704522

0.0501731262

0.0557373278

0.0726050287

0.0146940285

0.0218788106

0.0306231771

0.0506125316

0.058383815

0.075703837

0.0139986025

0.0222219881

0.032015793

0.0497401133

0.0559549071

0.074360244

0.0135240145

0.0207043197

0.0305091944

0.0507361926

0.0582740642

0.0743066668

0.0158683043

0.0237223152

0.0327192619

0.0505064391

0.0576750115

0.0766951293

0.0120029617

0.0204456299

0.030569043

0.0503563322

0.0570113398

0.0730380267

0.0162262991

0.0234922078

0.0320965275

0.0507033169

0.0586560518

0.0777430534

0.0128958393

0.0218993109

0.0317998528

0.0507314764

0.056645304

0.074114427

0.0153586539

0.0228283666

0.0317429826

0.05076354

0.0598284341

0.0770811886

0.0145884603

0.023138687

0.0331407636

0.0511245057

0.0570264533

0.0758446902

0.0142344069

0.0224788748

0.0318986587

0.0518896915

0.0598602816

0.0763737261

0.0159845501

0.0245544445

0.0336443149

0.0510583222

0.058454562

0.0780268684

0.0135929715

0.0225125179

0.0325098932

0.0520704426

0.0590853542

0.0755750835

0.01725691

0.0251114555

0.0338796973

0.0523252599

0.0603559464

0.0797966197

0.013624222

0.0240291972

0.0336894058

0.0522781052

0.0587872118

0.0763470679

0.0171225779

0.0246890411

0.0337823443

0.0527791567

0.0618372038

0.0798355639

0.0152339423

0.0253401995

0.0353921577

0.0530727059

0.0597775429

0.0781804696

0.0157088488

0.0247740448

0.0342884883

0.053644903

0.0622109883

0.0797649249

0.0178607609

0.0269038174

0.0359706208

0.0539276376

0.0613389835

0.0805695727

0.0150772119

0.0251515266

0.0351397023

0.0544931293

0.0617529824

0.0792010426

0.0186766442

0.0273878314

0.0365021266

0.0540480539

0.0629580319

0.0828762725

0.0159399975

0.0267153997

0.036501199

0.0555240363

0.0617275275

0.0793053731

0.0180153158

0.0264184438

0.0363457799

0.0546016693

0.0645102486

0.0828521773

0.0162503216

0.0274755452

0.036737714

0.0546862446

0.0611955188

0.0804248452

0.017615702

0.0267198328

0.0363797806

0.0558229499

0.0647997856

0.0821959972

0.0179739539

0.0275664739

0.0373754948

0.0543386191

0.0623661466

0.0822308809

0.0156521946

0.0265827887

0.0353582911

0.0553791262

0.062924251

0.0810063779

0.0198520515

0.0283229426

0.0381269604

0.0553472228

0.0650879517

0.0847423151

0.0155867189

0.0275846776

0.0367958918

0.0556832962

0.0622729808

0.080466345

0.0186776165

0.027805347

0.036817532

0.0552869774

0.0656042844

0.0849626511

0.0168277211

0.0279160552

0.0375387333

0.0555776358

0.0623250306

0.0819106698

0.0170347784

0.0268634185

0.0360465832

0.0551606044

0.0651536956

0.0831352472

0.0182549041

0.0283705797

0.0378120765

0.0550066195

0.0630829856

0.0839090198

0.0161558203

0.0268035009

0.0355388932

0.0552582815

0.063283667

0.0818568096

0.01826052

0.0272137281

0.0371755138

0.0540789254

0.0642481521

0.0845416933

0.0148389144

0.0266246498

0.034941338

0.0544604398

0.0607840158

0.0807101428

0.0185588915

0.0264125019

0.0356118008

0.0544025786

0.0648343489

0.0844527632

0.0154256234

0.0267348904

0.0364098698

0.0543271191

0.0609825663

0.0815211982

0.0186676178

0.0275059622

0.0356703326

0.055426769

0.0650284439

0.0849782005

0.0177124087

0.0270706881

0.0369624942

0.0543132164

0.0621804297

0.0833668709

0.0164257307

0.0269219112

0.0353308283

0.0557974875

0.0636444986

0.0836198926

0.0190759636

0.0276501942

0.0363970622

0.0542604178

0.0637228787

0.0855725482

0.0158632025

0.0265738722

0.0354659408

0.0552181266

0.0614417903

0.0824047476

0.019108586

0.0268689264

0.0356447026

0.0546486378

0.0650032237

0.0863748789

0.0161488075

0.0267239343

0.0355032161

0.0545386784

0.0606964268

0.0829029903

0.0192652084

0.0268582143

0.0355974697

0.0556685552

0.0644523501

0.0859528631

0.0185658336

0.0278323386

0.0372328199

0.0554441512

0.0634488538

0.086034432

0.0174601842

0.0277257636

0.0350693427

0.0557692014

0.0630414709

0.0850104392

0.0197713096

0.026800856

0.0366970077

0.0548786223

0.0644249693

0.0870676711

0.0164933484

0.0274068285

0.0355836488

0.0558716133

0.0623658784

0.0843440816

0.0198964644

0.0270116516

0.0356503539

0.0549690127

0.0648005083

0.0876179859

0.0173971858

0.0269384645

0.0368632898

0.0552402027

0.0620042309

0.0843875557

0.0195798408

0.0275881272

0.0353014283

0.0563867912

0.0650017783

0.0883906558

0.0188590623

0.027445212

0.0369020663

0.0548802093

0.0631276146

0.0865857974

0.0180138051

0.0271327924

0.0351814404

0.0562245026

0.0632427931

0.08629217

0.02064416

0.0275887065

0.037316788

0.0556142069

0.0656765476

0.0891356245

0.0164141711

0.0271682851

0.0345642753

0.0556832068

0.0612141453

0.0851695165

0.0214261022

0.0273034181

0.0369687788

0.0557041019

0.0660837367

0.0895384103

0.017294379

0.0275078379

0.0362937115

0.0558231585

0.0620086789

0.0865386575

0.019982433

0.0278537832

0.0353866257

0.0559321158

0.0649726167

0.0891391486

0.0188335162

0.0272339024

0.0373676792

0.0549825542

0.0631097481

0.0878251418

0.0186955873

0.0276374221

0.0346420109

0.0567316972

0.0640023574

0.0883350074

0.0200364292

0.0275191441

0.036971204

0.0551481694

0.0648513883

0.089798592

0.0178113226

0.027341295

0.0355939865

0.0563326217

0.0622547567

0.0871236026

0.0216798801

0.0278667565

0.0366898254

0.05626617

0.0666001663

0.0917045623

0.0169976559

0.0272022635

0.0362011343

0.0548440516

0.0617027618

0.0870254114

0.0208264571

0.0274372418

0.0357625447

0.0564925894

0.065438129

0.0908968747

0.0186878312

0.027581865

0.0372172259

0.0557905436

0.0641200766

0.0898436979

0.0187130999

0.0273089036

0.0343936346

0.0559740178

0.063168183

0.0890288428

0.0203709919

0.0273105018

0.0375880413

0.0557548106

0.0650740936

0.0917572901

0.0175723843

0.0268990528

0.0348011702

0.0557662584

0.0621993095

0.0883417651

0.0215085931

0.0277496595

0.0362556949

0.0558875091

0.0657233745

0.0924525857

0.0176496431

0.0274696983

0.0367809012

0.0554565899

0.0625382215

0.0891506597

0.0205711424

0.0271105282

0.0349067748

0.0562575646

0.0653619021

0.0921486542

0.0182797145

0.027173575

0.0368178412

0.0546572693

0.063504912

0.0898981094

0.0195696875

0.0274896082

0.0352417678

0.0566263981

0.0638659522

0.0916027129

0.0198800154

0.0267390758

0.0368619934

0.0552304126

0.0656133443

0.092302531

0.0182526633

0.0280115772

0.0354685523

0.0560328551

0.0625283867

0.0899281353

0.0221372377

0.0278651826

0.0372781456

0.0566423237

0.0668998882

0.0950178876

0.0178943444

0.0274845343

0.0359681733

0.0552579313

0.0628458336

0.0904898941

0.0211441256

0.02820912

0.0357934907

0.0567090139

0.0657750219

0.0939264074

0.0192656685

0.0275331009

0.0377223902

0.0558570996

0.0643949136

0.0928684324

0.0196120404

0.0279256329

0.0350029767

0.0565877371

0.0644891337

0.0926445648

0.0210298337

0.0278981682

0.0378988385

0.0560812764

0.0661049858

0.0945993364

0.0190819409

0.0278460831

0.0359874368

0.0565442741

0.0636045188

0.0923363119

0.0216492414

0.0281850901

0.0370730795

0.0564379059

0.0669831485

0.0959578305

0.0185896102

0.0283851158

0.0366267338

0.0557738245

0.063447386

0.0924999192

0.0222206265

0.0284429304

0.0365378857

0.0576079115

0.066863291

0.0959338471

0.0184557829

0.027593147

0.0372070447

0.0551094934

0.0643960535

0.0937590375

0.0218004677

0.0298680738

0.0366287343

0.0580660626

0.0658725947

0.0956071839

0.0199178476

0.0273160711

0.0376848988

0.0558439121

0.0662138089

0.0961882249

0.0199330505

0.0288017373

0.0363360681

0.0570608452

0.064667128

0.09424036

0.0220545735

0.0291600674

0.0375525914

0.0570304096

0.0679106116

0.0982633606

0.0187192354

0.0275288262

0.0368792117

0.0560687259

0.0640241951

0.0941412523

0.0220273398

0.0293433163

0.0363775305

0.0580169447

0.0677704662

0.0983252972

0.0198625103

0.0285306629

0.0383781902

0.0560998619

0.0657651797

0.0966971144

0.0216973219

0.0292530377

0.0364614464

0.0586077906

0.0662908181

0.0971668363

0.0207717102

0.0288254432

0.0384242311

0.056553591

0.0679694265

0.0985829309

0.0201996788

0.0288907606

0.0364655256

0.0570297614

0.0649836212

0.09604498

0.0227321237

0.0294742249

0.0383595303

0.0580789037

0.0687904358

0.1003544256

0.0188375171

0.028194895

0.0367167294

0.0560641624

0.0651049167

0.0959592834

0.0229488388

0.0307759773

0.0379011854

0.0584858656

0.0686771423

0.1001683623

0.0192941353

0.0274782199

0.0376795605

0.0562371165

0.0662848502

0.0980800763

0.0224299729

0.030760806

0.0374135003

0.0590338707

0.0677993298

0.0992016792

0.0212408882

0.0293033253

0.0387663916

0.0568953231

0.068394579

0.1010048985

0.0207225382

0.029267963

0.0369825885

0.0583704598

0.0662026554

0.0983952954

0.0228517503

0.030592151

0.0388641879

0.0585523322

0.0698635504

0.1020407304

0.0196991991

0.0290066153

0.037545111

0.0569487102

0.06597922

0.0990945101

0.0232802182

0.0307375789

0.0377125367

0.0595180206

0.0694687218

0.1017681435

0.0200640541

0.0287345834

0.0387543887

0.0570006855

0.067966938

0.100917697

0.0224482901

0.0309951324

0.0369325876

0.0588076338

0.067719698

0.1006560549

0.0215381607

0.0294490699

0.0392688289

0.0578453839

0.069678247

0.103183724

0.0208740942

0.0299261417

0.0366174392

0.0581133179

0.0670106933

0.0996701792

0.0229090787

0.0310992878

0.0389306918

0.0589310974

0.0703516528

0.10438779

0.020270111

0.0289665181

0.0372760296

0.0574058704

0.0670758784

0.1009986922

0.0236581266

0.0321797878

0.0384291522

0.0604803003

0.0708527044

0.1042844653

0.0203400124

0.0289035421

0.0387703516

0.0569931306

0.0682537332

0.1029006019

0.0227678847

0.0310521014

0.0368275344

0.0602924414

0.0686859637

0.1030568555

0.0215836726

0.0302952249

0.0390346423

0.0577861816

0.0707474947

0.105002135

0.0209956821

0.0299112499

0.0369382836

0.0587720349

0.067190811

0.1025876701

0.0225048009

0.0308708809

0.0384697057

0.0590499155

0.0710655227

0.1056810096

0.0205317624

0.0295527987

0.0374659263

0.0581303053

0.0680574328

0.1031681597

0.0230891351

0.0315262042

0.0379411839

0.059864562

0.0699468032

0.1056158021

0.0209602006

0.0294217281

0.0386374891

0.058124505

0.0697727427

0.1051599756

0.023004951

0.0315634236

0.0372487269

0.0599831268

0.0695543289

0.1048469618

0.020866815

0.0297000688

0.0387604199

0.0577588566

0.0703781918

0.106640473

0.0223458074

0.0305602662

0.0369700454

0.0597237199

0.0685246214

0.1049652472

0.022098586

0.031328734

0.0386467129

0.0589638315

0.0717491731

0.1075143442

0.0207933802

0.0296780337

0.0377312005

0.0583595336

0.0684216395

0.1057765707

0.0238833726

0.0320376418

0.0381786823

0.0610690825

0.0713663623

0.1078236476

0.020209603

0.0292183179

0.0379683599

0.0572168604

0.0694244951

0.1067476347

0.0232592989

0.032125406

0.0377143733

0.0609739013

0.0699153915

0.1074834093

0.021671962

0.0306955706

0.0389756262

0.0593036972

0.0719445869

0.1096740663

0.0215258114

0.0301359333

0.0364483818

0.0586157292

0.0684645846

0.1060737669

0.0226488002

0.0322236679

0.0392309763

0.0605937652

0.0723065734

0.1108390838

0.0207830891

0.0284918807

0.0368368886

0.0579739325

0.0683817044

0.1067352518

0.0233918279

0.0323346443

0.0379787572

0.0603998527

0.0718382299

0.1099007502

0.0206964463

0.0297368523

0.0387857482

0.0582103618

0.0700758174

0.1098926514

0.0235354099

0.0312889218

0.0365744382

0.0607283674

0.0703780726

0.1090409309

0.0207659267

0.0308779124

0.0390644073

0.0582698882

0.0719091222

0.111212492

0.0225870889

0.0307322722

0.0369262211

0.0605980493

0.0694922954

0.1093630791

0.0226928182

0.0315640904

0.0387465209

0.0598072819

0.072580643

0.1121845022

0.020658819

0.0290798191

0.0371708907

0.0587116405

0.0694219768

0.1095527261

0.0240455586

0.0329333395

0.0386889055

0.0613937825

0.0722520575

0.1126425713

0.0201725066

0.0287442897

0.0374464281

0.0578580722

0.0706765801

0.1113874912

0.0234525874

0.0315852202

0.0370745994

0.0608482137

0.0708631575

0.1108458042

0.0212798994

0.0310035851

0.0390923358

0.0588220358

0.0722691789

0.113999173

0.0221570414

0.029490266

0.0358294472

0.0596339107

0.0693941861

0.1105602533

0.0224869996

0.0318789072

0.0389805809

0.0599156097

0.0731774345

0.1143440828

0.0211214349

0.0292413812

0.0375403166

0.0589011274

0.0697968453

0.1122381315

0.023288548

0.0319296084

0.0377025418

0.0606696345

0.0723648816

0.1135343984

0.0205959231

0.0292498264

0.0384772867

0.0582647659

0.0713326186

0.1140832901

0.0231477227

0.031227611

0.0370828323

0.0610637181

0.0710190311

0.1131856665

0.021042902

0.030351324

0.0384916551

0.0585646853

0.0725042894

0.115715757

0.0223799832

0.0300716795

0.0369542353

0.0599622056

0.0704437643

0.113293983

0.0227948111

0.0323061719

0.0393740237

0.0605507307

0.0735071152

0.1170392781

0.0214724448

0.0285753105

0.0365229063

0.058657147

0.0702661276

0.1140865907

0.0233336426

0.0322202668

0.0383295007

0.0611151159

0.0731078982

0.1164781451

0.0209373292

0.0293243732

0.0381536409

0.0585530437

0.0712644383

0.1160177067

0.0232188813

0.0306079276

0.0366036408

0.0607802048

0.0717953146

0.1153274924

0.0212292001

0.0308802463

0.0392498188

0.0589196235

0.073310785

0.1181866303

0.0224061217

0.0294304825

0.0363479741

0.0601594597

0.0705218911

0.1153215468

0.0223283395

0.031760864

0.0390078537

0.0599065758

0.0743205249

0.1186884269

0.0215182211

0.0290944055

0.0375959165

0.0594391786

0.0713958666

0.1171426624

0.0230791159

0.0320845172

0.0380407721

0.0612651445

0.073494792

0.1182946414

0.0212482009

0.0293960795

0.0380181707

0.0588732585

0.072587654

0.1189904064

0.0234004594

0.031583216

0.0373708978

0.0615544356

0.0728073791

0.1181320921

0.0218080077

0.0311531275

0.0392541252

0.0597348288

0.0740399808

0.121099472

0.0224204864

0.029345559

0.0365415215

0.0605416261

0.0717663392

0.1176921949

0.0227176398

0.0322902799

0.0395598225

0.060517434

0.0753009021

0.1213332266

0.0214792713

0.0287427139

0.0369976126

0.0596375614

0.071591638

0.1192681342

0.0236080252

0.0318731107

0.0381359495

0.0615366586

0.0747917071

0.1209386438

0.021141082

0.029445773

0.0385128409

0.0589727275

0.073376745

0.1214581132

0.0232621655

0.0309996922

0.0364345871

0.0614840165

0.0725516751

0.1203598455

0.0220825709

0.0314124599

0.0399235934

0.0603418462

0.0756356791

0.1237189472

0.0223943479

0.0295183025

0.0369069986

0.0606085882

0.0721175671

0.1203973144

0.0225056205

0.0326778442

0.0393762626

0.060814891

0.0761011094

0.1236122996

0.0227038376

0.0291761234

0.037791431

0.060560137

0.0734482855

0.1224845126

0.0230489802

0.0320518799

0.0383564197

0.0614768304

0.0755463392

0.123145096

0.0220866017

0.030359596

0.0387125611

0.0603979789

0.0745991543

0.1248339266

0.0233354457

0.0313488208

0.0375841483

0.0619420968

0.0747626796

0.1231255084

0.0220093932

0.0316569097

0.0401345268

0.0604669079

0.0762146264

0.1258665174

0.0229832269

0.0301569663

0.0368854403

0.0619282462

0.0735214651

0.1236538962

0.0233435854

0.0331540927

0.0403170697

0.0614395849

0.0779692158

0.1268452853

0.0221822392

0.0293098055

0.0378554538

0.0615057275

0.0742389783

0.1251396984

0.0239580162

0.0332921632

0.0390345864

0.0624751449

0.0772025436

0.126760751

0.0224561952

0.0308446176

0.0393944904

0.0614804998

0.0764318481

0.1272455901

0.0232783072

0.0312783234

0.0381824412

0.0622278377

0.0757689252

0.1259020418

0.0232085325

0.0331270732

0.040923439

0.0622470193

0.0785818398

0.1297174543

0.0239272434

0.0310543254

0.0385104939

0.0630610436

0.0761632621

0.1269052625

0.02272694

0.0334835947

0.0405296981

0.0622693338

0.0793489963

0.1298723519

0.0240085963

0.031184027

0.0389104485

0.0634963736

0.076065734

0.1293778419

0.0237290412

0.0337086804

0.0394736342

0.0627496615

0.079503566

0.1293984056

0.0233914722

0.0321726799

0.0407448188

0.0632229447

0.0778649673

0.1310017258

0.0241035912

0.0326333865

0.0386900343

0.0637084618

0.0780906975

0.1295971125

0.0239738543

0.0342214033

0.0418615863

0.0636415034

0.0810280964

0.1327082366

0.0233163256

0.0309887398

0.0390054174

0.0635532439

0.0770343021

0.1299574673

0.0249699559

0.0355022326

0.0416576229

0.0643099844

0.0819057599

0.1339596361

0.0233320035

0.0313489623

0.0397675708

0.0636039153

0.0776860639

0.131747067

0.0243012533

0.0346702449

0.0406820998

0.0638680235

0.0810876787

0.1328459978

0.0242096651

0.0339314192

0.0417553633

0.0652652904

0.0801208466

0.1350913048

0.024438018

0.0331100598

0.0396226905

0.0642074868

0.0807297453

0.1326275319

0.0238948334

0.0350716151

0.0428896509

0.064623177

0.0820774958

0.1363230646

0.0250137448

0.0327264368

0.0397162251

0.0655379072

0.0797266364

0.1340199709

0.0242330395

0.0356341116

0.0421011858

0.0647182018

0.0837388784

0.1366714239

0.0247127153

0.0329902284

0.0411841161

0.0656770915

0.0798511803

0.1361442804

0.0249639228

0.0356375687

0.04098434

0.065588057

0.0835996494

0.1367302835

0.0247864034

0.0344848186

0.0428712778

0.0656205714

0.0821005181

0.1379794478

0.0247423649

0.0336313658

0.0406163223

0.0656690821

0.0825116038

0.1365795881

0.0252733864

0.0365757607

0.0434670933

0.0668510273

0.0842826888

0.140210256

0.0250981264

0.033089444

0.040883448

0.0658942536

0.0821359158

0.1374678016

0.0253297184

0.0368526951

0.0435250066

0.0668187887

0.0860682949

0.1404676139

0.02544556

0.0340157598

0.0420104116

0.0670580268

0.0820780322

0.1398915201

0.0250400957

0.0363809913

0.0421246849

0.0664278343

0.0862796977

0.1402439624

0.0264812242

0.0363520831

0.04459887

0.068362765

0.0847150385

0.1431501657

0.0248675607

0.0346860848

0.0409366079

0.0667811409

0.08444006

0.1403114349

0.026079027

0.0374138951

0.0442093201

0.0679259822

0.0865511671

0.1439772695

0.026253501

0.0344313495

0.0426991992

0.0681108758

0.0844701156

0.142090112

0.0257035922

0.0378763862

0.0430187061

0.0676571354

0.0875516012

0.1441133618

0.0264168475

0.0352719463

0.0434706695

0.0689022392

0.0851349086

0.1438892186

0.025226526

0.0365247652

0.042867966

0.0675478578

0.0876782313

0.1436070055

0.0273340717

0.0372006148

0.0443553664

0.0700464621

0.0865611583

0.1465016454

0.0255548172

0.0351883732

0.042574551

0.0677033886

0.0876822546

0.1440403163

0.0269914046

0.0383494049

0.0450941771

0.069656454

0.0885476768

0.147678256

0.0263216756

0.0350168087

0.0425031185

0.0686247796

0.0861423984

0.145547837

0.0264393799

0.03868163

0.044423379

0.069458209

0.090610683

0.1478829235

0.02770162

0.0362831317

0.0448653251

0.0702941567

0.0870259851

0.1484150738

0.0258129425

0.0370845832

0.0425620154

0.0689840987

0.0899816006

0.1472854167

0.0280528571

0.0379769467

0.0457660444

0.0711676106

0.0888992474

0.1506695151

0.026263291

0.0359523408

0.0433293805

0.069411099

0.0894203037

0.1482399851

0.0284413006

0.0388792194

0.044962611

0.0712777078

0.0903567672

0.1512095481

0.0275272541

0.036213655

0.0447439849

0.0706230923

0.0896157548

0.1503032744

0.0279983524

0.0390557721

0.0449063703

0.0712972656

0.0919188634

0.1522549987

0.0289231315

0.0375608057

0.045839943

0.0723837241

0.089488849

0.1528936923

0.0270517338

0.0385646932

0.0447119921

0.0712811872

0.093135871

0.1523079723

0.029799616

0.039027337

0.0466950983

0.0731431842

0.0908125341

0.1552272588

0.0279999524

0.0379284695

0.0448178798

0.0718317553

0.0932771042

0.1531504691

0.0300753694

0.040258985

0.0469428822

0.0735037774

0.0932649374

0.1564560533

0.027733352

0.0369683281

0.0451306514

0.0720010176

0.0915948823

0.1547168791

0.0300740637

0.0412162803

0.0462146588

0.0738894343

0.0953292772

0.157390222

0.0300173629

0.0388037525

0.0477345921

0.0743430704

0.0928897783

0.1581119448

0.0283942632

0.0392391644

0.0451199375

0.0727647394

0.0954424217

0.1567387581

0.0316596106

0.0411579646

0.0481886864

0.0765017047

0.0945205241

0.1605974883

0.028585013

0.0382464938

0.0462300628

0.0724450424

0.0958967209

0.1576271653

0.0311526265

0.0413275287

0.0474796258

0.07661286

0.0954072401

0.1614559889

0.0301080774

0.0389630832

0.0471052006

0.0742332339

0.0957400203

0.1600443274

0.0304830913

0.0415619873

0.0476769842

0.0755851865

0.0973554701

0.1618371755

0.0309670828

0.0395603031

0.048703894

0.0761345774

0.0957903639

0.1628648639

0.030512305

0.0414542668

0.0470222309

0.0753508061

0.0990528166

0.1622496843

0.0321998894

0.0416640341

0.0494166389

0.07773491

0.0971665159

0.1646973938

0.0296379291

0.039413169

0.0469322689

0.0753532127

0.0981197879

0.1632961035

0.0335290059

0.0438385643

0.049761828

0.0787328407

0.0997929275

0.1669431031

0.03009809

0.0391496383

0.0482592955

0.0760059059

0.0983449668

0.1647882611

0.0321205817

0.0426314846

0.0488397852

0.078206256

0.1000351459

0.1671643555

0.0324900597

0.0415568873

0.0494075902

0.0779300332

0.0994608775

0.167761296

0.030247543

0.040485397

0.0481250323

0.0768937394

0.1010592878

0.1660653204

0.0335661136

0.0423614047

0.0500463135

0.0795455649

0.0995092168

0.1700211763

0.0305397138

0.0401552245

0.0482081845

0.0766374692

0.1015622765

0.1674840003

0.033732459

0.0434347652

0.0502536483

0.0802384093

0.1013705656

0.1711654514

0.0318117477

0.0412510633

0.0498381518

0.0779032111

0.101430133

0.1707951725

0.0333806276

0.0432022661

0.0493351705

0.0801360682

0.1032571942

0.171257019

0.0324843675

0.0420882367

0.0512689911

0.0798160955

0.1022335291

0.1726950705

0.0322254822

0.042353753

0.0490907095

0.079354465

0.1039756685

0.171845004

0.0343138427

0.0429997295

0.0505339764

0.0811640322

0.1028508693

0.1745842695

0.0309355035

0.0409734994

0.0495644212

0.0785034299

0.1042860821

0.1724676341

0.0350084752

0.0441971421

0.0508935601

0.0829237625

0.1042547822

0.17633228

0.0311718434

0.0409436896

0.0495708622

0.0780772194

0.1040746048

0.1741330922

0.0334491208

0.043230202

0.0499623157

0.0822614133

0.1056017056

0.1757653654

0.0338563882

0.0430583209

0.0517241172

0.0814411342

0.1052526534

0.1780044734

0.0320123658

0.0418573394

0.0491459854

0.0801206604

0.1066710129

0.1754311919

0.0344834998

0.0433954857

0.0512915961

0.083110109

0.105592005

0.1793951243

0.0321024917

0.0416369401

0.0503240116

0.0805140138

0.1074645445

0.1774719507

0.0341183171

0.0438389368

0.0503515676

0.0832042471

0.106532447

0.1797287166

0.0319749154

0.0417251848

0.051364664

0.0809148028

0.1078548357

0.1793819368

0.0344283246

0.0435851589

0.0504104607

0.0835746452

0.1081340984

0.1807301342

0.0330145284

0.0430979393

0.0516461507

0.0829437524

0.1082003787

0.1817357987

0.0329821557

0.0424525626

0.0503888615

0.0824731663

0.1093598828

0.1809235811

0.0350259282

0.0440909714

0.0516672581

0.0847722441

0.108635284

0.1846158952

0.0315393992

0.0417867117

0.0501002297

0.0815457776

0.1098113135

0.1815799326

0.0352508053

0.0445389487

0.0517858528

0.0858848095

0.1100148559

0.1850457937

0.0322283246

0.0428532511

0.0515170433

0.0826122835

0.1109435782

0.1844771653

0.0342541188

0.0430820733

0.0503422953

0.0848607272

0.1109583825

0.1845655292

0.0339596607

0.0442047343

0.0530437194

0.0855671614

0.1124227941

0.1877634525

0.0330499187

0.0418871567

0.0499338284

0.0836343616

0.1116242111

0.1852576733

0.0352857038

0.0454720147

0.0525049977

0.086834386

0.1127623618

0.1897767186

0.0320312306

0.0418133326

0.0511124805

0.0841073766

0.1133662984

0.1872404069

0.0362751111

0.0456793047

0.0519351996

0.0879299715

0.1135808304

0.1910487413

0.0320976153

0.0428158827

0.0519447103

0.0844597742

0.1147633716

0.1891965419

0.0358455554

0.0447307564

0.0518520623

0.0885446668

0.1149810925

0.191403687

0.0341773219

0.0448021255

0.0528659523

0.08711683

0.1153826267

0.1927874833

0.0337706208

0.0428305939

0.0513194762

0.0867133439

0.1160646081

0.191223681

0.0356720202

0.0455686636

0.0529353954

0.0891504958

0.1160199717

0.1951057613

0.0328558274

0.0425241291

0.0515375026

0.086018905

0.1169722453

0.1928564906

0.0367470682

0.0466029532

0.0530969836

0.0906949788

0.1181964874

0.1968017071

0.0328992754

0.0434707254

0.0530736707

0.0870028287

0.1182086468

0.1954101175

0.0365969949

0.0447732545

0.0524640419

0.0905604511

0.1188994125

0.1970769465

0.0338992626

0.0457006134

0.0533437692

0.0891319364

0.1199857667

0.1986207366

0.0344920754

0.0431201234

0.0525590144

0.0893653482

0.1195935905

0.197290659

0.035809543

0.0463014208

0.0528560691

0.0911716968

0.1203051731

0.2008921951

0.0331554301

0.0439226441

0.0531803593

0.0887784958

0.1219912022

0.1995779872

0.036554981

0.0458847657

0.0529914834

0.0930843279

0.1209083796

0.2023147494

0.0333485641

0.0445873961

0.0535578355

0.0894330591

0.1228071377

0.2019283175

0.0364784487

0.0457756221

0.0531176068

0.0935424864

0.1229997277

0.2032119781

0.0344223268

0.0454311743

0.0538210571

0.0914519951

0.1230019629

0.2052371204

0.0353618264

0.0443796813

0.0527749471

0.0922685638

0.1241477281

0.2038139254

0.0365987979

0.047554709

0.0545584895

0.0944525003

0.125644207

0.2080340087

0.0337754637

0.0438402817

0.0535095222

0.0914443582

0.1256049722

0.2055419385

0.037514858

0.0473462381

0.053866595

0.0957471505

0.1259600222

0.2093515098

0.0339520201

0.0453534648

0.05467638

0.092309542

0.1274392605

0.2088247687

0.0368280113

0.045451723

0.0533275828

0.0962245986

0.1267767251

0.2094249576

0.0352848619

0.0470022149

0.0549047962

0.0939371362

0.128066957

0.2125790268

0.0360999405

0.0450593419

0.0543613248

0.095593214

0.1294115931

0.2107034624

0.0364029482

0.0476894937

0.0546804331

0.0966097042

0.1292847395

0.2149847597

0.034905035

0.0449547134

0.0545586944

0.0949621573

0.1303644031

0.2130291611

0.0375582948

0.0477941446

0.054886464

0.0981247872

0.1312481016

0.2161075026

0.0344652012

0.0452203564

0.0549841113

0.0953270867

0.1309567988

0.2163901776

0.0379917808

0.0474226549

0.0547703095

0.0988826901

0.1327349544

0.2172816098

0.035355594

0.0472943932

0.0553721562

0.096741654

0.1329673231

0.2192222774

0.036784254

0.0450085476

0.054799851

0.0981362686

0.1331419796

0.2179863453

0.0377380066

0.0494769178

0.0559272878

0.0996699184

0.1352564692

0.2230722308

0.0353670493

0.045275256

0.0558333732

0.0978382677

0.1352489144

0.2203307152

0.0387538225

0.0479027256

0.056209065

0.1013964564

0.1364128143

0.2238194495

0.0353227966

0.0469058528

0.0561417788

0.0986601189

0.137196511

0.2244885266

0.0384419337

0.0467902571

0.0562278032

0.1019400954

0.1378662437

0.22408472

0.0363634825

0.0480834469

0.0563162342

0.0999809802

0.1384673715

0.2280563414

0.0370873734

0.0461157672

0.0559547879

0.1010514125

0.1390044689

0.2259023488

0.037486583

0.0496153161

0.057093937

0.1020869985

0.1403492391

0.2302302867

0.0365818143

0.0458540395

0.0570786744

0.1015298367

0.1409746855

0.2289745212

0.0391099267

0.0495426878

0.0567931458

0.1039032191

0.1420577615

0.2319033146

0.0359270908

0.0472123399

0.0574926511

0.1017051265

0.1427724808

0.2323002666

0.0393966138

0.047749415

0.0567861535

0.1048955023

0.1437316537

0.2327008992

0.0369290672

0.0493067801

0.0577491596

0.1029887944

0.1445338726

0.2362546772

0.0382609963

0.0469814725

0.0574383698

0.1046385765

0.1461582929

0.2344814986

0.0393405259

0.0503524952

0.0580479838

0.1056562811

0.1465219259

0.2393410355

0.0371339805

0.0469062589

0.0579008087

0.1040205285

0.1474452615

0.237543121

0.039554663

0.0489136837

0.0577137694

0.1063116714

0.1480122209

0.2398798615

0.0375111625

0.0485405996

0.058530204

0.1056259423

0.149598971

0.2415284812

0.0394525975

0.048123382

0.0578971095

0.1072754115

0.1498893499

0.2414369434

0.0378438756

0.0498301648

0.0587355532

0.1058525369

0.1514980644

0.2446530461

0.0398803465

0.0477625057

0.0595160015

0.1084540412

0.1527103037

0.2440104485

0.0390603878

0.0507221669

0.0583939142

0.1079474613

0.1536680013

0.2480585426

0.0384042077

0.0477869213

0.0601588078

0.1079805195

0.15500471

0.2468549162

0.0406760164

0.0500301048

0.058796104

0.1096896306

0.1551590562

0.2493839115

0.0378373526

0.0492216498

0.059405636

0.1078204289

0.1567445546

0.251029253

0.0405744575

0.0490965955

0.0597544312

0.110428378

0.157911703

0.2509521246

0.0394442342

0.0506104939

0.0600153133

0.1098071486

0.1590992212

0.2554274797

0.0396484397

0.048039265

0.0601917505

0.1106249988

0.1603599638

0.2533415556

0.0403142571

0.0518749319

0.0604710467

0.111730665

0.1618780196

0.2578961253

0.0395813435

0.048015587

0.0607178286

0.1111835688

0.1624550819

0.2573491037

0.040529754

0.0508889593

0.0602781959

0.1122606248

0.1637316346

0.2588905394

0.0395525619

0.0501029305

0.0610610656

0.1117942482

0.1654631644

0.2616387606

0.0414750837

0.0498166941

0.0614678823

0.1138090938

0.1659020036

0.2614023387

0.0397535264

0.0518946797

0.0605813265

0.1124275923

0.1680436879

0.265966773

0.0413545482

0.0493718572

0.0620496161

0.1146411672

0.1691610366

0.2634245157

0.0409292691

0.0517727584

0.0614149533

0.1144150272

0.1697587371

0.2689459324

0.0403209329

0.0501588285

0.0616006702

0.1140535697

0.1719143391

0.2673794329

0.0421527252

0.0514578223

0.0621735901

0.1159975231

0.1732019484

0.2704018652

0.0406678021

0.051293198

0.0623315126

0.115156807

0.1743091643

0.272746563

0.0422172248

0.0508218817

0.0621619709

0.1161513552

0.176002413

0.2722323835

0.040866524

0.0527794771

0.062959291

0.116492562

0.1774284393

0.2767679691

0.0418676883

0.0498327203

0.0627702102

0.1171776503

0.1782903671

0.275049448

0.0416416414

0.0531914197

0.0626314133

0.1172840148

0.1800071895

0.2800026834

0.0417870246

0.0510536917

0.0636107176

0.1183701381

0.182021752

0.2794111669

0.0425001495

0.0523668714

0.0630154908

0.1184528247

0.1824249327

0.2821358442

0.0417576134

0.0527279749

0.0635714307

0.1186943129

0.1848968565

0.2843053341

0.042630516

0.0516389795

0.0647118613

0.120013237

0.1864502579

0.2844404578

0.042103637

0.0537484549

0.0635754466

0.1199583635

0.1875495464

0.2890344262

0.042404525

0.0505874902

0.0642980114

0.1203000844

0.1891368479

0.2865114808

0.0426483042

0.0542495921

0.0644528344

0.1210773364

0.1911089867

0.2928434312

0.0426081009

0.0513392873

0.064368315

0.1218197271

0.1926033646

0.2915477157

0.0436528474

0.0540241599

0.0652544946

0.1221454293

0.1941497624

0.2947971821

0.0425130799

0.0534040965

0.0649522021

0.1226842329

0.1963770688

0.2970428765

0.0438275971

0.0523782931

0.0657210276

0.1234551445

0.1971669644

0.296895802

0.0428939089

0.0549684837

0.0652703717

0.1238112599

0.2001943737

0.3016732633

0.0431948043

0.0515303649

0.065988563

0.1245164797

0.2008097768

0.2997528017

0.0428035967

0.0548973642

0.0652268156

0.1245117933

0.2020208091

0.3051802814

0.0440008417

0.05323736

0.0664007738

0.1257699877

0.2053205967

0.3049887121

0.0428228229

0.0533385016

0.0658266842

0.125078097

0.2050809413

0.3069388866

0.0447010584

0.055860512

0.0668940321

0.1277391165

0.2092789412

0.3114247024

0.0435227454

0.0530375764

0.0667094141

0.1268586069

0.2092973441

0.3092782199

0.0440550446

0.0556038804

0.066536434

0.1279665977

0.2121497393

0.315230161

0.0444698595

0.0533467233

0.067016311

0.1286339164

0.2130631953

0.3132872581

0.0445585661

0.0565541834

0.067769222

0.1289421916

0.2159943879

0.3192927241

0.04427341

0.0533417501

0.0668696016

0.1291655749

0.2171188593

0.3179167509

0.0459154658

0.0568552799

0.0689559728

0.132372871

0.2260634154

0.3294987977

0.0457927957

0.0566089712

0.0698209852

0.1303785443

0.2258324176

0.3313527703

0.0477565527

0.0592843816

0.0706195608

0.1339781135

0.2305431813

0.3355103731

0.0459915735

0.0567341447

0.0693809092

0.1326302141

0.2314931452

0.3363513052

0.048298467

0.0596426688

0.0719214603

0.1340088397

0.2343128324

0.3411184251

0.0462917127

0.0576074943

0.0702216402

0.1356833875

0.237446636

0.3414307535

0.0488540083

0.0591483265

0.0721721202

0.1341108084

0.2381347716

0.3456197977

0.0471463725

0.0591854341

0.0717248395

0.138044104

0.2434748113

0.3478105366

0.0483050905

0.0588790104

0.0720577314

0.1356987804

0.2426541448

0.3498062789

0.0487919338

0.0602515228

0.073515825

0.1387054622

0.2476596683

0.3548618853

0.0472626425

0.0585989617

0.071779497

0.1380022466

0.248949796

0.3540771306

0.0503094792

0.0615039393

0.0746966973

0.1393996924

0.251781702

0.3605329692

0.0481009707

0.0589835793

0.0723416433

0.141247198

0.2557248175

0.3607119918

0.049876824

0.0611949526

0.0747055486

0.1400675625

0.2561188042

0.3652707338

0.049989529

0.0615586117

0.0751470849

0.1444584578

0.262388885

0.3683373928

0.0492080823

0.0600056536

0.0737903267

0.1408329904

0.2616900504

0.369633466

0.0507560037

0.0624803454

0.0766125545

0.1451445222

0.2674603164

0.3753267229

0.0489735156

0.0602761768

0.074494265

0.1442405283

0.2682781518

0.3751422465

0.0516870581

0.0622754581

0.076890558

0.1448359936

0.271589458

0.3811710477

0.0497327112

0.0616244152

0.075616084

0.1483374834

0.2763582766

0.3817974925

0.0521714017

0.063200213

0.0777249113

0.1461467594

0.2762274146

0.3863571584

0.0513019376

0.0627170578

0.077259317

0.15032655

0.2825929821

0.3899860978

0.0508707427

0.0628037378

0.0776603371

0.1480965614

0.2825553715

0.3911240101

0.0527707078

0.0645006671

0.0796464905

0.1516189426

0.2884916961

0.3977090716

0.050847549

0.0617880486

0.0769881234

0.151075989

0.2895601094

0.3972821832

0.0536381677

0.0654370114

0.0808354095

0.1526502967

0.2939430773

0.4041189253

0.0518965758

0.0632414445

0.0786650479

0.1549131721

0.297875464

0.404586792

0.0538686141

0.0648407489

0.0804575607

0.1535363346

0.2985391617

0.4099453986

0.0531795137

0.0651113167

0.0809824243

0.1581034064

0.3058332205

0.4133262634

0.0536251068

0.0650973394

0.0806048214

0.1550444365

0.3052071631

0.4153951108

0.053950645

0.065531373

0.0818702877

0.1586619318

0.3112125397

0.4211732447

0.0534150451

0.0649729148

0.0809770301

0.1592851281

0.3133702874

0.4212094545

0.0554250032

0.0665881559

0.0835515782

0.1593564898

0.3163862526

0.428172797

0.0543676615

0.0661245138

0.08232674

0.1630077809

0.3224253356

0.4296704829

0.0551916994

0.0670628026

0.0843013302

0.1611196548

0.322751224

0.4340897501

0.0551941395

0.0669542775

0.0843217298

0.1655039042

0.3297544718

0.4380532205

0.0551299192

0.0665831715

0.0832980648

0.1632051766

0.330332607

0.4408475757

0.0557871275

0.0677468628

0.0861985609

0.1671946347

0.3365450799

0.446135968

0.0557030737

0.0671409294

0.084163554

0.1673762053

0.3388997912

0.4478362501

0.0567896329

0.0681500584

0.0868627131

0.1679693162

0.3425213695

0.4543828666

0.0558822975

0.0682985708

0.0858090147

0.1717372388

0.348304987

0.4560108483

0.0572877973

0.0683352575

0.0873030499

0.1692257077

0.3484934866

0.460529685

0.056810759

0.0693058446

0.0875231028

0.1744077057

0.3565343022

0.4651997685

0.0566567779

0.0692152157

0.0871342942

0.1723614782

0.3572546542

0.4671972394

0.0581269897

0.0698832497

0.0897108689

0.1762896627

0.3632347286

0.4738537669

0.0573211461

0.0698418692

0.0878396183

0.1768848598

0.3669307828

0.475174427

0.0585405417

0.0710505247

0.0907944441

0.1772824079

0.370193243

0.4817897677

0.0580516793

0.0705131516

0.089753963

0.181222707

0.3763512671

0.483869493

0.0592845268

0.0711453483

0.0908246636

0.1790437102

0.3771943748

0.4893352091

0.0583100021

0.0716700032

0.0914518014

0.1844842881

0.3853028715

0.4934122562

0.0601492934

0.0721385032

0.0916805565

0.1832843721

0.3861640394

0.4963774681

0.0593802892

0.0716266781

0.0933077112

0.1854580194

0.3927264214

0.5029436946

0.0595695041

0.0731518269

0.0918538049

0.1879070997

0.396232307

0.5040969849

0.061119765

0.073397249

0.0952361152

0.1880555153

0.4000912905

0.5114327073

0.0603445806

0.0735212192

0.0937136561

0.1923469156

0.4066756368

0.5139245391

0.0607575439

0.0740910918

0.0949238613

0.1902210265

0.4074888825

0.5186707973

0.061255306

0.0742082372

0.096452713

0.1952519417

0.4156734347

0.5235292315

0.0617595762

0.0744119138

0.0950140581

0.1944210082

0.4170594215

0.5265910625

0.0611408614

0.0750986189

0.0979362726

0.1973206699

0.4239115417

0.5330215096

0.0630097166

0.0757687762

0.097044602

0.2002387047

0.4282563031

0.5356442928

0.06243103

0.0749803409

0.0989182815

0.1991846114

0.4313557744

0.5422428846

0.062042091

0.0765127912

0.0985237881

0.2044409662

0.4384687245

0.5447039008

0.0641848594

0.0767398849

0.1005838066

0.2032397538

0.4404504895

0.5513410568

0.0633703768

0.0766907483

0.1002765149

0.2077074349

0.4485105276

0.5550444126

0.0643276647

0.0781483278

0.1005775407

0.2078237534

0.450555414

0.5586601496

0.0641118512

0.077913776

0.1029767543

0.2106477469

0.4570302069

0.5656497478

0.0656007603

0.0789644569

0.1016466022

0.213657245

0.4621553123

0.5679972768

0.0646931156

0.0788004994

0.1046833396

0.213516742

0.4654993713

0.5743634701

0.0663329139

0.0802038759

0.1043423638

0.2186875045

0.4731969237

0.5784851313

0.0656720325

0.0793105885

0.1044331565

0.2167079598

0.4742285609

0.5831122398

0.0662818924

0.0808077529

0.106885545

0.2227740139

0.4840612411

0.5884659886

0.0680425316

0.082183741

0.1065144837

0.2234602273

0.4859516621

0.5937401056

0.0658458695

0.0802726671

0.1079694331

0.2249196768

0.4920954108

0.5979543924

0.0693097636

0.0837037861

0.108567141

0.2300355732

0.4983640611

0.6027578115

0.0670386329

0.0816205591

0.1097970158

0.228468135

0.5006501079

0.6080673337

0.0693536699

0.0841588453

0.1097988486

0.2340521961

0.5089440942

0.6122597456

0.0688912868

0.0842199922

0.1116786376

0.2339743376

0.5110362172

0.6177094579

0.0691022947

0.083903119

0.1120716333

0.2386575788

0.5190368891

0.6222110987

0.0706789195

0.0855827033

0.1124819219

0.23953031

0.522071898

0.627341032

0.0696267039

0.0847998038

0.1151181981

0.2429650575

0.5298604965

0.6330105066

0.0723828301

0.0872246325

0.1146267131

0.2463398129

0.5343217254

0.6370753646

0.070356518

0.0854065791

0.1163305566

0.2459972352

0.5378926396

0.6431342959

0.0726551786

0.0887827799

0.1172448844

0.2528514266

0.5471898913

0.64666605

0.0724573359

0.0874776319

0.1179468185

0.25163728

0.5482658744

0.6530386806

0.0723297149

0.0885926858

0.1190893501

0.2572751641

0.5578634143

0.6571797132

0.0748024061

0.0905731171

0.1205132529

0.2593772411

0.5608130097

0.6625004411

0.0725626275

0.0880497322

0.1216036901

0.2610394359

0.5665903687

0.6674892902

0.0756093711

0.0917417481

0.1214730069

0.2653146088

0.572548449

0.6717807651

0.0735120848

0.0902300924

0.124132432

0.2662844658

0.5769452453

0.6780295968

0.0762833133

0.0922557265

0.1238591149

0.2721721232

0.5845518708

0.6817977428

0.0759977922

0.0925325975

0.1259328872

0.2721947432

0.5881310701

0.6886609197

0.0756556764

0.0929629132

0.1268416494

0.2779155672

0.5961956978

0.6916860342

0.0787480771

0.0940522328

0.127824232

0.2799099088

0.5994814038

0.698671639

0.0765531138

0.0939057395

0.1296104789

0.2829600275

0.6066197157

0.7025143504

0.0793247297

0.0963135213

0.1302968115

0.2873730958

0.6118647456

0.7078663707

0.0776776373

0.0944771469

0.1321130693

0.2882309854

0.6166974306

0.7127610445

0.0804932341

0.0978266224

0.1323427558

0.2945730984

0.62506181

0.7172901034

0.0792866349

0.0967235416

0.134475708

0.2949953377

0.6273655295

0.723126173

0.0800832436

0.0971015096

0.1349848211

0.3006530106

0.6356108785

0.7262516618

0.082426466

0.0998875648

0.1366935521

0.3030629456

0.6395602226

0.7339975834

0.0799588412

0.09802109

0.1380673647

0.3059290051

0.6461598873

0.7360665202

0.0840396136

0.101767458

0.1391631067

0.3112360835

0.6523846984

0.7431736588

0.0811850652

0.0994881839

0.140373975

0.3122305572

0.6566879153

0.747747004

0.0844271034

0.1027590632

0.1419104487

0.3194027543

0.665391624

0.751768291

0.0836108848

0.1014780328

0.1432558894

0.3194346428

0.6679585576

0.7583915591

0.0845877305

0.1031467542

0.14460361

0.3264541328

0.6766806245

0.761244297

0.0861948356

0.104430519

0.1459253132

0.3279985785

0.6799369454

0.7678111792

0.0846423358

0.1038002446

0.1479533613

0.3323617876

0.6866905689

0.771302402

0.0883282498

0.1073876396

0.1484902799

0.3373121023

0.6930521131

0.7775942683

0.0853089318

0.104548566

0.1513690352

0.3393332064

0.6977683902

0.7809778452

0.0894100964

0.1085946262

0.1515388638

0.3458815813

0.7055023313

0.7864522338

0.0877529904

0.1068064198

0.1537192613

0.3469446003

0.709048748

0.7923872471

0.088601768

0.1082485393

0.1553608328

0.3542402089

0.7173720002

0.7943978906

0.0906785205

0.1100967675

0.1563951224

0.3561810255

0.7207036018

0.8026754856

0.0883783773

0.1092208177

0.1584114879

0.3613474667

0.7285799384

0.8040952086

0.0928258896

0.1128075346

0.1600737423

0.3666019142

0.7341883779

0.8116174936

0.089911893

0.1105431542

0.1615954787

0.3685680926

0.7386555076

0.8144180179

0.0940531343

0.1142429858

0.163374126

0.3761849701

0.7469783425

0.819740355

0.0920321122

0.1130426824

0.1652057469

0.3780050576

0.7500454783

0.8240653872

0.0940523297

0.11462944

0.1668531895

0.3845854998

0.7584970593

0.8275126815

0.0948083401

0.1159590781

0.1681747437

0.3873878121

0.7616334558

0.8339146972

0.0932412967

0.1144463569

0.1704424173

0.3929710388

0.7691892982

0.83502388

0.0982367769

0.1196311638

0.1723167449

0.3984951973

0.7755038738

0.84401685

0.0944782421

0.1164994314

0.1736757159

0.4018361568

0.7802260518

0.8454928994

0.0990659222

0.1205830947

0.176562652

0.409419924

0.7886732221

0.8507646918

0.0973521024

0.1192710251

0.1777533442

0.4111828208

0.7907109261

0.8553795218

0.0982469693

0.1210120395

0.1790473461

0.4181369543

0.7988612652

0.8575264215

0.1003513634

0.1228368506

0.1822836697

0.4227921665

0.8033488989

0.8647631407

0.0989288464

0.1218851879

0.1835941076

0.4276282191

0.809322238

0.8647503257

0.1025829539

0.1257194281

0.1850740612

0.4333896637

0.8159844279

0.8725534081

0.1002524197

0.1236642897

0.1888109744

0.4383968711

0.8202933073

0.8742836714

0.1041680723

0.1272691935

0.1889860183

0.4445302486

0.8268550038

0.8784686327

0.1022623852

0.1261716634

0.1921801418

0.4481909275

0.8304218054

0.8831911683

0.1048304215

0.1286858171

0.1948430091

0.4560026824

0.8388442397

0.8853884339

0.1053486839

0.1296391636

0.1958857924

0.4593156576

0.841624558

0.8909347057

0.1046692729

0.1294641495

0.1994225532

0.4665276706

0.8491411209

0.8921787739

0.1086170003

0.1332684457

0.2012277097

0.4724474549

0.8544723392

0.8992422819

0.1057970524

0.1309556663

0.2035461068

0.4770957828

0.8577577472

0.8990405798

0.1099368259

0.1348901391

0.2053254098

0.4844124019

0.8662145138

0.90514642

0.1084434092

0.1343987286

0.2093081176

0.4889921546

0.8688448668

0.9077214599

0.1100572124

0.1356590837

0.209442392

0.4950606525

0.8752843142

0.9088408351

0.1122247875

0.1382143497

0.2142992467

0.5015377998

0.8805883527

0.9161911607

0.110772565

0.1372295618

0.2162338495

0.5086275339

0.8861382604

0.9148856997

0.1149943471

0.1417247206

0.2183185965

0.5141952634

0.8919087052

0.9228386879

0.1124649197

0.1397953182

0.2221213132

0.5210508108

0.8956471682

0.9222621918

0.1164840311

0.1436996162

0.2244997174

0.5278994441

0.9031713605

0.9274045825

0.1148004606

0.1430542171

0.2271383852

0.5326562524

0.9054919481

0.9293711782

0.1175248921

0.1458212882

0.2302815318

0.5418379307

0.913615346

0.9327445626

0.1181465983

0.146716103

0.233101353

0.5466725826

0.917771399

0.9374125004

0.118417263

0.1473583579

0.2359342575

0.554269731

0.9226663113

0.9374366403

0.1212507784

0.1509982049

0.2391199619

0.5615603328

0.9296098948

0.9454391599

0.1193281636

0.1491043717

0.2424334139

0.567653358

0.9317840934

0.9423282146

0.1237170175

0.1538831145

0.244629398

0.5746920109

0.9397949576

0.9497552514

0.1228368506

0.1537436694

0.2501412332

0.5830463767

0.9442415833

0.9525597692

0.1244429722

0.1560621411

0.2513843179

0.5899643898

0.9503395557

0.9534567595

0.126324147

0.1578268111

0.2559287548

0.5966150165

0.9551231861

0.959816277

0.1254324764

0.1578340679

0.2588013411

0.6055383682

0.9602577686

0.9592418075

0.129191637

0.1617389917

0.2629569173

0.6117939353

0.9665575624

0.9662078619

0.1278320104

0.160996154

0.2664532959

0.6195319891

0.9695192575

0.9649262428

0.1318084598

0.1648338437

0.2698364556

0.6278797388

0.9787639976

0.9716488123

0.1305550784

0.1647986621

0.2750052512

0.6347492337

0.9802313447

0.9722033143

0.1332439929

0.1677339077

0.277013123

0.6433045864

0.9875546694

0.9751030207

0.1348190904

0.1696141213

0.2824428976

0.6511793733

0.9927946329

0.9804052114

0.1341036558

0.1700563282

0.2858826816

0.6593210697

0.9970682263

0.9785959721

0.1387579143

0.1745261997

0.2901519239

0.6668660641

1.003928661

0.9857177734

0.1361587197

0.1733258218

0.2948643267

0.6756740808

1.006558657

0.9840660095

0.1407927871

0.177864328

0.2981565595

0.6831086278

1.013806105

0.9892837405

0.1405860335

0.1791534722

0.3044697344

0.6923884153

1.016373992

0.9908961654

0.1428176463

0.1811737567

0.3069387674

0.7005649209

1.022813916

0.9921090603

0.1441093534

0.1833723336

0.3133740425

0.7083262205

1.026186824

0.9956565499

0.1450554729

0.1851883978

0.3169155717

0.7174673676

1.029828429

0.9944312572

0.1475209147

0.1878530085

0.3212622404

0.7239003778

1.035241246

0.9998377562

0.1470529586

0.188422516

0.3277073205

0.7329797149

1.036686063

0.9963595867

0.1513976902

0.1930493563

0.3306426704

0.7406049371

1.042888165

1.001311898

0.1501505077

0.1927888542

0.3377272487

0.7497310042

1.043769836

1.000543118

0.1539373398

0.1971754432

0.3407458961

0.7570797801

1.049038053

1.000952601

0.1546087116

0.1986955851

0.3476005793

0.7652646303

1.050744772

1.003545165

0.1561194211

0.2011691332

0.3520925939

0.7747312784

1.054383636

1.00097847

0.1590165198

0.2046396285

0.3581024706

0.780926466

1.058048368

1.004607677

0.1594552845

0.2061368078

0.3639572263

0.7910397053

1.059215546

1.001766205

0.1620135009

0.2091319859

0.3680289984

0.7972675562

1.064297318

1.004649997

0.1633661985

0.2115345746

0.37671417

0.8071607351

1.065841675

1.003993154

0.1652069092

0.21449022

0.3786381781

0.8133242726

1.068227053

1.003461003

0.1666947603

0.2165619135

0.3876191974

0.8226456046

1.071669579

1.00587678

0.1684917808

0.2193016559

0.3923774958

0.8305777311

1.073403478

1.002144814

0.1715629399

0.223054409

0.3987001181

0.8381433487

1.076684952

1.007173896

0.1720045209

0.2248003781

0.4060626924

0.8487046361

1.079538465

1.003892541

0.1757141501

0.2292654812

0.4114616513

0.8547256589

1.08442235

1.006244302

0.1761866212

0.2311607152

0.4200609624

0.8651655316

1.084397078

1.006233335

0.1795207709

0.2354485095

0.4245830178

0.8722150922

1.090144277

1.006203175

0.1818449348

0.2387233227

0.4349671602

0.8823294044

1.092837691

1.008749485

0.1833293885

0.2410167754

0.4392668009

0.8893505335

1.094300032

1.005154133

0.1867349148

0.2458004802

0.4481619895

0.8982739449

1.100185275

1.009661674

0.188192755

0.2484549433

0.4561396241

0.9075249434

1.101225853

1.006640196

0.19121629

0.2525059581

0.4612654746

0.9132201672

1.105788708

1.008616447

0.192975238

0.256064117

0.4727832973

0.9258913994

1.107533455

1.009639025

0.1966967434

0.2604880929

0.4779832363

0.9308621287

1.112250924

1.007668138

0.1975914836

0.2628588378

0.4876793921

0.9402144551

1.112769008

1.010032177

0.201131776

0.2674970925

0.494459331

0.9489406347

1.116450787

1.006931067

0.2039268613

0.2721725702

0.5045588613

0.9558693767

1.120395303

1.010255814

0.2063640952

0.2755298913

0.51238662

0.9667984843

1.120598316

1.007092118

0.2096721381

0.28107059

0.5209982991

0.9715896249

1.126665354

1.008879662

0.2119767517

0.2845902145

0.5318155289

0.9827024341

1.12571013

1.00807631

0.2153272182

0.2894200981

0.5371006131

0.9878094196

1.129252553

1.005448818

0.2180424929

0.293952167

0.550327003

0.9985793829

1.132581592

1.008596897

0.2213489413

0.2988690734

0.5568163991

1.003589988

1.133016944

1.003955126

0.2243558466

0.304124862

0.5677027702

1.011757851

1.136623979

1.007427931

0.2276325524

0.3086942434

0.5778204203

1.02103579

1.137784123

1.003647923

0.2308048755

0.3140780926

0.5858976841

1.024536371

1.140361071

1.003679991

0.2341327965

0.3192391396

0.5986320972

1.036451817

1.140478492

1.003009796

0.2380585819

0.3246313632

0.605353117

1.039593935

1.14412117

1.000050902

0.241268307

0.3302800357

0.619602859

1.048669696

1.144917846

1.001510262

0.2458131462

0.3364745975

0.6271868348

1.054814577

1.146541238

0.9968471527

0.2481638193

0.3417761028

0.6389197111

1.061567426

1.149173856

0.9988555908

0.2529240549

0.3486307859

0.6503332257

1.069201231

1.148497939

0.9948298335

0.2563100457

0.3543290198

0.6583480835

1.07290864

1.151217103

0.9944956899

0.2600540221

0.3598985374

0.6721470952

1.082848549

1.151648998

0.9938445091

0.2642479837

0.3665084541

0.6794252992

1.08370769

1.152046442

0.9882320166

0.2690300345

0.3741501868

0.694835484

1.094415069

1.154512048

0.9917734861

0.2733763456

0.3807949424

0.7027015686

1.097745895

1.1544801

0.9854907393

0.2777011096

0.3881687522

0.7168314457

1.104251146

1.156444192

0.9865729809

0.2820987105

0.3949564397

0.7266893983

1.11084342

1.155773878

0.9826661348

0.2862952352

0.4021746218

0.7375029922

1.114145637

1.157826543

0.9806851149

0.2914579511

0.4098955989

0.7514712811

1.122469783

1.157423377

0.9798749685

0.2966749072

0.4184342325

0.759509027

1.124315262

1.158993363

0.9749361277

0.3006640673

0.4250556529

0.7746037245

1.132002831

1.159893632

0.9766978025

0.3068937957

0.4348270893

0.783927083

1.134832025

1.158799052

0.9698846936

0.3112061024

0.4422498643

0.7970719934

1.140916348

1.160839558

0.9712542295

0.3170220554

0.4513848424

0.8084225655

1.145800352

1.159321785

0.9663069844

0.3231116831

0.4599477947

0.8192478418

1.147697568

1.160600424

0.9641622901

0.3278616667

0.4687747061

0.8322745562

1.154400587

1.160170317

0.9618641138

0.3339216411

0.4787815511

0.8419613838

1.155067444

1.158795953

0.9577733278

0.3407703042

0.4891664386

0.8566474915

1.162144184

1.162278533

0.9551762938

0.3464403749

0.4981963933

0.8671504259

1.166507363

1.158794761

0.9541517496

0.3533309698

0.5099471807

0.8794324398

1.167847037

1.161659837

0.9483277798

0.3593889773

0.5191468596

0.8913630843

1.175356865

1.160494447

0.9486818314

0.3661376536

0.5299317837

0.9015777707

1.175037742

1.157916069

0.9425678253

0.3724931777

0.541174233

0.9143717289

1.181027174

1.159813523

0.940816164

0.379327476

0.551192224

0.9235641956

1.181610107

1.156875253

0.9377596378

0.3865959644

0.5619814396

0.936565578

1.186595201

1.157507181

0.932749033

0.3943259418

0.5748062134

0.9475363493

1.189852953

1.156492591

0.9326133728

0.4018912017

0.5863358974

0.9578442574

1.190144539

1.155426383

0.9257190228

0.4104160666

0.5986425877

0.9709204435

1.197470546

1.15550518

0.9263163209

0.417401582

0.6110926867

0.9787942767

1.195253134

1.152472019

0.9191915989

0.4259725511

0.6226460338

0.992112577

1.202450514

1.153245091

0.9175065756

0.4346943796

0.6360500455

1.000892282

1.202139378

1.149999022

0.9146780372

0.4434637725

0.6490842104

1.012516856

1.205547214

1.151391625

0.9091109037

0.4512735307

0.6610806584

1.020840049

1.207111835

1.14800334

0.9083487988

0.4617097676

0.675978899

1.031918406

1.208042502

1.147093415

0.9014397264

0.4695294797

0.6886118054

1.04113543

1.212215781

1.145883322

0.9006737471

0.4800186753

0.7025451064

1.049931407

1.211217761

1.142211676

0.8947587013

0.4901249111

0.7167692184

1.061144352

1.217335343

1.142488956

0.8930261135

0.4996772707

0.7314119339

1.06902194

1.216252565

1.139731169

0.8886390924

0.511562109

0.7470437288

1.081800103

1.223020554

1.141167283

0.8854119778

0.5214024782

0.7616019249

1.089458704

1.224589348

1.138582468

0.8851797581

0.5325913429

0.7766606212

1.096417189

1.222853303

1.135274887

0.8752403855

0.5435158014

0.7896326184

1.105563045

1.2262609

1.133428574

0.876036346

0.5544971228

0.8051570654

1.110978961

1.22389102

1.12808454

0.8693053126

0.5665345192

0.8199093342

1.119878292

1.227363348

1.129226208

0.8663429022

0.5779491663

0.8340613842

1.125442386

1.226149917

1.122485638

0.8632653952

0.5909212232

0.8498820066

1.13375771

1.228971243

1.122162938

0.8576695323

0.6022484899

0.864189744

1.138903141

1.227573633

1.119385242

0.8565605283

0.6161417365

0.8790012002

1.147106409

1.228943825

1.114758134

0.8494714499

0.6286300421

0.894064784

1.153142571

1.231264114

1.113544822

0.8488777876

0.6409141421

0.9095789194

1.157624722

1.227173328

1.107738137

0.8413179517

0.6573277712

0.9244919419

1.166753888

1.232803345

1.106988907

0.8409770727

0.6678010821

0.9383097887

1.167756915

1.228839278

1.099704266

0.836070776

0.6838025451

0.9541985989

1.175560951

1.230501294

1.100136042

0.8306517601

0.6974413991

0.9666994214

1.179046273

1.230447054

1.095001459

0.8305599093

0.7105241418

0.9810374975

1.184834838

1.229465485

1.089990497

0.8226388693

0.726561904

0.9956142306

1.189276338

1.231415987

1.088585734

0.823195219

0.740036428

1.009011865

1.193350196

1.228348851

1.081900239

0.8167923689

0.7551802397

1.021310925

1.198092818

1.231624961

1.07990253

0.8149929047

0.7692411542

1.035830259

1.199873567

1.226472497

1.073741078

0.8108044863

0.7860484719

1.048073769

1.205992341

1.228947997

1.070489883

0.8064590693

0.8002260923

1.059981227

1.207149506

1.226378083

1.066227198

0.8045210838

0.8151068091

1.073206902

1.211553454

1.224945068

1.060499191

0.7982513905

0.8325647712

1.084140658

1.215193868

1.226534247

1.058083534

0.7998776436

0.8452168703

1.095877886

1.216841221

1.223044038

1.050554156

0.7922702432

0.8618928194

1.106370449

1.220824361

1.223775268

1.049048543

0.7920158505

0.8760063648

1.116521478

1.221211314

1.220226169

1.041039228

0.7881334424

0.8920080066

1.126253009

1.225732207

1.22070539

1.03824842

0.7841260433

0.9058858156

1.136577845

1.225515485

1.218145967

1.033433437

0.7838580608

0.9215585589

1.145670295

1.228761196

1.216079831

1.025759101

0.7769784331

0.9370963573

1.155071497

1.230902076

1.215598941

1.024122119

0.7785394788

0.9510987401

1.16472888

1.231957197

1.211654425

1.015862703

0.772850275

0.9686421752

1.172770619

1.235111833

1.212171197

1.013611078

0.7731538415

0.9796742797

1.180367589

1.233240128

1.206313133

1.005876422

0.7683237791

0.9964489341

1.189060688

1.237383366

1.206674933

1.001634359

0.7665948272

1.009453893

1.19500947

1.236314893

1.203159451

0.9962051511

0.7664369941

1.02239728

1.202747941

1.238167048

1.200195789

0.9892261028

0.7604594231

1.03791678

1.207983851

1.238691688

1.198619485

0.9871687293

0.7631759644

1.048612595

1.215483785

1.239015102

1.193780661

0.9779248238

0.7578321099

1.064365745

1.220299721

1.23999238

1.192709088

0.976098001

0.7580137849

1.075669885

1.22697556

1.240078211

1.187986851

0.9690269232

0.7563767433

1.089390755

1.231965661

1.241356611

1.186362028

0.963732481

0.7540236712

1.100861311

1.237514257

1.239584923

1.180768728

0.9588680863

0.7541545033

1.11259079

1.243278623

1.241025209

1.179114819

0.9518707991

0.7515604496

1.12543714

1.245720744

1.24035573

1.174936056

0.9493468404

0.7533156872

1.133086801

1.250087619

1.23991859

1.169483781

0.9408484697

0.7486824989

1.147044063

1.253713012

1.240117192

1.167387128

0.9393286705

0.7519638538

1.154013276

1.257326007

1.23741591

1.161275387

0.9308398366

0.7488604188

1.165831804

1.261894584

1.239405632

1.158844352

0.927572906

0.7498714924

1.17504847

1.264666319

1.235918283

1.153009415

0.9224045277

0.7501942515

1.182376504

1.267581105

1.237426519

1.150341272

0.915450573

0.7483253479

1.19372499

1.270719528

1.234959602

1.144422412

0.9150137901

0.7513326406

1.198543191

1.272908568

1.233212829

1.139149308

0.9058048725

0.7485123873

1.210045576

1.274718881

1.232523322

1.135896921

0.9041775465

0.7518973351

1.213283181

1.278103709

1.228815913

1.129031181

0.8979517221

0.7496979833

1.223534942

1.28039515

1.229191899

1.125890136

0.8937932253

0.752844274

1.229235053

1.279640198

1.225755095

1.118988991

0.8902962804

0.7528868914

1.234586716

1.284160376

1.22608006

1.115718365

0.8855561018

0.7538284063

1.24270153

1.283424139

1.220931172

1.108703613

0.8827341199

0.7567597032

1.245732546

1.286022663

1.220535159

1.103767991

0.8765422106

0.7553402185

1.253943801

1.28707242

1.217891097

1.099303126

0.8764694929

0.7601527572

1.255819321

1.288313746

1.212822795

1.091570854

0.8698077798

0.7590929866

1.262362003

1.289410353

1.213075876

1.087886691

0.8675354719

0.7628406286

1.267102003

1.290303469

1.208763003

1.081202269

0.8668984175

0.7654619813

1.26980412

1.290884137

1.206505418

1.076127529

0.8595929742

0.7660343647

1.276843071

1.290347815

1.202287793

1.070559144

0.8615678549

0.7708988786

1.276279807

1.292613268

1.199146271

1.064120412

0.8547948599

0.7700099349

1.284130573

1.292185307

1.195786238

1.059839964

0.8551303148

0.7759805918

1.283977985

1.292134762

1.192235708

1.052685738

0.8516272902

0.7762455344

1.288739204

1.29384768

1.189654827

1.049154162

0.8510033488

0.7807091475

1.291740298

1.292578697

1.183778524

1.041400313

0.8496011496

0.7826805115

1.292682648

1.29337275

1.182670593

1.037495732

0.8472551703

0.7859233022

1.297460914

1.291918159

1.176075459

1.031029582

0.8488916755

0.7900546193

1.297441125

1.293758035

1.173700929

1.026856065

0.8446474075

0.7919943333

1.302396178

1.291917801

1.16831696

1.021514297

0.8467243314

0.7975586057

1.300434351

1.292498231

1.16439271

1.015931487

0.8455608487

0.7989050746

1.306410789

1.291614652

1.159985185

1.012861967

0.8447681665

0.8042189479

1.306660771

1.290306568

1.156033278

1.007650375

0.8480424285

0.8077068925

1.306840301

1.290229917

1.151364446

1.002500892

0.8449098468

0.8098276854

1.311464548

1.288184881

1.145916343

0.9991436005

0.8491124511

0.8162708282

1.308196306

1.288959742

1.142297983

0.9947504997

0.8474798203

0.816849947

1.314117193

1.287733436

1.137122035

0.9911417961

0.8515751362

0.8238124251

1.311529636

1.286309838

1.13232398

0.9878703952

0.8511073589

0.8250045776

1.315263748

1.285328865

1.128194213

0.9853856564

0.8534423113

0.8304734826

1.314574838

1.283245921

1.122293949

0.9798935056

0.8568469286

0.8329803944

1.315056562

1.282976985

1.118454337

0.9790663123

0.85687989

0.8372211456

1.317080975

1.28066504

1.112991571

0.9759886265

0.8638784289

0.8421516418

1.315532446

1.280632019

1.109723449

0.9738634825

0.8631082773

0.8431117535

1.319790602

1.278532743

1.104221702

0.9736244678

0.8688809276

0.8499493599

1.315534949

1.27592504

1.099999905

0.9709412456

0.8716771007

0.8500388265

1.319747925

1.275182843

1.095953226

0.9706174731

0.8746196628

0.8560699224

1.318341017

1.272469044

1.09085536

0.9689968228

0.8800460696

0.8577347398

1.317506075

1.271259546

1.08818078

0.9696143866

0.8816839457

0.8615932465

1.321224451

1.268984079

1.083503842

0.9692185521

0.8895566463

0.8649238944

1.317804098

1.267542243

1.079811335

0.9705873132

0.8906376362

0.8668275476

1.320346951

1.264176726

1.0762676

0.9709071517

0.8978686929

0.8712202907

1.318492889

1.262513161

1.07382226

0.9716243744

0.9021715522

0.8714914918

1.320747018

1.260659575

1.069514275

0.9741190672

0.9058622718

0.8766940236

1.318015099

1.25679934

1.066604972

0.9742578864

0.9135020971

0.8769480586

1.319222331

1.256936193

1.065408707

0.9785940051

0.9156526327

0.8797784448

1.320440292

1.253443122

1.06089139

0.9807913303

0.9230610728

0.8824647665

1.31586647

1.251223326

1.060481548

0.983757019

0.9257336259

0.8821607828

1.321511626

1.249770164

1.058302045

0.987813592

0.9332689047

0.8862504363

1.315939903

1.247538686

1.057257891

0.9905660152

0.9371003509

0.8850350976

1.317489386

1.243570209

1.055245519

0.993783772

0.9412775636

0.8877286911

1.317060113

1.243306637

1.056241393

0.9985969067

0.9489257336

0.8880307674

1.316345334

1.240588665

1.054729462

1.003711224

0.9498167038

0.8887298107

1.317161441

1.23752141

1.054864764

1.006486535

0.9581974745

0.8892912269

1.314787745

1.237964153

1.056357503

1.013010502

0.9600173831

0.8885650039

1.316997051

1.234672785

1.055537343

1.017194867

0.9654764533

0.8899676204

1.313072562

1.232955217

1.058728576

1.021220088

0.9695129991

0.8878197074

1.31642735

1.233058929

1.058635831

1.027953148

0.9729372859

0.8890503049

1.31341064

1.230384946

1.060802579

1.030903935

0.9772424698

0.8868753314

1.313212156

1.229627252

1.062806964

1.037017465

0.9784361124

0.8860347867

1.314885259

1.227438927

1.064480424

1.040935159

0.9846291542

0.8847545385

1.310530305

1.226659536

1.067908168

1.046779394

0.9842739105

0.8821616769

1.313331842

1.225102067

1.069018364

1.050158858

0.9888691306

0.8812947869

1.309548855

1.224963665

1.073962808

1.05514884

0.9904212356

0.8771256208

1.310732603

1.22335124

1.074307323

1.059160471

0.9900009632

0.8755193949

1.309183598

1.221920013

1.079200268

1.062604666

0.9951364398

0.8713473082

1.308012605

1.222845912

1.080906391

1.068285584

0.9917565584

0.8681588769

1.306798697

1.220138907

1.083345771

1.069311261

0.9951193333

0.8642085195

1.303389668

1.220208406

1.088269234

1.073762774

0.9934398532

0.8596283197

1.305375695

1.219380379

1.088080883

1.075437188

0.9936902523

0.8557832241

1.299759865

1.217179298

1.092628479

1.077628016

0.9924758673

0.8496916294

1.301947355

1.217937708

1.093666434

1.080727458

0.990241468

0.8462937474

1.298270941

1.216073394

1.096560597

1.081154346

0.9892122746

0.8383463025

1.296401501

1.216175556

1.097939491

1.083723307

0.9842580557

0.8345404267

1.295767665

1.214349508

1.100208282

1.08320868

0.9840763807

0.8273512125

1.291086197

1.213461161

1.10264492

1.084203124

0.9778485894

0.8204359412

1.292164087

1.212790847

1.100546956

1.082651734

0.9739700556

0.8148586154

1.286475301

1.211657882

1.10635674

1.083188415

0.9706154466

0.8074707389

1.287349701

1.210901141

1.102434635

1.081243753

0.9616513252

0.8014419079

1.282949328

1.208209395

1.105449915

1.07966733

0.9592332244

0.7943095565

1.28011322

1.208399177

1.104552031

1.077130079

0.9497807026

0.7881212831

1.278834105

1.206439257

1.103869915

1.073817492

0.9449911118

0.7804620266

1.273245215

1.204706073

1.103896022

1.070398569

0.9365848899

0.7747781277

1.273476481

1.202400208

1.100721121

1.065284014

0.9281007648

0.7680531144

1.267754197

1.201036453

1.101016998

1.061057687

0.9205074906

0.7609103322

1.265460491

1.198977232

1.095634103

1.05448997

0.9102069736

0.7558019161

1.261374116

1.195245266

1.094644785

1.048810482

0.9042996168

0.7487124205

1.257557392

1.194126606

1.089838624

1.042750359

0.8920084834

0.7433082461

1.25437367

1.189499497

1.085152984

1.033691406

0.8864350915

0.7379257083

1.24875474

1.186955929

1.081619859

1.027206779

0.8755261302

0.7328639627

1.246914744

1.182605982

1.074041009

1.018629909

0.8661503792

0.7276762724

1.238998294

1.177098036

1.069638968

1.009515643

0.8591557145

0.7227094173

1.236288786

1.172876239

1.061173916

1.001201153

0.8483620286

0.7182962298

1.229311585

1.166671515

1.054994702

0.9916719794

0.8427627087

0.7131475806

1.223313212

1.161178231

1.045644283

0.981540978

0.8321795464

0.7096711397

1.217784643

1.153531671

1.037496209

0.9717615843

0.8268326521

0.7043548822

1.210105538

1.147167444

1.029449701

0.963226974

0.8174487352

0.7011900544

1.204503775

1.139344454

1.017804623

0.9531340599

0.810775578

0.6974642873

1.195175767

1.130303144

1.010596991

0.9444351792

0.8046703339

0.692921102

1.188721657

1.123906612

0.9980124235

0.9352670312

0.7955429554

0.6897932887

1.179817796

1.113324523

0.989915669

0.9253958464

0.792737484

0.6861615181

1.171040297

1.104416609

0.9780757427

0.9171478152

0.7823318839

0.6815335155

1.164208174

1.095845222

0.9698389769

0.9079332948

0.7797733545

0.6785354018

1.152052283

1.084860325

0.9585497975

0.8993182182

0.7716718316

0.6753892303

1.145477772

1.075302839

0.9470070601

0.891443491

0.766169548

0.6706032753

1.13337636

1.064926386

0.9397720098

0.8834574819

0.7609890103

0.6669848561

1.124554038

1.054514885

0.9252315164

0.8746644258

0.7527341843

0.6630076766

1.113913894

1.042880654

0.9178903699

0.8663445711

0.749383986

0.6584606767

1.103498459

1.033905387

0.9067187309

0.8588115573

0.7395899892

0.655254066

1.093280196

1.022756934

0.8958309293

0.8496333361

0.7362316251

0.6505898237

1.083022237

1.011786222

0.8880357742

0.844111979

0.7283453345

0.6473638415

1.073963404

1.002692342

0.8761395216

0.834518373

0.7225900292

0.6421099901

1.06068635

0.9897770286

0.8668768406

0.8258766532

0.716439724

0.6379727721

1.052373052

0.9803350568

0.8552504778

0.8185189962

0.7077349424

0.63234061

1.041059017

0.9701244235

0.8477073312

0.8096311688

0.7034060955

0.6277372241

1.029280543

0.9583390951

0.8355339766

0.8012481928

0.6932374239

0.6227648258

1.020957589

0.9495863914

0.8271489739

0.7925555706

0.6890243292

0.6170853376

1.008365035

0.9383130074

0.8172845244

0.7839872837

0.679235518

0.6121346951

0.9993004203

0.928362906

0.804930985

0.7745523453

0.672329247

0.6049687266

0.9882913828

0.9177103043

0.7980615497

0.7665882111

0.6657650471

0.6004834771

0.9793432355

0.9092140794

0.7864392996

0.75733006

0.6560967565

0.5934655666

0.9700767994

0.8990120292

0.7783923745

0.7488160729

0.652269125

0.5882578492

0.9623004198

0.8907085061

0.7704942822

0.7417500615

0.6422373056

0.5835254192

0.9546609521

0.8844347

0.7613984942

0.7335016727

0.6384387016

0.5768467188

0.9447354078

0.8747773767

0.7541508079

0.7266077995

0.6300641894

0.5730160475

0.9410071373

0.8699206114

0.7468417287

0.7208858728

0.6252936125

0.5672895908

0.9322909117

0.8626645803

0.7424505949

0.7149270773

0.6211881042

0.563870132

0.9280403256

0.8586921692

0.7359503508

0.7107926607

0.6162584424

0.5596282482

0.9235818386

0.853895843

0.7335051298

0.7063720226

0.6151333451

0.558204174

0.9179546237

0.8502429128

0.7291799188

0.7042834759

0.6103892922

0.5563156009

0.9169152379

0.8495588303

0.7276382446

0.7038649917

0.6134479642

0.5560917258

0.9129740596

0.8461802602

0.72856462

0.7034224272

0.611436367

0.5586311817

0.9110053778

0.8477658033

0.7259539962

0.7049664259

0.6148222685

0.5591402054

0.9089867473

0.8475057483

0.731082499

0.7095608115

0.6203275323

0.5657379031

0.9093526006

0.8495733142

0.732755065

0.7136312127

0.6247444153

0.5711150765

0.9071387053

0.8522772193

0.7389395237

0.719448328

0.6342608929

0.5789929032

0.9062461257

0.8551138043

0.7437283397

0.7292508483

0.6420929432

0.5905632973

0.9071542025

0.8597335815

0.7516504526

0.7377262712

0.6567671895

0.6015701294

0.9038737416

0.8636994362

0.760936141

0.7494397759

0.6681557298

0.6167895794

0.9063048363

0.871101737

0.7692659497

0.7640630603

0.6879826784

0.6331140399

0.9048106074

0.87616992

0.7839030623

0.7783448696

0.705129087

0.6522397995

0.9058224559

0.8856015205

0.7965903282

0.7970302701

0.7267135978

0.6727399826

0.9733333588

0.9599548578

0.8684533834

0.8740618229

0.7985913157

0.7377735376

0.9750301242

0.9709341526

0.8892921209

0.9014493823

0.8287805319

0.7672493458

0.97533077

0.9823461175

0.9117990136

0.929890275

0.8628869057

0.7974998951

0.9807552695

0.9979508519

0.9385613203

0.9637514353

0.9032617211

0.8331242204

0.9863315821

1.011336088

0.9668840766

1.00148356

0.9464247227

0.8710155487

0.994579196

1.027355313

0.9971338511

1.043391109

0.9955765009

0.9149456024

1.00826633

1.045042992

1.030619144

1.087797403

1.048738837

0.9639217854

1.028092027

1.06712997

1.066393614

1.136614442

1.1049788

1.016823173

1.054728985

1.093820453

1.104494572

1.186897039

1.166103005

1.078880191

1.091844678

1.129909396

1.14781332

1.241287947

1.231844068

1.147537947

1.145206213

1.179441571

1.204286933

1.307140231

1.307359934

1.227883458

1.20906198

1.237694502

1.268474221

1.375963926

1.384611487

1.314948916

1.28080833

1.305575371

1.33725512

1.446549773

1.460769773

1.404239416

1.361479998

1.382891059

1.412823677

1.517117023

1.533830285

1.491653204

1.448283076

1.464705348

1.494135737

1.590235591

1.609548569

1.576894283

1.536935925

1.549436927

1.575757146

1.658007979

1.673242807

1.651681066

1.617738724

1.628750801

1.647894621

1.7149297

1.725677848

1.712076426

1.691123843

1.695801497

1.706980824

1.758720994

1.767252803

1.756344557

1.745920181

1.744558096

1.749981046

1.788815379

1.788666964

1.781818509

1.784119248

1.778484464

1.773397446

1.80053854

1.802235723

1.796707392

1.811276317

1.804504991

1.793800354

1.812994838

1.814087391

1.807539225

1.840416789

1.82758534

1.815347433

1.831430674

1.832310796

1.82536006

1.864438534

1.852928758

1.836463571

1.851408601

1.848557234

1.845167637

1.874094486

1.861882687

1.845985174

1.860192299

1.856782317

1.851943374

1.884035349

1.871584773

1.853646517

1.865749717

1.863653183

1.85836184

1.890745163

1.877074957

1.862043858

1.875377059

1.872929215

1.866829038

1.899503112

1.887789607

1.869135857

1.88215673

1.880827427

1.876304746

1.910404801

1.896823406

1.880577207

1.894495368

1.8901577

1.884179831

1.91841805

1.906368613

1.887055397

1.902732491

1.899686575

1.894309402

1.928045034

1.916141033

1.897176266

1.911868572

1.90711832

1.903667808

1.938729525

1.926888704

1.909356475

1.921038508

1.919786572

1.915018797

1.950038552

1.938117146

1.919741511

1.932259321

1.929985046

1.925370574

1.960016608

1.947107911

1.928025961

1.944459558

1.939796209

1.936094999

1.973348618

1.959777474

1.941220522

1.954971671

1.953185797

1.9476825

1.984342933

1.971986413

1.954559565

1.967201591

1.965475917

1.959713101

1.998122811

1.985553503

1.963556528

1.98090744

1.975117803

1.972846866

2.010336876

1.998644471

1.979325533

1.993489265

1.990357637

1.984447479

2.02315855

2.011645794

1.993350148

2.005951166

2.004091501

1.999473572

2.037929058

2.027572393

2.007319689

2.020556211

2.016840219

2.012627602

2.053810835

2.041829109

2.02325058

2.036775827

2.035426855

2.028541088

2.07103157

2.058821201

2.039162636

2.053296804

2.051171303

2.04583931

2.087637663

2.075046301

2.058201075

2.069793463

2.066412687

2.062792778

2.105557203

2.092630625

2.074004173

2.086630106

2.084991455

2.082505941

2.123043776

2.112460136

2.093773603

2.107057333

2.104228735

2.096922398

2.142566442

2.130038261

2.112263918

2.12517786

2.122294664

2.115981817

2.158494711

2.148288727

2.128970146

2.141339302

2.137434959

2.135761261

2.181208372

2.169014931

2.151164532

2.165286541

2.159607172

2.154870033

2.202627182

2.185171604

2.169195652

2.18274045

2.179484606

2.173501492

2.2207582

2.206782341

2.188762665

2.202424765

2.196546316

2.194206238

2.240747929

2.231615067

2.207388878

2.222135305

2.221634865

2.214984894

2.260965586

2.250156403

2.230051517

2.245923281

2.240779638

2.236120701

2.284926653

2.272777319

2.251844168

2.266075611

2.261110306

2.260594845

2.305863857

2.295619965

2.275959253

2.288650274

2.287572384

2.280642033

2.330272913

2.318605423

2.298411608

2.314754725

2.309851885

2.302912474

2.354282141

2.340743542

2.32325983

2.334731102

2.332131386

2.329854965

2.377481222

2.3659904

2.346066475

2.358736038

2.354894876

2.353958607

2.405405045

2.391025543

2.374455214

2.385395288

2.383758307

2.37673831

2.42798996

2.41639328

2.396900177

2.413499832

2.410240889

2.4039042

2.458187342

2.444197893

2.424460411

2.439724684

2.433080912

2.430332184

2.485316753

2.470208406

2.451948643

2.46655035

2.4615798

2.459382296

2.512802839

2.500377178

2.482297182

2.494452238

2.490579367

2.486534595

2.538684607

2.5226264

2.508983374

2.521341562

2.520218611

2.514970541

2.569158792

2.560197115

2.53602457

2.55322361

2.545452833

2.544037819

2.604174376

2.58275342

2.568992376

2.579592466

2.580224514

2.57145524

2.630784035

2.617961407

2.597158194

2.607329607

2.603327751

2.603729725

2.659896851

2.641292095

2.621114016

2.635610819

2.632410765

2.63070631

2.691900253

2.673765421

2.660014868

2.669256687

2.658501387

2.66274929

2.716645956

2.698727846

2.683701515

2.692553759

2.695926905

2.683506966

2.741710186

2.734544754

2.714060783

2.726266146

2.726308107

2.717008352

2.77270031

2.764629841

2.73866868

2.747835636

2.746420383

2.744980574

2.801817417

2.791547298

2.766046524

2.78265357

2.782426119

2.774620056

2.830864668

2.823174477

2.799591541

2.813214302

2.806782961

2.799069881

2.861397743

2.846561432

2.829802275

2.845590353

2.835073233

2.829343319

2.886965036

2.869882584

2.854388237

2.867933035

2.861502886

2.863604784

2.917737484

2.897720575

2.880481482

2.89585638

2.895371199

2.898761749

2.949547291

2.929819107

2.91076088

2.928063869

2.915442944

2.916047812

2.972976923

2.961583853

2.935750246

2.956188202

2.952793837

2.942692518

2.999206066

2.988361835

2.966634274

2.98918891

2.970829248

2.974577665

3.027080059

3.01718688

2.995622873

3.008948565

3.004870653

2.98980689

3.055162668

3.047641039

3.021552324

3.042714596

3.031894445

3.031687498

3.085556269

3.076480389

3.053472281

3.067758322

3.057028055

3.056747675

3.116258621

3.099772692

3.067605019

3.087203503

3.078454971

3.091547012

3.152440548

3.143591642

3.099947691

3.116024256

3.120199203

3.126536846

3.172914743

3.154415846

3.139768124

3.159693003

3.143480778

3.154538631

3.182496786

3.193313599

3.169722795

3.175163507

3.180856705

3.170911551

3.228628635

3.227827311

3.222527981

3.206670761

3.206367254

3.219012022

3.277305126

3.263291359

3.241729498

3.253112316

3.261965036

3.259848118

3.31329608

3.281884909

3.281544209

3.288741589

3.281687737

3.289090633

3.350407362

3.332759619

3.315854311

3.328338385

3.315697432

3.328701019

3.403533936

3.373592138

3.339332581

3.338307142

3.378865242

3.352288246

3.420790434

3.389136314

3.41577816

3.387535334

3.39994812

3.411682844

3.475645304

3.451436758

3.418663502

3.451120377

3.432926893

3.449617624

3.535998821

3.501534939

3.479568005

3.520163059

3.467889786

3.47472167

3.586701632

3.57977891

3.518327951

3.509049654

3.523874521

3.503142834

3.548225164

3.608881235

3.605920076

3.585052967

3.531385899

3.599353075

3.679704905

3.632938385

3.610846043

3.655734301

3.65571022

3.642739534

3.696271896

3.692894936

3.687651396

3.668826342

3.724720478

3.727652311

3.751741886

3.816732168

3.761534214

3.751514912

3.775454283

3.72884202

3.868525505

3.816065073

3.808227539

3.839382648

3.827325106

3.843429804

3.846783876

3.94229126

3.858917236

3.932317257

3.932315111

3.884958982

3.923796415

4.019248486

4.019060612

4.045046329

3.988646269

3.983032465

4.011974812

4.063092709

4.161924362

4.062977791

4.049508095

4.145241261

4.326330185

4.269194603

4.148329735

4.351456165

4.047641754

4.238190651

4.421421051

4.279222965

4.391935349

4.155272484

4.364257813

4.351031303

4.474615097

4.736787796

4.598481178

4.648642063

4.457201958

4.276803017

4.508003235

4.471586704

4.615650654

4.52752924

4.508068085

4.832441807

5.345303535

4.659316063

4.65947628

4.6866045

5.234732628

4.585981846

10

5.397972584

5.276053429

4.869915962

4.968685627

10

10

4.557677269

5.305988789

4.604577541

4.971921921

4.971568584

5.893539429

10

5.392305374

4.651087761

4.777432919

4.742642403

4.471457958

4.93928051

5.769113064

5.346741676

4.64609766

4.996114731

10

6.1237607

4.420078278

5.117731571

10

4.547430038

10

4.58865118

4.693018436

5.032169819

4.756530762

4.434542656

4.912548065

5.022548199

5.895875454

4.751767635

5.172263622

5.267916203

10

4.56223011

4.660056591

7.651486874

4.864278316

4.95979023

4.632021427

5.859137058

10

4.821280956

4.959474087

4.686859608

5.016840458

4.783183575

4.908617973

4.71603632

4.687067986

10

5.267323017

10

10

4.606669903

5.270998955

4.748487949

4.786524773

4.824655056

4.660243511

4.659395218

4.584196091

10

5.293178558

5.435760021

4.753528118

5.435078621

10

6.080562115

4.501020432

4.635935783

4.586522579

4.834225655

4.758263111

4.636159897

4.612102509

6.539505959

4.695804119

4.761481285

10

4.501261234

4.998143196

4.589401722

4.543585777

5.368629456

5.068303108

5.000288486

4.805845737

10

4.848795891

10

4.806729794

5.005648613

4.396090031

5.591585636

4.412034035

4.522441387

5.011723995

10

10

10

10

5.608605385

4.809394836

4.852201462

10

4.898332596

10

6.020089626

4.481509686

4.701313972

5.169856548

4.808971405

10

10

10

10

4.701568604

10

4.8546772

5.016879559

4.70236063

4.735989571

5.448981285

10

10

5.299739838

5.693670273

5.29981041

4.81945467

5.323551178

4.443203449

10

10

5.3265872

10

10

4.481883526

10

5.05582428

10

5.006942272

10

4.945216179

5.006758213

4.796839237

5.007407188

10

10

4.632629395

10

5.037568092

4.528817177

4.70637846

4.933169842

4.997412682

10

10

5.279998302

4.738007545

6.171595573

10

10

10

5.416012764

4.889334202

5.176970959

4.458500385

4.840126991

4.499573708

4.946001053

10

10

4.928081512

4.871600151

5.066273689

10

5.251711845

4.760968208

5.140692711

4.854536533

5.412552834

4.855380535

10

10

10

5.131233692

5.047746181

4.858020306

10

5.23759222

4.755196095

10

5.39647913

4.847342968

10

10

10

5.394041061

4.568932056

10

4.504105568

4.852285862

10

5.054071903

5.732789516

4.977471352

10

10

10

10

4.569268703

4.998065472

4.877878189

4.941928864

4.824157238

5.016970158

5.222789288

10

10

10

5.58779335

10

10

6.096329689

5.449694633

4.705516815

10

5.448122025

10

5.447840214

10

10

4.683895588

5.174703121

10

10

5.715008736

10

4.535290718

10

10

10



Agshapecontrol3_72700

		12				11				10				9				8				7

		Wavelength (nm)		Abs		Wavelength (nm)		Abs		Wavelength (nm)		Abs		Wavelength (nm)		Abs		Wavelength (nm)		Abs		Wavelength (nm)		Abs

		1260		0.0022825552		1260		0.0081941932		1260		0.0169226117		1260		0.038249433		1260		0.0415504202		1260		0.0556665249

		1259		0.0056957039		1259		0.0095049646		1259		0.0179543942		1259		0.0388209038		1259		0.0448219553		1259		0.0582381859

		1258		0.0018327052		1258		0.0085996436		1258		0.0175968856		1258		0.0385809876		1258		0.0415023118		1258		0.0547540113

		1257		0.0063131489		1257		0.0096747829		1257		0.0182958599		1257		0.0391402356		1257		0.0449937321		1257		0.0593983643

		1256		0.0025765775		1256		0.0088061951		1256		0.0178378895		1256		0.0384146981		1256		0.0420078747		1256		0.0547523685

		1255		0.0044317176		1255		0.0088808807		1255		0.0171710234		1255		0.0389175527		1255		0.043499738		1255		0.058583498

		1254		0.0051449044		1254		0.0090472838		1254		0.0191339329		1254		0.038655512		1254		0.0436244533		1254		0.0573684387

		1253		0.0021277235		1253		0.0088054817		1253		0.016824061		1253		0.0386196636		1253		0.0418910645		1253		0.0562794581

		1252		0.0062308158		1252		0.0096808448		1252		0.0187618565		1252		0.0390116461		1252		0.0452196933		1252		0.0591210946

		1251		0.0023813734		1251		0.0088975523		1251		0.0180160981		1251		0.0390838385		1251		0.0417150371		1251		0.0555765182

		1250		0.0060452758		1250		0.0096245212		1250		0.0177183412		1250		0.0388173945		1250		0.0448068008		1250		0.0594194382

		1249		0.0034029353		1249		0.0091921231		1249		0.0186190605		1249		0.0385405347		1249		0.0426827483		1249		0.0560164228

		1248		0.0049648024		1248		0.0091795642		1248		0.0173552353		1248		0.0388057344		1248		0.0429075398		1248		0.0590683296

		1247		0.0048657088		1247		0.0096779857		1247		0.018824704		1247		0.0388419665		1247		0.0445883684		1247		0.0573856607

		1246		0.0034402972		1246		0.0095964419		1246		0.0177377295		1246		0.039097406		1246		0.0424615555		1246		0.0576056354

		1245		0.0067930394		1245		0.009620578		1245		0.0191163216		1245		0.0392066389		1245		0.0454528742		1245		0.0596416891

		1244		0.0023993594		1244		0.0095598958		1244		0.0178298783		1244		0.0392277464		1244		0.0425362624		1244		0.0560784191

		1243		0.00752621		1243		0.0109101841		1243		0.0194943044		1243		0.0397375003		1243		0.0458519086		1243		0.0612205826

		1242		0.0032054558		1242		0.0089961169		1242		0.0187125597		1242		0.0391466096		1242		0.042942144		1242		0.0561399497

		1241		0.0057682293		1241		0.0111717796		1241		0.0185976066		1241		0.0398774259		1241		0.0446247719		1241		0.0604085065

		1240		0.0050143972		1240		0.0096224565		1240		0.0195733421		1240		0.0393502451		1240		0.0449143536		1240		0.0582708344

		1239		0.0046092439		1239		0.0108391829		1239		0.0190193281		1239		0.0404070616		1239		0.0436691344		1239		0.0592940226

		1238		0.0070009963		1238		0.0105333356		1238		0.0194734857		1238		0.0395829044		1238		0.0464792252		1238		0.0601720959

		1237		0.0047470098		1237		0.0119845737		1237		0.0204914082		1237		0.0412787311		1237		0.0445461199		1237		0.0588944256

		1236		0.0076095532		1236		0.0109320572		1236		0.0199733526		1236		0.0401990674		1236		0.0461512618		1236		0.0621577911

		1235		0.0045549348		1235		0.0116210962		1235		0.0205354523		1235		0.0410083234		1235		0.0455737226		1235		0.0584766269

		1234		0.0077184183		1234		0.012755624		1234		0.0203463044		1234		0.041549027		1234		0.046299547		1234		0.0626196042

		1233		0.0064920243		1233		0.0117136324		1233		0.0218295939		1233		0.0413087644		1233		0.0474730134		1233		0.0604265966

		1232		0.006577061		1232		0.0132266786		1232		0.0206745639		1232		0.0421906635		1232		0.0459316634		1232		0.0613925308

		1231		0.0089173689		1231		0.0132657224		1231		0.0227265861		1231		0.0425462834		1231		0.0487950891		1231		0.0635156706

		1230		0.0064133615		1230		0.0135351764		1230		0.0223272759		1230		0.0430881083		1230		0.0466693267		1230		0.061395213

		1229		0.0102244439		1229		0.0144976117		1229		0.0226290002		1229		0.0435010567		1229		0.0495264679		1229		0.0653996319

		1228		0.0069301319		1228		0.0141989933		1228		0.0233341064		1228		0.043906033		1228		0.0483341999		1228		0.0620812401

		1227		0.0101485476		1227		0.0153723312		1227		0.0228370987		1227		0.0441270173		1227		0.0491907448		1227		0.065716356

		1226		0.0092854388		1226		0.0155251706		1226		0.0254164115		1226		0.0459293909		1226		0.0516750738		1226		0.0641775355

		1225		0.0102019701		1225		0.0167677999		1225		0.0244175065		1225		0.0454701781		1225		0.0498056337		1225		0.0661295801

		1224		0.011935507		1224		0.0164605193		1224		0.0265469588		1224		0.0467541628		1224		0.0531821437		1224		0.0674508214

		1223		0.0108097773		1223		0.0189494509		1223		0.02625845		1223		0.047979217		1223		0.0521501228		1223		0.0668091252

		1222		0.0140718864		1222		0.0187590197		1222		0.0277727842		1222		0.047540471		1222		0.054072503		1222		0.0702618658

		1221		0.0119323675		1221		0.0193725694		1221		0.0287944917		1221		0.0502076745		1221		0.0545636564		1221		0.0684867054

		1220		0.0151840523		1220		0.0216396097		1220		0.0292300005		1220		0.0501020886		1220		0.0558079369		1220		0.0722785667

		1219		0.0134751741		1219		0.0201993808		1219		0.0308890026		1219		0.0509127974		1219		0.0565147921		1219		0.0702364892

		1218		0.016165385		1218		0.0241890829		1218		0.0311631393		1218		0.0525458083		1218		0.0571373105		1218		0.0740301534

		1217		0.0160007719		1217		0.0217402372		1217		0.0321501829		1217		0.052305609		1217		0.058960896		1217		0.0726855323

		1216		0.0153632136		1216		0.0240526721		1216		0.0321252942		1216		0.0533888154		1216		0.0579395853		1216		0.0738785118

		1215		0.0185139123		1215		0.0236836318		1215		0.0330501422		1215		0.0533282869		1215		0.0594073571		1215		0.0756104812

		1214		0.0155539587		1214		0.0240717959		1214		0.0329107493		1214		0.0543918386		1214		0.059780661		1214		0.0732971206

		1213		0.0191303343		1213		0.0260243006		1213		0.033591032		1213		0.054224018		1213		0.0595940612		1213		0.0777025893

		1212		0.0171167888		1212		0.0236910135		1212		0.0343964361		1212		0.0551066734		1212		0.0610347614		1212		0.0742073134

		1211		0.0185058881		1211		0.0274833217		1211		0.033914905		1211		0.0558795594		1211		0.0607969649		1211		0.0776860267

		1210		0.0182593577		1210		0.0235552769		1210		0.0344773084		1210		0.0539526381		1210		0.0604558401		1210		0.0755137205

		1209		0.0170905367		1209		0.0263477229		1209		0.0339374952		1209		0.0559834987		1209		0.0606133491		1209		0.0762063637

		1208		0.0187046677		1208		0.0249955375		1208		0.0341695659		1208		0.0541807041		1208		0.0603108518		1208		0.0767969713

		1207		0.0156740658		1207		0.0241183955		1207		0.0339278951		1207		0.0549286455		1207		0.0603930987		1207		0.074784264

		1206		0.0193794444		1206		0.0258066785		1206		0.033080142		1206		0.0540316068		1206		0.0597853251		1206		0.0777249411

		1205		0.0149381943		1205		0.0227308404		1205		0.0333194137		1205		0.0543502942		1205		0.0598527044		1205		0.0732929483

		1204		0.0182200242		1204		0.0262124743		1204		0.0328969546		1204		0.0541168638		1204		0.0591778122		1204		0.0777827203

		1203		0.0163890626		1203		0.022263648		1203		0.0332005843		1203		0.0531551987		1203		0.0589517951		1203		0.073992826

		1202		0.0154398931		1202		0.0245835614		1202		0.0316963941		1202		0.0536124222		1202		0.0585988723		1202		0.0748915076

		1201		0.016917685		1201		0.0232328363		1201		0.0330014564		1201		0.0521509089		1201		0.058260683		1201		0.075923577

		1200		0.0147649124		1200		0.0222184192		1200		0.0316875689		1200		0.0534347743		1200		0.0586494468		1200		0.0728754327

		1199		0.0160618499		1199		0.0238910317		1199		0.0314385332		1199		0.0516691543		1199		0.0577142723		1199		0.0756076723

		1198		0.0135814594		1198		0.0210902095		1198		0.0312694758		1198		0.0516831502		1198		0.0575504527		1198		0.0722362846

		1197		0.016921347		1197		0.0241378248		1197		0.0315773413		1197		0.05143952		1197		0.0577813312		1197		0.0764189139

		1196		0.0139849419		1196		0.0207015499		1196		0.0315121226		1196		0.0509495586		1196		0.0565829016		1196		0.0720014796

		1195		0.0150328865		1195		0.0231301952		1195		0.0310448725		1195		0.0513496287		1195		0.0583023056		1195		0.0754506141

		1194		0.0159206893		1194		0.0218391474		1194		0.0317972638		1194		0.0503919721		1194		0.0558781177		1194		0.0737841576

		1193		0.0133357067		1193		0.0209569149		1193		0.0302941427		1193		0.0511573255		1193		0.0582453497		1193		0.0731206685

		1192		0.0163084529		1192		0.0235134661		1192		0.032444559		1192		0.050794702		1192		0.0567551181		1192		0.0759031996

		1191		0.013133713		1191		0.0195657332		1191		0.0304486882		1191		0.0504694842		1191		0.0566576012		1191		0.0718341991

		1190		0.0158185549		1190		0.0236459635		1190		0.0314196683		1190		0.0511448607		1190		0.0580606759		1190		0.076365985

		1189		0.0140374489		1189		0.021271009		1189		0.0320186354		1189		0.0507027358		1189		0.0562801659		1189		0.0729954019

		1188		0.0141516281		1188		0.0217507705		1188		0.0294931736		1188		0.0502467006		1188		0.0574594662		1188		0.0746311843

		1187		0.015330228		1187		0.0225180238		1187		0.0324323438		1187		0.0510109216		1187		0.0567027889		1187		0.0749946758

		1186		0.0129267462		1186		0.0209357794		1186		0.0303946305		1186		0.0508128293		1186		0.0577941947		1186		0.0737913698

		1185		0.0163362976		1185		0.0231000539		1185		0.031744875		1185		0.0499659181		1185		0.0565644726		1185		0.0757757053

		1184		0.012539885		1184		0.0204062332		1184		0.0309461225		1184		0.0511370264		1184		0.0575216971		1184		0.072809279

		1183		0.0158142056		1183		0.0230896268		1183		0.0315547101		1183		0.0500541292		1183		0.0574425943		1183		0.07682129

		1182		0.0130416742		1182		0.0208479389		1182		0.0310704522		1182		0.0501731262		1182		0.0557373278		1182		0.0726050287

		1181		0.0146940285		1181		0.0218788106		1181		0.0306231771		1181		0.0506125316		1181		0.058383815		1181		0.075703837

		1180		0.0139986025		1180		0.0222219881		1180		0.032015793		1180		0.0497401133		1180		0.0559549071		1180		0.074360244

		1179		0.0135240145		1179		0.0207043197		1179		0.0305091944		1179		0.0507361926		1179		0.0582740642		1179		0.0743066668

		1178		0.0158683043		1178		0.0237223152		1178		0.0327192619		1178		0.0505064391		1178		0.0576750115		1178		0.0766951293

		1177		0.0120029617		1177		0.0204456299		1177		0.030569043		1177		0.0503563322		1177		0.0570113398		1177		0.0730380267

		1176		0.0162262991		1176		0.0234922078		1176		0.0320965275		1176		0.0507033169		1176		0.0586560518		1176		0.0777430534

		1175		0.0128958393		1175		0.0218993109		1175		0.0317998528		1175		0.0507314764		1175		0.056645304		1175		0.074114427

		1174		0.0153586539		1174		0.0228283666		1174		0.0317429826		1174		0.05076354		1174		0.0598284341		1174		0.0770811886

		1173		0.0145884603		1173		0.023138687		1173		0.0331407636		1173		0.0511245057		1173		0.0570264533		1173		0.0758446902

		1172		0.0142344069		1172		0.0224788748		1172		0.0318986587		1172		0.0518896915		1172		0.0598602816		1172		0.0763737261

		1171		0.0159845501		1171		0.0245544445		1171		0.0336443149		1171		0.0510583222		1171		0.058454562		1171		0.0780268684

		1170		0.0135929715		1170		0.0225125179		1170		0.0325098932		1170		0.0520704426		1170		0.0590853542		1170		0.0755750835

		1169		0.01725691		1169		0.0251114555		1169		0.0338796973		1169		0.0523252599		1169		0.0603559464		1169		0.0797966197

		1168		0.013624222		1168		0.0240291972		1168		0.0336894058		1168		0.0522781052		1168		0.0587872118		1168		0.0763470679

		1167		0.0171225779		1167		0.0246890411		1167		0.0337823443		1167		0.0527791567		1167		0.0618372038		1167		0.0798355639

		1166		0.0152339423		1166		0.0253401995		1166		0.0353921577		1166		0.0530727059		1166		0.0597775429		1166		0.0781804696

		1165		0.0157088488		1165		0.0247740448		1165		0.0342884883		1165		0.053644903		1165		0.0622109883		1165		0.0797649249

		1164		0.0178607609		1164		0.0269038174		1164		0.0359706208		1164		0.0539276376		1164		0.0613389835		1164		0.0805695727

		1163		0.0150772119		1163		0.0251515266		1163		0.0351397023		1163		0.0544931293		1163		0.0617529824		1163		0.0792010426

		1162		0.0186766442		1162		0.0273878314		1162		0.0365021266		1162		0.0540480539		1162		0.0629580319		1162		0.0828762725

		1161		0.0159399975		1161		0.0267153997		1161		0.036501199		1161		0.0555240363		1161		0.0617275275		1161		0.0793053731

		1160		0.0180153158		1160		0.0264184438		1160		0.0363457799		1160		0.0546016693		1160		0.0645102486		1160		0.0828521773

		1159		0.0162503216		1159		0.0274755452		1159		0.036737714		1159		0.0546862446		1159		0.0611955188		1159		0.0804248452

		1158		0.017615702		1158		0.0267198328		1158		0.0363797806		1158		0.0558229499		1158		0.0647997856		1158		0.0821959972

		1157		0.0179739539		1157		0.0275664739		1157		0.0373754948		1157		0.0543386191		1157		0.0623661466		1157		0.0822308809

		1156		0.0156521946		1156		0.0265827887		1156		0.0353582911		1156		0.0553791262		1156		0.062924251		1156		0.0810063779

		1155		0.0198520515		1155		0.0283229426		1155		0.0381269604		1155		0.0553472228		1155		0.0650879517		1155		0.0847423151

		1154		0.0155867189		1154		0.0275846776		1154		0.0367958918		1154		0.0556832962		1154		0.0622729808		1154		0.080466345

		1153		0.0186776165		1153		0.027805347		1153		0.036817532		1153		0.0552869774		1153		0.0656042844		1153		0.0849626511

		1152		0.0168277211		1152		0.0279160552		1152		0.0375387333		1152		0.0555776358		1152		0.0623250306		1152		0.0819106698

		1151		0.0170347784		1151		0.0268634185		1151		0.0360465832		1151		0.0551606044		1151		0.0651536956		1151		0.0831352472

		1150		0.0182549041		1150		0.0283705797		1150		0.0378120765		1150		0.0550066195		1150		0.0630829856		1150		0.0839090198

		1149		0.0161558203		1149		0.0268035009		1149		0.0355388932		1149		0.0552582815		1149		0.063283667		1149		0.0818568096

		1148		0.01826052		1148		0.0272137281		1148		0.0371755138		1148		0.0540789254		1148		0.0642481521		1148		0.0845416933

		1147		0.0148389144		1147		0.0266246498		1147		0.034941338		1147		0.0544604398		1147		0.0607840158		1147		0.0807101428

		1146		0.0185588915		1146		0.0264125019		1146		0.0356118008		1146		0.0544025786		1146		0.0648343489		1146		0.0844527632

		1145		0.0154256234		1145		0.0267348904		1145		0.0364098698		1145		0.0543271191		1145		0.0609825663		1145		0.0815211982

		1144		0.0186676178		1144		0.0275059622		1144		0.0356703326		1144		0.055426769		1144		0.0650284439		1144		0.0849782005

		1143		0.0177124087		1143		0.0270706881		1143		0.0369624942		1143		0.0543132164		1143		0.0621804297		1143		0.0833668709

		1142		0.0164257307		1142		0.0269219112		1142		0.0353308283		1142		0.0557974875		1142		0.0636444986		1142		0.0836198926

		1141		0.0190759636		1141		0.0276501942		1141		0.0363970622		1141		0.0542604178		1141		0.0637228787		1141		0.0855725482

		1140		0.0158632025		1140		0.0265738722		1140		0.0354659408		1140		0.0552181266		1140		0.0614417903		1140		0.0824047476

		1139		0.019108586		1139		0.0268689264		1139		0.0356447026		1139		0.0546486378		1139		0.0650032237		1139		0.0863748789

		1138		0.0161488075		1138		0.0267239343		1138		0.0355032161		1138		0.0545386784		1138		0.0606964268		1138		0.0829029903

		1137		0.0192652084		1137		0.0268582143		1137		0.0355974697		1137		0.0556685552		1137		0.0644523501		1137		0.0859528631

		1136		0.0185658336		1136		0.0278323386		1136		0.0372328199		1136		0.0554441512		1136		0.0634488538		1136		0.086034432

		1135		0.0174601842		1135		0.0277257636		1135		0.0350693427		1135		0.0557692014		1135		0.0630414709		1135		0.0850104392

		1134		0.0197713096		1134		0.026800856		1134		0.0366970077		1134		0.0548786223		1134		0.0644249693		1134		0.0870676711

		1133		0.0164933484		1133		0.0274068285		1133		0.0355836488		1133		0.0558716133		1133		0.0623658784		1133		0.0843440816

		1132		0.0198964644		1132		0.0270116516		1132		0.0356503539		1132		0.0549690127		1132		0.0648005083		1132		0.0876179859

		1131		0.0173971858		1131		0.0269384645		1131		0.0368632898		1131		0.0552402027		1131		0.0620042309		1131		0.0843875557

		1130		0.0195798408		1130		0.0275881272		1130		0.0353014283		1130		0.0563867912		1130		0.0650017783		1130		0.0883906558

		1129		0.0188590623		1129		0.027445212		1129		0.0369020663		1129		0.0548802093		1129		0.0631276146		1129		0.0865857974

		1128		0.0180138051		1128		0.0271327924		1128		0.0351814404		1128		0.0562245026		1128		0.0632427931		1128		0.08629217

		1127		0.02064416		1127		0.0275887065		1127		0.037316788		1127		0.0556142069		1127		0.0656765476		1127		0.0891356245

		1126		0.0164141711		1126		0.0271682851		1126		0.0345642753		1126		0.0556832068		1126		0.0612141453		1126		0.0851695165

		1125		0.0214261022		1125		0.0273034181		1125		0.0369687788		1125		0.0557041019		1125		0.0660837367		1125		0.0895384103

		1124		0.017294379		1124		0.0275078379		1124		0.0362937115		1124		0.0558231585		1124		0.0620086789		1124		0.0865386575

		1123		0.019982433		1123		0.0278537832		1123		0.0353866257		1123		0.0559321158		1123		0.0649726167		1123		0.0891391486

		1122		0.0188335162		1122		0.0272339024		1122		0.0373676792		1122		0.0549825542		1122		0.0631097481		1122		0.0878251418

		1121		0.0186955873		1121		0.0276374221		1121		0.0346420109		1121		0.0567316972		1121		0.0640023574		1121		0.0883350074

		1120		0.0200364292		1120		0.0275191441		1120		0.036971204		1120		0.0551481694		1120		0.0648513883		1120		0.089798592

		1119		0.0178113226		1119		0.027341295		1119		0.0355939865		1119		0.0563326217		1119		0.0622547567		1119		0.0871236026

		1118		0.0216798801		1118		0.0278667565		1118		0.0366898254		1118		0.05626617		1118		0.0666001663		1118		0.0917045623

		1117		0.0169976559		1117		0.0272022635		1117		0.0362011343		1117		0.0548440516		1117		0.0617027618		1117		0.0870254114

		1116		0.0208264571		1116		0.0274372418		1116		0.0357625447		1116		0.0564925894		1116		0.065438129		1116		0.0908968747

		1115		0.0186878312		1115		0.027581865		1115		0.0372172259		1115		0.0557905436		1115		0.0641200766		1115		0.0898436979

		1114		0.0187130999		1114		0.0273089036		1114		0.0343936346		1114		0.0559740178		1114		0.063168183		1114		0.0890288428

		1113		0.0203709919		1113		0.0273105018		1113		0.0375880413		1113		0.0557548106		1113		0.0650740936		1113		0.0917572901

		1112		0.0175723843		1112		0.0268990528		1112		0.0348011702		1112		0.0557662584		1112		0.0621993095		1112		0.0883417651

		1111		0.0215085931		1111		0.0277496595		1111		0.0362556949		1111		0.0558875091		1111		0.0657233745		1111		0.0924525857

		1110		0.0176496431		1110		0.0274696983		1110		0.0367809012		1110		0.0554565899		1110		0.0625382215		1110		0.0891506597

		1109		0.0205711424		1109		0.0271105282		1109		0.0349067748		1109		0.0562575646		1109		0.0653619021		1109		0.0921486542

		1108		0.0182797145		1108		0.027173575		1108		0.0368178412		1108		0.0546572693		1108		0.063504912		1108		0.0898981094

		1107		0.0195696875		1107		0.0274896082		1107		0.0352417678		1107		0.0566263981		1107		0.0638659522		1107		0.0916027129

		1106		0.0198800154		1106		0.0267390758		1106		0.0368619934		1106		0.0552304126		1106		0.0656133443		1106		0.092302531

		1105		0.0182526633		1105		0.0280115772		1105		0.0354685523		1105		0.0560328551		1105		0.0625283867		1105		0.0899281353

		1104		0.0221372377		1104		0.0278651826		1104		0.0372781456		1104		0.0566423237		1104		0.0668998882		1104		0.0950178876

		1103		0.0178943444		1103		0.0274845343		1103		0.0359681733		1103		0.0552579313		1103		0.0628458336		1103		0.0904898941

		1102		0.0211441256		1102		0.02820912		1102		0.0357934907		1102		0.0567090139		1102		0.0657750219		1102		0.0939264074

		1101		0.0192656685		1101		0.0275331009		1101		0.0377223902		1101		0.0558570996		1101		0.0643949136		1101		0.0928684324

		1100		0.0196120404		1100		0.0279256329		1100		0.0350029767		1100		0.0565877371		1100		0.0644891337		1100		0.0926445648

		1099		0.0210298337		1099		0.0278981682		1099		0.0378988385		1099		0.0560812764		1099		0.0661049858		1099		0.0945993364

		1098		0.0190819409		1098		0.0278460831		1098		0.0359874368		1098		0.0565442741		1098		0.0636045188		1098		0.0923363119

		1097		0.0216492414		1097		0.0281850901		1097		0.0370730795		1097		0.0564379059		1097		0.0669831485		1097		0.0959578305

		1096		0.0185896102		1096		0.0283851158		1096		0.0366267338		1096		0.0557738245		1096		0.063447386		1096		0.0924999192

		1095		0.0222206265		1095		0.0284429304		1095		0.0365378857		1095		0.0576079115		1095		0.066863291		1095		0.0959338471

		1094		0.0184557829		1094		0.027593147		1094		0.0372070447		1094		0.0551094934		1094		0.0643960535		1094		0.0937590375

		1093		0.0218004677		1093		0.0298680738		1093		0.0366287343		1093		0.0580660626		1093		0.0658725947		1093		0.0956071839

		1092		0.0199178476		1092		0.0273160711		1092		0.0376848988		1092		0.0558439121		1092		0.0662138089		1092		0.0961882249

		1091		0.0199330505		1091		0.0288017373		1091		0.0363360681		1091		0.0570608452		1091		0.064667128		1091		0.09424036

		1090		0.0220545735		1090		0.0291600674		1090		0.0375525914		1090		0.0570304096		1090		0.0679106116		1090		0.0982633606

		1089		0.0187192354		1089		0.0275288262		1089		0.0368792117		1089		0.0560687259		1089		0.0640241951		1089		0.0941412523

		1088		0.0220273398		1088		0.0293433163		1088		0.0363775305		1088		0.0580169447		1088		0.0677704662		1088		0.0983252972

		1087		0.0198625103		1087		0.0285306629		1087		0.0383781902		1087		0.0560998619		1087		0.0657651797		1087		0.0966971144

		1086		0.0216973219		1086		0.0292530377		1086		0.0364614464		1086		0.0586077906		1086		0.0662908181		1086		0.0971668363

		1085		0.0207717102		1085		0.0288254432		1085		0.0384242311		1085		0.056553591		1085		0.0679694265		1085		0.0985829309

		1084		0.0201996788		1084		0.0288907606		1084		0.0364655256		1084		0.0570297614		1084		0.0649836212		1084		0.09604498

		1083		0.0227321237		1083		0.0294742249		1083		0.0383595303		1083		0.0580789037		1083		0.0687904358		1083		0.1003544256

		1082		0.0188375171		1082		0.028194895		1082		0.0367167294		1082		0.0560641624		1082		0.0651049167		1082		0.0959592834

		1081		0.0229488388		1081		0.0307759773		1081		0.0379011854		1081		0.0584858656		1081		0.0686771423		1081		0.1001683623

		1080		0.0192941353		1080		0.0274782199		1080		0.0376795605		1080		0.0562371165		1080		0.0662848502		1080		0.0980800763

		1079		0.0224299729		1079		0.030760806		1079		0.0374135003		1079		0.0590338707		1079		0.0677993298		1079		0.0992016792

		1078		0.0212408882		1078		0.0293033253		1078		0.0387663916		1078		0.0568953231		1078		0.068394579		1078		0.1010048985

		1077		0.0207225382		1077		0.029267963		1077		0.0369825885		1077		0.0583704598		1077		0.0662026554		1077		0.0983952954

		1076		0.0228517503		1076		0.030592151		1076		0.0388641879		1076		0.0585523322		1076		0.0698635504		1076		0.1020407304

		1075		0.0196991991		1075		0.0290066153		1075		0.037545111		1075		0.0569487102		1075		0.06597922		1075		0.0990945101

		1074		0.0232802182		1074		0.0307375789		1074		0.0377125367		1074		0.0595180206		1074		0.0694687218		1074		0.1017681435

		1073		0.0200640541		1073		0.0287345834		1073		0.0387543887		1073		0.0570006855		1073		0.067966938		1073		0.100917697

		1072		0.0224482901		1072		0.0309951324		1072		0.0369325876		1072		0.0588076338		1072		0.067719698		1072		0.1006560549

		1071		0.0215381607		1071		0.0294490699		1071		0.0392688289		1071		0.0578453839		1071		0.069678247		1071		0.103183724

		1070		0.0208740942		1070		0.0299261417		1070		0.0366174392		1070		0.0581133179		1070		0.0670106933		1070		0.0996701792

		1069		0.0229090787		1069		0.0310992878		1069		0.0389306918		1069		0.0589310974		1069		0.0703516528		1069		0.10438779

		1068		0.020270111		1068		0.0289665181		1068		0.0372760296		1068		0.0574058704		1068		0.0670758784		1068		0.1009986922

		1067		0.0236581266		1067		0.0321797878		1067		0.0384291522		1067		0.0604803003		1067		0.0708527044		1067		0.1042844653

		1066		0.0203400124		1066		0.0289035421		1066		0.0387703516		1066		0.0569931306		1066		0.0682537332		1066		0.1029006019

		1065		0.0227678847		1065		0.0310521014		1065		0.0368275344		1065		0.0602924414		1065		0.0686859637		1065		0.1030568555

		1064		0.0215836726		1064		0.0302952249		1064		0.0390346423		1064		0.0577861816		1064		0.0707474947		1064		0.105002135

		1063		0.0209956821		1063		0.0299112499		1063		0.0369382836		1063		0.0587720349		1063		0.067190811		1063		0.1025876701

		1062		0.0225048009		1062		0.0308708809		1062		0.0384697057		1062		0.0590499155		1062		0.0710655227		1062		0.1056810096

		1061		0.0205317624		1061		0.0295527987		1061		0.0374659263		1061		0.0581303053		1061		0.0680574328		1061		0.1031681597

		1060		0.0230891351		1060		0.0315262042		1060		0.0379411839		1060		0.059864562		1060		0.0699468032		1060		0.1056158021

		1059		0.0209602006		1059		0.0294217281		1059		0.0386374891		1059		0.058124505		1059		0.0697727427		1059		0.1051599756

		1058		0.023004951		1058		0.0315634236		1058		0.0372487269		1058		0.0599831268		1058		0.0695543289		1058		0.1048469618

		1057		0.020866815		1057		0.0297000688		1057		0.0387604199		1057		0.0577588566		1057		0.0703781918		1057		0.106640473

		1056		0.0223458074		1056		0.0305602662		1056		0.0369700454		1056		0.0597237199		1056		0.0685246214		1056		0.1049652472

		1055		0.022098586		1055		0.031328734		1055		0.0386467129		1055		0.0589638315		1055		0.0717491731		1055		0.1075143442

		1054		0.0207933802		1054		0.0296780337		1054		0.0377312005		1054		0.0583595336		1054		0.0684216395		1054		0.1057765707

		1053		0.0238833726		1053		0.0320376418		1053		0.0381786823		1053		0.0610690825		1053		0.0713663623		1053		0.1078236476

		1052		0.020209603		1052		0.0292183179		1052		0.0379683599		1052		0.0572168604		1052		0.0694244951		1052		0.1067476347

		1051		0.0232592989		1051		0.032125406		1051		0.0377143733		1051		0.0609739013		1051		0.0699153915		1051		0.1074834093

		1050		0.021671962		1050		0.0306955706		1050		0.0389756262		1050		0.0593036972		1050		0.0719445869		1050		0.1096740663

		1049		0.0215258114		1049		0.0301359333		1049		0.0364483818		1049		0.0586157292		1049		0.0684645846		1049		0.1060737669

		1048		0.0226488002		1048		0.0322236679		1048		0.0392309763		1048		0.0605937652		1048		0.0723065734		1048		0.1108390838

		1047		0.0207830891		1047		0.0284918807		1047		0.0368368886		1047		0.0579739325		1047		0.0683817044		1047		0.1067352518

		1046		0.0233918279		1046		0.0323346443		1046		0.0379787572		1046		0.0603998527		1046		0.0718382299		1046		0.1099007502

		1045		0.0206964463		1045		0.0297368523		1045		0.0387857482		1045		0.0582103618		1045		0.0700758174		1045		0.1098926514

		1044		0.0235354099		1044		0.0312889218		1044		0.0365744382		1044		0.0607283674		1044		0.0703780726		1044		0.1090409309

		1043		0.0207659267		1043		0.0308779124		1043		0.0390644073		1043		0.0582698882		1043		0.0719091222		1043		0.111212492

		1042		0.0225870889		1042		0.0307322722		1042		0.0369262211		1042		0.0605980493		1042		0.0694922954		1042		0.1093630791

		1041		0.0226928182		1041		0.0315640904		1041		0.0387465209		1041		0.0598072819		1041		0.072580643		1041		0.1121845022

		1040		0.020658819		1040		0.0290798191		1040		0.0371708907		1040		0.0587116405		1040		0.0694219768		1040		0.1095527261

		1039		0.0240455586		1039		0.0329333395		1039		0.0386889055		1039		0.0613937825		1039		0.0722520575		1039		0.1126425713

		1038		0.0201725066		1038		0.0287442897		1038		0.0374464281		1038		0.0578580722		1038		0.0706765801		1038		0.1113874912

		1037		0.0234525874		1037		0.0315852202		1037		0.0370745994		1037		0.0608482137		1037		0.0708631575		1037		0.1108458042

		1036		0.0212798994		1036		0.0310035851		1036		0.0390923358		1036		0.0588220358		1036		0.0722691789		1036		0.113999173

		1035		0.0221570414		1035		0.029490266		1035		0.0358294472		1035		0.0596339107		1035		0.0693941861		1035		0.1105602533

		1034		0.0224869996		1034		0.0318789072		1034		0.0389805809		1034		0.0599156097		1034		0.0731774345		1034		0.1143440828

		1033		0.0211214349		1033		0.0292413812		1033		0.0375403166		1033		0.0589011274		1033		0.0697968453		1033		0.1122381315

		1032		0.023288548		1032		0.0319296084		1032		0.0377025418		1032		0.0606696345		1032		0.0723648816		1032		0.1135343984

		1031		0.0205959231		1031		0.0292498264		1031		0.0384772867		1031		0.0582647659		1031		0.0713326186		1031		0.1140832901

		1030		0.0231477227		1030		0.031227611		1030		0.0370828323		1030		0.0610637181		1030		0.0710190311		1030		0.1131856665

		1029		0.021042902		1029		0.030351324		1029		0.0384916551		1029		0.0585646853		1029		0.0725042894		1029		0.115715757

		1028		0.0223799832		1028		0.0300716795		1028		0.0369542353		1028		0.0599622056		1028		0.0704437643		1028		0.113293983

		1027		0.0227948111		1027		0.0323061719		1027		0.0393740237		1027		0.0605507307		1027		0.0735071152		1027		0.1170392781

		1026		0.0214724448		1026		0.0285753105		1026		0.0365229063		1026		0.058657147		1026		0.0702661276		1026		0.1140865907

		1025		0.0233336426		1025		0.0322202668		1025		0.0383295007		1025		0.0611151159		1025		0.0731078982		1025		0.1164781451

		1024		0.0209373292		1024		0.0293243732		1024		0.0381536409		1024		0.0585530437		1024		0.0712644383		1024		0.1160177067

		1023		0.0232188813		1023		0.0306079276		1023		0.0366036408		1023		0.0607802048		1023		0.0717953146		1023		0.1153274924

		1022		0.0212292001		1022		0.0308802463		1022		0.0392498188		1022		0.0589196235		1022		0.073310785		1022		0.1181866303

		1021		0.0224061217		1021		0.0294304825		1021		0.0363479741		1021		0.0601594597		1021		0.0705218911		1021		0.1153215468

		1020		0.0223283395		1020		0.031760864		1020		0.0390078537		1020		0.0599065758		1020		0.0743205249		1020		0.1186884269

		1019		0.0215182211		1019		0.0290944055		1019		0.0375959165		1019		0.0594391786		1019		0.0713958666		1019		0.1171426624

		1018		0.0230791159		1018		0.0320845172		1018		0.0380407721		1018		0.0612651445		1018		0.073494792		1018		0.1182946414

		1017		0.0212482009		1017		0.0293960795		1017		0.0380181707		1017		0.0588732585		1017		0.072587654		1017		0.1189904064

		1016		0.0234004594		1016		0.031583216		1016		0.0373708978		1016		0.0615544356		1016		0.0728073791		1016		0.1181320921

		1015		0.0218080077		1015		0.0311531275		1015		0.0392541252		1015		0.0597348288		1015		0.0740399808		1015		0.121099472

		1014		0.0224204864		1014		0.029345559		1014		0.0365415215		1014		0.0605416261		1014		0.0717663392		1014		0.1176921949

		1013		0.0227176398		1013		0.0322902799		1013		0.0395598225		1013		0.060517434		1013		0.0753009021		1013		0.1213332266

		1012		0.0214792713		1012		0.0287427139		1012		0.0369976126		1012		0.0596375614		1012		0.071591638		1012		0.1192681342

		1011		0.0236080252		1011		0.0318731107		1011		0.0381359495		1011		0.0615366586		1011		0.0747917071		1011		0.1209386438

		1010		0.021141082		1010		0.029445773		1010		0.0385128409		1010		0.0589727275		1010		0.073376745		1010		0.1214581132

		1009		0.0232621655		1009		0.0309996922		1009		0.0364345871		1009		0.0614840165		1009		0.0725516751		1009		0.1203598455

		1008		0.0220825709		1008		0.0314124599		1008		0.0399235934		1008		0.0603418462		1008		0.0756356791		1008		0.1237189472

		1007		0.0223943479		1007		0.0295183025		1007		0.0369069986		1007		0.0606085882		1007		0.0721175671		1007		0.1203973144

		1006		0.0225056205		1006		0.0326778442		1006		0.0393762626		1006		0.060814891		1006		0.0761011094		1006		0.1236122996

		1005		0.0227038376		1005		0.0291761234		1005		0.037791431		1005		0.060560137		1005		0.0734482855		1005		0.1224845126

		1004		0.0230489802		1004		0.0320518799		1004		0.0383564197		1004		0.0614768304		1004		0.0755463392		1004		0.123145096

		1003		0.0220866017		1003		0.030359596		1003		0.0387125611		1003		0.0603979789		1003		0.0745991543		1003		0.1248339266

		1002		0.0233354457		1002		0.0313488208		1002		0.0375841483		1002		0.0619420968		1002		0.0747626796		1002		0.1231255084

		1001		0.0220093932		1001		0.0316569097		1001		0.0401345268		1001		0.0604669079		1001		0.0762146264		1001		0.1258665174

		1000		0.0229832269		1000		0.0301569663		1000		0.0368854403		1000		0.0619282462		1000		0.0735214651		1000		0.1236538962

		999		0.0233435854		999		0.0331540927		999		0.0403170697		999		0.0614395849		999		0.0779692158		999		0.1268452853

		998		0.0221822392		998		0.0293098055		998		0.0378554538		998		0.0615057275		998		0.0742389783		998		0.1251396984

		997		0.0239580162		997		0.0332921632		997		0.0390345864		997		0.0624751449		997		0.0772025436		997		0.126760751

		996		0.0224561952		996		0.0308446176		996		0.0393944904		996		0.0614804998		996		0.0764318481		996		0.1272455901

		995		0.0232783072		995		0.0312783234		995		0.0381824412		995		0.0622278377		995		0.0757689252		995		0.1259020418

		994		0.0232085325		994		0.0331270732		994		0.040923439		994		0.0622470193		994		0.0785818398		994		0.1297174543

		993		0.0239272434		993		0.0310543254		993		0.0385104939		993		0.0630610436		993		0.0761632621		993		0.1269052625

		992		0.02272694		992		0.0334835947		992		0.0405296981		992		0.0622693338		992		0.0793489963		992		0.1298723519

		991		0.0240085963		991		0.031184027		991		0.0389104485		991		0.0634963736		991		0.076065734		991		0.1293778419

		990		0.0237290412		990		0.0337086804		990		0.0394736342		990		0.0627496615		990		0.079503566		990		0.1293984056

		989		0.0233914722		989		0.0321726799		989		0.0407448188		989		0.0632229447		989		0.0778649673		989		0.1310017258

		988		0.0241035912		988		0.0326333865		988		0.0386900343		988		0.0637084618		988		0.0780906975		988		0.1295971125

		987		0.0239738543		987		0.0342214033		987		0.0418615863		987		0.0636415034		987		0.0810280964		987		0.1327082366

		986		0.0233163256		986		0.0309887398		986		0.0390054174		986		0.0635532439		986		0.0770343021		986		0.1299574673

		985		0.0249699559		985		0.0355022326		985		0.0416576229		985		0.0643099844		985		0.0819057599		985		0.1339596361

		984		0.0233320035		984		0.0313489623		984		0.0397675708		984		0.0636039153		984		0.0776860639		984		0.131747067

		983		0.0243012533		983		0.0346702449		983		0.0406820998		983		0.0638680235		983		0.0810876787		983		0.1328459978

		982		0.0242096651		982		0.0339314192		982		0.0417553633		982		0.0652652904		982		0.0801208466		982		0.1350913048

		981		0.024438018		981		0.0331100598		981		0.0396226905		981		0.0642074868		981		0.0807297453		981		0.1326275319

		980		0.0238948334		980		0.0350716151		980		0.0428896509		980		0.064623177		980		0.0820774958		980		0.1363230646

		979		0.0250137448		979		0.0327264368		979		0.0397162251		979		0.0655379072		979		0.0797266364		979		0.1340199709

		978		0.0242330395		978		0.0356341116		978		0.0421011858		978		0.0647182018		978		0.0837388784		978		0.1366714239

		977		0.0247127153		977		0.0329902284		977		0.0411841161		977		0.0656770915		977		0.0798511803		977		0.1361442804

		976		0.0249639228		976		0.0356375687		976		0.04098434		976		0.065588057		976		0.0835996494		976		0.1367302835

		975		0.0247864034		975		0.0344848186		975		0.0428712778		975		0.0656205714		975		0.0821005181		975		0.1379794478

		974		0.0247423649		974		0.0336313658		974		0.0406163223		974		0.0656690821		974		0.0825116038		974		0.1365795881

		973		0.0252733864		973		0.0365757607		973		0.0434670933		973		0.0668510273		973		0.0842826888		973		0.140210256

		972		0.0250981264		972		0.033089444		972		0.040883448		972		0.0658942536		972		0.0821359158		972		0.1374678016

		971		0.0253297184		971		0.0368526951		971		0.0435250066		971		0.0668187887		971		0.0860682949		971		0.1404676139

		970		0.02544556		970		0.0340157598		970		0.0420104116		970		0.0670580268		970		0.0820780322		970		0.1398915201

		969		0.0250400957		969		0.0363809913		969		0.0421246849		969		0.0664278343		969		0.0862796977		969		0.1402439624

		968		0.0264812242		968		0.0363520831		968		0.04459887		968		0.068362765		968		0.0847150385		968		0.1431501657

		967		0.0248675607		967		0.0346860848		967		0.0409366079		967		0.0667811409		967		0.08444006		967		0.1403114349

		966		0.026079027		966		0.0374138951		966		0.0442093201		966		0.0679259822		966		0.0865511671		966		0.1439772695

		965		0.026253501		965		0.0344313495		965		0.0426991992		965		0.0681108758		965		0.0844701156		965		0.142090112

		964		0.0257035922		964		0.0378763862		964		0.0430187061		964		0.0676571354		964		0.0875516012		964		0.1441133618

		963		0.0264168475		963		0.0352719463		963		0.0434706695		963		0.0689022392		963		0.0851349086		963		0.1438892186

		962		0.025226526		962		0.0365247652		962		0.042867966		962		0.0675478578		962		0.0876782313		962		0.1436070055

		961		0.0273340717		961		0.0372006148		961		0.0443553664		961		0.0700464621		961		0.0865611583		961		0.1465016454

		960		0.0255548172		960		0.0351883732		960		0.042574551		960		0.0677033886		960		0.0876822546		960		0.1440403163

		959		0.0269914046		959		0.0383494049		959		0.0450941771		959		0.069656454		959		0.0885476768		959		0.147678256

		958		0.0263216756		958		0.0350168087		958		0.0425031185		958		0.0686247796		958		0.0861423984		958		0.145547837

		957		0.0264393799		957		0.03868163		957		0.044423379		957		0.069458209		957		0.090610683		957		0.1478829235

		956		0.02770162		956		0.0362831317		956		0.0448653251		956		0.0702941567		956		0.0870259851		956		0.1484150738

		955		0.0258129425		955		0.0370845832		955		0.0425620154		955		0.0689840987		955		0.0899816006		955		0.1472854167

		954		0.0280528571		954		0.0379769467		954		0.0457660444		954		0.0711676106		954		0.0888992474		954		0.1506695151

		953		0.026263291		953		0.0359523408		953		0.0433293805		953		0.069411099		953		0.0894203037		953		0.1482399851

		952		0.0284413006		952		0.0388792194		952		0.044962611		952		0.0712777078		952		0.0903567672		952		0.1512095481

		951		0.0275272541		951		0.036213655		951		0.0447439849		951		0.0706230923		951		0.0896157548		951		0.1503032744

		950		0.0279983524		950		0.0390557721		950		0.0449063703		950		0.0712972656		950		0.0919188634		950		0.1522549987

		949		0.0289231315		949		0.0375608057		949		0.045839943		949		0.0723837241		949		0.089488849		949		0.1528936923

		948		0.0270517338		948		0.0385646932		948		0.0447119921		948		0.0712811872		948		0.093135871		948		0.1523079723

		947		0.029799616		947		0.039027337		947		0.0466950983		947		0.0731431842		947		0.0908125341		947		0.1552272588

		946		0.0279999524		946		0.0379284695		946		0.0448178798		946		0.0718317553		946		0.0932771042		946		0.1531504691

		945		0.0300753694		945		0.040258985		945		0.0469428822		945		0.0735037774		945		0.0932649374		945		0.1564560533

		944		0.027733352		944		0.0369683281		944		0.0451306514		944		0.0720010176		944		0.0915948823		944		0.1547168791

		943		0.0300740637		943		0.0412162803		943		0.0462146588		943		0.0738894343		943		0.0953292772		943		0.157390222

		942		0.0300173629		942		0.0388037525		942		0.0477345921		942		0.0743430704		942		0.0928897783		942		0.1581119448

		941		0.0283942632		941		0.0392391644		941		0.0451199375		941		0.0727647394		941		0.0954424217		941		0.1567387581

		940		0.0316596106		940		0.0411579646		940		0.0481886864		940		0.0765017047		940		0.0945205241		940		0.1605974883

		939		0.028585013		939		0.0382464938		939		0.0462300628		939		0.0724450424		939		0.0958967209		939		0.1576271653

		938		0.0311526265		938		0.0413275287		938		0.0474796258		938		0.07661286		938		0.0954072401		938		0.1614559889

		937		0.0301080774		937		0.0389630832		937		0.0471052006		937		0.0742332339		937		0.0957400203		937		0.1600443274

		936		0.0304830913		936		0.0415619873		936		0.0476769842		936		0.0755851865		936		0.0973554701		936		0.1618371755

		935		0.0309670828		935		0.0395603031		935		0.048703894		935		0.0761345774		935		0.0957903639		935		0.1628648639

		934		0.030512305		934		0.0414542668		934		0.0470222309		934		0.0753508061		934		0.0990528166		934		0.1622496843

		933		0.0321998894		933		0.0416640341		933		0.0494166389		933		0.07773491		933		0.0971665159		933		0.1646973938

		932		0.0296379291		932		0.039413169		932		0.0469322689		932		0.0753532127		932		0.0981197879		932		0.1632961035

		931		0.0335290059		931		0.0438385643		931		0.049761828		931		0.0787328407		931		0.0997929275		931		0.1669431031

		930		0.03009809		930		0.0391496383		930		0.0482592955		930		0.0760059059		930		0.0983449668		930		0.1647882611

		929		0.0321205817		929		0.0426314846		929		0.0488397852		929		0.078206256		929		0.1000351459		929		0.1671643555

		928		0.0324900597		928		0.0415568873		928		0.0494075902		928		0.0779300332		928		0.0994608775		928		0.167761296

		927		0.030247543		927		0.040485397		927		0.0481250323		927		0.0768937394		927		0.1010592878		927		0.1660653204

		926		0.0335661136		926		0.0423614047		926		0.0500463135		926		0.0795455649		926		0.0995092168		926		0.1700211763

		925		0.0305397138		925		0.0401552245		925		0.0482081845		925		0.0766374692		925		0.1015622765		925		0.1674840003

		924		0.033732459		924		0.0434347652		924		0.0502536483		924		0.0802384093		924		0.1013705656		924		0.1711654514

		923		0.0318117477		923		0.0412510633		923		0.0498381518		923		0.0779032111		923		0.101430133		923		0.1707951725

		922		0.0333806276		922		0.0432022661		922		0.0493351705		922		0.0801360682		922		0.1032571942		922		0.171257019

		921		0.0324843675		921		0.0420882367		921		0.0512689911		921		0.0798160955		921		0.1022335291		921		0.1726950705

		920		0.0322254822		920		0.042353753		920		0.0490907095		920		0.079354465		920		0.1039756685		920		0.171845004

		919		0.0343138427		919		0.0429997295		919		0.0505339764		919		0.0811640322		919		0.1028508693		919		0.1745842695

		918		0.0309355035		918		0.0409734994		918		0.0495644212		918		0.0785034299		918		0.1042860821		918		0.1724676341

		917		0.0350084752		917		0.0441971421		917		0.0508935601		917		0.0829237625		917		0.1042547822		917		0.17633228

		916		0.0311718434		916		0.0409436896		916		0.0495708622		916		0.0780772194		916		0.1040746048		916		0.1741330922

		915		0.0334491208		915		0.043230202		915		0.0499623157		915		0.0822614133		915		0.1056017056		915		0.1757653654

		914		0.0338563882		914		0.0430583209		914		0.0517241172		914		0.0814411342		914		0.1052526534		914		0.1780044734

		913		0.0320123658		913		0.0418573394		913		0.0491459854		913		0.0801206604		913		0.1066710129		913		0.1754311919

		912		0.0344834998		912		0.0433954857		912		0.0512915961		912		0.083110109		912		0.105592005		912		0.1793951243

		911		0.0321024917		911		0.0416369401		911		0.0503240116		911		0.0805140138		911		0.1074645445		911		0.1774719507

		910		0.0341183171		910		0.0438389368		910		0.0503515676		910		0.0832042471		910		0.106532447		910		0.1797287166

		909		0.0319749154		909		0.0417251848		909		0.051364664		909		0.0809148028		909		0.1078548357		909		0.1793819368

		908		0.0344283246		908		0.0435851589		908		0.0504104607		908		0.0835746452		908		0.1081340984		908		0.1807301342

		907		0.0330145284		907		0.0430979393		907		0.0516461507		907		0.0829437524		907		0.1082003787		907		0.1817357987

		906		0.0329821557		906		0.0424525626		906		0.0503888615		906		0.0824731663		906		0.1093598828		906		0.1809235811

		905		0.0350259282		905		0.0440909714		905		0.0516672581		905		0.0847722441		905		0.108635284		905		0.1846158952

		904		0.0315393992		904		0.0417867117		904		0.0501002297		904		0.0815457776		904		0.1098113135		904		0.1815799326

		903		0.0352508053		903		0.0445389487		903		0.0517858528		903		0.0858848095		903		0.1100148559		903		0.1850457937

		902		0.0322283246		902		0.0428532511		902		0.0515170433		902		0.0826122835		902		0.1109435782		902		0.1844771653

		901		0.0342541188		901		0.0430820733		901		0.0503422953		901		0.0848607272		901		0.1109583825		901		0.1845655292

		900		0.0339596607		900		0.0442047343		900		0.0530437194		900		0.0855671614		900		0.1124227941		900		0.1877634525

		899		0.0330499187		899		0.0418871567		899		0.0499338284		899		0.0836343616		899		0.1116242111		899		0.1852576733

		898		0.0352857038		898		0.0454720147		898		0.0525049977		898		0.086834386		898		0.1127623618		898		0.1897767186

		897		0.0320312306		897		0.0418133326		897		0.0511124805		897		0.0841073766		897		0.1133662984		897		0.1872404069

		896		0.0362751111		896		0.0456793047		896		0.0519351996		896		0.0879299715		896		0.1135808304		896		0.1910487413

		895		0.0320976153		895		0.0428158827		895		0.0519447103		895		0.0844597742		895		0.1147633716		895		0.1891965419

		894		0.0358455554		894		0.0447307564		894		0.0518520623		894		0.0885446668		894		0.1149810925		894		0.191403687

		893		0.0341773219		893		0.0448021255		893		0.0528659523		893		0.08711683		893		0.1153826267		893		0.1927874833

		892		0.0337706208		892		0.0428305939		892		0.0513194762		892		0.0867133439		892		0.1160646081		892		0.191223681

		891		0.0356720202		891		0.0455686636		891		0.0529353954		891		0.0891504958		891		0.1160199717		891		0.1951057613

		890		0.0328558274		890		0.0425241291		890		0.0515375026		890		0.086018905		890		0.1169722453		890		0.1928564906

		889		0.0367470682		889		0.0466029532		889		0.0530969836		889		0.0906949788		889		0.1181964874		889		0.1968017071

		888		0.0328992754		888		0.0434707254		888		0.0530736707		888		0.0870028287		888		0.1182086468		888		0.1954101175

		887		0.0365969949		887		0.0447732545		887		0.0524640419		887		0.0905604511		887		0.1188994125		887		0.1970769465

		886		0.0338992626		886		0.0457006134		886		0.0533437692		886		0.0891319364		886		0.1199857667		886		0.1986207366

		885		0.0344920754		885		0.0431201234		885		0.0525590144		885		0.0893653482		885		0.1195935905		885		0.197290659

		884		0.035809543		884		0.0463014208		884		0.0528560691		884		0.0911716968		884		0.1203051731		884		0.2008921951

		883		0.0331554301		883		0.0439226441		883		0.0531803593		883		0.0887784958		883		0.1219912022		883		0.1995779872

		882		0.036554981		882		0.0458847657		882		0.0529914834		882		0.0930843279		882		0.1209083796		882		0.2023147494

		881		0.0333485641		881		0.0445873961		881		0.0535578355		881		0.0894330591		881		0.1228071377		881		0.2019283175

		880		0.0364784487		880		0.0457756221		880		0.0531176068		880		0.0935424864		880		0.1229997277		880		0.2032119781

		879		0.0344223268		879		0.0454311743		879		0.0538210571		879		0.0914519951		879		0.1230019629		879		0.2052371204

		878		0.0353618264		878		0.0443796813		878		0.0527749471		878		0.0922685638		878		0.1241477281		878		0.2038139254

		877		0.0365987979		877		0.047554709		877		0.0545584895		877		0.0944525003		877		0.125644207		877		0.2080340087

		876		0.0337754637		876		0.0438402817		876		0.0535095222		876		0.0914443582		876		0.1256049722		876		0.2055419385

		875		0.037514858		875		0.0473462381		875		0.053866595		875		0.0957471505		875		0.1259600222		875		0.2093515098

		874		0.0339520201		874		0.0453534648		874		0.05467638		874		0.092309542		874		0.1274392605		874		0.2088247687

		873		0.0368280113		873		0.045451723		873		0.0533275828		873		0.0962245986		873		0.1267767251		873		0.2094249576

		872		0.0352848619		872		0.0470022149		872		0.0549047962		872		0.0939371362		872		0.128066957		872		0.2125790268

		871		0.0360999405		871		0.0450593419		871		0.0543613248		871		0.095593214		871		0.1294115931		871		0.2107034624

		870		0.0364029482		870		0.0476894937		870		0.0546804331		870		0.0966097042		870		0.1292847395		870		0.2149847597

		869		0.034905035		869		0.0449547134		869		0.0545586944		869		0.0949621573		869		0.1303644031		869		0.2130291611

		868		0.0375582948		868		0.0477941446		868		0.054886464		868		0.0981247872		868		0.1312481016		868		0.2161075026

		867		0.0344652012		867		0.0452203564		867		0.0549841113		867		0.0953270867		867		0.1309567988		867		0.2163901776

		866		0.0379917808		866		0.0474226549		866		0.0547703095		866		0.0988826901		866		0.1327349544		866		0.2172816098

		865		0.035355594		865		0.0472943932		865		0.0553721562		865		0.096741654		865		0.1329673231		865		0.2192222774

		864		0.036784254		864		0.0450085476		864		0.054799851		864		0.0981362686		864		0.1331419796		864		0.2179863453

		863		0.0377380066		863		0.0494769178		863		0.0559272878		863		0.0996699184		863		0.1352564692		863		0.2230722308

		862		0.0353670493		862		0.045275256		862		0.0558333732		862		0.0978382677		862		0.1352489144		862		0.2203307152

		861		0.0387538225		861		0.0479027256		861		0.056209065		861		0.1013964564		861		0.1364128143		861		0.2238194495

		860		0.0353227966		860		0.0469058528		860		0.0561417788		860		0.0986601189		860		0.137196511		860		0.2244885266

		859		0.0384419337		859		0.0467902571		859		0.0562278032		859		0.1019400954		859		0.1378662437		859		0.22408472

		858		0.0363634825		858		0.0480834469		858		0.0563162342		858		0.0999809802		858		0.1384673715		858		0.2280563414

		857		0.0370873734		857		0.0461157672		857		0.0559547879		857		0.1010514125		857		0.1390044689		857		0.2259023488

		856		0.037486583		856		0.0496153161		856		0.057093937		856		0.1020869985		856		0.1403492391		856		0.2302302867

		855		0.0365818143		855		0.0458540395		855		0.0570786744		855		0.1015298367		855		0.1409746855		855		0.2289745212

		854		0.0391099267		854		0.0495426878		854		0.0567931458		854		0.1039032191		854		0.1420577615		854		0.2319033146

		853		0.0359270908		853		0.0472123399		853		0.0574926511		853		0.1017051265		853		0.1427724808		853		0.2323002666

		852		0.0393966138		852		0.047749415		852		0.0567861535		852		0.1048955023		852		0.1437316537		852		0.2327008992

		851		0.0369290672		851		0.0493067801		851		0.0577491596		851		0.1029887944		851		0.1445338726		851		0.2362546772

		850		0.0382609963		850		0.0469814725		850		0.0574383698		850		0.1046385765		850		0.1461582929		850		0.2344814986

		849		0.0393405259		849		0.0503524952		849		0.0580479838		849		0.1056562811		849		0.1465219259		849		0.2393410355

		848		0.0371339805		848		0.0469062589		848		0.0579008087		848		0.1040205285		848		0.1474452615		848		0.237543121

		847		0.039554663		847		0.0489136837		847		0.0577137694		847		0.1063116714		847		0.1480122209		847		0.2398798615

		846		0.0375111625		846		0.0485405996		846		0.058530204		846		0.1056259423		846		0.149598971		846		0.2415284812

		845		0.0394525975		845		0.048123382		845		0.0578971095		845		0.1072754115		845		0.1498893499		845		0.2414369434

		844		0.0378438756		844		0.0498301648		844		0.0587355532		844		0.1058525369		844		0.1514980644		844		0.2446530461

		843		0.0398803465		843		0.0477625057		843		0.0595160015		843		0.1084540412		843		0.1527103037		843		0.2440104485

		842		0.0390603878		842		0.0507221669		842		0.0583939142		842		0.1079474613		842		0.1536680013		842		0.2480585426

		841		0.0384042077		841		0.0477869213		841		0.0601588078		841		0.1079805195		841		0.15500471		841		0.2468549162

		840		0.0406760164		840		0.0500301048		840		0.058796104		840		0.1096896306		840		0.1551590562		840		0.2493839115

		839		0.0378373526		839		0.0492216498		839		0.059405636		839		0.1078204289		839		0.1567445546		839		0.251029253

		838		0.0405744575		838		0.0490965955		838		0.0597544312		838		0.110428378		838		0.157911703		838		0.2509521246

		837		0.0394442342		837		0.0506104939		837		0.0600153133		837		0.1098071486		837		0.1590992212		837		0.2554274797

		836		0.0396484397		836		0.048039265		836		0.0601917505		836		0.1106249988		836		0.1603599638		836		0.2533415556

		835		0.0403142571		835		0.0518749319		835		0.0604710467		835		0.111730665		835		0.1618780196		835		0.2578961253

		834		0.0395813435		834		0.048015587		834		0.0607178286		834		0.1111835688		834		0.1624550819		834		0.2573491037

		833		0.040529754		833		0.0508889593		833		0.0602781959		833		0.1122606248		833		0.1637316346		833		0.2588905394

		832		0.0395525619		832		0.0501029305		832		0.0610610656		832		0.1117942482		832		0.1654631644		832		0.2616387606

		831		0.0414750837		831		0.0498166941		831		0.0614678823		831		0.1138090938		831		0.1659020036		831		0.2614023387

		830		0.0397535264		830		0.0518946797		830		0.0605813265		830		0.1124275923		830		0.1680436879		830		0.265966773

		829		0.0413545482		829		0.0493718572		829		0.0620496161		829		0.1146411672		829		0.1691610366		829		0.2634245157

		828		0.0409292691		828		0.0517727584		828		0.0614149533		828		0.1144150272		828		0.1697587371		828		0.2689459324

		827		0.0403209329		827		0.0501588285		827		0.0616006702		827		0.1140535697		827		0.1719143391		827		0.2673794329

		826		0.0421527252		826		0.0514578223		826		0.0621735901		826		0.1159975231		826		0.1732019484		826		0.2704018652

		825		0.0406678021		825		0.051293198		825		0.0623315126		825		0.115156807		825		0.1743091643		825		0.272746563

		824		0.0422172248		824		0.0508218817		824		0.0621619709		824		0.1161513552		824		0.176002413		824		0.2722323835

		823		0.040866524		823		0.0527794771		823		0.062959291		823		0.116492562		823		0.1774284393		823		0.2767679691

		822		0.0418676883		822		0.0498327203		822		0.0627702102		822		0.1171776503		822		0.1782903671		822		0.275049448

		821		0.0416416414		821		0.0531914197		821		0.0626314133		821		0.1172840148		821		0.1800071895		821		0.2800026834

		820		0.0417870246		820		0.0510536917		820		0.0636107176		820		0.1183701381		820		0.182021752		820		0.2794111669

		819		0.0425001495		819		0.0523668714		819		0.0630154908		819		0.1184528247		819		0.1824249327		819		0.2821358442

		818		0.0417576134		818		0.0527279749		818		0.0635714307		818		0.1186943129		818		0.1848968565		818		0.2843053341

		817		0.042630516		817		0.0516389795		817		0.0647118613		817		0.120013237		817		0.1864502579		817		0.2844404578

		816		0.042103637		816		0.0537484549		816		0.0635754466		816		0.1199583635		816		0.1875495464		816		0.2890344262

		815		0.042404525		815		0.0505874902		815		0.0642980114		815		0.1203000844		815		0.1891368479		815		0.2865114808

		814		0.0426483042		814		0.0542495921		814		0.0644528344		814		0.1210773364		814		0.1911089867		814		0.2928434312

		813		0.0426081009		813		0.0513392873		813		0.064368315		813		0.1218197271		813		0.1926033646		813		0.2915477157

		812		0.0436528474		812		0.0540241599		812		0.0652544946		812		0.1221454293		812		0.1941497624		812		0.2947971821

		811		0.0425130799		811		0.0534040965		811		0.0649522021		811		0.1226842329		811		0.1963770688		811		0.2970428765

		810		0.0438275971		810		0.0523782931		810		0.0657210276		810		0.1234551445		810		0.1971669644		810		0.296895802

		809		0.0428939089		809		0.0549684837		809		0.0652703717		809		0.1238112599		809		0.2001943737		809		0.3016732633

		808		0.0431948043		808		0.0515303649		808		0.065988563		808		0.1245164797		808		0.2008097768		808		0.2997528017

		807		0.0428035967		807		0.0548973642		807		0.0652268156		807		0.1245117933		807		0.2020208091		807		0.3051802814

		806		0.0440008417		806		0.05323736		806		0.0664007738		806		0.1257699877		806		0.2053205967		806		0.3049887121

		805		0.0428228229		805		0.0533385016		805		0.0658266842		805		0.125078097		805		0.2050809413		805		0.3069388866

		804		0.0447010584		804		0.055860512		804		0.0668940321		804		0.1277391165		804		0.2092789412		804		0.3114247024

		803		0.0435227454		803		0.0530375764		803		0.0667094141		803		0.1268586069		803		0.2092973441		803		0.3092782199

		802		0.0440550446		802		0.0556038804		802		0.066536434		802		0.1279665977		802		0.2121497393		802		0.315230161

		801		0.0444698595		801		0.0533467233		801		0.067016311		801		0.1286339164		801		0.2130631953		801		0.3132872581

		800		0.0445585661		800		0.0565541834		800		0.067769222		800		0.1289421916		800		0.2159943879		800		0.3192927241

		799		0.04427341		799		0.0533417501		799		0.0668696016		799		0.1291655749		799		0.2171188593		799		0.3179167509

		798		0.0459154658		798		0.0568552799		798		0.0689559728		798		0.132372871		798		0.2260634154		798		0.3294987977

		797		0.0457927957		797		0.0566089712		797		0.0698209852		797		0.1303785443		797		0.2258324176		797		0.3313527703

		796		0.0477565527		796		0.0592843816		796		0.0706195608		796		0.1339781135		796		0.2305431813		796		0.3355103731

		795		0.0459915735		795		0.0567341447		795		0.0693809092		795		0.1326302141		795		0.2314931452		795		0.3363513052

		794		0.048298467		794		0.0596426688		794		0.0719214603		794		0.1340088397		794		0.2343128324		794		0.3411184251

		793		0.0462917127		793		0.0576074943		793		0.0702216402		793		0.1356833875		793		0.237446636		793		0.3414307535

		792		0.0488540083		792		0.0591483265		792		0.0721721202		792		0.1341108084		792		0.2381347716		792		0.3456197977

		791		0.0471463725		791		0.0591854341		791		0.0717248395		791		0.138044104		791		0.2434748113		791		0.3478105366

		790		0.0483050905		790		0.0588790104		790		0.0720577314		790		0.1356987804		790		0.2426541448		790		0.3498062789

		789		0.0487919338		789		0.0602515228		789		0.073515825		789		0.1387054622		789		0.2476596683		789		0.3548618853

		788		0.0472626425		788		0.0585989617		788		0.071779497		788		0.1380022466		788		0.248949796		788		0.3540771306

		787		0.0503094792		787		0.0615039393		787		0.0746966973		787		0.1393996924		787		0.251781702		787		0.3605329692

		786		0.0481009707		786		0.0589835793		786		0.0723416433		786		0.141247198		786		0.2557248175		786		0.3607119918

		785		0.049876824		785		0.0611949526		785		0.0747055486		785		0.1400675625		785		0.2561188042		785		0.3652707338

		784		0.049989529		784		0.0615586117		784		0.0751470849		784		0.1444584578		784		0.262388885		784		0.3683373928

		783		0.0492080823		783		0.0600056536		783		0.0737903267		783		0.1408329904		783		0.2616900504		783		0.369633466

		782		0.0507560037		782		0.0624803454		782		0.0766125545		782		0.1451445222		782		0.2674603164		782		0.3753267229

		781		0.0489735156		781		0.0602761768		781		0.074494265		781		0.1442405283		781		0.2682781518		781		0.3751422465

		780		0.0516870581		780		0.0622754581		780		0.076890558		780		0.1448359936		780		0.271589458		780		0.3811710477

		779		0.0497327112		779		0.0616244152		779		0.075616084		779		0.1483374834		779		0.2763582766		779		0.3817974925

		778		0.0521714017		778		0.063200213		778		0.0777249113		778		0.1461467594		778		0.2762274146		778		0.3863571584

		777		0.0513019376		777		0.0627170578		777		0.077259317		777		0.15032655		777		0.2825929821		777		0.3899860978

		776		0.0508707427		776		0.0628037378		776		0.0776603371		776		0.1480965614		776		0.2825553715		776		0.3911240101

		775		0.0527707078		775		0.0645006671		775		0.0796464905		775		0.1516189426		775		0.2884916961		775		0.3977090716

		774		0.050847549		774		0.0617880486		774		0.0769881234		774		0.151075989		774		0.2895601094		774		0.3972821832

		773		0.0536381677		773		0.0654370114		773		0.0808354095		773		0.1526502967		773		0.2939430773		773		0.4041189253

		772		0.0518965758		772		0.0632414445		772		0.0786650479		772		0.1549131721		772		0.297875464		772		0.404586792

		771		0.0538686141		771		0.0648407489		771		0.0804575607		771		0.1535363346		771		0.2985391617		771		0.4099453986

		770		0.0531795137		770		0.0651113167		770		0.0809824243		770		0.1581034064		770		0.3058332205		770		0.4133262634

		769		0.0536251068		769		0.0650973394		769		0.0806048214		769		0.1550444365		769		0.3052071631		769		0.4153951108

		768		0.053950645		768		0.065531373		768		0.0818702877		768		0.1586619318		768		0.3112125397		768		0.4211732447

		767		0.0534150451		767		0.0649729148		767		0.0809770301		767		0.1592851281		767		0.3133702874		767		0.4212094545

		766		0.0554250032		766		0.0665881559		766		0.0835515782		766		0.1593564898		766		0.3163862526		766		0.428172797

		765		0.0543676615		765		0.0661245138		765		0.08232674		765		0.1630077809		765		0.3224253356		765		0.4296704829

		764		0.0551916994		764		0.0670628026		764		0.0843013302		764		0.1611196548		764		0.322751224		764		0.4340897501

		763		0.0551941395		763		0.0669542775		763		0.0843217298		763		0.1655039042		763		0.3297544718		763		0.4380532205

		762		0.0551299192		762		0.0665831715		762		0.0832980648		762		0.1632051766		762		0.330332607		762		0.4408475757

		761		0.0557871275		761		0.0677468628		761		0.0861985609		761		0.1671946347		761		0.3365450799		761		0.446135968

		760		0.0557030737		760		0.0671409294		760		0.084163554		760		0.1673762053		760		0.3388997912		760		0.4478362501

		759		0.0567896329		759		0.0681500584		759		0.0868627131		759		0.1679693162		759		0.3425213695		759		0.4543828666

		758		0.0558822975		758		0.0682985708		758		0.0858090147		758		0.1717372388		758		0.348304987		758		0.4560108483

		757		0.0572877973		757		0.0683352575		757		0.0873030499		757		0.1692257077		757		0.3484934866		757		0.460529685

		756		0.056810759		756		0.0693058446		756		0.0875231028		756		0.1744077057		756		0.3565343022		756		0.4651997685

		755		0.0566567779		755		0.0692152157		755		0.0871342942		755		0.1723614782		755		0.3572546542		755		0.4671972394

		754		0.0581269897		754		0.0698832497		754		0.0897108689		754		0.1762896627		754		0.3632347286		754		0.4738537669

		753		0.0573211461		753		0.0698418692		753		0.0878396183		753		0.1768848598		753		0.3669307828		753		0.475174427

		752		0.0585405417		752		0.0710505247		752		0.0907944441		752		0.1772824079		752		0.370193243		752		0.4817897677

		751		0.0580516793		751		0.0705131516		751		0.089753963		751		0.181222707		751		0.3763512671		751		0.483869493

		750		0.0592845268		750		0.0711453483		750		0.0908246636		750		0.1790437102		750		0.3771943748		750		0.4893352091

		749		0.0583100021		749		0.0716700032		749		0.0914518014		749		0.1844842881		749		0.3853028715		749		0.4934122562

		748		0.0601492934		748		0.0721385032		748		0.0916805565		748		0.1832843721		748		0.3861640394		748		0.4963774681

		747		0.0593802892		747		0.0716266781		747		0.0933077112		747		0.1854580194		747		0.3927264214		747		0.5029436946

		746		0.0595695041		746		0.0731518269		746		0.0918538049		746		0.1879070997		746		0.396232307		746		0.5040969849

		745		0.061119765		745		0.073397249		745		0.0952361152		745		0.1880555153		745		0.4000912905		745		0.5114327073

		744		0.0603445806		744		0.0735212192		744		0.0937136561		744		0.1923469156		744		0.4066756368		744		0.5139245391

		743		0.0607575439		743		0.0740910918		743		0.0949238613		743		0.1902210265		743		0.4074888825		743		0.5186707973

		742		0.061255306		742		0.0742082372		742		0.096452713		742		0.1952519417		742		0.4156734347		742		0.5235292315

		741		0.0617595762		741		0.0744119138		741		0.0950140581		741		0.1944210082		741		0.4170594215		741		0.5265910625

		740		0.0611408614		740		0.0750986189		740		0.0979362726		740		0.1973206699		740		0.4239115417		740		0.5330215096

		739		0.0630097166		739		0.0757687762		739		0.097044602		739		0.2002387047		739		0.4282563031		739		0.5356442928

		738		0.06243103		738		0.0749803409		738		0.0989182815		738		0.1991846114		738		0.4313557744		738		0.5422428846

		737		0.062042091		737		0.0765127912		737		0.0985237881		737		0.2044409662		737		0.4384687245		737		0.5447039008

		736		0.0641848594		736		0.0767398849		736		0.1005838066		736		0.2032397538		736		0.4404504895		736		0.5513410568

		735		0.0633703768		735		0.0766907483		735		0.1002765149		735		0.2077074349		735		0.4485105276		735		0.5550444126

		734		0.0643276647		734		0.0781483278		734		0.1005775407		734		0.2078237534		734		0.450555414		734		0.5586601496

		733		0.0641118512		733		0.077913776		733		0.1029767543		733		0.2106477469		733		0.4570302069		733		0.5656497478

		732		0.0656007603		732		0.0789644569		732		0.1016466022		732		0.213657245		732		0.4621553123		732		0.5679972768

		731		0.0646931156		731		0.0788004994		731		0.1046833396		731		0.213516742		731		0.4654993713		731		0.5743634701

		730		0.0663329139		730		0.0802038759		730		0.1043423638		730		0.2186875045		730		0.4731969237		730		0.5784851313

		729		0.0656720325		729		0.0793105885		729		0.1044331565		729		0.2167079598		729		0.4742285609		729		0.5831122398

		728		0.0662818924		728		0.0808077529		728		0.106885545		728		0.2227740139		728		0.4840612411		728		0.5884659886

		727		0.0680425316		727		0.082183741		727		0.1065144837		727		0.2234602273		727		0.4859516621		727		0.5937401056

		726		0.0658458695		726		0.0802726671		726		0.1079694331		726		0.2249196768		726		0.4920954108		726		0.5979543924

		725		0.0693097636		725		0.0837037861		725		0.108567141		725		0.2300355732		725		0.4983640611		725		0.6027578115

		724		0.0670386329		724		0.0816205591		724		0.1097970158		724		0.228468135		724		0.5006501079		724		0.6080673337

		723		0.0693536699		723		0.0841588453		723		0.1097988486		723		0.2340521961		723		0.5089440942		723		0.6122597456

		722		0.0688912868		722		0.0842199922		722		0.1116786376		722		0.2339743376		722		0.5110362172		722		0.6177094579

		721		0.0691022947		721		0.083903119		721		0.1120716333		721		0.2386575788		721		0.5190368891		721		0.6222110987

		720		0.0706789195		720		0.0855827033		720		0.1124819219		720		0.23953031		720		0.522071898		720		0.627341032

		719		0.0696267039		719		0.0847998038		719		0.1151181981		719		0.2429650575		719		0.5298604965		719		0.6330105066

		718		0.0723828301		718		0.0872246325		718		0.1146267131		718		0.2463398129		718		0.5343217254		718		0.6370753646

		717		0.070356518		717		0.0854065791		717		0.1163305566		717		0.2459972352		717		0.5378926396		717		0.6431342959

		716		0.0726551786		716		0.0887827799		716		0.1172448844		716		0.2528514266		716		0.5471898913		716		0.64666605

		715		0.0724573359		715		0.0874776319		715		0.1179468185		715		0.25163728		715		0.5482658744		715		0.6530386806

		714		0.0723297149		714		0.0885926858		714		0.1190893501		714		0.2572751641		714		0.5578634143		714		0.6571797132

		713		0.0748024061		713		0.0905731171		713		0.1205132529		713		0.2593772411		713		0.5608130097		713		0.6625004411

		712		0.0725626275		712		0.0880497322		712		0.1216036901		712		0.2610394359		712		0.5665903687		712		0.6674892902

		711		0.0756093711		711		0.0917417481		711		0.1214730069		711		0.2653146088		711		0.572548449		711		0.6717807651

		710		0.0735120848		710		0.0902300924		710		0.124132432		710		0.2662844658		710		0.5769452453		710		0.6780295968

		709		0.0762833133		709		0.0922557265		709		0.1238591149		709		0.2721721232		709		0.5845518708		709		0.6817977428

		708		0.0759977922		708		0.0925325975		708		0.1259328872		708		0.2721947432		708		0.5881310701		708		0.6886609197

		707		0.0756556764		707		0.0929629132		707		0.1268416494		707		0.2779155672		707		0.5961956978		707		0.6916860342

		706		0.0787480771		706		0.0940522328		706		0.127824232		706		0.2799099088		706		0.5994814038		706		0.698671639

		705		0.0765531138		705		0.0939057395		705		0.1296104789		705		0.2829600275		705		0.6066197157		705		0.7025143504

		704		0.0793247297		704		0.0963135213		704		0.1302968115		704		0.2873730958		704		0.6118647456		704		0.7078663707

		703		0.0776776373		703		0.0944771469		703		0.1321130693		703		0.2882309854		703		0.6166974306		703		0.7127610445

		702		0.0804932341		702		0.0978266224		702		0.1323427558		702		0.2945730984		702		0.62506181		702		0.7172901034

		701		0.0792866349		701		0.0967235416		701		0.134475708		701		0.2949953377		701		0.6273655295		701		0.723126173

		700		0.0800832436		700		0.0971015096		700		0.1349848211		700		0.3006530106		700		0.6356108785		700		0.7262516618

		699		0.082426466		699		0.0998875648		699		0.1366935521		699		0.3030629456		699		0.6395602226		699		0.7339975834

		698		0.0799588412		698		0.09802109		698		0.1380673647		698		0.3059290051		698		0.6461598873		698		0.7360665202

		697		0.0840396136		697		0.101767458		697		0.1391631067		697		0.3112360835		697		0.6523846984		697		0.7431736588

		696		0.0811850652		696		0.0994881839		696		0.140373975		696		0.3122305572		696		0.6566879153		696		0.747747004

		695		0.0844271034		695		0.1027590632		695		0.1419104487		695		0.3194027543		695		0.665391624		695		0.751768291

		694		0.0836108848		694		0.1014780328		694		0.1432558894		694		0.3194346428		694		0.6679585576		694		0.7583915591

		693		0.0845877305		693		0.1031467542		693		0.14460361		693		0.3264541328		693		0.6766806245		693		0.761244297

		692		0.0861948356		692		0.104430519		692		0.1459253132		692		0.3279985785		692		0.6799369454		692		0.7678111792

		691		0.0846423358		691		0.1038002446		691		0.1479533613		691		0.3323617876		691		0.6866905689		691		0.771302402

		690		0.0883282498		690		0.1073876396		690		0.1484902799		690		0.3373121023		690		0.6930521131		690		0.7775942683

		689		0.0853089318		689		0.104548566		689		0.1513690352		689		0.3393332064		689		0.6977683902		689		0.7809778452

		688		0.0894100964		688		0.1085946262		688		0.1515388638		688		0.3458815813		688		0.7055023313		688		0.7864522338

		687		0.0877529904		687		0.1068064198		687		0.1537192613		687		0.3469446003		687		0.709048748		687		0.7923872471

		686		0.088601768		686		0.1082485393		686		0.1553608328		686		0.3542402089		686		0.7173720002		686		0.7943978906

		685		0.0906785205		685		0.1100967675		685		0.1563951224		685		0.3561810255		685		0.7207036018		685		0.8026754856

		684		0.0883783773		684		0.1092208177		684		0.1584114879		684		0.3613474667		684		0.7285799384		684		0.8040952086

		683		0.0928258896		683		0.1128075346		683		0.1600737423		683		0.3666019142		683		0.7341883779		683		0.8116174936

		682		0.089911893		682		0.1105431542		682		0.1615954787		682		0.3685680926		682		0.7386555076		682		0.8144180179

		681		0.0940531343		681		0.1142429858		681		0.163374126		681		0.3761849701		681		0.7469783425		681		0.819740355

		680		0.0920321122		680		0.1130426824		680		0.1652057469		680		0.3780050576		680		0.7500454783		680		0.8240653872

		679		0.0940523297		679		0.11462944		679		0.1668531895		679		0.3845854998		679		0.7584970593		679		0.8275126815

		678		0.0948083401		678		0.1159590781		678		0.1681747437		678		0.3873878121		678		0.7616334558		678		0.8339146972

		677		0.0932412967		677		0.1144463569		677		0.1704424173		677		0.3929710388		677		0.7691892982		677		0.83502388

		676		0.0982367769		676		0.1196311638		676		0.1723167449		676		0.3984951973		676		0.7755038738		676		0.84401685

		675		0.0944782421		675		0.1164994314		675		0.1736757159		675		0.4018361568		675		0.7802260518		675		0.8454928994

		674		0.0990659222		674		0.1205830947		674		0.176562652		674		0.409419924		674		0.7886732221		674		0.8507646918

		673		0.0973521024		673		0.1192710251		673		0.1777533442		673		0.4111828208		673		0.7907109261		673		0.8553795218

		672		0.0982469693		672		0.1210120395		672		0.1790473461		672		0.4181369543		672		0.7988612652		672		0.8575264215

		671		0.1003513634		671		0.1228368506		671		0.1822836697		671		0.4227921665		671		0.8033488989		671		0.8647631407

		670		0.0989288464		670		0.1218851879		670		0.1835941076		670		0.4276282191		670		0.809322238		670		0.8647503257

		669		0.1025829539		669		0.1257194281		669		0.1850740612		669		0.4333896637		669		0.8159844279		669		0.8725534081

		668		0.1002524197		668		0.1236642897		668		0.1888109744		668		0.4383968711		668		0.8202933073		668		0.8742836714

		667		0.1041680723		667		0.1272691935		667		0.1889860183		667		0.4445302486		667		0.8268550038		667		0.8784686327

		666		0.1022623852		666		0.1261716634		666		0.1921801418		666		0.4481909275		666		0.8304218054		666		0.8831911683

		665		0.1048304215		665		0.1286858171		665		0.1948430091		665		0.4560026824		665		0.8388442397		665		0.8853884339

		664		0.1053486839		664		0.1296391636		664		0.1958857924		664		0.4593156576		664		0.841624558		664		0.8909347057

		663		0.1046692729		663		0.1294641495		663		0.1994225532		663		0.4665276706		663		0.8491411209		663		0.8921787739

		662		0.1086170003		662		0.1332684457		662		0.2012277097		662		0.4724474549		662		0.8544723392		662		0.8992422819

		661		0.1057970524		661		0.1309556663		661		0.2035461068		661		0.4770957828		661		0.8577577472		661		0.8990405798

		660		0.1099368259		660		0.1348901391		660		0.2053254098		660		0.4844124019		660		0.8662145138		660		0.90514642

		659		0.1084434092		659		0.1343987286		659		0.2093081176		659		0.4889921546		659		0.8688448668		659		0.9077214599

		658		0.1100572124		658		0.1356590837		658		0.209442392		658		0.4950606525		658		0.8752843142		658		0.9088408351

		657		0.1122247875		657		0.1382143497		657		0.2142992467		657		0.5015377998		657		0.8805883527		657		0.9161911607

		656		0.110772565		656		0.1372295618		656		0.2162338495		656		0.5086275339		656		0.8861382604		656		0.9148856997

		655		0.1149943471		655		0.1417247206		655		0.2183185965		655		0.5141952634		655		0.8919087052		655		0.9228386879

		654		0.1124649197		654		0.1397953182		654		0.2221213132		654		0.5210508108		654		0.8956471682		654		0.9222621918

		653		0.1164840311		653		0.1436996162		653		0.2244997174		653		0.5278994441		653		0.9031713605		653		0.9274045825

		652		0.1148004606		652		0.1430542171		652		0.2271383852		652		0.5326562524		652		0.9054919481		652		0.9293711782

		651		0.1175248921		651		0.1458212882		651		0.2302815318		651		0.5418379307		651		0.913615346		651		0.9327445626

		650		0.1181465983		650		0.146716103		650		0.233101353		650		0.5466725826		650		0.917771399		650		0.9374125004

		649		0.118417263		649		0.1473583579		649		0.2359342575		649		0.554269731		649		0.9226663113		649		0.9374366403

		648		0.1212507784		648		0.1509982049		648		0.2391199619		648		0.5615603328		648		0.9296098948		648		0.9454391599

		647		0.1193281636		647		0.1491043717		647		0.2424334139		647		0.567653358		647		0.9317840934		647		0.9423282146

		646		0.1237170175		646		0.1538831145		646		0.244629398		646		0.5746920109		646		0.9397949576		646		0.9497552514

		645		0.1228368506		645		0.1537436694		645		0.2501412332		645		0.5830463767		645		0.9442415833		645		0.9525597692

		644		0.1244429722		644		0.1560621411		644		0.2513843179		644		0.5899643898		644		0.9503395557		644		0.9534567595

		643		0.126324147		643		0.1578268111		643		0.2559287548		643		0.5966150165		643		0.9551231861		643		0.959816277

		642		0.1254324764		642		0.1578340679		642		0.2588013411		642		0.6055383682		642		0.9602577686		642		0.9592418075

		641		0.129191637		641		0.1617389917		641		0.2629569173		641		0.6117939353		641		0.9665575624		641		0.9662078619

		640		0.1278320104		640		0.160996154		640		0.2664532959		640		0.6195319891		640		0.9695192575		640		0.9649262428

		639		0.1318084598		639		0.1648338437		639		0.2698364556		639		0.6278797388		639		0.9787639976		639		0.9716488123

		638		0.1305550784		638		0.1647986621		638		0.2750052512		638		0.6347492337		638		0.9802313447		638		0.9722033143

		637		0.1332439929		637		0.1677339077		637		0.277013123		637		0.6433045864		637		0.9875546694		637		0.9751030207

		636		0.1348190904		636		0.1696141213		636		0.2824428976		636		0.6511793733		636		0.9927946329		636		0.9804052114

		635		0.1341036558		635		0.1700563282		635		0.2858826816		635		0.6593210697		635		0.9970682263		635		0.9785959721

		634		0.1387579143		634		0.1745261997		634		0.2901519239		634		0.6668660641		634		1.003928661		634		0.9857177734

		633		0.1361587197		633		0.1733258218		633		0.2948643267		633		0.6756740808		633		1.006558657		633		0.9840660095

		632		0.1407927871		632		0.177864328		632		0.2981565595		632		0.6831086278		632		1.013806105		632		0.9892837405

		631		0.1405860335		631		0.1791534722		631		0.3044697344		631		0.6923884153		631		1.016373992		631		0.9908961654

		630		0.1428176463		630		0.1811737567		630		0.3069387674		630		0.7005649209		630		1.022813916		630		0.9921090603

		629		0.1441093534		629		0.1833723336		629		0.3133740425		629		0.7083262205		629		1.026186824		629		0.9956565499

		628		0.1450554729		628		0.1851883978		628		0.3169155717		628		0.7174673676		628		1.029828429		628		0.9944312572

		627		0.1475209147		627		0.1878530085		627		0.3212622404		627		0.7239003778		627		1.035241246		627		0.9998377562

		626		0.1470529586		626		0.188422516		626		0.3277073205		626		0.7329797149		626		1.036686063		626		0.9963595867

		625		0.1513976902		625		0.1930493563		625		0.3306426704		625		0.7406049371		625		1.042888165		625		1.001311898

		624		0.1501505077		624		0.1927888542		624		0.3377272487		624		0.7497310042		624		1.043769836		624		1.000543118

		623		0.1539373398		623		0.1971754432		623		0.3407458961		623		0.7570797801		623		1.049038053		623		1.000952601

		622		0.1546087116		622		0.1986955851		622		0.3476005793		622		0.7652646303		622		1.050744772		622		1.003545165

		621		0.1561194211		621		0.2011691332		621		0.3520925939		621		0.7747312784		621		1.054383636		621		1.00097847

		620		0.1590165198		620		0.2046396285		620		0.3581024706		620		0.780926466		620		1.058048368		620		1.004607677

		619		0.1594552845		619		0.2061368078		619		0.3639572263		619		0.7910397053		619		1.059215546		619		1.001766205

		618		0.1620135009		618		0.2091319859		618		0.3680289984		618		0.7972675562		618		1.064297318		618		1.004649997

		617		0.1633661985		617		0.2115345746		617		0.37671417		617		0.8071607351		617		1.065841675		617		1.003993154

		616		0.1652069092		616		0.21449022		616		0.3786381781		616		0.8133242726		616		1.068227053		616		1.003461003

		615		0.1666947603		615		0.2165619135		615		0.3876191974		615		0.8226456046		615		1.071669579		615		1.00587678

		614		0.1684917808		614		0.2193016559		614		0.3923774958		614		0.8305777311		614		1.073403478		614		1.002144814

		613		0.1715629399		613		0.223054409		613		0.3987001181		613		0.8381433487		613		1.076684952		613		1.007173896

		612		0.1720045209		612		0.2248003781		612		0.4060626924		612		0.8487046361		612		1.079538465		612		1.003892541

		611		0.1757141501		611		0.2292654812		611		0.4114616513		611		0.8547256589		611		1.08442235		611		1.006244302

		610		0.1761866212		610		0.2311607152		610		0.4200609624		610		0.8651655316		610		1.084397078		610		1.006233335

		609		0.1795207709		609		0.2354485095		609		0.4245830178		609		0.8722150922		609		1.090144277		609		1.006203175

		608		0.1818449348		608		0.2387233227		608		0.4349671602		608		0.8823294044		608		1.092837691		608		1.008749485

		607		0.1833293885		607		0.2410167754		607		0.4392668009		607		0.8893505335		607		1.094300032		607		1.005154133

		606		0.1867349148		606		0.2458004802		606		0.4481619895		606		0.8982739449		606		1.100185275		606		1.009661674

		605		0.188192755		605		0.2484549433		605		0.4561396241		605		0.9075249434		605		1.101225853		605		1.006640196

		604		0.19121629		604		0.2525059581		604		0.4612654746		604		0.9132201672		604		1.105788708		604		1.008616447

		603		0.192975238		603		0.256064117		603		0.4727832973		603		0.9258913994		603		1.107533455		603		1.009639025

		602		0.1966967434		602		0.2604880929		602		0.4779832363		602		0.9308621287		602		1.112250924		602		1.007668138

		601		0.1975914836		601		0.2628588378		601		0.4876793921		601		0.9402144551		601		1.112769008		601		1.010032177

		600		0.201131776		600		0.2674970925		600		0.494459331		600		0.9489406347		600		1.116450787		600		1.006931067

		599		0.2039268613		599		0.2721725702		599		0.5045588613		599		0.9558693767		599		1.120395303		599		1.010255814

		598		0.2063640952		598		0.2755298913		598		0.51238662		598		0.9667984843		598		1.120598316		598		1.007092118

		597		0.2096721381		597		0.28107059		597		0.5209982991		597		0.9715896249		597		1.126665354		597		1.008879662

		596		0.2119767517		596		0.2845902145		596		0.5318155289		596		0.9827024341		596		1.12571013		596		1.00807631

		595		0.2153272182		595		0.2894200981		595		0.5371006131		595		0.9878094196		595		1.129252553		595		1.005448818

		594		0.2180424929		594		0.293952167		594		0.550327003		594		0.9985793829		594		1.132581592		594		1.008596897

		593		0.2213489413		593		0.2988690734		593		0.5568163991		593		1.003589988		593		1.133016944		593		1.003955126

		592		0.2243558466		592		0.304124862		592		0.5677027702		592		1.011757851		592		1.136623979		592		1.007427931

		591		0.2276325524		591		0.3086942434		591		0.5778204203		591		1.02103579		591		1.137784123		591		1.003647923

		590		0.2308048755		590		0.3140780926		590		0.5858976841		590		1.024536371		590		1.140361071		590		1.003679991

		589		0.2341327965		589		0.3192391396		589		0.5986320972		589		1.036451817		589		1.140478492		589		1.003009796

		588		0.2380585819		588		0.3246313632		588		0.605353117		588		1.039593935		588		1.14412117		588		1.000050902

		587		0.241268307		587		0.3302800357		587		0.619602859		587		1.048669696		587		1.144917846		587		1.001510262

		586		0.2458131462		586		0.3364745975		586		0.6271868348		586		1.054814577		586		1.146541238		586		0.9968471527

		585		0.2481638193		585		0.3417761028		585		0.6389197111		585		1.061567426		585		1.149173856		585		0.9988555908

		584		0.2529240549		584		0.3486307859		584		0.6503332257		584		1.069201231		584		1.148497939		584		0.9948298335

		583		0.2563100457		583		0.3543290198		583		0.6583480835		583		1.07290864		583		1.151217103		583		0.9944956899

		582		0.2600540221		582		0.3598985374		582		0.6721470952		582		1.082848549		582		1.151648998		582		0.9938445091

		581		0.2642479837		581		0.3665084541		581		0.6794252992		581		1.08370769		581		1.152046442		581		0.9882320166

		580		0.2690300345		580		0.3741501868		580		0.694835484		580		1.094415069		580		1.154512048		580		0.9917734861

		579		0.2733763456		579		0.3807949424		579		0.7027015686		579		1.097745895		579		1.1544801		579		0.9854907393

		578		0.2777011096		578		0.3881687522		578		0.7168314457		578		1.104251146		578		1.156444192		578		0.9865729809

		577		0.2820987105		577		0.3949564397		577		0.7266893983		577		1.11084342		577		1.155773878		577		0.9826661348

		576		0.2862952352		576		0.4021746218		576		0.7375029922		576		1.114145637		576		1.157826543		576		0.9806851149

		575		0.2914579511		575		0.4098955989		575		0.7514712811		575		1.122469783		575		1.157423377		575		0.9798749685

		574		0.2966749072		574		0.4184342325		574		0.759509027		574		1.124315262		574		1.158993363		574		0.9749361277

		573		0.3006640673		573		0.4250556529		573		0.7746037245		573		1.132002831		573		1.159893632		573		0.9766978025

		572		0.3068937957		572		0.4348270893		572		0.783927083		572		1.134832025		572		1.158799052		572		0.9698846936

		571		0.3112061024		571		0.4422498643		571		0.7970719934		571		1.140916348		571		1.160839558		571		0.9712542295

		570		0.3170220554		570		0.4513848424		570		0.8084225655		570		1.145800352		570		1.159321785		570		0.9663069844

		569		0.3231116831		569		0.4599477947		569		0.8192478418		569		1.147697568		569		1.160600424		569		0.9641622901

		568		0.3278616667		568		0.4687747061		568		0.8322745562		568		1.154400587		568		1.160170317		568		0.9618641138

		567		0.3339216411		567		0.4787815511		567		0.8419613838		567		1.155067444		567		1.158795953		567		0.9577733278

		566		0.3407703042		566		0.4891664386		566		0.8566474915		566		1.162144184		566		1.162278533		566		0.9551762938

		565		0.3464403749		565		0.4981963933		565		0.8671504259		565		1.166507363		565		1.158794761		565		0.9541517496

		564		0.3533309698		564		0.5099471807		564		0.8794324398		564		1.167847037		564		1.161659837		564		0.9483277798

		563		0.3593889773		563		0.5191468596		563		0.8913630843		563		1.175356865		563		1.160494447		563		0.9486818314

		562		0.3661376536		562		0.5299317837		562		0.9015777707		562		1.175037742		562		1.157916069		562		0.9425678253

		561		0.3724931777		561		0.541174233		561		0.9143717289		561		1.181027174		561		1.159813523		561		0.940816164

		560		0.379327476		560		0.551192224		560		0.9235641956		560		1.181610107		560		1.156875253		560		0.9377596378

		559		0.3865959644		559		0.5619814396		559		0.936565578		559		1.186595201		559		1.157507181		559		0.932749033

		558		0.3943259418		558		0.5748062134		558		0.9475363493		558		1.189852953		558		1.156492591		558		0.9326133728

		557		0.4018912017		557		0.5863358974		557		0.9578442574		557		1.190144539		557		1.155426383		557		0.9257190228

		556		0.4104160666		556		0.5986425877		556		0.9709204435		556		1.197470546		556		1.15550518		556		0.9263163209

		555		0.417401582		555		0.6110926867		555		0.9787942767		555		1.195253134		555		1.152472019		555		0.9191915989

		554		0.4259725511		554		0.6226460338		554		0.992112577		554		1.202450514		554		1.153245091		554		0.9175065756

		553		0.4346943796		553		0.6360500455		553		1.000892282		553		1.202139378		553		1.149999022		553		0.9146780372

		552		0.4434637725		552		0.6490842104		552		1.012516856		552		1.205547214		552		1.151391625		552		0.9091109037

		551		0.4512735307		551		0.6610806584		551		1.020840049		551		1.207111835		551		1.14800334		551		0.9083487988

		550		0.4617097676		550		0.675978899		550		1.031918406		550		1.208042502		550		1.147093415		550		0.9014397264

		549		0.4695294797		549		0.6886118054		549		1.04113543		549		1.212215781		549		1.145883322		549		0.9006737471

		548		0.4800186753		548		0.7025451064		548		1.049931407		548		1.211217761		548		1.142211676		548		0.8947587013

		547		0.4901249111		547		0.7167692184		547		1.061144352		547		1.217335343		547		1.142488956		547		0.8930261135

		546		0.4996772707		546		0.7314119339		546		1.06902194		546		1.216252565		546		1.139731169		546		0.8886390924

		545		0.511562109		545		0.7470437288		545		1.081800103		545		1.223020554		545		1.141167283		545		0.8854119778

		544		0.5214024782		544		0.7616019249		544		1.089458704		544		1.224589348		544		1.138582468		544		0.8851797581

		543		0.5325913429		543		0.7766606212		543		1.096417189		543		1.222853303		543		1.135274887		543		0.8752403855

		542		0.5435158014		542		0.7896326184		542		1.105563045		542		1.2262609		542		1.133428574		542		0.876036346

		541		0.5544971228		541		0.8051570654		541		1.110978961		541		1.22389102		541		1.12808454		541		0.8693053126

		540		0.5665345192		540		0.8199093342		540		1.119878292		540		1.227363348		540		1.129226208		540		0.8663429022

		539		0.5779491663		539		0.8340613842		539		1.125442386		539		1.226149917		539		1.122485638		539		0.8632653952

		538		0.5909212232		538		0.8498820066		538		1.13375771		538		1.228971243		538		1.122162938		538		0.8576695323

		537		0.6022484899		537		0.864189744		537		1.138903141		537		1.227573633		537		1.119385242		537		0.8565605283

		536		0.6161417365		536		0.8790012002		536		1.147106409		536		1.228943825		536		1.114758134		536		0.8494714499

		535		0.6286300421		535		0.894064784		535		1.153142571		535		1.231264114		535		1.113544822		535		0.8488777876

		534		0.6409141421		534		0.9095789194		534		1.157624722		534		1.227173328		534		1.107738137		534		0.8413179517

		533		0.6573277712		533		0.9244919419		533		1.166753888		533		1.232803345		533		1.106988907		533		0.8409770727

		532		0.6678010821		532		0.9383097887		532		1.167756915		532		1.228839278		532		1.099704266		532		0.836070776

		531		0.6838025451		531		0.9541985989		531		1.175560951		531		1.230501294		531		1.100136042		531		0.8306517601

		530		0.6974413991		530		0.9666994214		530		1.179046273		530		1.230447054		530		1.095001459		530		0.8305599093

		529		0.7105241418		529		0.9810374975		529		1.184834838		529		1.229465485		529		1.089990497		529		0.8226388693

		528		0.726561904		528		0.9956142306		528		1.189276338		528		1.231415987		528		1.088585734		528		0.823195219

		527		0.740036428		527		1.009011865		527		1.193350196		527		1.228348851		527		1.081900239		527		0.8167923689

		526		0.7551802397		526		1.021310925		526		1.198092818		526		1.231624961		526		1.07990253		526		0.8149929047

		525		0.7692411542		525		1.035830259		525		1.199873567		525		1.226472497		525		1.073741078		525		0.8108044863

		524		0.7860484719		524		1.048073769		524		1.205992341		524		1.228947997		524		1.070489883		524		0.8064590693

		523		0.8002260923		523		1.059981227		523		1.207149506		523		1.226378083		523		1.066227198		523		0.8045210838

		522		0.8151068091		522		1.073206902		522		1.211553454		522		1.224945068		522		1.060499191		522		0.7982513905

		521		0.8325647712		521		1.084140658		521		1.215193868		521		1.226534247		521		1.058083534		521		0.7998776436

		520		0.8452168703		520		1.095877886		520		1.216841221		520		1.223044038		520		1.050554156		520		0.7922702432

		519		0.8618928194		519		1.106370449		519		1.220824361		519		1.223775268		519		1.049048543		519		0.7920158505

		518		0.8760063648		518		1.116521478		518		1.221211314		518		1.220226169		518		1.041039228		518		0.7881334424

		517		0.8920080066		517		1.126253009		517		1.225732207		517		1.22070539		517		1.03824842		517		0.7841260433

		516		0.9058858156		516		1.136577845		516		1.225515485		516		1.218145967		516		1.033433437		516		0.7838580608

		515		0.9215585589		515		1.145670295		515		1.228761196		515		1.216079831		515		1.025759101		515		0.7769784331

		514		0.9370963573		514		1.155071497		514		1.230902076		514		1.215598941		514		1.024122119		514		0.7785394788

		513		0.9510987401		513		1.16472888		513		1.231957197		513		1.211654425		513		1.015862703		513		0.772850275

		512		0.9686421752		512		1.172770619		512		1.235111833		512		1.212171197		512		1.013611078		512		0.7731538415

		511		0.9796742797		511		1.180367589		511		1.233240128		511		1.206313133		511		1.005876422		511		0.7683237791

		510		0.9964489341		510		1.189060688		510		1.237383366		510		1.206674933		510		1.001634359		510		0.7665948272

		509		1.009453893		509		1.19500947		509		1.236314893		509		1.203159451		509		0.9962051511		509		0.7664369941

		508		1.02239728		508		1.202747941		508		1.238167048		508		1.200195789		508		0.9892261028		508		0.7604594231

		507		1.03791678		507		1.207983851		507		1.238691688		507		1.198619485		507		0.9871687293		507		0.7631759644

		506		1.048612595		506		1.215483785		506		1.239015102		506		1.193780661		506		0.9779248238		506		0.7578321099

		505		1.064365745		505		1.220299721		505		1.23999238		505		1.192709088		505		0.976098001		505		0.7580137849

		504		1.075669885		504		1.22697556		504		1.240078211		504		1.187986851		504		0.9690269232		504		0.7563767433

		503		1.089390755		503		1.231965661		503		1.241356611		503		1.186362028		503		0.963732481		503		0.7540236712

		502		1.100861311		502		1.237514257		502		1.239584923		502		1.180768728		502		0.9588680863		502		0.7541545033

		501		1.11259079		501		1.243278623		501		1.241025209		501		1.179114819		501		0.9518707991		501		0.7515604496

		500		1.12543714		500		1.245720744		500		1.24035573		500		1.174936056		500		0.9493468404		500		0.7533156872

		499		1.133086801		499		1.250087619		499		1.23991859		499		1.169483781		499		0.9408484697		499		0.7486824989

		498		1.147044063		498		1.253713012		498		1.240117192		498		1.167387128		498		0.9393286705		498		0.7519638538

		497		1.154013276		497		1.257326007		497		1.23741591		497		1.161275387		497		0.9308398366		497		0.7488604188

		496		1.165831804		496		1.261894584		496		1.239405632		496		1.158844352		496		0.927572906		496		0.7498714924

		495		1.17504847		495		1.264666319		495		1.235918283		495		1.153009415		495		0.9224045277		495		0.7501942515

		494		1.182376504		494		1.267581105		494		1.237426519		494		1.150341272		494		0.915450573		494		0.7483253479

		493		1.19372499		493		1.270719528		493		1.234959602		493		1.144422412		493		0.9150137901		493		0.7513326406

		492		1.198543191		492		1.272908568		492		1.233212829		492		1.139149308		492		0.9058048725		492		0.7485123873

		491		1.210045576		491		1.274718881		491		1.232523322		491		1.135896921		491		0.9041775465		491		0.7518973351

		490		1.213283181		490		1.278103709		490		1.228815913		490		1.129031181		490		0.8979517221		490		0.7496979833

		489		1.223534942		489		1.28039515		489		1.229191899		489		1.125890136		489		0.8937932253		489		0.752844274

		488		1.229235053		488		1.279640198		488		1.225755095		488		1.118988991		488		0.8902962804		488		0.7528868914

		487		1.234586716		487		1.284160376		487		1.22608006		487		1.115718365		487		0.8855561018		487		0.7538284063

		486		1.24270153		486		1.283424139		486		1.220931172		486		1.108703613		486		0.8827341199		486		0.7567597032

		485		1.245732546		485		1.286022663		485		1.220535159		485		1.103767991		485		0.8765422106		485		0.7553402185

		484		1.253943801		484		1.28707242		484		1.217891097		484		1.099303126		484		0.8764694929		484		0.7601527572

		483		1.255819321		483		1.288313746		483		1.212822795		483		1.091570854		483		0.8698077798		483		0.7590929866

		482		1.262362003		482		1.289410353		482		1.213075876		482		1.087886691		482		0.8675354719		482		0.7628406286

		481		1.267102003		481		1.290303469		481		1.208763003		481		1.081202269		481		0.8668984175		481		0.7654619813

		480		1.26980412		480		1.290884137		480		1.206505418		480		1.076127529		480		0.8595929742		480		0.7660343647

		479		1.276843071		479		1.290347815		479		1.202287793		479		1.070559144		479		0.8615678549		479		0.7708988786

		478		1.276279807		478		1.292613268		478		1.199146271		478		1.064120412		478		0.8547948599		478		0.7700099349

		477		1.284130573		477		1.292185307		477		1.195786238		477		1.059839964		477		0.8551303148		477		0.7759805918

		476		1.283977985		476		1.292134762		476		1.192235708		476		1.052685738		476		0.8516272902		476		0.7762455344

		475		1.288739204		475		1.29384768		475		1.189654827		475		1.049154162		475		0.8510033488		475		0.7807091475

		474		1.291740298		474		1.292578697		474		1.183778524		474		1.041400313		474		0.8496011496		474		0.7826805115

		473		1.292682648		473		1.29337275		473		1.182670593		473		1.037495732		473		0.8472551703		473		0.7859233022

		472		1.297460914		472		1.291918159		472		1.176075459		472		1.031029582		472		0.8488916755		472		0.7900546193

		471		1.297441125		471		1.293758035		471		1.173700929		471		1.026856065		471		0.8446474075		471		0.7919943333

		470		1.302396178		470		1.291917801		470		1.16831696		470		1.021514297		470		0.8467243314		470		0.7975586057

		469		1.300434351		469		1.292498231		469		1.16439271		469		1.015931487		469		0.8455608487		469		0.7989050746

		468		1.306410789		468		1.291614652		468		1.159985185		468		1.012861967		468		0.8447681665		468		0.8042189479

		467		1.306660771		467		1.290306568		467		1.156033278		467		1.007650375		467		0.8480424285		467		0.8077068925

		466		1.306840301		466		1.290229917		466		1.151364446		466		1.002500892		466		0.8449098468		466		0.8098276854

		465		1.311464548		465		1.288184881		465		1.145916343		465		0.9991436005		465		0.8491124511		465		0.8162708282

		464		1.308196306		464		1.288959742		464		1.142297983		464		0.9947504997		464		0.8474798203		464		0.816849947

		463		1.314117193		463		1.287733436		463		1.137122035		463		0.9911417961		463		0.8515751362		463		0.8238124251

		462		1.311529636		462		1.286309838		462		1.13232398		462		0.9878703952		462		0.8511073589		462		0.8250045776

		461		1.315263748		461		1.285328865		461		1.128194213		461		0.9853856564		461		0.8534423113		461		0.8304734826

		460		1.314574838		460		1.283245921		460		1.122293949		460		0.9798935056		460		0.8568469286		460		0.8329803944

		459		1.315056562		459		1.282976985		459		1.118454337		459		0.9790663123		459		0.85687989		459		0.8372211456

		458		1.317080975		458		1.28066504		458		1.112991571		458		0.9759886265		458		0.8638784289		458		0.8421516418

		457		1.315532446		457		1.280632019		457		1.109723449		457		0.9738634825		457		0.8631082773		457		0.8431117535

		456		1.319790602		456		1.278532743		456		1.104221702		456		0.9736244678		456		0.8688809276		456		0.8499493599

		455		1.315534949		455		1.27592504		455		1.099999905		455		0.9709412456		455		0.8716771007		455		0.8500388265

		454		1.319747925		454		1.275182843		454		1.095953226		454		0.9706174731		454		0.8746196628		454		0.8560699224

		453		1.318341017		453		1.272469044		453		1.09085536		453		0.9689968228		453		0.8800460696		453		0.8577347398

		452		1.317506075		452		1.271259546		452		1.08818078		452		0.9696143866		452		0.8816839457		452		0.8615932465

		451		1.321224451		451		1.268984079		451		1.083503842		451		0.9692185521		451		0.8895566463		451		0.8649238944

		450		1.317804098		450		1.267542243		450		1.079811335		450		0.9705873132		450		0.8906376362		450		0.8668275476

		449		1.320346951		449		1.264176726		449		1.0762676		449		0.9709071517		449		0.8978686929		449		0.8712202907

		448		1.318492889		448		1.262513161		448		1.07382226		448		0.9716243744		448		0.9021715522		448		0.8714914918

		447		1.320747018		447		1.260659575		447		1.069514275		447		0.9741190672		447		0.9058622718		447		0.8766940236

		446		1.318015099		446		1.25679934		446		1.066604972		446		0.9742578864		446		0.9135020971		446		0.8769480586

		445		1.319222331		445		1.256936193		445		1.065408707		445		0.9785940051		445		0.9156526327		445		0.8797784448

		444		1.320440292		444		1.253443122		444		1.06089139		444		0.9807913303		444		0.9230610728		444		0.8824647665

		443		1.31586647		443		1.251223326		443		1.060481548		443		0.983757019		443		0.9257336259		443		0.8821607828

		442		1.321511626		442		1.249770164		442		1.058302045		442		0.987813592		442		0.9332689047		442		0.8862504363

		441		1.315939903		441		1.247538686		441		1.057257891		441		0.9905660152		441		0.9371003509		441		0.8850350976

		440		1.317489386		440		1.243570209		440		1.055245519		440		0.993783772		440		0.9412775636		440		0.8877286911

		439		1.317060113		439		1.243306637		439		1.056241393		439		0.9985969067		439		0.9489257336		439		0.8880307674

		438		1.316345334		438		1.240588665		438		1.054729462		438		1.003711224		438		0.9498167038		438		0.8887298107

		437		1.317161441		437		1.23752141		437		1.054864764		437		1.006486535		437		0.9581974745		437		0.8892912269

		436		1.314787745		436		1.237964153		436		1.056357503		436		1.013010502		436		0.9600173831		436		0.8885650039

		435		1.316997051		435		1.234672785		435		1.055537343		435		1.017194867		435		0.9654764533		435		0.8899676204

		434		1.313072562		434		1.232955217		434		1.058728576		434		1.021220088		434		0.9695129991		434		0.8878197074

		433		1.31642735		433		1.233058929		433		1.058635831		433		1.027953148		433		0.9729372859		433		0.8890503049

		432		1.31341064		432		1.230384946		432		1.060802579		432		1.030903935		432		0.9772424698		432		0.8868753314

		431		1.313212156		431		1.229627252		431		1.062806964		431		1.037017465		431		0.9784361124		431		0.8860347867

		430		1.314885259		430		1.227438927		430		1.064480424		430		1.040935159		430		0.9846291542		430		0.8847545385

		429		1.310530305		429		1.226659536		429		1.067908168		429		1.046779394		429		0.9842739105		429		0.8821616769

		428		1.313331842		428		1.225102067		428		1.069018364		428		1.050158858		428		0.9888691306		428		0.8812947869

		427		1.309548855		427		1.224963665		427		1.073962808		427		1.05514884		427		0.9904212356		427		0.8771256208

		426		1.310732603		426		1.22335124		426		1.074307323		426		1.059160471		426		0.9900009632		426		0.8755193949

		425		1.309183598		425		1.221920013		425		1.079200268		425		1.062604666		425		0.9951364398		425		0.8713473082

		424		1.308012605		424		1.222845912		424		1.080906391		424		1.068285584		424		0.9917565584		424		0.8681588769

		423		1.306798697		423		1.220138907		423		1.083345771		423		1.069311261		423		0.9951193333		423		0.8642085195

		422		1.303389668		422		1.220208406		422		1.088269234		422		1.073762774		422		0.9934398532		422		0.8596283197

		421		1.305375695		421		1.219380379		421		1.088080883		421		1.075437188		421		0.9936902523		421		0.8557832241

		420		1.299759865		420		1.217179298		420		1.092628479		420		1.077628016		420		0.9924758673		420		0.8496916294

		419		1.301947355		419		1.217937708		419		1.093666434		419		1.080727458		419		0.990241468		419		0.8462937474

		418		1.298270941		418		1.216073394		418		1.096560597		418		1.081154346		418		0.9892122746		418		0.8383463025

		417		1.296401501		417		1.216175556		417		1.097939491		417		1.083723307		417		0.9842580557		417		0.8345404267

		416		1.295767665		416		1.214349508		416		1.100208282		416		1.08320868		416		0.9840763807		416		0.8273512125

		415		1.291086197		415		1.213461161		415		1.10264492		415		1.084203124		415		0.9778485894		415		0.8204359412

		414		1.292164087		414		1.212790847		414		1.100546956		414		1.082651734		414		0.9739700556		414		0.8148586154

		413		1.286475301		413		1.211657882		413		1.10635674		413		1.083188415		413		0.9706154466		413		0.8074707389

		412		1.287349701		412		1.210901141		412		1.102434635		412		1.081243753		412		0.9616513252		412		0.8014419079

		411		1.282949328		411		1.208209395		411		1.105449915		411		1.07966733		411		0.9592332244		411		0.7943095565

		410		1.28011322		410		1.208399177		410		1.104552031		410		1.077130079		410		0.9497807026		410		0.7881212831

		409		1.278834105		409		1.206439257		409		1.103869915		409		1.073817492		409		0.9449911118		409		0.7804620266

		408		1.273245215		408		1.204706073		408		1.103896022		408		1.070398569		408		0.9365848899		408		0.7747781277

		407		1.273476481		407		1.202400208		407		1.100721121		407		1.065284014		407		0.9281007648		407		0.7680531144

		406		1.267754197		406		1.201036453		406		1.101016998		406		1.061057687		406		0.9205074906		406		0.7609103322

		405		1.265460491		405		1.198977232		405		1.095634103		405		1.05448997		405		0.9102069736		405		0.7558019161

		404		1.261374116		404		1.195245266		404		1.094644785		404		1.048810482		404		0.9042996168		404		0.7487124205

		403		1.257557392		403		1.194126606		403		1.089838624		403		1.042750359		403		0.8920084834		403		0.7433082461

		402		1.25437367		402		1.189499497		402		1.085152984		402		1.033691406		402		0.8864350915		402		0.7379257083

		401		1.24875474		401		1.186955929		401		1.081619859		401		1.027206779		401		0.8755261302		401		0.7328639627

		400		1.246914744		400		1.182605982		400		1.074041009		400		1.018629909		400		0.8661503792		400		0.7276762724

		399		1.238998294		399		1.177098036		399		1.069638968		399		1.009515643		399		0.8591557145		399		0.7227094173

		398		1.236288786		398		1.172876239		398		1.061173916		398		1.001201153		398		0.8483620286		398		0.7182962298

		397		1.229311585		397		1.166671515		397		1.054994702		397		0.9916719794		397		0.8427627087		397		0.7131475806

		396		1.223313212		396		1.161178231		396		1.045644283		396		0.981540978		396		0.8321795464		396		0.7096711397

		395		1.217784643		395		1.153531671		395		1.037496209		395		0.9717615843		395		0.8268326521		395		0.7043548822

		394		1.210105538		394		1.147167444		394		1.029449701		394		0.963226974		394		0.8174487352		394		0.7011900544

		393		1.204503775		393		1.139344454		393		1.017804623		393		0.9531340599		393		0.810775578		393		0.6974642873

		392		1.195175767		392		1.130303144		392		1.010596991		392		0.9444351792		392		0.8046703339		392		0.692921102

		391		1.188721657		391		1.123906612		391		0.9980124235		391		0.9352670312		391		0.7955429554		391		0.6897932887

		390		1.179817796		390		1.113324523		390		0.989915669		390		0.9253958464		390		0.792737484		390		0.6861615181

		389		1.171040297		389		1.104416609		389		0.9780757427		389		0.9171478152		389		0.7823318839		389		0.6815335155

		388		1.164208174		388		1.095845222		388		0.9698389769		388		0.9079332948		388		0.7797733545		388		0.6785354018

		387		1.152052283		387		1.084860325		387		0.9585497975		387		0.8993182182		387		0.7716718316		387		0.6753892303

		386		1.145477772		386		1.075302839		386		0.9470070601		386		0.891443491		386		0.766169548		386		0.6706032753

		385		1.13337636		385		1.064926386		385		0.9397720098		385		0.8834574819		385		0.7609890103		385		0.6669848561

		384		1.124554038		384		1.054514885		384		0.9252315164		384		0.8746644258		384		0.7527341843		384		0.6630076766

		383		1.113913894		383		1.042880654		383		0.9178903699		383		0.8663445711		383		0.749383986		383		0.6584606767

		382		1.103498459		382		1.033905387		382		0.9067187309		382		0.8588115573		382		0.7395899892		382		0.655254066

		381		1.093280196		381		1.022756934		381		0.8958309293		381		0.8496333361		381		0.7362316251		381		0.6505898237

		380		1.083022237		380		1.011786222		380		0.8880357742		380		0.844111979		380		0.7283453345		380		0.6473638415

		379		1.073963404		379		1.002692342		379		0.8761395216		379		0.834518373		379		0.7225900292		379		0.6421099901

		378		1.06068635		378		0.9897770286		378		0.8668768406		378		0.8258766532		378		0.716439724		378		0.6379727721

		377		1.052373052		377		0.9803350568		377		0.8552504778		377		0.8185189962		377		0.7077349424		377		0.63234061

		376		1.041059017		376		0.9701244235		376		0.8477073312		376		0.8096311688		376		0.7034060955		376		0.6277372241

		375		1.029280543		375		0.9583390951		375		0.8355339766		375		0.8012481928		375		0.6932374239		375		0.6227648258

		374		1.020957589		374		0.9495863914		374		0.8271489739		374		0.7925555706		374		0.6890243292		374		0.6170853376

		373		1.008365035		373		0.9383130074		373		0.8172845244		373		0.7839872837		373		0.679235518		373		0.6121346951

		372		0.9993004203		372		0.928362906		372		0.804930985		372		0.7745523453		372		0.672329247		372		0.6049687266

		371		0.9882913828		371		0.9177103043		371		0.7980615497		371		0.7665882111		371		0.6657650471		371		0.6004834771

		370		0.9793432355		370		0.9092140794		370		0.7864392996		370		0.75733006		370		0.6560967565		370		0.5934655666

		369		0.9700767994		369		0.8990120292		369		0.7783923745		369		0.7488160729		369		0.652269125		369		0.5882578492

		368		0.9623004198		368		0.8907085061		368		0.7704942822		368		0.7417500615		368		0.6422373056		368		0.5835254192

		367		0.9546609521		367		0.8844347		367		0.7613984942		367		0.7335016727		367		0.6384387016		367		0.5768467188

		366		0.9447354078		366		0.8747773767		366		0.7541508079		366		0.7266077995		366		0.6300641894		366		0.5730160475

		365		0.9410071373		365		0.8699206114		365		0.7468417287		365		0.7208858728		365		0.6252936125		365		0.5672895908

		364		0.9322909117		364		0.8626645803		364		0.7424505949		364		0.7149270773		364		0.6211881042		364		0.563870132

		363		0.9280403256		363		0.8586921692		363		0.7359503508		363		0.7107926607		363		0.6162584424		363		0.5596282482

		362		0.9235818386		362		0.853895843		362		0.7335051298		362		0.7063720226		362		0.6151333451		362		0.558204174

		361		0.9179546237		361		0.8502429128		361		0.7291799188		361		0.7042834759		361		0.6103892922		361		0.5563156009

		360		0.9169152379		360		0.8495588303		360		0.7276382446		360		0.7038649917		360		0.6134479642		360		0.5560917258

		359		0.9129740596		359		0.8461802602		359		0.72856462		359		0.7034224272		359		0.611436367		359		0.5586311817

		358		0.9110053778		358		0.8477658033		358		0.7259539962		358		0.7049664259		358		0.6148222685		358		0.5591402054

		357		0.9089867473		357		0.8475057483		357		0.731082499		357		0.7095608115		357		0.6203275323		357		0.5657379031

		356		0.9093526006		356		0.8495733142		356		0.732755065		356		0.7136312127		356		0.6247444153		356		0.5711150765

		355		0.9071387053		355		0.8522772193		355		0.7389395237		355		0.719448328		355		0.6342608929		355		0.5789929032

		354		0.9062461257		354		0.8551138043		354		0.7437283397		354		0.7292508483		354		0.6420929432		354		0.5905632973

		353		0.9071542025		353		0.8597335815		353		0.7516504526		353		0.7377262712		353		0.6567671895		353		0.6015701294

		352		0.9038737416		352		0.8636994362		352		0.760936141		352		0.7494397759		352		0.6681557298		352		0.6167895794

		351		0.9063048363		351		0.871101737		351		0.7692659497		351		0.7640630603		351		0.6879826784		351		0.6331140399

		350		0.9048106074		350		0.87616992		350		0.7839030623		350		0.7783448696		350		0.705129087		350		0.6522397995

		349		0.9058224559		349		0.8856015205		349		0.7965903282		349		0.7970302701		349		0.7267135978		349		0.6727399826

		348		0.9733333588		348		0.9599548578		348		0.8684533834		348		0.8740618229		348		0.7985913157		348		0.7377735376

		347		0.9750301242		347		0.9709341526		347		0.8892921209		347		0.9014493823		347		0.8287805319		347		0.7672493458

		346		0.97533077		346		0.9823461175		346		0.9117990136		346		0.929890275		346		0.8628869057		346		0.7974998951

		345		0.9807552695		345		0.9979508519		345		0.9385613203		345		0.9637514353		345		0.9032617211		345		0.8331242204

		344		0.9863315821		344		1.011336088		344		0.9668840766		344		1.00148356		344		0.9464247227		344		0.8710155487

		343		0.994579196		343		1.027355313		343		0.9971338511		343		1.043391109		343		0.9955765009		343		0.9149456024

		342		1.00826633		342		1.045042992		342		1.030619144		342		1.087797403		342		1.048738837		342		0.9639217854

		341		1.028092027		341		1.06712997		341		1.066393614		341		1.136614442		341		1.1049788		341		1.016823173

		340		1.054728985		340		1.093820453		340		1.104494572		340		1.186897039		340		1.166103005		340		1.078880191

		339		1.091844678		339		1.129909396		339		1.14781332		339		1.241287947		339		1.231844068		339		1.147537947

		338		1.145206213		338		1.179441571		338		1.204286933		338		1.307140231		338		1.307359934		338		1.227883458

		337		1.20906198		337		1.237694502		337		1.268474221		337		1.375963926		337		1.384611487		337		1.314948916

		336		1.28080833		336		1.305575371		336		1.33725512		336		1.446549773		336		1.460769773		336		1.404239416

		335		1.361479998		335		1.382891059		335		1.412823677		335		1.517117023		335		1.533830285		335		1.491653204

		334		1.448283076		334		1.464705348		334		1.494135737		334		1.590235591		334		1.609548569		334		1.576894283

		333		1.536935925		333		1.549436927		333		1.575757146		333		1.658007979		333		1.673242807		333		1.651681066

		332		1.617738724		332		1.628750801		332		1.647894621		332		1.7149297		332		1.725677848		332		1.712076426

		331		1.691123843		331		1.695801497		331		1.706980824		331		1.758720994		331		1.767252803		331		1.756344557

		330		1.745920181		330		1.744558096		330		1.749981046		330		1.788815379		330		1.788666964		330		1.781818509

		329		1.784119248		329		1.778484464		329		1.773397446		329		1.80053854		329		1.802235723		329		1.796707392

		328		1.811276317		328		1.804504991		328		1.793800354		328		1.812994838		328		1.814087391		328		1.807539225

		327		1.840416789		327		1.82758534		327		1.815347433		327		1.831430674		327		1.832310796		327		1.82536006

		326		1.864438534		326		1.852928758		326		1.836463571		326		1.851408601		326		1.848557234		326		1.845167637

		325		1.874094486		325		1.861882687		325		1.845985174		325		1.860192299		325		1.856782317		325		1.851943374

		324		1.884035349		324		1.871584773		324		1.853646517		324		1.865749717		324		1.863653183		324		1.85836184

		323		1.890745163		323		1.877074957		323		1.862043858		323		1.875377059		323		1.872929215		323		1.866829038

		322		1.899503112		322		1.887789607		322		1.869135857		322		1.88215673		322		1.880827427		322		1.876304746

		321		1.910404801		321		1.896823406		321		1.880577207		321		1.894495368		321		1.8901577		321		1.884179831

		320		1.91841805		320		1.906368613		320		1.887055397		320		1.902732491		320		1.899686575		320		1.894309402

		319		1.928045034		319		1.916141033		319		1.897176266		319		1.911868572		319		1.90711832		319		1.903667808

		318		1.938729525		318		1.926888704		318		1.909356475		318		1.921038508		318		1.919786572		318		1.915018797

		317		1.950038552		317		1.938117146		317		1.919741511		317		1.932259321		317		1.929985046		317		1.925370574

		316		1.960016608		316		1.947107911		316		1.928025961		316		1.944459558		316		1.939796209		316		1.936094999

		315		1.973348618		315		1.959777474		315		1.941220522		315		1.954971671		315		1.953185797		315		1.9476825

		314		1.984342933		314		1.971986413		314		1.954559565		314		1.967201591		314		1.965475917		314		1.959713101

		313		1.998122811		313		1.985553503		313		1.963556528		313		1.98090744		313		1.975117803		313		1.972846866

		312		2.010336876		312		1.998644471		312		1.979325533		312		1.993489265		312		1.990357637		312		1.984447479

		311		2.02315855		311		2.011645794		311		1.993350148		311		2.005951166		311		2.004091501		311		1.999473572

		310		2.037929058		310		2.027572393		310		2.007319689		310		2.020556211		310		2.016840219		310		2.012627602

		309		2.053810835		309		2.041829109		309		2.02325058		309		2.036775827		309		2.035426855		309		2.028541088

		308		2.07103157		308		2.058821201		308		2.039162636		308		2.053296804		308		2.051171303		308		2.04583931

		307		2.087637663		307		2.075046301		307		2.058201075		307		2.069793463		307		2.066412687		307		2.062792778

		306		2.105557203		306		2.092630625		306		2.074004173		306		2.086630106		306		2.084991455		306		2.082505941

		305		2.123043776		305		2.112460136		305		2.093773603		305		2.107057333		305		2.104228735		305		2.096922398

		304		2.142566442		304		2.130038261		304		2.112263918		304		2.12517786		304		2.122294664		304		2.115981817

		303		2.158494711		303		2.148288727		303		2.128970146		303		2.141339302		303		2.137434959		303		2.135761261

		302		2.181208372		302		2.169014931		302		2.151164532		302		2.165286541		302		2.159607172		302		2.154870033

		301		2.202627182		301		2.185171604		301		2.169195652		301		2.18274045		301		2.179484606		301		2.173501492

		300		2.2207582		300		2.206782341		300		2.188762665		300		2.202424765		300		2.196546316		300		2.194206238

		299		2.240747929		299		2.231615067		299		2.207388878		299		2.222135305		299		2.221634865		299		2.214984894

		298		2.260965586		298		2.250156403		298		2.230051517		298		2.245923281		298		2.240779638		298		2.236120701

		297		2.284926653		297		2.272777319		297		2.251844168		297		2.266075611		297		2.261110306		297		2.260594845

		296		2.305863857		296		2.295619965		296		2.275959253		296		2.288650274		296		2.287572384		296		2.280642033

		295		2.330272913		295		2.318605423		295		2.298411608		295		2.314754725		295		2.309851885		295		2.302912474

		294		2.354282141		294		2.340743542		294		2.32325983		294		2.334731102		294		2.332131386		294		2.329854965

		293		2.377481222		293		2.3659904		293		2.346066475		293		2.358736038		293		2.354894876		293		2.353958607

		292		2.405405045		292		2.391025543		292		2.374455214		292		2.385395288		292		2.383758307		292		2.37673831

		291		2.42798996		291		2.41639328		291		2.396900177		291		2.413499832		291		2.410240889		291		2.4039042

		290		2.458187342		290		2.444197893		290		2.424460411		290		2.439724684		290		2.433080912		290		2.430332184

		289		2.485316753		289		2.470208406		289		2.451948643		289		2.46655035		289		2.4615798		289		2.459382296

		288		2.512802839		288		2.500377178		288		2.482297182		288		2.494452238		288		2.490579367		288		2.486534595

		287		2.538684607		287		2.5226264		287		2.508983374		287		2.521341562		287		2.520218611		287		2.514970541

		286		2.569158792		286		2.560197115		286		2.53602457		286		2.55322361		286		2.545452833		286		2.544037819

		285		2.604174376		285		2.58275342		285		2.568992376		285		2.579592466		285		2.580224514		285		2.57145524

		284		2.630784035		284		2.617961407		284		2.597158194		284		2.607329607		284		2.603327751		284		2.603729725

		283		2.659896851		283		2.641292095		283		2.621114016		283		2.635610819		283		2.632410765		283		2.63070631

		282		2.691900253		282		2.673765421		282		2.660014868		282		2.669256687		282		2.658501387		282		2.66274929

		281		2.716645956		281		2.698727846		281		2.683701515		281		2.692553759		281		2.695926905		281		2.683506966

		280		2.741710186		280		2.734544754		280		2.714060783		280		2.726266146		280		2.726308107		280		2.717008352

		279		2.77270031		279		2.764629841		279		2.73866868		279		2.747835636		279		2.746420383		279		2.744980574

		278		2.801817417		278		2.791547298		278		2.766046524		278		2.78265357		278		2.782426119		278		2.774620056

		277		2.830864668		277		2.823174477		277		2.799591541		277		2.813214302		277		2.806782961		277		2.799069881

		276		2.861397743		276		2.846561432		276		2.829802275		276		2.845590353		276		2.835073233		276		2.829343319

		275		2.886965036		275		2.869882584		275		2.854388237		275		2.867933035		275		2.861502886		275		2.863604784

		274		2.917737484		274		2.897720575		274		2.880481482		274		2.89585638		274		2.895371199		274		2.898761749

		273		2.949547291		273		2.929819107		273		2.91076088		273		2.928063869		273		2.915442944		273		2.916047812

		272		2.972976923		272		2.961583853		272		2.935750246		272		2.956188202		272		2.952793837		272		2.942692518

		271		2.999206066		271		2.988361835		271		2.966634274		271		2.98918891		271		2.970829248		271		2.974577665

		270		3.027080059		270		3.01718688		270		2.995622873		270		3.008948565		270		3.004870653		270		2.98980689

		269		3.055162668		269		3.047641039		269		3.021552324		269		3.042714596		269		3.031894445		269		3.031687498

		268		3.085556269		268		3.076480389		268		3.053472281		268		3.067758322		268		3.057028055		268		3.056747675

		267		3.116258621		267		3.099772692		267		3.067605019		267		3.087203503		267		3.078454971		267		3.091547012

		266		3.152440548		266		3.143591642		266		3.099947691		266		3.116024256		266		3.120199203		266		3.126536846

		265		3.172914743		265		3.154415846		265		3.139768124		265		3.159693003		265		3.143480778		265		3.154538631

		264		3.182496786		264		3.193313599		264		3.169722795		264		3.175163507		264		3.180856705		264		3.170911551

		263		3.228628635		263		3.227827311		263		3.222527981		263		3.206670761		263		3.206367254		263		3.219012022

		262		3.277305126		262		3.263291359		262		3.241729498		262		3.253112316		262		3.261965036		262		3.259848118

		261		3.31329608		261		3.281884909		261		3.281544209		261		3.288741589		261		3.281687737		261		3.289090633

		260		3.350407362		260		3.332759619		260		3.315854311		260		3.328338385		260		3.315697432		260		3.328701019

		259		3.403533936		259		3.373592138		259		3.339332581		259		3.338307142		259		3.378865242		259		3.352288246

		258		3.420790434		258		3.389136314		258		3.41577816		258		3.387535334		258		3.39994812		258		3.411682844

		257		3.475645304		257		3.451436758		257		3.418663502		257		3.451120377		257		3.432926893		257		3.449617624

		256		3.535998821		256		3.501534939		256		3.479568005		256		3.520163059		256		3.467889786		256		3.47472167

		255		3.586701632		255		3.57977891		255		3.518327951		255		3.509049654		255		3.523874521		255		3.503142834

		254		3.548225164		254		3.608881235		254		3.605920076		254		3.585052967		254		3.531385899		254		3.599353075

		253		3.679704905		253		3.632938385		253		3.610846043		253		3.655734301		253		3.65571022		253		3.642739534

		252		3.696271896		252		3.692894936		252		3.687651396		252		3.668826342		252		3.724720478		252		3.727652311

		251		3.751741886		251		3.816732168		251		3.761534214		251		3.751514912		251		3.775454283		251		3.72884202

		250		3.868525505		250		3.816065073		250		3.808227539		250		3.839382648		250		3.827325106		250		3.843429804

		249		3.846783876		249		3.94229126		249		3.858917236		249		3.932317257		249		3.932315111		249		3.884958982

		248		3.923796415		248		4.019248486		248		4.019060612		248		4.045046329		248		3.988646269		248		3.983032465

		247		4.011974812		247		4.063092709		247		4.161924362		247		4.062977791		247		4.049508095		247		4.145241261

		246		4.326330185		246		4.269194603		246		4.148329735		246		4.351456165		246		4.047641754		246		4.238190651

		245		4.421421051		245		4.279222965		245		4.391935349		245		4.155272484		245		4.364257813		245		4.351031303

		244		4.474615097		244		4.736787796		244		4.598481178		244		4.648642063		244		4.457201958		244		4.276803017

		243		4.508003235		243		4.471586704		243		4.615650654		243		4.52752924		243		4.508068085		243		4.832441807

		242		5.345303535		242		4.659316063		242		4.65947628		242		4.6866045		242		5.234732628		242		4.585981846

		241		10		241		5.397972584		241		5.276053429		241		4.869915962		241		4.968685627		241		10

		240		10		240		4.557677269		240		5.305988789		240		4.604577541		240		4.971921921		240		4.971568584

		239		5.893539429		239		10		239		5.392305374		239		4.651087761		239		4.777432919		239		4.742642403

		238		4.471457958		238		4.93928051		238		5.769113064		238		5.346741676		238		4.64609766		238		4.996114731

		237		10		237		6.1237607		237		4.420078278		237		5.117731571		237		10		237		4.547430038

		236		10		236		4.58865118		236		4.693018436		236		5.032169819		236		4.756530762		236		4.434542656

		235		4.912548065		235		5.022548199		235		5.895875454		235		4.751767635		235		5.172263622		235		5.267916203

		234		10		234		4.56223011		234		4.660056591		234		7.651486874		234		4.864278316		234		4.95979023

		233		4.632021427		233		5.859137058		233		10		233		4.821280956		233		4.959474087		233		4.686859608

		232		5.016840458		232		4.783183575		232		4.908617973		232		4.71603632		232		4.687067986		232		10

		231		5.267323017		231		10		231		10		231		4.606669903		231		5.270998955		231		4.748487949

		230		4.786524773		230		4.824655056		230		4.660243511		230		4.659395218		230		4.584196091		230		10

		229		5.293178558		229		5.435760021		229		4.753528118		229		5.435078621		229		10		229		6.080562115

		228		4.501020432		228		4.635935783		228		4.586522579		228		4.834225655		228		4.758263111		228		4.636159897

		227		4.612102509		227		6.539505959		227		4.695804119		227		4.761481285		227		10		227		4.501261234

		226		4.998143196		226		4.589401722		226		4.543585777		226		5.368629456		226		5.068303108		226		5.000288486

		225		4.805845737		225		10		225		4.848795891		225		10		225		4.806729794		225		5.005648613

		224		4.396090031		224		5.591585636		224		4.412034035		224		4.522441387		224		5.011723995		224		10

		223		10		223		10		223		10		223		5.608605385		223		4.809394836		223		4.852201462

		222		10		222		4.898332596		222		10		222		6.020089626		222		4.481509686		222		4.701313972

		221		5.169856548		221		4.808971405		221		10		221		10		221		10		221		10

		220		4.701568604		220		10		220		4.8546772		220		5.016879559		220		4.70236063		220		4.735989571

		219		5.448981285		219		10		219		10		219		5.299739838		219		5.693670273		219		5.29981041

		218		4.81945467		218		5.323551178		218		4.443203449		218		10		218		10		218		5.3265872

		217		10		217		10		217		4.481883526		217		10		217		5.05582428		217		10

		216		5.006942272		216		10		216		4.945216179		216		5.006758213		216		4.796839237		216		5.007407188

		215		10		215		10		215		4.632629395		215		10		215		5.037568092		215		4.528817177

		214		4.70637846		214		4.933169842		214		4.997412682		214		10		214		10		214		5.279998302

		213		4.738007545		213		6.171595573		213		10		213		10		213		10		213		5.416012764

		212		4.889334202		212		5.176970959		212		4.458500385		212		4.840126991		212		4.499573708		212		4.946001053

		211		10		211		10		211		4.928081512		211		4.871600151		211		5.066273689		211		10

		210		5.251711845		210		4.760968208		210		5.140692711		210		4.854536533		210		5.412552834		210		4.855380535

		209		10		209		10		209		10		209		5.131233692		209		5.047746181		209		4.858020306

		208		10		208		5.23759222		208		4.755196095		208		10		208		5.39647913		208		4.847342968

		207		10		207		10		207		10		207		5.394041061		207		4.568932056		207		10

		206		4.504105568		206		4.852285862		206		10		206		5.054071903		206		5.732789516		206		4.977471352

		205		10		205		10		205		10		205		10		205		4.569268703		205		4.998065472

		204		4.877878189		204		4.941928864		204		4.824157238		204		5.016970158		204		5.222789288		204		10

		203		10		203		10		203		5.58779335		203		10		203		10		203		6.096329689

		202		5.449694633		202		4.705516815		202		10		202		5.448122025		202		10		202		5.447840214

		201		10		201		10		201		4.683895588		201		5.174703121		201		10		201		10

		200		5.715008736		200		10		200		4.535290718		200		10		200		10		200		10






