SUPPLEMENTARY INFORMATION

An Abrupt Thermal Spin-State Transition Mediated by Anion Disorder in

[FeL2][BF4]2 (L = 2,6-di{pyrazol-1-yl}pyridine)

Joanne M. Holland,a Judith A. McAllister,b,c Zhibao Lu,d Colin A. Kilner,a

Mark Thornton-Petta and Malcolm A. Halcrow*,a.

aSchool of Chemistry, University of Leeds, Woodhouse Lane, Leeds LS2 9JT, U.K.

# Email: M.A.Halcrow@chem.leeds.ac.uk

bDepartment of Chemistry, University of Cambridge, Lensfield Road,

Cambridge CB2 1EW, UK.

cInterdisciplinary Research Centre in Superconductivity,

University of Cambridge, Madingley Road, Cambridge CB3 0HE, UK.

dCentre for Self-Organising Molecular Systems,

School of Chemistry, University of Leeds, Woodhouse Lane, Leeds LS2 9JT, U.K.

Unit cell parameters for [Fe(L1H)2][BF4]2 (1).

(i) Cooling mode:

| T, K | a, Å | b, Å | c, Å | , ° | V, Å3 |
| --- | --- | --- | --- | --- | --- |
| 290 | 8.486(11) | 8.503(7) | 19.02(2) | 95.66(6) | 1366 |
| 273 | 8.490(12) | 8.504(8) | 19.02(3) | 95.85(7) | 1366 |
| 270 | 8.492(12) | 8.500(8) | 19.00(3) | 95.86(7) | 1364 |
| 268 | 8.476(11) | 8.492(7) | 18.97(2) | 95.81(6) | 1359 |
| 266 | 8.479(10) | 8.494(5) | 18.98(2) | 95.85(5) | 1360 |
| 264 | 8.476(10) | 8.492(5) | 18.96(2) | 95.85(5) | 1358 |
| 262 | 8.465(9) | 8.484(6) | 18.941(19) | 95.81(4) | 1353 |
| 261 | 8.477(9) | 8.492(6) | 18.964(19) | 95.87(5) | 1358 |
| 260 | 8.47(4) | 8.49(3) | 18.35(9) | 97.2(2) | 1293 |
| 259 | 8.47(5) | 8.56(4) | 18.55(13) | 97.8(3) | 1333 |
| 257 | 8.47(4) | 8.55(3) | 18.41(9) | 97.7(2) | 1321 |
| 255 | 8.49(3) | 8.55(2) | 18.40(6) | 97.84(14) | 1324 |
| 253 | 8.46(4) | 8.54(2) | 18.36(8) | 97.74(19) | 1315 |
| 250 | 8.48(3) | 8.546(17) | 18.38(6) | 97.82(14) | 1319 |
| 245 | 8.47(2) | 8.547(16) | 18.39(6) | 97.89(13) | 1319 |
| 240 | 8.45(3) | 8.528(18) | 18.33(6) | 97.78(15) | 1308 |

(ii) Warming mode:

| T, K | a, Å | b, Å | c, Å | , ° | V, Å3 |
| --- | --- | --- | --- | --- | --- |
| 240 | 8.45(3) | 8.528(18) | 18.33(6) | 97.78(15) | 1308 |
| 245 | 8.49(4) | 8.55(3) | 18.42(9) | 97.9(2) | 1325 |
| 250 | 8.47(2) | 8.542(15) | 18.36(5) | 97.82(13) | 1312 |
| 257 | 8.47(4) | 8.55(3) | 18.41(9) | 97.7(2) | 1321 |
| 259 | 8.47(5) | 8.56(4) | 18.55(13) | 97.8(3) | 1333 |
| 260 | 8.49(4) | 8.58(3) | 18.68(9) | 98.0(2) | 1347 |
| 261 | 8.60(5) | 8.57(3) | 18.95(11) | 96.9(2) | 1386 |
| 262 | 8.467(10) | 8.485(7) | 18.94(2) | 95.81(6) | 1354 |
| 264 | 4.469(9) | 8.488(6) | 18.96(2) | 95.82(5) | 1356 |
| 270 | 8.474(10) | 8.491(6) | 18.97(2) | 95.78(5) | 1358 |
| 290 | 8.481(11) | 8.500(7) | 19.01(3) | 95.64(6) | 1364 |

Figure S1. Temperature dependence of the unit cell parameters of 1, in cooling mode.

Magnetic susceptibility data for [Fe(L1H)2][BF4]2 (1).

(i) Cooling mode:

| T, K | , cm3 | STD() | M, cm3.mol–1 | MT, cm3.K.mol–1 | eff, BM |
| --- | --- | --- | --- | --- | --- |
| 329.87 | 7.5666 x10–4 | 3.5755 x10–7 | 0.0114 | 3.7544 | 5.4796 |
| 328.12 | 7.5835 x10–4 | 7.3625 x10–7 | 0.0114 | 3.7426 | 5.4710 |
| 326.54 | 7.6217 x10–4 | 7.3111 x10–7 | 0.0115 | 3.7429 | 5.4712 |
| 324.99 | 7.6540 x10–4 | 7.1637 x10–7 | 0.0115 | 3.7405 | 5.4694 |
| 323.33 | 7.6917 x10–4 | 9.4765 x10–7 | 0.0116 | 3.7392 | 5.4685 |
| 321.75 | 7.7234 x10–4 | 9.9119 x10–7 | 0.0116 | 3.7359 | 5.4661 |
| 320.23 | 7.7637 x10–4 | 7.6469 x10–7 | 0.0117 | 3.7372 | 5.4670 |
| 318.76 | 7.7972 x10–4 | 1.0151 x10–6 | 0.0117 | 3.7356 | 5.4659 |
| 317.19 | 7.8358 x10–4 | 8.3557 x10–7 | 0.0118 | 3.7352 | 5.4656 |
| 315.68 | 7.8711 x10–4 | 1.1075 x10–6 | 0.0118 | 3.7337 | 5.4645 |
| 314.13 | 7.9113 x10–4 | 9.5950 x10–7 | 0.0119 | 3.7339 | 5.4646 |
| 312.67 | 7.9476 x10–4 | 8.4277 x10–7 | 0.0119 | 3.7332 | 5.4641 |
| 311.11 | 7.9844 x10–4 | 1.4001 x10–6 | 0.0120 | 3.7313 | 5.4627 |
| 309.65 | 8.0202 x10–4 | 1.1489 x10–6 | 0.0120 | 3.7300 | 5.4618 |
| 308.08 | 8.0546 x10–4 | 1.0540 x10–6 | 0.0121 | 3.7267 | 5.4593 |
| 306.64 | 8.0951 x10–4 | 1.2768 x10–6 | 0.0122 | 3.7274 | 5.4599 |
| 305.14 | 8.1305 x10–4 | 9.3674 x10–7 | 0.0122 | 3.7250 | 5.4581 |
| 303.63 | 8.1691 x10–4 | 8.0721 x10–7 | 0.0123 | 3.7238 | 5.4572 |
| 302.15 | 8.2063 x10–4 | 9.4061 x10–7 | 0.0123 | 3.7221 | 5.4560 |
| 300.65 | 8.2443 x10–4 | 8.6331 x10–7 | 0.0124 | 3.7203 | 5.4547 |
| 299.17 | 8.2827 x10–4 | 9.9926 x10–7 | 0.0124 | 3.7189 | 5.4536 |
| 297.65 | 8.3223 x10–4 | 1.0062 x10–6 | 0.0125 | 3.7172 | 5.4524 |
| 296.09 | 8.3624 x10–4 | 9.6678 x10–7 | 0.0125 | 3.7151 | 5.4509 |
| 294.67 | 8.3989 x10–4 | 1.0177 x10–6 | 0.0126 | 3.7131 | 5.4494 |
| 293.06 | 8.4396 x10–4 | 9.3102 x10–7 | 0.0127 | 3.7103 | 5.4473 |
| 291.57 | 8.4774 x10–4 | 7.9667 x10–7 | 0.0127 | 3.7075 | 5.4453 |
| 290.00 | 8.5158 x10–4 | 1.0277 x10–6 | 0.0128 | 3.7039 | 5.4426 |
| 288.50 | 8.5565 x10–4 | 6.4480 x10–7 | 0.0128 | 3.7019 | 5.4412 |
| 286.95 | 8.5970 x10–4 | 1.0155 x10–6 | 0.0129 | 3.6991 | 5.4391 |
| 285.48 | 8.6352 x10–4 | 9.4402 x10–7 | 0.0129 | 3.6961 | 5.4369 |
| 283.93 | 8.6745 x10–4 | 1.1901 x10–6 | 0.0130 | 3.6924 | 5.4342 |
| 282.41 | 8.7129 x10–4 | 8.9134 x10–7 | 0.0131 | 3.6885 | 5.4313 |
| 280.55 | 8.7771 x10–4 | 4.3361 x10–6 | 0.0132 | 3.6906 | 5.4329 |
| 279.98 | 8.8070 x10–4 | 3.1981 x10–8 | 0.0132 | 3.6954 | 5.4364 |
| 279.99 | 8.8083 x10–4 | 1.9769 x10–7 | 0.0132 | 3.6960 | 5.4368 |
| 279.17 | 8.8256 x10–4 | 3.4001 x10–7 | 0.0132 | 3.6923 | 5.4341 |
| 277.98 | 8.8533 x10–4 | 1.1022 x10–7 | 0.0133 | 3.6878 | 5.4308 |
| 276.99 | 8.8800 x10–4 | 2.7412 x10–8 | 0.0133 | 3.6855 | 5.4291 |
| 275.99 | 8.9045 x10–4 | 1.9225 x10–7 | 0.0133 | 3.6821 | 5.4266 |
| 274.99 | 8.9315 x10–4 | 2.9676 x10–8 | 0.0134 | 3.6797 | 5.4248 |
| 274.00 | 8.9539 x10–4 | 6.1615 x10–8 | 0.0134 | 3.6754 | 5.4217 |
| 272.99 | 8.9817 x10–4 | 3.6220 x10–8 | 0.0135 | 3.6730 | 5.4199 |
| 272.01 | 9.0068 x10–4 | 1.9933 x10–7 | 0.0135 | 3.6698 | 5.4175 |
| 271.00 | 9.0338 x10–4 | 2.6115 x10–7 | 0.0135 | 3.6669 | 5.4154 |
| 269.99 | 9.0586 x10–4 | 2.5708 x10–7 | 0.0136 | 3.6630 | 5.4125 |
| 269.00 | 9.0846 x10–4 | 2.8379 x10–7 | 0.0136 | 3.6598 | 5.4102 |
| 268.00 | 9.1087 x10–4 | 1.1669 x10–7 | 0.0136 | 3.6557 | 5.4071 |
| 266.99 | 9.1333 x10–4 | 1.1607 x10–7 | 0.0137 | 3.6515 | 5.4040 |
| 266.00 | 9.1574 x10–4 | 1.3797 x10–7 | 0.0137 | 3.6474 | 5.4010 |
| 264.99 | 9.1819 x10–4 | 6.6390 x10–8 | 0.0137 | 3.6431 | 5.3977 |
| 263.98 | 9.2051 x10–4 | 2.1901 x10–7 | 0.0138 | 3.6381 | 5.3941 |
| 262.98 | 9.2304 x10–4 | 4.2847 x10–8 | 0.0138 | 3.6341 | 5.3911 |
| 261.97 | 9.2535 x10–4 | 1.3611 x10–7 | 0.0139 | 3.6290 | 5.3873 |
| 260.98 | 9.2733 x10–4 | 3.8504 x10–7 | 0.0139 | 3.6229 | 5.3828 |
| 259.99 | 9.2925 x10–4 | 1.8933 x10–9 | 0.0139 | 3.6164 | 5.3780 |
| 258.98 | 9.1318 x10–4 | 3.7545 x10–7 | 0.0137 | 3.5414 | 5.3219 |
| 257.98 | 6.5423 x10–4 | 7.2078 x10–6 | 9.8809 x10–3 | 2.5491 | 4.5151 |
| 257.00 | 2.3802 x10–4 | 9.3036 x10–6 | 3.7833 x10–3 | 0.9723 | 2.7886 |
| 255.97 | 7.2803 x10–5 | 1.1334 x10–7 | 1.3629 x10–3 | 0.3489 | 1.6703 |
| 255.01 | 6.7005 x10–5 | 2.5493 x10–8 | 1.2780 x10–3 | 0.3259 | 1.6144 |
| 254.01 | 6.3599 x10–5 | 7.1519 x10–8 | 1.2281 x10–3 | 0.3119 | 1.5795 |
| 252.99 | 6.0762 x10–5 | 4.8182 x10–8 | 1.1865 x10–3 | 0.3002 | 1.5494 |
| 251.98 | 5.8464 x10–5 | 3.6194 x10–8 | 1.1528 x10–3 | 0.2905 | 1.5242 |
| 250.98 | 5.6529 x10–5 | 4.3935 x10–8 | 1.1245 x10–3 | 0.2822 | 1.5024 |
| 249.97 | 5.4775 x10–5 | 8.7000 x10–9 | 1.0988 x10–3 | 0.2747 | 1.4821 |
| 248.98 | 5.3204 x10–5 | 3.4064 x10–8 | 1.0758 x10–3 | 0.2678 | 1.4636 |
| 247.98 | 5.1829 x10–5 | 3.8705 x10–8 | 1.0556 x10–3 | 0.2618 | 1.4469 |
| 246.98 | 5.0563 x10–5 | 6.8877 x10–8 | 1.0371 x10–3 | 0.2561 | 1.4312 |
| 245.97 | 4.9403 x10–5 | 3.4854 x10–8 | 1.0201 x10–3 | 0.2509 | 1.4166 |
| 244.97 | 4.8379 x10–5 | 4.4830 x10–8 | 1.0051 x10–3 | 0.2462 | 1.4033 |
| 243.97 | 4.7402 x10–5 | 6.2791 x10–8 | 9.9076 x10–4 | 0.2417 | 1.3904 |
| 242.98 | 4.6527 x10–5 | 1.4954 x10–8 | 9.7795 x10–4 | 0.2376 | 1.3785 |
| 241.97 | 4.5623 x10–5 | 8.3321 x10–9 | 9.6470 x10–4 | 0.2334 | 1.3663 |
| 240.98 | 4.4808 x10–5 | 4.5018 x10–9 | 9.5276 x10–4 | 0.2296 | 1.3551 |
| 239.97 | 4.4065 x10–5 | 3.1232 x10–8 | 9.4188 x10–4 | 0.2260 | 1.3445 |
| 238.97 | 4.3396 x10–5 | 6.3732 x10–8 | 9.3208 x10–4 | 0.2227 | 1.3347 |
| 237.97 | 4.2764 x10–5 | 1.6258 x10–9 | 9.2282 x10–4 | 0.2196 | 1.3253 |
| 236.97 | 4.2174 x10–5 | 2.5995 x10–8 | 9.1417 x10–4 | 0.2166 | 1.3163 |
| 235.96 | 4.1623 x10–5 | 1.8385 x10–8 | 9.0610 x10–4 | 0.2138 | 1.3076 |
| 234.97 | 4.1087 x10–5 | 1.8846 x10–8 | 8.9825 x10–4 | 0.2111 | 1.2992 |
| 233.97 | 4.0612 x10–5 | 8.3090 x10–10 | 8.9129 x10–4 | 0.2085 | 1.2914 |
| 232.96 | 4.0150 x10–5 | 3.8180 x10–8 | 8.8452 x10–4 | 0.2061 | 1.2837 |
| 232.01 | 3.9689 x10–5 | 3.5857 x10–8 | 8.7777 x10–4 | 0.2037 | 1.2762 |
| 230.97 | 3.9285 x10–5 | 3.7532 x10–9 | 8.7185 x10–4 | 0.2014 | 1.2690 |
| 229.97 | 3.8896 x10–5 | 3.3012 x10–8 | 8.6615 x10–4 | 0.1992 | 1.2622 |
| 228.96 | 3.8525 x10–5 | 8.9469 x10–9 | 8.6072 x10–4 | 0.1971 | 1.2554 |
| 227.99 | 3.8213 x10–5 | 2.9897 x10–8 | 8.5614 x10–4 | 0.1952 | 1.2494 |
| 226.96 | 3.7867 x10–5 | 1.8167 x10–8 | 8.5108 x10–4 | 0.1932 | 1.2429 |
| 225.96 | 3.7565 x10–5 | 1.7634 x10–8 | 8.4665 x10–4 | 0.1913 | 1.2369 |
| 224.97 | 3.7258 x10–5 | 3.2078 x10–8 | 8.4215 x10–4 | 0.1895 | 1.2309 |
| 223.96 | 3.7030 x10–5 | 4.4992 x10–9 | 8.3881 x10–4 | 0.1879 | 1.2257 |
| 222.97 | 3.6777 x10–5 | 1.5177 x10–9 | 8.3511 x10–4 | 0.1862 | 1.2203 |
| 221.96 | 3.6527 x10–5 | 3.4111 x10–9 | 8.3144 x10–4 | 0.1845 | 1.2149 |
| 221.00 | 3.6373 x10–5 | 1.1321 x10–8 | 8.2919 x10–4 | 0.1833 | 1.2106 |
| 219.96 | 3.6166 x10–5 | 8.6563 x10–9 | 8.2616 x10–4 | 0.1817 | 1.2055 |
| 218.96 | 3.5982 x10–5 | 7.2800 x10–9 | 8.2346 x10–4 | 0.1803 | 1.2008 |
| 217.97 | 3.5794 x10–5 | 1.6592 x10–9 | 8.2071 x10–4 | 0.1789 | 1.1961 |
| 216.97 | 3.5628 x10–5 | 1.5517 x10–8 | 8.1827 x10–4 | 0.1775 | 1.1916 |
| 215.97 | 3.5488 x10–5 | 6.0169 x10–9 | 8.1622 x10–4 | 0.1763 | 1.1874 |
| 214.98 | 3.5356 x10–5 | 9.0241 x10–9 | 8.1429 x10–4 | 0.1751 | 1.1832 |
| 213.97 | 3.5237 x10–5 | 8.2318 x10–9 | 8.1255 x10–4 | 0.1739 | 1.1792 |
| 212.95 | 3.5087 x10–5 | 2.3450 x10–8 | 8.1035 x10–4 | 0.1726 | 1.1748 |
| 211.96 | 3.4977 x10–5 | 1.1779 x10–8 | 8.0874 x10–4 | 0.1714 | 1.1709 |
| 210.95 | 3.4872 x10–5 | 1.2114 x10–8 | 8.0720 x10–4 | 0.1703 | 1.1670 |
| 209.98 | 3.4714 x10–5 | 2.0324 x10–10 | 8.0488 x10–4 | 0.1690 | 1.1626 |
| 208.95 | 3.4630 x10–5 | 8.1598 x10–9 | 8.0365 x10–4 | 0.1679 | 1.1589 |
| 207.96 | 3.4548 x10–5 | 6.4954 x10–9 | 8.0245 x10–4 | 0.1669 | 1.1553 |
| 206.96 | 3.4411 x10–5 | 6.3025 x10–10 | 8.0045 x10–4 | 0.1657 | 1.1510 |
| 205.96 | 3.4339 x10–5 | 4.8105 x10–9 | 7.9939 x10–4 | 0.1646 | 1.1475 |
| 204.96 | 3.4274 x10–5 | 5.9063 x10–9 | 7.9844 x10–4 | 0.1636 | 1.1440 |
| 203.96 | 3.4247 x10–5 | 1.0408 x10–8 | 7.9804 x10–4 | 0.1628 | 1.1409 |
| 202.95 | 3.4149 x10–5 | 1.1453 x10–8 | 7.9661 x10–4 | 0.1617 | 1.1371 |
| 201.95 | 3.4097 x10–5 | 4.8413 x10–9 | 7.9584 x10–4 | 0.1607 | 1.1337 |
| 200.95 | 3.4062 x10–5 | 1.7981 x10–8 | 7.9533 x10–4 | 0.1598 | 1.1306 |
| 199.96 | 3.3995 x10–5 | 1.5561 x10–8 | 7.9435 x10–4 | 0.1588 | 1.1271 |
| 200.03 | 3.4000 x10–5 | 6.2639 x10–9 | 7.9442 x10–4 | 0.1589 | 1.1273 |
| 198.23 | 3.3935 x10–5 | 4.5172 x10–9 | 7.9347 x10–4 | 0.1573 | 1.1216 |
| 196.64 | 3.3879 x10–5 | 7.2800 x10–10 | 7.9265 x10–4 | 0.1559 | 1.1165 |
| 195.01 | 3.3806 x10–5 | 7.9540 x10–9 | 7.9158 x10–4 | 0.1544 | 1.1111 |
| 193.49 | 3.3765 x10–5 | 2.6283 x10–8 | 7.9098 x10–4 | 0.1530 | 1.1063 |
| 191.96 | 3.3702 x10–5 | 5.2269 x10–8 | 7.9006 x10–4 | 0.1517 | 1.1013 |
| 190.43 | 3.3725 x10–5 | 1.1928 x10–8 | 7.9040 x10–4 | 0.1505 | 1.0972 |
| 188.95 | 3.3712 x10–5 | 1.7055 x10–9 | 7.9020 x10–4 | 0.1493 | 1.0928 |
| 187.50 | 3.3708 x10–5 | 1.4303 x10–9 | 7.9015 x10–4 | 0.1482 | 1.0885 |
| 185.95 | 3.3702 x10–5 | 6.1558 x10–9 | 7.9006 x10–4 | 0.1469 | 1.0839 |
| 184.54 | 3.3728 x10–5 | 1.2687 x10–8 | 7.9044 x10–4 | 0.1459 | 1.0801 |
| 182.94 | 3.3727 x10–5 | 4.5782 x10–8 | 7.9042 x10–4 | 0.1446 | 1.0754 |
| 181.55 | 3.3728 x10–5 | 3.0844 x10–9 | 7.9044 x10–4 | 0.1435 | 1.0713 |
| 179.96 | 3.3688 x10–5 | 6.4723 x10–9 | 7.8985 x10–4 | 0.1421 | 1.0662 |
| 178.49 | 3.3700 x10–5 | 2.1475 x10–8 | 7.9003 x10–4 | 0.1410 | 1.0620 |
| 176.96 | 3.3720 x10–5 | 8.3784 x10–9 | 7.9032 x10–4 | 0.1399 | 1.0576 |
| 175.49 | 3.3751 x10–5 | 5.4546 x10–8 | 7.9078 x10–4 | 0.1388 | 1.0535 |
| 173.99 | 3.3768 x10–5 | 1.6695 x10–9 | 7.9102 x10–4 | 0.1376 | 1.0491 |
| 172.52 | 3.3811 x10–5 | 1.3441 x10–8 | 7.9165 x10–4 | 0.1366 | 1.0451 |
| 170.95 | 3.3801 x10–5 | 2.0142 x10–9 | 7.9151 x10–4 | 0.1353 | 1.0403 |
| 169.52 | 3.3780 x10–5 | 1.1543 x10–8 | 7.9120 x10–4 | 0.1341 | 1.0357 |
| 167.96 | 3.3813 x10–5 | 1.5640 x10–8 | 7.9168 x10–4 | 0.1330 | 1.0312 |
| 166.53 | 3.3874 x10–5 | 3.8767 x10–9 | 7.9258 x10–4 | 0.1320 | 1.0274 |
| 164.96 | 3.3887 x10–5 | 1.6754 x10–8 | 7.9277 x10–4 | 0.1308 | 1.0227 |
| 163.49 | 3.3917 x10–5 | 7.7173 x10–9 | 7.9321 x10–4 | 0.1297 | 1.0184 |
| 161.95 | 3.3992 x10–5 | 1.7274 x10–8 | 7.9431 x10–4 | 0.1286 | 1.0143 |
| 160.48 | 3.4000 x10–5 | 6.4182 x10–9 | 7.9442 x10–4 | 0.1275 | 1.0098 |
| 158.97 | 3.4061 x10–5 | 1.0933 x10–9 | 7.9532 x10–4 | 0.1264 | 1.0056 |
| 157.52 | 3.4087 x10–5 | 3.7540 x10–8 | 7.9570 x10–4 | 0.1253 | 1.0012 |
| 155.98 | 3.4102 x10–5 | 1.8882 x10–9 | 7.9592 x10–4 | 0.1241 | 0.9964 |
| 154.49 | 3.4118 x10–5 | 6.0247 x10–9 | 7.9615 x10–4 | 0.1230 | 0.9918 |
| 153.02 | 3.4168 x10–5 | 2.1403 x10–8 | 7.9689 x10–4 | 0.1219 | 0.9875 |
| 151.53 | 3.4251 x10–5 | 8.2884 x10–9 | 7.9810 x10–4 | 0.1209 | 0.9835 |
| 150.01 | 3.4292 x10–5 | 1.4722 x10–8 | 7.9870 x10–4 | 0.1198 | 0.9789 |
| 148.55 | 3.4344 x10–5 | 1.0686 x10–8 | 7.9946 x10–4 | 0.1188 | 0.9746 |
| 147.05 | 3.4371 x10–5 | 7.5938 x10–9 | 7.9986 x10–4 | 0.1176 | 0.9699 |
| 145.56 | 3.4405 x10–5 | 2.7021 x10–8 | 8.0036 x10–4 | 0.1165 | 0.9653 |
| 144.06 | 3.4458 x10–5 | 1.9422 x10–9 | 8.0113 x10–4 | 0.1154 | 0.9607 |
| 142.56 | 3.4523 x10–5 | 4.5221 x10–8 | 8.0209 x10–4 | 0.1143 | 0.9563 |
| 141.02 | 3.4587 x10–5 | 1.3132 x10–8 | 8.0302 x10–4 | 0.1132 | 0.9517 |
| 139.58 | 3.4644 x10–5 | 6.9970 x10–9 | 8.0386 x10–4 | 0.1122 | 0.9473 |
| 138.03 | 3.4706 x10–5 | 3.6390 x10–8 | 8.0477 x10–4 | 0.1111 | 0.9425 |
| 136.59 | 3.4710 x10–5 | 1.4200 x10–9 | 8.0483 x10–4 | 0.1099 | 0.9376 |
| 135.07 | 3.4780 x10–5 | 4.1905 x10–9 | 8.0585 x10–4 | 0.1088 | 0.9330 |
| 133.60 | 3.4854 x10–5 | 1.0385 x10–8 | 8.0694 x10–4 | 0.1078 | 0.9285 |
| 132.07 | 3.4924 x10–5 | 1.3423 x10–8 | 8.0796 x10–4 | 0.1067 | 0.9238 |
| 130.63 | 3.5003 x10–5 | 3.1551 x10–8 | 8.0912 x10–4 | 0.1057 | 0.9194 |
| 129.07 | 3.5084 x10–5 | 1.5777 x10–8 | 8.1030 x10–4 | 0.1046 | 0.9146 |
| 127.59 | 3.5136 x10–5 | 1.9720 x10–8 | 8.1107 x10–4 | 0.1035 | 0.9097 |
| 126.11 | 3.5185 x10–5 | 5.2282 x10–8 | 8.1178 x10–4 | 0.1024 | 0.9048 |
| 124.63 | 3.5232 x10–5 | 2.4613 x10–8 | 8.1247 x10–4 | 0.1013 | 0.8999 |
| 123.04 | 3.5298 x10–5 | 2.4816 x10–8 | 8.1344 x10–4 | 0.1001 | 0.8947 |
| 121.62 | 3.5381 x10–5 | 1.9808 x10–8 | 8.1466 x10–4 | 0.0991 | 0.8902 |
| 120.08 | 3.5466 x10–5 | 9.5386 x10–9 | 8.1590 x10–4 | 0.0980 | 0.8852 |
| 118.67 | 3.5526 x10–5 | 1.2775 x10–8 | 8.1678 x10–4 | 0.0969 | 0.8804 |
| 117.10 | 3.5635 x10–5 | 2.2704 x10–8 | 8.1838 x10–4 | 0.0958 | 0.8755 |
| 115.62 | 3.5695 x10–5 | 2.2151 x10–8 | 8.1926 x10–4 | 0.0947 | 0.8704 |
| 114.06 | 3.5756 x10–5 | 1.9653 x10–9 | 8.2015 x10–4 | 0.0935 | 0.8650 |
| 112.61 | 3.5838 x10–5 | 3.1556 x10–8 | 8.2135 x10–4 | 0.0925 | 0.8601 |
| 111.12 | 3.5945 x10–5 | 9.6166 x10–8 | 8.2292 x10–4 | 0.0914 | 0.8552 |
| 109.64 | 3.6028 x10–5 | 3.1245 x10–8 | 8.2413 x10–4 | 0.0904 | 0.8501 |
| 108.09 | 3.6125 x10–5 | 5.6226 x10–8 | 8.2556 x10–4 | 0.0892 | 0.8448 |
| 106.61 | 3.6205 x10–5 | 3.7146 x10–9 | 8.2673 x10–4 | 0.0881 | 0.8396 |
| 105.11 | 3.6300 x10–5 | 4.3021 x10–8 | 8.2812 x10–4 | 0.0870 | 0.8343 |
| 103.63 | 3.6394 x10–5 | 2.2758 x10–8 | 8.2950 x10–4 | 0.0860 | 0.8291 |
| 102.09 | 3.6544 x10–5 | 2.0075 x10–8 | 8.3169 x10–4 | 0.0849 | 0.8240 |
| 100.66 | 3.6646 x10–5 | 2.1300 x10–8 | 8.3319 x10–4 | 0.0839 | 0.8190 |
| 99.11 | 3.6744 x10–5 | 3.5510 x10–8 | 8.3462 x10–4 | 0.0827 | 0.8134 |
| 97.65 | 3.6843 x10–5 | 2.2519 x10–8 | 8.3607 x10–4 | 0.0816 | 0.8081 |
| 96.16 | 3.6958 x10–5 | 4.0727 x10–8 | 8.3776 x10–4 | 0.0806 | 0.8027 |
| 94.65 | 3.7104 x10–5 | 2.3756 x10–8 | 8.3990 x10–4 | 0.0795 | 0.7974 |
| 93.20 | 3.7223 x10–5 | 1.9327 x10–8 | 8.4164 x10–4 | 0.0784 | 0.7921 |
| 91.69 | 3.7384 x10–5 | 5.5089 x10–8 | 8.4400 x10–4 | 0.0774 | 0.7867 |
| 90.16 | 3.7533 x10–5 | 3.5955 x10–8 | 8.4618 x10–4 | 0.0763 | 0.7811 |
| 88.70 | 3.7670 x10–5 | 5.4039 x10–8 | 8.4819 x10–4 | 0.0752 | 0.7757 |
| 87.12 | 3.7685 x10–5 | 1.3063 x10–7 | 8.4841 x10–4 | 0.0739 | 0.7688 |
| 85.64 | 3.7968 x10–5 | 5.9061 x10–8 | 8.5256 x10–4 | 0.0730 | 0.7642 |
| 84.12 | 3.8154 x10–5 | 6.7202 x10–8 | 8.5528 x10–4 | 0.0719 | 0.7586 |
| 82.71 | 3.8341 x10–5 | 3.5649 x10–8 | 8.5802 x10–4 | 0.0710 | 0.7534 |
| 81.16 | 3.8502 x10–5 | 4.0526 x10–8 | 8.6038 x10–4 | 0.0698 | 0.7473 |
| 79.66 | 3.8676 x10–5 | 4.0315 x10–8 | 8.6293 x10–4 | 0.0687 | 0.7415 |
| 78.05 | 3.8865 x10–5 | 6.6763 x10–8 | 8.6570 x10–4 | 0.0676 | 0.7351 |
| 76.64 | 3.9048 x10–5 | 8.8819 x10–8 | 8.6838 x10–4 | 0.0666 | 0.7296 |
| 75.11 | 3.9268 x10–5 | 6.9440 x10–8 | 8.7160 x10–4 | 0.0655 | 0.7236 |
| 73.71 | 3.9451 x10–5 | 6.0928 x10–8 | 8.7428 x10–4 | 0.0644 | 0.7179 |
| 72.17 | 3.9688 x10–5 | 5.7569 x10–8 | 8.7775 x10–4 | 0.0633 | 0.7118 |
| 70.69 | 3.9914 x10–5 | 9.7573 x10–9 | 8.8106 x10–4 | 0.0623 | 0.7058 |
| 69.14 | 4.0101 x10–5 | 6.8239 x10–8 | 8.8380 x10–4 | 0.0611 | 0.6990 |
| 67.68 | 4.0361 x10–5 | 1.0018 x10–7 | 8.8761 x10–4 | 0.0601 | 0.6931 |
| 66.19 | 4.0600 x10–5 | 7.2646 x10–8 | 8.9111 x10–4 | 0.0590 | 0.6868 |
| 64.65 | 4.0895 x10–5 | 6.9865 x10–8 | 8.9544 x10–4 | 0.0579 | 0.6804 |
| 63.08 | 4.1214 x10–5 | 9.3184 x10–8 | 9.0011 x10–4 | 0.0568 | 0.6738 |
| 61.63 | 4.1488 x10–5 | 1.1163 x10–7 | 9.0412 x10–4 | 0.0557 | 0.6675 |
| 60.12 | 4.1832 x10–5 | 1.3446 x10–7 | 9.0916 x10–4 | 0.0547 | 0.6612 |
| 58.64 | 4.2192 x10–5 | 1.4992 x10–7 | 9.1444 x10–4 | 0.0536 | 0.6549 |
| 57.08 | 4.2518 x10–5 | 9.9080 x10–8 | 9.1921 x10–4 | 0.0525 | 0.6478 |
| 55.65 | 4.2863 x10–5 | 1.3659 x10–7 | 9.2427 x10–4 | 0.0514 | 0.6414 |
| 54.11 | 4.3283 x10–5 | 1.4502 x10–7 | 9.3042 x10–4 | 0.0503 | 0.6345 |
| 52.67 | 4.3693 x10–5 | 1.4811 x10–7 | 9.3643 x10–4 | 0.0493 | 0.6280 |
| 51.13 | 4.4116 x10–5 | 1.7400 x10–7 | 9.4262 x10–4 | 0.0482 | 0.6208 |
| 49.63 | 4.4619 x10–5 | 1.6311 x10–7 | 9.4999 x10–4 | 0.0471 | 0.6140 |
| 48.08 | 4.5120 x10–5 | 1.7635 x10–7 | 9.5733 x10–4 | 0.0460 | 0.6067 |
| 46.54 | 4.5642 x10–5 | 1.8570 x10–7 | 9.6498 x10–4 | 0.0449 | 0.5993 |
| 44.95 | 4.6250 x10–5 | 2.1296 x10–7 | 9.7389 x10–4 | 0.0438 | 0.5917 |
| 43.40 | 4.6908 x10–5 | 1.7958 x10–7 | 9.8353 x10–4 | 0.0427 | 0.5843 |
| 41.77 | 4.7607 x10–5 | 2.7593 x10–7 | 9.9377 x10–4 | 0.0415 | 0.5762 |
| 40.24 | 4.8351 x10–5 | 2.0691 x10–7 | 1.0047 x10–3 | 0.0404 | 0.5686 |
| 38.69 | 4.9074 x10–5 | 2.4325 x10–7 | 1.0153 x10–3 | 0.0393 | 0.5605 |
| 37.16 | 4.9905 x10–5 | 2.5669 x10–7 | 1.0274 x10–3 | 0.0382 | 0.5526 |
| 35.67 | 5.0770 x10–5 | 3.0436 x10–7 | 1.0401 x10–3 | 0.0371 | 0.5447 |
| 34.24 | 5.1705 x10–5 | 3.1391 x10–7 | 1.0538 x10–3 | 0.0361 | 0.5372 |
| 32.72 | 5.2745 x10–5 | 3.3633 x10–7 | 1.0690 x10–3 | 0.0350 | 0.5289 |
| 31.23 | 5.3834 x10–5 | 3.9499 x10–7 | 1.0850 x10–3 | 0.0339 | 0.5206 |
| 29.81 | 5.5068 x10–5 | 4.1961 x10–7 | 1.1031 x10–3 | 0.0329 | 0.5128 |
| 28.41 | 5.6325 x10–5 | 4.3728 x10–7 | 1.1215 x10–3 | 0.0319 | 0.5048 |
| 27.00 | 5.7697 x10–5 | 4.5820 x10–7 | 1.1416 x10–3 | 0.0308 | 0.4965 |
| 25.69 | 5.9164 x10–5 | 4.8307 x10–7 | 1.1631 x10–3 | 0.0299 | 0.4888 |
| 24.23 | 6.0912 x10–5 | 6.1161 x10–7 | 1.1887 x10–3 | 0.0288 | 0.4799 |
| 22.95 | 6.2654 x10–5 | 3.7575 x10–7 | 1.2142 x10–3 | 0.0279 | 0.4721 |
| 20.94 | 6.5378 x10–5 | 9.3357 x10–7 | 1.2541 x10–3 | 0.0263 | 0.4583 |
| 19.77 | 6.7318 x10–5 | 4.5776 x10–7 | 1.2825 x10–3 | 0.0254 | 0.4504 |
| 17.71 | 7.0359 x10–5 | 9.9840 x10–7 | 1.3271 x10–3 | 0.0235 | 0.4336 |
| 16.35 | 7.2623 x10–5 | 6.1855 x10–7 | 1.3603 x10–3 | 0.0222 | 0.4217 |
| 15.70 | 7.3751 x10–5 | 1.0481 x10–7 | 1.3768 x10–3 | 0.0216 | 0.4158 |
| 13.58 | 7.6824 x10–5 | 8.5851 x10–7 | 1.4218 x10–3 | 0.0193 | 0.3929 |
| 12.09 | 7.9288 x10–5 | 8.2551 x10–7 | 1.4579 x10–3 | 0.0176 | 0.3754 |
| 11.08 | 8.1321 x10–5 | 5.4869 x10–7 | 1.4877 x10–3 | 0.0165 | 0.3630 |
| 10.01 | 8.4067 x10–5 | 9.5952 x10–9 | 1.5279 x10–3 | 0.0153 | 0.3498 |

(ii) Warming mode:

| T, K | , cm3 | STD() | M, cm3.mol–1 | MT, cm3.K.mol–1 | eff, BM |
| --- | --- | --- | --- | --- | --- |
| 10.01 | 8.4090 x10–5 | 4.0928 x10–8 | 1.5282 x10–3 | 0.0153 | 0.3498 |
| 11.99 | 8.0191 x10–5 | 7.0414 x10–7 | 1.4711 x10–3 | 0.0176 | 0.3757 |
| 13.61 | 7.7081 x10–5 | 6.4331 x10–7 | 1.4256 x10–3 | 0.0194 | 0.3939 |
| 15.12 | 7.4761 x10–5 | 6.1046 x10–7 | 1.3916 x10–3 | 0.0210 | 0.4101 |
| 16.60 | 7.2495 x10–5 | 5.7688 x10–7 | 1.3584 x10–3 | 0.0226 | 0.4247 |
| 18.05 | 7.0304 x10–5 | 6.0546 x10–7 | 1.3263 x10–3 | 0.0239 | 0.4376 |
| 19.57 | 6.8004 x10–5 | 5.9658 x10–7 | 1.2926 x10–3 | 0.0253 | 0.4497 |
| 21.05 | 6.5776 x10–5 | 5.7572 x10–7 | 1.2599 x10–3 | 0.0265 | 0.4605 |
| 22.60 | 6.3510 x10–5 | 5.2005 x10–7 | 1.2267 x10–3 | 0.0277 | 0.4709 |
| 24.06 | 6.1565 x10–5 | 4.5499 x10–7 | 1.1983 x10–3 | 0.0288 | 0.4802 |
| 25.54 | 5.9757 x10–5 | 4.8493 x10–7 | 1.1718 x10–3 | 0.0299 | 0.4892 |
| 27.04 | 5.8089 x10–5 | 4.2295 x10–7 | 1.1473 x10–3 | 0.0310 | 0.4981 |
| 28.59 | 5.6547 x10–5 | 3.6022 x10–7 | 1.1247 x10–3 | 0.0322 | 0.5071 |
| 30.04 | 5.5296 x10–5 | 3.2722 x10–7 | 1.1064 x10–3 | 0.0332 | 0.5155 |
| 32.21 | 5.3556 x10–5 | 3.1198 x10–7 | 1.0809 x10–3 | 0.0348 | 0.5277 |
| 33.37 | 5.2704 x10–5 | 2.7304 x10–7 | 1.0684 x10–3 | 0.0357 | 0.5340 |
| 34.58 | 5.1841 x10–5 | 2.5614 x10–7 | 1.0558 x10–3 | 0.0365 | 0.5403 |
| 36.04 | 5.0951 x10–5 | 2.2475 x10–7 | 1.0428 x10–3 | 0.0376 | 0.5482 |
| 37.53 | 5.0117 x10–5 | 2.2991 x10–7 | 1.0305 x10–3 | 0.0387 | 0.5562 |
| 39.03 | 4.9226 x10–5 | 2.0427 x10–7 | 1.0175 x10–3 | 0.0397 | 0.5635 |
| 40.55 | 4.8472 x10–5 | 2.0085 x10–7 | 1.0064 x10–3 | 0.0408 | 0.5713 |
| 41.99 | 4.7752 x10–5 | 2.0200 x10–7 | 9.9589 x10–4 | 0.0418 | 0.5783 |
| 43.52 | 4.7107 x10–5 | 1.0649 x10–7 | 9.8644 x10–4 | 0.0429 | 0.5859 |
| 44.99 | 4.6467 x10–5 | 1.3836 x10–7 | 9.7707 x10–4 | 0.0440 | 0.5929 |
| 46.48 | 4.5914 x10–5 | 1.4083 x10–7 | 9.6897 x10–4 | 0.0450 | 0.6001 |
| 48.03 | 4.5404 x10–5 | 1.0341 x10–7 | 9.6149 x10–4 | 0.0462 | 0.6077 |
| 49.49 | 4.4870 x10–5 | 9.7434 x10–8 | 9.5367 x10–4 | 0.0472 | 0.6144 |
| 50.94 | 4.4403 x10–5 | 1.1936 x10–7 | 9.4683 x10–4 | 0.0482 | 0.6211 |
| 53.15 | 4.3747 x10–5 | 6.2593 x10–8 | 9.3722 x10–4 | 0.0498 | 0.6312 |
| 54.34 | 4.3411 x10–5 | 1.2072 x10–7 | 9.3230 x10–4 | 0.0507 | 0.6365 |
| 55.53 | 4.3155 x10–5 | 1.0341 x10–7 | 9.2855 x10–4 | 0.0516 | 0.6422 |
| 56.95 | 4.2733 x10–5 | 1.1335 x10–7 | 9.2236 x10–4 | 0.0525 | 0.6482 |
| 58.53 | 4.2323 x10–5 | 1.4477 x10–7 | 9.1636 x10–4 | 0.0536 | 0.6549 |
| 60.00 | 4.1938 x10–5 | 1.1202 x10–7 | 9.1072 x10–4 | 0.0546 | 0.6611 |
| 61.51 | 4.1594 x10–5 | 8.6035 x10–8 | 9.0568 x10–4 | 0.0557 | 0.6675 |
| 62.98 | 4.1314 x10–5 | 8.1299 x10–8 | 9.0157 x10–4 | 0.0568 | 0.6739 |
| 64.47 | 4.1022 x10–5 | 1.4334 x10–8 | 8.9730 x10–4 | 0.0578 | 0.6802 |
| 65.94 | 4.0762 x10–5 | 5.7111 x10–8 | 8.9349 x10–4 | 0.0589 | 0.6864 |
| 67.50 | 4.0489 x10–5 | 6.4000 x10–8 | 8.8949 x10–4 | 0.0600 | 0.6929 |
| 68.96 | 4.0236 x10–5 | 7.5316 x10–8 | 8.8578 x10–4 | 0.0611 | 0.6989 |
| 70.48 | 3.9950 x10–5 | 1.1026 x10–7 | 8.8159 x10–4 | 0.0621 | 0.7049 |
| 71.89 | 3.9730 x10–5 | 3.6547 x10–8 | 8.7837 x10–4 | 0.0631 | 0.7107 |
| 74.10 | 3.9377 x10–5 | 8.1163 x10–8 | 8.7320 x10–4 | 0.0647 | 0.7193 |
| 75.31 | 3.9183 x10–5 | 7.8675 x10–8 | 8.7036 x10–4 | 0.0655 | 0.7240 |
| 76.54 | 3.9012 x10–5 | 7.3387 x10–8 | 8.6785 x10–4 | 0.0664 | 0.7289 |
| 77.94 | 3.8844 x10–5 | 4.7714 x10–8 | 8.6539 x10–4 | 0.0674 | 0.7345 |
| 79.48 | 3.8628 x10–5 | 4.7778 x10–8 | 8.6222 x10–4 | 0.0685 | 0.7403 |
| 80.93 | 3.8441 x10–5 | 7.6687 x10–8 | 8.5948 x10–4 | 0.0696 | 0.7458 |
| 82.45 | 3.8267 x10–5 | 2.2023 x10–8 | 8.5694 x10–4 | 0.0707 | 0.7517 |
| 83.91 | 3.8146 x10–5 | 1.6073 x10–8 | 8.5516 x10–4 | 0.0718 | 0.7576 |
| 85.44 | 3.7945 x10–5 | 4.5807 x10–8 | 8.5222 x10–4 | 0.0728 | 0.7631 |
| 86.83 | 3.7792 x10–5 | 1.6412 x10–8 | 8.4998 x10–4 | 0.0738 | 0.7683 |
| 88.47 | 3.7683 x10–5 | 3.9608 x10–8 | 8.4838 x10–4 | 0.0751 | 0.7747 |
| 89.90 | 3.7517 x10–5 | 5.0080 x10–8 | 8.4595 x10–4 | 0.0761 | 0.7799 |
| 91.45 | 3.7359 x10–5 | 2.5228 x10–8 | 8.4363 x10–4 | 0.0771 | 0.7855 |
| 92.95 | 3.7214 x10–5 | 5.4904 x10–8 | 8.4151 x10–4 | 0.0782 | 0.7909 |
| 95.14 | 3.7030 x10–5 | 2.8855 x10–8 | 8.3881 x10–4 | 0.0798 | 0.7989 |
| 96.28 | 3.6928 x10–5 | 9.6569 x10–9 | 8.3732 x10–4 | 0.0806 | 0.8030 |
| 97.47 | 3.6868 x10–5 | 4.0724 x10–8 | 8.3644 x10–4 | 0.0815 | 0.8075 |
| 98.85 | 3.6763 x10–5 | 4.0845 x10–8 | 8.3490 x10–4 | 0.0825 | 0.8124 |
| 100.43 | 3.6585 x10–5 | 1.8444 x10–9 | 8.3229 x10–4 | 0.0836 | 0.8176 |
| 101.87 | 3.6476 x10–5 | 1.7493 x10–8 | 8.3070 x10–4 | 0.0846 | 0.8227 |
| 103.37 | 3.6352 x10–5 | 1.4668 x10–8 | 8.2888 x10–4 | 0.0857 | 0.8278 |
| 104.84 | 3.6215 x10–5 | 3.9037 x10–8 | 8.2687 x10–4 | 0.0867 | 0.8327 |
| 106.39 | 3.6122 x10–5 | 2.5735 x10–8 | 8.2551 x10–4 | 0.0878 | 0.8381 |
| 107.88 | 3.6034 x10–5 | 3.2979 x10–9 | 8.2422 x10–4 | 0.0889 | 0.8433 |
| 109.40 | 3.5953 x10–5 | 2.3173 x10–8 | 8.2304 x10–4 | 0.0900 | 0.8486 |
| 110.84 | 3.5872 x10–5 | 3.2567 x10–9 | 8.2185 x10–4 | 0.0911 | 0.8535 |
| 112.38 | 3.5782 x10–5 | 6.8530 x10–9 | 8.2053 x10–4 | 0.0922 | 0.8588 |
| 113.80 | 3.5690 x10–5 | 9.3122 x10–9 | 8.1918 x10–4 | 0.0932 | 0.8635 |
| 116.03 | 3.5587 x10–5 | 2.7703 x10–8 | 8.1767 x10–4 | 0.0949 | 0.8711 |
| 117.20 | 3.5515 x10–5 | 1.9515 x10–8 | 8.1662 x10–4 | 0.0957 | 0.8749 |
| 118.37 | 3.5461 x10–5 | 2.3294 x10-11 | 8.1583 x10–4 | 0.0966 | 0.8788 |
| 119.84 | 3.5397 x10–5 | 1.3377 x10–10 | 8.1489 x10–4 | 0.0977 | 0.8838 |
| 121.38 | 3.5329 x10–5 | 2.4706 x10–8 | 8.1389 x10–4 | 0.0988 | 0.8889 |
| 122.79 | 3.5259 x10–5 | 2.6699 x10–8 | 8.1287 x10–4 | 0.0998 | 0.8935 |
| 124.34 | 3.5187 x10–5 | 8.0209 x10–9 | 8.1181 x10–4 | 0.1009 | 0.8985 |
| 125.77 | 3.5106 x10–5 | 2.7003 x10–8 | 8.1063 x10–4 | 0.1020 | 0.9030 |
| 127.34 | 3.5009 x10–5 | 8.8055 x10–9 | 8.0921 x10–4 | 0.1030 | 0.9078 |
| 128.82 | 3.4912 x10–5 | 2.4189 x10–8 | 8.0778 x10–4 | 0.1041 | 0.9123 |
| 130.32 | 3.4842 x10–5 | 2.1228 x10–8 | 8.0676 x10–4 | 0.1051 | 0.9170 |
| 131.77 | 3.4776 x10–5 | 1.2373 x10–9 | 8.0579 x10–4 | 0.1062 | 0.9215 |
| 133.29 | 3.4683 x10–5 | 1.7426 x10–8 | 8.0443 x10–4 | 0.1072 | 0.9260 |
| 134.80 | 3.4606 x10–5 | 1.0496 x10–8 | 8.0330 x10–4 | 0.1083 | 0.9306 |
| 137.05 | 3.4551 x10–5 | 1.7377 x10–8 | 8.0250 x10–4 | 0.1100 | 0.9379 |
| 138.25 | 3.4496 x10–5 | 1.6448 x10–8 | 8.0169 x10–4 | 0.1108 | 0.9415 |
| 139.44 | 3.4429 x10–5 | 1.3703 x10–8 | 8.0071 x10–4 | 0.1117 | 0.9450 |
| 140.81 | 3.4403 x10–5 | 1.3937 x10–8 | 8.0033 x10–4 | 0.1127 | 0.9494 |
| 142.30 | 3.4343 x10–5 | 2.6674 x10–8 | 7.9945 x10–4 | 0.1138 | 0.9538 |
| 143.76 | 3.4273 x10–5 | 2.6725 x10–8 | 7.9842 x10–4 | 0.1148 | 0.9581 |
| 145.27 | 3.4229 x10–5 | 1.1579 x10–8 | 7.9778 x10–4 | 0.1159 | 0.9627 |
| 146.75 | 3.4163 x10–5 | 3.4453 x10–8 | 7.9681 x10–4 | 0.1169 | 0.9670 |
| 148.29 | 3.4121 x10–5 | 4.0035 x10–8 | 7.9620 x10–4 | 0.1181 | 0.9717 |
| 149.73 | 3.4047 x10–5 | 3.1942 x10–8 | 7.9511 x10–4 | 0.1191 | 0.9758 |
| 151.30 | 3.3991 x10–5 | 4.1056 x10–9 | 7.9429 x10–4 | 0.1202 | 0.9804 |
| 152.69 | 3.3956 x10–5 | 1.9599 x10–8 | 7.9378 x10–4 | 0.1212 | 0.9845 |
| 154.29 | 3.3911 x10–5 | 9.6158 x10–9 | 7.9312 x10–4 | 0.1224 | 0.9893 |
| 155.74 | 3.3850 x10–5 | 2.7330 x10–8 | 7.9223 x10–4 | 0.1234 | 0.9934 |
| 157.97 | 3.3787 x10–5 | 1.9797 x10–8 | 7.9130 x10–4 | 0.1250 | 0.9999 |
| 159.17 | 3.3782 x10–5 | 7.1308 x10–9 | 7.9123 x10–4 | 0.1259 | 1.0036 |
| 160.41 | 3.3754 x10–5 | 2.1315 x10–8 | 7.9082 x10–4 | 0.1269 | 1.0072 |
| 161.71 | 3.3730 x10–5 | 1.0112 x10–8 | 7.9047 x10–4 | 0.1278 | 1.0111 |
| 163.21 | 3.3708 x10–5 | 3.7028 x10–8 | 7.9015 x10–4 | 0.1290 | 1.0156 |
| 164.70 | 3.3676 x10–5 | 3.6400 x10–9 | 7.8968 x10–4 | 0.1301 | 1.0199 |
| 166.23 | 3.3650 x10–5 | 6.5083 x10–10 | 7.8930 x10–4 | 0.1312 | 1.0244 |
| 167.68 | 3.3612 x10–5 | 2.6015 x10–8 | 7.8874 x10–4 | 0.1323 | 1.0285 |
| 169.21 | 3.3565 x10–5 | 1.3330 x10–8 | 7.8805 x10–4 | 0.1333 | 1.0327 |
| 170.68 | 3.3543 x10–5 | 2.1498 x10–8 | 7.8773 x10–4 | 0.1344 | 1.0370 |
| 172.18 | 3.3522 x10–5 | 1.1998 x10–8 | 7.8742 x10–4 | 0.1356 | 1.0413 |
| 173.70 | 3.3476 x10–5 | 1.6798 x10–8 | 7.8675 x10–4 | 0.1367 | 1.0454 |
| 175.15 | 3.3432 x10–5 | 9.2273 x10–9 | 7.8610 x10–4 | 0.1377 | 1.0494 |
| 176.63 | 3.3412 x10–5 | 1.4997 x10–9 | 7.8581 x10–4 | 0.1388 | 1.0536 |
| 178.84 | 3.3376 x10–5 | 2.0971 x10–8 | 7.8528 x10–4 | 0.1404 | 1.0598 |
| 179.99 | 3.3374 x10–5 | 1.1638 x10–8 | 7.8525 x10–4 | 0.1413 | 1.0632 |
| 181.19 | 3.3408 x10–5 | 1.7845 x10–8 | 7.8575 x10–4 | 0.1424 | 1.0671 |
| 182.64 | 3.3383 x10–5 | 1.6026 x10–9 | 7.8538 x10–4 | 0.1434 | 1.0711 |
| 184.19 | 3.3369 x10–5 | 7.1359 x10–9 | 7.8518 x10–4 | 0.1446 | 1.0755 |
| 185.64 | 3.3384 x10–5 | 4.9597 x10–9 | 7.8540 x10–4 | 0.1458 | 1.0798 |
| 187.19 | 3.3397 x10–5 | 5.7906 x10–9 | 7.8559 x10–4 | 0.1471 | 1.0845 |
| 188.62 | 3.3380 x10–5 | 1.0521 x10–8 | 7.8534 x10–4 | 0.1481 | 1.0884 |
| 190.14 | 3.3396 x10–5 | 1.6379 x10–8 | 7.8558 x10–4 | 0.1494 | 1.0930 |
| 191.63 | 3.3422 x10–5 | 8.1855 x10–9 | 7.8596 x10–4 | 0.1506 | 1.0975 |
| 193.15 | 3.3439 x10–5 | 3.3339 x10–9 | 7.8621 x10–4 | 0.1519 | 1.1020 |
| 194.58 | 3.3445 x10–5 | 6.3797 x10–9 | 7.8629 x10–4 | 0.1530 | 1.1062 |
| 196.17 | 3.3477 x10–5 | 1.8563 x10–8 | 7.8676 x10–4 | 0.1543 | 1.1110 |
| 197.59 | 3.3529 x10–5 | 4.4992 x10–9 | 7.8752 x10–4 | 0.1556 | 1.1156 |
| 199.73 | 3.3597 x10–5 | 1.9612 x10–8 | 7.8852 x10–4 | 0.1575 | 1.1223 |
| 200.01 | 3.3671 x10–5 | 6.2613 x10–9 | 7.8960 x10–4 | 0.1579 | 1.1239 |
| 199.92 | 3.3697 x10–5 | 6.2870 x10–9 | 7.8998 x10–4 | 0.1579 | 1.1239 |
| 201.15 | 3.3793 x10–5 | 2.8461 x10–8 | 7.9139 x10–4 | 0.1592 | 1.1283 |
| 202.14 | 3.3855 x10–5 | 1.6968 x10–8 | 7.9230 x10–4 | 0.1602 | 1.1317 |
| 203.13 | 3.3925 x10–5 | 1.7215 x10–8 | 7.9333 x10–4 | 0.1611 | 1.1353 |
| 204.13 | 3.4019 x10–5 | 1.5273 x10–8 | 7.9470 x10–4 | 0.1622 | 1.1390 |
| 205.20 | 3.4078 x10–5 | 1.9502 x10–8 | 7.9557 x10–4 | 0.1633 | 1.1426 |
| 206.12 | 3.4158 x10–5 | 7.1025 x10–9 | 7.9674 x10–4 | 0.1642 | 1.1460 |
| 207.13 | 3.4234 x10–5 | 2.6470 x10–9 | 7.9785 x10–4 | 0.1653 | 1.1496 |
| 208.13 | 3.4326 x10–5 | 1.2196 x10–8 | 7.9920 x10–4 | 0.1663 | 1.1534 |
| 209.13 | 3.4423 x10–5 | 5.3764 x10–9 | 8.0062 x10–4 | 0.1674 | 1.1572 |
| 210.20 | 3.4533 x10–5 | 4.9134 x10–9 | 8.0223 x10–4 | 0.1686 | 1.1613 |
| 211.13 | 3.4668 x10–5 | 1.0624 x10–9 | 8.0421 x10–4 | 0.1698 | 1.1653 |
| 212.13 | 3.4780 x10–5 | 2.3648 x10–8 | 8.0585 x10–4 | 0.1709 | 1.1693 |
| 213.13 | 3.4925 x10–5 | 1.9504 x10–8 | 8.0798 x10–4 | 0.1722 | 1.1735 |
| 214.13 | 3.5041 x10–5 | 7.5836 x10–9 | 8.0967 x10–4 | 0.1734 | 1.1775 |
| 215.20 | 3.5165 x10–5 | 1.5383 x10–9 | 8.1149 x10–4 | 0.1746 | 1.1818 |
| 216.13 | 3.5357 x10–5 | 3.9513 x10–9 | 8.1430 x10–4 | 0.1760 | 1.1864 |
| 217.13 | 3.5483 x10–5 | 1.3701 x10–8 | 8.1615 x10–4 | 0.1772 | 1.1905 |
| 218.13 | 3.5663 x10–5 | 9.4280 x10–9 | 8.1879 x10–4 | 0.1786 | 1.1952 |
| 219.13 | 3.5860 x10–5 | 2.9707 x10–8 | 8.2167 x10–4 | 0.1801 | 1.2000 |
| 220.20 | 3.6054 x10–5 | 1.8293 x10–8 | 8.2452 x10–4 | 0.1816 | 1.2050 |
| 221.13 | 3.6259 x10–5 | 2.5639 x10–8 | 8.2752 x10–4 | 0.1830 | 1.2097 |
| 222.13 | 3.6498 x10–5 | 2.4101 x10–8 | 8.3102 x10–4 | 0.1846 | 1.2150 |
| 223.12 | 3.6746 x10–5 | 4.7667 x10–9 | 8.3465 x10–4 | 0.1862 | 1.2204 |
| 224.20 | 3.6985 x10–5 | 8.0466 x10–9 | 8.3815 x10–4 | 0.1879 | 1.2259 |
| 225.13 | 3.7267 x10–5 | 8.4325 x10–9 | 8.4229 x10–4 | 0.1896 | 1.2315 |
| 226.13 | 3.7553 x10–5 | 1.8823 x10–8 | 8.4648 x10–4 | 0.1914 | 1.2373 |
| 227.20 | 3.7839 x10–5 | 4.0161 x10–8 | 8.5067 x10–4 | 0.1933 | 1.2433 |
| 228.13 | 3.8169 x10–5 | 9.1450 x10–9 | 8.5550 x10–4 | 0.1952 | 1.2493 |
| 229.14 | 3.8498 x10–5 | 1.3104 x10–8 | 8.6032 x10–4 | 0.1971 | 1.2556 |
| 230.13 | 3.8871 x10–5 | 1.0452 x10–8 | 8.6578 x10–4 | 0.1992 | 1.2623 |
| 231.13 | 3.9266 x10–5 | 2.2900 x10–8 | 8.7157 x10–4 | 0.2014 | 1.2693 |
| 232.13 | 3.9670 x10–5 | 1.9602 x10–8 | 8.7749 x10–4 | 0.2037 | 1.2763 |
| 233.14 | 4.0147 x10–5 | 6.4825 x10–9 | 8.8448 x10–4 | 0.2062 | 1.2842 |
| 234.13 | 4.0607 x10–5 | 1.9144 x10–8 | 8.9122 x10–4 | 0.2087 | 1.2918 |
| 235.13 | 4.1132 x10–5 | 1.6757 x10–8 | 8.9891 x10–4 | 0.2114 | 1.3001 |
| 236.13 | 4.1651 x10–5 | 6.4594 x10–9 | 9.0651 x10–4 | 0.2141 | 1.3084 |
| 237.12 | 4.2210 x10–5 | 4.7976 x10–9 | 9.1470 x10–4 | 0.2169 | 1.3171 |
| 238.13 | 4.2806 x10–5 | 3.6799 x10–8 | 9.2343 x10–4 | 0.2199 | 1.3261 |
| 239.19 | 4.3425 x10–5 | 3.3660 x10–8 | 9.3250 x10–4 | 0.2230 | 1.3356 |
| 240.13 | 4.4113 x10–5 | 2.6941 x10–8 | 9.4258 x10–4 | 0.2263 | 1.3454 |
| 241.13 | 4.4880 x10–5 | 1.4586 x10–8 | 9.5382 x10–4 | 0.2300 | 1.3562 |
| 242.13 | 4.5655 x10–5 | 1.5502 x10–8 | 9.6517 x10–4 | 0.2337 | 1.3671 |
| 243.13 | 4.6522 x10–5 | 1.4380 x10–8 | 9.7787 x10–4 | 0.2378 | 1.3789 |
| 244.12 | 4.7411 x10–5 | 8.5302 x10–9 | 9.9090 x10–4 | 0.2419 | 1.3909 |
| 245.12 | 4.8359 x10–5 | 1.1116 x10–8 | 1.0048 x10–3 | 0.2463 | 1.4035 |
| 246.13 | 4.9402 x10–5 | 2.1320 x10–8 | 1.0201 x10–3 | 0.2511 | 1.4170 |
| 247.13 | 5.0514 x10–5 | 1.5352 x10–8 | 1.0364 x10–3 | 0.2561 | 1.4312 |
| 248.13 | 5.1753 x10–5 | 4.2602 x10–8 | 1.0545 x10–3 | 0.2617 | 1.4466 |
| 249.14 | 5.3124 x10–5 | 2.4847 x10–8 | 1.0746 x10–3 | 0.2677 | 1.4633 |
| 250.13 | 5.4610 x10–5 | 2.1238 x10–8 | 1.0964 x10–3 | 0.2742 | 1.4809 |
| 251.13 | 5.6241 x10–5 | 3.0465 x10–8 | 1.1203 x10–3 | 0.2813 | 1.5000 |
| 252.13 | 5.8073 x10–5 | 3.7102 x10–8 | 1.1471 x10–3 | 0.2892 | 1.5209 |
| 253.13 | 6.0183 x10–5 | 2.1076 x10–8 | 1.1780 x10–3 | 0.2982 | 1.5443 |
| 254.12 | 6.2634 x10–5 | 3.6009 x10–8 | 1.2139 x10–3 | 0.3085 | 1.5707 |
| 255.13 | 6.5589 x10–5 | 3.1687 x10–8 | 1.2572 x10–3 | 0.3208 | 1.6016 |
| 256.12 | 6.9452 x10–5 | 4.6654 x10–8 | 1.3138 x10–3 | 0.3365 | 1.6405 |
| 257.12 | 7.4980 x10–5 | 1.5567 x10–7 | 1.3948 x10–3 | 0.3586 | 1.6936 |
| 258.12 | 8.5395 x10–5 | 2.9793 x10–7 | 1.5474 x10–3 | 0.3994 | 1.7873 |
| 259.12 | 1.2657 x10–4 | 2.7200 x10–6 | 2.1506 x10–3 | 0.5573 | 2.1111 |
| 260.11 | 3.1930 x10–4 | 1.0225 x10–5 | 4.9741 x10–3 | 1.2938 | 3.2167 |
| 261.12 | 6.2223 x10–4 | 2.8013 x10–5 | 9.4121 x10–3 | 2.4577 | 4.4334 |
| 262.13 | 8.4592 x10–4 | 7.0922 x10–6 | 0.0127 | 3.3262 | 5.1577 |
| 263.13 | 9.1980 x10–4 | 1.8069 x10–8 | 0.0138 | 3.6237 | 5.3834 |
| 264.14 | 9.1709 x10–4 | 1.3385 x10–7 | 0.0137 | 3.6271 | 5.3859 |
| 265.13 | 9.1507 x10–4 | 3.2228 x10–8 | 0.0137 | 3.6329 | 5.3902 |
| 266.12 | 9.1289 x10–4 | 4.4287 x10–8 | 0.0137 | 3.6379 | 5.3939 |
| 267.12 | 9.1050 x10–4 | 1.0405 x10–7 | 0.0136 | 3.6422 | 5.3971 |
| 268.13 | 9.0828 x10–4 | 5.6264 x10–8 | 0.0136 | 3.6473 | 5.4009 |
| 269.13 | 9.0615 x10–4 | 1.5756 x10–7 | 0.0136 | 3.6525 | 5.4047 |
| 270.12 | 9.0367 x10–4 | 1.9588 x10–7 | 0.0135 | 3.6561 | 5.4074 |
| 271.13 | 9.0132 x10–4 | 5.2437 x10–8 | 0.0135 | 3.6605 | 5.4106 |
| 272.13 | 8.9914 x10–4 | 3.8278 x10–8 | 0.0135 | 3.6653 | 5.4142 |
| 273.13 | 8.9675 x10–4 | 1.2570 x10–7 | 0.0134 | 3.6692 | 5.4171 |
| 274.13 | 8.9407 x10–4 | 2.4901 x10–8 | 0.0134 | 3.6718 | 5.4190 |
| 275.13 | 8.9181 x10–4 | 2.5819 x10–7 | 0.0134 | 3.6761 | 5.4222 |
| 276.13 | 8.8918 x10–4 | 1.6846 x10–7 | 0.0133 | 3.6789 | 5.4242 |
| 277.13 | 8.8653 x10–4 | 2.6095 x10–7 | 0.0133 | 3.6814 | 5.4261 |
| 278.13 | 8.8417 x10–4 | 1.6925 x10–7 | 0.0132 | 3.6851 | 5.4288 |
| 279.13 | 8.8173 x10–4 | 7.8573 x10–8 | 0.0132 | 3.6884 | 5.4312 |
| 280.13 | 8.7954 x10–4 | 1.4200 x10–8 | 0.0132 | 3.6926 | 5.4343 |
| 279.90 | 8.8000 x10–4 | 1.7353 x10–7 | 0.0132 | 3.6914 | 5.4335 |
| 282.11 | 8.7749 x10–4 | 4.2661 x10–7 | 0.0132 | 3.7102 | 5.4473 |
| 283.68 | 8.7465 x10–4 | 8.1322 x10–7 | 0.0131 | 3.7191 | 5.4538 |
| 285.29 | 8.7097 x10–4 | 8.0388 x10–7 | 0.0131 | 3.7248 | 5.4580 |
| 286.79 | 8.6773 x10–4 | 1.1443 x10–6 | 0.0130 | 3.7308 | 5.4623 |
| 288.34 | 8.6380 x10–4 | 1.4703 x10–6 | 0.0130 | 3.7343 | 5.4649 |
| 289.81 | 8.6018 x10–4 | 1.4225 x10–6 | 0.0129 | 3.7380 | 5.4676 |
| 291.36 | 8.5621 x10–4 | 1.1844 x10–6 | 0.0128 | 3.7410 | 5.4698 |
| 292.82 | 8.5230 x10–4 | 1.0755 x10–6 | 0.0128 | 3.7430 | 5.4713 |
| 294.32 | 8.4823 x10–4 | 1.0791 x10–6 | 0.0127 | 3.7446 | 5.4725 |
| 295.81 | 8.4451 x10–4 | 1.2267 x10–6 | 0.0127 | 3.7475 | 5.4745 |
| 297.30 | 8.4005 x10–4 | 1.2013 x10–6 | 0.0126 | 3.7469 | 5.4741 |
| 298.81 | 8.3641 x10–4 | 1.0303 x10–6 | 0.0125 | 3.7500 | 5.4764 |
| 300.33 | 8.3237 x10–4 | 1.0887 x10–6 | 0.0125 | 3.7513 | 5.4774 |
| 302.55 | 8.2658 x10–4 | 1.1480 x10–6 | 0.0124 | 3.7534 | 5.4789 |
| 303.74 | 8.2376 x10–4 | 9.1126 x10–7 | 0.0124 | 3.7556 | 5.4805 |
| 304.97 | 8.2074 x10–4 | 8.0367 x10–7 | 0.0123 | 3.7573 | 5.4817 |
| 306.41 | 8.1705 x10–4 | 1.0783 x10–6 | 0.0123 | 3.7585 | 5.4826 |
| 307.91 | 8.1328 x10–4 | 9.7827 x10–7 | 0.0122 | 3.7599 | 5.4836 |
| 309.40 | 8.0948 x10–4 | 1.1233 x10–6 | 0.0122 | 3.7608 | 5.4843 |
| 310.92 | 8.0575 x10–4 | 9.1254 x10–7 | 0.0121 | 3.7623 | 5.4854 |
| 312.42 | 8.0221 x10–4 | 1.0170 x10–6 | 0.0120 | 3.7643 | 5.4868 |
| 313.98 | 7.9835 x10–4 | 8.3129 x10–7 | 0.0120 | 3.7653 | 5.4876 |
| 315.51 | 7.9481 x10–4 | 8.6957 x10–7 | 0.0119 | 3.7673 | 5.4890 |
| 317.01 | 7.9113 x10–4 | 9.1554 x10–7 | 0.0119 | 3.7681 | 5.4896 |
| 318.48 | 7.8772 x10–4 | 8.6335 x10–7 | 0.0118 | 3.7697 | 5.4908 |
| 320.06 | 7.8376 x10–4 | 8.2919 x10–7 | 0.0118 | 3.7698 | 5.4909 |
| 321.53 | 7.8055 x10–4 | 9.5991 x10–7 | 0.0117 | 3.7720 | 5.4925 |
| 323.76 | 7.7528 x10–4 | 1.0346 x10–6 | 0.0117 | 3.7732 | 5.4933 |
| 324.95 | 7.7246 x10–4 | 8.8611 x10–7 | 0.0116 | 3.7736 | 5.4936 |
| 326.14 | 7.6982 x10–4 | 8.5895 x10–7 | 0.0116 | 3.7748 | 5.4945 |
| 327.62 | 7.6635 x10–4 | 9.0044 x10–7 | 0.0115 | 3.7753 | 5.4948 |
| 329.13 | 7.6285 x10–4 | 1.0226 x10–6 | 0.0115 | 3.7758 | 5.4952 |
| 330.02 | 7.5444 x10–4 | 1.6669 x10–8 | 0.0113 | 3.7454 | 5.4730 |

Applied field: 1000 G.

Mass of sample used: 44.5 mg.

Diamagnetic correction applied (Pascal’s constants): 296.3 x10 cm3.mol–1.