Electronic Supplementary Information

Table D1. The crystallographically derived Mn and I site occupancies in

[Mn2(-dppO2)4I2]I2.CH3COCH3.4CH3OH, 4, compared to those calculated for using 56% a, 14% b and 30% c . See Scheme below for defenition of a, b and c.

|  | # Calculated site occupancies | Actual site occupancies obtained from Least-Squares refinement |
| --- | --- | --- |
| # Central I | 0.44 | 0.443(1) |
| Inner Mn | 0.37 | 0.375(3) |
| Outer Mn | 0.63 | 0.625(3) |
| Outer I | 0.63 | 0.624(2) |
| Calixarene I | 0.15 | 0.126(2) |

### Sample preparation

[Mn2(-dppO2)4Cl2]Cl2.CH3COCH3.4CH3OH. (2)  MnCl2 (1 equiv) and dppO2.H2O (2 equiv) were  stirred together in acetone/methanol (1:1 for several hours, following which the solid was filtered off under suction, washed with diethyl ether and dried in vacuo.  Yield: 80%; Mpt: 177-178C; Elemental analysis calculated for C108H104P8O8Mn2Cl4.2H2O: C 61.7, H 5.3, P 11.7; found: C 61.5, H 5.2, P 11.5.

[Mn2(-dppO2)4Br2]Br2.CH3COCH3.2CH3OH. (3) The same experimental technique was employed as in the synthesis of 2.  Yield: 58%; Mpt: 164-166C; Elemental analysis calculated for C108H104P8O8Mn2Br4.2H2O: C 56.9 H 5.0 Br 14.0; found: C 57.1, H 5.0, Br 17.9. Crystals of 2 and 3 suitable for X-ray structural analysis, were grown by the vapor diffusion of diethyl ether onto an acetone/methanol (1:1) solution of the synthesized complex.

[Mn2(-dppO2)4I2]I2.CH3COCH3.4CH3OH. (4) MnI2 (1 equiv) was stirred with dppO2.H20 (2 equiv) in diethyl ether for several days.  Elemental analysis based on C108H104P8O8Mn2I4.2H2O; C 52.6, H 4.6, I 20.6; found: C 52.1 H 4.6 I 20.9.  Crystals of 4 were grown from the liquid diffusion of diethyl ether onto acetone/methanol (1:1).

TGA measurements were carried out by means of a CAHN TG-131. Exhaust gases from this instrument were fed to an enclosed powder sample in a Scintag XDS2000 powder diffractometer, employing copper radiation ( = 1.5418 Å) for simultaneous TGA/XRD analysis.

### Crystallography

† Crystal structure analysis for 2 : Nonius MACH-3 diffractometer, graphite monochromated Mok,  = 0.71073 Å, 223 K. Data collection and refinement: -2, corrections for Lorentz and polarization effects and absorption using -scans ( = 5.14  cm-1). The structure was solved using Direct methods and refined by full-matrix least-squares SHELXS, SHELXL, SHELXS97. C115H126O13P8Mn2Cl4 , tetragonal, space group I4/m, a = b = 14.382(3), c = 26.076(9) Å, V = 5393(2) Å3 , Z = 2 , calc = 1.366 g cm-1 , 0  2  50o, crystal dimensions   0.20  0.20   0.15 mm3. 2645 reflections measured, 2441 unique (Rint = 0.053). Hydrogen atoms of disordered acetone (4/m site) and methanol molecules (mirror plane) were ignored. Each manganese atom was divided equally between  two sites , Mn(1) and Mn(2) and  the external capping chlorine site, Cl(2A), was also semi-populated. Refinement  of 180 variables with anisotropic parameters for all non-hydrogen atoms  resulted in wR2 = 0.152 for all reflections and R1 = 0.070 for 1321 reflections [I>2(I)]  , S = 1.07.

- Crystal structure analysis for 3 : Nonius MACH-3 diffractometer, graphite monochromated Mok,  = 0.71073 Å, 223 K. Data collection and refinement: -2, corrections for Lorentz and polarization effects and absorption using -scans ( = 18.74 cm-1). The structure was solved using Direct methods and refined by full-matrix least-squares SHELXS, SHELXL, SHELXS97. C115H126O13P8Mn2Br4 , tetragonal, space group I4/m, a = b = 14.523(4), c = 25.874(12) Å, V = 5457(3) Å3 , Z = 2 , calc = 1.458 g cm-1 , 0  2  50o, crystal dimensions   0.30  0.30   0.20 mm3. 2750 reflections measured, 2750 unique. Hydrogen atoms of disordered acetone (4/m site) and methanol molecules (mirror plane) were ignored. Each manganese atom was divided equally between  two sites , Mn(1) and Mn(2) and  the external capping bromine  site, Br(2A), was also semi-populated. Refinement  of 180 variables with anisotropic parameters for all non-hydrogen atoms  resulted in wR2 = 0.158 for all reflections and R1 = 0.073 for 1500 reflections [I>2(I)]  , S = 1.03.

Crystal structure analysis for 4 : Bruker SMART 2000 diffractometer, graphite monochromated Mok,  = 0.71073 Å, 223 K. Data collection and refinement: narrow range data sets, corrections for Lorentz and polarization effects and absorption using empirical ellipsoidal method (14.55cm-1). The structure was solved using Direct methods and refined by full-matrix least-squares SHELXS, SHELXL, SHELXS97. C115H126O13P8Mn2I4 , tetragonal, space group I4/m, a = b = 14.984(4), c = 25.761(12) Å, V = 5784(3) Å3 , Z = 2 , calc = 1.483 g cm-1 , 0  2  61o, crystal dimensions   0.18  0.10   0.05 mm3. 29054 reflections measured, 4499 unique (Rint = 0.079). Hydrogen atoms of disordered acetone (4/m site) and methanol molecules (mirror plane) were ignored. Refinement of 179 variables with anisotropic parameters for all non-hydrogen atoms  resulted in wR2 = 0.100 for all reflections and R1 = 0.041 for  2103  reflections [I>2(I)]  , S = 0.84. Crystal drawing were prepared using WebLab Viewer. Crystallographic data (excluding structure

X

a Footnote text.

Table XX Caption

X

a Footnote text.

| X | (X) |
| --- | --- |