###### A Novel Synthesis Route to Rare Earth Polyborates

(Supplementary Materials)

Peichao Lu, Yingxia Wang and Jianhua Lin*

State Key Laboratory for Rare Earth Materials Chemistry and Applications, College of Chemistry and Molecular Engineering, Peking University, Beijing 100871, P. R. China

Liping You

Laboratory of Electron Microscopy, Department of Physics, Peking University, Beijing 100871, P. R. China

# Table of Contents

Part 1 Supplementary materials for H3GdB6O12

Table 1-1 Crystallographic data of H3GdB6O12

Table 1-2 Atomic coordinates of H3GdB6O12

Table 1-3 Selected bond lengths and angles in H3GdB6O12

Figure 1-1 Profile fit of the x-ray diffraction pattern for H3GdB6O12

Figure 1-2 TGA and DTA curves of H3GdB6O12

Figure 1-3  A projection of the crystal structure of H3GdB6O12 (1) on [100] direction; the open small circles represent BO4 and dark small circles represent BO3 groups; the large circles are the rare earth atoms; the oxygen atoms are not shown in the figure for clarity.

Figure 1-4 IR spectrum of H3GdB6O12 and GdB5O9

Part 2 Supplementary materials for GdB5O9

Table 2-1 crystallographic data of GdB5O9

Table 2-2 Atomic coordinates of GdB5O9

Table 2-3 Selected bond lengths and angles in GdB5O9

Figure 2-1 Profile fit of the x-ray diffraction pattern for GdB5O9 (there are some very weak reflection peaks (less than 2% of the main phase), which may originate from another phase in the decomposition product).

## Part 1 Supplementary materials for H3GdB6O12

Table 1-1 Crystallographic data of H3GdB6O12

| Molecular formula | H3GdB6O12 |
| --- | --- |
| Formula weight | 417.10 |
| Crystal system | Rhombohedral |
| Space group | R3c (No.161) |
| Unit cell dimension | a = 8.4076(2) Å, c = 20.7427(5)Å, V = 1269.81(5) Å3 |
| Z | 6 |
| Density (calculated) | 3.272 g/cm3 |
| X-ray diffraction | Rigaku D/max-2000 Scan range/speed: 12-120o, 0.3o/min |
| Structure solution | Direct method, Sirpow92 |
| Structure refinement | GSAS, Rietveld refinement |
| Residual value | Rp = 0.089, Rwp = 0.115 |

Table 1-2 Refined atomic coordinates in H3GdB6O12

| Atom | site | Atomic coordinates |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | x | y | z | Ui/Ue |
| Gd1 | 6a | 0 | 0 | 1/2 | 79(2) |
| O1 | 18b | 0.244(1) | 0.098(1) | 0.4254(4) | 168(9) |
| O2 | 18b | 0.137(1) | -0.201(1) | 0.3621(3) | 168(9) |
| O3 | 18b | 0.497(1) | 0.386(1) | 0.4150(5) | 168(9) |
| O4 | 18b | 0.011(1) | 0.605(1) | 0.1492(4) | 168(9) |
| B1 | 18b | 0.032(2) | 0.270(2) | 0.3674(7) | 74(28) |
| B2 | 18b | 0.068(2) | 0.690(2) | 0.0748(7) | 74(28) |

Table 1-3 Selected bond length and angles in H3GdB6O12

Vector            Length          Optr Cell        Neighbor atom coordinates

GD1_O1          2.362(7)           1 0 0 0      .24350    .09814    .42540

GD1_O1          2.362(7)           2 0 0 0     -.09814    .14535    .42540

GD1_O1          2.362(7)           3 0 0 0     -.14535   -.24350    .42540

GD1_O3          2.394(9)         104 0-1-1      .22241    .05304    .58164

GD1_O3          2.394(9)         105 0 0-1     -.05304    .16937    .58164

GD1_O3          2.394(9)         106-1-1-1     -.16937   -.22241    .58164

GD1_O4          2.518(8)         201-1-1 0     -.32219   -.06120    .48251

GD1_O4          2.518(8)         202 0 0 0      .06120   -.26099    .48251

GD1_O4          2.518(8)         203-1 0 0      .26099    .32219    .48251

B1_O1          1.611(14)          2 0 0 0     -.09814    .14535    .42540

*     B1_O2          1.247(14)          2 0 0 0      .20160    .33889    .36212

B1_O4          1.389(16)        104-1-1-1     -.07234    .27214    .31584

B2_O1          1.309(14)        102 0 0-1      .23519    .81202    .09207

B2_O2          1.513(14)        103 0 0-1     -.00556    .52937    .02879

B2_O3          1.529(16)        102 0 0-1     -.05304    .77759    .08164

B2_O4          1.666(15)          1 0 0 0      .01114    .60547    .14917

Angle             Degrees         atom 1 loc  atom 3 loc

O1_B1_O2           127.9(13)          2 0 0 0     2 0 0 0

O1_B1_O4           110.9(18)          2 0 0 0   104-1-1-1

O2_B1_O4           120.6(32)          2 0 0 0   104-1-1-1

O1_B2_O2           132.1(11)        102 0 0-1   103 0 0-1

O1_B2_O3           108.2(12)        102 0 0-1   102 0 0-1

O2_B2_O3           114.5(11)        103 0 0-1   102 0 0-1

* We have not yet applied geometric constrained to rationalize the B-O bond distances and angles.

Figure 1-1

Figure 1-2

Figure 1-3

Figure 1-4

### Part 2 Supplementary materials for GdB5O9

Table 2-1. Crystallographic data of GdB5O9

| Molecular formula | GdB5O9 |
| --- | --- |
| Formula weight | 355.30 |
| Crystal system | Tetragonal |
| Space group | I41/acd (No.142) |
| Unit cell dimension | a = 8.2380(1) Å, c = 33.6372(6) Å, V = 2282.80(6) Å3 |
| Z | 16 |
| Density (calculated) | 4.123 g/cm3 |
| X-ray diffraction | Rigaku D/max-2000 Scan range/speed: 10-120o, 0.5o/min |
| Structure solution | Direct method, Sirpow92 |
| Structure refinement | GSAS, Rietveld refinement |
| Residual value | Rp = 0.069, Rwp = 0.098 |

Table 2-2 Refined atomic coordinates of GdB5O9

Name         X           Y             Z                               Ui/Ue*

GD1       .0000000(0)   .2500000(0)   .068839(27)   2(001)  GD    1 1.000(0)

O1       -.5248(15)     .4509(25)     .0484(4)        1     O     2 1.000(0)

O2        .5000000(0)   .2500000(0)  -.00027(25)    2(001)  O     3 1.000(0)

O3       -.2982(24)     .2817(15)     .05214(34)      1     O     4 1.000(0)

O4       -.1227(8)      .3727(8)      .1250000(0)   2(+-0)  O     5 1.000(0)

O5        .2500000(0)   .4201(15)     .0000000(0)   2(010)  O     6 1.000(0)

O6        .1663(11)     .4876(9)      .09218(24)      1     O    10 1.000(0)

B1       -.2290(21)     .4790(21)     .1250000(0)   2(+-0)  B     7 1.000(0)

B2       -.6328(29)     .3389(28)     .0211(5)        1     B     8 1.000(0)

B3       -.3891(27)     .4001(23)     .0659(7)        1     B     9 1.000(0)

Table 2-3 Selected bond length and angles in GdB5O9

Vector         Length           Optr Cell        Neighbor atom coordinates

GD1_O1          2.566(19)          7 0 1 0     -.02481    .54911    .04840

GD1_O1          2.566(19)        105-1-1-1      .02481   -.04911    .04840

GD1_O2          2.307(9)          -7 1 0 0      .00000    .25000    .00027

GD1_O3          2.533(19)          1 0 0 0     -.29816    .28165    .05214

GD1_O3          2.533(19)        103-1 0-1      .29816    .21835    .05214

GD1_O4          2.369(6)           1 0 0 0     -.12268    .37268    .12500

GD1_O4          2.369(6)          -6 0 1 1      .12268    .12732    .12500

GD1_B3          3.025(21)          7 0 1 0      .11091    .59990    .06591

GD1_B3          3.025(21)        105-1-1-1     -.11091   -.09990    .06591

GD1_O6          2.515(8)           1 0 0 0      .16625    .48760    .09218

GD1_O6          2.515(8)         103-1 0-1     -.16625    .01240    .09218

Vector         Length           Optr Cell        Neighbor atom coordinates

B1_O4          1.239(24)          1 0 0 0     -.12268    .37268    .12500

B1_O6          1.428(14)          7-1 1 0     -.33375    .51240    .09218

B1_O6          1.428(14)       -102-1 1 0     -.26240    .58375    .15782

Angle             Degrees         atom 1 loc  atom 3 loc

O4_B1_O6           124.3(9)           1 0 0 0     7-1 1 0

O4_B1_O6           124.3(9)           1 0 0 0  -102-1 1 0

O6_B1_O6           111.4(18)          7-1 1 0  -102-1 1 0

Vector         Length           Optr Cell        Neighbor atom coordinates

B2_O1          1.577(23)          1 0 0 0     -.52481    .45089    .04840

B2_O2          1.499(17)          1-1 0 0     -.50000    .25000   -.00027

B2_O3          1.550(23)        103-2 0-1     -.70184    .21835    .05214

B2_O5          1.372(18)          1-1 0 0     -.75000    .42012    .00000

Angle             Degrees         atom 1 loc  atom 3 loc

O1_B2_O2            98.8(15)          1 0 0 0     1-1 0 0

O1_B2_O3           100.9(12)          1 0 0 0   103-2 0-1

O1_B2_O5           114.4(17)          1 0 0 0     1-1 0 0

O2_B2_O3           106.1(13)          1-1 0 0   103-2 0-1

O2_B2_O5           120.3(13)          1-1 0 0     1-1 0 0

O3_B2_O5           113.7(18)        103-2 0-1     1-1 0 0

Vector         Length           Optr Cell        Neighbor atom coordinates

B3_O1          1.331(25)          1 0 0 0     -.52481    .45089    .04840

B3_O3          1.314(25)          1 0 0 0     -.29816    .28165    .05214

B3_O6          1.358(19)          7-1 1 0     -.33375    .51240    .09218

Angle             Degrees         atom 1 loc  atom 3 loc

O1_B3_O3           123.8(19)          1 0 0 0     1 0 0 0

O1_B3_O6           110.8(19)          1 0 0 0     7-1 1 0

O3_B3_O6           122.9(21)          1 0 0 0     7-1 1 0

Figure 2-1