Supporting material 1. 1H-NMR of PLGA-g-PEG in CDCl3

13C-NMR (75 MHz) spectra of 25 wt% PLGA-g-PEG copolymer in D2O as a function of temperature.  The zoomed spectra around  73 are shown to the left.  The sample was equilibrated for 15 minutes at each temperature before measurement.  20 oC (sol phase), 33 oC (just above sol-to-gel transition), 40 oC (gel phase), and 50 oC (syneresis) are the various measured temperatures.   13C-NMR spectrum in CDCl3 at room temperature is also shown as a reference.