Electronic Supplementary Information

New, Efficient, Electroluminescent Materials Based on Organometallic Ir Complexes

Vladimir V. Grushin, Norman Herron, Daniel D. LeCloux, William J. Marshall, Viacheslav A. Petrov, and Ying Wang

Central Research and Development, E. I. DuPont de Nemours and Co., Inc., Experimental Station, Wilmington, DE 19880-0328

I. X-Ray Crystal Structure Analysis of 2g.

2g: tris-(2-(5-trifluoromethylpyridyl),4-trifluoromethylphenyl)iridium

CRYSTAL DATA: C40 H20 Cl F18 Ir N3, from dichloroethane, gold, prism, ~0.22 x 0.16 x 0.15mm, cubic , Pa-3 , a = 25.010(3) Å, b = 25.010(3) Å, c = 25.010(3) Å, alpha = 90.000(10) °, beta = 90.000(10) °, gamma = 90.000(10) °, Vol = 15644(3) Å3, Z = 16, T = -100.°C, Formula weight = 1112.24, Density = 1.889 g cm-3, µ(Mo) = 3.60mm-1.

DATA COLLECTION: Bruker SMART 1K CCD system, MoKalpha radiation, standard focus tube , anode power = 50kV x 40mA, crystal to plate distance = 5.0cm, 512 x 512 pixels/frame, multirun data aquisition, total scans = 9, total frames = 6170, oscillation/frame = -0.30°, exposure/frame = 10.0 sec/frame, maximum detector swing angle = -42.0°, beam center = (254.75,252.00), in plane spot width = 1.49, omega half width = 0.39, SAINT integration, 8592, hkl min/max = ( -33, 33, -33, 33, -32, 33), data collected = 244961, unique data = 6485, two-theta range = 2.82 to 56.50°, completeness to two-theta 56.50 = 100.00%, R(int) = 0.0753, SADABS correction applied.

SOLUTION AND REFINEMENT: Structure solved using XS(Shelxtl), refined using shelxtl software package, refinement by full-matrix least squares on F 2, scattering factors from Int. Tab. Vol C Tables 4.2.6.8 and 6.1.1.4, number of data = 6485, number of restraints = 0, number of parameters = 382, data/parameter ratio = 16.98, goodness-of-fit on F2 = 1.12, W = 1/[2(Fo2) + (0.048P)2 + 11.98P] where P = [2Fc2 + Max(Fo2,0)]/3, R indices[I>4sigma(I)] R1 = 0.0356, wR2 = 0.0625, R indices(all data) R1 = 0.0838, wR2 = 0.0870, max difference peak and hole = 1.487 and -1.048 e/Å3. All hydrogen atoms have been idealized as riding hydrogens.

RESULTS: This study determines the structure of tris-(2-(5-trifluoromethylpyridyl), 4-trifluoromethylphenyl)iridium for luminescent materials research.  The asymmetric unit contains two - thirds of the molecule and one disordered dichloroethane solvent molecule as shown in Figure 1 with thermal ellipsoids drawn to the 50% probability level. Both iridium atoms of the asymmetric unit sit on three fold axes as does the disordered solvent molecule. The solvent molecule becomes disordered as the carbon atoms are moved off of the three-fold axis. The structure was difficult to solve for two reasons.  First, the data suggested I-centering with the non-icentered reflections being much weaker. Second, space group Pa-3 is a unique case where the axes must be chosen in the correct order to give the proper cyclic permutation of the miller indices. For the drawings all of the labels marked with * are symmetry generated

atoms.  For the tables symmetry generated atoms are identified by:  #1 z,x,y,  #2 y,z,x, #3 -y,z-1/2,-x+1/2,    and #4 -z+1/2,-x,y+1/2. Besides the # notation the last integer in each atom name is the residue number 1, 2

or 3 for the solvent molecule.

Table 1.  Atomic coordinates ( x 10^4) and equivalent isotropic displacement parameters (A^2 x 10^3) for 2g.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

Ir11          913(1)        913(1)        913(1)       19(1)

N11           734(2)       1733(2)       1056(2)       25(1)

F11          1057(2)       3121(2)       2194(2)       74(1)

F21           209(2)       3043(2)       2216(2)       69(1)

C21           622(2)       2023(2)        609(2)       24(1)

F31           707(2)       2417(2)       2524(1)       73(1)

C31           557(2)       2581(2)        648(2)       31(1)

C41           577(2)       2826(2)       1138(2)       35(1)

C51           662(2)       2518(2)       1594(2)       33(1)

C61           748(2)       1976(2)       1535(2)       29(1)

C71           663(3)       2767(3)       2139(2)       48(2)

C111          178(2)        693(2)       1148(2)       24(1)

F111        -1376(2)        302(2)       2345(2)       83(2)

F121        -1411(2)       -314(3)       1780(3)      126(3)

C121          124(2)        582(2)       1700(2)       24(1)

F131        -1746(2)        422(3)       1585(2)      112(2)

C131         -365(2)        428(2)       1924(2)       30(1)

C141         -811(2)        382(2)       1600(2)       33(1)

C151         -769(2)        483(2)       1057(2)       34(1)

C161         -286(2)        640(2)        834(2)       28(1)

C171        -1328(3)        206(3)       1828(3)       56(2)

Ir212         880(1)       -880(1)       4120(1)       20(1)

N212         1731(2)       -866(2)       4186(2)       25(1)

F212         3284(2)      -1768(2)       4571(2)       68(1)

F222         2667(2)      -2191(2)       4159(2)       73(1)

C222         1949(2)       -367(2)       4217(2)       26(1)

F232         3252(2)      -1748(2)       3721(2)       71(1)

C232         2503(2)       -302(2)       4231(2)       34(1)

C242         2833(2)       -748(2)       4213(2)       37(1)

C252         2601(2)      -1255(2)       4185(2)       34(1)

C262         2049(2)      -1296(2)       4180(2)       29(1)

C272         2948(2)      -1740(3)       4157(3)       46(2)

C312           87(2)       -812(2)       3994(2)       25(1)

F312        -1786(3)       -247(4)       3660(5)      215(6)

C322          -70(2)       -770(2)       3447(2)       27(1)

F322        -1677(2)       -738(3)       3036(2)      109(2)

C332         -607(2)       -725(2)       3300(2)       31(1)

F332        -1868(2)      -1030(5)       3761(4)      226(6)

C342        -1000(2)       -727(2)       3686(2)       36(1)

C352         -859(2)       -771(2)       4225(2)       33(1)

C362         -324(2)       -812(2)       4371(2)       30(1)

C372        -1576(3)       -690(4)       3542(3)       57(2)

Cl403        3001(1)       3001(1)       3001(1)       74(1)

C403         2759(13)      2631(15)      2420(11)      86(9)

Cl413        2020(1)       2020(1)       2020(1)       86(1)

C413         2279(16)      2376(18)      2626(12)     107(12)

________________________________________________________________

Table 2.  Bond lengths [A] and angles [deg] for 2g.

_____________________________________________________________

Ir11-C111#1                   2.007(5)

Ir11-C111#2                   2.007(5)

Ir11-C111                     2.007(5)

Ir11-N11#1                    2.130(4)

Ir11-N11                      2.130(4)

Ir11-N11#2                    2.130(4)

N11-C61                       1.342(6)

N11-C21                       1.363(6)

F11-C71                       1.332(8)

F21-C71                       1.343(8)

C21-C31                       1.408(7)

C21-C121#2                    1.462(7)

F31-C71                       1.305(7)

C31-C41                       1.372(7)

C41-C51                       1.392(8)

C51-C61                       1.381(7)

C51-C71                       1.498(8)

C111-C161                     1.407(7)

C111-C121                     1.415(7)

F111-C171                     1.321(8)

F121-C171                     1.322(9)

C121-C131                     1.397(7)

C121-C21#1                    1.462(7)

F131-C171                     1.324(9)

C131-C141                     1.383(7)

C141-C151                     1.386(8)

C141-C171                     1.481(8)

C151-C161                     1.388(7)

Ir212-C312#3                  2.015(5)

Ir212-C312                    2.015(5)

Ir212-C312#4                  2.015(5)

Ir212-N212#4                  2.134(4)

Ir212-N212#3                  2.134(4)

Ir212-N212                    2.134(4)

N212-C262                     1.339(6)

N212-C222                     1.365(6)

F212-C272                     1.334(7)

F222-C272                     1.329(7)

C222-C232                     1.396(7)

C222-C322#4                   1.473(7)

F232-C272                     1.330(8)

C232-C242                     1.389(8)

C242-C252                     1.394(8)

C252-C262                     1.385(7)

C252-C272                     1.492(8)

C312-C362                     1.394(7)

C312-C322                     1.429(7)

F312-C372                     1.260(10)

C322-C332                     1.397(7)

C322-C222#3                   1.473(7)

F322-C372                     1.295(9)

C332-C342                     1.379(8)

F332-C372                     1.248(10)

C342-C352                     1.400(8)

C342-C372                     1.487(8)

C352-C362                     1.390(7)

Cl403-C403#1                  1.83(3)

Cl403-C403#2                  1.83(3)

Cl403-C403                    1.83(3)

C403-C413#1                   0.95(4)

C403-C413#2                   1.02(4)

C403-C403#2                   1.05(5)

C403-C403#1                   1.05(5)

C403-C413                     1.45(3)

Cl413-C413                    1.87(3)

Cl413-C413#2                  1.87(3)

Cl413-C413#1                  1.87(3)

C413-C403#2                   0.95(4)

C413-C403#1                   1.02(4)

C413-C413#2                   1.10(5)

C413-C413#1                   1.10(5)

C111#1-Ir11-C111#2           95.66(19)

C111#1-Ir11-C111             95.65(19)

C111#2-Ir11-C111             95.66(19)

C111#1-Ir11-N11#1            91.26(18)

C111#2-Ir11-N11#1           171.85(18)

C111-Ir11-N11#1              79.33(18)

C111#1-Ir11-N11             171.84(18)

C111#2-Ir11-N11              79.33(18)

C111-Ir11-N11                91.27(18)

N11#1-Ir11-N11               94.27(15)

C111#1-Ir11-N11#2            79.32(18)

C111#2-Ir11-N11#2            91.26(18)

C111-Ir11-N11#2             171.84(18)

N11#1-Ir11-N11#2             94.27(15)

N11-Ir11-N11#2               94.27(15)

C61-N11-C21                 119.7(4)

C61-N11-Ir11                125.6(3)

C21-N11-Ir11                114.7(3)

N11-C21-C31                 119.6(5)

N11-C21-C121#2              113.7(4)

C31-C21-C121#2              126.7(5)

C41-C31-C21                 120.0(5)

C31-C41-C51                 119.4(5)

C61-C51-C41                 118.5(5)

C61-C51-C71                 120.4(5)

C41-C51-C71                 121.0(5)

N11-C61-C51                 122.5(5)

F31-C71-F11                 107.9(6)

F31-C71-F21                 108.1(6)

F11-C71-F21                 105.6(5)

F31-C71-C51                 113.1(5)

F11-C71-C51                 111.9(6)

F21-C71-C51                 110.0(5)

C161-C111-C121              116.6(5)

C161-C111-Ir11              128.1(4)

C121-C111-Ir11              115.3(4)

C131-C121-C111              121.9(5)

C131-C121-C21#1             121.6(5)

C111-C121-C21#1             116.5(4)

C141-C131-C121              119.5(5)

C131-C141-C151              119.9(5)

C131-C141-C171              120.3(5)

C151-C141-C171              119.7(5)

C141-C151-C161              120.7(5)

C151-C161-C111              121.4(5)

F111-C171-F121              104.6(7)

F111-C171-F131              107.7(6)

F121-C171-F131              103.6(6)

F111-C171-C141              113.8(5)

F121-C171-C141              113.2(6)

F131-C171-C141              113.1(6)

C312#3-Ir212-C312            94.81(19)

C312#3-Ir212-C312#4          94.81(19)

C312-Ir212-C312#4            94.81(19)

C312#3-Ir212-N212#4          79.74(19)

C312-Ir212-N212#4            90.58(17)

C312#4-Ir212-N212#4         172.65(18)

C312#3-Ir212-N212#3         172.66(18)

C312-Ir212-N212#3            79.74(18)

C312#4-Ir212-N212#3          90.58(17)

N212#4-Ir212-N212#3          95.30(15)

C312#3-Ir212-N212            90.58(17)

C312-Ir212-N212             172.65(18)

C312#4-Ir212-N212            79.74(18)

N212#4-Ir212-N212            95.30(15)

N212#3-Ir212-N212            95.30(15)

C262-N212-C222              119.8(4)

C262-N212-Ir212             125.4(3)

C222-N212-Ir212             114.7(3)

N212-C222-C232              120.3(5)

N212-C222-C322#4            114.3(4)

C232-C222-C322#4            125.4(5)

C242-C232-C222              119.7(5)

C232-C242-C252              119.1(5)

C262-C252-C242              118.8(5)

C262-C252-C272              121.2(5)

C242-C252-C272              120.0(5)

N212-C262-C252              122.3(5)

F222-C272-F232              106.9(6)

F222-C272-F212              106.6(6)

F232-C272-F212              106.0(5)

F222-C272-C252              112.5(5)

F232-C272-C252              112.5(6)

F212-C272-C252              111.9(5)

C362-C312-C322              116.3(5)

C362-C312-Ir212             128.4(4)

C322-C312-Ir212             115.2(4)

C332-C322-C312              121.5(5)

C332-C322-C222#3            122.5(5)

C312-C322-C222#3            116.0(4)

C342-C332-C322              120.1(5)

C332-C342-C352              119.7(5)

C332-C342-C372              121.4(6)

C352-C342-C372              118.9(5)

C362-C352-C342              120.1(5)

C352-C362-C312              122.3(5)

F332-C372-F312              104.6(9)

F332-C372-F322              104.6(8)

F312-C372-F322              103.2(8)

F332-C372-C342              114.6(7)

F312-C372-C342              113.7(7)

F322-C372-C342              114.8(6)

C403#1-Cl403-C403#2          33.4(15)

C403#1-Cl403-C403            33.4(15)

C403#2-Cl403-C403            33.4(15)

C413#1-C403-C413#2           68(4)

C413#1-C403-C403#2           61(4)

C413#2-C403-C403#2           89(3)

C413#1-C403-C403#1           93(3)

C413#2-C403-C403#1           55(3)

C403#2-C403-C403#1           59.998(11)

C413#1-C403-C413             49(3)

C413#2-C403-C413             49(3)

C403#2-C403-C413             40.6(19)

C403#1-C403-C413             45(2)

C413#1-C403-Cl403           133(4)

C413#2-C403-Cl403           126(3)

C403#2-C403-Cl403            73.3(8)

C403#1-C403-Cl403            73.3(7)

C413-C403-Cl403             102.3(19)

C413-Cl413-C413#2            34.1(17)

C413-Cl413-C413#1            34.1(17)

C413#2-Cl413-C413#1          34.1(17)

C403#2-C413-C403#1           64(4)

C403#2-C413-C413#2           90(3)

C403#1-C413-C413#2           53(3)

C403#2-C413-C413#1           59(4)

C403#1-C413-C413#1           87(3)

C413#2-C413-C413#1           59.996(10)

C403#2-C413-C403             46(3)

C403#1-C413-C403             46(2)

C413#2-C413-C403             44(2)

C413#1-C413-C403             40.7(18)

C403#2-C413-Cl413           131(4)

C403#1-C413-Cl413           125(3)

C413#2-C413-Cl413            73.0(9)

C413#1-C413-Cl413            73.0(9)

C403-C413-Cl413             102(2)

_____________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 z,x,y    #2 y,z,x    #3 -y,z-1/2,-x+1/2    #4 -z+1/2,-x,y+1/2

Table 3.  Anisotropic displacement parameters (A^2 x 10^3) for 2g.  The anisotropic displacement factor exponent takes the form: -2 pi^2 [ h^2 a*^2 U11 + ... + 2 h k a* b* U12 ]

_______________________________________________________________________

U11        U22        U33        U23        U13        U12

_______________________________________________________________________

Ir11     19(1)      19(1)      19(1)       0(1)       0(1)       0(1)

N11      24(2)      26(2)      25(2)      -2(2)      -1(2)       0(2)

F11     107(4)      55(3)      61(3)     -26(2)     -23(3)      -9(3)

F21      89(3)      67(3)      50(2)     -22(2)       0(2)      31(2)

C21      23(2)      28(3)      22(2)       2(2)       1(2)      -3(2)

F31     151(5)      45(2)      23(2)      -3(2)      -9(2)      23(3)

C31      34(3)      27(3)      30(3)       6(2)      -1(2)       0(2)

C41      43(3)      27(3)      35(3)      -3(2)      -3(3)       3(2)

C51      42(3)      30(3)      28(3)      -8(2)      -3(2)       5(2)

C61      36(3)      29(3)      22(3)      -3(2)       0(2)       2(2)

C71      78(5)      34(3)      33(3)      -9(3)      -8(3)       7(3)

C111     20(2)      25(2)      28(3)      -3(2)       1(2)       1(2)

F111     40(2)     157(5)      53(3)     -16(3)      16(2)     -32(3)

F121    115(5)     118(5)     145(6)     -43(4)      66(4)     -79(4)

C121     24(2)      26(3)      23(2)      -1(2)       0(2)       0(2)

F131     25(2)     231(8)      79(3)      25(4)       4(2)      -5(3)

C131     26(3)      35(3)      28(3)      -2(2)       6(2)      -2(2)

C141     26(3)      36(3)      37(3)      -6(2)       5(2)      -6(2)

C151     29(3)      42(3)      33(3)      -1(2)      -9(2)      -2(2)

C161     22(2)      31(3)      31(3)      -4(2)      -4(2)      -2(2)

C171     31(3)      88(6)      47(4)     -11(4)       5(3)     -20(4)

Ir212    20(1)      20(1)      20(1)       0(1)       0(1)       0(1)

N212     23(2)      28(2)      24(2)      -1(2)      -2(2)       0(2)

F212     51(2)      78(3)      74(3)      -4(2)     -22(2)      34(2)

F222     48(2)      39(2)     131(4)      -3(2)     -10(3)      15(2)

C222     28(3)      27(3)      22(2)       4(2)       0(2)      -1(2)

F232     63(3)      81(3)      70(3)      -9(2)      17(2)      31(2)

C232     28(3)      36(3)      37(3)       5(2)      -4(2)      -7(2)

C242     25(3)      51(4)      34(3)       0(3)      -1(2)      -3(2)

C252     30(3)      40(3)      33(3)       1(2)      -1(2)       9(2)

C262     31(3)      30(3)      28(3)       0(2)      -2(2)       7(2)

C272     32(3)      47(4)      60(4)      -6(3)      -6(3)      11(3)

C312     23(2)      21(2)      32(3)      -3(2)      -2(2)      -1(2)

F312     77(4)     241(10)    327(13)   -182(10)   -108(6)     101(6)

C322     25(3)      27(3)      30(3)       0(2)      -3(2)       0(2)

F322     36(2)     207(7)      83(4)      -8(4)     -22(2)       8(3)

C332     27(3)      37(3)      29(3)       1(2)      -4(2)      -2(2)

F332     41(3)     411(16)    226(9)     217(11)    -41(4)     -69(6)

C342     25(3)      36(3)      47(3)       0(3)      -1(2)       0(2)

C352     31(3)      31(3)      38(3)      -3(2)       6(2)       1(2)

C362     29(3)      30(3)      31(3)      -4(2)       2(2)       0(2)

C372     29(3)      87(6)      55(4)       4(4)      -2(3)       5(4)

Cl403    74(1)      74(1)      74(1)     -20(1)     -20(1)     -20(1)

Cl413    86(1)      86(1)      86(1)     -27(1)     -27(1)     -27(1)

_______________________________________________________________________

Table 4.  Hydrogen coordinates ( x 10^4) and isotropic displacement parameters (A^2 x 10^3) for 2g.

________________________________________________________________

x             y             z           U(eq)

________________________________________________________________

H3A1          500          2788           335          37

H4A1          533          3202          1166          42

H6A1          820          1767          1844          35

H13A1        -390           356          2296          36

H15A1       -1075           444           835          41

H16A1        -268           712           462          34

H23A2        2654            46          4253          40

H24A2        3211          -709          4220          44

H26A2        1891         -1641          4171          35

H33A2        -701          -694          2933          37

H35A2       -1129          -773          4493          40

H36A2        -236          -840          4739          36

________________________________________________________________

Table 5.  Torsion angles [deg] for 2g.

________________________________________________________________

C111#1-Ir11-N11-C61                               -130.9(12)

C111#2-Ir11-N11-C61                                176.6(5)

C111-Ir11-N11-C61                                   81.1(4)

N11#1-Ir11-N11-C61                                   1.7(4)

N11#2-Ir11-N11-C61                                 -92.9(3)

C111#1-Ir11-N11-C21                                 46.1(14)

C111#2-Ir11-N11-C21                                 -6.4(3)

C111-Ir11-N11-C21                                 -102.0(4)

N11#1-Ir11-N11-C21                                 178.7(3)

N11#2-Ir11-N11-C21                                  84.0(4)

C61-N11-C21-C31                                      4.3(7)

Ir11-N11-C21-C31                                  -172.9(4)

C61-N11-C21-C121#2                                -175.8(4)

Ir11-N11-C21-C121#2                                  7.0(5)

N11-C21-C31-C41                                     -3.8(8)

C121#2-C21-C31-C41                                 176.4(5)

C21-C31-C41-C51                                      0.1(9)

C31-C41-C51-C61                                      2.9(9)

C31-C41-C51-C71                                   -177.4(6)

C21-N11-C61-C51                                     -1.2(8)

Ir11-N11-C61-C51                                   175.6(4)

C41-C51-C61-N11                                     -2.4(9)

C71-C51-C61-N11                                    177.9(6)

C61-C51-C71-F31                                     -5.4(9)

C41-C51-C71-F31                                    175.0(6)

C61-C51-C71-F11                                    116.7(6)

C41-C51-C71-F11                                    -63.0(8)

C61-C51-C71-F21                                   -126.3(6)

C41-C51-C71-F21                                     54.1(8)

C111#1-Ir11-C111-C161                              -85.7(4)

C111#2-Ir11-C111-C161                               10.6(5)

N11#1-Ir11-C111-C161                              -175.9(5)

N11-Ir11-C111-C161                                  90.0(5)

N11#2-Ir11-C111-C161                              -137.3(11)

C111#1-Ir11-C111-C121                               94.6(5)

C111#2-Ir11-C111-C121                             -169.1(4)

N11#1-Ir11-C111-C121                                 4.4(4)

N11-Ir11-C111-C121                                 -89.7(4)

N11#2-Ir11-C111-C121                                43.0(14)

C161-C111-C121-C131                                 -0.2(7)

Ir11-C111-C121-C131                                179.5(4)

C161-C111-C121-C21#1                               178.2(4)

Ir11-C111-C121-C21#1                                -2.1(6)

C111-C121-C131-C141                                  0.1(8)

C21#1-C121-C131-C141                              -178.2(5)

C121-C131-C141-C151                                  0.6(8)

C121-C131-C141-C171                                178.5(6)

C131-C141-C151-C161                                 -1.1(9)

C171-C141-C151-C161                               -179.0(6)

C141-C151-C161-C111                                  1.0(8)

C121-C111-C161-C151                                 -0.4(8)

Ir11-C111-C161-C151                                180.0(4)

C131-C141-C171-F111                                 24.6(10)

C151-C141-C171-F111                               -157.5(6)

C131-C141-C171-F121                                -94.6(8)

C151-C141-C171-F121                                 83.3(8)

C131-C141-C171-F131                                147.9(6)

C151-C141-C171-F131                                -34.2(9)

C312#3-Ir212-N212-C262                              85.1(4)

C312-Ir212-N212-C262                              -137.6(13)

C312#4-Ir212-N212-C262                             179.9(4)

N212#4-Ir212-N212-C262                               5.4(4)

N212#3-Ir212-N212-C262                             -90.5(3)

C312#3-Ir212-N212-C222                             -97.4(4)

C312-Ir212-N212-C222                                39.9(15)

C312#4-Ir212-N212-C222                              -2.6(3)

N212#4-Ir212-N212-C222                            -177.1(3)

N212#3-Ir212-N212-C222                              87.1(4)

C262-N212-C222-C232                                  1.3(7)

Ir212-N212-C222-C232                              -176.4(4)

C262-N212-C222-C322#4                             -178.9(4)

Ir212-N212-C222-C322#4                               3.4(5)

N212-C222-C232-C242                                  0.1(8)

C322#4-C222-C232-C242                             -179.7(5)

C222-C232-C242-C252                                 -0.5(8)

C232-C242-C252-C262                                 -0.5(8)

C232-C242-C252-C272                                179.2(6)

C222-N212-C262-C252                                 -2.3(8)

Ir212-N212-C262-C252                               175.1(4)

C242-C252-C262-N212                                  1.9(8)

C272-C252-C262-N212                               -177.8(5)

C262-C252-C272-F222                                 -3.5(9)

C242-C252-C272-F222                                176.9(6)

C262-C252-C272-F232                                117.4(6)

C242-C252-C272-F232                                -62.3(8)

C262-C252-C272-F212                               -123.4(6)

C242-C252-C272-F212                                 56.9(8)

C312#3-Ir212-C312-C362                               4.9(5)

C312#4-Ir212-C312-C362                             -90.3(4)

N212#4-Ir212-C312-C362                              84.7(5)

N212#3-Ir212-C312-C362                             179.9(5)

N212-Ir212-C312-C362                              -132.2(13)

C312#3-Ir212-C312-C322                            -173.9(4)

C312#4-Ir212-C312-C322                              90.9(5)

N212#4-Ir212-C312-C322                             -94.1(4)

N212#3-Ir212-C312-C322                               1.2(4)

N212-Ir212-C312-C322                                49.1(15)

C362-C312-C322-C332                                  0.5(7)

Ir212-C312-C322-C332                               179.4(4)

C362-C312-C322-C222#3                             -178.7(4)

Ir212-C312-C322-C222#3                               0.3(6)

C312-C322-C332-C342                                 -0.6(8)

C222#3-C322-C332-C342                              178.5(5)

C322-C332-C342-C352                                  0.3(8)

C322-C332-C342-C372                               -179.0(6)

C332-C342-C352-C362                                  0.1(8)

C372-C342-C352-C362                                179.4(6)

C342-C352-C362-C312                                 -0.2(8)

C322-C312-C362-C352                                 -0.1(7)

Ir212-C312-C362-C352                              -178.8(4)

C332-C342-C372-F332                                131.1(10)

C352-C342-C372-F332                                -48.1(12)

C332-C342-C372-F312                               -108.6(10)

C352-C342-C372-F312                                 72.1(11)

C332-C342-C372-F322                                 10.0(11)

C352-C342-C372-F322                               -169.3(7)

C403#1-Cl403-C403-C413#1                           -79(4)

C403#2-Cl403-C403-C413#1                           -16(4)

C403#1-Cl403-C403-C413#2                            13(4)

C403#2-Cl403-C403-C413#2                            76(3)

C403#1-Cl403-C403-C403#2                           -62.9(3)

C403#2-Cl403-C403-C403#1                            62.9(3)

C403#1-Cl403-C403-C413                             -34(2)

C403#2-Cl403-C403-C413                              29(2)

C413#1-C403-C413-C403#2                             92(7)

C413#2-C403-C413-C403#2                           -173(6)

C403#1-C403-C413-C403#2                            -95(3)

Cl403-C403-C413-C403#2                             -45(3)

C413#1-C403-C413-C403#1                           -173(6)

C413#2-C403-C413-C403#1                            -78(6)

C403#2-C403-C413-C403#1                             95(3)

Cl403-C403-C413-C403#1                              50(2)

C413#1-C403-C413-C413#2                            -95(3)

C403#2-C403-C413-C413#2                            173(6)

C403#1-C403-C413-C413#2                             78(6)

Cl403-C403-C413-C413#2                             128(4)

C413#2-C403-C413-C413#1                             95(3)

C403#2-C403-C413-C413#1                            -92(7)

C403#1-C403-C413-C413#1                            173(6)

Cl403-C403-C413-C413#1                            -137(4)

C413#1-C403-C413-Cl413                             -45(3)

C413#2-C403-C413-Cl413                              50(2)

C403#2-C403-C413-Cl413                            -137(5)

C403#1-C403-C413-Cl413                             128(4)

Cl403-C403-C413-Cl413                              177.9(18)

C413#2-Cl413-C413-C403#2                           -75(4)

C413#1-Cl413-C413-C403#2                           -12(4)

C413#2-Cl413-C413-C403#1                            10(3)

C413#1-Cl413-C413-C403#1                            73(3)

C413#1-Cl413-C413-C413#2                            63.1(3)

C413#2-Cl413-C413-C413#1                           -63.1(3)

C413#2-Cl413-C413-C403                             -34(2)

C413#1-Cl413-C413-C403                              29(2)

________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 z,x,y    #2 y,z,x    #3 -y,z-1/2,-x+1/2    #4 -z+1/2,-x,y+1/2