### Supplementary information for use with communication “Phase-Transfer Catalyst Separation and Re-Use by Solvent Resistant Nanofiltration Membranes”

### Section 1 - Experimental Procedure

Chemicals

Bromoheptane 99%, iodoheptane 98%, tetraoctylammonium bromide (TOABr) 98%, potassium iodide 98% and HPLC grade toluene were obtained from Aldrich Chemical Co., Dorset, UK. Water was deionised with a conductivity of < 1Siemen.cm-1. All chemicals were used as supplied.

General reaction procedure

The reaction was carried out in a thick walled glass vessel fitted with a screw-on sample cap of 100 mL with a 40 mL aqueous phase (0.5M KI) and 40 mL organic phase (0.5 M bromoheptane + 0.05 M TOABr in toluene). The desired masses of bromoheptane and TOABr were weighed directly into the bottle and the volume was made up to 40ml with the toluene (measured using a 50ml measuring cylinder). The temperature was 50 ± 10C and stirring speed was 400 rpm. An initial sample was taken using a needle and l syringe for immediate GC analysis. Sampling was carried out at various recorded intervals during the reaction period until it was determined that between 95 and 100% conversion of iodoheptane had been attained.

After the reaction was completed, the organic phase (40 mL) was transferred into the SEPA cell and the cell was pressurized at 30 bar at room temperature. After 35 mL of 40 mL was filtered out, two different procedures were employed to reclaim the catalyst in the permeate and carry on the subsequent reactions:

Case 1:  the 5 ml of retentate left in the cell was washed out with pure toluene and the toluene was evaporated at 50 ± 10C (overnight in fume cupboard). This catalyst was then added to 40 mL 0.5 M bromoheptane-toluene (no other TOABr added) and mixed with 40 mL of 0.5 M KI aqueous phase. The reaction and nanofiltration were carried out as the above. In case 1 a new membrane disc was used each time. The reaction profiles for case 1 are shown in fig. 2 and flux results are shown in fig. 3 below.

Case 2:  the 5 ml of retentate left in the cell was washed out with 40 mL of 0.5 M bromoheptane-toluene to form the organic phase for the subsequent reaction. This organic phase was then mixed with 40 mL of 0.5 M KI aqueous phase. The reaction and nanofiltration were carried out as the above. In case 2 the same membrane disc was used for the repeated experiments. This procedure mimics more closely the likely procedure which would be used industrially. Graphical results of the flux from case 2 are shown in fig.4.

Filtration details

A schematic and detail of the nanofiltration set-up can be found in fig. 1. Nanofiltration was performed in a Sepa ST pressure cell (Osmonics, U.S.A) at a transmembrane pressure of 3.0Mpa (30BarGauge). The cell was immersed in a water bath controlled at a temperature of 20±0.10C. The membrane used was the solvent-resistant polyimide membrane, either 142A or 142C (W.R. Grace, Colombia, USA). A disk of membrane of surface area 1.69×10-3m2 was cut from the flat sheet coupons which have a molecular weight cut-off of 220 Daltons and 400Da respectively (as measured by manufacturer). The properties of the 142 series of membranes are provided in table 1, displayed are the MWCO’s and the rejection of n-decane from a toluene solution. The ring-seal necessary to fix the membrane disk in place was Viton rubber which was resistant to solvent swelling. The cell and bath were mounted on a magnetic stirrer and a Teflon stirrer bar effected stirring of the cell contents at 300rpm. Firstly the rejection of the catalyst from a toluene solution was attempted, to ensure the catalyst could not cross the membrane, the results from this initial experiment can be found in table 3. Two catalysts were studied, the hydrophilic Tetra Butyl Ammonium Bromide (TBABr), and the hydrophobic TOABr. The second step after ensuring the membranes could retain the catalyst was to attempt retention in the presence of the product and reactant, with the intention that both product and reactant would cross the membrane and the catalyst would not. These results are displayed in table 4, and show a minimal amount of product/ reactant rejection while complete catalyst rejection occurred. Finally, the actual reaction- filtration run using case 1 and case 2 was performed; these results are in table 5.

Permeate was collected in a 25ml measuring cylinder, which was covered to prevent any solvent losses by evaporation. The time taken to collect 20ml of permeate was recorded for the generation of flux data. It should be noted that the relevant pure solvent was passed through the membrane for a minimum of one hour prior to filtration of a given reaction solution in order to ensure that flux decline was avoided.

Analytical procedures

Gas chromatography

Concentrations of bromoheptane, iodoheptane and tetraoctylammonium bromide were all determined using a Shimadzu GC-14A Gas Chromatograph with a flame ionisation detector (FID) and a Megabore column 25m long and 0.23mm i.d. with BP1 (SGE, Australia) as the stationary phase. The temperature programme ran from 500C to 2800C at a rate of 200C.min-1 following being held at initial temperature for 2.5 minutes.

# Calculation of reaction parameters

Reaction conversion

Reaction conversion was calculated on the basis of simultaneous disappearance of bromoheptane, and evolution of iodoheptane. Thus, conversion was calculated using the following equation:

conversion=((CBrHeptane,0−CBrHeptane,t)(CBrHeptane,0))×100% 				(1.1)

where CBrHeptane,0 is initial bromoheptane concentration and CBrHeptane,t is bromoheptane concentration at time t during the reaction. A similar equation was used for the iodoheptane evolution.

Flux

The solvent flux through the membrane was calculated from the following formula,

Flux=VpAmemt				(l.m-2.hr-1)						(1.2)

where Vp is the volume of permeate collected, Amem is the membrane area, and t is the time taken to collect Vp. The fluxes of pure toluene across the membranes are shown in table 2 for the entire membrane series.

Rejection

The rejection of the membrane, R, is a measure of the extent a solute is retained by a membrane, and  is defined by the equation,

R=1−Cp,xCr,x											(1.3)

where Cp,x is the concentration of solute x in the permeate and Cr,x is the concentration of solute x in the retentate.

The flux and rejection results using 142 A & C of the products, reactants and catalyst are detailed in table 4.

For all retention experiments, a mass balance was calculated which is defined as

MB=CPVP+CRVRCBVB×100%								(1.4)

where VP, VR, VB are volume of permeate, retentate and the bulk solution, respectively, CB is the concentration of bulk solution.

key

1. nitrogen cylinder		6. temperature controller			11. magnetic stirrer					16. porous stainless steel disk

2. pressure regulator		7. Sepa ST pressure cell			12. Teflon stirrer-bar setup

3. isolation valve			8. copper heat-exchange coil		13. Ring seals (outer Viton, inner Teflon-coated rubber)

4. pressure gauge			9. water bath				14. high pressure clamps (69 BarG rating)

5. pressure relief valve		10. measuring cylinder with cap		15. membrane disk

Fig. 1.  Schematic of SEPA ST cell for nanofiltration used in this study. The liquid volume of the cell is 300 ml and diameter of the membrane disc is 49 mm.

PART 2 - Detailed experimental results

Tables

Table 1.  Solvent stable NF Membranes: Manufacturers Data

| Manufacturer | Membrane | Nominal MWCO | Membrane | Rejection | Flux (L/m2 h) |
| --- | --- | --- | --- | --- | --- |
|  | type |  | property | (%) | Toluene |
| WR Grace | 142A | 220 | hydrophobic | 62 (2% n-decane, MW=142, in toluene) | 35 (54 bar) |
|  | 142B | 200 | hydrophobic | 74 (2% n-decane, MW=142, in toluene) | 20 (54 bar) |
|  | 142C | 400 | hydrophobic | 28 (2% n-decane, MW=142, in toluene) | 19 (54 bar) |

Table 2.  Toluene fluxes at 30 bar

| Membrane | 142A | 142B | 142C |
| --- | --- | --- | --- |
| MWCO | 220 | 200 | 400 |
| Flux (L m-2 h-1) | 39 | 34 | 38 |

Table 3.  Solvent fluxes and catalyst retention by NF and non-porous membranes at 30 bar

| Membrane | Nominal MWCO | Toluene / TBABr (MW322) |  | Toluene / TOABr (MW546) |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Flux (L m-2 h-1) | Rejection (%) | Flux * (L m-2 h-1) | Rejection (%) |
| 142A | 220 | 23 | >99 | 26 | >99 |
| 142B | 200 | 20 | >99 | 24 | >99 |
| 142C | 400 | 28 | 80 | 16 | >99 |

Table 4.  Separation of catalyst from a synthetic solution [Br-C7H15 (0.01 M) + I-C7H15 (0.01 M) + TOABr (0.01  M) + Toluene]

| Membrane | NominalMWCO | Flux (L m-2 h-1) |  | Rejection (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | Pure | Solution | Br-C7H15 (MW=179) | I-C7H15 (MW=226) | TOABr (MW=546) |
| 142A | 220 | 65 | 25 | 20 | 22 | >99 |
| 142C | 400 | 88 | 32 | 8 | 5 | >99 |

Table 5.  Separation of catalyst from reaction product mixture by 142A (MWCO=220) membrane

|  | Reaction | Conversion (%) | Solution flux | Rejection (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | time (hrs) |  | (L m-2 h-1) | TOABr (MW=546) | I-C7H15 (MW=226) | Br-C7H15 (MW=179) |
|  |  | Case 1 Case 2 | Case 1 Case 2 | Case 1 Case 2 | Case 1 Case 2 | Case 1 Case 2 |
| Reaction 1 | 5 | 97 98 | 12 9.1 | >99 >99 | 12 11 | 10 11 |
| Reaction 2 | 5 | 90 97 | 14 8.5 | >99 >99 | 18 15 | 14 18 |
| Reaction 3 | 5 | 96 96 | 15 7.0 | >99 >99 | 5 8 | 13 7 |

Case 1: the 5 ml of retentate was washed out with pure toluene and then recovered by toluene evaporation; each filtration was carried out with a fresh membrane disc.

Case 2: the retentate was washed out each time with fresh organic reactant solution containing no catalyst, and consecutive filtrations were carried out with the same membrane disc.

Graphical results

(A)

(B)

(C)

Fig. 2 Evolution of bromoheptane and iodoheptane concentration over time in the reaction in the presence of 0.05 M TOABr at 50 C. The aqueous phase: 40 ml 2 M KI; the organic phase: 40 ml 0.5 M bromoheptane + 0.05 M TOABr. Stirring speed: 400 rpm. (A) Reaction 1; (B) Reaction 2 using TOABr separated from the Reaction 1 mixture; (C) Reaction 3 using TOABr separated from the Reaction 2 mixture.

Fig. 3. Permeate fluxes of post-reaction mixtures as a function of time at 30 bar. Case 1 where each subsequent filtration used a new membrane disc. Between filtrations, the membranes were soaked in toluene. The closed squares (■) show data for filtration of the reaction mixture, while the open squares (□)show data for pure toluene, passed through the membranes to provide a benchmark on flux prior to each catalyst separation.

Fig. 4. Permeate fluxes of post-reaction mixtures as a function of time at 30 bar. Case 2, each subsequent filtration using the same membrane disc. Between filtrations, the membrane was soaked in toluene. The closed squares (■) show data for filtration of the reaction mixture, while the open squares (□) show data for pure toluene, passed through the membranes to provide a benchmark on flux prior to each catalyst separation.