Fig.4 : ORTEP view of the polymer [{Cu2(medpt)2Ni(CN)4}2(ClO4)2]n. (ClO4 anions omitted for clarity, Cu1 and Cu2 are not symmetry related by a symmetry mirror).

Selected intra-chain distances (for a comparison the correspondent value detected in the hydrated species is reported in parentheses):

N1 – N1a  5.378 Å (4.811, H-bonded to a water molecule);

N3 – N3a  6.724 Å (8.008).

inter-chain distances :

N3 – N3’  3.588 Å (3.655, H-bonded to a water molecule);

N3a – N3a’  4.032 Å (3.655, symmetry equivalent to N3 – N3’).