Electron micrographs of PANI/MWNT composites. SEM of composite 10 wt% (a) and 30 wt% (b). TEM of composite 30 wt% (c). All micrographs confirm that MWNTs are irregularly mixed with the polymer matrix and that no additional order has been introduced.