Supplementary Information

belonging to

Detection of ppm quantitites of gaseous SO2 by organoplatinum dendritic sites immobilised on a quartz microbalance

Martin Albrecht, Martin Schlupp, Joachim Bargon,* Gerard van Koten*

UV–vis spectroscopy of 3 and 4

3 (toluene): max () = 281 nm (3.86  103 M–1cm–1), 332 nm (7.25  104 M–1cm–1)

4 (3 M SO2 in toluene): max () = 353 nm (9.74  103 M–1cm–1) 417 nm (4.31  104 M–1cm–1)

Measurements using QMB discs coated with metallodendritic receptors.

Table S–1. SO2- and temperature-dependent negative frequency shift of discs coated with 2 or 3 a)

| SO2 /ppm | 35 ˚C |  | 40 °C |  | 45 °C |  | 50 °C |  | 55 °C |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 2 | 3 | 2 | 3 | 2 | 3 | 2 | 3 | 2 | 3 |
| 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| 5 | 8 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| 10 | 11 | 7 | 7 | 6 | 4 | 0 | 0 | 0 | 0 | 0 |
| 25 | 24 | 13 | 14 | 10 | 7 | 4 | 3 | 3 | 0 | 3 |
| 50 | 36 | 20 | 16 | 14 | 10 | 10 | 6 | 6 | 4 | 4 |
| 75 | 49 | 24 | 24 | 19 | 13 | 12 | 9 | 8 | 6 | 5 |
| 100 | 52 | 31 | 31 | 22 | 18 | 14 | 12 | 12 | 8 | 7 |
| 200 | 54 | 34 | 35 | 29 | 20 | 18 | 15 | 14 | 10 | 10 |
| 400 | 71 | 42 | 47 | 29 | 31 | 27 | 20 | 20 | 12 | 13 |
| 600 | 74 | 42 | 47 | 29 | 35 | 27 | 25 | 25 | 14 | 17 |
| 800 | 72 | 42 | 47 | 29 | 35 | 27 | 25 | 25 | 16 | 17 |
| 1000 | 72 | 42 | 47 | 29 | 35 | 27 | 25 | 25 | 18 | 17 |

a)	Negative frequency shift in Hz; a shift of 10 Hz corresponds to 44 ng cm–2 mass increase (0.69 nmol cm–2 bound SO2).

By using the direct correlation of the negative frequency shift with the mass increase (4.4 ng cm–2 Hz–1), the amount of bound SO2 in the saturated systems, i.e., in the presence of 1000 ppm SO2, was calculated and compared to the number of available platinum sites. This allows for the determination of the association constant Kass as a function of temperature.

Table S–2. Temperature-dependent association constants Kass (see also Fig. S–1)

| T /K |  | disc coated with 2 |  |  |  |  | disc coated with 3 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | c(Pt–SO2) a) |  | c(Pt) a) | # Kass | c(Pt–SO2) a) |  | c(Pt) a) | # Kass |
| 308 | 5.0 |  | 85.1 | 0.058 | 2.9 |  | 84.1 | 0.034 |
| 313 | 3.2 |  | 86.8 | 0.037 | 2.0 |  | 85.0 | 0.023 |
| 318 | 2.4 |  | 87.6 | 0.027 | 1.9 |  | 85.1 | 0.022 |
| 323 | 1.7 |  | 88.3 | 0.019 | 1.7 |  | 85.3 | 0.020 |
| 328 | 1.2 |  | 88.8 | 0.014 | 1.2 |  | 85.8 | 0.014 |

a)	concentrations c in nmol cm–2; c(Pt–SO2) refers to SO2-bound platinum sites, c(Pt) refers to SO2-free platinum sites; 
c(Pt)tot = 90 nmol cm–2 for 2 and 87 nmol cm–2 for 3.

According to eq 1

H˚ – TS˚ = –RTln(K)	(1)

the standard parameters for 2 have been calculated as H˚  –59 kJ mol–1; S˚  –215 J mol–1 K–1. The data for 3 are less accurate and reveal H˚  –34 kJ mol–1; S˚  –138 J mol–1 K–1.

Figure S–1. Plot of ln(K) against 1000/T demonstrating the temperature-dependence of the association constants K obtained from experiments with discs coated with 2 (diamonds, correlation of least-squares fit c > 0.997) and with 3 (bars), respectively.