Table S1  Results at the end of the one million Monte Carlo simulations involving sorption of sorbents 1a, 1b, 1c and 1d in mesoporous material Al-MCM-41 and zeolite HY at temperature: 333 K.

| Sorbate molecule | Al-MCM-41 |  | HY |  |
| --- | --- | --- | --- | --- |
|  | Average loading | Average energy (Kcal/mole) | Average loading | Average energy (Kcal/mole) |
| Cyclic molecule (1a) | 4.1 | -42.1 | 0.0 | 0.0 |
| Linear tetramer (1d) | 4.8 | -38.68 | 0.0 | 0.0 |
| Linear trimer (1c) | 12.5 | -28.1 | 0.0 | 0.0 |
| Linear dimer (1b) | 48.3 | -31.2 | 10.0 | -19.4 |