SUPPLEMENTARY DATA

# Intercalation and Controlled Release of Pharmaceutically Active Compounds from a Layered Double Hydroxide

# Aamir Khan and Dermot O’Hare*

Inorganic Chemistry Laboratory, South Parks Road, Oxford, OX1 3QR, UK,

Figure S1. X-ray diffraction patterns of (a) [LiAl2(OH)6]Cl.H2O and

(b) LDH/Ibuprofen Intercalate