# Supplementary data

A New Bifunctional Catalyst for Tandem Heck-Asymmetric Dihydroxylation of Olefins

Boyapati M. Choudary,* Naidu S. Chowdari, Karangula Jyothi, Nadakuditi S. Kumar and Mannepalli L. Kantam,

The BET surface areas of silica gel, mercaptopropyl silica gel 2, SGS-(DHQD)2PHAL and SGS-(DHQD)2PHAL(Pd) 3 are found to be 249, 210, 152 and 123 m2g-1 respectively. The reduction in the surface area after anchoring the spacer and ligand is due to the presence of organic moieties on the silica gel surface.