Supplementary Material (ESI) for Chemical Communications

This journal is © The Royal Society of Chemistry 2002

Table 1 : Crystal data and structure refinement parameters for Ga(P2O7)F.H3N(CH2)3NH3.3H2O (1) and Ga(P2O7)F.H3N(CH2)3NH3.H2O (2).

| Formula | Ga(P2O7)F.H3N(CH2)3NH3.3H2O (1) | Ga(P2O7)F.H3N(CH2)3NH3.H2O (2) |
| --- | --- | --- |
| Chemical formula weight (g.mol-1) | 392.85 | 356.82 |
| Calculated density (g.cm-3) | 2.015 | 1.996 |
| Crystal system | monoclinic | orthorhombic |
| Space group | P 21/m | C m c m |
| a (Å) | 9.5724(9) | 10.3093(4) |
| b (Å) | 7.1632(6) | 15.9456(6) |
| c (Å) | 9.9780(9) | 7.2219(3) |
|  (°) | 108.816(5) |  |
| V (Å3) | 647.6(2) | 1187.2(1) |
| Figures of Merit | M20 = 37 F20 = 61 | M20 = 103 F20 = 201 |
| Z | 2 | 4 |
| Radiation (Å) | 1.5418 | 1.5418 |
| 2 range (°) | 7 - 77 | 7 - 77 |
| No. reflections | 380 | 201 |
| No. atoms | 17 | 11 |
| No. structural parameters | 37 | 22 |
| RP | 0.116 | 0.103 |
| RWP | 0.151 | 0.132 |
| RB | 0.085 | 0.088 |
| RF | 0.063 | 0.082 |

Table 2a : Atomic coordinates and isotropic displacement parameters (Å2) for non-hydrogen atoms for Ga(P2O7)F.H3N(CH2)3NH3.3H2O (1).

| Atom | x | y | z | Biso |
| --- | --- | --- | --- | --- |
| Ga | 0 | 0 | 0 | 0.28(2) |
| P1 | 0.2092(9) | ¼ | 0.2534(8) | 0.38(3)a |
| P2 | 0.2671(8) | ¼ | -0.0095(8) | 0.38(3)a |
| F | -0.078(2) | ¼ | -0.031(2) | 2.4(3)b |
| O1 | 0.320(1) | ¼ | 0.1578(9) | 2.4(3)b |
| O2a | 0.295(2) | ¼ | 0.408(1) | 2.4(3)b |
| O2b | 0.392(2) | ¼ | -0.069(3) | 2.4(3)b |
| O3a | 0.120(1) | 0.075(1) | 0.215(2) | 2.4(3)b |
| O3b | -0.168(2) | -0.084(2) | 0.055(2) | 2.4(3)b |
| N1 | -0.126(3) | ¼ | 0.655(2) | 2.8(5)c |
| C1 | -0.101(1) | ¼ | 0.5181(9) | 2.8(5)c |
| C2 | -0.244(1) | ¼ | 0.4070(9) | 2.8(5)c |
| C3 | -0.212(1) | ¼ | 0.2730(9) | 2.8(5)c |
| N2 | -0.351(2) | ¼ | 0.156(2) | 2.8(5)c |
| Ow1 | 0.621(3) | ¼ | 0.837(3) | 4d |
| Ow2 | 0.182(3) | ¼ | 0.621(3) | 4d |
| Ow3 | ½ | 0 | ½ | 4d |

a, b and c : allowed to vary in the same manner; d : fixed

Table 2b : Atomic coordinates and isotropic displacement parameters (Å2) for non-hydrogen atoms for Ga(P2O7)F.H3N(CH2)3NH3.H2O (2).

| Atom | x | y | z | Biso | Occupancy |
| --- | --- | --- | --- | --- | --- |
| Ga | 0 | 0 | 0 | 1.75(9) | ¼ |
| P | 0.1428(5) | 0.1345(4) | ¼ | 2.3(2) | ½ |
| F | 0 | -0.0505(8) | ¼ | 2.1(2)a | ¼ |
| O1 | 0 | 0.1834(9) | ¼ | 2.1(2)a | ¼ |
| O2 | 0.2472(9) | 0.2000(6) | ¼ | 2.1(2)a | ½ |
| O3 | 0.1336(6) | 0.0812(3) | 0.4318(9) | 2.1(2)a | 1 |
| C1 | 0.1151(7) | 0.4204(6) | ¼ | 2.7(3)b | ½ |
| C2 | 0 | 0.3702(9) | ¼ | 2.7(3)b | ¼ |
| N | 0.231(1) | 0.3646(7) | ¼ | 2.7(3)b | ½ |
| Ow1 | ½ | 0.283(4) | ¼ | 4c | 0.061(2)d |
| Ow2 | ½ | 0.131(1) | ¼ | 4c | 0.189(2)d |

a and b : allowed to vary in the same manner; c : fixed; d : allowed to vary in the opposite manner.

Table 3a : Selected bonds lengths (Å) and angles (°) for Ga(P2O7)F.H3N(CH2)3NH3.3H2O (1).

Within the GaO4F2 octahedron

| Ga - F (x2) | 1.927(8) |
| --- | --- |
| Ga - O3b (x2) | 1.95(2) |
| Ga - O3a (x2) | 2.15(2) |
| F- Ga - F | 180 |
| F- Ga - O3a (x2) | 89(1) |
| F- Ga - O3a (x2) | 91(1) |
| F - Ga - O3b (x2) | 91(1) |
| F - Ga - O3b (x2) | 89(1) |
| O3a- Ga - O3a | 180 |
| O3a - Ga - O3b (x2) | 91(1) |
| O3a - Ga - O3b (x2) | 89(1) |
| O3b - Ga - O3b | 180 |

# Within the diphosphate groups

| P1 - O3a (x2) | 1.50(1) |  | P2 - O3b (x2) | 1.50(1) |
| --- | --- | --- | --- | --- |
| P1 - O1 | 1.64(1) |  | P2 - O1 | 1.58(1) |
| P1 - O2a | 1.50(1) |  | P2 - O2b | 1.50(2) |
| O3a - P1 - O3a | 114(1) |  | O3b - P2 - O3b | 105(1) |
| O3a - P1 - O1 (x2) | 106(1) |  | O3b - P2 - O1 (x2) | 106(1) |
| O3a - P1 - O2a (x2) | 110(1) |  | O3b - P2 - O2b (x2) | 113(1) |
| O1 - P1 - O2a | 111(1) |  | O1 - P2 - O2b | 113(1) |
| P1 - O1 - P2 124(1) |  |  |  |  |

#### Within the organic part

| N1 - C1 | 1.46(2) |  | N1 - C1 - C2 | 109(1) |
| --- | --- | --- | --- | --- |
| C1 - C2 | 1.45(1) |  | C1 - C2 - C3 | 106(1) |
| C2 - C3 | 1.46(1) |  | C2 - C3 - N2 | 109(2) |
| C3 - N2 | 1.46(1) |  |  |  |

# Most probable hydrogen bonds

| N1…..O3a (x2) | 2.66(1) |
| --- | --- |
| N1…..F | 3.02(1) |
| N1…..Ow2 | 3.08(3) |
| N2…..O2b | 2.75(1) |
| N2…..Ow1 | 3.11(3) |
| N2…..O1 | 3.16(3) |
| Ow1…..F | 2.75(3) |
| Ow1…..O2b | 2.65(3) |
| Ow2…..O2a | 2.68(3) |
| Ow2…..O2b | 3.10(3) |
| Ow3…..O2a (x2) | 2.59(1) |

Table 3b : Selected bonds lengths (Å) and angles (°) for Ga(P2O7)F.H3N(CH2)3NH3.H2O (2).

Within the GaO4F2 octahedron

| Ga - O3 (x4) | 1.953(6) |
| --- | --- |
| Ga - F (x2) | 1.977(5) |
| F - Ga - F | 180 |
| F - Ga - O3 (x4) | 92.3(5) |
| F - Ga - O3 (x4) | 87.7(4) |
| O3 - Ga - O3 (x2) | 90.3(4) |
| O3 - Ga - O3 (x2) | 89.7(4) |
| O3 - Ga - O3 (x2) | 180 |

# Within the diphosphate group

| P - O1 | 1.666(9) |
| --- | --- |
| P - O2 | 1.50(1) |
| P - O3 (x2) | 1.567(7) |
| O1 - P - O2 | 108.0(8) |
| O1 - P - O3 (x2) | 101.6(7) |
| O2 - P - O3 (x2) | 114.9(8) |
| O3 - P - O3 | 113.9(7) |
| P - O1 - P | 124.2(6) |

#### Within the organic part

| C1 - C2 | 1.43(1) |
| --- | --- |
| C1 - N | 1.49(1) |
| C1 - C2 - C1 | 112.0(9) |
| C2 - C1 - N | 109.3(9) |

# Most probable hydrogen bonds

| N…..F | 3.09(1) |
| --- | --- |
| N…..O2 | 2.63(1) |
| N…..O3 (x2) | 2.825(9) |
| N…..Ow1 (x2) | 3.06(3) |
| Ow1….F | 2.66(7) |
| Ow1….O2 (x2) | 2.92(3) |
| Ow1….N (x2) | 3.06(3) |
| Ow2….O2 (x2) | 2.83(1) |