Supplementary data

Conjugation of linoleic acid over a hydrogen pre-activated heterogeneous catalyst

Andreas Bernas, Narendra Kumar, Päivi Mäki-Arvela, Ensio Laine, Bjarne Holmbom, Tapio Salmi, and Dmitry Yu. Murzin

XRD measurements were performed using a diffractometer (Philips PW 1800) to determine structure, phase purity and crystallite size. The measuring conditions were as follows: Generator voltage 50 kV, generator current 40 mA, Cu tube anode, automatic divergence slit, irradiated sample length 12 mm, receiving slit 0.2 mm, step size 0.025, counting time 5.0 s per step. The effective crystallite size was measured using the single line and the approximate methods.

XRD measurements of Na-MCM-41 confirmed that the synthesized mesoporous material had MCM-41 structure. The XRD pattern exhibited the presence of four peaks, indicating presence of a hexagonal MCM-41 phase (Fig. 1). The XRD pattern of the reduced 5 wt-% Ni/H-MCM-41 sample indicates that a majority of NiO species are have been reduced to metallic Ni. The crystallite size of not reduced nickel was determined to be 98.9Å by the approximate method and 94.7Å by the single line method. The crystallite size of the reduced nickel was determined to be 57.7Å by the approximate method and 69.5Å by the single line method.

Fig. 1. XRD pattern of MCM-41. I = Na-MCM-41, II = 5 wt-% Ni/H-MCM-41, III = reduced 5 wt-% Ni/H-MCM-41.